International Conference on Catalysis and Pyrolysis 2018 (ICCP-2018) November 05-06, 2018 | San Francisco, USA

Photocatalytic activity of Zinc Oxide nanoparticles calcined at varying temperatures in the degradation of ethylbenzene

Darlington Ashiegbu

University of The Witwatersrand Johannesburg, South Africa

ZnO nanoparticles were synthesized via sol gel process and calcined at 400oC, 500oC and 650oC. The as synthesized nanoparticles were characterized by X-ray diffraction, scanning electron microscope, energy dispersive spectroscopy, and BET surface area measurement. XRD results revealed crystalline hexagonal wurtzite structure of the ZnO nanoparticles.All three samples were utilized in the degradation of ethylbenzene, and a UV-Vis spectrophotometer was utilized in monitoring degradation of ethylbenzene. The sample calcined at 500oC had the highest surface area of reaction, lowest agglomeration and the highest photocatalytic activity in the degradation of ethylbenzene. This revealed temperature as a very important factor in improved and higher photocatalytic activity.

Biography

Darlington Ashiegbu has expertise in the synthesis of Zinc Oxide nanoparticles for photocatalysis. His passion for photocatalysis is driven by the country of his birth which has serious problems with regards to crude oil pollution. He is currently a PhD candidate at the University of the Witwatersrand, Johannesburg South Africa. The sol gel method of synthesis is very appealing due to its homogeneity, excellent stability, very low cost of production, can be replicated easily, and allows for easy control of morphology of the nanoparticles and the guarantee of highly pure and uniform structured ZnO.

email id: darlingtonashiegbu1985@yahoo.com

Mobile: +27 73 567 9729