[bookmark: _Hlk516766933]Title: Sensing and healing efficiencies of cementitious composites incorporated carbon materials
Hocine Siad, PhD, Ryerson University, Canada; Mohamed Lachemi, Ryerson University, Canada; Mustafa Sahmaran, Hacettepe University, Turkey
International Conference on
Fibromyalgia and Chronic Pain (June 15-16, 2016   Philadelphia, USA)


J Pain Relief
ISSN: 2167-0846 JPAR an open access journa
Fibromyalgia 2016
June 15-16, 2016
Volume 5, Issue 3(Suppl)
Page 40

Abstract 
In recent years, the development of a new generation of smart structures has attracted researchers worldwide.  Efforts in this area have been directed toward the use of highly-conductive materials such as carbon nanotubes (CNT) and carbon fibers (CF) in cementitious materials for multifunctionality purposes. This study focused on developing a new generation of engineered cementitious composites (ECCs) with combined sensing and healing efficiencies. The goal was to detect and evaluate the damage in ECCs at their early time of occurrence, while insuring an automatic and repeated recovery of microcracks. Carbon nanotubes were incorporated in ECC compositions at 0.50% and 0.25% by mass of the cementitious materials, and carbon fibers occupied 1% and 0.5% by the total volume. Special mixing method was used for casting CNT-ECCs to insure a homogeneous dispersion of CNT particles and PVA fibers. Mechanical strengths, ductility and electrical resistivity (ER) of sound and pre-cracked specimens were assessed to evaluate the effect of CNTs and CFs on the intrinsic properties of ECCs.  The quantitative sensing/healing of microcracks was measured by comparing the fractional change in ER before and after pre-cracking, and at different recovery time. Microstructural investigations were completed on the healed crack lines to determine the relation between carbon materials and elf-sensing/self-healing efficiency. The results showed improvements in compressive and flexural strengths with the use of CNTs and CFs. Unlike CFs, CNTs in ECC showed equivalent ductility, increased crack numbers and decreased crack widths than control specimens, resulting in greater recovery rates in mechanical properties and ERs. In addition, CFs influenced negatively the sensing ability of microcracks and consequently, the accuracy of self-healing evaluation, while CNT-ECCs showed high precision in quantifying pre-cracking and self-healing rates. The SEM analyses showed bridged CFs across the healed microcracks, which explains the reduced sensing of initial cracking and healing in CF-ECCs.
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