# Bending of CR4 steel: Lattice strain measurement

Gupta Tilak Raj, PhD (Mechanical Engineering), Injectoplast, India

### Abstract

Statement of the Problem:

In this work, effect of deformation and different orientations on CR4 steel sheet at lattice constant, crystallite size and lattice strain has been analyzed.

Methodology & Theoretical Orientation:

The samples were prepared by air bending using 1mm thick CR4 steel. Air bending was carried out on a universal testing machine, using various sheet orientations, constant size of the specimen, constant process parameter and same tooling. Further, for analyses of deformation and orientation on CR4 steel, X-ray diffraction spectroscopy was performed. The samples were cut by wire electric discharge machining (WEDM) and polished for X-ray analysis. QualX 2.1 software was used for analyzing the peaks, lattice constant was analyzed using Bragg’s law and lattice strain using Williamson-Hall’s method. Crystallite size was analyzed by Scherrer’s method and Williamson-Hall’s method.

Conclusion & Significance:

The lattice constant is found to be the smallest on rolled face and after bending it increases along thickness. Further, the lattice strain was observed compressive in nature for all the three orientations. However, for 0◦orientation lattice strain (0.5%) was found to be more across the thickness as compared to 90◦orientation lattice strain (0.34%). Furthermore, the crystallite size was analyzed by Scherrer’s method and Williamson-Hall’s method, respectively. It is found that the crystallite size by using Williamson-Hall’s method is smaller than by using Scherrer’s method. Further, crystallite size is observed to be the smallest on the rolled face. Moreover, after application of bending force enhancement in the lattice strain is observed while the size of the crystallite is reduced noticeably.

### Recent Publications (minimum 5)

- Gupta, T. R., Sidhu, S. S., Katiyar, J. K., & Payal, H. S. (2021). Measurements of lattice strain in cold-rolled CR4 steel sheets using X-ray diffraction. Materials Science and Engineering B: Solid-State Materials for Advanced Technology, 264.

- Gupta, T. R., Sidhu, S. S., & Payal, H. S. (2020). Spring back in air bending of CRCS. International Journal of Precision Technology, 9(4), 345.

- Gupta, T. R., Sidhu, S. S., & Payal, H. S. (2018). Effect of die width on spring back of electrogalvanized CR4 steel during air bending. In Materials Today: Proceedings (Vol. 5, pp. 18416–18425).

- Gupta, T. R., & Payal, H. S. (2017). Effect of die and punch geometry on spring back in air bending of electrogalvanized CR4 steel. International Journal of Applied Engineering Research, 12(11), 2792–2797.

- Gupta, T. R., & Payal, H. S. (2017). Investigation of Spring Back in Air Bending of Electrogalvanized CR4 Steel. Indian Journal of Science and Technology, 10(16), 1–10.

- Gupta, T. R., & Payal, H. S. (2017). Effect of Tooling Parameters on Bending Force in Air Bending of CR4 steel. International Journal of Theoretical and Applied Mechanics, 12(3), 375.

- Gupta, T. R., & Payal, H. S. (2016). Investigative Study on Bending and Spring Back of Electro Galvanized Steel. In Vth International Symposium on “Fusion of Science & Technology”, New Delhi, India, January 18-22, 2016 (pp. 461–465)

Biography

Gupta Tilak Raj has obtained his PhD in Mechanical Engineering from Punjab Technical University and M.E. in Polymer Technology from University of Delhi. Presently, he is working as Vice President, Technical / Product Development, at Injectoplast, Kanpur-India and involved in the development of parts, assemblies and sub-systems for automotive industries. since last 25 years (Jan.1997onward). Previously, he was engaged in teaching of P.G. Diploma (Tool Design and Manufacture) & Diploma Tool & Die Making, student at Tool Room & Training Centre, (Now DITE), an Indo- Danish Project, Delhi-India for 17 years (Jan.1980- Dec.1996). His research interests are in the field of processing of metals and, polymers, product engineering and tool engineering. He is a Fellow member of the Institution of Engineers (India), designated as C. Eng. (I) FIE and Life Member of Indian Society for Technical Education.

Email: trg2in@yahoo.com

Notes/Comments: