Bio-inspired Semi-transparent Silver Nanowires Conductor based on Vein Network with Excellent Electromechanical and Photothermal Properties

Chun-Hua Zhu, PhD, China

Abstract

Bio-inspired conductive binary-network of vein-silver nanowires (AgNWs) was embedded in poly (dimethysiloxane) (PDMS) to prepare semi-transparent stretchable conductor (vein-AgNWs-PDMS) by a simple dipping process (see Figure). The special conductive structure was constructed by using vein with porous structure as an ideal skeleton to load AgNWs networks, which allowed vein-AgNWs-PDMS composite to show a low sheet resistance of 1 Ω sq-1 with 74% transmittance. The figure of merit of vein-AgNWs-PDMS is as high as 2502 and can be adjusted easily by controlling the times of dipping cycle. Furthermore, the vein-AgNWs-PDMS conductor can retain high conductivity after 150% mechanical elongation and exhibit excellent electromechanical stability in repeated stretch/release tests with 60% strain (500 cycles). As an example of applications, vein-AgNWs-PDMS conductors with patterned light-emitting diode (LED) arrays have been fabricated, which worked well under deformation. Moreover, the photo-thermal properties of vein-AgNWs-PDMS composite have been demonstrated by a position heating experiment induced by near-infrared (NIR) laser irradiation, and the generated heat can be effectively dissipated through vein network to avoid local overheating. Due to the high-performance and facile fabrication process, vein-AgNWs-PDMS conductors will have multifunctional applications in the stretchable electronic devices.

Image

Recent Publications

- Qiang Y, Zhu CH* et al. (2018) Bio-inspired semi-transparent silver nanowire conductor based on a vein network with excellent electromechanical and photothermal properties. RSC Adv. 8: 23066–23076.

- Zhu CH* (2017) Three-dimensional highly conductive silvernanowires sponges based on cotton-templated porous structures for stretchable conductors. RSC Adv. 7: 51

- Li l, Zhu CH* et al. (2015) A conductive ternary network of a highly stretchable AgNWs/AgNPs conductor based on a polydopamine- modified polyurethane sponge. RSC Adv. 5:62905-62912

Chunhua Zhu has her expertise in preparing stretchable conductor and related nanocomposites.

Email:chzhu@caep.cn