# Forging of Ti-Nb-Ta-Zr-O alloy –new material for hip implant

K. Halmešová, J. Stráský, J. Džugan, D. Preisler, M. Janeček

### Abstract

Nowadays the life time of hip joint implants is limited to 15-20 years which is not sufficient because of prolonged human lives and activity. This is due to a big difference in elastic modulus of an implant and a bone where the bone degrades in the area of non-loaded bone in a vicinity of too tough metal implant (stress-shielding). So the demand for new material for metal implants is increasing. The utilization of beta Ti- alloys is discussed in scientific literature for 2 decades.  The advantages include using biocompatible elements and lower elastic modulus. A new developed beta titanium alloy (Ti-Nb-Ta-Zr-O) was prepared by sequential plasma arc melting but was prepared only in the as-cast condition. The main task is to specify and optimize the process of implant manufacturing. The current issue is to prepare the forging state of the alloy with sufficient fatigue resistance. Cold rotary swaging of this material with different degrees of deformation (40-80%) was successfully performed and recrystallization of the material was studied. Process optimization regime was selected and applied on bigger part of the material. Mechanical and fatigue properties were tested and were found to reach better results compared with the cast-state of the material.

Recent Publications

- D. Preisler et al., "Cold Swaging and Recrystallization Annealing of Ti-Nb-Ta-Zr-O Alloy - Microstructure, Texture and Microhardness Evolution", Materials Science Forum, Vol. 941, 2018, pp. 1132-1136.

- Trojanová Z, Džugan J, Halmešová K, Németh G, Minárik P, Lukáč P, Bohlen J. Influence of Accumulative Roll Bonding on the Texture and Tensile Properties of an AZ31 Magnesium Alloy Sheets. Materials, 2018; 11(1):73.

- Drozd, Z., Trojanová, Z., Halmešová, K., Džugan, J., Lukáč, P., Minárik, P.: Anisotropy of thermal expansion in an AZ31 Magnesium Alloy Subjected to the Accumulative Roll Bonding, Acta Physica Polonica A, 2018,  134(3), pp. 820-823.

- Trojanová, Z., Džugan, J., Halmešová, K., Németh, G., Minárik, P., Lukáč, P.: Effect of Accumulative Roll Bonding of an AZ31 Alloy on the Microstructure and Tensile Stress, Acta Physica Polonica A, 2018, 134(3), pp. 863-866.

- Trojanová, Z.; Lukáč, P.; Džugan, J.; Halmešová, K.: Amplitude Dependent Internal Friction in a Mg-Al-Zn Alloy Studied after Thermal and Mechanical Treatment, Metals, 2017, 7, 433.

- Z. Trojanová, K. Halmešová, Z. Drozd, V. Šíma, P. Lukáč, J. Džugan, and P. Minárik, Thermal conductivity of an AZ31 sheet after accumulative roll bonding, Crystals, 2018, 8(7),278.

Biography

Kristýna Halmešová started her research in the field of thin films, now she works in applied research. She got a lot of experiences in the field of magnesium alloys and their treatment. Now she has begun to be one of the team that develops new biomaterial for hip implants. She has some experiences in thermo-physical measurements.

Email: kristyna.halmesova@comtesfht.cz