Phase composition, microstructure, and mechanical properties of polymer-derived SiOC glass-ceramics reinforced by WC particles

Jiongjie Liu, PhD, TU Darmstadt

Abstract

Statement of the Problem: The design and preparation of ceramic materials are closely related to the development of modern industry. In this work, a tungsten carbide (WC)-containing silicon oxycarbide (SiOC) glass-ceramic was prepared from WC-filled polysiloxane via pyrolysis and subsequent spark plasma sintering (SPS). The sintering behavior of SiOC was investigated by monitoring the densification temperature and shrinkage displacement. The phase composition and microstructure of ceramics were characterized by using FTIR, XRD, SEM, Raman spectrum, and optical microscope. It was shown that upon increasing the sintering temperature from 1400 °C to 1600 °C, the densification of ceramics was further improved, and the disorder of free carbon in SiOC was linearly decreased with sintering temperature. In addition, it was found that the incorporation of WC particles was effective to reinforce the mechanical properties of ceramics, and relevant strengthening mechanisms were discussed here. Finally, a correlation between phase composition, microstructure, and macroscopic performances of SiOC glass-ceramics was successfully derived.

Image

Figure 1: Schematic diagram to describe the relationship between phase composition, microstructure and properties of SiOC glass-ceramics.

Recent Publications (minimum 5)

- J. Liu, et al. Sn-containing Si3N4-based composites for adaptive excellent friction and wear in a wide temperature range. J. Eur. Ceram. Soc 42(2022), 913-920.

- J. Liu, et al. Effect of high-temperature oxidation on Si3N4 containingTi3AlC2, Ceram. Int 46(2020), 14697-14705.

- J. Liu, et al. Temperature-driven wear behavior of Si3N4-based ceramic reinforced by in situ formed TiC0.3N0.7 particles, J. Am. Ceram. Soc 102 (2019) 4333-4343.

- J. Liu, et al. Temperature-driven wear behavior of Si3N4-based ceramic reinforced by in situ formed TiC0.3N0.7 particles, J. Am. Ceram. Soc 102 (2019) 4333-4343.

- J. Liu, et al. Study on tribological behaviors of Si3N4 based ceramics sliding against POM under different solutions, Tribol. Int 118 (2018) 368-372.

Paste your Logo here

Biography

Jiongjie Liu has his expertise in design and preparation of ceramic-based composites for applying in harsh environments. He received his M.S. and PhD degrees in Physical Chemistry in 2018 and 2020 from the Lanzhou Institute of Chemical Physics, Chinese Academy of Sciences (China). Since October 2020 he has been a postdoctoral fellow in the Institute of Materials Science, TU Darmstadt, Germany. His scientific background and interests relate in general to (inorganic) materials synthesis and processing and in particular to the development of advanced ceramics with tailor‐made chemical/phase compositions, morphologies, microstructures and property profiles for structural applications (construction materials, high‐temperature resistant materials, materials for extreme, harsh environmental conditions).

Email: jiongjieliu92@gmail.com

Notes/Comments:

Presenting author details 
Full name: Dr. Jiongjie Liu
Contact number: 01624005135
Twitter account:
Linked In account:

Session name/ number: ceramics and composite materials
Category: Oral presentation