Light-induced Superconductivity in an Organic Mott Insulator

induced by Light-driven Carrier Doping

Masayuki Suda, PhD in Science, Institute for Molecular Science

Abstract (300 word limit)

Recently, electric-double-layers (EDL) of ionic liquids with huge capacitance has been employed in superconducting field-effect transistors as a nano-gap capacitor. However, due to the freezing of the ionic motions below ~200 K, modulations of the carrier density so far have been limited to the high-temperature regime. In this study, we fabricated novel photo-active superconducting devices by laminating a single crystal of κ-(BEDT-TTF)2Cu[N(CN)2]Br on the substrates coated with self-assembled monolayer of spyropiran-derivatives (SP-SAM) [1]. The initial resistances for the devices showed Mott insulator phase in the resistance measurements. After UV irradiation, however, superconducting transition was clearly observed. This photo-induced superconducting phase remained even after the irradiation was stopped. The resistance recovered to nearly the initial value by visible light irradiation, showing a reversible switching capability. From our previous measurements, κ-Br is known to evoke superconductivity by electrostatic carrier doping [2,3]. The above reversible switching of superconductivity should also be due to a carrier doping by the formation of EDL at the interface. Indeed, spyropirans can switch between a non-ionic isomer and a zwitterionic isomer when triggered by light-irradiation with diﬀerent wavelengths, resulting in a signiﬁcant change in the electric dipole moment. Reversible changes in dipole moment of SP-SAM produced two distinct electric ﬁelds between the κ-Br and the substrates that created electrostatically doped carriers. Thus, superconductivity could be switched by photo-irradiation by photo-induced EDL formation.   This result opens new possibilities for the novel electronics utilizing a photo-active electric double layer, which can modulate electric-fields by light irradiation.
Image

Figure 1.  Schematic illustration of the κ-Br device; the spiropyran-monolayer can isomerize reversibly by UV and visible light irradiation at interface.

Recent Publications (minimum 5)

- Suda M et al. N-type superconductivity in an organic Mott insulator induced by light-driven electron-doping. (2016) submitted.

- Suda M, Kato R, Yamamoto HM (2015) Light-induced superconductivity using a photoactive electric double layer. Science 347:743-746.

- Suda M et al. (2014) Strain-tunable superconducting field-effect transistor with an organic strongly-correlated electron system. Advanced Materials 26:3490-3495.

- Yamamoto HM, Suda M et al. (2013) A strained organic field-effect transistor with a gate-tunable superconducting channel. Nature Communications 4:2379.

- Tajima N, Suda M et al. (2013) Quantum Hall effect in multilayered massless Dirac fermion systems with tilted cones. 88:075315.

Biography (150 word limit)

Masayuki Suda is an assistant professor of the Research Center of Integrative Molecular Systems, Institute for Molecular Science, Japan. He has his expertise in photo-functional magnetic and conducting molecular devices. He developed new photo-control method for organic-inorganic interface dipoles which can modulate the magnetic or conducting properties at the device interfaces. He recently applied this method to the field-effect transistor devices based on organic Mott insulators and realized first light-induced superconductivity in organic materilas. In recognition of this achievement, He got the PCCP award from Royal Society of Chemistry in 2016

Email: msuda@ims.ac.jp

Notes/Comments: