Study of adsorption of Brilliant Green by modified clays

Ismail Ltifi1, Fadhila Ayari1, Dalila Ben Hassen Chehimi1, Malika Trabelsi Ayadi1

1 Laboratoire d'Application de la Chimie aux Ressources et Substances Naturelles et à l'Environnement
Faculté des Sciences de Bizerte, Université de Carthage, Tunisie

Abstract

The adsorption of Bright Green (BG), a cationic dye, was studied by clay treatment experiments by modification with an aqueous solution of a cationic surfactant. Hexadecyltrimethylammonium bromide (HDTMA) and Cetylpyridinium chloride (CPC) were used for the modification of the clay. Clay modified HDTMA showed the greatest adsorption capacity compared to the other adsorbents studied.

The adsorption of HDTMA on BG depended on the adsorbent dose, the pH of the solution, the contact time and the initial dye concentration studied.

The adsorption data to correspond to the HDTMA experiments have been better described by the Langmuir isotherm model. The isothermal adsorption capacity of BG on HDTMA modified clay was found to be 45.5 mg / g (for an initial BG concentration of 50 mg / L), which is significantly higher than that of other adsorbents. The kinetics of adsorption of BG on clay modified by HDTMA has been described more precisely by the pseudo-second order kinetics model. The adsorbent was characterized by analysis of the Brunauer-Emmett-Teller surface (BET), Fourier transform infrared spectroscopy (FTIR) and X-ray diffraction (XRD). The BG adsorption mechanism on the surfactant-modified clay may comprise a hydrophobic interaction or van der Waals interaction or a combination of the two.

Keywords:

Adsorption, Cationic dye, Surfactant, HDTMA, CPC, Modified clay.