# Main-chain polyelectrolyte based on 1,2,3-triazolium with pentaethylene oxide spacer obtained via ‘click’ chemistry                      for all-solid state electrochromic device applications

John Marc C. Puguan and Hern Kim*

Myongji University, South Korea

### Abstract

Currently. the use of ionic liquids as electrolytes is enhancing the performance, security, speed, cyclability and long term stability of various electrochemical devices such as batteries, solar cells, fuel cells, supercapacitors, electrochromic devices, light-emitting electrochemical cells, actuators, biosensors and field effect transistors among others as well as in catalysis. However, ionic liquids are intrinsically liquids that present drawbacks that are difficult to overcome such as the need of thorough encapsulation due to leakage. Replacement of the liquid electrolyte with safer and mechanically stable material but still exhibiting excellent electrochemical properties is the goal of this study. A new poly(ionic liquid) or PIL which is a special type of polyelectrolyte carrying a cationic center constrained in the repeating units of the main chain is synthesized. This exhibits a dynamic combination of the unique properties of ionic liquids and the solid state properties of a polymer. A heterobifunctional ethylene glycol (EG)-based monomer was synthesized prior to the cycloaddition reaction. Propargyl group was introduced on one of the terminal end of the PEG unit and an azide group on the other end. Monomer was purified and underwent a copper(I) catalysed azide-alkyne cycloaddition (CuAAC) reaction to yield poly(1,2,3-triazole). PIL was reacted with methyl iodide to activate the cationic moiety. Subsequently, the iodide anion underwent anion exchange with bis(trifluoromethane)sulfonimide lithium (LiNTf2) salt to yield poly(3-methyl-1,2,3-triazolium bis(trifluoromethane)sulfonimide). This new PIL exhibits ionic conductivity of 1.2 × 10-4 S cm-1 at 30oC which is at par with best side-chain PILs in literature. This new electrolyte efficiently switches an electrochromic device (ECD) with 18% optical contrast from its transparent state to a colored state and vice versa. The development of this polyelectrolyte with simple structure and excellent physical and thermal properties is promising for the design of new all-solid state electrochromic devices and other electrochemical device applications.

Recent Publications

- J.M. Puguan, H. Kim, ZrO2-silane-graft-PVdFHFP hybrid polymer electrolyte: synthesis, properties and its application on electrochromic devices, Electrochimica Acta 196, 236-244(2016).

- J.M. Puguan, W.J. Chung, H. Kim, Synthesis and characterization of electrospun PVdF-HFP/silane-functionalized ZrO2 hybrid nanofiber electrolyte with enhanced optical and electrochemical properties, Solid State Sciences, 62, 34-42 (2016).

- J.M. Puguan, W.J. Chung, H. Kim, Ion-conductive and transparent PVdF-HFP/silane-functionalized ZrO2 nanocomposite electrolyte for electrochromic applications, Electrochimica Acta 196, 236–244 (2016).

- J.M. Puguan1, A. Chinnappan1, S.V. Kostjuk, H. Kim, Enhanced ionic conductivity and optical transmissivity of functionalized ZrO2/PVdF-HFP  hybrid electrolyte for energy efficient windows, Solar Energy Materials and Solar Cells 137, 265-273 (2015).

- J.M. Puguan, A. Chinnappan, S.V. Kostjuk, H. Kim, Ziroconium dioxide nanofilled PVDF-HFP complexed with lithium trifluoromethanesulfonate as composite polymer electrolyte for electrochromic devices, Materials Research Bulletin 69, 104–111 (2015).

Biography

John Marc C. Puguan, Ph.D. is currently an Assistant Research Professor at the Department of Energy Science and Technology, Myongji University (South Korea). He is passionate in producing and enhancing new class of advanced materials for energy applications. His specific interest covers the synthesis of organic-inorganic based  electrolytes for electrochemical devices such as energy efficient electrochromic glass and windows. Recently, he has expanded his research area into synthesizing polyelectrolytes based on ionic liquids/polyionic liquids for ECDs. He plans to explore the various electrochemical applications such as batteries, solar cells, fuel cells, supercapacitors, light-emitting electrochemical cells, actuators, biosensors and field effect transistors among others of these new materials.

Email: jmpuguan@gmail.com

Notes/Comments: