# Illumination effects on the electric characteristics of AU/GaN/GaAs Schottky diode

Rabehi Abdelaziz

Unité de Recherche Appliquée en Energies Renouvelables,

URAER, Centre de Développement des Energies Renouvelables, CDER, 47133, Ghardaïa, Algeria

### Abstract (300 word limit)

In this paper, we studied the electrical caracteristic of Schottky diodes based on gold contact on nitridated GaAs substrates. The used (100) GaAs substrate is n-type with concentration of Nd= 4.9×1015 cm−3. Nitridation process was performed using a N2 glow discharge source (GDS) creating N atomic species. A ultra-thin film with a thickness of 2.2 nm GaN is performed on GaAs surface. In order to study the electric characteristics under illumination, we use of a He–Ne laser of 1 mW power and 632.8 nm wavelength. The current–voltage (I–V) of the Au/GaN/GaAs structures was investigated at room temperature. The saturation current IS, the series resistance RS and the mean ideality factor n are, respectively, equal to 4.46×10-07 A, 172 Ω, 1.4 in the dark and to 5.64×10-07 A, 148 Ω, 1.21 under illumination.

Key words: Au/GaN/GaAs, Schottky diode, photoelectrical, traps states, DOS,W-U-shaped distribution, surface nitridation.

Biography

Abdelaziz Rabehi was born in Djelfa, Algeria, in 1986. He received the B.E. degree in electrical engineering from the University of Djelfa, Algeria, in 2009, and the M.S. degree. and Ph.D. degrees in micro-electronics from University Djillali Liabés, Sidi-Bel-Abbes, Algeria, in 2012 and 2017, respectively. He is currently a researcher at the Renewable Energy Development Centre URAER, Ghardaia, Algeria. His research interests are III-V-semiconductor materials, thin-film process and devices, characteristic evaluations, solar energy. neural networks, thin-film device applications, etc

Email: rab_ehi@hotmail.fr