# Effects of Time on the Morphological Property of Hydrogen and Sulphur-free Biogas Solid Oxide Fuel Cell Cermet Anodes

M Amine Essafi, Independent PhD Research, 
Frankfurt University of Applied Sciences ,GERMANY

### Abstract

High-temperature solid oxide fuel cells have mainly been used for large-scale stationary power generation in the last decade. The major advantages of this kind of fuel cells is that they can achieve high electric efficiencies; According to the manufacturer, the SOFCs were operating under high temperatures between T=800–1000 °C, with hydrogen and sulphur-free biogas as operating gases. The specimens were taken systematically after 2500 hours, then 15000 hours, then 20000 hours, then impregnated by low viscosity epoxy resin and finally ground and polished until obtaining a smooth proper surface for the for laboratory analysis. In this work, a nickel particle distribution in anodes were clearly noticed. The porous cermet anodes composed with Nickel and gadolinium-doped ceria were investigated with the optical microscopy, scanning electron microscopy and energy dispersive X-ray spectroscopy to understand the kinetics of the phenomena. All results conducted to the conclusion, that the degeneration of the cells performance is caused by the depletion of nickel in the region of the electrolyte/anode interface, to the coarsening/agglomeration of Nickel particles and also to formation of gadolinium-doped ceria agglomerates through the long operation time.

Figure1: Schematic representation of the SOFC anode microstructure

### Image

Figure 2: Light microscopy images of the embedded SOFC cells after 20000 hours

Recent Publications

- Zekri A, Schnetger B, Essafi M A, Plaggenborg T, Parisi P, Knipper M (2017) Microstructure Degradation of LSM/YSZ Cathodes for Solid Oxide Fuel Cells Aged in Stack after Long Operation Time. J. Electrochem. Soc. 2017 volume 164, issue 13, F1385-F1391.

- Essafi M A, Microstructural Investigation of Nickel Percolation in Porous Ni–CGO Anodes for Solid Oxide Fuel Cells by Low-Voltage Field Emission Scanning Electron Microscopy (2017), 7th International Conference on Fundamentals & Development of Fuel Cells, German Aerospace Centre (DLR), Stuttgart, 2017

Biography

M. AMINE ESSAFI, obtained his two engineer’s degrees (Dipl.-Ing.) in Mechatronics/ Micro Systems Technology from the Saarland University and in Engineering Physics (B.Eng.) from Trier University of Applied Sciences. His main areas of research are measurement technology, material sciences and experimental physics. His previous works focused on microstructure investigations of degradation mechanisms in Solid oxide fuel cells (SOFC). He is currently working at the high-tech industry and doing an independent PhD and part-time MBA at Frankfurt University of Applied Sciences, Germany. He is author of a number of publications and he holds a patent.

Email: essafi@web.de

Notes/Comments: