Elaboration and characterization of AlSi13 modified using Directional Solidification Processing

K. Ghedjati1,3,4*, E. Fleury4, M. Hacini5, O. Guellati1,3 and Y. Samih4

1   Université de Souk-Ahras, BP. 1553, Souk-Ahras 41000, ALGERIA.

2   Laboratoire des Systèmes et des Matériaux Avancés (LASMA), Univ Annaba, Fac. Sci, Dept. Physiq, 23000 Annaba, Algeria. * Corresponding author: ghedjati@ymail.com

3   Laboratoire d’Etude et de Recherche des Etats Condensés (LEREC), Département de Physique, Université Badji-Mokhtar de Annaba, BP. 12, Annaba 23000, ALGERIA. guellati23@yahoo.fr

4   Laboratoire d’Etude des Microstructures et Mécanique des Matériaux (LEM3), CNRS, Université de Lorraine-Metz ile de Saulcy, 57000Metz, France.

5   Laboratoire de Recherche de Fonderie (LRF), Univ Annaba, Fac Sci of Eng, Dept. Met, 23000 Annaba, Algeria.

### Abstract

In order to improve the mechanical properties, various treatments and procedures are recommended such as rapid solidification or modification treatment of the molten alloy, which makes it possible to obtain a lamellar or fibrous structure resulting in a notable improvement in elongation and strength. However, the non-respect of the strict procedure often results in a structure far from the desired one.

In this work, the effects of the modification of the alloy composition owing to the addition of 1 wt.% and 2 wt.% modifier composed of 40 wt.% NaCl and 45 wt.% NaF and 15 wt.% KCl, combined with the application of unidirectional solidification by means of the Bridgman type were studied on the Al-Si13alloy. The microstructure, in particular the spacing of the SDAS and its effect on the HB, was characterized on cylindrical shaped samples. Microstructural analyses revealed a decrease in the interdendritic spacing, in particular owing 2% of the modifier prepared with a reduced pulling traction. The dendrites were preferably oriented along the direction of the sample translation within the furnace for fairly low pulling velocity (500 µm/s). These microstructural modifications enabled an increase of both the HB values and the impact toughness.

Keywords

AlSi13 alloy, Modification treatment, Directionally solidification, Bridgman technique, Silicon eutectic.

Recent Publications

[1] Dahle A.K., Nogita K., McDonald S.D., Dinnis C., Lu L., Eutectic modification and microstructure development in Al-Si Alloys, Mat. Sci. and Eng. A. 413-414 (2005) 243-248.

[2] Shabestari S.G., Shahri F., Influence of modification, solidification conditions and heat treatment on the microstructure and mechanical properties of A356 aluminum alloy, J. Mater. Sci. 39 (2004) 2023–2032.

[3] Pacz A., U.S. Patent No. 1,387,900 (February 13, 1920).; A. Pacz, British Patent No. 158,827 (January 26, 1921).

[4] Smith R.W., in: R.W. Smith (Eds.), Modification of Aluminum–Silicon Alloys, Proceedings of the Conference on ‘The Solidification of Metals’, Iron and Steel Institute, London, Brighton, December, 1967, pp. 224–236.

[5] Ghedjati K, Fleury E, Hamani MS, Benchiheub M, Bouacha K, Bolle B, Elaboration of AlSi10Mg casting alloys using directional solidification processing international journal of minerals metallurgy and materials, 2015, vol. 22, pp. 509-515].

Biography

K. Ghedjati, permanent researcher in LASMA laboratory in Algeria, has completed her PhD from Badji-Mokhtar University of Annaba 2015, Algeria on elaboration of casting alloys using directional solidification processing. She has published 2 papers in reputed journals. Actually, she is working on the production of different kind of intermetallics and materials with high mechanic properties using directional solidification processing. She is working in collaboration with Laboratoire d’Etude des Microstructures et Mécanique des Matériaux (LEM3), Metz, France.

Email: ghedjati@ymail.com

Phone: +213698358846