Abstract Title

Magnesium ferrite/polyvinyl alcohol (PVA) nanocomposites: fabrication and characterization

Name

Gulfam Nasar

University/Organization, Country/State

Balochistan University of Information Technology, Engineering and Management Sciences Quetta Pakistan

Abstract (200-500 Words)

Terbium doped magnesium spinel ferrites (Mg1-xTbxFe2O4) and PVA/Mg1-xTbxFe2O4 composites having composition x=0.12, 0.14, 0.16, 0.18 were synthesized using micro-emulsion method and in-situ polymerization technique respectively. The structural properties were demonstrated using X-ray diffraction (XRD) and Fourier transform infra-red spectroscopy (FTIR). XRD analysis confirmed the fabrication of small concentration of Terbium into the spinel lattice whereas FTIR exposed the developed interactions between ferrite nanoparticles with polyvinyl alcohol matrix. The peaks obtained in both the above characterization techniques quite matched with those as reported in the literature and confirmed the formation of resulting nanocomposites. The dielectric and resistivity analyses were performed by determining dielectric parameters and current-voltage measurements. The values of dielectric constant, dielectric loss and tan δ were inversely proportional to the frequency under applied electric field at room temperature but become constant at higher frequency values. The lower values of dielectric constant of terbium incorporated magnesium ferrite polymer composites (MgFe2O4/PVA) are because of hindrance in electron exchange mechanism created by lockup among iron and terbium ions. The resistivity values of all the composites were found from 2.5x109 Ωcm to 18.8x109 Ωcm which showed a non- linear behavior.

Research Work Related Image/Table (if Applicable)

Figure 3: The variation of dielectric constant with frequency of pure PVA and PVA/Mg1-xTbx Fe2O4 nanocomposites.

Recent Publications (3 to 5)

- Cyclic-RGD penta-peptides cRGDyK derivatized with cyclopentadienyl complexes of technetium and rhenium as radiopharmaceutical probes. Qaisar Nadeem, Yunjun Shen, Farooq Warsi, Gulfam Nasar, Muhammad Qadir, Roger Alberto. Journal of Labelled Compounds and Radiopharmaceuticals.60:394–400, April 2017 DOI:10.1002/jlcr.3515. - Role of ytterbium on structural and magnetic properties of NiCr0.1Fe1.9O4 co-precipitated ferrites, Mushtaq Ahmad, Muhammad Azhar Khan, Azhar Mahmood, Shu-Sen Liu, Adeel Hussain Chughtai, Weng-Chon Cheong, Bilal Akram, Gulfam Nasar, Ceramics International, Volume 44, Issue 5, 1 April 2018, Pages 5433-5439. doi.org/10.1016/j.ceramint.2017.12.173 - Dosimetric, Radiobiological and Secondary Cancer Risk Evaluation in Head-and-Neck Three-dimensional Conformal Radiation Therapy, Intensity-Modulated Radiation Therapy, and Volumetric Modulated Arc Therapy: A Phantom Study. Rehman JU, Isa M, Ahmad N, Nasar G, Asghar HMNUHK, Gilani ZA, Chow JCL, Afzal M, Ibbott GS.April 2018. Journal of Medical Physics 43(2):129-135, DOI: 10.4103/jmp.JMP_106_17 - Dose Verification of Volumetric Modulated Arc Therapy using One and Two Dimensional Dosimeters. Jalil ur Rehman, Zahra, Ghulam Hussain, Nisar Ahmad, H M Noor ul Huda Khan Asghar, Zaheer Abbas Gilani, Gulfam Nasar, Malik M Akhter, Muhammad Isa, Geoffrey S. Ibbott May 2018) - Intensity modulated radiation therapy: A review of current practice and future outlooks. Jalil ur Rehman, Zahra, NisarAhmad, Muhammad Khalid, H.M.Noor ul Huda Khan Asghar, Zaheer Abbas Gilani, Irfan Ullahb, Gulfam Nasar, Malik Muhammad Akhtar, Muhammad Nauman Usmani. Journal of Radiation Research and Applied Sciences. July 2018, doi.org/10.1016/j.jrras.2018.07.006

Biography (100-200 words)

Gulfam Nasar currently works at BUITEMS, Quetta Pakistan as Assistant Professor. His research interests are mainly Material Chemistry, Polymer Chemistry and Nanotechnology. His current project is on 'polymer-ferrites nanocomposites'. Dr. Gulfam Nasar is a member of editorial boards of a number of research journals. He has presented his work in many international conferences around the world. He has published more than 20 publications in internationally reputed journals

E-mail

gulfamnsar@gmail.com

Mobile Number

+923333641818

Author Details

- Full Name: Gulfam Nasar - Linked in Account: gulfamnsar - Session/Track Name: - Category (Oral Presentation/ Poster Presentation): Oral Presentation - Date of Birth: 26th April 1974 - Postal Address: Department of Chemistry, Balochistan University of Information Technology, Engineering and Management Sciences, Airport Road, Quetta Pakistan

Notes/Comments(if any)

Replace with your Comments(if/any)