# Functional spintronic material Co40Fe40B20 for tunable radio frequency magnetic sensors

Ryan A. O’Dell, The University of Toledo

Adam B. Philips, The University of Toledo

Daniel G. Georgiev, The University of Toledo

Michael J. Heben, The University of Toledo

John G. Jones, Air Force Research Laboratory

Gail J. Brown, Airforce Research Laboratory

### Abstract (300 word limit)

Statement of the Problem: Radio frequency (RF) electronic devices tend to be large and have limited tune ability. Aerospace systems would be more versatile if smaller tunable passive RF electronic devices were available for replacement. The use of spintronic materials such as Co40Fe40B20 can be used to create spin torque transfer nano oscillators (STNO) that are fabricated using complimentary metal oxide semiconductor (CMOS) technology and offer current tunable microwave frequency generation. This would allow for on chip fabrication of passive RF electronics, which could easily replace heavier electronic circuits on aircraft to reduce weight. Improvements have been shown to increase when annealing up to 350°C however rapidly declines with increased annealing temperature.  Methodology & Theoretical Orientation: Using RF magnetron sputtering of Co40Fe40B20 onto silicon substrates both heated substrate and post deposition annealing effects can be studied. Examining the crystallinity of thin films throughout thermal treatments by X-Ray diffraction (XRD) provide the long-range order of the material. Ferromagnetic resonance (FMR) shows frequency dependent magnetic properties of the material, which change from thermal annealing. Magnetic force microscopy (MFM) shows microscopic magnetic changes at the sample surface. Conclusion & Significance: Depositing at a substrate temperature of 400C can reduce FMR peak-to-peak line width from 85 Oe to 54 Oe. Post deposition annealing of substrate heated depositions at 400C can continue to reduce peak to peak line widths down to 51 Oe until unwanted crystallization of secondary phase takes place. Magnetic force microscopy images show magnetic inclusions from secondary Co7Fe3 forming on the surface. Choosing the appropriate substrate deposition temperature can make device improvements and degradation is a result of secondary magnetic phase material impeding domain wall motion.

### Image

Recent Publications (minimum 5)

1.	J. G. Jones et al., "Al2O3−BaTiO3 nanolaminates fabricated by multistationary target pulsed laser deposition with in situ ellipsometry," Journal of Nanophotonics 11(4), 043506-043506 (2017), http://dx.doi.org/10.1117/1.JNP.11.043506.

2.	J. Jones et al., "PLD Of Oxide Nanolaminates and Thin Films For Charge Storage," EMN Meeting on Batteries 2016((2016),

3.	J. G. Jones et al., "Tunable stoichiometry of SiOx-BaTiOy-BOz fabricated by multitarget pulsed laser deposition," Journal of Nanophotonics 9(1), 093590-093590 (2015), http://dx.doi.org/10.1117/1.JNP.9.093590.

4.	W. Lu, W. Chen, P. Thapaliya, R.O. Dell, R. Jha, Switching characteristics of MgO based self-compliant ReRAM devices, in:  2015 IEEE 58th International Midwest Symposium on Circuits and Systems (MWSCAS), 2015, pp. 1-4.

5.	J. G. Jones et al., "Tunable stoichiometry of BCxNy thin films through multitarget pulsed laser deposition monitored via in situ ellipsometry (vol 8, 083999,2014)," Journal of Nanophotonics 8(1 (2014),

6.	J. G. Jones et al., "Tunable stoichiometry of BCxNy thin films through multitarget pulsed laser deposition monitored via in situ ellipsometry," Journal of Nanophotonics 8(1), 12 (2014), http://dx.doi.org/10.1117/1.jnp.8.083999.

7.	J. G. Jones et al., "Optical Multichannel Imaging of Pulsed Laser Deposition of ZnO," Plasma Science, IEEE Transactions on 42(10), 2590-2591 (2014), http://dx.doi.org/10.1109/TPS.2014.2342159.

8.	N. Reilly, M. Wehrung, R.A. O'Dell, L. Sun, Ultrasmall colloidal PbS quantum dots, Materials Chemistry and Physics, 147 (2014) 1-4.

Biography (150 word limit)

Ryan O’Dell has his expertise in materials research on innovative nanotechnology and magnetic thin films. His exploration of lead sulfide quantum dot materials has shown how both size and interlinking molecules modify optical absorption properties of thin films. The temperature dependent studies of ferromagnetic thin films show how crystallization affects magnetic properties. His foundation has been built by years of research in a diverse array of topics with a fellowship at the united state air force research laboratory. The use of cutting age technology and real world problem solving for military applications has shaped the way problem solving is approached.

Email: rodell@ashland.edu

Notes/Comments: