PLGA-PAA copolymers: Their size and structure influenced drug delivery  applications

Elham Ahmadi , M.Sc.Medical Biotechnology Student , Faculty of advanced medical sciences , Tabriz university of Medical Sciences , Tabriz , Iran.

Mohammad Rahmati-Yamchi Department of Clinical Biochemistry and Laboratory Sciences , Tabriz University of Medical Sciences , Tabriz , Iran.

Roya Salehi Department of Medical Nanotechnology , Faculty of Advanced Medical Sciences, Tabriz University of Medical Sciences , Tabriz , Iran.

### Abstract

Statement of the problem: The need for high cellular drug uptake and reduce the adverse effects of chemotherapeutic drugs obligate us to design and prepare a suitable nano-carrier. Poly(lactide-co-glycolic acid)PLGA is one of the most well used polymer for the development of biocompatible nanoparticles. the purpose of the study is to prepare the PLGA-PAA(Poly-lactide-co-glycolide)-(poly acrylic acid) co-polymer which is the first new developed biocompatible nano-carrier until now. We co-encapsulated hydrophilic doxorubicin and hydrophilic hydroxytyrosol in PLGA-PAA biocompatible nanocapsules. Methodology and theoretical orientation: We synthesised the poly(acrylic acid)(PAA) polymer by radical polymerization method in the presence of dry tetrahydrofuran as solvent of the reaction. Then PLGA-PAA copolymer synthesised by ring opening polymerization method in the presence of stannous octanoate(snoct2) as catalyst of the reaction. An oil-in-water emulsion process was utilized for the encapsulation of hydrophilic doxorubicin and hydroxytyrosol. findings: FTIR confirmed the PAA and PLGA-PAA copolymer formation is correct. HNMR, CNMR also approved it. The size of PLGA-PAA nanoparticles is measured 24nm by DLS technique and Spherical particles with an average diameter of 16nm is determined by SEM technique. The amount of drug loading and unloading is computed. Conclusion and significance: PLGA-PAA co-polymer was found to be a promising co-polymer for the preparation of nanoparticles with small size distribution and relatively high drug loading. Formulation of functionalized PLGA-PAA nanoparticles leads to enhance the high drug loading efficiency of hydrophilic drugs.

### Image

Figure1: Scanning electron microscopy(SEM) image of morphology and size of the NPs

Recent Publications

1 Acharya, Sarbari and Sanjeeb K Sahoo. "Plga Nanoparticles Containing Various Anticancer Agents and Tumour Delivery by Epr Effect." Advanced drug delivery reviews 63, no. 3 (2011): 170-83.

2 Betancourt, Tania, Brandon Brown, and Lisa Brannon-Peppas. "Doxorubicin-Loaded Plga Nanoparticles by Nanoprecipitation: Preparation, Characterization and in Vitro Evaluation." Nanomedicine 2, no. 2 (2007): 219-32.

3 Qureshi, Waseem Akhtar, Ruifang Zhao, Hai Wang, Tianjiao Ji, Yanping Ding, Ayesha Ihsan, Ayeesha Mujeeb, Guangjun Nie, and Yuliang Zhao. "Co-Delivery of Doxorubicin and Quercetin Via Mpeg–Plga Copolymer Assembly for Synergistic Anti-Tumor Efficacy and Reducing Cardio-Toxicity." Science Bulletin 61, no. 21 (2016): 1689-98.

4 Vasi, Ana‐Maria, Marcel Ionel Popa, Edi Constantin Tanase, Maria Butnaru, and Liliana Verestiuc. "Poly (Acrylic Acid)–Poly (Ethylene Glycol) Nanoparticles Designed for Ophthalmic Drug Delivery." Journal of pharmaceutical sciences 103, no. 2 (2014): 676-86.

5 Zhao, Yuan, Meng-lei Huan, Miao Liu, Ying Cheng, Yang Sun, Han Cui, Dao-zhou Liu, Qi-bing Mei, and Si-yuan Zhou. "Doxorubicin and Resveratrol Co-Delivery Nanoparticle to Overcome Doxorubicin Resistance." Scientific reports 6 (2016).

Biography Elham Ahmadi is master student of medical biotechnology at Tabriz university of medical sciences  , bachelor graduated  of cellular and molecular biology from Azarbijan shahid madani university of Tabriz. she is working on a project. Her project goal is nanotechnology based drug delivery for anti-cancer targeting and treatment.

Email:

Ahmadi.elham1993@gmail.com