# Nanoformulations for Hsp90 Inhibitors for Cancer Therapy

Ankit K. Rochani, Ph.D., Toyo University, Japan

Toru Maekawa, Ph.D., Toyo University, Japan

D. Sakthi Kumar, Ph.D., Toyo University, Japan

### Abstract (300-word limit)

Heat shock protein (Hsp) 90 plays an important role in maintaining protein homeostasis and helps in cancer proliferation. Since two decades, there is a significant rise in the pieces of evidence pertaining to the concept of using hsp90 inhibitors as a smart anticancer therapy. Molecules targeting Hsp90 in multiple cancers have entered advanced clinical trials. However, Hsp90 targeted cancer therapy faces a major problem of the aqueous dispensability of drugs due to their hydrophobic nature. Nanoformulation using soft polymers have played an important role in the aqueous delivery of hydrophobic anticancer drugs. Hence, in order to address the formulation issue of hydrophobic- Hsp90 targeted drugs; we have developed Hsp90 inhibitors loaded polymeric nanoformulations, which can be dispensed using aqueous phase (devoid of organic solvents). We have developed 17AAG (first generation Hsp90 inhibitor) and Fe3O4 loaded PLGA magnetic nanoparticles (MNPs). We had developed two types of formulations (1:1:10 and 1:1:20) by relatively varying the concentration of PLGA polymer. Our study showed that ratio of 1:1:10 for (17AAG, Fe3O4 and PLGA) provided relatively better physicochemical and pharmacological response. The size of drug loaded polymeric MNPs from 1:1:10 nanoformulation were found to be 204 nm (confirmed with SEM and TEM images). These NPs provided dual mode of Pancreatic cancer (MiaPaCa-2) cells destruction under Invitro conditions; rendered by magnetic hyperthermia (provide by Fe3O4) and Hsp90 inhibition (rendered by 17AAG). We have also developed novel albumin conjugated Hsp90 inhibitor loaded nanoparticles. We used standard desolvation method for the synthesis of drug conjugated albumin nanoparticles. Our studies showed that nab-Hsp90 inhibitor nanomedicine was found to have average particle size of around 222 nm (confirmed with high-resolution SEM and TEM images). Our study shows that the synthesized drug loaded albumin nanoparticles were found to be effective under Invitro condition against both pancreatic (MiaPaCa-2) and breast cancer (MCF7) cell lines. Our studies indicate that our nanomedicine platform, which consists of both synthetic and natural (protein based) polymers that can play a significant role the delivery of Hsp90 targeted anticancer drugs for next-generation anticancer therapy.

### Image

Recent Publications (minimum 5)

- Rochani AK et al (2016) Dual mode of cancer cell destruction for pancreatic cancer therapy using Hsp90 inhibitor loaded polymeric nano magnetic formulation Int J Pharm 511(1):648-58.

- Rochani AK et al (2016) Heat-Shock Protein 90-Targeted Nano Anticancer Therapy J Pharm Sci 105(4):1454-66.

- Borah A, Palaninathan V, Girija AR, Balasubramanian S, Rochani AK, et al (2016) Poly-lactic-co-glycolic acid Nanoformulation of Small Molecule Antagonist GANT61 for Cancer Annihilation by Modulating Hedgehog Pathway NanoWorld J 3(1): 1-10.

- Rochani AK, et al (2013) Heat Shock Protein 90 Inhibitors as Broad Spectrum Anti-infective Curr Pharm Des. 19(3):377-86

5.  Balasubramanian Sivakumar and Ravindran Girija Aswathy et al (2013) Aptamer conjugated theragnostic multifunctional magnetic nanoparticles as a nanoplatform for pancreatic cancer therapy RSC advances. 3, 20579-20598.

Biography (150-word limit)

Ankit Rochani is a pharmaceutical chemist and has extensive expertise in drug discovery and formulation development. He has received PhD in Bio Nano Fusion Science for nanoformulation development. He has around seven years of collective research experience in the field of Hsp90 targeted drug development for both cancer and infectious disease conditions like Malaria and Surra. He has developed intriguing nanomedicinal concepts for cancer therapy. His research interests include nanomedicine, proteomics, metabolomics and re-positional based approaches for drug design and development.

Email: anrochani@gmail.com