Nanostructured supports design: a prospective way to modern catalysts constructing

Vera I. Isaeva, Dr. Sci, National University of Science and Technology “MISiS”, Russia

Abstract

Statement of the Problem: Intense research efforts are focused on the development of nanostructured catalysts thanks to their advanced properties regarding activity and selectivity. Numerous works dealing with nanostructured catalysts relate to metal nanoparticles deposited on different supports. Some reports consider also nanoporous matrices with well-controlled surfaces. The modulation of textural and compositional properties of nanostructured carriers allows to enhance the performance of heterogeneous catalysts on their basis in a specific process. Besides creation of nanoporosity using appropriate templates in synthesis course like in zeolites and mesoporous silicas other promising way for the design of nanostructured heterogeneous catalysts is the utilization of carriers composed by nanoparticles. In this context, using a novel type of nanoporous matrices - Metal-organic frameworks (MOFs) - is a promising approach to rational design of supported catalysts. MOFs are hybrid coordination polymers built from small metal clusters and organic linkers and feature 3D-frameworks comprising nano-dimensional channels, pores or cavities. The purpose of this study is to explore two principal approaches to design of nanostructured MOFs supports for heterogeneous catalysts. Our work was focused on clarifying the possibility to control the activity and selectivity of the heterogeneous catalyst changing the MOF support dispersion between micro- and nanoscale. Methodology: MOFs materials in form of nanocrystals and microgranules were utilized as host matrices for metal nanoparticles deposition. In order to administer the particles size and morphology we have synthesized MOF samples by MW-assisted synthesis at an atmospheric pressure according to the original approach and by convenient solvothermal procedure. The structural characteristics and catalytic performance of M@MOF nanohybrids based on MOF supports with nano- and micro particles are compared. The catalytic performance of thus obtained M@MOF catalysts was demonstrated in practically important reactions, e.g. hydroformylation and Fisher-Tropsh synthesis. Findings: This work results demonstrate the strong impact of support crystal size and morphology on the catalytic performance of M@MOFs nanohybrids. Conclusion & The activity and selectivity of heterogeneous catalysts can be controlled using MOF materials with different dispersion and morphology as host matrices for M NPs deposition.

Recent Publications

- Isaeva VI, Eliseev Ol, R.V. Kazantsev RV, Chernyshev VV, Davydov PE, Saifutdinov BR, Lapidus AL, Kustov LM (2016) Fischer – Tropsch synthesis over MOF-supported cobalt catalysts (Co@MIL-53(Al)). 45:12006-12014.

- Isaeva VI, Kustov LM (2016) Catalytic Hydroamination of Unsaturated Hydrocarbons. Topics in Catalysis 59:1196–1206.

- Isaeva VI, Barkova MI, Kustov LM, Syrtsova DA, Efimova EA, Teplyakov VV (2015). In situ synthesis of novel ZIF-8 membranes on polymeric and inorganic supports. Journal of Materials Chemistry A 3:7469 – 7476.

- Isaeva VI, Tarasov AL, Chernyshev VV, Kustov LM (2015) Control of Morphology and Size of Microporous Framework MIL-53(Al) Crystals by Synthesis Procedure. Mendeleev Communications 25:466-467.

- Isaeva V, Tkachenko O, Afonina E, Kozlova LM, Grünert W, Solov’eva SE, Antipin IS, Kustov L (2013), 2-Butyne-l,4-diol hydrogenation over palladium supported on Zn2+-based MOF and host-guest MOF/calix[4]arene materials. Microporous Mesoporous Materials 166:167–175.

Biography

Vera Isaeva (1962) is a leading researcher in National University of Science and Technology “MISiS”, Moscow, Russia. Her activity is focused on the development of nanostructured materials including MOFs and composites on their basis, from synthesis to application, especially for energy saving processes. She has co-authored over 100 publications in peer-reviewed journals and 2 book chapters.

Email: sharf@ioc.ac.ru

Notes/Comments: