Keynote Speech

Azeez A. Barzinjy

Salahaddin University-Erbil/Tishk International University, Erbil, Iraq

Green Synthesis and Characterization of Nanoparticles: Highlighting some recent achievements

Azeez Abdullah Barzinjy1*

1 Department of Physics Education, Faculty of Education, Tishk International University, Erbil, Kurdistan Region, Iraq

*Email: azeez.azeez@su.edu.krd

Google Scholar: https://scholar.google.com/citations?user=6Ftd6I4AAAAJ&hl=en

Reseachgate: https://www.researchgate.net/profile/Dr-Azeez-Barzinjy

Abstract

In continuation of our recent works [1-9] regarding green synthesis nanomaterials, here in this talk an active and easy process of one-pot green synthesis of a number of nanoparticles is proposed. In our investigations, a variety of plant extracts, as efficient chelation and capping agents together with different salts, were utilized as salt ions sources. The plant extracts, were analyzed using both UV-Vis, quantitative, and FT-IR, qualitative methods in order to identify the essential phytochemicals which are necessary for reducing, capping and stabilizing of nanoparticles. Our studies showed that the salts with unlike counter-ions cause (dissimilar nucleation and growth kinetics). The structure, size, morphology, thermal behavior, surface area, surface charge, chemical composition and optical properties of the nanoparticles were investigated using several characterization techniques, namely UV-Vis, FT-IR, XRD, FE-SEM, EDX, DSC, DLS, Zeta potential and BET analysis.

The DSC analysis utilized to analysis the endothermic and exothermic peaks and water absorption by the synthesized NPs. It can also ascribe the loss of unstable wetting agent molecules adsorbed on the surface of the NPs throughout the synthesizing process. The XRD analysis showed that the change in plant extracts resulted in a range in crystallite size, while, the DLS analysis showed that the particles size alters with changing the plant extract and corresponding salts. The utilized method can produce nanoparticles with different shapes, highest crystallinity ranging between 96.96% to 100.0%, relatively high stability and good specific surface area.

After synthesizing and characterization process, the green synthesized NPs were employed for removing organic pollutants, explicitly methyl orange (MO) from water using UV-Vis spectroscopy. Nearly an entire degradation of MO was achieved within a very short time and the degradation process was reproducible for several runs. On the other hand, the synthesized NPs can be, also, utilized as a thin film layer on the top of the p-type or n-type Si wafer. Then the synthesized NPs thin film can be utilized for many applications such as gas-sensing, UV emission LED apparatus, solar panel and many other applications.

References

1.	Azeeza, H.H. and A.A. Barzinjya, Biosynthesis zinc oxide nanoparticles using Apium graveolens L. leaf extract and its use in removing the organic pollutants in water. DESALINATION AND WATER TREATMENT, 2020. 190: p. 179-192.

2.	Barzinjy, A.A. and H.H. Azeez, Green synthesis and characterization of zinc oxide nanoparticles using Eucalyptus globulus Labill. leaf extract and zinc nitrate hexahydrate salt. SN Applied Sciences, 2020. 2(5): p. 1-14.

3.	Barzinjy, A.A., et al., Green synthesis of the magnetite (Fe3O4) nanoparticle using Rhus coriaria extract: a reusable catalyst for efficient synthesis of some new 2-naphthol bis-Betti bases. Inorganic and Nano-Metal Chemistry, 2020: p. 1-10.

4.	Barzinjy, A.A., et al., Biosynthesis, characterization and mechanism of formation of ZnO nanoparticles using Petroselinum crispum leaf extract. Current Organic Synthesis, 2020.

5.	Barzinjy, A.A., et al., Biosynthesis and characterisation of zinc oxide nanoparticles from Punica granatum (pomegranate) juice extract and its application in thin films preparation by spin-coating method. Micro & Nano Letters, 2020. 15(6): p. 415-420.

6.	Barzinjy, A.A., et al., Green and eco‑friendly synthesis of Nickel oxide nanoparticles and its photocatalytic activity for methyl orange degradation.

7.	Nasrollahzadeh, M., et al., Biosynthesis of the palladium/sodium borosilicate nanocomposite using Euphorbia milii extract and evaluation of its catalytic activity in the reduction of chromium (VI), nitro compounds and organic dyes. Materials Research Bulletin, 2018. 102: p. 24-35.

8.	Sajadi, S.M., et al., Green Synthesis of the Ag/Bentonite Nanocomposite UsingEuphorbia larica Extract: A Reusable Catalyst for Efficient Reduction of Nitro Compounds and Organic Dyes. ChemistrySelect, 2018. 3(43): p. 12274-12280.

9.	Barzinjy, A., S. Mustafa, and H. Ismael, Characterization of ZnO NPs Prepared from Green Synthesis Using Euphorbia Petiolata Leaves. EAJSE, 2019. 4: p. 74-83.