Fabrication of Chemically Reduced Graphene Oxide Thin Films by

Atomized Spray Pyrolysis Deposition

D.C. Maddumage1,2, S.A. Panamaldeniya1,2, D.N.P.R. Jayakantha3, M.A.H.M. Munasinghe3, K. Pemasiri1,2, N.Gunawardhana3, B.S. Dassanayake1,2

1 Department of Physics, Faculty of Science, University of Peradeniya, Sri Lanka.

2 Postgraduate Institute of Science, University of Peradeniya, Peradeiya, Sri Lanka.

3 Department of Postdoctoral Research Unit, Sri Lanka Technological campus, Padukka, Sri Lanka.

Synthesis of reduced graphene oxide (RGO) by Modified Hummers method is an excellent method for bulk production of RGO powder. RGO has received a considerable attraction due to its properties such as extremely high carrier mobility, carrier density etc. RGO is used in many industrial applications, mostly by fabricating it on a substrate as a thin film (TF). In the reporting work, a novel method has been used to deposit RGO-TF on borosilicate glass substrates by Atomized Spray Pyrolysis Deposition (ASPD). In order to prepare the RGO ink used for ASPD, first 1 g of RGO flakes was dispersed in 100 ml of N-Methyl-2-pyrrolidone. Then ultrasonic treatment was carried out for the initial dispersion for six hours. Later, supernatant (ink) was extracted by a pipet after allowing the dispersion to settle overnight. During the ASPD, the distance between the substrate and the nozzle, and the speed of the substrate relative to the nozzle was set to 4 mm and 1.2 cm s-1, respectively. The deposition was carried out for 70 minutes. Compressed air was used as the carrier gas by maintaining the atomization pressure at 100 psi.

Deposited RGO-TF were optimized to obtain the lowest sheet resistance, highest carrier concentration and highest mobility by altering deposition temperature, thickness of the RGO-TF and annealing temperature. GIXRD, SEM, XPS and Hall measurements were carried-out to study structure, surface topography/film thickness, work function and carrier mobility of RGO-TF, respectively. Further discussion of characterization of the optimized sample will be presented at the conference.

Biography

D.C. Maddumage has completed his B.Sc. special degree in physics at the age of 25 years from University of Peradeniya and is following M.Phil. degree at Postgraduate Institute of Science, University of Peradeniya under grant no. NSF-PSF/ICRP/2017/EA & ICT/03.

Presenting author details 
Full name: Dileepa Chamikara Maddumage.
Contact number: +94 771 785 085
Twitter account: N/A
Linked In account: Dileepa Maddumage

Session name/ number: Nano Fabrication/ 3
Category: Oral presentation