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Abstract
[bookmark: _GoBack](E)-2-(1-(2-oxo-2h-chromen-3-yl)ethylidene)hydrazinecarbothioamide [H3L3] was prepared by the reaction of an intermediate (3-acetylcoumarin) formed by cyloaddition and cyclocondensation of ethyl acetoacetate and salicyaldehyde with thiosemicarbazide in ethanol. The metal complexes were then successfully synthesized in ethanolic solution of N,N'-dicyclohexyldithiooxamide and [H3L3]. TGA showed weight loss of about 60%, subdivided into two weight loss stages: the first stage occurred in the temperature range 150 - 300 oC, accounting 42% loss related to removal of hydrazinecarbothioamide derivative ligand, while the second occurred between 300 - 400 oC, 18% weight loss accounting for the dicyclohexyl derivative loss. Binary PbS and SnS nanoparticles were equally synthesized from their respective precursors (metal complexes) through solvothermal decomposition at 200 and 240 °C in oleylamine and were characterized by p-XRD, SEM-EDX, TEM and HRTEM. Pure cubic crystal phases of PbS NPs (galena) with space group of F m -3 m (ICDD# 96-901-3403) and orthorhombic SnS NPs (Herzenbergite) with P b n m space group (ICDD# 96-152-7227) were obtained. Their crystallite sizes varied with temperature, the average diameter for PbS nanoparticles at 200 °C being 38.5 ± 4.0 nm, and at 240 °C, 53.1 ± 6.9 nm appearing as agglomerated rod-shaped particles. Similarly, agglomerated SnS nanoparticles with an average diameter of 77.5 ± 13.9 nm were obtained at 200 °C, while at 240 °C, irregular triangular shaped particles with an average size of 525.1 ± 73.9 nm were formed. The PbS and SnS nanocrystals band-gap energies were 3.25-3.45 eV and 1.2-1.3 eV respectively in the optimum range for photovoltaic applications.  
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