# Antibacterial surface modification of Ti based material for implants

Jie Sun, MSc1; Tzvetanka Boiadjieva-Scherzer, PhD. 1; Hermann Kronberger, Prof. 2; Ievgen Kolesnyk, PhD;3

Kevin Staats MD4; Johannes Holinka, MD Prof. 4; Reinhard Windhager, MD Prof.4

1 Centre of Electrochemical Surface Technology GmbH (CEST)

2 Technical University of Vienna, Institute of Chemical Technologies and Analytics

3 Ukrainian State University of Chemical Technology, Department of Materials Science

4 Medical University of Vienna, Department of Orthopaedic Surgery

### Abstract

### Statement of the Problem: Titanium and its alloys are widely used as implant material due to their tensile strength, flexibility, corrosion resistance, high hemo- and biocompatibility [1]. A defined surface nanotopology offers guidance of the implant vs. cell interaction [2, 3] and at the same time gives opportunities for further modifications; promoting the bone growth [4], providing nano-containers for antibacterial agents [5, 6], etc..

### Methodology & Theoretical Orientation: Different strategies are applied to modify titanium and titanium alloy implant material, aiming at better antibacterial properties and biocompatibility. Pure titanium and titanium alloy Ti7Al are anodized to create titanium nanotubes. Subsequently, the nanotubes are annealed in order to transform the obtained TiO2 into TiO2 anatase phase (XRD and Raman spectroscopy). In a following step the surface is electrochemically modified.

### Findings: It is shown that addition of phosphate to the ethylene glycol based bath has certain influence on the titanium nanotubes topology. Nanotubes (pTNT) with a diameter of 100 nm are produced in ethylene glycol containing fluoride and phosphate, as additives. By electrochemical deposition the pTNT are uniformly filled with Se and coated with Cu2Se or Ag2Se. The composition and the structure of the layers are confirmed by EDX, FIB, SEM and XRD. A positive effect of Se on the nucleation of hydroxyapatite (HAp) during the electrodeposition was established. The quality and adhesion of the HAp coating is found to strongly depend on the structure of the substrate, the pH value of the bath, the applied voltage and the temperature.

### Conclusion & Significance: Uniform and circular pTNT with a diameter of 100 nm are produced and regularly filled with antibacterial agent. A bone like substance HAp with nano-crystalline structure is successfully electrodeposited on the pTNT surface. The as prepared coatings will be further examined in medical in-vitro and in-vivo experiments and undergo clinical tests.
Image

Recent Publications

1.	Actis, L., et al., Antimicrobial surfaces for craniofacial implants: 	state of the art. Journal of the Korean Association of Oral and 	Maxillofacial Surgeons, 2013. 39(2): p. 43-54.

2.	Xu, Z., et al., Increased Mesenchymal Stem Cell Response and 	Decreased Staphylococcus aureus Adhesion on Titania Nanotubes 	without Pharmaceuticals. BioMed Research International, 2015. 	2015: p. 9.

3.	Batur, E., et al., Diameter of titanium nanotubes influences anti-	bacterial efficacy. Nanotechnology, 2011. 22(29): p. 295102.

4.	Parcharoen, Y., P. Termsuksawad, and S. Sirivisoot, Improved 	Bonding Strength of Hydroxyapatite on Titanium Dioxide 	Nanotube Arrays following Alkaline Pretreatment for Orthopedic 	Implants. Journal of Nanomaterials, 2016. 2016: p. 13.

5.	Liu, W., et al., Selenium nanoparticles incorporated into titania 	nanotubes inhibit bacterial growth and macrophage proliferation. 	Nanoscale, 2016. 8(34): p. 15783-15794.

6.	Chen, X., et al., Fabrication of selenium-deposited and chitosan-	coated titania nanotubes with anticancer and antibacterial 	properties. Colloids and Surfaces B: Biointerfaces, 2013. 103: p. 	149-157.

Biography

Jie Sun is a PhD student at the technical university of Vienna working at the Institute of Chemical Technologies and Analytics. He obtained the Master of Science degree in chemistry. His research focuses on electrochemical surface modification of medical implants based on titanium.

Email: jie.sun@cest.at

Acknowledgement

These investigations were performed with the support of the Austrian Science Foundation FFG and the government of Lower and Upper Austria in the frame of the COMET program.