Implementation of Spinels (NiAl2O4, CoAl2O4 and Ni-Co2O4) as Emerging Catalysts for Upgrading of Extra Heavy Oil Including Hydrogen Production under Supercritical Water Conditions

Name: Djimasbe Richard

Department of Petroleum Engineering, Kazan Federal University, Kazan 420008, Russia

Spinel types catalysts were synthesized and employed in this work in order to consider its upgrading performance for extra heavy oil from the Taha oilfield (China) to produce light oil and mainly for gases production (methane and hydrogen). The results of synthesis and that of XRD patterns and SEM showed that the following spinel types denoted CoAl2O4 (2); NiAl2O4(3); and Ni-Co2O4 (4) with an average particle size around 59.13 nm, and the Ni and Co composition in catalysts is 9.29% and 4.68%, respectively. The results of the product distribution showed smaller yield of upgraded oil of 58.83 % and higher yield of coke of 33.64 % were obtained using only the supercritical water (SCW). However, using catalysts CoAl2O4 and NiAl2O4, the upgraded oil yields reach 63.34% and 61.07%, respectively. Therefore, the use of alloys of metals (Ni and Co) in form of spinel Ni-Co2O4, a higher yield of 67.26 % of upgraded oil was obtained with smaller yield of coke of 22%, while the greater yields 13.00% of gases is obtained in the sample (3). The viscosity of crude oil of 230000 Pa*s at 60 oC decreased to the smaller value of 54.8 mPa*s at 25 oC. So, high conversion of asphaltenes was also observed in the sample (4), hence the decreased from 39.04 % to 1.79%. Additionally, 8.07% of hydrogen and 43.61% of methane were obtained in the gaseous product. Therefore, the alloys of Ni-Co2O4 catalyst with high synergetic performances demonstrate its possible use for hydrogen and methane production on the industry's scale.

Fig 1. XRD patterns of fresh spinels catalysts.

Table 1. Results of SARA fraction of crude and upgraded oil under SCW conditions.

| № | Samples | Saturate, % | Aromatics,% | Resins,% | Asphaltenes,% |
| --- | --- | --- | --- | --- | --- |
| 1 | Crude taha oil | 12.35 | 11.87 | 36.74 | 39.04 |
| 3 | Oil + SCW | 73.74 | 3.68 | 22.13 | 0.43 |
| 4 | Oil + CoAl2O4 | 63.17 | 20.43 | 14.15 | 2.22 |
| 5 | Oil + NiAl2O4 | 65.71 | 22.70 | 9.62 | 1.94 |
| 6 | Oil + Ni-Co2O4 | 57.95 | 30.40 | 9.85 | 1.79 |

Biography

Richard Djimasbe will complete his PhD in september 2021 at the Kazan Federal University, speciality of Petrochemistry. He complted it bachelor and master degree in chemical technology at the Kazan National Research Technological University respectively in 2015 and 2017. He is junior searcher in the rheological and thermochemical laboratory at Kazan Federal University.

Presenting author details 
Full name: Richard Djimasbe
Contact number: +79046676953

Session name/ number: Petroleum Chemistry and Processing Technology 
     Category: (Poster presentation)