Tunisian clays: Perspectives of use in the medical field?

Moufida Ben M'barek Jemai a, Imed Ben Salah a, Ali Sdiri b, Aycer Ben Saad a.

a: University of sciences of Bizerte - Carthage university

b: National engineering school of Sfax – Sfax University

Abstract

This work has focused on the physico-chemical characterization of three series of clays in the North-West, central and North-East regions of Tunisia related with medical use.

The clays of the region of Nabeul (northeastern Tunisia) contain 37% of Attapulgite with a chemical composition including magnesium and aluminum. This clays show 3,26%  of CaO, 15,29%  of Al2O3 ,  5,5% of Fe2O3 and 49,78% of SiO2. The percentage of MgO achieve 7,55%.  Thanks to their high swelling potential, their low permeability, their cationic exchange capacity, their specific surface, their chemical and mechanical stability, it has a broad spectrum of applications, and one of the most important is medicine field. Principally, attapulgite is known for its excellent absorption property. Therefore, it is considered ideal for drugs that need to control stomach disorders such as diarrhea.

The white clays of Ain Khémouda (center-west of Tunisia) shows significant levels of alumina, zinc and iron. All these characteristics would allow its identification as hydrated halloysite (10Å) of the aluminous zinciferous type. The outer surface of halloysite nanotubes has properties similar to SiO2 while the inner core of the cylinder is related to Al2O3. The zeta potential can be roughly described by the superposition of a predominantly negative (at pH 6-7) surface potential of SiO2, with a small contribution of the positive Al2O3 inner surface. The charge of the internal promotes the loading of halloysite nanotubes with negative macromolecules, which are at the same time repelled from negatively charged external surfaces. A wide range of active agents, including drugs, nicotinamide adenine dineculeotide (NAD) and marine biocides, can be trapped in the internal lumen, as well as in the voids of multilayer aluminosilicate casings.

The smectitic clays of northwestern Tunisia (Kef area) shows a 23,89%  of CaO, 10%  of Al2O3,  4,51% of Fe2O3 and 29,48% of SiO2. The percentage of MgO achieved  5%.  This clay has 85% smectite, 10% kaolonite and a specific surface of 577m2/g and a C.E.C. of 69 meq / 100g. Diosmectite (DSM) extracted from smectite is a purified clay consisting of a double sheet of aluminum silicate and magnesium, indicated for the symptomatic treatment of diarrhea, also an antacid agent and as a protector of the gastrointestinal mucosa.

Recent Publication :

1. Technological Characterization and Industrial Application of Tunisian Clays from Makthar Area (Central Tunisia) in the Ceramic Industry .Jul 2016 Open Journal of Geology

2. Geological and technological characterization of the Late Jurassic-Early Cretaceous clay deposits (Jebel Ammar, Northeastern Tunisia) for ceramic industry. January 2017Journal of African Earth Sciences

3. Late Cretaceous and Palaeocene clays of the northern Tunisia: Potential use for manufacturing clay products. Mar 2015Arabian Journal of Geosciences

4. Reconstruction of the Late Cretaceous-Paleocene paleoenvironment (northern Tunisia) from biostratigraphy, geochemistry and clay mineralogy. Nov 2015Arabian Journal of Geosciences

5. Characterization of the Ain Khemouda Halloysite (western Tunisia) for potential use in ceramic manufacturing. Jul 2015Journal of African Earth Sciences

Biography (150 mots)

Ms. Moufida Ben M'Barek-Jemaï have more than 18 years of experience as a teacher at the university  of Science of Bizerte. I have extensive and varied experience in the field of geomaterials, clay Palenvironnement  and clay geochemistry. Since 2010 I works closely and in a consultative approach as an expert in a research laboratory of: Geomaterials. I have 18 international publications. I ensured supervision of a 30th of students in Master and 3 doctoral thesis, I was named member in several scientific commutes. I participated in projects in the field of geomaterials mainly in the field of clays and their industrial applications.

In addition to her local work, I has participated in several scientific events as a speaker in expertise field related to geology, mineralogy and paleontology.

Email : benmbarek_moufida@hotmail.fr