Title: Development of chitosan coated calcium-alginate nanocapsules for oral delivery of liraglutide to diabetic patients

Name: Fatemeh Shamekhi

Tarbiat Modares University, Tehran, Iran

Increasing prevalence, variable pathogenesis and natural history of progressive type II diabetes, highlight the necessity of immediate development of new therapeutic strategies Glucagon-like peptide-1 receptor agonists are a new class of injectable antidiabetic drugs. Chitosan coated calcium-alginate nanocapsules were developed for oral sustained delivery of liraglutide, a long-acting analog of glucagon like peptid-1. The aim of such drug delivery system is to recover diabetic patient compliance which otherwise demands prolonged repeatedly injections. The effect of coating components including sodium alginate, calcium chloride and chitosan concentrations on the particle size was studied based on response surface methodology. The beads were characterized through dynamic light scattering (DLS), scanning and transmission electron microscopy (SEM and TEM) as well as fourier transform infrared spectroscopy (FTIR). It was shown that the diameter of the formed beads was most dependent on the encapsulation technique and alginate concentration. SEM revealed spherical and smooth particles of up to 100 nm diameter for optimum composition of alginate 0.5%, chitosan 0.5% and calcium chloride 0.5% in the ratio of 3:1:1. The resulting bead formulation had a loading efficiency of 92.5% and loading capacity of 54.16 %. In-vitro release studies in simulated gastrointestinal conditions were carried out in a sequential technique and the amount of drug release was found to be 39.1% after 8 hours. The MTT results of developed nanocarrier revealed up to 52.05% viability enhancement compared to free drug in 0.3 mg concentration. The results of this study demonstrated that chitosan coated calcium-alginate nanoparticles hold promise as a potential natural biodegradable polymer-based oral carrier of liraglutide for better management of diabetes.

Biography

Dr. Fatemeh Shamekhi has her expertise in encapsulation methods and optimization techniques of coating components for oral drug delivery. She had her specific focus on nanostructures and their characterization methods as well as their behavior through simulated gastrointestinal tract condition (in vitro models).

She has extensive experience in the academic field which extends to more than 10 years. She is currently a Lecturer at Azad University. She earned her Ph.D. degree in Nano-biotechnology from Tarbiat Modares University in 2018. Her master degree was in Enzyme Biotechnology from University Putra Malaysia. She published many peer-reviewed papers in Scopus indexed journals with impact factor as well as conference papers.

Dr.   Fatemeh   Shamekhi   has  her   expertise   in

encapsulation   methods   and   optimization

techniques   of   coating   components   for   oral

drug delivery. She had her specific focus on

nanostructures   and   their   characterization

methods   as   well   as   their   behavior   through

simulated   gastrointestinal   tract   condition   (in

vitro models).

She has extensive experience in the academic

field which extends to more than 10 years. She

is currently a Lecturer at Azad University. She

earned   her   Ph.D.   degree   in   Nano-

biotechnology   from   Tarbiat   Modares

University in 2018. Her master degree was in

Enzyme Biotechnology from University Putra

Malaysia. She published many peer-reviewed

papers in Scopus indexed journals with impact

factor as well as conference papers

Dr.   Fatemeh   Shamekhi   has  her   expertise   in

encapsulation   methods   and   optimization

techniques   of   coating   components   for   oral

drug delivery. She had her specific focus on

nanostructures   and   their   characterization

methods   as   well   as   their   behavior   through

simulated   gastrointestinal   tract   condition   (in

vitro models).

She has extensive experience in the academic

field which extends to more than 10 years. She

is currently a Lecturer at Azad University. She

earned   her   Ph.D.   degree   in   Nano-

biotechnology   from   Tarbiat   Modares

University in 2018. Her master degree was in

Enzyme Biotechnology from University Putra

Malaysia. She published many peer-reviewed

papers in Scopus indexed journals with impact

factor as well as conference papers

Presenting author details 
Full name: Seyedeh Fatemeh Shamekhi
Contact number: +989128209158
Category: (Oral presentation)