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Title: Glipizide-PEOX (Poly-2-ethyl-2-oxazoline): Novel Solid Dispersion for Solubility and Dissolution Rate Enhancement 
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PEOX (poly 2-ethyl-2-oxazoline), a biocompatible non-ionic polymer, was employed for the first time to prepare solid dispersion with glipizide (GPZ), a BCS class II model drug, to enhance its solubility and dissolution rate. PEOX-GPZ Solid dispersion was compared to another commonly used polymer in solid dispersions, namely polyvinylpyrrolidone (PVP). The solid dispersions and their physical mixtures with glipizide were characterized and investigated by X-Ray diffractometry, differential scanning calorimetry, scanning electron microscopy, and Fourier transform infrared spectroscopy. The solubility and dissolution profile of prepared solid dispersions and their physical blends were in-vitro examined and evaluated. A significant enhancement in glipizide solubility was obtained with PEOX compared to the pure drug and PVP, despite slight crystallinity of glipizide in solid dispersion with PEOX compared to amorphous form in solid dispersion with PVP. A big improvement of the intrinsic dissolution rate and dissolved amount was also achieved with PEOX and PVP both in phosphate buffer at pH 6.8 and in FaSSIF (fasted state simulated intestinal fluid). Moreover, two molecular weights of PEOX were tested and PEOX 5K was superior to PEOX 50K in the dissolution behaviour. In conclusion, the findings of this study indicate a very promising formulation toward better glipizide bioavailability.  
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Dissolution profile of GPZ and its SDs with PEOX 1:2, PEOX 1:3, PVP 1:1 and PVP 1:2 at full sequence of pHs (1.5, 4.0, 5.5 and 6.8) each pH lasts for 30 minutes.
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		20.65543		20.7458		20.64665		20.76223		20.65578
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		24.26963		24.3651		24.26015		24.39923		24.27368

		24.78413		24.8818		24.77705		24.91623		24.79028

		25.30313		25.3998		25.29265		25.43253		25.30628

		25.81923		25.9169		25.80985		25.95023		25.82268

		26.33513		26.4321		26.32655		26.46853		26.33968

		26.85243		26.9498		26.84355		26.98483		26.85598

		27.36843		27.4691		27.35805		27.50083		27.37068

		27.88443		27.9858		27.87355		28.01753		27.88698

		28.39973		28.5048		28.39305		28.53423		28.40368
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		36.32743		36.4409		36.23715		36.55853		36.23728

		36.84163		36.9599		36.75505		37.07633		36.75678

		37.35813		37.4771		37.27405		37.59303		37.27548

		37.87713		37.9961		37.78835		38.10983		37.79448

		38.39473		38.5124		38.30605		38.62883		38.31048

		38.91093		39.0271		38.82215		39.14773		38.82728

		39.42573		39.5458		39.33805		39.66333		39.34478

		39.94343		40.0651		39.85705		40.18123		39.86278

		40.46073		40.5839		40.37555		40.69733		40.37868

		40.97613		41.1021		40.89135		41.21573		40.89618

		41.49323		41.6193		41.40615		41.73233		41.41168

		42.01223		42.1344		41.92185		42.25183		41.92948

		42.53093		42.6511		42.44115		42.77083		42.44498

		43.04663		43.1659		42.95835		43.28853		42.96278

		43.56273		43.6818		43.47455		43.80383		43.47998

		44.07913		44.2008		43.98855		44.31853		43.99578

		44.59463		44.7166		44.50435		44.83383		44.51248

		45.11123		45.2346		45.02165		45.35203		45.03078

		45.62843		45.7534		45.54065		45.87223		45.54628

		46.14743		46.2693		46.05685		46.38773		46.06228

		46.66173		46.7896		46.57315		46.90423		46.57968

		47.17763		47.3066		47.09215		47.41983		47.09668

		47.69243		47.8234		47.60885		47.93773		47.61578

		48.20673		48.3399		48.12685		48.45523		48.13248

		48.72373		48.8559		48.64685		48.97103		48.64678

		49.23863		49.3726		49.16305		49.48883		49.16298

		49.75443		49.8919		49.67705		50.00433		49.67768

		50.27113		50.4096		50.19435		50.52103		50.19568

		50.78823		50.9271		50.71385		51.04003		50.71328

		51.30543		51.4458		51.23005		51.56153		51.22998

		51.82073		51.9618		51.74585		52.08233		51.74668

		52.33813		52.4786		52.26405		52.60053		52.26378

		52.85523		52.9956		52.78305		53.11803		52.78148

		53.37063		53.5159		53.30105		53.63533		53.29818

		53.88643		54.0326		53.81755		54.15253		53.81578

		54.40243		54.5479		54.33305		54.66983		54.33148

		54.92213		55.0661		54.85015		55.18703		54.84848

		55.43923		55.5828		55.36755		55.70603		55.36718

		55.95473		56.0994		55.88385		56.22273		55.88378

		56.47263		56.6201		56.40005		56.73833		56.40048

		56.99043		57.1373		56.91815		57.25473		56.91478

		57.50573		57.6539		57.43855		57.77373		57.43078

		58.02293		58.1696		57.95565		58.29183		57.94748

		58.54113		58.6841		58.47235		58.80833		58.46278

		59.05763		59.2011		58.98885		59.32523		58.97818

		59.57443		59.7174		59.50785		59.84223		59.49268

		60.08993		60.2328		60.02415		60.35933		60.01048

		60.60593		60.7521		60.54455		60.87553		60.52828

		61.12193		61.2683		61.05885		61.39083		61.04448

		61.63813		61.7878		61.57585		61.90783		61.56068

		63.22013		63.4211		63.15605		63.48883		63.13178

		63.73723		63.9378		63.67705		64.00673		63.64748

		64.25393		64.4539		64.19135		64.52333		64.16568

		64.76923		64.9688		64.71335		65.04003		64.68078

		65.28543		65.4846		65.23105		65.55673		65.19668

		65.80443		66.0044		65.74965		66.07923		65.71698

		66.32013		66.5214		66.26805		66.59583		66.23328

		66.83623		67.0404		66.78755		67.11253		66.75028

		67.35063		67.5594		67.30465		67.62753		67.26578

		67.87013		68.0748		67.82135		68.14273		67.78128

		68.38673		68.5919		68.33855		68.66073		68.29798

		68.90163		69.1073		68.85515		69.17603		68.81568

		69.41513		69.6226		69.37285		69.69273		69.32998
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		70.44823		70.6583		70.40555		70.73103		70.35998

		70.96493		71.1774		70.92315		71.24873		70.87668

		71.48093		71.6976		71.44035		71.76623		71.39348

		71.99513		72.2133		71.95935		72.28303		71.91018

		72.50993		72.7309		72.47585		72.79823		72.42768
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		74.05663		74.2826		74.03185		74.35253		73.97898

		74.57373		74.8029		74.54955		74.86803		74.49618

		75.08913		75.3184		75.06455		75.38583		75.01198

		75.60623		75.8339		75.58015		75.90753		75.52718

		76.12293		76.3548		76.10235		76.42523		76.04528

		76.63823		76.8706		76.61905		76.94073		76.56048

		77.15123		77.3874		77.13515		77.45803		77.07728

		77.66663		77.9076		77.65235		77.97553		77.59478

		78.18463		78.4239		78.17105		78.49303		78.11148

		78.70393		78.9411		78.68905		79.01353		78.63278

		79.22113		79.4594		79.20515		79.53153		79.14948

		79.73493		79.9771		79.72265		80.04673		79.66648

		80.24973		80.4951		80.23985		80.56483		80.18278

		80.76463		81.0114		80.75615		81.08353		80.69768

		81.28163		81.5299		81.27365		81.60153		81.21648

		81.79573		82.0483		81.79185		82.11823		81.73328

		82.31173		82.5654		82.30805		82.63283		82.25128

		82.82613		83.0841		82.82465		83.15283		82.76878

		83.34243		83.6036		83.34015		83.67003		83.28548

		83.85863		84.1234		83.85985		84.18903		83.80368

		84.37293		84.6416		84.37405		84.70573		84.32128

		84.88923		85.1578		84.88985		85.22403		84.83728

		85.40413		85.6738		85.40465		85.74183		85.35228

		85.91963		86.1916		85.91905		86.25753		85.86898

		86.43673		86.7091		86.43485		86.77603		86.38848

		86.95113		87.2266		86.95085		87.29173		86.90448

		87.46743		87.7429		87.47035		87.80933		87.42178

		87.98223		88.2609		87.98755		88.32603		87.93618

		88.49713		88.7791		88.50465		88.84353		88.45398

		89.01513		89.2979		89.02365		89.36273		88.97268

		89.52973		89.8131		89.53985		89.87933		89.48828

		90.04563		90.3289		90.05515		90.39553		90.00398

		90.56223		90.8443		90.57515		90.91173		90.52068

		91.07713		91.3619		91.09185		91.42873		91.03698

		91.59663		91.8813		91.61265		91.95023		91.55418

		92.11193		92.3979		92.13065		92.46573		92.06948

		92.62843		92.9136		92.64715		92.98203		92.58598

		93.14463		93.4298		93.16485		93.49823		93.10028

		94.93363		95.2256		94.96305		95.29153		94.88978

		95.45023		95.7436		95.48105		95.81053		95.40548

		95.96593		96.2616		95.99885		96.32653		95.92098

		96.48493		96.7786		96.51785		96.84253		96.43798

		97.00093		97.2986		97.04185		97.36253		96.95798

		97.51593		97.8186		97.56285		97.88053		97.47398

		98.03093		98.3346		98.07885		98.39753		97.99198

		98.54593		98.8516		98.59685		98.91353		98.50798

		99.06093		99.3676		99.11385		99.43053		99.02498

		99.57993		99.8866		99.63485		99.95153		99.54298

		100.09393		100.4046		100.15285		100.46853		100.06098

		100.60693		100.9246		100.66885		100.98453		100.57598

		101.12393		101.4406		101.18985		101.50253		101.09398

		101.64093		101.9566		101.70485		102.01753		101.60798

		102.15993		102.4786		102.22385		102.53653		102.12598

		102.67693		102.9976		102.73985		103.05253		102.64398

		103.19093		103.5126		103.25585		103.56853		103.16298

		103.70493		104.0286		103.77185		104.08653		103.68098

		104.21993		104.5436		104.28585		104.60253		104.19998

		104.73693		105.0606		104.80685		105.11953		104.71898

		105.25093		105.5766		105.32285		105.63653		105.23598

		105.76493		106.0926		105.84285		106.15353		105.75198

		106.27993		106.6106		106.35885		106.67053		106.26798

		106.79593		107.1266		106.87285		107.18753		106.78298

		107.31493		107.6446		107.39285		107.70753		107.30198

		107.82993		108.1616		107.90985		108.22253		107.82098

		108.34493		108.6776		108.42785		108.73953		108.33598

		108.86093		109.1946		108.94485		109.25553		108.85198

		109.37593		109.7096		109.45985		109.77053		109.36698

		109.89493		110.2286		109.97885		110.28953		109.88798

		110.41093		110.7446		110.49485		110.80453		110.40598

		110.92593		111.2606		111.01085		111.32153		110.92098

		111.44293		111.7786		111.52785		111.83753		111.43798

		111.95693		112.2946		112.04285		112.35553		111.95398

		112.47393		112.8146		112.56185		112.87253		112.47498

		112.98993		113.3306		113.07685		113.38853		112.99198

		113.50393		113.8476		113.59185		113.90353		113.51098

		114.02093		114.3626		114.10685		114.42053		114.02698

		114.53493		114.8776		114.62385		114.93753		114.54598

		115.05493		115.3976		115.14385		115.45653		115.06598

		115.57093		115.9126		115.66185		115.97553		115.58498

		116.08693		116.4276		116.17785		116.49353		116.10298

		116.60093		116.9446		116.69485		117.00853		116.62098

		117.11793		117.4596		117.20885		117.52553		117.13998

		117.63693		117.9806		117.72785		118.04553		117.65998

		118.15393		118.4956		118.24485		118.56353		118.17598

		118.66893		119.0126		118.76185		119.07753		118.69198

		119.18393		119.5316		119.27685		119.59353		119.20598

		119.69993		120.0486		119.79485		120.11053		119.72098

		120.21793		120.5696		120.31285		120.63153		120.23998

		120.73493		121.0866		120.82885		121.14853		120.75698

		121.25093		121.6016		121.34385		121.66553		121.27398

		121.76593		122.1176		121.86085		122.18153		121.79198

		122.28193		122.6336		122.37485		122.69653		122.30798

		122.80193		123.1546		122.89285		123.21653		122.82798

		123.31693		123.6726		123.41085		123.73453		123.34298

		123.82993		124.1896		123.92485		124.24953		123.85898

		124.34593		124.7066		124.44285		124.76753		124.37498

		124.86093		125.2236		124.95785		125.28453		124.89198
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314.609

37.6113

3.5933

52.7149

52.0101

342.599

39.7686

3.6561

54.5489

53.6952

368.343

42.3661

4.37268

55.9691

57.4704

390.509

44.9157

4.69985

59.2524

58.7159

408.799

46.7905

5.19696

60.8809

62.0059

424.208

49.1554

5.39825

62.5847

63.8189

436.89

51.0858

4.85072

63.95

65.5631

449.715

53.6451

5.25452

65.186

67.6846

461.088

55.3411

5.39198

65.985

69.2616

469.957

56.5265

5.01972

67.7696

70.8329

476.435

58.856

5.37026

69.3802

71.6111

481.968

60.9508

5.61235

70.4483

72.8645

486.241

63.1976

4.88932

70.132

75.0646

490.563

64.0041

5.60924

72.1421

75.5748

493.894

65.6058

5.81417

72.6811

78.4955

496.969

66.5905

5.89386

73.7249

77.3798

499.658

69.3286

6.16529

74.7711

79.6673

501.035

71.3495

6.0779

75.3261

79.2154

502.021

73.6732

6.21655

75.8121

80.7294

500.773

75.9705

6.35158

77.3089

81.8682

500.669

78.9663

5.77284

78.7651

81.6332

499.11

80.9326

6.22506

79.1597

82.3747

495.607

83.3257

6.4062

80.5233

82.9173

493.715

84.281

5.93422

82.3771

83.8861

491.599

86.7128

6.52371

83.4044

83.4627

488.804

90.4765

6.12004

85.0778

85.9998

485.198

88.7838

6.64909

86.4479

84.8666

482.752

91.4244

6.44314

91.7819

88.1654

479.533

93.6118

6.80042

96.0703

86.5239

476.435

96.467

5.97075

98.085

89.2064

471.224

98.6871

6.61581

100.437

89.0999

468.356

100.99

6.72129

101.68

90.2767

463.756

98.4869

7.07465

106.728

90.8624

459.776

102.353

6.98132

104.291

89.495

454.275

103.665

6.91263

105.709

91.5174

448.117

107.126

6.85811

108.828

93.3582

439.569

106.202

6.89151

110.019

92.3779

431.389

109.119

7.19697

110.442

90.4963

422.255

110.113

7.02273

113.782

93.6766

413.74

110.359

6.82324

113.732

93.1471

405.755

111.596

7.33506

112.898

93.389

396.85

113.724

7.5185

114.938

94.9921

389.544

114.449

7.22993

115.605

94.6657

381.003

117.861

7.44805

118.338

94.4435

372.8

117.118

6.90892

117.329

94.7514

365.176

115.075

7.25318

118.789

96.0043

356.796

121.781

7.38183

118.629

96.0059

349.343

121.092

7.76419

121.241

96.3183

342.401

122.684

7.64505

124.435

96.3988

333.593

122.246

7.65454

123.064

97.7658

327.373

121.939

7.17478

122.513

98.1708

320.604

123.059

7.81242

125.724

96.8593

313.979

121.113

7.89113

124.375

95.9193

306.845

126.441

7.39435

125.086

98.7945

300.264

127.954

7.69857

219.347

172.726

324.119

210.291

11.5002

215.472

166.397

318.965

204.367

12.4178

216.121

162.928

313.42

205.261

12.9878

210.239

158.597

308.221

195.991

12.6468

210.347

155.775

303.934

197.538

12.6809

210.324

153.022

299.353

194.816

13.1452

205.967

152.526

295.123

192.869

12.6189

202.152

149.272

291.531

190.927

13.0881

205.254

147.6

286.511

192.628

12.5011

203.723

144.219

282.222

191.137

12.8982

203.098

143.776

279.671

187.914

13.5741

197.306

140.76

275.348

192.032

13.0709

201.331

140.078

271.561

190.452

13.482

200.1

140.039

267.71

187.768

13.1747

200.419

137.133

264.877

185.829

13.3116

196.621

138.042

260.778

191.552

13.1537

200.091

137.15

257.979

189.455

13.2646

196.656

134.613

254.894

187.097

13.6062

194.777

134.843

251.671

190.901

13.0198

204.263

135.259

248.485

193.919

12.8409

203.59

132.453

245.337

192.168

12.9446

208.432

133.796

243.002

192.795

13.4861

202.886

133.186

239.84

192.014

13.2768

207.243

132.088

237.002

190.623

13.351

204.712

128.953

233.715

190.681

13.2871

207.208

129.154

231.525

193.892

13.2347

206.061

129.528

229.058

193.286

13.1467

209.682

128.795

227.044

194.371

12.8585

206.405

127.787

223.564

190.848

13.0138

207.771

128.76

220.522

192.273

13.2226

212.421

126.26

219.839

195.39

12.9891

207.483

126.704

216.821

198.623

13.5273

209.286

128.626

214.295

199.655

13.2433

210.01

125.346

212.392

195.489

13.3878

206.615

125.391

209.849

197.141

13.0554

209.279

127.428

207.489

198.849

12.4123

210.309

126.469

205.551

198.5

13.2748

207.614

125.264

203.53

199.924

13.1812

209.793

124.155

200.815

197.977

13.3365

209.483

126.223

198.258

201.804

13.2892

206.629

124.77

197.456

205.526

13.174

214.341

123.153

194.788

203.806

13.421

214.82

123.679

191.548

203.148

13.4002

214.662

121.647

190.459

206.114

13.2216

212.783

123.687

189.283

205.105

12.6064

215.523

123.67

186.421

206.841

13.4078

214.393

123.702

184.38

208.552

13.3184

224.338

123.968

183.763

209.767

13.7112

227.345

124.572

181.264

206.643

13.468

226.016

122.788

180.055

210.268

13.7052

228.291

123.818

178.178

211.411

13.3895

229.929

123.064

176.153

212.609

14.2743

233.037

123.884

174.061

212.734

13.0801

224.071

122.194

172.242

215.086

12.9385

230.924

123.146

171.568

216.252

12.7592

232.139

122.779

170.59

214.865

13.8277

224.259

121.897

169.438

216.769

13.9357

228.98

120.367

167.683

220.178

13.2599

232.979

123.927

166.132

220.628

13.7364

333.906

182.914

188.742

270.099

13.5086

337.417

184.925

190.459

281.31

13.4551

343.896

187.829

191.302

281.031

14.024

347.22

187.587

193.028

279.351

13.2998

357.22

188.611

195.776

286.236

13.9298

360.89

190.496

196.102

288.66

13.6325

358.417

191.668

197.883

286.033

13.86

366.976

190.128

198.677

290.129

14.0521

363.701

194.051

199.964

297.538

13.9198

373.884

191.953

199.612

293.004

13.8875

380.612

192.678

201.593

296.115

13.9697

376.14

196.482

202.86

295.972

14.4625

384.001

195.365

203.659

298.594

14.4139

380.504

197.55

204.493

298.281

14.4092

387.916

196.455

205.72

299.769

14.7062

389.656

194.287

205.291

302.065

14.3492

388.873

197.245

206.519

305.659

14.5598

377.067

197.408

207.427

302.866

14.9788

388.941

195.971

208.233

310.204

15.124

400.863

196.108

209.429

314.229

15.0359

387.217

198.261

209.413

306.314

14.9701

394.235

196.496

211.126

309.579

15.2219

395.901

200.036

211.289

309.115

15.1877

390.398

198.458

211.465

310.977

15.2842

401.654

200.288

213.272

312.755

15.0217

393.131

198.902

213.295

308.481

16.1979

411.604

199.837

213.439

318.962

15.3935

407.674

202.435

214.883

320.346

15.8844

409.125

199.711

215.117

323.951

15.4401

418.999

200.49

216.096

325.759

16.0061

428.888

200.252

215.897

322.739

15.4982

426.463

209.691

217.248

325.33

16.0417

434.784

211.022

218.041

322.152

15.5253

441.935

211.192

217.891

327.313

14.9313

443.924

214.286

218.333

336.85

16.3351

440.712

213.752

219.737

337.858

16.0673

442.522

214.015

220.523

329.313

15.9961

444.983

214.859

222.262

338.469

15.6983

451.163

216.7

220.67

340.349

15.9116

453.721

215.711

221.286

340.602

16.2627

468.187

215.15

222.205

338.02

16.5628

469.261

217.353

222.769

347.053

16.7382

453.017

215.07

223.531

348.58

16.0627

467.873

217.097

224.043

356.41

16.1962

464.01

219.661

224.872

348.974

16.2816

475.498

221.773

225.121

351.913

16.4721

470.786

216.591

225.605

353.682

16.1977

484.695

220.868

226.9

356.916

16.4831

493.42

221.081

227.292

350.056

16.4032

497.445

221.312

226.965

358.864

17.0974

502.693

218.794

227.985

360.612

16.648

503.023

223.841

227.89

356.936

16.7124

496.285

221.033

228.392

367.176

16.8697

494.616

223.285

229.516

367.399

16.9481

500.348

225.246

230.18

373.727

16.9415

508.72

221.776

231.835

365.689

16.7462

504.076

220.934

230.755

368.128

16.7105

509.85

225.023

231.089

374.97

17.6249

508.93

226.171

232.771

382.06

17.4152

1744.33

1088.72

521.697

1018.97

19.3387

1888.89

1172.31

580.798

1069.49

20.0416

1981.1

1222.57

631.316

1110.1

20.3898

2049.31

1266.56

675.571

1137.72

20.6035

2103.84

1305.82

710.127

1163.67

21.6337

2196.76

1313.64

740.967

1180.8

22.6663

2238.22

1322.41

770.218

1196.84

22.4276

2245.03

1346.25

792.009

1213.47

22.9685

2280.49

1360.37

815.407

1225.71

23.8344

2296.71

1374.16

834.623

1240.13

23.953

2328.04

1387.39

852.375

1256.42

24.3037

2330.58

1395.21

871.266

1267.7

25.4893

2378.78

1404.58

884.8

1271.7

25.9696

2405.46

1414.6

899.299

1284.3

25.1605

2400.86

1415.38

912.131

1289.48

26.7864

2380.85

1415.86

925.132

1316.21

27.2879

2418.52

1436.35

936.431

1319.96

27.9728

2485.57

1427.65

947.309

1320.05

29.0831

2453.4

1434.36

955.935

1334.48

29.0723

2471.88

1435.87

966.822

1331.16

29.8248

2558.95

1442.9

977.438

1340.97

29.37

2564.89

1451.92

985.857

1342.08

30.0683

2583.08

1440.1

992.771

1353.98

29.6182

2578.06

1453.29

1000.19

1345.05

31.2247

2595.63

1457.41

1007.24

1353.72

30.5334

2623.12

1458.81

1015.84

1379.44

32.3002

2596.99

1462.15

1021.13

1377.18

32.4927

2610.01

1470.97

1029.61

1381.3

33.3334

2610.67

1473.88

1035.56

1380.65

33.0639

2628.7

1483.84

1040.7

1367.47

33.8884

2650.12

1481.38

1045.84

1393.33

34.7608

2606.85

1496.6

1053.98

1392.13

34.9122

2637.83

1499.75

1059.26

1405.77

34.9211

2635.89

1499.71

1064.25

1397.69

35.3567

2646.26

1500.68

1068.71

1401.87

35.974

2647.7

1507.49

1075.24

1414.92

36.9903

2675.55

1503.62

1077.62

1410.06

37.3261

2691.69

1512.12

1080.3

1416.05

38.1163

2665.05

1500.71

1090.12

1423.98

37.7857

2677.38

1510.46

1091.37

1431.42

38.5586

2684.12

1509.03

1094.85

1435.76

39.331

2697.82

1530.92

1096.41

1434.46

38.1976

2699.81

1537.97

1102.66

1443.47

39.4338

2675.95

1525.13

1106.8

1457.23

40.034

2676.13

1549.11

1108.99

1443.99

40.2066

2686.53

1536.42

1115.26

1459

41.1115

2708.19

1596.56

1114.59

1443.91

40.5824

2721.83

1603.5

1119.16

1465.22

41.9113

2739.61

1619.03

1124.53

1455

42.4756

2720.38

1694.66

1125.12

1458.21

42.9773

2684.21

1717.77

1128.19

1480.48

43.04

2761.86

1753.22

1134.43

1462.56

43.7465

2680.8

1771.14

1133.93

1471.55

43.9405

2736.31

1769.23

1138.59

1485.83

43.8085

2737.9

1770.17

1140.29

1475.43

45.1326

2752.84

1768.95

1142.58

1486.69

45.5357

2780.61

1850.1

1148.31

1476.04

46.4376

2786.63

1801.22

1150.26

1483.18

46.655

2752.09

1875.35

1156.79

1500.57

46.89



CALCULATION

		

		Experiment		File		Medium		Dissolved amount		IDR		% Dissolved at the end		IDR (mg/min/cm2)

		GLP		17B-26003		1.5		0.008		3.64		0.14		0.0036				pH		GLP		GLP-PEOX 5K 1:2		GLP-PEOX 50K 1:2		GLP-PVP 1:1		GLP-PVP 1:2

		GLP		17B-26001		1.5		0.018		6.97		0.33		0.0070				1.5		0.013		0.099		0.070		0.128		0.111

		GLP						0.013		5.31		0.24		0.005				4.0		0.019		0.124		0.117		0.221		0.114

		GLP-PVP 1:1		17B-27001		1.5		0.128		65.15		2.78		0.0652				5.5		0.020		0.226		0.221		0.382		0.146

		GLP-PVP 1:2		17C-09018		1.5		0.111		186.14		2.77		0.1861				6.8		0.047		1.875		0.948		1.501		1.501

		GLP-PEOX 5K 1:2		17B-27015		1.5		0.099		89.00		1.93		0.0890

		GLP-PEOX 50K 1:2		17B-27017		1.5		0.070		43.24		1.49		0.0432

		GLP		17B-26003		4		0.014				0.26

		GLP		17B-26001		4.0		0.024				0.44

		GLP						0.019				0.35

		GLP-PVP 1:1		17B-27001		4		0.221				4.79

		GLP-PVP 1:2		17C-09018		4		0.114				2.84

		GLP-PEOX 5K 1:2		17B-27015		4		0.124				2.42

		GLP-PEOX 50K 1:2		17B-27017		4		0.117				2.47

		GLP		17B-26003		5.5		0.017				0.33

		GLP		17B-26001		5.5		0.023				0.42

		GLP						0.020				0.37

		GLP-PVP 1:1		17B-27001		5.5		0.382				8.30

		GLP-PVP 1:2		17C-09018		5.5		0.146				3.65

		GLP-PEOX 5K 1:2		17B-27015		5.5		0.226				4.41

		GLP-PEOX 50K 1:2		17B-27017		5.5		0.221				4.68

		GLP		17B-26003		6.8		0.047		3.64		0.88		0.0036

		GLP		17B-26001		6.8		0.047		6.97		0.86		0.0070										Buffer		Buffer		FASSIF		FASSIF

		GLP						0.047				0.87		0.01						Solid Dispersion		Physical Mixture		Intrinsic Dissolution Rate		Dissolved Amount		Intrinsic Dissolution Rate		Dissolved Amount

		GLP-PVP 1:1		17B-27001		6.8		1.501		572.65		32.58		0.5727				GLP				0.043		19.3		0.043		45.7		34.2				91.856869762

		GLP-PVP 1:2		17C-09018		6.8		1.501		970.38		34.04		0.9704				GLP-PEOX 1:2		1.099		0.083		755.4		1.099		967.3		987.9				63.2075926942		38.0783415027

		GLP-PEOX 5K 1:2		17B-27015		6.8		1.875		671.96		36.55		0.6720				GLP-PEOX 1:3		1.627		0.090		1218.8		1.627		2097.1		2199.6				39.1778897456		45.8486712977

		GLP-PEOX 50K 1:2		17B-27017		6.8		0.948		549.43		20.11		0.5494				GLP-PVP 1:1		1.086		0.183		640.0		1.086		461.0		498.7				33.191336711		64.3265031584

														0.0000				GLP-PVP 1:2		2.197		0.192		1771.2		2.197		1545.8		1143.4

																				PEOX 5K 1:2		PEOX 5K 1:3		PEOX 50K 1:2		PEOX 50K 1:3

																				Intrinsic Dissolution Rate		Intrinsic Dissolution Rate		Intrinsic Dissolution Rate		Intrinsic Dissolution Rate

																		Buffer		755.4		1218.789		84.3		234.4

																		FaSSIF		967.3		2097.078		177.9		154.3





CALCULATION

		



GLP

GLP-PEOX 5K 1:2

GLP-PEOX 50K 1:2

GLP-PVP 1:1

GLP-PVP 1:2

Dissolved amount



GLP+PM

		



Solid Dispersion

Physical Mixture

Dissolved amount



GLP-PVP 11

		



IDR - FaSSIF

IDR - Buffer pH 6.8



GLP-PVP 12

		



Intrinsic Dissolution Rate

Dissolved Amount

BUFFER



GLP-PX 5K 12

		



IDR - FaSSIF

IDR - Buffer pH 6.8



GLP-PX 5K 13

		



PEOX 5K 1:2

PEOX 5K 1:3

PEOX 50K 1:2

PEOX 50K 1:3



GLP-PX 10K 13 

		



PEOX 5K 1:2

PEOX 5K 1:3

PEOX 50K 1:2

PEOX 50K 1:3



GLP-PX 25K 13

		GLP								445.54																GLP pH 6.8-1				17B-26005								GLP pH 6.8-2				17B-26007								GLP pH 6.8-3						GLP pH 6.8												GLP FaSSIF-1				17C-09001								GLP FaSSIF-2				17E-11001								GLP FaSSIF-3						GLP FaSSIF										GLP-PVP 1:1 PM				17B-28015								GLP-PVP 1:2 PM				17B-28017								GLP-PEOX 5K 1:2 PM				17B-28019								GLP-PEOX 50K 1:2 PM				17B-28021								GLP-PL 1:5 PM				17C-01001								GLP-PEG 1:5 PM				17C-01003								GLP-PX 1:3 PM				17k-09004

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/ml)		IDR (ug/min/cm2)

		GLP pH 6.8-1		17B-26005		0.051		5.04		1.00		5.04		1.01		1.51		21.5987

		GLP pH 6.8-2		17B-26007		0.034		5.05		1.00		5.05		0.68		1.17		16.7133				Dissolution Profile												Dissolution Profile												Dissolution Profile																		Dissolution Profile												Dissolution Profile												Dissolution Profile																Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile

						0.043										1.37		19.5349																																						AVERAGE				TIME		SD																																				AVERAGE		TIME		SD

		AVG				0.04273								0.848		1.3498		19.282				Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		%		Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		%		Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		mg		Weight (µg)						Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		%		Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		mg						Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		%		Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		%		Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		%		Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		%		Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		%		Time (minutes)		Amount (mols)				Weight (mg)		Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (µg)		Weight (mg)		Time zero (min)

		SD				0.00840								0.237		0.17167		2.452				5.03593		16.9765				0.0169765		0		0.3368353175		5.03307		13.7405				0.0137405		0		0.2720891089		5.034		15				0.015		0		0.015239		15.239		0.00		1.6311850753		1.88307		4.72456				0.00472456		0		0.0935556436		2.58022		-0.195557				-0.000195557		0		-0.0038724158		2.58022		0.0022645015						0		0.0022645015		0.00		0.0024600585		5.06328		14.3071				0.0143071		0		0.2794355469		5.04713		9.55478				0.00955478		0		0.2011532632		5.06797		10.3427				0.0103427		0		0.206854		5.0612		10.7029				0.0107029		0		0.212359127		5.1336		0				0		0		0		4.48698		0				0		0		0		5.01718		61.3935		24.511		0.0613935		0

		RSD				19.659								27.926		12.719		12.719				5.55182		18.1418				0.0181418		0.51589		0.3599563492		5.54973		14.2714				0.0142714		0.51666		0.2826019802		5.549		16				0.016		0.515		0.0161377333		16.1377333333		0.52		1.9388725831		1.9198		5.55463				0.00555463		0.03673		0.1099926733		3.09583		4.70065				0.00470065		0.51561		0.0930821782		3.09583		0.00512764						0.51561		0.00512764		0.36		0.00042699		5.58022		19.4524				0.0194524		0.51694		0.3799296875		5.56223		12.5881				0.0125881		0.5151		0.2650126316		5.5836		15.379				0.015379		0.51563		0.30758		5.575		14.1699				0.0141699		0.5138		0.2811488095		5.65365		0				0		0.52005		0		5.0073		0				0		0.52032		0		5.54037		24.5431		25.6158		0.0245431		0.52319

		GLP FaSSIF-1		17C-09001		0.029		5.05		1.00		5.05		0.58		2.22		31.74				6.07135		19.4759				0.0194759		1.03542		0.3864265873		6.06745		14.037				0.014037		1.03438		0.277960396		6.068		17				0.017		1.034		0.0168376333		16.8376333333		1.03		2.7230829042		2.4388		5.62946				0.00562946		0.55573		0.1114744554		3.61147		5.66916				0.00566916		1.03125		0.1122605941		3.61147		0.00564931						1.03125		0.00564931		0.87		0.00001985		6.09583		24.6502				0.0246502		1.03255		0.4814492188		6.07605		14.2018				0.0142018		1.02892		0.2989852632		6.09818		15.5472				0.0155472		1.03021		0.310944		6.0901		15.4066				0.0154066		1.0289		0.3056865079		6.17527		0				0		1.04167		0		5.52397		0				0		1.03699		0		6.05885		25.9915		26.7105		0.0259915		1.04167

		GLP FaSSIF-2		17E-11001		0.040		4.82		1.00		4.82		0.84		4.16		59.48				6.58647		20.2703				0.0202703		1.55054		0.4021884921		6.58307		14.7504				0.0147504		1.55		0.2920871287		6.611		17.6				0.0176		1.577		0.0175402333		17.5402333333		1.56		2.7604352996		2.95625		8.21291				0.00821291		1.07318		0.1626318812		4.125		9.3677				0.0093677		1.54478		0.1854990099		4.125		0.008790305						1.54478		0.008790305		1.39		0.000577395		6.61042		26.5817				0.0265817		1.54714		0.5191738281		6.59088		16.0661				0.0160661		1.54375		0.3382336842		6.61172		16.8696				0.0168696		1.54375		0.337392		6.60522		17.1354				0.0171354		1.54402		0.3399880952		6.69323		0				0		1.55963		0		6.04088		0				0		1.5539		0		6.57552		27.1458		27.8011		0.0271458		1.55834

						0.033										3.22		46.00				7.10287		21.0371				0.0210371		2.06694		0.4174027778		7.09765		15.0473				0.0150473		2.06458		0.2979663366		7.012		18				0.018		1.978		0.0180281333		18.0281333333		2.04		2.9949991024		3.47188		8.6838				0.0086838		1.58881		0.1719564356		4.64115		11.6699				0.0116699		2.06093		0.2310871287		4.64115		0.01017685						2.06093		0.01017685		1.90		0.00149305		7.12552		30.794				0.030794		2.06224		0.6014453125		7.1073		19.9472				0.0199472		2.06017		0.4199410526		7.12552		18.7964				0.0187964		2.05755		0.375928		7.12057		18.8642				0.0188642		2.05937		0.3742896825		7.21277		0				0		2.07917		0		6.55938		0				0		2.0724		0		7.08958		27.9466		28.8859		0.0279466		2.0724

		AVG		amount at		0.0342								0.71		3.20		45.74				7.61953		21.5162				0.0215162		2.5836		0.4269087302		7.61537		15.6133				0.0156133		2.5823		0.3091742574		7.621		18.5				0.0185		2.587		0.0185431667		18.5431666667		2.58		2.9516867421		3.98593		9.21822				0.00921822		2.10286		0.1825390099		5.15677		14.2327				0.0142327		2.57655		0.2818356436		5.15677		0.01172546						2.57655		0.01172546		2.42		0.00250724		7.64167		33.8099				0.0338099		2.57839		0.6603496094		7.6276		21.1897				0.0211897		2.58047		0.4460989474		7.6388		18.954				0.018954		2.57083		0.37908		7.63593		19.9355				0.0199355		2.57473		0.3955456349		7.73307		0				0		2.59947		0		7.08098		0				0		2.594		0		7.60598		29.0114		29.9753		0.0290114		2.5888

		SD		15 min		0.006								0.18		0.97		13.87				8.13515		22.1003				0.0221003		3.09922		0.4384980159		8.13203		15.9772				0.0159772		3.09896		0.316380198		8.133		19				0.019		3.099		0.0190258333		19.0258333333		3.10		3.061631742		4.50208		10.7269				0.0107269		2.61901		0.2124138614		5.67292		16.7271				0.0167271		3.0927		0.331229703		5.67292		0.013727						3.0927		0.013727		2.93		0.0030001		8.15677		37.2978				0.0372978		3.09349		0.7284726563		8.14453		22.6409				0.0226409		3.0974		0.4766505263		8.15495		20.3526				0.0203526		3.08698		0.407052		8.15105		23.0872				0.0230872		3.08985		0.4580793651		8.24948		0				0		3.11588		0		7.59948		0				0		3.1125		0		8.12292		30.264		31.0657		0.030264		3.10574

		RSD				16.502								25.75		30.33		30.33				8.64973		22.8796				0.0228796		3.6138		0.4539603175		8.64843		15.7902				0.0157902		3.61536		0.3126772277		8.651		19.4				0.0194		3.617		0.0193566		19.3566		3.62		3.5448992595		5.01823		11.5945				0.0115945		3.13516		0.2295940594		6.18802		17.6746				0.0176746		3.6078		0.3499920792		6.18802		0.01463455						3.6078		0.01463455		3.45		0.00304005		8.6724		39.6589				0.0396589		3.60912		0.7745878906		8.66068		25.5881				0.0255881		3.61355		0.5386968421		8.66848		23.4404				0.0234404		3.60051		0.468808		8.66718		24.0098				0.0240098		3.60598		0.4763849206		8.76875		0				0		3.63515		0		8.11745		0				0		3.63047		0		8.63907		33.5942		32.1541		0.0335942		3.62189

		GLP-PVP 1:1 PM		17B-28015		0.1833		5.12		1.00		5.12		3.58		6.3		90.0				9.16667		23.8191				0.0238191		4.13074		0.4726011905		9.16588		18.462				0.018462		4.13281		0.3655841584		9.171		21.1				0.0211		4.137		0.0211270333		21.1270333333		4.13		2.678652311		5.5323		15.2487				0.0152487		3.64923		0.3019544554		6.70313		20.1803				0.0201803		4.12291		0.399609901		6.70313		0.0177145						4.12291		0.0177145		3.97		0.0024658		9.18985		43.6288				0.0436288		4.12657		0.852125		9.17527		27.2877				0.0272877		4.12814		0.5744778947		9.18438		24.7595				0.0247595		4.11641		0.49519		9.18333		25.1984				0.0251984		4.12213		0.499968254		9.28672		0				0		4.15312		0		8.6349		0				0		4.14792		0		9.15417		33.0495		33.24		0.0330495		4.13699

		GLP-PVP 1:2 PM		17B-28017		0.1923		4.75		1.00		4.75		4.05		4.5		64.1				9.68307		24.3262				0.0243262		4.64714		0.4826626984		9.68307		18.9023				0.0189023		4.65		0.3743029703		9.693		21.6				0.0216		4.659		0.0216095		21.6095		4.65		2.7119624795		6.04843		14.1872				0.0141872		4.16536		0.2809346535		7.21848		20.8602				0.0208602		4.63826		0.4130732673		7.21848		0.0175237						4.63826		0.0175237		4.48		0.0033365		9.70547		44.1048				0.0441048		4.64219		0.861421875		9.68985		31.3552				0.0313552		4.64272		0.6601094737		9.69973		26.8357				0.0268357		4.63176		0.536714		9.69792		27.5043				0.0275043		4.63672		0.5457202381		9.80417		0				0		4.67057		0		9.15468		0				0		4.6677		0		9.66902		35.037		34.3252		0.035037		4.65184

		GLP-PEOX 5K 1:2 PM		17B-28019		0.0834		5		1.00		5.00		1.67		3.2		45.1				10.2011		24.9532				0.0249532		5.16517		0.4951031746		10.1987		19.4953				0.0194953		5.16563		0.3860455446		10.199		22.3				0.0223		5.165		0.0222495		22.2495		5.17		2.7293004214		6.56407		15.0187				0.0150187		4.681		0.2974		7.73385		23.0358				0.0230358		5.15363		0.4561544554		7.73385		0.01902725						5.15363		0.01902725		5.00		0.00400855		10.2229		49.4215				0.0494215		5.15962		0.9652636719		10.2031		32.8689				0.0328689		5.15597		0.6919768421		10.2141		27.971				0.027971		5.14613		0.55942		10.213		25.6317				0.0256317		5.1518		0.5085654762		10.3198		0				0		5.1862		0		9.67162		0				0		5.18464		0		10.1862		36.2203		35.4149		0.0362203		5.16902

		GLP-PEOX 50K 1:2 PM		17B-28021		0.0632		5.04		1.00		5.04		1.25		3.1		44.5				10.7206		26.4499				0.0264499		5.68467		0.5247996032		10.7172		20.1616				0.0201616		5.68413		0.399239604		10.721		23.3				0.0233		5.687		0.0233038333		23.3038333333		5.69		3.1441517526		7.07917		16.1977				0.0161977		5.1961		0.3207465347		8.24948		24.1503				0.0241503		5.66926		0.4782237624		8.24948		0.020174						5.66926		0.020174		5.51		0.0039763		10.7398		51.4756				0.0514756		5.67652		1.0053828125		10.7193		35.4417				0.0354417		5.67217		0.7461410526		10.7297		30.1373				0.0301373		5.66173		0.602746		10.7281		30.0331				0.0300331		5.6669		0.5958948413		10.9091		0				0		5.7755		0		10.1893		0				0		5.70232		0		10.7023		39.3168		36.5023		0.0393168		5.68512

		GLP-PX 1:3 PM		17k-09004		0.0875				1.00		0.00		0.00		2.1		30.1				11.2357		26.3681				0.0263681		6.19977		0.5231765873		11.2338		20.3558				0.0203558		6.20073		0.4030851485		11.231		23.4				0.0234		6.197		0.0233746333		23.3746333333		6.20		3.0062302678		7.59505		16.7221				0.0167221		5.71198		0.3311306931		8.76563		24.1874				0.0241874		6.18541		0.4789584158		8.76563		0.02045475						6.18541		0.02045475		6.03		0.00373265		11.2552		53.9919				0.0539919		6.19192		1.0545292969		11.2349		37.8167				0.0378167		6.18777		0.7961410526		11.2438		29.9096				0.0299096		6.17583		0.598192		11.2432		29.2113				0.0292113		6.182		0.5795892857		11.4294		0				0		6.2958		0		10.7104		0				0		6.22342		0		11.2177		37.889		37.5877		0.037889		6.20052

																						11.7529		27.0566				0.0270566		6.71697		0.5368373016		11.7513		20.7648				0.0207648		6.71823		0.4111841584		11.755		23.9				0.0239		6.721		0.0239071333		23.9071333333		6.72		3.1459060656		8.1099		17.4403				0.0174403		6.22683		0.3453524752		9.27968		24.6165				0.0246165		6.69946		0.4874554455		9.27968		0.0210284						6.69946		0.0210284		6.54		0.0035881		11.7721		57.1166				0.0571166		6.70882		1.1155585938		11.7495		41.3912				0.0413912		6.70237		0.8713936842		11.7576		31.8907				0.0318907		6.68963		0.637814		11.7594		30.9148				0.0309148		6.6982		0.6133888889		11.9492		0				0		6.8156		0		11.2287		0				0		6.74172		0		11.7336		39.2162		38.674		0.0392162		6.71642

																						12.2698		27.7016				0.0277016		7.23387		0.5496349206		12.2693		21.2145				0.0212145		7.23623		0.4200891089		12.271		24.4				0.0244		7.237		0.0244387		24.4387		7.24		3.2437231494		8.625		18.3666				0.0183666		6.74193		0.3636950495		9.79583		28.0847				0.0280847		7.21561		0.5561326733		9.79583		0.02322565						7.21561		0.02322565		7.06		0.00485905		12.2867		59.3998				0.0593998		7.22342		1.1601523438		12.268		43.9195				0.0439195		7.22087		0.9246210526		12.2727		33.1359				0.0331359		7.20473		0.662718		12.275		32.514				0.032514		7.2138		0.6451190476		12.4664		0				0		7.3328		0		11.7487		0				0		7.26172		0		12.25		39.4639		39.7611		0.0394639		7.23282

																						12.7857		28.3975				0.0283975		7.74977		0.5634424603		12.7849		21.6264				0.0216264		7.75183		0.4282455446		12.791		25				0.025		7.757		0.0250079667		25.0079666667		7.75		3.38555703		9.1401		19.3273				0.0193273		7.25703		0.3827188119		10.3099		27.5544				0.0275544		7.72968		0.5456316832		10.3099		0.02344085						7.72968		0.02344085		7.57		0.00411355		12.8016		62.7476				0.0627476		7.73832		1.2255390625		12.7841		46.662				0.046662		7.73697		0.9823578947		12.7872		34.4465				0.0344465		7.71923		0.68893		12.7904		32.8054				0.0328054		7.7292		0.6509007937		12.9826		488.086				0.488086		7.849		9.6842460317		12.269		0				0		7.78202		0		12.7656		41.4237		40.8463		0.0414237		7.74842

																						13.3018		28.6851				0.0286851		8.26587		0.5691488095		13.3026		21.7023				0.0217023		8.26953		0.4297485149		13.311		25.1				0.0251		8.277		0.0251624667		25.1624666667		8.27		3.4918190851		9.65598		20.3995				0.0203995		7.77291		0.403950495		10.825		27.8837				0.0278837		8.24478		0.5521524752		10.825		0.0241416						8.24478		0.0241416		8.09		0.0037421		13.3151		64.9118				0.0649118		8.25182		1.2678085938		13.3005		48.9881				0.0489881		8.25337		1.0313284211		13.3011		36.4211				0.0364211		8.23313		0.728422		13.3042		33.8189				0.0338189		8.243		0.6710099206		13.5003		486.671				0.486671		8.3667		9.6561706349		12.7893		0				0		8.30232		0		13.2818		42.635		41.9323		0.042635		8.26462

																						13.8164		29.3547				0.0293547		8.78047		0.5824345238		13.8193		22.5859				0.0225859		8.78623		0.4472455446		13.821		26				0.026		8.787		0.0259802		25.9802		8.78		3.3844434387		10.1703		20.239				0.020239		8.28723		0.4007722772		11.3417		31.4262				0.0314262		8.76148		0.6223009901		11.3417								8.76148		0.0258326		8.60		0.007910545		13.8313		67.9083				0.0679083		8.76802		1.3263339844		13.8156		53.2705				0.0532705		8.76847		1.1214842105		13.8164		36.8091				0.0368091		8.74843		0.736182		13.8198		34.5965				0.0345965		8.7586		0.6864384921		14.0151		495.852				0.495852		8.8815		9.8383333333		13.3115		0				0		8.82452		0		13.7992		43.9438		43.0208		0.0439438		8.78202

																						14.3323		29.8696				0.0298696		9.29637		0.5926507937		14.3359		23.1227				0.0231227		9.30283		0.4578752475		14.351		26.5				0.0265		9.317		0.0264974333		26.4974333333		9.31		3.3734507323		10.6857		24.2583				0.0242583		8.80263		0.4803623762		11.8557		31.7766				0.0317766		9.27548		0.629239604		11.8557								9.27548		0.02801745		9.12		0.0053162409		14.3492		71.1099				0.0711099		9.28592		1.3888652344		14.3307		56.0469				0.0560469		9.28357		1.1799347368		14.3318		40.0404				0.0400404		9.26383		0.800808		14.3359		35.822				0.035822		9.2747		0.7107539683		14.5302		483.606				0.483606		9.3966		9.5953571429		13.8307		0				0		9.34372		0		14.313		44.5842		44.1013		0.0445842		9.29582

																						14.8484		29.7455				0.0297455		9.81247		0.5901884921		14.8516		24.2748				0.0242748		9.81853		0.4806891089		14.855		27				0.027		9.821		0.0270067667		27.0067666667		9.82		2.7353562772		11.2021		23.0365				0.0230365		9.31903		0.4561683168		12.3719		31.5492				0.0315492		9.79168		0.6247366337		12.3719								9.79168		0.02729285		9.63		0.0060193879		14.8643		73.893				0.073893		9.80102		1.4432226562		14.8469		59.0672				0.0590672		9.79977		1.24352		14.8463		37.6046				0.0376046		9.77833		0.752092		14.8516		35.8239				0.0358239		9.7904		0.7107916667		15.0463		500.827				0.500827		9.9127		9.9370436508		14.3526		0				0		9.86562		0		14.8302		45.1534		45.1888		0.0451534		9.81302

																						15.3643		30.9932				0.0309932		10.32837		0.6149444444		15.3669		23.6031				0.0236031		10.33383		0.4673881188		15.378		27.3				0.0273		10.344		0.0272987667		27.2987666667		10.34		3.6950501544		11.7162		21.864				0.021864		9.83313		0.432950495		12.8859		32.3379				0.0323379		10.30568		0.6403544554		12.8859								10.30568		0.02710095		10.15		0.0074061657		15.3792		73.299				0.073299		10.31592		1.4316210938		15.3643		61.9224				0.0619224		10.31717		1.3036294737		15.3628		40.4633				0.0404633		10.29483		0.809266		15.3656		37.1678				0.0371678		10.3044		0.7374563492		15.5599		395.206				0.395206		10.4263		7.8413888889		14.8727		0				0		10.38572		0		15.3453		47.3655		46.2715		0.0473655		10.32812

																						15.8797		32.0944				0.0320944		10.84377		0.6367936508		15.8844		24.1009				0.0241009		10.85133		0.4772455446		15.893		28.1				0.0281		10.859		0.0280984333		28.0984333333		10.85		3.9967502303		12.231		25.0468				0.0250468		10.34793		0.4959762376		13.4013		33.3117				0.0333117		10.82108		0.6596376238		13.4013								10.82108		0.02917925		10.66		0.0058441668		15.895		77.7921				0.0777921		10.83172		1.5193769531		15.88		67.0391				0.0670391		10.83287		1.4113494737		15.8781		42.1996				0.0421996		10.81013		0.843992		15.882		38.3482				0.0383482		10.8208		0.7608769841		16.0768		449.652				0.449652		10.9432		8.9216666667		15.3932		0				0		10.90622		0		15.8596		46.7847		47.3524		0.0467847		10.84242

																						16.3974		32.7752				0.0327752		11.36147		0.6503015873		16.4005		24.4726				0.0244726		11.36743		0.4846059406		16.411		28.6				0.0286		11.377		0.0286159333		28.6159333333		11.37		4.1513229329		12.7479		25.0778				0.0250778		10.86483		0.496590099		13.918		34.6732				0.0346732		11.33778		0.6865980198		13.918								11.33778		0.0298755		11.18		0.0067849724		16.4104		80.6686				0.0806686		11.34712		1.5755585938		16.3956		68.9545				0.0689545		11.34847		1.4516736842		16.3932		43.3464				0.0433464		11.32523		0.866928		16.3979		39.1816				0.0391816		11.3367		0.7774126984		16.5912		410.26				0.41026		11.4576		8.1400793651		15.912		0				0		11.42502		0		16.3763		48.0369		48.4379		0.0480369		11.35912

																						16.9147		33.2121				0.0332121		11.87877		0.6589702381		16.9162		24.739				0.024739		11.88313		0.4898811881		16.923		29				0.029		11.889		0.0289837		28.9837		11.88		4.2365735176		13.2636		25.8443				0.0258443		11.38053		0.5117683168		14.4323		34.0396				0.0340396		11.85208		0.6740514851		14.4323								11.85208		0.02994195		11.69		0.0057949522		16.9247		82.6094				0.0826094		11.86142		1.6134648438		16.9125		72.8825				0.0728825		11.86537		1.5343684211		16.9088		44.1904				0.0441904		11.84083		0.883808		16.913		40.3368				0.0403368		11.8518		0.8003333333		17.1068		412.426				0.412426		11.9732		8.1830555556		16.4276		0				0		11.94062		0		16.8925		50.0363		49.5222		0.0500363		11.87532

																						17.432		34.9248				0.0349248		12.39607		0.692952381		17.4325		25.5082				0.0255082		12.39943		0.5051128713		17.438		30.2				0.0302		12.404		0.030211		30.211		12.40		4.7083096372		13.7792		28.1313				0.0281313		11.89613		0.5570554455		14.949		36.6083				0.0366083		12.36878		0.7249168317		14.949								12.36878		0.0323698		12.21		0.0059941442		17.438		85.4129				0.0854129		12.37472		1.6682207031		17.4258		76.1713				0.0761713		12.37867		1.6036063158		17.424		45.6439				0.0456439		12.35603		0.912878		17.4282		41.1846				0.0411846		12.367		0.8171547619		17.6223		307.602				0.307602		12.4887		6.1032142857		16.9473		0				0		12.46032		0		17.408		51.0341		50.6047		0.0510341		12.39082

																						17.9492		34.3838				0.0343838		12.91327		0.682218254		17.9492		25.4573				0.0254573		12.91613		0.5041049505		17.953		30				0.03		12.919		0.0299470333		29.9470333333		12.92		4.4634857078		14.2937		27.3083				0.0273083		12.41063		0.5407584158		15.4638		34.4697				0.0344697		12.88358		0.6825683168		15.4638								12.88358		0.030889		12.73		0.0050638745		17.9537		87.6262				0.0876262		12.89042		1.7114492187		17.9438		78.9669				0.0789669		12.89667		1.6624610526		17.9398		46.8598				0.0468598		12.87183		0.937196		17.9432		41.4145				0.0414145		12.882		0.8217162698		18.1367		306.469				0.306469		13.0031		6.080734127		17.4648		0				0		12.97782		0		17.9253		51.9845		51.6909		0.0519845		12.90812

																						18.4685		36.8173				0.0368173		13.43257		0.7305019841		18.4635		26.7702				0.0267702		13.43043		0.5301029703		18.472		31				0.031		13.438		0.0315291667		31.5291666667		13.43		5.0444095416		14.8094		28.1134				0.0281134		12.92633		0.5567009901		15.9787		37.3519				0.0373519		13.39848		0.7396415842		15.9787								13.39848		0.03273265		13.24		0.006532606		18.4693		91.1948				0.0911948		13.40602		1.7811484375		18.4588		82.3978				0.0823978		13.41167		1.7346905263		18.4552		48.2715				0.0482715		13.38723		0.96543		18.4593		42.3266				0.0423266		13.3981		0.8398134921		18.6537		340.642				0.340642		13.5201		6.7587698413		17.9833		0				0		13.49632		0		18.4403		52.5208		52.7718		0.0525208		13.42312

																						18.986		35.5922				0.0355922		13.95007		0.7061944444		18.9782		26.1191				0.0261191		13.94513		0.517209901		18.988		30.8				0.0308		13.954		0.0308371		30.8371		13.95		4.7366589713		15.3247		28.3798				0.0283798		13.44163		0.5619762376		16.4953		38.7373				0.0387373		13.91508		0.7670752475		16.4953								13.91508		0.03355855		13.76		0.0073238585		18.9842		92.4155				0.0924155		13.92092		1.8049902344		18.9773		86.0223				0.0860223		13.93017		1.8109957895		18.9722		48.7469				0.0487469		13.90423		0.974938		18.974		43.1128				0.0431128		13.9128		0.8554126984		19.1698		353.611				0.353611		14.0362		7.0160912698		18.5013		0				0		14.01432		0		18.9575		53.9263		53.8571		0.0539263		13.94032

																						19.5037		36.1002				0.0361002		14.46777		0.7162738095		19.4945		26.7651				0.0267651		14.46143		0.5300019802		19.512		31.4				0.0314		14.478		0.0314217667		31.4217666667		14.47		4.6675880649		15.8401		28.2332				0.0282332		13.95703		0.5590732673		17.0088		39.6541				0.0396541		14.42858		0.785229703		17.0088								14.42858		0.03394365		14.27		0.0080757958		19.4972		94.0781				0.0940781		14.43392		1.8374628906		19.4935		91.1473				0.0911473		14.44637		1.9188905263		19.4878		50.1367				0.0501367		14.41983		1.002734		19.4902		43.1187				0.0431187		14.429		0.8555297619		19.6838		330.15				0.33015		14.5502		6.5505952381		19.0222		0				0		14.53522		0		19.4727		55.3463		54.9379		0.0553463		14.45552

																						20.023		34.7127				0.0347127		14.98707		0.6887440476		20.011		27.211				0.027211		14.97793		0.5388316832		20.119		30.9				0.0309		15.085		0.0309412333		30.9412333333		15.02		3.7510199764		16.3547		29.2448				0.0292448		14.47163		0.5791049505		17.5222		39.3301				0.0393301		14.94198		0.7788138614		17.5222								14.94198		0.03428745		14.79		0.007131384		20.0112		96.6715				0.0966715		14.94792		1.8881152344		20.0083		89.47				0.08947		14.96117		1.8835789474		20.0028		49.7119				0.0497119		14.93483		0.994238		20.007		44.791				0.044791		14.9458		0.8887103175		20.1995		339.43				0.33943		15.0659		6.7347222222		19.5397		0				0		15.05272		0		19.9875		55.9001		56.0177		0.0559001		14.97032

																						20.5413		36.0353				0.0360353		15.50537		0.7149861111		20.5283		27.0861				0.0270861		15.49523		0.5363584158		20.521		31.5				0.0315		15.487		0.0315404667		31.5404666667		15.50		4.4747372351		16.8708		30.6354				0.0306354		14.98773		0.6066415842		18.0355		40.3392				0.0403392		15.45528		0.7987960396		18.0355								15.45528		0.0354873		15.30		0.0068616228		20.5273		99.3194				0.0993194		15.46402		1.9398320312		20.5232		95.8231				0.0958231		15.47607		2.0173284211		20.519		54.3911				0.0543911		15.45103		1.087822		20.5232		45.3796				0.0453796		15.462		0.9003888889		20.7147		343.856				0.343856		15.5811		6.8225396825		20.0598		0				0		15.57282		0		20.5028		57.2443		57.0983		0.0572443		15.48562

																						21.0575		36.4163				0.0364163		16.02157		0.7225456349		21.0458		27.3295				0.0273295		16.01273		0.5411782178		21.051		31.8				0.0318		16.017		0.0318486		31.8486		16.02		4.5435949456		17.386		31.1343				0.0311343		15.50293		0.6165207921		18.55		41.6219				0.0416219		15.96978		0.8241960396		18.55								15.96978		0.0363781		15.81		0.0074158531		21.0407		101.546				0.101546		15.97742		1.9833203125		21.0388		100.214				0.100214		15.99167		2.1097684211		21.0365		52.5261				0.0525261		15.96853		1.050522		21.0398		46.0357				0.0460357		15.9786		0.913406746		21.2305		371.335				0.371335		16.0969		7.3677579365		20.5802		0				0		16.09322		0		21.0185		58.1188		58.1794		0.0581188		16.00132

																						21.5745		37.2294				0.0372294		16.53857		0.7386785714		21.5625		27.6725				0.0276725		16.52943		0.547970297		21.571		32.4				0.0324		16.537		0.0324339667		32.4339666667		16.54		4.7785405411		17.9018		34.6454				0.0346454		16.01873		0.6860475248		19.064		43.0611				0.0430611		16.48378		0.8526950495		19.064								16.48378		0.03885325		16.33		0.0059507985		21.5563		105.097				0.105097		16.49302		2.0526757813		21.5592		102.629				0.102629		16.51207		2.1606105263		21.551		55.701				0.055701		16.48303		1.11402		21.556		46.7075				0.0467075		16.4948		0.9267361111		21.7477		316.354				0.316354		16.6141		6.2768650794		21.0977		0				0		16.61072		0		21.5337		58.646		59.2591		0.058646		16.51652

																						22.0897		37.4758				0.0374758		17.05377		0.7435674603		22.0792		27.9671				0.0279671		17.04613		0.5538039604		22.078		32.7				0.0327		17.044		0.0327143		32.7143		17.05		4.7543661291		18.4158		33.2456				0.0332456		16.53273		0.6583287129		19.5783		41.5139				0.0415139		16.99808		0.8220574257		19.5783								16.99808		0.03737975		16.84		0.005846571		22.0718		107.695				0.107695		17.00852		2.1034179688		22.0783		106.861				0.106861		17.03117		2.2497052632		22.0663		55.8742				0.0558742		16.99833		1.117484		22.0708		48.1899				0.0481899		17.0096		0.9561488095		22.2622		345.33				0.34533		17.1286		6.8517857143		21.6185		0				0		17.13152		0		22.0472		60.1584		60.3351		0.0601584		17.03002

																						22.6075		38.1955				0.0381955		17.57157		0.7578472222		22.5955		28.1399				0.0281399		17.56243		0.5572257426		22.601		33.1				0.0331		17.567		0.0331451333		33.1451333333		17.57		5.0279519293		18.9318		33.3951				0.0333951		17.04873		0.6612891089		20.0917		43.3904				0.0433904		17.51148		0.8592158416		20.0917								17.51148		0.03839275		17.36		0.0070677444		22.5867		110.656				0.110656		17.52342		2.16125		22.5945		110.79				0.11079		17.54737		2.3324210526		22.5823		57.4851				0.0574851		17.51433		1.149702		22.587		48.3336				0.0483336		17.5258		0.959		22.7777		315.467				0.315467		17.6441		6.259265873		22.1378		0				0		17.65082		0		22.5638		61.7397		61.4175		0.0617397		17.54662

																						23.1253		38.6358				0.0386358		18.08937		0.7665833333		23.1125		29.9312				0.0299312		18.07943		0.5926970297		23.113		34.3				0.0343		18.079		0.034289		34.289		18.08		4.3523104255		19.4468		34.244				0.034244		17.56373		0.6780990099		20.6078		42.396				0.042396		18.02758		0.8395247525		20.6078								18.02758		0.03832		17.87		0.0057643345		23.101		112.91				0.11291		18.03772		2.2052734375		23.1138		114.435				0.114435		18.06667		2.4091578947		23.0973		58.1738				0.0581738		18.02933		1.163476		23.1027		50.2488				0.0502488		18.0415		0.997		23.2935		319.774				0.319774		18.1599		6.3447222222		22.6533		0				0		18.16632		0		23.0788		61.7695		62.4961		0.0617695		18.06162

																						23.6448		38.9901				0.0389901		18.60887		0.7736130952		23.6282		29.5124				0.0295124		18.59513		0.5844039604		23.631		34.2				0.0342		18.597		0.0342341667		34.2341666667		18.60		4.738942376		19.963		34.1				0.0341		18.07993		0.6752475248		21.123		43.4974				0.0434974		18.54278		0.8613346535		21.123								18.54278		0.0387987		18.39		0.0066449653		23.6172		116.033				0.116033		18.55392		2.2662695312		23.6295		117.775				0.117775		18.58237		2.4794736842		23.6107		59.9318				0.0599318		18.54273		1.198636		23.6177		49.9319				0.0499319		18.5565		0.9907123016		23.8102		308.685				0.308685		18.6766		6.124702381		23.1675		0				0		18.68052		0		23.5938		61.6633		63.5744		0.0616633		18.57662

																						24.1622		39.1708				0.0391708		19.12627		0.7771984127		24.1458		29.2973				0.0292973		19.11273		0.5801445545		24.152		34.3				0.0343		19.118		0.0342560333		34.2560333333		19.12		4.9368968354		20.4777		36.1884				0.0361884		18.59463		0.7166019802		21.6385		45.4614				0.0454614		19.05828		0.9002257426		21.6385								19.05828		0.0408249		18.90		0.0065570012		24.1328		119.638				0.119638		19.06952		2.3366796875		24.1485		120.842				0.120842		19.10137		2.5440421053		24.1282		60.8835				0.0608835		19.06023		1.21767		24.1347		50.0743				0.0500743		19.0735		0.9935376984		24.3263		282.382				0.282382		19.1927		5.6028174603		23.6875		0				0		19.20052		0		24.1105		62.9184		64.656		0.0629184		19.09332

																						24.6782		39.8796				0.0398796		19.64227		0.7912619048		24.6607		29.5375				0.0295375		19.62763		0.5849009901		24.659		34.7				0.0347		19.625		0.0347057		34.7057		19.63		5.1710523561		20.9935		36.9259				0.0369259		19.11043		0.7312059406		22.1537		46.6695				0.0466695		19.57348		0.9241485149		22.1537								19.57348		0.0417977		19.42		0.0068897656		24.648		122.213				0.122213		19.58472		2.3869726563		24.662		125.233				0.125233		19.61487		2.6364842105		24.6438		62.3126				0.0623126		19.57583		1.246252		24.6497		51.6719				0.0516719		19.5885		1.0252361111		24.8398		291.624				0.291624		19.7062		5.7861904762		24.2063		0				0		19.71932		0		24.6272		65.7985		65.7373		0.0657985		19.61002

																						25.1943		40.8701				0.0408701		20.15837		0.8109146825		25.176		29.5154				0.0295154		20.14293		0.5844633663		25.177		35.2				0.0352		20.143		0.0351951667		35.1951666667		20.15		5.677351543		21.5088		38.725				0.038725		19.62573		0.7668316832		22.6695		47.4519				0.0474519		20.08928		0.9396415842		22.6695								20.08928		0.04308845		19.93		0.0061708502		25.1682		123.377				0.123377		20.10492		2.4097070312		25.1787		127.52				0.12752		20.13157		2.6846315789		25.1598		62.1544				0.0621544		20.09183		1.243088		25.1658		51.6912				0.0516912		20.1046		1.0256190476		25.3555		309.598				0.309598		20.2219		6.1428174603		24.725		0				0		20.23802		0		25.1422		66.5039		66.8148		0.0665039		20.12502

																						25.7115		41.3604				0.0413604		20.67557		0.8206428571		25.694		29.9781				0.0299781		20.66093		0.5936257426		25.699		35.6				0.0356		20.665		0.0356461667		35.6461666667		20.67		5.6912904374		22.025		37.2083				0.0372083		20.14193		0.7367980198		23.1838		44.1984				0.0441984		20.60358		0.8752158416		23.1838								20.60358		0.04070335		20.45		0.0049427471		25.6823		124.955				0.124955		20.61902		2.4405273437		25.6945		131.494				0.131494		20.64737		2.7682947368		25.675		64.8373				0.0648373		20.60703		1.296746		25.681		52.597				0.052597		20.6198		1.0435912698		25.8705		331.765				0.331765		20.7369		6.5826388889		25.2427		0				0		20.75572		0		25.6593		66.6773		67.8966		0.0666773		20.64212

																						26.2292		41.5201				0.0415201		21.19327		0.8238115079		26.2102		30.8357				0.0308357		21.17713		0.6106079208		26.212		36.2				0.0362		21.178		0.0361852667		36.1852666667		21.18		5.3422152375		22.539		40.6592				0.0406592		20.65593		0.8051326733		23.6987		47.4538				0.0474538		21.11848		0.9396792079		23.6987								21.11848		0.0440565		20.96		0.0048045077		26.1972		127.833				0.127833		21.13392		2.4967382812		26.2112		135.477				0.135477		21.16407		2.8521473684		26.1897		64.8856				0.0648856		21.12173		1.297712		26.199		53.3017				0.0533017		21.1378		1.0575734127		26.3862		372.546				0.372546		21.2526		7.3917857143		25.7625		0				0		21.27552		0		26.1755		67.8437		68.9761		0.0678437		21.15832

																						26.7448		42.5724				0.0425724		21.70887		0.8446904762		26.726		30.3089				0.0303089		21.69293		0.6001762376		26.731		36.4				0.0364		21.697		0.0364271		36.4271		21.70		6.1317949142		23.0547		39.7				0.0397		21.17163		0.7861386139		24.2152		48.1485				0.0481485		21.63498		0.9534356436		24.2152								21.63498		0.04392425		21.48		0.0059739916		26.7112		131.083				0.131083		21.64792		2.5602148437		26.7268		138.452				0.138452		21.67967		2.9147789474		26.7042		66.094				0.066094		21.63623		1.32188		26.7135		53.5073				0.0535073		21.6523		1.0616527778		26.9013		361.734				0.361734		21.7677		7.1772619048		26.2787		0				0		21.79172		0		26.6917		69.3635		70.0553		0.0693635		21.67452

																						27.2625		43.3161				0.0433161		22.22657		0.8594464286		27.2425		29.8029				0.0298029		22.20943		0.5901564356		27.251		36.5				0.0365		22.217		0.0365396667		36.5396666667		22.22		6.7566873276		23.5693		40.6943				0.0406943		21.68623		0.8058277228		24.7307		49.8511				0.0498511		22.15048		0.987150495		24.7307								22.15048		0.0452727		22.00		0.0064748354		27.225		135.408				0.135408		22.16172		2.6446875		27.2432		142.31				0.14231		22.19607		2.996		27.22		65.8326				0.0658326		22.15203		1.316652		27.2292		54.4996				0.0544996		22.168		1.0813412698		27.4175		307.654				0.307654		22.2839		6.1042460317		26.7987		0				0		22.31172		0		27.2078		70.9304		71.1343		0.0709304		22.19062

																						27.7782		44.6235				0.0446235		22.74227		0.8853869048		27.7597		30.8472				0.0308472		22.72663		0.6108356436		27.763		37.7				0.0377		22.729		0.0377235667		37.7235666667		22.73		6.888180236		24.0825		41.742				0.041742		22.19943		0.8265742574		25.2462		50.1298				0.0501298		22.66598		0.9926693069		25.2462								22.66598		0.0459359		22.51		0.0059310703		27.7425		137.541				0.137541		22.67922		2.6863476563		27.7598		144.56				0.14456		22.71267		3.0433684211		27.733		68.014				0.068014		22.66503		1.36028		27.7453		54.6933				0.0546933		22.6841		1.0851845238		27.9315		292.103				0.292103		22.7979		5.7956944444		27.3153		0				0		22.82832		0		27.7223		70.3683		72.2094		0.0703683		22.70512

																						28.2977		44.1005				0.0441005		23.26177		0.8750099206		28.2758		31.286				0.031286		23.24273		0.6195247525		28.282		37.7				0.0377		23.248		0.0376955		37.6955		23.25		6.4072511852		24.5992		41.0084				0.0410084		22.71613		0.8120475248		25.7633		51.4099				0.0514099		23.18308		1.0180178218		25.7633								23.18308		0.04620915		23.03		0.0073549712		28.2575		139.403				0.139403		23.19422		2.7227148437		28.2745		148.483				0.148483		23.22737		3.1259578947		28.2492		69.0085				0.0690085		23.18123		1.38017		28.2605		55.6335				0.0556335		23.1993		1.1038392857		28.4448		290.317				0.290317		23.3112		5.7602579365		27.8333		0				0		23.34632		0		28.2372		72.3291		73.2851		0.0723291		23.22002

																						28.8128		44.2909				0.0442909		23.77687		0.8787876984		28.7938		33.0601				0.0330601		23.76073		0.6546554455		28.803		38.7				0.0387		23.769		0.0386836667		38.6836666667		23.77		5.6154178156		25.1138		42.6843				0.0426843		23.23073		0.8452336634		26.2783		51.1258				0.0511258		23.69808		1.0123920792		26.2783								23.69808		0.04690505		23.54		0.0059690419		28.7755		141.815				0.141815		23.71222		2.7698242188		28.7925		152.369				0.152369		23.74537		3.2077684211		28.7638		70.6309				0.0706309		23.69583		1.412618		28.7745		55.1642				0.0551642		23.7133		1.0945277778		28.9593		341.592				0.341592		23.8257		6.7776190476		28.3513		0				0		23.86432		0		28.7532		73.508		74.3629		0.073508		23.73602

																						29.3295		44.9015				0.0449015		24.29357		0.8909027778		29.3107		32.0387				0.0320387		24.27763		0.634429703		29.311		38.4				0.0384		24.277		0.0384467333		38.4467333333		24.28		6.431527343		25.6295		43.8228				0.0438228		23.74643		0.8677782178		26.7945		52.1394				0.0521394		24.21428		1.0324633663		26.7945								24.21428		0.0479811		24.06		0.0058807243		29.2945		144.287				0.144287		24.23122		2.8181054687		29.3087		155.766				0.155766		24.26157		3.2792842105		29.2783		69.9755				0.0699755		24.21033		1.39951		29.2912		57.194				0.057194		24.23		1.1348015873		29.4755		308.253				0.308253		24.3419		6.1161309524		28.8722		0				0		24.38522		0		29.2695		74.5157		75.4411		0.0745157		24.25232

																						29.8458		45.997				0.045997		24.80987		0.9126388889		29.8283		31.8801				0.0318801		24.79523		0.6312891089		29.83		38.9				0.0389		24.796		0.0389257		38.9257		24.80		7.0584850903		26.1453		44.2517				0.0442517		24.26223		0.8762712871		27.3097		52.5655				0.0525655		24.72948		1.0409009901		27.3097								24.72948		0.0484086		24.57		0.0058787444		29.811		148.98				0.14898		24.74772		2.909765625		29.8237		158.58				0.15858		24.77657		3.3385263158		29.7932		72.5975				0.0725975		24.72523		1.45195		29.8063		57.9769				0.0579769		24.7451		1.1503353175		29.9912		320.115				0.320115		24.8576		6.3514880952		29.3897		0				0		24.90272		0		29.7838		75.9647		76.5149		0.0759647		24.76662

																						30.3643		46.1679				0.0461679		25.32837		0.9160297619		30.345		32.3183				0.0323183		25.31193		0.6399663366		30.35		39.2				0.0392		25.316		0.0392287333		39.2287333333		25.32		6.924844709		26.6592		43.9561				0.0439561		24.77613		0.8704178218		27.8247		52.4342				0.0524342		25.24448		1.0383009901		27.8247								25.24448		0.04819515		25.09		0.005994922		30.3272		152.27				0.15227		25.26392		2.9740234375		30.3378		161.835				0.161835		25.29067		3.4070526316		30.3083		73.849				0.073849		25.24033		1.47698		30.3218		57.0616				0.0570616		25.2606		1.1321746032		30.5063		305.787				0.305787		25.3727		6.067202381		29.9105		0				0		25.42352		0		30.2987		76.8821		77.5895		0.0768821		25.28152

																						30.8828		45.7385				0.0457385		25.84687		0.9075099206		30.8593		32.8027				0.0328027		25.82623		0.6495584158		30.861		39.3				0.0393		25.827		0.0392804		39.2804		25.83		6.467922273		27.1763		45.7594				0.0457594		25.29323		0.9061267327		28.3408		53.8984				0.0538984		25.76058		1.0672950495		28.3408								25.76058		0.0498289		25.60		0.0057551421		30.845		155.648				0.155648		25.78172		3.04		30.8573		166.092				0.166092		25.81017		3.4966736842		30.8218		74.319				0.074319		25.75383		1.48638		30.8388		58.5126				0.0585126		25.7776		1.1609642857		31.0218		383.754				0.383754		25.8882		7.6141666667		30.432		0				0		25.94502		0		30.8158		79.2553		78.6687		0.0792553		25.79862

																						31.401		47.1791				0.0471791		26.36507		0.936093254		31.3763		33.2526				0.0332526		26.34323		0.6584673267		31.377		40.2				0.0402		26.343		0.0402105667		40.2105666667		26.35		6.9632560131		27.6927		46.6804				0.0466804		25.80963		0.9243643564		28.856		53.7749				0.0537749		26.27578		1.064849505		28.856								26.27578		0.05022765		26.12		0.0050165691		31.3648		160.032				0.160032		26.30152		3.125625		31.3753		170.995				0.170995		26.32817		3.5998947368		31.338		75.7188				0.0757188		26.27003		1.514376		31.355		59.5341				0.0595341		26.2938		1.1812321429		31.538		346.949				0.346949		26.4044		6.8839087302		30.9477		0				0		26.46072		0		31.331		81.2956		79.7434		0.0812956		26.31382

																						31.9188		47.4079				0.0474079		26.88287		0.9406329365		31.8932		33.1115				0.0331115		26.86013		0.6556732673		31.894		40.2				0.0402		26.86		0.0402398		40.2398		26.87		7.1482830995		28.2073		46.4828				0.0464828		26.32423		0.9204514851		29.3718		54.9412				0.0549412		26.79158		1.0879445545		29.3718								26.79158		0.050712		26.64		0.005980992		31.8847		162.713				0.162713		26.82142		3.1779882813		31.8925		172.462				0.172462		26.84537		3.6307789474		31.8537		78.353				0.078353		26.78573		1.56706		31.8703		58.1313				0.0581313		26.8091		1.1533988095		32.0515		316.717				0.316717		26.9179		6.2840674603		31.4675		0				0		26.98052		0		31.8487		82.2356		80.8232		0.0822356		26.83152

																						32.4342		48.2616				0.0482616		27.39827		0.9575714286		32.4097		33.7289				0.0337289		27.37663		0.6678990099		32.412		41				0.041		27.378		0.0409968333		40.9968333333		27.38		7.2663505175		28.7227		47.4997				0.0474997		26.83963		0.9405881188		29.8862		54.5634				0.0545634		27.30598		1.0804633663		29.8862								27.30598		0.05103155		27.15		0.0049947902		32.4032		167.123				0.167123		27.33992		3.2641210938		32.4097		176.469				0.176469		27.36257		3.7151368421		32.3693		77.6474				0.0776474		27.30133		1.552948		32.3847		61.0992				0.0610992		27.3235		1.2122857143		32.5648		335.692				0.335692		27.4312		6.6605555556		31.9855		0				0		27.49852		0		32.3633		83.4245		81.8963		0.0834245		27.34612

																						32.9487		48.4023				0.0484023		27.91277		0.9603630952		32.9255		33.6849				0.0336849		27.89243		0.6670277228		32.926		41				0.041		27.892		0.0410290667		41.0290666667		27.90		7.3587430546		29.238		50.9038				0.0509038		27.35493		1.0079960396		30.4008		55.0133				0.0550133		27.82058		1.0893722772		30.4008								27.82058		0.05295855		27.67		0.0029058553		32.9205		169.713				0.169713		27.85722		3.3147070313		32.9282		177.361				0.177361		27.88107		3.7339157895		32.8872		79.4393				0.0794393		27.81923		1.588786		32.9008		60.8639				0.0608639		27.8396		1.2076170635		33.081		352.534				0.352534		27.9474		6.9947222222		32.5005		0				0		28.01352		0		32.8805		84.2567		82.9745		0.0842567		27.86332

																						33.4667		49.4119				0.0494119		28.43077		0.9803948413		33.443		34.0712				0.0340712		28.40993		0.6746772277		33.461		41.7				0.0417		28.427		0.0417277		41.7277		28.42		7.6703875124		29.7542		49.3825				0.0493825		27.87113		0.9778712871		30.9163		56.4386				0.0564386		28.33608		1.1175960396		30.9163								28.33608		0.05291055		28.18		0.0049894162		33.4378		173.194				0.173194		28.37452		3.3826953125		33.4417		181.584				0.181584		28.39457		3.8228210526		33.4028		80.0545				0.0800545		28.33483		1.60109		33.4153		61.6529				0.0616529		28.3541		1.2232718254		33.5955		328.414				0.328414		28.4619		6.5161507937		33.0185		0				0		28.53152		0		33.3967		85.2034		84.0503		0.0852034		28.37952

																						33.9837		50.0193				0.0500193		28.94777		0.9924464286		33.958		34.1577				0.0341577		28.92493		0.676390099		33.965		42				0.042		28.931		0.042059		42.059		28.93		7.9309645939		30.2695		49.7601				0.0497601		28.38643		0.9853485149		31.4325		57.024				0.057024		28.85228		1.1291881188		31.4325								28.85228		0.05339205		28.70		0.0051363529		33.956		176.75				0.17675		28.89272		3.4521484375		33.9583		185.811				0.185811		28.91117		3.9118105263		33.9185		81.5026				0.0815026		28.85053		1.630052		33.9315		62.348				0.062348		28.8703		1.2370634921		34.1112		304.985				0.304985		28.9776		6.0512896825		33.5342		0				0		29.04722		0		33.9128		85.251		85.1258		0.085251		28.89562

																						34.5057		50.8666				0.0508666		29.46977		1.0092579365		34.4768		34.4677				0.0344677		29.44373		0.6825287129		34.481		42.6				0.0426		29.447		0.0426447667		42.6447666667		29.45		8.1995416545		30.7825		50.5313				0.0505313		28.89943		1.000619802		31.948		57.3435				0.0573435		29.36778		1.1355148515		31.948								29.36778		0.0539374		29.21		0.0048169528		34.4712		180.601				0.180601		29.40792		3.5273632812		34.4758		189.47				0.18947		29.42867		3.9888421053		34.433		82.3281				0.0823281		29.36503		1.646562		34.4467		62.3137				0.0623137		29.3855		1.2363829365		34.6263		364.147				0.364147		29.4927		7.2251388889		34.0532		0				0		29.56622		0		34.4302		86.9962		86.2035		0.0869962		29.41302

																						35.0217		51.1525				0.0511525		29.98577		1.0149305556		34.9935		34.3503				0.0343503		29.96043		0.6802039604		34.999		42.7				0.0427		29.965		0.0427342667		42.7342666667		29.97		8.4011524128		31.2987		52.1902				0.0521902		29.41563		1.0334693069		32.4628		55.9056				0.0559056		29.88258		1.1070415842		32.4628								29.88258		0.0540479		29.73		0.0026271845		34.9862		183.293				0.183293		29.92292		3.5799414063		34.9908		192.28				0.19228		29.94367		4.048		34.9482		83.4299				0.0834299		29.88023		1.668598		34.9617		63.2306				0.0632306		29.9005		1.2545753968		35.143		355.538				0.355538		30.0094		7.0543253968		34.5695		0				0		30.08252		0		34.9453		87.5154		87.2764		0.0875154		29.92812

																																																																												32.9773		57.7916										32.9773

																																																																												33.493		58.212										33.493
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GLP

GLP-PVP 1:1 PM

GLP-PVP 1:2 PM

GLP-PEOX 5K 1:2 PM

GLP-PEOX 50K 1:2 PM

Time (min)

mg Dissolved



GLP-PX 50K 12

		GLP-PVP 1:1								445.54																GLP-PVP 1:1 -1				17B-28001								GLP-PVP 1:1 -2				17B-28003								GLP-PVP 1:1 -3				17E-10003								GLP-PVP 1:1 -4				17E-10013				GLP-PVP 1:1 pH 6.8												GLP-PVP 1:1 FaSSIF -1				17C-09005								GLP-PVP 1:1 FaSSIF -2				17C-09008				GLP-PVP 1:1 FaSSIF

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/ml)		IDR (ug/min/cm2)

		GLP-PVP 1:1 -1		17B-28001		1.104		10.56		0.44		4.69		23.56		50.8016		725.7373

		GLP-PVP 1:1 -2		17B-28003		1.065		10.44		0.44		4.63		23.00		43.3858		619.7966				Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile																				Dissolution Profile												Dissolution Profile

		GLP-PVP 1:1 -3		17E-10003		1.088		10.86		0.44		4.82		22.57		40.2139		574.4845																																																				AVERAGE				TIME		SD																										AVERAGE		TIME

		GLP-PVP 1:1 -4		17E-10013		0.563		10.74		0.44		4.77		11.82		26.2989		375.6990				Time (minutes)		Weight (mg)		Weight (µg)				Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (µg)				Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)		Weight (µg)		Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (µg)		Weight (mg)		Time zero (min)		%		mg		Weight (µg)						Time (minutes)		Weight (µg)		Weight (µg)		Weight (mg)		Time zero (min)		%		Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		%		mg

		AVG				1.0855								23.042		44.800		640.006				5.3948		0.0752367		75.2367				0		1.6057443092		5.07397		0.0719341		71.9341				0		1.5529049952		5.07188		0.0834789		0.0842109		83.4789		0		1.7324370531		4.06407		49.8642		54.0919		0.0498642		0		1046.393771019		0.0768832333		76.8832333333		0		5.9459150493		1.80157		14.8299		14.5512		0.0148299		0		292.1613545346		1.7526		11.9307				0.0119307		0		0.2350447051		0.0133803		0

		SD				0.0194								0.496		5.434		77.625				5.9151		0.0975581		97.5581				0.5203		2.0821402838		5.58958		0.0943222		94.3222				0.51561		2.0362166975		5.58985		0.104176		0.106026		104.176		0.51797		2.1619638309		4.58152		66.4015		68.4427		0.0664015		0.51745		1393.4268670974		0.0986854333		98.6854333333		0.51796		5.0226988705		2.31718		34.6828		34.1749		0.0346828		0.51561		683.2799834828		2.27057		30.9483				0.0309483		0.51797		0.6097072299		0.03281555		0.51679

		RSD				1.787								2.152		12.129		12.129				6.43022		0.123665		123.665				1.03542		2.6393285458		6.10755		0.110963		110.963				1.03358		2.3954563549		6.10938		0.124603		0.127706		124.603		1.0375		2.5858852252		5.09922		79.1792		82.5157		0.0791792		1.03515		1661.5652446899		0.1197436667		119.7436666667		1.0355		7.6187296404		2.83515		54.2721		53.605		0.0542721		1.03358		1069.2054733637		2.7875		41.6925				0.0416925		1.0349		0.821376899		0.0479823		1.03424

		GLP-PVP 1:1 FaSSIF -1		17C-09005		0.498		11.44		0.44		5.08		9.81		35.47		506.68				6.94765		0.150762		150.762				1.55285		3.2176480833		6.62735		0.135535		135.535				1.55338		2.9259138367		6.62448		0.142511		0.149006		142.511		1.5526		2.9575298293		5.61693		94.5652		96.3101		0.0945652		1.55286		1984.4384595594		0.142936		142.936		1.5529433333		7.6223914226		3.35287		72.2495		72.7464		0.0722495		1.5513		1423.3751936592		3.30652		56.4394				0.0564394		1.55392		1.1119030845		0.06434445		1.55261

		GLP-PVP 1:1 FaSSIF -2		17C-09008		0.500		10.5		0.44		4.66		10.72		29.07		415.36				7.46615		0.175434		175.434				2.07135		3.7442118958		7.14532		0.156254		156.254				2.07135		3.3731932021		7.14167		0.164372		0.170196		164.372		2.06979		3.411211016		6.13412		105.774		109.817		0.105774		2.07005		2219.6536740941		0.1653533333		165.3533333333		2.07083		9.6275833589		3.87083		90.2848		91.6214		0.0902848		2.06926		1778.685592073		3.82057		71.0628				0.0710628		2.06797		1.3999962174		0.0806738		2.068615

		AVG		amount at		0.499								10.27		32.27		461.02				7.98385		0.202423		202.423				2.58905		4.3202264361		7.66223		0.174669		174.669				2.58826		3.770734083		7.65807		0.184811		0.191162		184.811		2.58619		3.8353814462		6.65078		118.793		123.043		0.118793		2.58671		2492.8557008968		0.187301		187.301		2.5878333333		14.043546703		4.38855		109.554		110.216		0.109554		2.58698		2158.3048459316		4.33698		85.569				0.085569		2.58438		1.685780413		0.0975615		2.58568

		SD		15 min		0.001								0.65		4.52		64.57				8.50208		0.231934		231.934				3.10728		4.9500669303		8.17995		0.199324		199.324				3.10598		4.3029833592		8.17343		0.20504		0.211895		205.04		3.10155		4.2551937479		7.16772		132.27		136.014		0.13227		3.10365		2775.6687983098		0.2120993333		212.0993333333		3.1049366667		17.4134621869		4.90598		128.743		128.533		0.128743		3.10441		2536.3440931392		4.85287		101.984				0.101984		3.10027		2.0091695548		0.1153635		3.10234

		RSD				0.260								6.32		14.01		14.01				9.01718		0.258635		258.635				3.62238		5.5199348113		8.69532		0.220608		220.608				3.62135		4.7624598789		8.69037		0.227092		0.232502		227.092		3.61849		4.7128387563		7.68438		144.921		148.722		0.144921		3.62031		3041.1483928317		0.235445		235.445		3.62074		20.3431226462		5.42448		146.455		146.624		0.146455		3.62291		2885.2852128714		5.3698		116.97				0.11697		3.6172		2.3044062091		0.1317125		3.620055

																						9.5336		0.28532		285.32				4.1388		6.0894612112		9.21485		0.245657		245.657				4.14088		5.3032147813		9.20625		0.24807		0.25288		248.07		4.13437		5.1481950499		8.20157		159.483		161.191		0.159483		4.1375		3346.7300745509		0.2596823333		259.6823333333		4.1380166667		22.2356269607		5.94088		164		164.382		0.164		4.13931		3230.9362938166		5.88958		131.777				0.131777		4.13698		2.5961164146		0.1478885		4.138145

																						10.0503		0.310869		310.869				4.6555		6.634742455		9.73125		0.27088		270.88				4.65728		5.8477259755		9.7237		0.269681		0.273133		269.681		4.65182		5.5966879883		8.72135		175.498		173.473		0.175498		4.65728		3682.8027728568		0.28381		283.81		4.6548666667		23.4414485687		6.4586		181.006		181.93		0.181006		4.65703		3565.9686268206		6.40468		147.577				0.147577		4.65208		2.9073895453		0.1642915		4.654555

																						10.5688		0.335287		335.287				5.174		7.1558852555		10.2469		0.294537		294.537				5.17293		6.3584305436		10.2427		0.291319		0.293262		291.319		5.17082		6.0457412575		9.23723		187.45		185.421		0.18745		5.17316		3933.6139430194		0.3070476667		307.0476666667		5.1725833333		24.5088523055		6.97735		201.357		199.26		0.201357		5.17578		3966.9002397197		6.92135		161.892				0.161892		5.16875		3.1894069419		0.1816245		5.172265

																						11.0867		0.358285		358.285				5.6919		7.646721611		10.7651		0.320211		320.211				5.69113		6.9126778734		10.7588		0.311451		0.313096		311.451		5.68692		6.4635405188		9.75573		201.852		197.192		0.201852		5.69166		4235.838045486		0.3299823333		329.9823333333		5.6899833333		24.8990984843		7.4948		216.4		216.297		0.2164		5.69323		4263.2598413531		7.43647		179.764				0.179764		5.68387		3.5415001946		0.198082		5.68855

																						11.6042		0.382489		382.489				6.2094		8.1632971022		11.2823		0.343772		343.772				6.20833		7.4213100046		11.2742		0.331472		0.332721		331.472		6.20232		6.8790361978		10.2742		214.241		208.729		0.214241		6.21013		4495.8196039819		0.3525776667		352.5776666667		6.2066833333		26.6240191619		8.01147		233.594		233.064		0.233594		6.2099		4601.9959305963		7.95417		193.521				0.193521		6.20157		3.8125245275		0.2135575		6.205735

																						12.1224		0.405062		405.062				6.7276		8.6450628667		11.7992		0.36911		369.11				6.72523		7.9683038054		11.7925		0.352068		0.352274		352.068		6.72062		7.306464848		10.7893		226.543		219.964		0.226543		6.72523		4753.9754787593		0.3754133333		375.4133333333		6.7244833333		27.0534659024		8.5276		250.949		249.574		0.250949		6.72603		4943.9038536402		8.4724		213.91				0.21391		6.7198		4.214204772		0.2324295		6.722915
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																						24.0227		0.863101		863.101				18.6279		18.4207909043		23.7065		0.804201		804.201				18.63253		17.3609977747		23.6958		0.747802		0.75533		747.802		18.62392		15.5191299017		22.689		427.505		425.887		0.427505		18.62493		8971.1369896532		0.8050346667		805.0346666667		18.6281166667		57.6540206779		20.3995		569.97		570.352		0.56997		18.59793		11228.8826791869		20.3688		602.267				0.602267		18.6162		11.8651604199		0.5861185		18.607065
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																						28.6722		0.967124		967.124				23.2774		20.6409087494		28.3527		0.910621		910.621				23.27873		19.6583803733		28.3487		0.873778		0.891162		873.778		23.27682		18.1335089867		27.336		483.656		483.838		0.483656		23.27193		10149.4584434514		0.9171743333		917.1743333333		23.27765		47.0167902173		25.0435		673.23		669.553		0.67323		23.24193		13263.1904944278		25.0148		715.688				0.715688		23.2622		14.0996483796		0.694459		23.252065

																						29.1872		0.978771		978.771				23.7924		20.8894856271		28.8695		0.920749		920.749				23.79553		19.8770224609		28.864		0.892071		0.905529		892.071		23.79212		18.5131434933		27.8513		485.838		489.646		0.485838		23.78723		10195.2474305076		0.9305303333		930.5303333333		23.79335		44.1698807032		25.5587		682.607		679.784		0.682607		23.75713		13447.9251872761		25.5295		727.592				0.727592		23.7769		14.3341670725		0.7050995		23.767015

																						29.7042		0.989318		989.318				24.3094		21.114585681		29.3857		0.938768		938.768				24.31173		20.2660145399		29.3805		0.907692		0.919797		907.692		24.30862		18.8373260017		28.3667		496.653		495.34		0.496653		24.30263		10422.1988031069		0.9452593333		945.2593333333		24.3099166667		41.198349789		26.0737		688.834		689.866		0.688834		24.27213		13570.6022622858		26.048		744.103				0.744103		24.2954		14.6594474941		0.7164685		24.283765

																						30.2198		0.999584		999.584				24.825		21.3336884736		29.9055		0.946472		946.472				24.83153		20.432327597		29.8967		0.921276		0.933926		921.276		24.82482		19.1192346628		28.8805		499.179		500.905		0.499179		24.81643		10475.2065855559		0.9557773333		955.7773333333		24.8271166667		39.9747124734		26.5903		701.29		699.835		0.70129		24.78873		13815.9958139674		26.5625		758.226				0.758226		24.8099		14.9376823312		0.729758		24.799315

																						30.7375		1.01098		1010.98				25.3427		21.576908367		30.4205		0.95671		956.71				25.34653		20.6533443518		30.4125		0.942648		0.947917		942.648		25.34062		19.5627676358		29.398		497.857		506.398		0.497857		25.33393		10447.4645869821		0.9701126667		970.1126666667		25.3432833333		36.083779754		27.106		718.029		709.642		0.718029		25.30443		14145.7680250784		27.0792		772.46				0.77246		25.3266		15.2181039605		0.7452445		25.315515

																						31.2547		1.02231		1022.31				25.8599		21.8187196509		30.9362		0.970717		970.717				25.86223		20.9557258408		30.9282		0.955659		0.961777		955.659		25.85632		19.8327848317		29.912		506.989		511.747		0.506989		25.84793		10639.0984228191		0.9828953333		982.8953333333		25.8594833333		34.9545819934		27.6235		716.922		719.342		0.716922		25.82193		14123.9592050951		27.5958		786.26				0.78626		25.8432		15.4899754291		0.751591		25.832565

																						31.7727		1.03345		1033.45				26.3779		22.056475847		31.4513		0.987477		987.477				26.37733		21.317538774		31.4468		0.976593		0.97559		976.593		26.37492		20.2672279936		30.4297		519.183		517.028		0.519183		26.36563		10894.9879316011		0.9991733333		999.1733333333		26.3767166667		30.1791777942		28.1408		732.287		728.9		0.732287		26.33923		14426.6624743298		28.1125		795.111				0.795111		26.3599		15.6643474848		0.763699		26.349565

																						32.2912		1.04321		1043.21				26.8964		22.2647793008		31.9693		0.995616		995.616				26.89533		21.4932425606		31.9652		0.994672		0.989268		994.672		26.89332		20.6424213596		30.9467		524.151		522.197		0.524151		26.88263		10999.2407673915		1.011166		1011.166		26.8950166667		27.7549317419		28.6565		756.534		738.291		0.756534		26.85493		14904.3485250382		28.6297		808.777				0.808777		26.8771		15.9335790421		0.7826555		26.866015

																						32.8087		1.05196		1051.96				27.4139		22.4515267619		32.4855		1.013		1013				27.41153		21.8685263333		32.483		1.01264		1.00281		1012.64		27.41112		21.0153111434		31.4617		530.545		527.244		0.530545		27.39763		11133.41802827		1.0258666667		1025.8666666667		27.4121833333		22.5982064185		29.1713		762.289		747.532		0.762289		27.36973		15017.7268077877		29.1453		827.071				0.827071		27.3927		16.2939860455		0.79468		27.381215

																						33.326		1.06965		1069.65				27.9312		22.8290767718		32.9995		1.02296		1022.96				27.92553		22.0835416564		32.9992		1.03192		1.01618		1031.92		27.92732		21.4154288544		31.9778		529.189		532.203		0.529189		27.91373		11104.962544105		1.04151		1041.51		27.9280166667		24.778319152		29.6867		758.571		756.65		0.758571		27.88513		14944.4791179071		29.6617		833.467				0.833467		27.9091		16.419992561		0.796019		27.897115

																						33.8413		1.07645		1076.45				28.4465		22.9742062272		33.5158		1.03032		1030.32				28.44183		22.2424284815		33.514		1.04231		1.0294		1042.31		28.44212		21.6310524549		32.4925		539.755		537.05		0.539755		28.42843		11326.6886839926		1.0496933333		1049.6933333333		28.4434833333		23.9348999023		30.2018		769.056		765.634		0.769056		28.40023		15151.0423315697		30.1765		853.586				0.853586		28.4239		16.8163535811		0.811321		28.412065

																						34.3568		1.08558		1085.58				28.962		23.1690638638		34.0313		1.03854		1038.54				28.95733		22.4198808867		34.0282		1.05895		1.04248		1058.95		28.95632		21.9763822635		33.008		545.588		541.809		0.545588		28.94393		11449.093432617		1.0610233333		1061.0233333333		28.95855		23.5884385523		30.7175		771.784		774.498		0.771784		28.91593		15204.786198701		30.693		853.402				0.853402		28.9404		16.8127286281		0.812593		28.928165

																						34.875		1.09688		1096.88				29.4802		23.4102348707		34.5463		1.0494		1049.4				29.47233		22.6543253052		34.5463		1.07217		1.05554		1072.17		29.47442		22.250736835		33.5237		554.785		546.475		0.554785		29.45963		11642.0912850253		1.0728166667		1072.8166666667		29.47565		23.7466046696		31.233		791.911		783.233		0.791911		29.43143		15601.3048254428		31.208		864.822				0.864822		29.4554		17.0377121188		0.8283665		29.443415

																						35.3927		1.10384		1103.84				29.9979		23.5587791369		35.062		1.06521		1065.21				29.98803		22.9956297488		35.0617		1.08757		1.06841		1087.57		29.98982		22.570332932		34.039		563.033		551.047		0.563033		29.97493		11815.1744954922		1.08554		1085.54		29.9919166667		19.3948420978		31.7487		806.713		791.845		0.806713		29.94713		15892.9165267908		31.7242		881.899				0.881899		29.9716		17.3741432109		0.844306		29.959365

																																																																														32.2638		844.992		800.325

																																																																														32.7788		833.015		808.682





GLP-PX 50K 12

		



GLP-PVP 1:1 FaSSIF

GLP-PVP 1:1 pH 6.8

Time (min)

Dissolved (mg)



GLP-PL 15 

		0				0		0		0		0

		0.5178833333				0.5170166667		0.51789		0.51614		0.51585

		1.03612				1.0347266667		1.0344666667		1.030985		1.0346

		1.55287				1.5525233333		1.5526066667		1.546095		1.55918

		2.0716233333				2.0707466667		2.0700633333		2.06003		2.0365066667

		2.5888066667				2.5879366667		2.5874266667		2.57592		2.5843

		3.1066				3.1055533333		3.10366		3.09128		3.09906

		3.62231				3.6230033333		3.6192766667		3.606125		3.6153866667

		4.1402833333				4.1392433333		4.13594		4.121745		4.1335166667

		4.6591333333				4.65955		4.6541733333		4.6358		4.6520466667

		5.1767333333				5.1764933333		5.1708566667		5.151325		5.1652666667

		5.6945433333				5.69316		5.6879566667		5.667435		5.6852666667

		6.21146				6.2099266667		6.20589		6.183235		6.1991666667

		6.7296266667				6.72616		6.7234566667		6.698035		6.7187333333

		7.2465266667				7.24206		7.2392566667		7.214335		7.2357

		7.7639933333				7.7589266667		7.7565566667		7.729335		7.7528666667

		8.2789266667				8.2756933333		8.2735233333		8.244135		8.2708

		8.79386				8.79106		8.7890566667		8.760035		8.7845666667

		9.3098266667				9.3078933333		9.3053233333		9.275385		9.3054

		9.8255933333				9.8241933333		9.8232566667		9.790485		9.8173333333

		10.3419266667				10.3418266667		10.33909		10.305735		10.3354

		10.8573266667				10.8573933333		10.8555566667		10.821485		10.8513666667

		11.3734266667				11.37276		11.37179		11.336335		11.3686333333

		11.89026				11.8902266667		11.8895233333		11.850535		11.8836333333

		12.40696				12.4055933333		12.40519		12.366685		12.3998333333

		12.92376				12.9224933333		12.9200233333		12.882885		12.9161333333

		13.4399266667				13.4393266667		13.4362566667		13.397835		13.4336666667

		13.95596				13.95506		13.95239		13.913685		13.9497333333

		14.47336				14.4713266667		14.4689233333		14.428285		14.4690666667

		14.9897266667				14.9869266667		14.98429		14.943635		15.0166666667

		15.5043266667				15.50156		15.49909		15.459035		15.4958666667

		16.0202933333				16.0177266667		16.01439		15.974285		16.0171

		16.5374266667				16.5340266667		16.5310566667		16.490735		16.535

		17.0543266667				17.04996		17.0470233333		17.007985		17.0479666667

		17.57186				17.5647933333		17.5626233333		17.523285		17.567

		18.0884933333				18.0800933333		18.0795566667		18.037635		18.0826

		18.6048266667				18.5978933333		18.59589		18.552235		18.6003333333

		19.1218266667				19.1153933333		19.1115566667		19.067985		19.119

		19.63926				19.6307266667		19.6267233333		19.582335		19.6316333333

		20.1550266667				20.14686		20.1422233333		20.097385		20.1481

		20.6704933333				20.66366		20.6588233333		20.615185		20.6671666667

		21.18756				21.1804266667		21.1740233333		21.130285		21.1828

		21.7047933333				21.6967266667		21.6902233333		21.647385		21.6996

		22.2206933333				22.2128266667		22.2069233333		22.163335		22.2176666667

		22.73576				22.72906		22.7223566667		22.678885		22.7326333333

		23.2509933333				23.24676		23.23859		23.193635		23.2508333333

		23.76716				23.7637266667		23.7551233333		23.709435		23.7688666667

		24.28536				24.28086		24.27059		24.226285		24.2827333333

		24.8014266667				24.7980266667		24.7871233333		24.742885		24.8003666667

		25.3181266667				25.31506		25.3025566667		25.259135		25.3187666667

		25.8331266667				25.83246		25.81739		25.775285		25.8333666667

		26.3504933333				26.34796		26.3324233333		26.292985		26.3504333333

		26.86676				26.8641266667		26.84889		26.808435		26.8676666667

		27.3830266667				27.3806266667		27.36369		27.323485		27.3843

		27.8985266667				27.8961266667		27.8791566667		27.837135		27.8990666667

		28.41336				28.4127266667		28.39409		28.352935		28.4225666667

		28.9296266667				28.92996		28.9101566667		28.869485		28.9345666667

		29.44636				29.4466266667		29.4267566667		29.387135		29.4535

		29.9618266667				29.9636933333		29.9416233333		29.903785		29.9704



GLP-PVP 1:2

GLP-PVP 1:1

GLP-PEOX 5K 1:2

GLP-PEOX 5K 1:3

GLP-PEOX 50K 1:2

GLP

Time (min)

Dissolved (mg)

0.3916136667

0.229591

0.353012

0.01890105

0.015239

0.4773146667

0.2641983333

0.4166193333

0.02156585

0.0161377333

0.5575406667

0.2954036667

0.4755086667

0.0249777

0.0168376333

0.6364353333

0.3251736667

0.531405

0.02902735

0.0175402333

0.70391

0.3544093333

0.5821953333

0.0315467

0.0180281333

0.7695206667

0.382845

0.628817

0.03427755

0.0185431667

0.828553

0.409325

0.669415

0.03815485

0.0190258333

0.8887833333

0.435051

0.7081396667

0.04032165

0.0193566

0.947196

0.4621816667

0.7443113333

0.04359575

0.0211270333

1.0008243333

0.4858623333

0.781955

0.04598835

0.0216095

1.055525

0.5101496667

0.8138376667

0.04913805

0.0222495

1.1080296667

0.5321473333

0.8449713333

0.05260925

0.0233038333

1.1585393333

0.5588093333

0.87429

0.05609815

0.0233746333

1.2055266667

0.580905

0.9029843333

0.0592637

0.0239071333

1.2529266667

0.603812

0.9313176667

0.0641529

0.0244387

1.2969966667

0.6239553333

0.955801

0.0681118

0.0250079667

1.33802

0.6436683333

0.9767513333

0.073203

0.0251624667

1.38512

0.6634923333

1.000092

0.0760616

0.0259802

1.42324

0.6824613333

1.022125

0.0803274

0.0264974333

1.4562866667

0.6970513333

1.0423853333

0.08403675

0.0270067667

1.5014233333

0.71554

1.0643583333

0.0881892

0.0272987667

1.5399233333

0.729298

1.0784153333

0.09017585

0.0280984333

1.5789533333

0.7445856667

1.094268

0.09638745

0.0286159333

1.6103666667

0.7611403333

1.1078803333

0.1008098

0.0289837

1.6464433333

0.7741223333

1.129778

0.10456255

0.030211

1.67159

0.788483

1.1455046667

0.1094837

0.0299470333

1.6954566667

0.8023253333

1.15648

0.1139037

0.0315291667

1.73513

0.818561

1.17257

0.11725935

0.0308371

1.7671966667

0.8289733333

1.18437

0.1201785

0.0314217667

1.7855733333

0.8402746667

1.1942266667

0.12467865

0.0309412333

1.8138566667

0.8530113333

1.2065666667

0.12748165

0.0315404667

1.84393

0.860333

1.2160866667

0.1320528

0.0318486

1.8609033333

0.8727543333

1.2335033333

0.1372514

0.0324339667

1.8843

0.8837356667

1.25168

0.141884

0.0327143

1.90115

0.89302

1.2656966667

0.145486

0.0331451333

1.9146033333

0.903624

1.2778266667

0.1502

0.034289

1.94081

0.9128333333

1.2986233333

0.1543955

0.0342341667

1.9487133333

0.9250593333

1.3087

0.157178

0.0342560333

1.9735466667

0.9344963333

1.3263433333

0.161939

0.0347057

1.9837966667

0.9449376667

1.3422666667

0.1774965

0.0351951667

1.9950833333

0.9533356667

1.34749

0.1829285

0.0356461667

2.01461

0.9620463333

1.36293

0.190632

0.0361852667

2.0192966667

0.972891

1.3772133333

0.1967635

0.0364271

2.0370633333

0.9820866667

1.3935366667

0.2022005

0.0365396667

2.0468366667

0.99732

1.40573

0.207977

0.0377235667

2.0654633333

1.0009643333

1.4253266667

0.2131785

0.0376955

2.0793533333

1.0116643333

1.4412966667

0.2173315

0.0386836667

2.08682

1.022053

1.4495533333

0.224329

0.0384467333

2.0977366667

1.0306523333

1.47227

0.2282855

0.0389257

2.1094866667

1.0373473333

1.4798566667

0.2335025

0.0392287333

2.1326833333

1.046982

1.4833133333

0.2377155

0.0392804

2.13812

1.051491

1.4963933333

0.2426205

0.0402105667

2.1556866667

1.0578483333

1.5148366667

0.2463365

0.0402398

2.1560333333

1.0670453333

1.5356466667

0.2504985

0.0409968333

2.1574533333

1.0740566667

1.54769

0.2547365

0.0410290667

2.1691833333

1.07896

1.5577633333

0.260412

0.0417277

2.18143

1.08386

1.5751233333

0.2648915

0.042059

2.1960233333

1.0927466667

1.5987233333

0.2693635

0.0426447667

2.1966433333

1.0989533333

1.62725

0.2734405

0.0427342667



GLP-PEG 15 

		0		0		0				0		102.6292848021		102.6292848021		169.5051903011		169.5051903011		126.3520987176		126.3520987176		5.9459150493		5.9459150493		1.6311850753		1.6311850753

		0.51789		0.5170166667		0.5178833333				0.51585		118.4525056988		118.4525056988		174.1803256896		174.1803256896		122.0209849343		122.0209849343		5.0226988705		5.0226988705		1.9388725831		1.9388725831

		1.0344666667		1.0347266667		1.03612				1.0346		124.2219259484		124.2219259484		179.5772552645		179.5772552645		120.8354481985		120.8354481985		7.6187296404		7.6187296404		2.7230829042		2.7230829042

		1.5526066667		1.5525233333		1.55287				1.55918		125.7764660539		125.7764660539		184.4545371883		184.4545371883		128.7810966654		128.7810966654		7.6223914226		7.6223914226		2.7604352996		2.7604352996

		2.0700633333		2.0707466667		2.0716233333				2.0365066667		131.1996611441		131.1996611441		188.5328557608		188.5328557608		137.0287633783		137.0287633783		9.6275833589		9.6275833589		2.9949991024		2.9949991024

		2.5874266667		2.5879366667		2.5888066667				2.5843		136.0742084783		136.0742084783		191.4913702781		191.4913702781		142.6181061168		142.6181061168		14.043546703		14.043546703		2.9516867421		2.9516867421

		3.10366		3.1055533333		3.1066				3.09906		136.419262104		136.419262104		191.2560394576		191.2560394576		151.7443964007		151.7443964007		17.4134621869		17.4134621869		3.061631742		3.061631742

		3.6192766667		3.6230033333		3.62231				3.6153866667		136.3015086723		136.3015086723		191.1968310642		191.1968310642		161.6042295001		161.6042295001		20.3431226462		20.3431226462		3.5448992595		3.5448992595

		4.13594		4.1392433333		4.1402833333				4.1335166667		134.8347934857		134.8347934857		192.4611221944		192.4611221944		169.6313184763		169.6313184763		22.2356269607		22.2356269607		2.678652311		2.678652311

		4.6541733333		4.65955		4.6591333333				4.6520466667		132.2928776919		132.2928776919		193.82251861		193.82251861		176.2676662815		176.2676662815		23.4414485687		23.4414485687		2.7119624795		2.7119624795

		5.1708566667		5.1764933333		5.1767333333				5.1652666667		129.3372111356		129.3372111356		193.3804237981		193.3804237981		185.1450816927		185.1450816927		24.5088523055		24.5088523055		2.7293004214		2.7293004214

		5.6879566667		5.69316		5.6945433333				5.6852666667		123.7492390212		123.7492390212		191.7913339813		191.7913339813		194.4039993939		194.4039993939		24.8990984843		24.8990984843		3.1441517526		3.1441517526

		6.20589		6.2099266667		6.21146				6.1991666667		127.6200423288		127.6200423288		190.5016173956		190.5016173956		200.8714917088		200.8714917088		26.6240191619		26.6240191619		3.0062302678		3.0062302678

		6.7234566667		6.72616		6.7296266667				6.7187333333		123.2322911794		123.2322911794		187.9495439659		187.9495439659		208.0038214393		208.0038214393		27.0534659024		27.0534659024		3.1459060656		3.1459060656

		7.2392566667		7.24206		7.2465266667				7.2357		124.7997468921		124.7997468921		186.4863898278		186.4863898278		216.1420566048		216.1420566048		29.0958958847		29.0958958847		3.2437231494		3.2437231494

		7.7565566667		7.7589266667		7.7639933333				7.7528666667		123.8112953773		123.8112953773		183.9160756985		183.9160756985		218.9099167085		218.9099167085		27.6197920762		27.6197920762		3.38555703		3.38555703

		8.2735233333		8.2756933333		8.2789266667				8.2708		119.1334633314		119.1334633314		182.0761899243		182.0761899243		216.4863970322		216.4863970322		30.3329847086		30.3329847086		3.4918190851		3.4918190851

		8.7890566667		8.79106		8.79386				8.7845666667		122.3816248135		122.3816248135		180.4324000321		180.4324000321		215.4936108102		215.4936108102		27.6621970446		27.6621970446		3.3844434387		3.3844434387

		9.3053233333		9.3078933333		9.3098266667				9.3054		122.7681470293		122.7681470293		180.2891714617		180.2891714617		214.2053755161		214.2053755161		34.096433924		34.096433924		3.3734507323		3.3734507323

		9.8232566667		9.8241933333		9.8255933333				9.8173333333		120.7958189067		120.7958189067		179.4591593158		179.4591593158		207.9443041618		207.9443041618		36.3075687977		36.3075687977		2.7353562772		2.7353562772

		10.33909		10.3418266667		10.3419266667				10.3354		123.1233264184		123.1233264184		176.8561859054		176.8561859054		198.0702770062		198.0702770062		37.648455245		37.648455245		3.6950501544		3.6950501544

		10.8555566667		10.8573933333		10.8573266667				10.8513666667		121.3997164137		121.3997164137		176.4166701675		176.4166701675		194.4257581529		194.4257581529		38.8700797658		38.8700797658		3.9967502303		3.9967502303

		11.37179		11.37276		11.3734266667				11.3686333333		125.0105881596		125.0105881596		175.2059472231		175.2059472231		188.0215680004		188.0215680004		40.6260006933		40.6260006933		4.1513229329		4.1513229329

		11.8895233333		11.8902266667		11.89026				11.8836333333		126.1306357327		126.1306357327		175.2756760715		175.2756760715		176.592843664		176.592843664		43.6235045054		43.6235045054		4.2365735176		4.2365735176

		12.40519		12.4055933333		12.40696				12.3998333333		131.545730193		131.545730193		173.1041959466		173.1041959466		172.5547769067		172.5547769067		42.7537036057		42.7537036057		4.7083096372		4.7083096372

		12.9200233333		12.9224933333		12.92376				12.9161333333		130.8974737928		130.8974737928		169.9547668881		169.9547668881		164.8503014859		164.8503014859		46.7353417055		46.7353417055		4.4634857078		4.4634857078

		13.4362566667		13.4393266667		13.4399266667				13.4336666667		128.7301437116		128.7301437116		167.7913943691		167.7913943691		169.7647962133		169.7647962133		48.7836200515		48.7836200515		5.0444095416		5.0444095416

		13.95239		13.95506		13.95596				13.9497333333		129.4585597788		129.4585597788		169.0055510716		169.0055510716		154.0330341193		154.0330341193		51.1391994169		51.1391994169		4.7366589713		4.7366589713

		14.4689233333		14.4713266667		14.47336				14.4690666667		130.3639854408		130.3639854408		165.016392814		165.016392814		155.7390819073		155.7390819073		50.200477926		50.200477926		4.6675880649		4.6675880649

		14.98429		14.9869266667		14.9897266667				15.0166666667		131.4797267009		131.4797267009		162.7477432112		162.7477432112		144.0180132252		144.0180132252		53.4411108074		53.4411108074		3.7510199764		3.7510199764

		15.49909		15.50156		15.5043266667				15.4958666667		133.4119538622		133.4119538622		163.1742749037		163.1742749037		142.1693610921		142.1693610921		54.0297367413		54.0297367413		4.4747372351		4.4747372351

		16.01439		16.0177266667		16.0202933333				16.0171		136.952583887		136.952583887		160.8813452113		160.8813452113		144.3890255525		144.3890255525		58.2753275094		58.2753275094		4.5435949456		4.5435949456

		16.5310566667		16.5340266667		16.5374266667				16.535		138.7431736459		138.7431736459		161.4502881891		161.4502881891		134.9598245158		134.9598245158		53.9134985076		53.9134985076		4.7785405411		4.7785405411

		17.0470233333		17.04996		17.0543266667				17.0479666667		152.3410223807		152.3410223807		159.6265741233		159.6265741233		138.1604165454		138.1604165454		59.1793983945		59.1793983945		4.7543661291		4.7543661291

		17.5626233333		17.5647933333		17.57186				17.567		158.7342084534		158.7342084534		155.5292699012		155.5292699012		127.6695582353		127.6695582353		60.554643136		60.554643136		5.0279519293		5.0279519293

		18.0795566667		18.0800933333		18.0884933333				18.0826		157.6657046835		157.6657046835		154.8749373785		154.8749373785		120.8481693421		120.8481693421		60.9827037309		60.9827037309		4.3523104255		4.3523104255

		18.59589		18.5978933333		18.6048266667				18.6003333333		163.8174057704		163.8174057704		151.3308621278		151.3308621278		118.6056756652		118.6056756652		57.6540206779		57.6540206779		4.738942376		4.738942376

		19.1115566667		19.1153933333		19.1218266667				19.119		169.5525204767		169.5525204767		149.528935532		149.528935532		113.8119705186		113.8119705186		57.5644189611		57.5644189611		4.9368968354		4.9368968354

		19.6267233333		19.6307266667		19.63926				19.6316333333		168.3077640316		168.3077640316		149.6609287701		149.6609287701		118.1358105459		118.1358105459		57.5151766667		57.5151766667		5.1710523561		5.1710523561

		20.1422233333		20.14686		20.1550266667				20.1481		167.0650131935		167.0650131935		147.7008728489		147.7008728489		119.572821466		119.572821466		56.9069628809		56.9069628809		5.677351543		5.677351543

		20.6588233333		20.66366		20.6704933333				20.6671666667		162.9826220798		162.9826220798		147.9360405186		147.9360405186		123.4896701483		123.4896701483		56.5541633481		56.5541633481		5.6912904374		5.6912904374

		21.1740233333		21.1804266667		21.18756				21.1828		159.1977754242		159.1977754242		142.6926414723		142.6926414723		132.8020771675		132.8020771675		55.2938463243		55.2938463243		5.3422152375		5.3422152375

		21.6902233333		21.6967266667		21.7047933333				21.6996		164.4141907906		164.4141907906		142.0859286242		142.0859286242		133.7938120144		133.7938120144		51.7743452912		51.7743452912		6.1317949142		6.1317949142

		22.2069233333		22.2128266667		22.2206933333				22.2176666667		161.5372540107		161.5372540107		143.2445475833		143.2445475833		132.8675123321		132.8675123321		51.0259311168		51.0259311168		6.7566873276		6.7566873276

		22.7223566667		22.72906		22.73576				22.7326333333		158.3172549029		158.3172549029		140.9255155002		140.9255155002		132.7330035573		132.7330035573		50.0862118851		50.0862118851		6.888180236		6.888180236

		23.23859		23.24676		23.2509933333				23.2508333333		164.0055225696		164.0055225696		132.86914934		132.86914934		143.7451555126		143.7451555126		47.0167902173		47.0167902173		6.4072511852		6.4072511852

		23.7551233333		23.7637266667		23.76716				23.7688666667		164.1766318126		164.1766318126		132.2055494158		132.2055494158		124.5774595717		124.5774595717		44.1698807032		44.1698807032		5.6154178156		5.6154178156

		24.27059		24.28086		24.28536				24.2827333333		166.7426659057		166.7426659057		129.2183957608		129.2183957608		133.8952489822		133.8952489822		41.198349789		41.198349789		6.431527343		6.431527343

		24.7871233333		24.7980266667		24.8014266667				24.8003666667		172.7405140666		172.7405140666		127.4442377683		127.4442377683		139.501965697		139.501965697		39.9747124734		39.9747124734		7.0584850903		7.0584850903

		25.3025566667		25.31506		25.3181266667				25.3187666667		174.4413392328		174.4413392328		123.7746142968		123.7746142968		140.1759217317		140.1759217317		36.083779754		36.083779754		6.924844709		6.924844709

		25.81739		25.83246		25.8331266667				25.8333666667		171.2350969671		171.2350969671		122.9386296816		122.9386296816		107.4525924924		107.4525924924		34.9545819934		34.9545819934		6.467922273		6.467922273

		26.3324233333		26.34796		26.3504933333				26.3504333333		176.1771172239		176.1771172239		123.3171099118		123.3171099118		100.8365072779		100.8365072779		30.1791777942		30.1791777942		6.9632560131		6.9632560131

		26.84889		26.8641266667		26.86676				26.8676666667		184.0711268324		184.0711268324		119.8620233115		119.8620233115		102.6777879258		102.6777879258		27.7549317419		27.7549317419		7.1482830995		7.1482830995

		27.36369		27.3806266667		27.3830266667				27.3843		191.2373431977		191.2373431977		119.2682795438		119.2682795438		95.7192479773		95.7192479773		22.5982064185		22.5982064185		7.2663505175		7.2663505175

		27.8791566667		27.8961266667		27.8985266667				27.8990666667		196.7166304612		196.7166304612		117.0151957369		117.0151957369		89.3017588479		89.3017588479		24.778319152		24.778319152		7.3587430546		7.3587430546

		28.39409		28.4127266667		28.41336				28.4225666667		192.8498769337		192.8498769337		119.4594441641		119.4594441641		71.4407379115		71.4407379115		23.9348999023		23.9348999023		7.6703875124		7.6703875124

		28.9101566667		28.92996		28.9296266667				28.9345666667		183.902826877		183.902826877		116.8881905925		116.8881905925		79.2924012753		79.2924012753		23.5884385523		23.5884385523		7.9309645939		7.9309645939

		29.4267566667		29.4466266667		29.44636				29.4535		189.61302232		189.61302232		122.6737642421		122.6737642421		71.010988821		71.010988821		23.7466046696		23.7466046696		8.1995416545		8.1995416545

		29.9416233333		29.9636933333		29.9618266667				29.9704		203.6708307539		203.6708307539		119.1131245217		119.1131245217		74.7003864336		74.7003864336		19.3948420978		19.3948420978		8.4011524128		8.4011524128



GPZ-PEOX 1:3

GPZ-PEOX 1:2

GPZ-PVP 1:2

GPZ-PVP 1:1

GPZ

Time (min)

Dissolved (mg)

353.012

229.591

391.6136666667

15.239

416.6193333333

264.1983333333

477.3146666667

16.1377333333

475.5086666667

295.4036666667

557.5406666667

16.8376333333

531.405

325.1736666667

636.4353333333

17.5402333333

582.1953333333

354.4093333333

703.91

18.0281333333

628.817

382.845

769.5206666667

18.5431666667

669.415

409.325

828.553

19.0258333333

708.1396666667

435.051

888.7833333333

19.3566

744.3113333333

462.1816666667

947.196

21.1270333333

781.955

485.8623333333

1000.8243333333

21.6095

813.8376666667

510.1496666667

1055.525

22.2495

844.9713333333

532.1473333333

1108.0296666667

23.3038333333

874.29

558.8093333333

1158.5393333333

23.3746333333

902.9843333333

580.905

1205.5266666667

23.9071333333

931.3176666667

603.812

1252.9266666667

24.4387

955.801

623.9553333333

1296.9966666667

25.0079666667

976.7513333333

643.6683333333

1338.02

25.1624666667

1000.092

663.4923333333

1385.12

25.9802

1022.125

682.4613333333

1423.24

26.4974333333

1042.3853333333

697.0513333333

1456.2866666667

27.0067666667

1064.3583333333

715.54

1501.4233333333

27.2987666667

1078.4153333333

729.298

1539.9233333333

28.0984333333

1094.268

744.5856666667

1578.9533333333

28.6159333333

1107.8803333333

761.1403333333

1610.3666666667

28.9837

1129.778

774.1223333333

1646.4433333333

30.211

1145.5046666667

788.483

1671.59

29.9470333333

1156.48

802.3253333333

1695.4566666667

31.5291666667

1172.57

818.561

1735.13

30.8371

1184.37

828.9733333333

1767.1966666667

31.4217666667

1194.2266666667

840.2746666667

1785.5733333333

30.9412333333

1206.5666666667

853.0113333333

1813.8566666667

31.5404666667

1216.0866666667

860.333

1843.93

31.8486

1233.5033333333

872.7543333333

1860.9033333333

32.4339666667

1251.68

883.7356666667

1884.3

32.7143

1265.6966666667

893.02

1901.15

33.1451333333

1277.8266666667

903.624

1914.6033333333

34.289

1298.6233333333

912.8333333333

1940.81

34.2341666667

1308.7

925.0593333333

1948.7133333333

34.2560333333

1326.3433333333

934.4963333333

1973.5466666667

34.7057

1342.2666666667

944.9376666667

1983.7966666667

35.1951666667

1347.49

953.3356666667

1995.0833333333

35.6461666667

1362.93

962.0463333333

2014.61

36.1852666667

1377.2133333333

972.891

2019.2966666667

36.4271

1393.5366666667

982.0866666667

2037.0633333333

36.5396666667

1405.73

997.32

2046.8366666667

37.7235666667

1425.3266666667

1000.9643333333

2065.4633333333

37.6955

1441.2966666667

1011.6643333333

2079.3533333333

38.6836666667

1449.5533333333

1022.053

2086.82

38.4467333333

1472.27

1030.6523333333

2097.7366666667

38.9257

1479.8566666667

1037.3473333333

2109.4866666667

39.2287333333

1483.3133333333

1046.982

2132.6833333333

39.2804

1496.3933333333

1051.491

2138.12

40.2105666667

1514.8366666667

1057.8483333333

2155.6866666667

40.2398

1535.6466666667

1067.0453333333

2156.0333333333

40.9968333333

1547.69

1074.0566666667

2157.4533333333

41.0290666667

1557.7633333333

1078.96

2169.1833333333

41.7277

1575.1233333333

1083.86

2181.43

42.059

1598.7233333333

1092.7466666667

2196.0233333333

42.6447666667

1627.25

1098.9533333333

2196.6433333333

42.7342666667



GLP FULL

		GLP-PVP 1:2								445.54																GLP-PVP 1:2 -1				17B-27003								GLP-PVP 1:2 -2				17C-13001								GLP-PVP 1:2 -3				17E-10005								GLP-PVP 1:2 -4				17E-10015				GLP-PVP 1:2 pH 6.8												GLP-PVP 1:2 FaSSIF-1				17C-09010								GLP-PVP 1:2 FaSSIF-2				17C-09012				GLP-PVP 1:2 FaSSIF

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/ml)		IDR (ug/min/cm2)

		GLP-PVP 1:2 -1		17B-27003		2.251		14.64		0.28		4.10		54.90		133.3957		1905.6526

		GLP-PVP 1:2 -2		17C-13001		2.228		14.22		0.28		3.98		55.96		130.4541		1863.6299				Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile																				Dissolution Profile												Dissolution Profile

		GLP-PVP 1:2 -3		17E-10005		1.730		14.92		0.28		4.18		41.40		123.6497		1766.4246																																																				AVERAGE				TIME		SD																										AVERAGE		TIME		SD

		GLP-PVP 1:2 -4		17E-10015		2.111		16.69		0.28		4.67		45.18		108.1052		1544.3594				Time (minutes)		Weight (mg)		Weight (mg)		Weight (µg)		Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)		Weight (µg)		Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)		Weight (µg)		Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)		Weight (µg)		Time zero (min)		%		mg		Weight (µg)						Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%		mg

		AVG				2.19664								52.013		124.0		1771.214				5.06797		0.5026		0.502979		502.6		0		12.2609289617		5.38515		0.418135		0.407997		418.135		0		10.5016827406		5.08593		0.345525		0.339356		345.525		0		8.2708971658		4.0638		0.254106		0.265251		254.106		0		5.437516049		0.3916136667		391.6136666667		0		126.3520987176		1.85755		0.0363764						0		0.824861678		1.90522		0.0477218						0		1.1339654025		0.0420491		0		0.0080224093

		SD				0.0747								5.940		13.831		197.582				5.58777		0.590509		0.590627		590.509		0.5198		14.4054693599		5.90182		0.493377		0.491018		493.377		0.51667		12.3914255576		5.6013		0.42852		0.424716		428.52		0.51537		10.2575641517		4.58098		0.348058		0.334777		348.058		0.51718		7.4479585723		0.4773146667		477.3146666667		0.5178833333		122.0209849343		2.37552		0.110967						0.51797		2.5162585034		2.4211		0.124667						0.51588		2.9623372303		0.117817		0.516925		0.0096873629

		RSD				3.401								11.421		11.155		11.155				6.10443		0.674758		0.673851		674.758		1.03646		16.4607240437		6.4198		0.564478		0.570791		564.478		1.03465		14.1771649588		6.11953		0.507627		0.505433		507.627		1.0336		12.1511633474		5.10105		0.433386		0.402468		433.386		1.03725		9.2738594539		0.5575406667		557.5406666667		1.03612		120.8354481985		2.89348		0.181881						1.03593		4.1242857143		2.93723		0.193529						1.03201		4.5986360612		0.187705		1.03397		0.0082363798

		GLP-PVP 1:2 FaSSIF-1		17C-09010		1.066		15.75		0.28		4.41		24.16		105.21		1502.97				6.6224		0.761697		0.75356		761.697		1.55443		18.5816012881		6.93438		0.643207		0.646752		643.207		1.54923		16.1544856339		6.63647		0.582054		0.581139		582.054		1.55054		13.9327364994		5.61875		0.504402		0.467708		504.402		1.55495		10.793503381		0.6364353333		636.4353333333		1.55287		128.7810966654		3.4099		0.23916						1.55235		5.4231292517		3.45522		0.261192						1.55		6.2064442543		0.250176		1.551175		0.0155789766

		GLP-PVP 1:2 FaSSIF-2		17C-09012		1.221		15.03		0.28		4.21		29.02		111.20		1588.60				7.14245		0.834369		0.830005		834.369		2.07448		20.3544350117		7.45287		0.716219		0.720112		716.219		2.06772		17.9882208158		7.1539		0.648758		0.652395		648.758		2.06797		15.5294427422		6.13647		0.561142		0.530879		561.142		2.07267		12.0076607036		0.70391		703.91		2.0716233333		137.0287633783		3.92552		0.299099						2.06797		6.7822902494		3.97318		0.319448						2.06796		7.5907233153		0.3092735		2.067965		0.0143889159

		AVG		amount at		1.143								26.59		108.20		1545.78				7.65912		0.901987		0.902555		901.987		2.59115		22.0039763856		7.97032		0.788019		0.790279		788.019		2.58517		19.7915159735		7.67005		0.710498		0.719236		710.498		2.58412		17.0073247798		6.6539		0.618556		0.592012		618.556		2.5901		13.2362406916		0.7695206667		769.5206666667		2.5888066667		142.6181061168		4.44115		0.354703						2.5836		8.0431519274		4.48777		0.383817						2.58255		9.120259481		0.36926		2.583075		0.0205867068

		SD		15 min		0.110								3.43		4.24		60.55				8.17708		0.966143		0.972041		966.143		3.10911		23.569062256		8.48802		0.853716		0.85756		853.716		3.10287		21.4415310428		8.18542		0.772118		0.782003		772.118		3.09949		18.4823343547		7.17162		0.6658		0.651238		665.8		3.10782		14.2471967816		0.828553		828.553		3.1066		151.7443964007		4.95625		0.409259						3.0987		9.2802494331		5.00573		0.428793						3.10051		10.1889791845		0.419026		3.099605		0.0138126239

		RSD				9.619								12.91		3.92		3.92				8.69375		1.03336		1.03826		1033.36		3.62578		25.2088212334		9.00338		0.918667		0.921758		918.667		3.61823		23.0728099257		8.70365		0.835775		0.841355		835.775		3.61772		20.0061039831		7.68672		0.714323		0.708299		714.323		3.62292		15.2855216982		0.8887833333		888.7833333333		3.62231		161.6042295001		5.47188		0.457576						3.61433		10.3758730159		5.5237		0.488657						3.61848		11.6114675411		0.4731165		3.616405		0.0219775859

																						9.21407		1.09744		1.10196		1097.44		4.1461		26.7720530835		9.51848		0.980908		0.983265		980.908		4.13333		24.6360257183		9.22213		0.899499		0.897185		899.499		4.1362		21.5314774033		8.20522		0.76324		0.763917		763.24		4.14142		16.3322776684		0.947196		947.196		4.1402833333		169.6313184763		5.98802		0.502613						4.13047		11.3971201814		6.0388		0.543204						4.13358		12.9076133447		0.5229085		4.132025		0.0287021714

																						9.73542		1.15542		1.16292		1155.42		4.66745		28.1864754098		10.0365		1.03818		1.04255		1038.18		4.65135		26.0744424352		9.73698		0.953992		0.949318		953.992		4.65105		22.8358866335		8.7224		0.808873		0.817633		808.873		4.6586		17.3087605923		1.0008243333		1000.8243333333		4.6591333333		176.2676662815		6.5026		0.549962						4.64505		12.4707936508		6.55547		0.590049						4.65025		14.0207442258		0.5700055		4.64765		0.0283457895

																						10.2539		1.21395		1.22082		1213.95		5.18593		29.6143149883		10.5539		1.10063		1.09931		1100.63		5.16875		27.6429073739		10.2537		1.00536		0.99852		1005.36		5.16777		24.0654921486		9.23932		0.851995		0.869619		851.995		5.17552		18.231511598		1.055525		1055.525		5.1767333333		185.1450816927		7.0211		0.599342						5.16355		13.590521542		7.06953		0.641231						5.16431		15.2369309001		0.6202865		5.16393		0.029619996

																						10.7732		1.27241		1.27622		1272.41		5.70523		31.0404469165		11.0711		1.15823		1.15368		1158.23		5.68595		29.0895619851		10.769		1.04999		1.04468		1049.99		5.68307		25.1338088855		9.75625		0.893449		0.91996		893.449		5.69245		19.1185697167		1.1080296667		1108.0296666667		5.6945433333		194.4039993939		7.53777		0.646303						5.68022		14.6553968254		7.58672		0.68791						5.6815		16.3461172892		0.6671065		5.68086		0.0294205918

																						11.2906		1.32787		1.32895		1327.87		6.22263		32.3933938329		11.587		1.21115		1.20567		1211.15		6.20185		30.4186759092		11.2859		1.09432		1.08821		1094.32		6.19997		26.1949444657		10.2737		0.936598		0.968753		936.598		6.2099		20.041898485		1.1585393333		1158.5393333333		6.21146		200.8714917088		8.05495		0.683882						6.1974		15.5075283447		8.10338		0.730695						6.19816		17.3627744511		0.7072885		6.19778		0.0331017897

																						11.8099		1.37976		1.3795		1379.76		6.74193		33.6592505855		12.1037		1.26158		1.25557		1261.58		6.71855		31.6852521599		11.8039		1.138		1.12924		1138		6.71797		27.2405208732		10.7922		0.97524		1.01609		975.24		6.7284		20.8687837028		1.2055266667		1205.5266666667		6.7296266667		208.0038214393		8.57397		0.723289						6.71642		16.4011111111		8.61718		0.772851						6.71196		18.3644853151		0.74807		6.71419		0.0350456263

																						12.3297		1.43603		1.42784		1436.03		7.26173		35.0319574551		12.6211		1.30825		1.30347		1308.25		7.23595		32.8573940125		12.3203		1.17455		1.16769		1174.55		7.23437		28.1154251245		11.3057		1.0145		1.0615		1014.5		7.2419		21.7088932637		1.2529266667		1252.9266666667		7.2465266667		216.1420566048		9.08802		0.759774						7.23047		17.2284353741		9.1323		0.809827						7.22708		19.2431090201		0.7848005		7.228775		0.0353928157

																						12.8487		1.48112		1.47394		1481.12		7.78073		36.1319281811		13.1391		1.35492		1.34943		1354.92		7.75395		34.029535865		12.8383		1.20683		1.20397		1206.83		7.75237		28.8881175795		11.8211		1.05495		1.10562		1054.95		7.7573		22.5744671745		1.2969966667		1296.9966666667		7.7639933333		218.9099167085		9.60182		0.794853						7.74427		18.023877551		9.64897		0.8419						7.74375		20.00522764		0.8183765		7.74401		0.0332672527

																						13.3659		1.52143		1.51782		1521.43		8.29793		37.1152907884		13.6526		1.39341		1.3931		1393.41		8.26745		34.9962326703		13.3526		1.23736		1.23784		1237.36		8.26667		29.618919954		12.3352		1.09922		1.14825		1099.22		8.2714		23.5217837884		1.33802		1338.02		8.2789266667		216.4863970322		10.1164		0.823242						8.25885		18.6676190476		10.1675		0.877419						8.26228		20.8492301112		0.8503305		8.260565		0.0383089241

																						13.8813		1.56921		1.5596		1569.21		8.81333		38.2808840749		14.1675		1.43806		1.43508		1438.06		8.78235		36.1176411493		13.869		1.26379		1.26982		1263.79		8.78307		30.2515798545		12.8497		1.14809		1.18957		1148.09		8.7859		24.5675340238		1.38512		1385.12		8.79386		215.4936108102		10.6297		0.859903						8.77215		19.4989342404		10.6825		0.906665						8.77728		21.5441735576		0.883284		8.774715		0.0330657273

																						14.399		1.60597		1.59969		1605.97		9.33103		39.1776444184		14.682		1.47624		1.4753		1476.24		9.29685		37.0765521398		14.3844		1.292		1.29984		1292		9.29847		30.926847951		13.3654		1.18751		1.22968		1187.51		9.3016		25.4110673628		1.42324		1423.24		9.3098266667		214.2053755161		11.1458		0.892141						9.28825		20.2299546485		11.1979		0.935728						9.29268		22.2347685581		0.9139345		9.290465		0.0308206633

																						14.9156		1.63676		1.63793		1636.76		9.84763		39.9287665886		15.1966		1.50321		1.51385		1503.21		9.81145		37.7539180229		14.9016		1.31385		1.32817		1313.85		9.81567		31.4498755266		13.8815		1.22889		1.26855		1228.89		9.8177		26.2965419841		1.4562866667		1456.2866666667		9.8255933333		207.9443041618		11.6615		0.906194						9.80395		20.54861678		11.7117		0.97121						9.80648		23.0778918354		0.938702		9.805215		0.0459732545

																						15.4323		1.67278		1.67445		1672.78		10.36433		40.8074746292		15.7133		1.54693		1.55096		1546.93		10.32815		38.8519690577		15.4177		1.33991		1.35476		1339.91		10.33177		32.0736786672		14.3971		1.28456		1.30615		1284.56		10.3333		27.4878027904		1.5014233333		1501.4233333333		10.3419266667		198.0702770062		12.1771		0.928424						10.31955		21.0526984127		12.2302		0.996397						10.32498		23.6763853246		0.9624105		10.322265		0.0480641692

																						15.9477		1.71103		1.70926		1711.03		10.87973		41.7405835285		16.2284		1.58024		1.58642		1580.24		10.84325		39.6885674101		15.9331		1.36925		1.37973		1369.25		10.84717		32.7759957871		14.9128		1.3285		1.34257		1328.5		10.849		28.4280578619		1.5399233333		1539.9233333333		10.8573266667		194.4257581529		12.6906		0.942444						10.83305		21.3706122449		12.7482		1.0301						10.84298		24.4772360042		0.986272		10.838015		0.061982152

																						16.4669		1.74721		1.74277		1747.21		11.39893		42.6231947697		16.7435		1.61365		1.62042		1613.65		11.35835		40.5276773157		16.4479		1.39565		1.40319		1395.65		11.36197		33.4079375718		15.4268		1.376		1.37773		1376		11.363		29.4444919969		1.5789533333		1578.9533333333		11.3734266667		188.0215680004		13.2073		0.972735						11.34975		22.0574829932		13.2638		1.05619						11.35858		25.0971865792		1.0144625		11.354165		0.0590115964

																						16.986		1.76619		1.77477		1766.19		11.91803		43.0862119438		17.2592		1.64636		1.65304		1646.36		11.87405		41.3492063492		16.964		1.41902		1.42531		1419.02		11.87807		33.9673496745		15.9425		1.41855		1.41188		1418.55		11.8787		30.3550029958		1.6103666667		1610.3666666667		11.89026		176.592843664		13.7213		0.980926						11.86375		22.2432199546		13.7784		1.08154						11.87318		25.6995532744		1.031233		11.868465		0.0711448417
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																						18.0195		1.81834		1.83427		1818.34		12.95153		44.3584113973		18.2922		1.70321		1.71438		1703.21		12.90705		42.7770243118		17.9945		1.4622		1.46561		1462.2		12.90857		35.0009574876		16.9765		1.49322		1.47715		1493.22		12.9127		31.9528374561		1.67159		1671.59		12.92376		164.8503014859		14.7516		1.02344						12.89405		23.2072562358		14.8102		1.1231						12.90498		26.6871019865		1.07327		12.899515		0.0704702618

																						18.5372		1.8441		1.8621		1844.1		13.46923		44.9868266979		18.8078		1.73181		1.74311		1731.81		13.42265		43.4953285112		18.513		1.47669		1.4841		1476.69		13.42707		35.3478073535		17.4917		1.51046		1.50814		1510.46		13.4279		32.3217495506		1.6954566667		1695.4566666667		13.4399266667		169.7647962133		15.2659		1.03102						13.40835		23.379138322		15.3242		1.1573						13.41898		27.49976238		1.09416		13.413665		0.0892934443

																						19.0552		1.87767		1.8887		1877.67		13.98723		45.8057669789		19.3223		1.75599		1.77059		1755.99		13.93715		44.1026220615		19.0292		1.49675		1.5014		1496.75		13.94327		35.8279873612		18.0073		1.57173		1.53817		1571.73		13.9435		33.6328425918		1.73513		1735.13		13.95596		154.0330341193		15.7815		1.0376						13.92395		23.5283446712		15.8404		1.16823						13.93518		27.7594810379		1.102915		13.929565		0.0923693588
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																						20.6073		1.94842		1.96149		1948.42		15.53933		47.5317135051		20.8688		1.82801		1.84652		1828.01		15.48365		45.9114426361		20.5787		1.54271		1.54739		1542.71		15.49277		36.9281405592		19.5538		1.66514		1.62266		1665.14		15.49		35.6316870667		1.8138566667		1813.8566666667		15.5043266667		142.1693610921		17.3268		1.06488						15.46925		24.1469387755		17.387		1.25046						15.48178		29.7134302823		1.15767		15.475515		0.1312248765

																						21.123		1.98251		1.98354		1982.51		16.05503		48.3633391881		21.3843		1.85492		1.86977		1854.92		15.99915		46.5873015873		21.0967		1.55534		1.56097		1555.34		16.01077		37.2304672539		20.0705		1.69436		1.64913		1694.36		16.0067		36.2569545493		1.84393		1843.93		16.0202933333		144.3890255525		17.843		1.07051						15.98545		24.2746031746		17.9008		1.23331						15.99558		29.3059119856		1.15191		15.990515		0.115116984

																						21.6412		1.98109		2.00472		1981.09		16.57323		48.3286982826		21.9		1.88672		1.89206		1886.72		16.51485		47.3859754872		21.6115		1.57775		1.57366		1577.75		16.52557		37.7668996553		20.588		1.7149		1.67479		1714.9		16.5242		36.696482068		1.8609033333		1860.9033333333		16.5374266667		134.9598245158		18.357		1.08662						16.49945		24.6399092971		18.4208		1.22287						16.51558		29.0578367075		1.154745		16.507515		0.0963432989

																						22.1587		2.00583		2.02492		2005.83		17.09073		48.9322306792		22.4157		1.91304		1.91342		1913.04		17.03055		48.0470162749		22.1268		1.59627		1.58561		1596.27		17.04087		38.2102163922		21.1055		1.73403		1.69964		1734.03		17.0417		37.1058375417		1.8843		1884.3		17.0543266667		138.1604165454		18.8713		1.09313						17.01375		24.7875283447		18.9378		1.22248						17.03258		29.0485695276		1.157805		17.023165		0.0914642621

																						22.6765		2.01804		2.04424		2018.04		17.60853		49.2300936768		22.9313		1.9205		1.9339		1920.5		17.54615		48.2343781394		22.645		1.60055		1.59691		1600.55		17.55907		38.3126675603		21.6247		1.76491		1.72378		1764.91		17.5609		37.7666267226		1.90115		1901.15		17.57186		127.6695582353		19.3878		1.1007						17.53025		24.9591836735		19.4523		1.22605						17.54708		29.1333998669		1.163375		17.538665		0.088635835

																						23.1932		2.029		2.06265		2029		18.12523		49.4974629196		23.4472		1.92661		1.95354		1926.61		18.06205		48.3878340366		23.1605		1.62964		1.60748		1629.64		18.07457		39.009000383		22.142		1.7882		1.74707		1788.2		18.0782		38.265000428		1.9146033333		1914.6033333333		18.0884933333		120.8481693421		19.9038		1.10423						18.04625		25.0392290249		19.9685		1.25138						18.06328		29.7352913221		1.177805		18.054765		0.1040507629

																						23.7088		2.04984		2.0802		2049.84		18.64083		50.0058548009		23.9633		1.95807		1.97238		1958.07		18.57815		49.1779686558		23.6777		1.63915		1.61745		1639.15		18.59177		39.2366430486		22.6593		1.81452		1.76962		1814.52		18.5955		38.8282119319		1.94081		1940.81		18.6048266667		118.6056756652		20.4195		1.10974						18.56195		25.1641723356		20.4833		1.25982						18.57808		29.9358426005		1.18478		18.570015		0.1061225857

																						24.2268		2.04914		2.09705		2049.14		19.15883		49.9887782982		24.4783		1.97191		1.99039		1971.91		19.09315		49.525567611		24.1948		1.65223		1.62683		1652.23		19.10887		39.5497414784		23.1773		1.82509		1.79149		1825.09		19.1135		39.0543952752		1.9487133333		1948.7133333333		19.1218266667		113.8119705186		20.9378		1.12369						19.08025		25.4804988662		20.9985		1.25867						19.09328		29.9085163007		1.19118		19.086765		0.0954452733

																						24.7472		2.07878		2.11322		2078.78		19.67923		50.7118462139		24.9945		1.9961		2.0077		1996.1		19.60935		50.1331123167		24.7087		1.65149		1.63559		1651.49		19.62277		39.5320279586		23.693		1.84576		1.81256		1845.76		19.6292		39.4967046135		1.9735466667		1973.5466666667		19.63926		118.1358105459		21.4537		1.11787						19.59615		25.3485260771		21.5143		1.24638						19.60908		29.6164813231		1.182125		19.602615		0.0908702925
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																						25.7782		2.10616		2.14314		2106.16		20.71023		51.3797814208		26.0247		2.01698		2.04012		2016.98		20.63955		50.6575246132		25.7393		1.66788		1.65163		1667.88		20.65337		39.9243584833		24.7255		1.86211		1.85278		1862.11		20.6617		39.8465719421		1.9950833333		1995.0833333333		20.6704933333		123.4896701483		22.4857		1.12689						20.62815		25.5530612245		22.5425		1.25519						20.63728		29.8258245414		1.19104		20.632715		0.0907218
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																						27.333		2.15638		2.18341		2156.38		22.26503		52.6048985168		27.5718		2.06093		2.08395		2060.93		22.18665		51.7613522202		27.286		1.68511		1.67229		1685.11		22.20007		40.3367962466		26.2742		1.89388		1.90845		1893.88		22.2104		40.5264058889		2.0370633333		2037.0633333333		22.2206933333		132.8675123321		24.0297		1.13253						22.17215		25.680952381		24.0875		1.26944						22.18228		30.1644330387		1.200985		22.177215		0.0968099894
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																						29.4063		2.19565		2.22919		2195.65		24.33833		53.5628903201		29.6315		2.12751		2.13429		2127.51		24.24635		53.4335443038		29.35		1.69777		1.69457		1697.77		24.26407		40.6398410571		28.3352		1.9373		1.97468		1937.3		24.2714		41.4555336814		2.08682		2086.82		24.28536		133.8952489822		26.0945		1.14091						24.23695		25.8709750567		26.1462		1.28264						24.24098		30.4780914362		1.211775		24.238965		0.1002182441

																						29.9227		2.21561		2.23935		2215.61		24.85473		54.049814598		30.1477		2.13388		2.14563		2133.88		24.76255		53.5935302391		29.8667		1.69926		1.69934		1699.26		24.78077		40.6755074684		28.8508		1.94372		1.98997		1943.72		24.787		41.5929127793		2.0977366667		2097.7366666667		24.8014266667		139.501965697		26.6093		1.13412						24.75175		25.7170068027		26.661		1.26342						24.75578		30.0213857998		1.19877		24.753765		0.0914289068

																						30.4422		2.23945		2.24911		2239.45		25.37423		54.631391491		30.6628		2.12806		2.15648		2128.06		25.27765		53.4473578461		30.3838		1.69935		1.70383		1699.35		25.29787		40.6776618154		29.3663		1.96095		2.00476		1960.95		25.3025		41.9616108876		2.1094866667		2109.4866666667		25.3181266667		140.1759217317		27.1247		1.13233						25.26715		25.6764172336		27.1765		1.25211						25.27128		29.752637582		1.19222		25.269215		0.0846972503

																						30.958		2.22366		2.25837		2223.66		25.89003		54.2461943794		31.1778		2.16026		2.16687		2160.26		25.79265		54.2560779586		30.8992		1.70061		1.70803		1700.61		25.81327		40.7078226733		29.8805		2.01413		2.01905		2014.13		25.8167		43.0995891466		2.1326833333		2132.6833333333		25.8331266667		107.4525924924		27.6393		1.13144						25.78175		25.6562358277		27.6922		1.25855						25.78698		29.9056648608		1.194995		25.784365		0.089880343

																						31.4777		2.21958		2.26729		2219.58		26.40973		54.1466627635		31.6935		2.16944		2.17685		2169.44		26.30835		54.4866385373		31.4163		1.7003		1.712		1700.3		26.33037		40.7004021448		30.3972		2.02534		2.03296		2025.34		26.3334		43.3394676025		2.13812		2138.12		26.3504933333		100.8365072779		28.1533		1.13633						26.29575		25.7671201814		28.2087		1.26772						26.30348		30.123562399		1.202025		26.299615		0.09290676
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																						33.0283		2.22938		2.29157		2229.38		27.96033		54.3857338017		33.2417		2.18548		2.20439		2185.48		27.85655		54.8894916616		32.962		1.71071		1.72252		1710.71		27.87607		40.9495882804		31.9425		2.0575		2.07198		2057.5		27.8787		44.0276470085		2.1574533333		2157.4533333333		27.8985266667		89.3017588479		29.699		1.12497						27.84145		25.5095238095		29.7578		1.26001						27.85258		29.9403573805		1.19249		27.847015		0.0954876997

																						33.544		2.21492		2.29894		2214.92		28.47603		54.0329820453		33.7573		2.20577		2.21281		2205.77		28.37215		55.3990857947		33.4772		1.71115		1.72561		1711.15		28.39127		40.9601206434		32.4557		2.08686		2.08413		2086.86		28.3919		44.655910297		2.1691833333		2169.1833333333		28.41336		71.4407379115		30.2158		1.12788						28.35825		25.5755102041		30.2745		1.26976						28.36928		30.1720368786		1.19882		28.363765		0.1003243101

																						34.0622		2.24606		2.30601		2246.06		28.99423		54.7926424668		34.2723		2.20528		2.22087		2205.28		28.88715		55.3867791842		33.9932		1.71234		1.72853		1712.34		28.90727		40.9886058981		32.9713		2.09295		2.09596		2092.95		28.9075		44.7862278524		2.18143		2181.43		28.9296266667		79.2924012753		30.732		1.15085						28.87445		26.0963718821		30.7893		1.24746						28.88408		29.6421442829		1.199155		28.879265		0.0683135861

																						34.5787		2.24297		2.31275		2242.97		29.51073		54.7172619048		34.7885		2.23077		2.22862		2230.77		29.40335		56.0269740808		34.5112		1.72259		1.73128		1722.59		29.42527		41.2339620835		33.4888		2.11433		2.10745		2114.33		29.425		45.2437302063		2.1960233333		2196.0233333333		29.44636		71.010988821		31.2472		1.15182						29.38965		26.1183673469		31.305		1.25216						29.39978		29.753825682		1.20199		29.394715		0.0709510944

																						35.0932		2.25063		2.31916		2250.63		30.02523		54.9041276347		35.3037		2.22791		2.23603		2227.91		29.91855		55.9551436608		35.0288		1.7297		1.73387		1729.7		29.94287		41.404155496		34.0055		2.11139		2.11855		2111.39		29.9417		45.180818283		2.1966433333		2196.6433333333		29.9618266667		74.7003864336		31.7625		1.14053						29.90495		25.8623582766		31.8188		1.27707						29.91358		30.3457370972		1.2088		29.909265		0.0965483599

																						35.6122		2.24197		2.32534

																						36.1273		2.2095		2.3312

																						36.6455		2.24286		2.33683

																						37.1612		2.23034		2.34218

																						37.6778		2.24624		2.34731

																						38.199		2.24757		2.35225

																						38.7205		2.23013		2.35697

																						39.2367		2.23545		2.36143

																						39.7575		2.24168		2.36573

																						40.2745		2.22159		2.36981

																						40.7922		2.2309		2.37371

																						41.3088		2.22497		2.37743

																						41.8245		2.21454		2.38097

																						42.3425		2.22098		2.38438

																						42.8607		2.24173		2.38763

																						43.3802		2.22522		2.39075

																						43.8958		2.22902		2.3937

																						44.414		2.23093		2.39654

																						44.9305		2.2386		2.39924

																						45.4482		2.22607		2.40182

																						45.964		2.23312		2.40428

																						46.4805		2.2113		2.40664

																						46.995		2.23406		2.40888

																						47.5117		2.2136		2.41103

																						48.0272		2.22804		2.41308

																						48.544		2.21255		2.41505

																						49.0617		2.19309		2.41693

																						49.5833		2.23539		2.41874

																						50.1038		2.21982		2.42046

																						50.6227		2.21718		2.4221

																						51.1383		2.20379		2.42366

																						51.656		2.21664		2.42516

																						52.174		2.21366		2.42658

																						52.6927		2.22328		2.42795

																						53.2093		2.22119		2.42925

																						53.7253		2.21768		2.43049

																						54.242		2.18959		2.43168

																						54.7607		2.22366		2.43282

																						55.2818		2.20292		2.43391

																						55.8013		2.20069		2.43495

																						56.3205		2.21679		2.43595

																						56.8362		2.18801		2.43689

																						57.3528		2.21264		2.43779

																						57.8705		2.22296		2.43865

																						58.3883		2.18882		2.43948

																						58.9052		2.21075		2.44027

																						59.4218		2.21896		2.44102

																						59.9362		2.21931		2.44173

																						60.4552		2.21141		2.44242

																						60.9742		2.20502		2.44308

																						61.4935		2.21588		2.44371

																						62.013		2.21316		2.44431

																						62.5307		2.20824		2.44488

																						63.0518		2.19475		2.44544

																						63.5685		2.20171		2.44596

																						64.0843		2.19785		2.44645

																						64.6018		2.19975		2.44693

																						65.1198		2.18393		2.44739

																						65.6367		2.20027		2.44782

																						66.1532		2.19265		2.44823





GLP FULL

		



GLP-PVP 1:2 FaSSIF

GLP-PVP 1:2 pH 6.8

Time (min)

Dissolved (mg)



GLP-PVP 11 FULL

		0		0				0		0.0211616766		0.0211616766		0.0072059131		0.0072059131		0.0080224093		0.0080224093		0.0024600585		0.0024600585

		0.5171033333		0.51706				0.3559833333		0.045864655		0.045864655		0.0027170578		0.0027170578		0.0096873629		0.0096873629		0.00042699		0.00042699

		1.0341166667		1.036715				0.8727433333		0.060059241		0.060059241		0.0092256222		0.0092256222		0.0082363798		0.0082363798		0.00001985		0.00001985

		1.55009		1.5539				1.38758		0.0642213917		0.0642213917		0.0144971032		0.0144971032		0.0155789766		0.0155789766		0.000577395		0.000577395

		2.06771		2.071875				1.9035566667		0.0705485517		0.0705485517		0.0133480547		0.0133480547		0.0143889159		0.0143889159		0.00149305		0.00149305

		2.58464		2.588935				2.4186533333		0.077359539		0.077359539		0.0090304607		0.0090304607		0.0205867068		0.0205867068		0.00250724		0.00250724

		3.1014766667		3.104425				2.9348033333		0.0921267193		0.0921267193		0.0031494536		0.0031494536		0.0138126239		0.0138126239		0.0030001		0.0030001

		3.6184966667		3.621225				3.4502533333		0.0987932048		0.0987932048		0.0032795613		0.0032795613		0.0219775859		0.0219775859		0.00304005		0.00304005

		4.1357633333		4.13997				3.9650166667		0.1106409963		0.1106409963		0.0095593766		0.0095593766		0.0287021714		0.0287021714		0.0024658		0.0024658

		4.6527766667		4.65599				4.4806266667		0.1200453469		0.1200453469		0.0183168941		0.0183168941		0.0283457895		0.0283457895		0.0033365		0.0033365

		5.16962		5.17109				4.9960866667		0.1202801197		0.1202801197		0.0236279731		0.0236279731		0.029619996		0.029619996		0.00400855		0.00400855

		5.6871533333		5.687885				5.51154		0.1205243836		0.1205243836		0.0235268568		0.0235268568		0.0294205918		0.0294205918		0.0039763		0.0039763

		6.2042466667		6.203775				6.0276		0.1209858243		0.1209858243		0.0266593399		0.0266593399		0.0331017897		0.0331017897		0.00373265		0.00373265

		6.7210933333		6.72005				6.5419166667		0.1282485096		0.1282485096		0.0329165278		0.0329165278		0.0350456263		0.0350456263		0.0035881		0.0035881

		7.23976		7.2349				7.0577166667		0.1384865021		0.1384865021		0.0310511801		0.0310511801		0.0353928157		0.0353928157		0.00485905		0.00485905

		7.7567666667		7.752215				7.57213		0.1572488475		0.1572488475		0.0353914015		0.0353914015		0.0332672527		0.0332672527		0.00411355		0.00411355

		8.2739666667		8.269675				8.08749		0.17861211		0.17861211		0.0623986379		0.0623986379		0.0383089241		0.0383089241		0.0037421		0.0037421

		8.7923		8.787225				8.6033966667		0.2062560787		0.2062560787		0.034289022		0.034289022		0.0330657273		0.0330657273		0.007910545		0.007910545

		9.3097		9.306275				9.1178633333		0.2404292624		0.2404292624		0.033301901		0.033301901		0.0308206633		0.0308206633		0.0053162409		0.0053162409

		9.8264666667		9.823675				9.63413		0.2828354997		0.2828354997		0.0315687822		0.0315687822		0.0459732545		0.0459732545		0.0060193879		0.0060193879

		10.3426		10.340625				10.1481633333		0.2919024615		0.2919024615		0.0326937891		0.0326937891		0.0480641692		0.0480641692		0.0074061657		0.0074061657

		10.8587		10.856675				10.6633633333		0.4050537375		0.4050537375		0.0317116178		0.0317116178		0.061982152		0.061982152		0.0058441668		0.0058441668

		11.3758		11.373225				11.18013		0.4345044576		0.4345044576		0.0302111372		0.0302111372		0.0590115964		0.0590115964		0.0067849724		0.0067849724

		11.8930666667		11.890075				11.6948966667		0.474875585		0.474875585		0.0310943136		0.0310943136		0.0711448417		0.0711448417		0.0057949522		0.0057949522

		12.4107666667		12.405825				12.21123		0.4880567519		0.4880567519		0.0339170839		0.0339170839		0.0733340443		0.0733340443		0.0059941442		0.0059941442

		12.9285		12.921625				12.72593		0.4465594676		0.4465594676		0.0361791185		0.0361791185		0.0704702618		0.0704702618		0.0050638745		0.0050638745

		13.4452333333		13.437375				13.2410966667		0.4505672259		0.4505672259		0.0393052375		0.0393052375		0.0892934443		0.0892934443		0.006532606		0.006532606

		13.9627666667		13.954175				13.7572633333		0.405039827		0.405039827		0.0401806357		0.0401806357		0.0923693588		0.0923693588		0.0073238585		0.0073238585

		14.4796333333		14.473025				14.2713966667		0.381103703		0.381103703		0.0417829397		0.0417829397		0.1041780421		0.1041780421		0.0080757958		0.0080757958

		14.9955333333		14.988425				14.7851966667		0.3546391758		0.3546391758		0.0372786695		0.0372786695		0.1099833887		0.1099833887		0.007131384		0.007131384

		15.5103		15.504525				15.29943		0.3016183304		0.3016183304		0.039533633		0.039533633		0.1312248765		0.1312248765		0.0068616228		0.0068616228

		16.0261333333		16.022375				15.8141633333		0.2896236774		0.2896236774		0.0429850212		0.0429850212		0.115116984		0.115116984		0.0074158531		0.0074158531

		16.5419333333		16.538175				16.3287633333		0.2654782736		0.2654782736		0.0456154585		0.0456154585		0.0963432989		0.0963432989		0.0059507985		0.0059507985

		17.0593		17.054275				16.8429633333		0.1953278035		0.1953278035		0.042963808		0.042963808		0.0914642621		0.0914642621		0.005846571		0.005846571

		17.5759666667		17.571325				17.35723		0.1946432985		0.1946432985		0.0512440284		0.0512440284		0.088635835		0.088635835		0.0070677444		0.0070677444

		18.0913666667		18.087825				17.8729633333		0.1389387787		0.1389387787		0.058810071		0.058810071		0.1040507629		0.1040507629		0.0057643345		0.0057643345

		18.6075333333		18.603925				18.3884966667		0.1704818196		0.1704818196		0.0691550432		0.0691550432		0.1061225857		0.1061225857		0.0066449653		0.0066449653

		19.1239		19.119425				18.90373		0.1870636622		0.1870636622		0.0627557268		0.0627557268		0.0954452733		0.0954452733		0.0065570012		0.0065570012

		19.6409333333		19.636625				19.41913		0.1701638143		0.1701638143		0.0760988318		0.0760988318		0.0908702925		0.0908702925		0.0068897656		0.0068897656

		20.1579666667		20.153125				19.9347633333		0.1989274869		0.1989274869		0.0559816439		0.0559816439		0.1000697517		0.1000697517		0.0061708502		0.0061708502

		20.6739666667		20.671575				20.4496966667		0.1690912335		0.1690912335		0.047552931		0.047552931		0.0907218		0.0907218		0.0049427471		0.0049427471

		21.19		21.187675				20.9642966667		0.163619917		0.163619917		0.0428011735		0.0428011735		0.07674937		0.07674937		0.0048045077		0.0048045077

		21.7061666667		21.704075				21.48053		0.2212762102		0.2212762102		0.0281994184		0.0281994184		0.0923340035		0.0923340035		0.0059739916		0.0059739916

		22.2222666667		22.219775				21.99573		0.1762282569		0.1762282569		0.0221748687		0.0221748687		0.0968099894		0.0968099894		0.0064748354		0.0064748354

		22.7384		22.734175				22.5104633333		0.1936966536		0.1936966536		0.0040305087		0.0040305087		0.0999707567		0.0999707567		0.0059310703		0.0059310703

		23.2559666667		23.250925				23.02743		0.1854307691		0.1854307691		0.0118511097		0.0118511097		0.1078054999		0.1078054999		0.0073549712		0.0073549712

		23.7709333333		23.768175				23.5422966667		0.1834939951		0.1834939951		0.0275205959		0.0275205959		0.0877307383		0.0877307383		0.0059690419		0.0059690419

		24.2855333333		24.285925				24.05833		0.1729283847		0.1729283847		0.022839549		0.022839549		0.1002182441		0.1002182441		0.0058807243		0.0058807243

		24.8009		24.801075				24.57373		0.1806177235		0.1806177235		0.0782837917		0.0782837917		0.0914289068		0.0914289068		0.0058787444		0.0058787444

		25.3156666667		25.316675				25.0883633333		0.1767766319		0.1767766319		0.086754931		0.086754931		0.0846972503		0.0846972503		0.005994922		0.005994922

		25.8312666667		25.835275				25.6047966667		0.1680868713		0.1680868713		0.0830426204		0.0830426204		0.089880343		0.089880343		0.0057551421		0.0057551421

		26.3468666667		26.350675				26.1203966667		0.1927370375		0.1927370375		0.0903894598		0.0903894598		0.09290676		0.09290676		0.0050165691		0.0050165691

		26.8619666667		26.866575				26.6357966667		0.1877377328		0.1877377328		0.1878287743		0.1878287743		0.0954169891		0.0954169891		0.005980992		0.005980992

		27.3781333333		27.381575				27.15053		0.1924761003		0.1924761003		0.1550968014		0.1550968014		0.099475782		0.099475782		0.0049947902		0.0049947902

		27.8934333333		27.897525				27.6653633333		0.2025833982		0.2025833982		0.1645649612		0.1645649612		0.0954876997		0.0954876997		0.0029058553		0.0029058553

		28.4108666667		28.415275				28.1810966667		0.1914515692		0.1914515692		0.1782404063		0.1782404063		0.1003243101		0.1003243101		0.0049894162		0.0049894162

		28.9254		28.931175				28.6969966667		0.1798995009		0.1798995009		0.1426092956		0.1426092956		0.0683135861		0.0683135861		0.0051363529		0.0051363529

		29.4409666667		29.447725				29.2116633333		0.196230169		0.196230169		0.1758291722		0.1758291722		0.0709510944		0.0709510944		0.0048169528		0.0048169528

		29.9560666667		29.963275				29.72693		0.2215739215		0.2215739215		0.1299945107		0.1299945107		0.0965483599		0.0965483599		0.0026271845		0.0026271845



GLP-PEOX 1:3 FaSSIF

GLP-PEOX 1:2 FaSSIF

GLP-PVP 1:2 FaSSIF

GLP FaSSIF

Time (min)

Dissolved (mg)

0.0466727333

0.02135565

0.0022645015

0.1257027667

0.06707405

0.00512764

0.202518

0.1102325

0.00564931

0.2785223333

0.151874

0.008790305

0.3586873333

0.1887415

0.01017685

0.432358

0.2229825

0.01172546

0.5115093333

0.255738

0.013727

0.5816053333

0.287839

0.01463455

0.6611563333

0.3196715

0.0177145

0.7366226667

0.349346

0.0175237

0.8088936667

0.3810035

0.01902725

0.879093

0.416357

0.020174

0.949867

0.448943

0.02045475

1.0248486667

0.4789645

0.0210284

1.0963596667

0.5144495

0.02322565

1.1769066667

0.5453855

0.02344085

1.2565566667

0.5599125

0.0241416

1.31822

0.613005

0.0258326

1.4001233333

0.646945

0.02801745

1.48436

0.6809415

0.02729285

1.5621033333

0.712533

0.02710095

1.6798533333

0.7453655

0.02917925

1.7356633333

0.7782045

0.0298755

1.8096033333

0.809162

0.02994195

1.9016933333

0.838316

0.0323698

1.92026

0.8676425

0.030889

1.9951533333

0.896028

0.03273265

2.0697666667

0.925876

0.03355855

2.1028766667

0.955003

0.03394365

2.1996233333

0.98793

0.03428745

2.2588866667

1.0158955

0.0354873

2.3230033333

1.042705

0.0363781

2.3740833333

1.069865

0.03885325

2.4443666667

1.10044

0.03737975

2.4928266667

1.123195

0.03839275

2.4977366667

1.146075

0.03832

2.5564

1.16669

0.0387987

2.5944433333

1.198825

0.0408249

2.58042

1.21683

0.0417977

2.6201566667

1.258145

0.04308845

2.6520633333

1.291035

0.04070335

2.6521733333

1.321065

0.0440565

2.66055

1.35782

0.04392425

2.6994533333

1.38814

0.0452727

2.6959133333

1.42682

0.0459359

2.7303366667

1.4637

0.04620915

2.7527233333

1.50024

0.04690505

2.7526533333

1.52224

0.0479811

2.7593966667

1.586385

0.0484086

2.77114

1.617135

0.04819515

2.7992

1.63907

0.0498289

2.8131733333

1.668505

0.05022765

2.78651

1.761505

0.050712

2.7891

1.76219

0.05103155

2.8406833333

1.792465

0.05295855

2.8409133333

1.825735

0.05291055

2.8459066667

1.82373

0.05339205

2.8754233333

1.87028

0.0539374

2.86007

1.86064

0.0540479



GLP-PVP 12 FULL 

		GLP-PX 5K 1:2								445.54																GLP-PX 5K -1				17B-27005								GLP-PX 5K -2				17C-09014								GLP-PX 5K -3				17E-10007								GLP-PX 5K -4				17E-10017								GLP-PX 5K -5				17E-11009				GLP-PX 5K 1:2 pH 6.8												GLP-PX 5K FaSSIF-1				17C-10001								GLP-PX 5K FaSSIF-2				17C-10003				GLP-PX 5K 1:2 FaSSIF

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/ml)		IDR (ug/min/cm2)

		GLP-PX 5K -1		17B-27005		1.024		15.9		0.31		4.90		20.89		49.4656		706.6518

		GLP-PX 5K -2		17C-09014		1.037		17.76		0.31		5.47		18.95		51.7548		739.3544				Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile																				Dissolution Profile												Dissolution Profile

		GLP-PX 5K -3		17E-10007		1.236		14.9		0.31		4.59		26.92		57.4221		820.3160																																																																AVERAGE				TIME		SD																										AVERAGE		TIME		SD

		GLP-PX 5K -4		17E-10017		0.589		17.15		0.31		5.29		11.15		17.6596		252.2797				Time (minutes)		Weight (mg)		Weight (mg)		Weight (µg)		Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)		Weight (µg)		Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)		Weight (µg)		Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (µg)		Weight (mg)		Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)		Weight (µg)		Time zero (min)		%		mg		Weight (µg)						Time (minutes)		Weight (mg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)				Time zero (min)		%		mg

		GLP-PX 5K -5		17E-11009		1.660		12.69		0.31		3.91		42.45		92.2281		1317.5437				5.04375		0.150816		0.146114		150.816		0		3.077638877		5.0388		0.113808		0.112728		113.808		0		2.0792044478		5.08047		0.424149		0.441184		424.149		0		9.2363321995		4.12708		207.514		208.805		0.207514		0		3926.0031443745		5.04505		0.26558		0.30996		265.58		0		6.790489939		0.229591		229.591		0		169.5051903011		2.52318		0.023219		0.026451				0		0.5936756755		1.86797		0.0162603		0.0473339				0		0.3461871573		0.02135565		0		0.0072059131

		AVG				1.0990								22.251		52.881		755.441				5.56172		0.182355		0.177716		182.355		0.51797		3.7212420261		5.55417		0.146013		0.142788		146.013		0.51537		2.6675706368		5.59818		0.464227		0.475014		464.227		0.51771		10.1090767348		4.64505		215.562		218.099		0.215562		0.51797		4078.2650317938		5.56223		0.327083		0.359258		327.083		0.51718		8.3630311798		0.2641983333		264.1983333333		0.5170166667		174.1803256896		3.04115		0.0694699		0.0651528				0.51797		1.7762431547		2.38412		0.0689953		0.0804331				0.51615		1.4689327243		0.06707405		0.51706		0.0027170578

		SD				0.1191								4.159		4.096		58.515				6.08152		0.211867		0.208446		211.867		1.03777		4.3234810362		6.0698		0.172812		0.172189		172.812		1.031		3.1571724223		6.11588		0.501532		0.507518		501.532		1.03541		10.9214360064		5.16302		227.66		227.271		0.22766		1.03594		4307.1497626584		6.08022		0.387877		0.407044		387.877		1.03517		9.9174443335		0.2954036667		295.4036666667		1.0347266667		179.5772552645		3.56198		0.10471		0.103709				1.0388		2.6772806744		2.9026		0.116756		0.113517				1.03463		2.4857738013		0.1102325		1.036715		0.0092256222

		RSD				10.839								18.690		7.746		7.746				6.6		0.238921		0.238148		238.921		1.55625		4.8755606708		6.58647		0.199647		0.200986		199.647		1.54767		3.6474319063		6.63412		0.536953		0.53878		536.953		1.55365		11.6927690117		5.6789		233.321		236.284		0.233321		1.55182		4414.2514704964		6.59662		0.443315		0.453151		443.315		1.55157		11.3349124457		0.3251736667		325.1736666667		1.5525233333		184.4545371883		4.0789		0.14131		0.141623				1.55572		3.6130888368		3.42005		0.162125		0.146371				1.55208		3.4516947955		0.151874		1.5539		0.0144971032

		GLP-PX 5K FaSSIF-1		17C-10001		1.014		12.69		0.31		3.91		25.93		71.36		1019.47				7.11875		0.265544		0.266944		265.544		2.075		5.4188450692		7.10443		0.226732		0.229207		226.732		2.06563		4.1422587415		7.15208		0.570952		0.568801		570.952		2.07161		12.4331363318		6.19843		246.796		245.241		0.246796		2.07135		4669.1879681325		7.1138		0.494748		0.497845		494.748		2.06875		12.6499785991		0.3544093333		354.4093333333		2.0707466667		188.5328557608		4.5974		0.17752		0.179303				2.07422		4.5389252729		3.9375		0.19818		0.179062				2.06953		4.2193176534		0.1887415		2.071875		0.0133480547

		GLP-PX 5K FaSSIF-2		17C-10003		0.962		15.24		0.31		4.70		20.47		64.05		915.06				7.63568		0.29073		0.294751		290.73		2.59193		5.932805211		7.62188		0.254819		0.256763		254.819		2.58308		4.6553915207		7.66927		0.602986		0.597603		602.986		2.5888		13.1307135173		6.71615		255.852		254.047		0.255852		2.58907		4840.5204299204		7.63073		0.54622		0.541081		546.22		2.58568		13.9660419252		0.382845		382.845		2.5879366667		191.4913702781		5.11537		0.21601		0.216597				2.59219		5.5230579552		4.45365		0.229368		0.211509				2.58568		4.883320474		0.2229825		2.588935		0.0090304607

																						8.15313		0.316097		0.321726		316.097		3.10938		6.450458944		8.13932		0.28256		0.283698		282.56		3.10052		5.1622030856		8.18723		0.629318		0.625318		629.318		3.10676		13.7041230962		7.23282		259.332		262.72		0.259332		3.10574		4906.3593176215		8.1474		0.59513		0.582907		595.13		3.10235		15.2165986799		0.409325		409.325		3.1055533333		191.2560394576		5.63282		0.254326		0.253511				3.10964		6.5027417134		4.96718		0.257965		0.243632				3.09921		5.4921600488		0.255738		3.104425		0.0031494536

		AVG		amount at		0.988								23.203		67.708		967.263				8.67213		0.343456		0.347944		343.456		3.62838		7.0087625858		8.65443		0.306883		0.30991		306.883		3.61563		5.6065698242		8.70547		0.654814		0.651961		654.814		3.625		14.2593278138		7.74948		271.505		271.277		0.271505		3.6224		5136.6629900315		8.66485		0.637891		0.623449		637.891		3.6198		16.3099345497		0.435051		435.051		3.6230033333		191.1968310642		6.1513		0.288613		0.290158				3.62812		7.3794098681		5.4823		0.28552		0.275695				3.61433		6.0788150994		0.287839		3.621225		0.0032795613

		SD		15 min		0.037								3.862		5.168		73.827				9.19063		0.367946		0.373325		367.946		4.14688		7.5085197474		9.17032		0.334998		0.335571		334.998		4.13152		6.1202141467		9.2198		0.683601		0.67737		683.601		4.13933		14.8861978407		8.26537		284.445		279.708		0.284445		4.13829		5381.4777046445		9.18177		0.681376		0.662647		681.376		4.13672		17.4217820344		0.4621816667		462.1816666667		4.1392433333		192.4611221944		6.66927		0.327757		0.326431				4.14609		8.3802643684		6.00182		0.312912		0.307872				4.13385		6.6619998263		0.3196715		4.13997		0.0095593766

		RSD				3.773								16.645		7.633		7.633				9.71198		0.388906		0.398053		388.906		4.66823		7.9362416792		9.69037		0.35965		0.360857		359.65		4.65157		6.5705915195		9.73932		0.709031		0.702032		709.031		4.65885		15.4399653324		8.78047		290.014		288.015		0.290014		4.65339		5486.838844187		9.69948		0.718548		0.700643		718.548		4.65443		18.3722153954		0.4858623333		485.8623333333		4.65955		193.82251861		7.1862		0.367585		0.362298				4.66302		9.3986077425		6.51693		0.336394		0.339617				4.64896		7.1619393617		0.349346		4.65599		0.0183168941

																						10.23		0.412058		0.421857		412.058		5.18625		8.4086948359		10.2055		0.385473		0.385337		385.473		5.1667		7.0423623656		10.257		0.732918		0.725643		732.918		5.17653		15.9601322248		9.29635		298.976		296.225		0.298976		5.16927		5656.3928992381		10.2159		0.756844		0.737324		756.844		5.17085		19.3513877831		0.5101496667		510.1496666667		5.1764933333		193.3804237981		7.7013		0.412664		0.397711				5.17812		10.5512114625		7.03203		0.364296		0.371205				5.16406		7.755982157		0.3810035		5.17109		0.0236279731

																						10.7477		0.434915		0.444914		434.915		5.70395		8.8751280513		10.7206		0.408446		0.409269		408.446		5.6818		7.4620654074		10.7742		0.753081		0.748307		753.081		5.69373		16.399204735		9.81223		306.605		304.326		0.306605		5.68515		5800.7276332244		10.7333		0.79175		0.772898		791.75		5.68825		20.2438828573		0.5321473333		532.1473333333		5.69316		191.7913339813		8.21927		0.459881		0.432993				5.69609		11.7584806976		7.54765		0.399721		0.402669				5.67968		8.5101921069		0.416357		5.687885		0.0235268568

																						11.2675		0.461879		0.467346		461.879		6.22375		9.4253710937		11.2362		0.436265		0.432688		436.265		6.1974		7.970301986		11.2891		0.778284		0.769987		778.284		6.20863		16.9480290407		10.3302		313.891		312.352		0.313891		6.20312		5938.5730745436		11.249		0.826512		0.807209		826.512		6.20395		21.1326960633		0.5588093333		558.8093333333		6.2099266667		190.5016173956		8.7349		0.505846		0.467794				6.21172		12.9337381343		8.0638		0.430092		0.434009				6.19583		9.1568007276		0.448943		6.203775		0.0266593399

																						11.7844		0.485478		0.488963		485.478		6.74065		9.9069459919		11.7542		0.459813		0.455684		459.813		6.7154		8.4005099356		11.8029		0.797424		0.790781		797.424		6.72243		17.3648245496		10.8482		325.533		320.271		0.325533		6.72112		6158.8306408129		11.7659		0.859634		0.840502		859.634		6.72085		21.9795768818		0.580905		580.905		6.72616		187.9495439659		9.25		0.544654		0.50224				6.72682		13.9260016088		8.58125		0.455689		0.465272				6.71328		9.7017693116		0.4789645		6.72005		0.0329165278

																						12.3011		0.510197		0.509903		510.197		7.25735		10.4113762606		12.2688		0.482678		0.478016		482.678		7.23		8.8182398817		12.3193		0.818561		0.810866		818.561		7.23883		17.8251070298		11.3659		331.314		328.082		0.331314		7.23882		6268.2026551234		12.2838		0.891008		0.872788		891.008		7.23875		22.7817639115		0.603812		603.812		7.24206		186.4863898278		9.76563		0.591516		0.536406				7.24245		15.124194016		9.09532		0.492493		0.496177				7.22735		10.485338627		0.5144495		7.2349		0.0310511801

																						12.819		0.534113		0.530246		534.113		7.77525		10.899420045		12.7872		0.502229		0.500011		502.229		7.7484		9.1754250194		12.8336		0.835524		0.83009		835.524		7.75313		18.1944958604		11.8813		334.707		335.753		0.334707		7.75422		6332.3955706321		12.8023		0.919686		0.904067		919.686		7.75725		23.5150181869		0.6239553333		623.9553333333		7.7589266667		183.9160756985		10.2836		0.638965		0.570411				7.76042		16.3373951499		9.61198		0.52036		0.527085				7.74401		11.0786362607		0.5453855		7.752215		0.0353914015

																						13.3372		0.557033		0.549969		557.033		8.29345		11.3671388749		13.3029		0.521087		0.521393		521.087		8.2641		9.5199494595		13.35		0.852885		0.848639		852.885		8.26953		18.5725515986		12.3964		339.436		343.32		0.339436		8.26932		6421.8645648674		13.3221		0.947919		0.934411		947.919		8.27705		24.2368944669		0.6436683333		643.6683333333		8.2756933333		182.0761899243		10.8005		0.67184		0.604035				8.27732		17.1779605416		10.13		0.51579		0.557917				8.26203		10.9813394513		0.5599125		8.269675		0.0623986379

																						13.8544		0.580051		0.569044		580.051		8.81065		11.8368575498		13.8175		0.539883		0.542253		539.883		8.7787		9.8633411965		13.8643		0.870543		0.866392		870.543		8.78383		18.9570748533		12.9143		346.123		350.828		0.346123		8.78722		6548.3773930449		13.8396		0.977582		0.963645		977.582		8.79455		24.9953337435		0.6634923333		663.4923333333		8.79106		180.4324000321		11.3159		0.715028		0.637251				8.79272		18.2822141732		10.6497		0.588759		0.588704				8.78173		12.534873561		0.613005		8.787225		0.034289022

																						14.3716		0.5999		0.587529		599.9		9.32785		12.2419077704		14.3331		0.558237		0.562686		558.237		9.2943		10.1986578564		14.382		0.889247		0.883565		889.247		9.30153		19.3643759609		13.4305		358.409		358.21		0.358409		9.30342		6780.8189373831		14.3565		1.00403		0.99191		1004.03		9.31145		25.6715701992		0.6824613333		682.4613333333		9.3078933333		180.2891714617		11.8365		0.767638		0.670493				9.31332		19.6273744854		11.1672		0.623397		0.619199				9.29923		13.272328021		0.646945		9.306275		0.033301901
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																						27.8115		0.931353		0.910816		931.353		22.76775		19.0057301679		27.7355		0.901477		0.959324		901.477		22.6967		16.4694484394		27.8032		1.15913		1.15528		1159.13		22.72273		25.2413886215		26.8492		524.569		519.34		0.524569		22.72212		9924.4366329085		27.7782		1.45977		1.47863		1459.77		22.73315		37.324171618		0.99732		997.32		22.72906		140.9255155002		25.2712		2.12696		1.42967				22.74802		54.3832384997		24.5883		1.42397		1.35941				22.72033		30.3167915983		1.42682		22.734175		0.0040305087

																						28.3297		0.93509		0.918755		935.09		23.28595		19.08198956		28.2533		0.913903		0.970442		913.903		23.2145		16.6964640663		28.3203		1.1539		1.16113		1153.9		23.23983		25.1274993576		27.3662		526.933		524.5		0.526933		23.23912		9969.1616704158		28.2938		1.48093		1.49032		1480.93		23.24875		37.8652016922		1.0009643333		1000.9643333333		23.24676		132.86914934		25.7867		2.17246		1.45532				23.26352		55.5466065704		25.1063		1.47208		1.38611				23.23833		31.3410693877		1.4637		23.250925		0.0118511097

																						28.8482		0.944353		0.926453		944.353		23.80445		19.2710157171		28.7703		0.92666		0.981292		926.66		23.7315		16.9295268663		28.8357		1.16398		1.16674		1163.98		23.75523		25.3470029485		27.8823		533.07		529.583		0.53307		23.75522		10085.2689272613		28.8093		1.48693		1.50162		1486.93		23.76425		38.0186128664		1.0116643333		1011.6643333333		23.7637266667		132.2055494158		26.3028		2.23271		1.48078				23.77962		57.0871104443		25.6247		1.5197		1.41269				23.75673		32.3549149153		1.50024		23.768175		0.0275205959

																						29.364		0.953912		0.933874		953.912		24.32025		19.4660822222		29.2888		0.941167		0.991929		941.167		24.25		17.194561125		29.3528		1.17108		1.17214		1171.08		24.27233		25.5016136127		28.3973		535.703		534.588		0.535703		24.27022		10135.083235111		29.325		1.48859		1.51257		1488.59		24.27995		38.0610566246		1.022053		1022.053		24.28086		129.2183957608		26.8208		2.28004		1.50609				24.29762		58.2972689231		26.1422		1.53839		1.4391				24.27423		32.7528311881		1.52224		24.285925		0.022839549

																						29.881		0.962746		0.941083		962.746		24.83725		19.6463539562		29.8068		0.951541		1.00232		951.541		24.768		17.3840879328		29.8693		1.17767		1.17732		1177.67		24.78883		25.6451184405		28.9128		539.909		539.532		0.539909		24.78572		10214.6574769706		29.839		1.51163		1.52314		1511.63		24.79395		38.6501555334		1.0306523333		1030.6523333333		24.7980266667		127.4442377683		27.336		2.31441		1.53103				24.81282		59.1760592658		26.6573		1.64174		1.46526				24.78933		34.9531868218		1.586385		24.801075		0.0782837917

																						30.3997		0.969183		0.948091		969.183		25.35595		19.7777111163		30.3237		0.962639		1.01244		962.639		25.2849		17.5868417899		30.3848		1.18022		1.18229		1180.22		25.30433		25.7006476227		29.4277		541.027		544.404		0.541027		25.30062		10235.8091656056		30.3557		1.53085		1.53341		1530.85		25.31065		39.1415826613		1.0373473333		1037.3473333333		25.31506		123.7746142968		27.8522		2.38605		1.55579				25.32902		61.0077886853		27.1723		1.67848		1.49128				25.30433		35.735393556		1.617135		25.316675		0.086754931

																						30.9177		0.980408		0.954874		980.408		25.87395		20.0067749848		30.8412		0.971688		1.02236		971.688		25.8024		17.752161636		30.9015		1.18885		1.18708		1188.85		25.82103		25.8885757962		29.9427		545.646		549.213		0.545646		25.81562		10323.1970455745		30.8698		1.54013		1.54332		1540.13		25.82475		39.3788586106		1.046982		1046.982		25.83246		122.9386296816		28.369		2.42801		1.58035				25.84582		62.0806441633		27.6927		1.69779		1.51744				25.82473		36.1465098336		1.63907		25.835275		0.0830426204

																						31.4343		0.983759		0.96143		983.759		26.39055		20.0751574368		31.3563		0.976884		1.03201		976.884		26.3175		17.8470894645		31.4163		1.19383		1.19166		1193.83		26.33583		25.9970210227		30.4583		562.625		553.965		0.562625		26.33122		10644.4264922062		31.386		1.55957		1.55294		1559.57		26.34095		39.8759108149		1.051491		1051.491		26.34796		123.3171099118		28.8838		2.48656		1.60459				26.36062		63.5776815378		28.2087		1.73242		1.54326				26.34073		36.8837939709		1.668505		26.350675		0.0903894598

																						31.9523		0.992577		0.9678		992.577		26.90855		20.2551026655		31.8718		0.984788		1.04144		984.788		26.833		17.9914908419		31.9313		1.19618		1.19607		1196.18		26.85083		26.0481949749		30.9737		548.683		558.651		0.548683		26.84662		10380.6547185482		31.9038		1.56938		1.56228		1569.38		26.85875		40.1267380847		1.0578483333		1057.8483333333		26.8641266667		119.8620233115		29.4003		2.56575		1.62869				26.87712		65.6024533515		28.724		1.89432		1.56891				26.85603		40.3306984421		1.761505		26.866575		0.1878287743

																						32.4717		0.997226		0.973988		997.226		27.42795		20.3499728592		32.387		0.99915		1.05066		999.15		27.3482		18.253876037		32.4462		1.20476		1.20031		1204.76		27.36573		26.235034341		31.4888		561.372		563.274		0.561372		27.36172		10620.7207087897		32.4195		1.60166		1.57128		1601.66		27.37445		40.9520902017		1.0670453333		1067.0453333333		27.3806266667		119.2682795438		29.9158		2.57752		1.65252				27.39262		65.9033949381		29.2385		1.87186		1.5944				27.37053		39.8525176241		1.76219		27.381575		0.1550968014

																						32.9872		1.00481		0.97994		1004.81		27.94345		20.5047363674		32.9027		1.0082		1.05969		1008.2		27.8639		18.4192141525		32.9615		1.20916		1.20438		1209.16		27.88103		26.3308494005		32.0037		557.927		567.832		0.557927		27.87662		10555.5439938096		32.9352		1.60386		1.58		1603.86		27.89015		41.0083409655		1.0740566667		1074.0566666667		27.8961266667		117.0151957369		30.4305		2.65209		1.6761				27.90732		67.8100401477		29.7557		1.90883		1.61989				27.88773		40.6396211343		1.792465		27.897525		0.1645649612

																						33.5047		1.00432		0.985732		1004.32		28.46095		20.4947371428		33.4182		1.01582		1.0685		1015.82		28.3794		18.5584270188		33.4783		1.21674		1.20831		1216.74		28.39783		26.4959126167		32.5193		575.629		572.338		0.575629		28.39222		10890.4520369379		33.4495		1.61644		1.58841		1616.44		28.40445		41.3299930607		1.07896		1078.96		28.4127266667		119.4594441641		30.9505		2.65456		1.6997				28.42732		67.8731944144		30.2712		1.95177		1.64517				28.40323		41.5538279162		1.825735		28.415275		0.1782404063

																						34.0217		1.01075		0.991339		1010.75		28.97795		20.6259514568		33.9357		1.02216		1.07715		1022.16		28.8969		18.6742550467		33.9955		1.21867		1.21208		1218.67		28.91503		26.537940586		33.0355		573.121		576.788		0.573121		28.90842		10843.0026316636		33.9658		1.62459		1.59659		1624.59		28.92075		41.5383765723		1.08386		1083.86		28.92996		116.8881905925		31.4663		2.75507		1.72289				28.94312		70.4430872669		30.7872		1.92457		1.67035				28.91923		40.9747309328		1.82373		28.931175		0.1426092956

																						34.5393		1.01374		0.996779		1013.74		29.49555		20.6869671332		34.4508		1.03043		1.08557		1030.43		29.412		18.8253430263		34.5128		1.23407		1.21571		1234.07		29.43233		26.8732932943		33.551		582.88		581.174		0.58288		29.42392		11027.635305536		34.4828		1.64744		1.60451		1647.44		29.43775		42.1226174605		1.0927466667		1092.7466666667		29.4466266667		122.6737642421		31.9838		2.74694		1.74595				29.46062		70.2352151259		31.3028		1.99461		1.69539				29.43483		42.4659056651		1.87028		29.447725		0.1758291722

																						35.0583		1.02351		1.00206		1023.51		30.01455		20.8863394267		34.9663		1.03708		1.09381		1037.08		29.9275		18.9468345698		35.0295		1.23627		1.21919		1236.27		29.94903		26.921200824		34.0657		589.293		585.494		0.589293		29.93862		11148.964267268		34.999		1.66038		1.61217		1660.38		29.95395		42.4534742262		1.0989533333		1098.9533333333		29.9636933333		119.1131245217		32.4995		2.82747		1.76872				29.97632		72.2942487685		31.8182		1.95256		1.72029				29.95023		41.5706472771		1.86064		29.963275		0.1299945107

																						35.574		1.02411		1.00715

																						36.0885		1.02318		1.01208

																						36.6038		1.04093		1.01685

																						37.1205		1.04341		1.0215

																						37.6383		1.04324		1.02601

																						38.1555		1.04984		1.03037

																						38.6722		1.05172		1.0346

																						39.1885		1.06432		1.03869

																						39.7052		1.06256		1.04266

																						40.223		1.0667		1.04651

																						40.7378		1.07107		1.05022

																						41.2538		1.06881		1.05383

																						41.7713		1.07669		1.05734

																						42.2885		1.08388		1.06073

																						42.8045		1.08547		1.06402

																						43.3208		1.09184		1.0672

																						43.8375		1.09393		1.07029

																						44.3545		1.10027		1.07329

																						44.8722		1.09825		1.07619

																						45.3878		1.10943		1.079

																						45.9023		1.11539		1.08171

																						46.4208		1.13007		1.08436

																						46.9388		1.13522		1.08693

																						47.4587		1.1364		1.08942

																						47.9823		1.14358		1.09185

																						48.4987		1.15412		1.09418

																						49.0143		1.15722		1.09643

																						49.5343		1.16195		1.09863

																						50.0523		1.16502		1.10075

																						50.57		1.16927		1.10281

																						51.0857		1.18004		1.1048

																						51.6003		1.18146		1.10672

																						52.1157		1.18059		1.10858

																						52.6333		1.18595		1.11039

																						53.1513		1.1944		1.11215

																						53.668		1.19776		1.11385

																						54.1837		1.20274		1.1155

																						54.7		1.19826		1.11709

																						55.217		1.20741		1.11864

																						55.7342		1.21505		1.12015

																						56.2513		1.21796		1.1216

																						56.7695		1.22088		1.12301

																						57.2865		1.21925		1.12438

																						57.8042		1.22728		1.12571

																						58.3218		1.23687		1.12699

																						58.842		1.23545		1.12824

																						59.3605		1.23786		1.12945

																						59.8778		1.25392		1.13062

																						60.3948		1.25059		1.13175

																						60.9117		1.27143		1.13284

																						61.4295		1.28709		1.13391

																						61.9473		1.30022		1.13494

																						62.4672		1.31648		1.13594

																						62.9867		1.32215		1.13691

																						63.5065		1.33665		1.13786

																						64.025		1.34389		1.13877

																						64.5438		1.35286		1.13965

																						65.0593		1.35675		1.1405

																						65.576		1.36119		1.14132

																						66.093		1.36466		1.14212





GLP-PVP 12 FULL 

		



GLP-PX 5K 1:2 FaSSIF

GLP-PX 5K 1:2 pH 6.8

Time (min)

Dissolved (mg)



GLP-PVP 12 FULL  (2)

		GLP-PX 5K 1:3								445.54																GLP-PX 5K -1				17E-07001								GLP-PX 5K -2				17E-07003								GLP-PX 5K -3				17E-10001								GLP-PX 5K -4				17E-10011								GLP-PX 5K -5				17E-11003				GLP-PX 5K 1:3 pH 6.8												GLP-PX 5K FaSSIF-1				17E-11007								GLP-PX 5K FaSSIF-2				17E-08001								GLP-PX 5K FaSSIF-3				17E-11005				GLP-PX 5K 1:3 FaSSIF

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/min)		IDR (ug/min/cm2)

		GLP-PX 5K -1		17E-07001		1.087		16.332		0.24		3.84		28.30		32.1009		458.5842

		GLP-PX 5K -2		17E-07003		1.270		18.7		0.24		4.40		28.88		37.7044		538.6345				Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile																				Dissolution Profile												Dissolution Profile												Dissolution Profile

		GLP-PX 5K -3		17E-10001		1.395		18.96		0.24		4.46		31.30		82.1607		1173.7249																																																																AVERAGE				TIME		SD																																						AVERAGE		TIME		SD

		GLP-PX 5K -4		17E-10011		1.711		22.55		0.24		5.30		32.27		88.0776		1258.2518				Time (minutes)		Weight (mg)				Weight (µg)		Time zero (min)		%		Time (minutes)		Weight (mg)				Weight (µg)		Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)		Weight (µg)		Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)		Weight (µg)		Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)		Weight (µg)		Time zero (min)		%		mg		Weight (µg)						Time (minutes)		Weight (mg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)				Time zero (min)		%		mg

		GLP-PX 5K -5		17E-11003		1.776		18.06		0.24		4.25		41.82		85.7074		1224.3911				5.36848		0.215056				215.056		0		5.6009225		5.03802		0.23043				230.43		0		5.2413695845		5.6875		0.238882		0.288137		238.882		0		5.3591074451		5.08463		0.437709		0.556339		437.709		0		8.2563158952		5.3289		0.382445		0.403206		382.445		0		9.0073826411		0.353012		353.012		0		102.6292848021		1.85598		0.0226697		0.0220574				0		0.6302338318		2.22552		0.054711		0.0141487				0		1.526993037		2.1086		0.0626375		0.0824294				0		1.2138003602		0.0466727333		0		0.0211616766

		AVG				1.6273								35.131		85.315		1218.789				5.88568		0.242984				242.984		0.5172		6.3282798561		5.55338		0.245985				245.985		0.51536		5.5951842088		6.20652		0.286365		0.330368		286.365		0.51902		6.4243467633		5.60078		0.51789		0.592555		517.89		0.51615		9.7687354817		5.8474		0.445603		0.454707		445.603		0.5185		10.4948861327		0.4166193333		416.6193333333		0.51789		118.4525056988		2.37422		0.0865593		0.0870081				0.51824		2.4064102885		2.74167		0.114381		0.115511				0.51615		3.1923925821		2.62552		0.176168		0.168078				0.51692		3.4138141187		0.1257027667		0.5171033333		0.045864655

		SD				0.2037								5.817		3.0		42.541				6.40182		0.262949				262.949		1.03334		6.8482486908		6.0711		0.263946				263.946		1.03308		6.0037258011		6.72213		0.34069		0.370836		340.69		1.03463		7.6430803303		6.11745		0.585333		0.627865		585.333		1.03282		11.0408836736		6.36485		0.500503		0.504062		500.503		1.03595		11.7878963877		0.4755086667		475.5086666667		1.0344666667		124.2219259484		2.89167		0.150355		0.151573				1.03569		4.1799762582		3.2599		0.189022		0.212958				1.03438		5.2756352074		3.14088		0.268177		0.251763				1.03228		5.1967805102		0.202518		1.0341166667		0.060059241

		RSD				12.516								16.558		3.490		3.490				6.92005		0.276321				276.321		1.55157		7.1965093097		6.5888		0.284788				284.788		1.55078		6.4777987294		7.24088		0.396809		0.410108		396.809		1.55338		8.9020607085		6.63542		0.645954		0.662342		645.954		1.55079		12.1843514247		6.88255		0.551452		0.551482		551.452		1.55365		12.9878522982		0.531405		531.405		1.5526066667		125.7764660539		3.40677		0.215086		0.215561				1.55079		5.9795442351		3.77708		0.27698		0.30607				1.55156		7.7305575		3.65652		0.343501		0.33382				1.54792		6.6564220721		0.2785223333		1.55009		0.0642213917

		GLP-PX 5K FaSSIF-1		17E-11007		2.003		15.3		0.24		3.60		55.68		125.17		1788.15				7.43907		0.292494				292.494		2.07059		7.6177192253		7.10495		0.302561				302.561		2.06693		6.8820640665		7.7599		0.444473		0.448003		444.473		2.0724		9.9713606025		7.15235		0.705717		0.695854		705.717		2.06772		13.3116350923		7.39897		0.596396		0.596909		596.396		2.07007		14.046377852		0.5821953333		582.1953333333		2.0700633333		131.1996611441		3.92473		0.281694		0.279621				2.06875		7.831294151		4.29402		0.374138		0.395183				2.0685		10.4422533104		4.17448		0.42023		0.414598				2.06588		8.1432899682		0.3586873333		2.06771		0.0705485517

		GLP-PX 5K FaSSIF-2		17E-08001		1.987		15.24		0.24		3.58		55.45		163.02		2328.90				7.95807		0.304775				304.775		2.58959		7.9375658197		7.62032		0.325048				325.048		2.5823		7.3935542277		8.27657		0.488468		0.484388		488.468		2.58907		10.9583497102		7.66902		0.76017		0.728477		760.17		2.58439		14.3387585223		7.91772		0.637813		0.640732		637.813		2.58882		15.0218351513		0.628817		628.817		2.5874266667		136.0742084783		4.44167		0.344708		0.343269				2.58569		9.5831283031		4.8099		0.461263		0.480341				2.58438		12.8739264355		4.69245		0.491103		0.493756				2.58385		9.5166792786		0.432358		2.58464		0.077359539

		GLP-PX 5K FaSSIF-3		17E-11005		2.609		21.95		0.24		5.16		50.56		152.19		2174.19				8.4724		0.321342				321.342		3.10392		8.3690370787		8.13855		0.347078				347.078		3.10053		7.8946494494		8.79272		0.530706		0.519452		530.706		3.10522		11.9059220693		8.18647		0.803423		0.7603		803.423		3.10184		15.1546211878		8.43282		0.674116		0.682521		674.116		3.10392		15.8768470145		0.669415		669.415		3.10366		136.419262104		4.95833		0.405142		0.406604				3.10235		11.2632366147		5.3263		0.566044		0.561969				3.10078		15.7983814337		5.2099		0.563342		0.571249				3.1013		10.9165391744		0.5115093333		3.1014766667		0.0921267193

		AVG		amount at		2.200								53.899		146.795		2097.078				8.98958		0.342228				342.228		3.6211		8.9129924546		8.65417		0.361386				361.386		3.61615		8.2200997641		9.30807		0.569861		0.553224		569.861		3.62057		12.7843300364		8.70287		0.842374		0.791232		842.374		3.61824		15.8893370845		8.94792		0.712184		0.722661		712.184		3.61902		16.7734283331		0.7081396667		708.1396666667		3.6192766667		136.3015086723		5.47527		0.467933		0.469691				3.61929		13.0088712076		5.8448		0.646751		0.640444				3.61928		18.0509271199		5.72552		0.630132		0.646923				3.61692		12.2108074013		0.5816053333		3.6184966667		0.0987932048

		SD		15 min		0.355								2.895		19.495		278.500				9.50495		0.359245				359.245		4.13647		9.356183522		9.1724		0.381022				381.022		4.13438		8.6667409704		9.825		0.603793		0.585902		603.793		4.1375		13.545564595		9.21953		0.872634		0.821375		872.634		4.1349		16.4601184003		9.46432		0.756507		0.76131		756.507		4.13542		17.8173280332		0.7443113333		744.3113333333		4.13594		134.8347934857		5.99323		0.53386		0.532623				4.13725		14.8416888377		6.36068		0.734194		0.715205				4.13516		20.4914756774		6.24348		0.715415		0.72142				4.13488		13.8634361959		0.6611563333		4.1357633333		0.1106409963

		RSD				16.123								5.372		13.280		13.280				10.0203		0.376738				376.738		4.65182		9.8117715423		9.68855		0.403982				403.982		4.65053		9.1889900077		10.3435		0.639983		0.617515		639.983		4.656		14.3574553965		9.73802		0.901771		0.850836		901.771		4.65339		17.009717052		9.98203		0.804111		0.798523		804.111		4.65313		18.9385021713		0.781955		781.955		4.6541733333		132.2928776919		6.50833		0.598691		0.594931				4.65235		16.644036886		6.87838		0.817506		0.787044				4.65286		22.8167273434		6.76172		0.793671		0.794461				4.65312		15.3798945634		0.7366226667		4.6527766667		0.1200453469

																						10.5362		0.388683				388.683		5.16772		10.1228673465		10.2063		0.424374				424.374		5.16828		9.6528272188		10.8612		0.671697		0.647962		671.697		5.1737		15.068931077		10.2534		0.924596		0.879358		924.596		5.16877		17.4402551728		10.499		0.84522		0.834205		845.22		5.1701		19.906705424		0.8138376667		813.8376666667		5.1708566667		129.3372111356		7.02682		0.670015		0.657371				5.17084		18.6268949661		7.39557		0.876975		0.855759				5.17005		24.4765169454		7.27657		0.879691		0.865573				5.16797		17.046805072		0.8088936667		5.16962		0.1202801197

		17E-11007 appears in raw data for 5k 1:2																				11.0505		0.40192				401.92		5.68202		10.4676120229		10.7229		0.440237				440.237		5.68488		10.0136476229		11.3797		0.705983		0.677372		705.983		5.6922		15.8381073141		10.7706		0.943198		0.907237		943.198		5.68597		17.7911366678		11.0146		0.885733		0.868388		885.733		5.6857		20.8608716255		0.8449713333		844.9713333333		5.6879566667		123.7492390212		7.5448		0.741406		0.719474				5.68882		20.6116156941		7.91223		0.930391		0.92149				5.68671		25.9673663187		7.79453		0.965482		0.935684				5.68593		18.7092779789		0.879093		5.6871533333		0.1205243836

																						11.5664		0.411444				411.444		6.19792		10.7156552576		11.2388		0.475423				475.423		6.20078		10.8139897233		11.8974		0.72949		0.705696		729.49		6.2099		16.365466172		11.2885		0.970388		0.934432		970.388		6.20387		18.3040098991		11.5328		0.922992		0.901383		922.992		6.2039		21.7383992957		0.87429		874.29		6.20589		127.6200423288		8.06223		0.81562		0.781236				6.20625		22.6748178358		8.42838		0.983511		0.984368				6.20286		27.4499542831		8.31223		1.05047		1.00435				6.20363		20.3561902123		0.949867		6.2042466667		0.1209858243

																						12.082		0.422054				422.054		6.71352		10.9919822967		11.7565		0.499548				499.548		6.71848		11.3627378951		12.4159		0.762051		0.733055		762.051		6.7284		17.0959435522		11.805		0.990467		0.960837		990.467		6.72037		18.6827514074		12.0505		0.956435		0.933036		956.435		6.7216		22.5260521547		0.9029843333		902.9843333333		6.7234566667		123.2322911794		8.57968		0.892516		0.842727				6.7237		24.8125814908		8.94427		1.03345		1.04455				6.71875		28.8437600128		8.82943		1.14858		1.07158				6.72083		22.257382842		1.0248486667		6.7210933333		0.1282485096

																						12.5966		0.431345				431.345		7.22812		11.2339572751		12.2727		0.522097				522.097		7.23468		11.8756383107		12.9331		0.787856		0.759377		787.856		7.2456		17.6748560178		12.3201		1.01484		0.986493		1014.84		7.23547		19.1424887838		12.5656		0.991257		0.963284		991.257		7.2367		23.3461833587		0.9313176667		931.3176666667		7.2392566667		124.7997468921		9.09818		0.967789		0.904069				7.2422		26.9052245881		9.4638		1.0783		1.10258				7.23828		30.0955309127		9.3474		1.24299		1.13756				7.2388		24.0868762287		1.0963596667		7.23976		0.1384865021

																						13.1109		0.438624				438.624		7.74242		11.4235316877		12.7898		0.541138				541.138		7.75178		12.3087456242		13.4508		0.813023		0.784793		813.023		7.7633		18.2394555149		12.8386		1.03352		1.01165		1033.52		7.75397		19.4948415591		13.0813		1.02086		0.992365		1020.86		7.7524		24.0433961562		0.955801		955.801		7.7565566667		123.8112953773		9.6151		1.04266		0.964953				7.75912		28.9866917985		9.98098		1.13815		1.15788				7.75546		31.7659542876		9.86432		1.34991		1.20209				7.75572		26.1587905694		1.1769066667		7.7567666667		0.1572488475

																						13.6266		0.447221				447.221		8.25812		11.647432117		13.3073		0.56201				562.01		8.26928		12.7835009337		13.9669		0.839474		0.809235		839.474		8.2794		18.8328604221		13.3565		1.05307		1.03612		1053.07		8.27187		19.8636047688		13.5982		1.03771		1.02037		1037.71		8.2693		24.4402490305		0.9767513333		976.7513333333		8.2735233333		119.1334633314		10.1315		1.11409		1.02551				8.27552		30.9724967543		10.4982		1.19864		1.21084				8.27268		33.4542401681		10.3823		1.45694		1.26545				8.2737		28.2328365093		1.2565566667		8.2739666667		0.17861211

																						14.1412		0.452781				452.781		8.77272		11.7922368614		13.8247		0.587089				587.089		8.78668		13.353948826		14.4828		0.859126		0.8328		859.126		8.7953		19.2737357476		13.8734		1.07916		1.0599		1079.16		8.78877		20.355729175		14.112		1.06199		1.0471		1061.99		8.7831		25.012094003		1.000092		1000.092		8.7890566667		122.3816248135		10.6511		1.16582		1.08616				8.79512		32.4106276567		11.0172		1.23592		1.26172				8.79168		34.4947311191		10.8987		1.55292		1.32736				8.7901		30.0927536288		1.31822		8.7923		0.2062560787

																						14.6563		0.459309				459.309		9.28782		11.9622522159		14.3409		0.606953				606.953		9.30288		13.8057761289		15.0003		0.880385		0.855601		880.385		9.3128		19.7506627039		14.3891		1.09508		1.08301		1095.08		9.30447		20.6560212619		14.6276		1.09091		1.07287		1090.91		9.2987		25.6932207166		1.022125		1022.125		9.3053233333		122.7681470293		11.169		1.23359		1.14636				9.31302		34.2946820015		11.5338		1.29102		1.31022				9.30828		36.0325812102		11.4164		1.67576		1.38817				9.3078		32.4731684961		1.4001233333		9.3097		0.2404292624

																						15.1727		0.469573				469.573		9.80422		12.2295680245		14.8568		0.624371				624.371		9.81878		14.2019666225		15.5177		0.902926		0.877593		902.926		9.8302		20.256350202		14.9075		1.11434		1.10565		1114.34		9.82287		21.0193143268		15.1456		1.10989		1.09773		1109.89		9.8167		26.1402395625		1.0423853333		1042.3853333333		9.8232566667		120.7958189067		11.687		1.31566		1.20629				9.83102		36.5762865475		12.0497		1.32653		1.35658				9.82418		37.0236711691		11.9328		1.81089		1.44762				9.8242		35.0917411192		1.48436		9.8264666667		0.2828354997

																						15.6872		0.47828				478.28		10.31872		12.4563332959		15.3732		0.637495				637.495		10.33518		14.5004856279		16.0349		0.922215		0.898795		922.215		10.3474		20.689081942		15.4227		1.13784		1.12755		1137.84		10.33807		21.4625846811		15.6607		1.13302		1.12147		1133.02		10.3318		26.6849996208		1.0643583333		1064.3583333333		10.33909		123.1233264184		12.2044		1.40085		1.2659				10.34842		38.9446293192		12.5651		1.3864		1.40094				10.33958		38.6946527473		12.4484		1.89906		1.5058				10.3398		36.8003147015		1.5621033333		10.3426		0.2919024615

																						16.2037		0.483857				483.857		10.83522		12.6015807886		15.8865		0.672229				672.229		10.84848		15.2905465191		16.5516		0.938236		0.919226		938.236		10.8641		21.0484989779		15.938		1.14896		1.14889		1148.96		10.85337		21.6723364403		16.1781		1.14805		1.14438		1148.05		10.8492		27.0389876742		1.0784153333		1078.4153333333		10.8555566667		121.3997164137		12.7219		1.46679		1.32525				10.86592		40.7778083586		13.0797		1.4258		1.44336				10.85418		39.7943132481		12.9646		2.14697		1.56287				10.856		41.6043577637		1.6798533333		10.8587		0.4050537375

																						16.7185		0.50485				504.85		11.35002		13.1483228746		16.4023		0.690456				690.456		11.36428		15.7051385575		17.0682		0.949924		0.938931		949.924		11.3807		21.310708972		16.4539		1.16756		1.1697		1167.56		11.36927		22.0231802101		16.6943		1.16532		1.16632		1165.32		11.3654		27.4457324303		1.094268		1094.268		11.37179		125.0105881596		13.2396		1.53192		1.38435				11.38362		42.5884688201		13.5961		1.44047		1.48412				11.37058		40.2037553685		13.4818		2.2346		1.61891				11.3732		43.3024671322		1.7356633333		11.3758		0.4345044576

																						17.2342		0.524038				524.038		11.86572		13.6480555067		16.9182		0.709285				709.285		11.88018		16.1334237109		17.5837		0.962251		0.957899		962.251		11.8962		21.5872543688		16.9742		1.18243		1.19014		1182.43		11.88957		22.3036666003		17.2117		1.17896		1.18745		1178.96		11.8828		27.7669830656		1.1078803333		1107.8803333333		11.8895233333		126.1306357327		13.7573		1.60152		1.4432				11.90132		44.5233984704		14.1143		1.47429		1.52329				11.88878		41.1476771486		13.9977		2.353		1.67369				11.8891		45.5968429079		1.8096033333		11.8930666667		0.474875585

																						17.7515		0.537497				537.497		12.38302		13.9985819553		17.4347		0.730241				730.241		12.39668		16.6100896876		18.0995		0.977904		0.976209		977.904		12.412		21.9384156486		17.4898		1.20795		1.20988		1207.95		12.40517		22.7850393426		17.7273		1.20348		1.20767		1203.48		12.3984		28.344480542		1.129778		1129.778		12.40519		131.545730193		14.2729		1.67525		1.50156				12.41692		46.5731450669		14.6349		1.56799		1.56096				12.40938		43.7628596085		14.5146		2.46184		1.72748				12.406		47.7059633423		1.9016933333		12.4107666667		0.4880567519

																						18.2677		0.549672				549.672		12.89922		14.3156678838		17.9497		0.749766				749.766		12.91168		17.0542060837		18.6153		0.994434		0.993872		994.434		12.9278		22.3092516516		18.0038		1.22521		1.22903		1225.21		12.91917		23.110607271		18.242		1.21687		1.22706		1216.87		12.9131		28.6598431524		1.1455046667		1145.5046666667		12.9200233333		130.8974737928		14.7909		1.74335		1.55991				12.93492		48.4663736471		15.1534		1.58926		1.59687				12.92788		44.3565088179		15.0313		2.42817		1.78018				12.9227		47.0535002311		1.92026		12.9285		0.4465594676
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																						31.1823		1.04183				1041.83		25.81382		27.1334400721		30.8412		1.19023				1190.23		25.80318		27.0730170573		31.5232		1.28632		1.28006		1286.32		25.8357		28.8574571912		30.8948		1.56709		1.57657		1567.09		25.81017		29.5593421113		31.1352		1.59653		1.52684		1596.53		25.8063		37.6016331968		1.4833133333		1483.3133333333		25.81739		171.2350969671		27.6917		2.86741		2.93283				25.83572		79.7160435137		28.0677		2.60773		2.13109				25.84218		72.7821745591		27.9245		2.92246		2.80242				25.8159		56.6319377496		2.7992		25.8312666667		0.1680868713

																						31.6987		1.04962				1049.62		26.33022		27.3363229783		31.356		1.19598				1195.98		26.31798		27.203806777		32.0383		1.29447		1.28698		1294.47		26.3508		29.0402952689		31.4087		1.57594		1.58624		1575.94		26.32407		29.7262758405		31.6513		1.61877		1.53365		1618.77		26.3224		38.1254318866		1.4963933333		1496.3933333333		26.3324233333		176.1771172239		28.2073		2.89353		2.98461				26.35132		80.4421981468		28.5837		2.59326		2.14267				26.35818		72.3783144716		28.4397		2.95273		2.83352				26.3311		57.2185150699		2.8131733333		26.3468666667		0.1927370375

																						32.2153		1.05427				1054.27		26.84682		27.4574276656		31.8713		1.2044				1204.4		26.83328		27.3953284187		32.5557		1.30229		1.29368		1302.29		26.8682		29.215730087		31.9232		1.62145		1.59567		1621.45		26.83857		30.5847113225		32.1688		1.62077		1.54021		1620.77		26.8399		38.1725360853		1.5148366667		1514.8366666667		26.84889		184.0711268324		28.7223		2.86852		3.0361				26.86632		79.7469023055		29.099		2.57172		2.15373				26.87348		71.7771295177		28.9547		2.91929		2.86398				26.8461		56.5705089387		2.78651		26.8619666667		0.1877377328

																						32.7305		1.0607				1060.7		27.36202		27.6248907063		32.3872		1.21446				1214.46		27.34918		27.6241535631		33.0713		1.31602		1.30012		1316.02		27.3838		29.5237505541		32.4388		1.62559		1.60487		1625.59		27.35417		30.6628023552		32.682		1.66533		1.54646		1665.33		27.3531		39.222017633		1.5356466667		1535.6466666667		27.36369		191.2373431977		29.238		2.82912		3.08743				27.38202		78.6515541989		29.6157		2.57976		2.16436				27.39018		72.0015272442		29.4708		2.95842		2.8939				27.3622		57.3287768787		2.7891		27.3781333333		0.1924761003

																						33.2468		1.06664				1066.64		27.87832		27.7795921778		32.9027		1.21723				1217.23		27.86468		27.6871600889		33.586		1.32063		1.30632		1320.63		27.8985		29.6271718472		32.9552		1.65572		1.61385		1655.72		27.87057		31.2311315372		33.1973		1.66672		1.55248		1666.72		27.8684		39.2547550511		1.54769		1547.69		27.8791566667		196.7166304612		29.7542		2.92993		3.13858				27.89822		81.4541441133		30.1307		2.6088		2.1745				27.90518		72.8120384356		29.9855		2.98332		2.92314				27.8769		57.8112934059		2.8406833333		27.8934333333		0.2025833982

																						33.7635		1.07118				1071.18		28.39502		27.897832023		33.4175		1.22359				1223.59		28.37948		27.8318248919		34.1015		1.33555		1.31232		1335.55		28.414		29.961888917		33.4685		1.65634		1.62255		1656.34		28.38387		31.2428263295		33.7133		1.6814		1.55828		1681.4		28.3844		39.6004998698		1.5577633333		1557.7633333333		28.39409		192.8498769337		30.2705		2.94798		3.18952				28.41452		81.9559469896		30.65		2.61988		2.18429				28.42448		73.1212830638		30.5022		2.95488		2.9519				28.3936		57.2601781436		2.8409133333		28.4108666667		0.1914515692

																						34.2792		1.07582				1075.82		28.91072		28.01867627		33.9323		1.22994				1229.94		28.89428		27.9762622345		34.619		1.36469		1.31812		1364.69		28.9315		30.6156191727		33.9847		1.65567		1.63106		1655.67		28.90007		31.2301884088		34.2278		1.70501		1.56383		1705.01		28.8989		40.1565649357		1.5751233333		1575.1233333333		28.9101566667		183.902826877		30.7838		2.90949		3.23994				28.92782		80.8858975321		31.1658		2.64285		2.1936				28.94028		73.7623795537		31.0167		2.98538		2.97998				28.9081		57.8512124439		2.8459066667		28.9254		0.1798995009

																						34.7962		1.08177				1081.77		29.42772		28.1736381817		34.45		1.26366				1263.66		29.41198		28.7432586429		35.1367		1.38142		1.32372		1381.42		29.4492		30.9909419997		34.5008		1.68419		1.63936		1684.19		29.41617		31.7681488558		34.7438		1.73056		1.56918		1730.56		29.4149		40.7583210745		1.5987233333		1598.7233333333		29.4267566667		189.61302232		31.2997		2.96882		3.29038				29.44372		82.5353138562		31.681		2.64994		2.20251				29.45548		73.9602626235		31.5323		3.00751		3.00755				29.4237		58.2800514297		2.8754233333		29.4409666667		0.196230169

																						35.3098		1.0865				1086.5		29.94132		28.2968263905		34.9643		1.26954				1269.54		29.92628		28.8770053476		35.6518		1.39508		1.3291		1395.08		29.9643		31.2973920784		35.0153		1.71086		1.64741		1710.86		29.93067		32.2712135516		35.2588		1.77581		1.5743		1775.81		29.9299		41.8240535707		1.62725		1627.25		29.9416233333		203.6708307539		31.8147		2.95169		3.34052				29.95872		82.0590876362		32.1963		2.60738		2.21104				29.97078		72.7724060014		32.0473		3.02114		3.03455				29.9387		58.5441759383		2.86007		29.9560666667		0.2215739215





GLP-PVP 12 FULL  (2)

		



GLP-PX 5K 1:3 FaSSIF

GLP-PX 5K 1:3 pH 6.8

Time (min)

Dissolved (mg)



GLP-PVP 12 FULL  (3)

				0		0		0		0		0.0211616766		0.0211616766		0.0002295269		0.0002295269		0.0049197235		0.0049197235		0.0009759608		0.0009759608						0.0024600585		0.0024600585

				0.51758		0.51649		0.51728		0.3559833333		0.045864655		0.045864655		0.0005164001		0.0005164001		0.0003363401		0.0003363401		0.0038877915		0.0038877915						0.00042699		0.00042699

				1.033595		1.0315933333		1.0325566667		0.8727433333		0.060059241		0.060059241		0.0012761156		0.0012761156		0.0012800802		0.0012800802		0.0036086847		0.0036086847						0.00001985		0.00001985

				1.549085		1.5464433333		1.55018		1.38758		0.0642213917		0.0642213917		0.0026588629		0.0026588629		0.0030641224		0.0030641224		0.0067311197		0.0067311197						0.000577395		0.000577395

				2.065235		2.0621466667		2.06615		1.9035566667		0.0705485517		0.0705485517		0.0021047033		0.0021047033		0.0041417169		0.0041417169		0.0064862455		0.0064862455						0.00149305		0.00149305

				2.580855		2.5771733333		2.5814333333		2.4186533333		0.077359539		0.077359539		0.0015325125		0.0015325125		0.0038124597		0.0038124597		0.0076895859		0.0076895859						0.00250724		0.00250724

				3.09649		3.0914033333		3.09714		2.9348033333		0.0921267193		0.0921267193		0.0028948245		0.0028948245		0.0051955973		0.0051955973		0.0082620883		0.0082620883						0.0030001		0.0030001

				3.611855		3.6058133333		3.6127666667		3.4502533333		0.0987932048		0.0987932048		0.0024435489		0.0024435489		0.0063641511		0.0063641511		0.0106337704		0.0106337704						0.00304005		0.00304005

				4.126695		4.1216133333		4.1276133333		3.9650166667		0.1106409963		0.1106409963		0.0008094251		0.0008094251		0.0060162201		0.0060162201		0.0108945747		0.0108945747						0.0024658		0.0024658

				4.64232		4.63637		4.6438466667		4.4806266667		0.1200453469		0.1200453469		0.0017855153		0.0017855153		0.0052292211		0.0052292211		0.0123526021		0.0123526021						0.0033365		0.0033365

				5.157285		5.1518266667		5.15808		4.9960866667		0.1202801197		0.1202801197		0.0010125062		0.0010125062		0.0054794519		0.0054794519		0.0148708277		0.0148708277						0.00400855		0.00400855

				5.67344		5.6666666667		5.67318		5.51154		0.1205243836		0.1205243836		0.0002182839		0.0002182839		0.0054817238		0.0054817238		0.0169467855		0.0169467855						0.0039763		0.0039763

				6.18971		6.1817633333		6.1899333333		6.0276		0.1209858243		0.1209858243		0.0016947935		0.0016947935		0.0052141255		0.0052141255		0.0176260764		0.0176260764						0.00373265		0.00373265

				6.70586		6.6972266667		6.7053		6.5419166667		0.1282485096		0.1282485096		0.0012914598		0.0012914598		0.0047796323		0.0047796323		0.0200322412		0.0200322412						0.0035881		0.0035881

				7.22162		7.2123266667		7.2217066667		7.0577166667		0.1384865021		0.1384865021		0.0006629126		0.0006629126		0.0045389309		0.0045389309		0.0193749852		0.0193749852						0.00485905		0.00485905

				7.73646		7.7273466667		7.7368966667		7.57213		0.1572488475		0.1572488475		0.000103874		0.000103874		0.0054211854		0.0054211854		0.0207444635		0.0207444635						0.00411355		0.00411355

				8.25237		8.2429933333		8.2522066667		8.08749		0.17861211		0.17861211		0.0003114805		0.0003114805		0.0050889491		0.0050889491		0.0193853513		0.0193853513						0.0037421		0.0037421

				8.76797		8.75896		8.7692066667		8.6033966667		0.2062560787		0.2062560787		0.0013605442		0.0013605442		0.0058034249		0.0058034249		0.0221904516		0.0221904516						0.007910545		0.007910545

				9.28347		9.27406		9.2844066667		9.1178633333		0.2404292624		0.2404292624		0.0003397648		0.0003397648		0.0056595706		0.0056595706		0.0209626155		0.0209626155						0.0053162409		0.0053162409

				9.79937		9.7904266667		9.7988066667		9.63413		0.2828354997		0.2828354997		0.0013320478		0.0013320478		0.0055589063		0.0055589063		0.0200364887		0.0200364887						0.0060193879		0.0060193879

				10.31462		10.30606		10.3148733333		10.1481633333		0.2919024615		0.2919024615		0.0015060667		0.0015060667		0.0049010295		0.0049010295		0.0222681141		0.0222681141						0.0074061657		0.0074061657

				10.83017		10.8205933333		10.8311733333		10.6633633333		0.4050537375		0.4050537375		0.0007927374		0.0007927374		0.0058877127		0.0058877127		0.0214915775		0.0214915775						0.0058441668		0.0058441668

				11.34582		11.3362266667		11.34594		11.18013		0.4345044576		0.4345044576		0.0011666555		0.0011666555		0.0062454339		0.0062454339		0.0225296928		0.0225296928						0.0067849724		0.0067849724

				11.86227		11.8511266667		11.8620733333		11.6948966667		0.474875585		0.474875585		0.0006107988		0.0006107988		0.006201845		0.006201845		0.0209992372		0.0209992372						0.0057949522		0.0057949522

				12.37667		12.3670266667		12.3766733333		12.21123		0.4880567519		0.4880567519		0.0009087029		0.0009087029		0.0064490838		0.0064490838		0.0201919182		0.0201919182						0.0059941442		0.0059941442

				12.89312		12.8821266667		12.8936733333		12.72593		0.4465594676		0.4465594676		0.0009094807		0.0009094807		0.005471504		0.005471504		0.021737247		0.021737247						0.0050638745		0.0050638745

				13.40837		13.3975933333		13.41034		13.2410966667		0.4505672259		0.4505672259		0.000620769		0.000620769		0.0070581086		0.0070581086		0.0211475267		0.0211475267						0.006532606		0.006532606

				13.92332		13.9123266667		13.92594		13.7572633333		0.405039827		0.405039827		0.0021169363		0.0021169363		0.0076952059		0.0076952059		0.0211375547		0.0211375547						0.0073238585		0.0073238585

				14.43987		14.42856		14.4421066667		14.2713966667		0.381103703		0.381103703		0.0019201485		0.0019201485		0.0070387866		0.0070387866		0.0226654224		0.0226654224						0.0080757958		0.0080757958

				14.95687		14.9446266667		14.9566733333		14.7851966667		0.3546391758		0.3546391758		0.00211432		0.00211432		0.008045405		0.008045405		0.0238120538		0.0238120538						0.007131384		0.007131384

				15.47232		15.45986		15.4717733333		15.29943		0.3016183304		0.3016183304		0.0033646969		0.0033646969		0.0085574798		0.0085574798		0.0233072483		0.0233072483						0.0068616228		0.0068616228

				15.98892		15.9752266667		15.98774		15.8141633333		0.2896236774		0.2896236774		0.0023324624		0.0023324624		0.0090811846		0.0090811846		0.0233708209		0.0233708209						0.0074158531		0.0074158531

				16.50487		16.4901933333		16.5035733333		16.3287633333		0.2654782736		0.2654782736		0.003362717		0.003362717		0.0089288396		0.0089288396		0.0239727408		0.0239727408						0.0059507985		0.0059507985

				17.02017		17.00606		17.0192066667		16.8429633333		0.1953278035		0.1953278035		0.0026384275		0.0026384275		0.0092761783		0.0092761783		0.0226477785		0.0226477785						0.005846571		0.005846571

				17.53677		17.5203933333		17.5367066667		17.35723		0.1946432985		0.1946432985		0.0013798482		0.0013798482		0.0075811938		0.0075811938		0.0227726661		0.0227726661						0.0070677444		0.0070677444

				18.05327		18.0362933333		18.0536733333		17.8729633333		0.1389387787		0.1389387787		0.0046205186		0.0046205186		0.0076470407		0.0076470407		0.0219933991		0.0219933991						0.0057643345		0.0057643345

				18.56912		18.5518933333		18.5691733333		18.3884966667		0.1704818196		0.1704818196		0.0025348364		0.0025348364		0.0087758993		0.0087758993		0.021586671		0.021586671						0.0066449653		0.0066449653

				19.08562		19.0682933333		19.0856733333		18.90373		0.1870636622		0.1870636622		0.0024441146		0.0024441146		0.0078834505		0.0078834505		0.0196614904		0.0196614904						0.0065570012		0.0065570012

				19.60217		19.5837933333		19.60194		19.41913		0.1701638143		0.1701638143		0.0033461707		0.0033461707		0.0072800503		0.0072800503		0.0209664053		0.0209664053						0.0068897656		0.0068897656

				20.11837		20.09816		20.1176066667		19.9347633333		0.1989274869		0.1989274869		0.0044503179		0.0044503179		0.0077420496		0.0077420496		0.0234362237		0.0234362237						0.0061708502		0.0061708502

				20.63497		20.6141266667		20.63404		20.4496966667		0.1690912335		0.1690912335		0.0039354028		0.0039354028		0.0080806325		0.0080806325		0.0188909807		0.0188909807						0.0049427471		0.0049427471

				21.15037		21.1283266667		21.1496733333		20.9642966667		0.163619917		0.163619917		0.0039817183		0.0039817183		0.0078649914		0.0078649914		0.0188242785		0.0188242785						0.0048045077		0.0048045077

				21.66602		21.64436		21.6660733333		21.48053		0.2212762102		0.2212762102		0.0026940768		0.0026940768		0.0071936868		0.0071936868		0.017604233		0.017604233						0.0059739916		0.0059739916

				22.18272		22.1591933333		22.18194		21.99573		0.1762282569		0.1762282569		0.0041075833		0.0041075833		0.0091893713		0.0091893713		0.0183144808		0.0183144808						0.0064748354		0.0064748354

				22.69882		22.6745266667		22.69924		22.5104633333		0.1936966536		0.1936966536		0.0049327769		0.0049327769		0.0093057648		0.0093057648		0.0225389041		0.0225389041						0.0059310703		0.0059310703

				23.21632		23.1905266667		23.21644		23.02743		0.1854307691		0.1854307691		0.004198093		0.004198093		0.0100802954		0.0100802954		0.0211257133		0.0211257133						0.0073549712		0.0073549712

				23.73267		23.70616		23.7321733333		23.5422966667		0.1834939951		0.1834939951		0.0050565206		0.0050565206		0.0100583048		0.0100583048		0.0224938156		0.0224938156						0.0059690419		0.0059690419

				24.24812		24.2211266667		24.2490733333		24.05833		0.1729283847		0.1729283847		0.0042016285		0.0042016285		0.0100733955		0.0100733955		0.0214822448		0.0214822448						0.0058807243		0.0058807243

				24.76382		24.7365266667		24.7640733333		24.57373		0.1806177235		0.1806177235		0.0054129024		0.0054129024		0.0097795343		0.0097795343		0.0218380328		0.0218380328						0.0058787444		0.0058787444

				25.27987		25.2510266667		25.2800733333		25.0883633333		0.1767766319		0.1767766319		0.0076112974		0.0076112974		0.0111176801		0.0111176801		0.0247668225		0.0247668225						0.005994922		0.005994922

				25.79662		25.7670266667		25.7957066667		25.6047966667		0.1680868713		0.1680868713		0.0046612479		0.0046612479		0.0116422963		0.0116422963		0.0259484349		0.0259484349						0.0057551421		0.0057551421

				26.31327		26.2821266667		26.3108066667		26.1203966667		0.1927370375		0.1927370375		0.0053761329		0.0053761329		0.0111321647		0.0111321647		0.024718202		0.024718202						0.0050165691		0.0050165691

				26.82947		26.7979266667		26.82564		26.6357966667		0.1877377328		0.1877377328		0.0047340799		0.0047340799		0.0109888505		0.0109888505		0.0256954727		0.0256954727						0.005980992		0.005980992

				27.34462		27.3132933333		27.3410066667		27.15053		0.1924761003		0.1924761003		0.0049822744		0.0049822744		0.0119221169		0.0119221169		0.0237611726		0.0237611726						0.0049947902		0.0049947902

				27.85987		27.82806		27.8576733333		27.6653633333		0.2025833982		0.2025833982		0.0050932901		0.0050932901		0.012273914		0.012273914		0.0248781787		0.0248781787						0.0029058553		0.0029058553

				28.37667		28.3432266667		28.3750733333		28.1810966667		0.1914515692		0.1914515692		0.0029210581		0.0029210581		0.0117054285		0.0117054285		0.0273618561		0.0273618561						0.0049894162		0.0049894162

				28.89187		28.85866		28.8914066667		28.6969966667		0.1798995009		0.1798995009		0.0048726728		0.0048726728		0.0133019557		0.0133019557		0.0250750388		0.0250750388						0.0051363529		0.0051363529

				29.40707		29.3730266667		29.40654		29.2116633333		0.196230169		0.196230169		0.0052375399		0.0052375399		0.0120344115		0.0120344115		0.0254470122		0.0254470122						0.0048169528		0.0048169528

				29.92162		29.88786		29.9240733333		29.72693		0.2215739215		0.2215739215		0.0051845069		0.0051845069		0.0129536161		0.0129536161		0.0316551949		0.0316551949						0.0026271845		0.0026271845



GLP-PEOX 5k 1:3 FaSSIF

GLP-PEOX 10k 1:3 FaSSIF

GLP-PEOX 25K 1:3 FASSIF

GLP-PEOX 50K 1:3 FASSIF

GLP FaSSIF

Time (min)

Dissolved (mg)

0.0120748

0.0076485567

0.0046769967

0.0022645015

0.01853485

0.0165576

0.0127199733

0.00512764

0.02190235

0.0238062333

0.0179219

0.00564931

0.0290841

0.0288667333

0.0234265

0.008790305

0.02971925

0.0345146667

0.0289509

0.01017685

0.03292265

0.0396076667

0.0342883333

0.01172546

0.03535105

0.0439156667

0.0395861667

0.013727

0.03774285

0.0492505

0.0452195

0.01463455

0.03906155

0.0537103667

0.0503108

0.0177145

0.04103565

0.0589762333

0.0550788333

0.0175237

0.04328655

0.0628546333

0.0621297333

0.01902725

0.04501355

0.0673071667

0.0682978667

0.020174

0.0471832

0.0717489667

0.0748797

0.02045475

0.0489373

0.0755051

0.0809486

0.0210284

0.05061325

0.078669

0.0851484333

0.02322565

0.05321585

0.0821901667

0.0920487333

0.02344085

0.05487295

0.0864736

0.0964482667

0.0241416

0.05774405

0.0909863333

0.1028047

0.0258326

0.05847735

0.0939612667

0.1074405667

0.02801745

0.0615733

0.0981079667

0.1136372667

0.02729285

0.06309625

0.1022691667

0.1204065333

0.02710095

0.06551345

0.1059583333

0.124876

0.02917925

0.06658305

0.1102336667

0.1305863333

0.0298755

0.0685541

0.1132546667

0.135482

0.02994195

0.07025735

0.1168213333

0.1420243333

0.0323698

0.0722861

0.1223056667

0.1488786667

0.030889

0.07454775

0.125932

0.1560926667

0.03273265

0.0765188

0.1310413333

0.1607593333

0.03355855

0.07741855

0.1348703333

0.167477

0.03394365

0.08043185

0.1391163333

0.1705473333

0.03428745

0.0822904

0.1437153333

0.177944

0.0354873

0.0831138

0.147866

0.183536

0.0363781

0.0863342

0.152188

0.190247

0.03885325

0.08791725

0.155201

0.1952123333

0.03737975

0.0905027

0.160088

0.2032416667

0.03839275

0.0923989

0.163258

0.2089296667

0.03832

0.0933247

0.1668206667

0.2150396667

0.0387987

0.09572735

0.1706006667

0.2221046667

0.0408249

0.0977659

0.174068

0.2275673333

0.0417977

0.09917015

0.1767

0.2370063333

0.04308845

0.10152525

0.181157

0.238801

0.04070335

0.1039295

0.18507

0.2438766667

0.0440565

0.105456

0.1880303333

0.248605

0.04392425

0.1075655

0.1921683333

0.2573466667

0.0452727

0.110125

0.1965633333

0.2642336667

0.0459359

0.1114055

0.1996463333

0.2665536667

0.04620915

0.1133805

0.2034866667

0.272085

0.04690505

0.115996

0.2056046667

0.2771586667

0.0479811

0.1193155

0.211155

0.2807626667

0.0484086

0.120096

0.2138586667

0.2879883333

0.04819515

0.121478

0.216614

0.294138

0.0498289

0.1235135

0.2200776667

0.2976706667

0.05022765

0.1250705

0.22269

0.3039896667

0.050712

0.126645

0.2258096667

0.3059643333

0.05103155

0.1279905

0.2295696667

0.311792

0.05295855

0.1317495

0.2315956667

0.317472

0.05291055

0.1327965

0.234528

0.3211663333

0.05339205

0.1339945

0.2375533333

0.3339766667

0.0539374

0.136656

0.2417353333

0.3339996667

0.0540479



GLP-PX 5K 12 FULL  

				0		0		0		0		102.6292848021		102.6292848021		0.006214717		0.006214717						0.0094777765		0.0094777765		0.0122560546		0.0122560546						1.6311850753		1.6311850753

				0.5205733333		0.51771		0.52253		0.51585		118.4525056988		118.4525056988		0.0069731827		0.0069731827						0.009631855		0.009631855		0.0096365901		0.0096365901						1.9388725831		1.9388725831

				1.0417566667		1.035415		1.04337		1.0346		124.2219259484		124.2219259484		0.0067276792		0.0067276792						0.0128318668		0.0128318668		0.0117151567		0.0117151567						2.7230829042		2.7230829042

				1.5625		1.55234		1.56654		1.55918		125.7764660539		125.7764660539		0.0076273108		0.0076273108						0.0141076995		0.0141076995		0.0135090356		0.0135090356						2.7604352996		2.7604352996

				2.0823766667		2.0694		2.091025		2.0365066667		131.1996611441		131.1996611441		0.0083303775		0.0083303775						0.0126681008		0.0126681008		0.018006596		0.018006596						2.9949991024		2.9949991024

				2.60191		2.58424		2.613285		2.5843		136.0742084783		136.0742084783		0.0094100928		0.0094100928						0.0135377715		0.0135377715		0.0181353833		0.0181353833						2.9516867421		2.9516867421

				3.1228333333		3.100135		3.13295		3.09906		136.419262104		136.419262104		0.0093648669		0.0093648669						0.0133005371		0.0133005371		0.0236145607		0.0236145607						3.061631742		3.061631742

				3.64228		3.615495		3.65261		3.6153866667		136.3015086723		136.3015086723		0.0099436403		0.0099436403						0.0137388019		0.0137388019		0.0187662633		0.0187662633						3.5448992595		3.5448992595

				4.1614566667		4.13125		4.173965		4.1335166667		134.8347934857		134.8347934857		0.0105026155		0.0105026155						0.0127328718		0.0127328718		0.0240192646		0.0240192646						2.678652311		2.678652311

				4.68099		4.647265		4.69505		4.6520466667		132.2928776919		132.2928776919		0.0116968317		0.0116968317						0.0151982703		0.0151982703		0.0253216735		0.0253216735						2.7119624795		2.7119624795

				5.2007		5.163265		5.213775		5.1652666667		129.3372111356		129.3372111356		0.0115488953		0.0115488953						0.0131526811		0.0131526811		0.0274269399		0.0274269399						2.7293004214		2.7293004214

				5.7205666667		5.680315		5.733725		5.6852666667		123.7492390212		123.7492390212		0.0114744018		0.0114744018						0.0143476209		0.0143476209		0.0261155695		0.0261155695						3.1441517526		3.1441517526

				6.2402666667		6.197665		6.254575		6.1991666667		127.6200423288		127.6200423288		0.0128854374		0.0128854374						0.0135644294		0.0135644294		0.0269727747		0.0269727747						3.0062302678		3.0062302678

				6.7582333333		6.712765		6.774775		6.7187333333		123.2322911794		123.2322911794		0.0135567818		0.0135567818						0.013488769		0.013488769		0.0344633053		0.0344633053						3.1459060656		3.1459060656

				7.2783		7.227315		7.295075		7.2357		124.7997468921		124.7997468921		0.0135738148		0.0135738148						0.0120752625		0.0120752625		0.0322415192		0.0322415192						3.2437231494		3.2437231494

				7.7978333333		7.742415		7.813775		7.7528666667		123.8112953773		123.8112953773		0.0143526137		0.0143526137						0.0123114362		0.0123114362		0.0282562562		0.0282562562						3.38555703		3.38555703

				8.3164		8.258065		8.334375		8.2708		119.1334633314		119.1334633314		0.0147411171		0.0147411171						0.0135651365		0.0135651365		0.0339800622		0.0339800622						3.4918190851		3.4918190851

				8.8363		8.774215		8.854425		8.7845666667		122.3816248135		122.3816248135		0.015911843		0.015911843						0.0143189123		0.0143189123		0.0338753624		0.0338753624						3.3844434387		3.3844434387

				9.356		9.289965		9.373825		9.3054		122.7681470293		122.7681470293		0.0162562171		0.0162562171						0.0135425091		0.0135425091		0.0316528778		0.0316528778						3.3734507323		3.3734507323

				9.8754666667		9.806265		9.894125		9.8173333333		120.7958189067		120.7958189067		0.0174665167		0.0174665167						0.0127668129		0.0127668129		0.0318905421		0.0318905421						2.7353562772		2.7353562772

				10.3954333333		10.322265		10.414475		10.3354		123.1233264184		123.1233264184		0.0174586152		0.0174586152						0.011774035		0.011774035		0.0374889263		0.0374889263						3.6950501544		3.6950501544

				10.9153666667		10.837765		10.934775		10.8513666667		121.3997164137		121.3997164137		0.0183870775		0.0183870775						0.0138373726		0.0138373726		0.03231125		0.03231125						3.9967502303		3.9967502303

				11.4338666667		11.353865		11.455875		11.3686333333		125.0105881596		125.0105881596		0.0190453648		0.0190453648						0.0097319106		0.0097319106		0.0342557631		0.0342557631						4.1513229329		4.1513229329

				11.9539666667		11.871215		11.975775		11.8836333333		126.1306357327		126.1306357327		0.019978101		0.019978101						0.0101271833		0.0101271833		0.035236723		0.035236723						4.2365735176		4.2365735176

				12.4746333333		12.386765		12.495775		12.3998333333		131.545730193		131.545730193		0.0196625913		0.0196625913						0.0102184001		0.0102184001		0.0392369303		0.0392369303						4.7083096372		4.7083096372

				12.9939666667		12.902515		13.015425		12.9161333333		130.8974737928		130.8974737928		0.0211791579		0.0211791579						0.0072987562		0.0072987562		0.0378132771		0.0378132771						4.4634857078		4.4634857078

				13.5137666667		13.417165		13.536875		13.4336666667		128.7301437116		128.7301437116		0.0218064153		0.0218064153						0.006224661		0.006224661		0.0363060485		0.0363060485						5.0444095416		5.0444095416

				14.0321		13.932115		14.056275		13.9497333333		129.4585597788		129.4585597788		0.0223665486		0.0223665486						0.0052460252		0.0052460252		0.036119662		0.036119662						4.7366589713		4.7366589713

				14.5517666667		14.447415		14.577675		14.4690666667		130.3639854408		130.3639854408		0.0230613045		0.0230613045						0.0017005918		0.0017005918		0.0357712874		0.0357712874						4.6675880649		4.6675880649

				15.0715		14.962215		15.096625		15.0166666667		131.4797267009		131.4797267009		0.0236861986		0.0236861986						0.0020110117		0.0020110117		0.035277804		0.035277804						3.7510199764		3.7510199764

				15.5910333333		15.477965		15.616075		15.4958666667		133.4119538622		133.4119538622		0.0244949543		0.0244949543						0.0011766257		0.0011766257		0.0339061737		0.0339061737						4.4747372351		4.4747372351

				16.1109666667		15.993615		16.134775		16.0171		136.952583887		136.952583887		0.0243021384		0.0243021384						0.0003585031		0.0003585031		0.0337843224		0.0337843224						4.5435949456		4.5435949456

				16.6292666667		16.510465		16.653675		16.535		138.7431736459		138.7431736459		0.0253972671		0.0253972671						0.0000007071		0.0000007071		0.0325286742		0.0325286742						4.7785405411		4.7785405411

				17.1491666667		17.026715		17.175925		17.0479666667		152.3410223807		152.3410223807		0.02597979		0.02597979						0.00084075		0.00084075		0.0357325125		0.0357325125						4.7543661291		4.7543661291

				17.6693666667		17.542615		17.695725		17.567		158.7342084534		158.7342084534		0.026874841		0.026874841						0.0045092199		0.0045092199		0.0334844565		0.0334844565						5.0279519293		5.0279519293

				18.1887333333		18.059665		18.215625		18.0826		157.6657046835		157.6657046835		0.0277954475		0.0277954475						0.004522655		0.004522655		0.0324453991		0.0324453991						4.3523104255		4.3523104255

				18.7085333333		18.577315		18.734775		18.6003333333		163.8174057704		163.8174057704		0.028623824		0.028623824						0.0054319943		0.0054319943		0.0316806938		0.0316806938						4.738942376		4.738942376

				19.2277666667		19.093465		19.254275		19.119		169.5525204767		169.5525204767		0.0286564168		0.0286564168						0.0067861038		0.0067861038		0.0291813559		0.0291813559						4.9368968354		4.9368968354

				19.7472		19.608865		19.774425		19.6316333333		168.3077640316		168.3077640316		0.0295531811		0.0295531811						0.0071043018		0.0071043018		0.0316378387		0.0316378387						5.1710523561		5.1710523561

				20.2661333333		20.125815		20.293375		20.1481		167.0650131935		167.0650131935		0.0298684462		0.0298684462						0.007522909		0.007522909		0.0299477903		0.0299477903						5.677351543		5.677351543

				20.7866333333		20.641715		20.812775		20.6671666667		162.9826220798		162.9826220798		0.0307000939		0.0307000939						0.0088063079		0.0088063079		0.0278076932		0.0278076932						5.6912904374		5.6912904374

				21.3062		21.157465		21.333025		21.1828		159.1977754242		159.1977754242		0.0316187548		0.0316187548						0.0083452742		0.0083452742		0.0290185051		0.0290185051						5.3422152375		5.3422152375

				21.8259333333		21.672715		21.852975		21.6996		164.4141907906		164.4141907906		0.0322120704		0.0322120704						0.0103315372		0.0103315372		0.0253644561		0.0253644561						6.1317949142		6.1317949142

				22.3454333333		22.189215		22.372125		22.2176666667		161.5372540107		161.5372540107		0.0333892004		0.0333892004						0.0098443406		0.0098443406		0.0271310402		0.0271310402						6.7566873276		6.7566873276

				22.8649		22.705515		22.891925		22.7326333333		158.3172549029		158.3172549029		0.0334183023		0.0334183023						0.0086938779		0.0086938779		0.02536536		0.02536536						6.888180236		6.888180236

				23.3843666667		23.221465		23.411875		23.2508333333		164.0055225696		164.0055225696		0.0347073158		0.0347073158						0.0143132555		0.0143132555		0.025824487		0.025824487						6.4072511852		6.4072511852

				23.9039333333		23.737915		23.930125		23.7688666667		164.1766318126		164.1766318126		0.0346053908		0.0346053908						0.0148853049		0.0148853049		0.0227892412		0.0227892412						5.6154178156		5.6154178156

				24.4241333333		24.254515		24.451675		24.2827333333		166.7426659057		166.7426659057		0.0353021997		0.0353021997						0.0122279976		0.0122279976		0.0240852571		0.0240852571						6.431527343		6.431527343

				24.9444333333		24.771615		24.972625		24.8003666667		172.7405140666		172.7405140666		0.0362293971		0.0362293971						0.012157994		0.012157994		0.0245128883		0.0245128883						7.0584850903		7.0584850903

				25.4635333333		25.287315		25.492575		25.3187666667		174.4413392328		174.4413392328		0.0381328546		0.0381328546						0.012826917		0.012826917		0.0239618113		0.0239618113						6.924844709		6.924844709

				25.9831333333		25.801965		26.011825		25.8333666667		171.2350969671		171.2350969671		0.0377563678		0.0377563678						0.0141605204		0.0141605204		0.0221322145		0.0221322145						6.467922273		6.467922273

				26.5026666667		26.317815		26.529025		26.3504333333		176.1771172239		176.1771172239		0.0393079247		0.0393079247						0.0143768951		0.0143768951		0.0226929485		0.0226929485						6.9632560131		6.9632560131

				27.0222333333		26.834665		27.049375		26.8676666667		184.0711268324		184.0711268324		0.0397009382		0.0397009382						0.0148980328		0.0148980328		0.0229691507		0.0229691507						7.1482830995		7.1482830995

				27.5409666667		27.350215		27.567025		27.3843		191.2373431977		191.2373431977		0.0411591506		0.0411591506						0.015011877		0.015011877		0.0241311673		0.0241311673						7.2663505175		7.2663505175

				28.0604		27.866765		28.088775		27.8990666667		196.7166304612		196.7166304612		0.0408003683		0.0408003683						0.0133317913		0.0133317913		0.0190669318		0.0190669318						7.3587430546		7.3587430546

				28.5801		28.381865		28.609375		28.4225666667		192.8498769337		192.8498769337		0.0418302772		0.0418302772						0.011217542		0.011217542		0.0251087275		0.0251087275						7.6703875124		7.6703875124

				29.1003		28.896365		29.128925		28.9345666667		183.902826877		183.902826877		0.0423259905		0.0423259905						0.0141209224		0.0141209224		0.0204219501		0.0204219501						7.9309645939		7.9309645939

				29.6203333333		29.412165		29.650325		29.4535		189.61302232		189.61302232		0.042756121		0.042756121						0.0140091995		0.0140091995		0.0232246743		0.0232246743						8.1995416545		8.1995416545

				30.1402666667		29.926415		30.169275		29.9704		203.6708307539		203.6708307539		0.0439510093		0.0439510093						0.0157691883		0.0157691883		0.0199498046		0.0199498046						8.4011524128		8.4011524128



GLP-PEOX 5k 1:3

GLP-PEOX 10k 1:3

GLP-PEOX 25K 1:3

GLP-PEOX 50K 1:3

GLP

Time (min)

Dissolved (mg)

0.0180313333

0.0437573

0.01955107

0.015239

0.0233372667

0.05007845

0.0269024

0.0161377333

0.0277155

0.0579302

0.0348003333

0.0168376333

0.0314690667

0.06301365

0.045588

0.0175402333

0.0357319667

0.0704984

0.0525918667

0.0180281333

0.0406055

0.07516045

0.0637067

0.0185431667

0.0429839

0.0814801

0.0685226667

0.0190258333

0.0466106

0.08547

0.0798978333

0.0193566

0.0502724

0.0904719

0.0877914333

0.0211270333

0.0537863

0.0951692

0.0967163

0.0216095

0.0570141

0.10123165

0.1039278333

0.0222495

0.0601752667

0.1036997

0.1124613333

0.0233038333

0.0629997667

0.1103155

0.1250751333

0.0233746333

0.0669001667

0.113412

0.1316813333

0.0239071333

0.0697541667

0.1173725

0.1370873333

0.0244387

0.0729926333

0.1228775

0.1477143333

0.0250079667

0.0758737333

0.125837

0.155227

0.0251624667

0.0789197667

0.130204

0.1619933333

0.0259802

0.0822514

0.134594

0.1701723333

0.0264974333

0.0847698667

0.1393345

0.1815613333

0.0270067667

0.0884945

0.1427045

0.1857956667

0.0272987667

0.0909850667

0.1466525

0.194618

0.0280984333

0.0943128333

0.1506775

0.2024693333

0.0286159333

0.097539

0.155622

0.2117313333

0.0289837

0.1002925

0.1605325

0.217777

0.030211

0.1034813667

0.165211

0.2234723333

0.0299470333

0.1064021

0.1690225

0.2303506667

0.0315291667

0.1085237

0.1744825

0.2373816667

0.0308371

0.1118294

0.1799655

0.2448383333

0.0314217667

0.1144947

0.183538

0.2518456667

0.0309412333

0.1170582333

0.188429

0.2596593333

0.0315404667

0.1199922333

0.1922575

0.266711

0.0318486

0.122477

0.1966275

0.2759973333

0.0324339667

0.1253941667

0.2013675

0.281419

0.0327143

0.128249

0.2039095

0.287459

0.0331451333

0.1310386667

0.208836

0.293313

0.034289

0.134112

0.214034

0.2976473333

0.0342341667

0.1365453333

0.2177425

0.305365

0.0342560333

0.1394483333

0.2213955

0.310646

0.0347057

0.1417396667

0.2248905

0.3150743333

0.0351951667

0.1445566667

0.229047

0.321442

0.0356461667

0.1471773333

0.23327

0.3251376667

0.0361852667

0.14997

0.2380895

0.3323176667

0.0364271

0.1523413333

0.24043

0.3363716667

0.0365396667

0.155431

0.2447345

0.342845

0.0377235667

0.1579553333

0.246467

0.3462276667

0.0376955

0.1606226667

0.2501275

0.3526083333

0.0386836667

0.163084

0.2547075

0.3578056667

0.0384467333

0.1657353333

0.259366

0.3625863333

0.0389257

0.1682866667

0.264005

0.3657923333

0.0392287333

0.1709946667

0.26614

0.371702

0.0392804

0.1732433333

0.268085

0.3759513333

0.0402105667

0.1760353333

0.2738535

0.3820376667

0.0402398

0.1788343333

0.279111

0.3831513333

0.0409968333

0.1816176667

0.28211

0.3917743333

0.0410290667

0.183581

0.284514

0.3927536667

0.0417277

0.1867716667

0.288525

0.3990376667

0.042059

0.1887153333

0.292637

0.4011436667

0.0426447667

0.191384

0.2967235

0.4049903333

0.0427342667



GLP-PX 5K 13 FULL 

		GLP-PX 10K 1:3								445.54																GLP-PX 10K -1				17J-31007								GLP-PX 10K -2				17J-31005								GLP-PX 10K -3				17K-02003				GLP-PX 10K 1:3 pH 6.8												GLP-PX 10K FaSSIF-1				17K-08008								GLP-PX 10K FaSSIF-2				17K-08012				GLP-PX 10K 1:3 FaSSIF

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/ml)		IDR (ug/min/cm2)

		GLP-PX 10K -1		17J-31007		0.146		16.332		0.24				0.00		5.7588		82.2689

		GLP-PX 10K -2		17J-31005		0.194		18.7		0.24				0.00		8.0136		114.4796				Dissolution Profile												Dissolution Profile												Dissolution Profile																				Dissolution Profile												Dissolution Profile

		GLP-PX 10K -3		17K-02003		0.234		18.96		0.24				0.00		7.9779		113.9704																																								AVERAGE				TIME		SD																										AVERAGE		TIME		SD

																						Time (minutes)		Weight (µg)		Weight (µg)		mg		Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (µg)		mg		Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)				Time zero (min)		%		mg		Weight (µg)						Time (minutes)		Weight (µg)		Weight (µg)		mg		Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (µg)		mg		Time zero (min)		%		mg

																						5.07213		14.2545		16.0847		0.0142545		0		0		5		15		20		0.0146354		0		0		5		0.0252041		0.0259914				0		0		0.0180313333		18.0313333333		0		0.006214717		1.90078		12.2371		18.5488		0.0122371		0		0		1.78698		11.9125		23.2101		0.0119125		0		0		0.0120748		0		0.0002295269

		AVG				0.191								0.000		7.250		103.573				5.59375		17.6864		19.0314		0.0176864		0.52162		0		6		21		24		0.0211952		0.52057		0		6		0.0311302		0.0300302				0.51953		0		0.0233372667		23.3372666667		0.5205733333		0.0069731827		2.41667		18.1697		20.8436		0.0181697		0.51589		0		2.30625		18.9		25.2101		0.0189		0.51927		0		0.01853485		0.51758		0.0005164001

		SD				0.044								0.000		1.292		18.452				6.11458		21.7885		21.9438		0.0217885		1.04245		0		6		26		28		0.0263299		1.04427		0		6		0.0350281		0.0340508				1.03855		0		0.0277155		27.7155		1.0417566667		0.0067276792		2.93385		22.8047		23.1368		0.0228047		1.03307		0		2.8211		21		27.1891		0.021		1.03412		0		0.02190235		1.033595		0.0012761156

		RSD				22.965								0.000		17.815		17.815				6.63463		24.5722		24.8224		0.0245722		1.5625		0		7		30		32		0.030174		1.56797		0		7		0.039661		0.038053				1.55703		0		0.0314690667		31.4690666667		1.5625		0.0076273108		3.45		27.204		25.418		0.027204		1.54922		0		3.33593		30.9642		29.1642		0.0309642		1.54895		0		0.0290841		1.549085		0.0026588629

		GLP-PX 10K FaSSIF-1		17K-08008		140.322		15.3		0.24				0.00		5.28		75.48				7.15573		27.6106		27.6777		0.0276106		2.0836		0		7		35		35		0.0353286		2.08802		0		7		0.0442567		0.0420412				2.07551		0		0.0357319667		35.7319666667		2.0823766667		0.0083303775		3.9638		28.231		27.6815		0.028231		2.06302		0		3.85443		31.2075		31.1495		0.0312075		2.06745		0		0.02971925		2.065235		0.0021047033

		GLP-PX 10K FaSSIF-2		17K-08012		132.990		15.24		0.24				0.00		5.50		78.64				7.67605		31.2515		30.4997		0.0312515		2.60392		0		8		40		39		0.0404943		2.60858		0		8		0.0500707		0.0460094				2.59323		0		0.0406055		40.6055		2.60191		0.0094100928		4.4789		31.839		29.9435		0.031839		2.57812		0		4.37057		34.0063		33.1218		0.0340063		2.58359		0		0.03292265		2.580855		0.0015325125

																						8.19532		33.1999		33.2876		0.0331999		3.12319		0		8		44		42		0.0438877		3.13593		0		8		0.0518641		0.0499518				3.10938		0		0.0429839		42.9839		3.1228333333		0.0093648669		4.99402		33.3041		32.1983		0.0333041		3.09324		0		4.88672		37.398		35.0903		0.037398		3.09974		0		0.03535105		3.09649		0.0028948245

		AVG				136.656								0.000		5.394		77.059				8.71407		36.6366		36.0445		0.0366366		3.64194		0		9		47		46		0.0466716		3.65755		0		9		0.0565236		0.0538941				3.62735		0		0.0466106		46.6106		3.64228		0.0099436403		5.50912		36.015		34.4458		0.036015		3.60834		0		5.40235		39.4707		37.053		0.0394707		3.61537		0		0.03774285		3.611855		0.0024435489

		SD				5.185								0.000		0.156		2.236				9.23307		39.2344		38.775		0.0392344		4.16094		0		9		51		50		0.0514409		4.17942		0		9		0.0601419		0.0578128				4.14401		0		0.0502724		50.2724		4.1614566667		0.0105026155		6.02343		38.4892		36.6826		0.0384892		4.12265		0		5.91772		39.6339		39.0109		0.0396339		4.13074		0		0.03906155		4.126695		0.0008094251

		RSD				3.794								0.000		2.901		2.901				9.75287		41.5307		41.482		0.0415307		4.68074		0		10		55		53		0.0549982		4.69947		0		10		0.06483		0.0617333				4.66276		0		0.0537863		53.7863		4.68099		0.0116968317		6.5388		39.7731		38.9169		0.0397731		4.63802		0		6.4336		42.2982		40.9668		0.0422982		4.64662		0		0.04103565		4.64232		0.0017855153

																						10.2729		44.8852		44.1629		0.0448852		5.20077		0		10		58		56		0.0582781		5.22005		0		10		0.067879		0.0656381				5.18128		0		0.0570141		57.0141		5.2007		0.0115488953		7.0539		42.5706		41.1428		0.0425706		5.15312		0		6.94843		44.0025		42.915		0.0440025		5.16145		0		0.04328655		5.157285		0.0010125062

																						10.7943		47.9866		46.8233		0.0479866		5.72217		0		11		62		60		0.0617708		5.74165		0		11		0.0707684		0.0695155				5.69788		0		0.0601752667		60.1752666667		5.7205666667		0.0114744018		7.57032		44.8592		43.3672		0.0448592		5.66954		0		7.46432		45.1679		44.8633		0.0451679		5.67734		0		0.04501355		5.67344		0.0002182839

																						11.3143		48.9864		49.4502		0.0489864		6.24217		0		11		66		63		0.0656759		6.26305		0		11		0.074337		0.0733871				6.21558		0		0.0629997667		62.9997666667		6.2402666667		0.0128854374		8.0862		45.9848		45.5822		0.0459848		6.18542		0		7.98098		48.3816		46.8107		0.0483816		6.194		0		0.0471832		6.18971		0.0016947935

																						11.8333		52.7081		52.0453		0.0527081		6.76117		0		12		68		67		0.0682756		6.78225		0		12		0.0797168		0.0772295				6.73128		0		0.0669001667		66.9001666667		6.7582333333		0.0135567818		8.60105		48.0241		47.7856		0.0480241		6.70027		0		8.49843		49.8505		48.7572		0.0498505		6.71145		0		0.0489373		6.70586		0.0012914598

																						12.3537		55.4901		54.6207		0.0554901		7.28157		0		12		71		70		0.0712603		7.30415		0		12		0.0825121		0.0810759				7.24918		0		0.0697541667		69.7541666667		7.2783		0.0135738148		9.11693		50.1445		49.9864		0.0501445		7.21615		0		9.01407		51.082		50.6932		0.051082		7.22709		0		0.05061325		7.22162		0.0006629126

																						12.8755		57.8425		57.1775		0.0578425		7.80337		0		13		75		73		0.0747494		7.82315		0		13		0.086386		0.0849068				7.76698		0		0.0729926333		72.9926333333		7.7978333333		0.0143526137		9.6323		53.2893		52.1779		0.0532893		7.73152		0		9.52838		53.1424		52.6203		0.0531424		7.7414		0		0.05321585		7.73646		0.000103874

																						13.3956		60.3928		59.6996		0.0603928		8.32347		0		13		77		77		0.0774859		8.34215		0		13		0.0897425		0.0887166				8.28358		0		0.0758737333		75.8737333333		8.3164		0.0147411171		10.1477		54.6527		54.3623		0.0546527		8.24692		0		10.0448		55.0932		54.5516		0.0550932		8.25782		0		0.05487295		8.25237		0.0003114805

																						13.9175		62.3262		62.205		0.0623262		8.84537		0		14		80		80		0.0803845		8.86195		0		14		0.0940486		0.0925225				8.80158		0		0.0789197667		78.9197666667		8.8363		0.015911843		10.6635		56.782		56.542		0.056782		8.76272		0		10.5602		58.7061		56.4751		0.0587061		8.77322		0		0.05774405		8.76797		0.0013605442

																						14.4383		65.1011		64.6799		0.0651011		9.36617		0		14		84		83		0.0842186		9.38255		0		14		0.0974345		0.0963131				9.31928		0		0.0822514		82.2514		9.356		0.0162562171		11.1797		58.7176		58.7157		0.0587176		9.27892		0		11.075		58.2371		58.3929		0.0582371		9.28802		0		0.05847735		9.28347		0.0003397648

																						14.9581		66.2831		67.1249		0.0662831		9.88597		0		15		87		86		0.0870305		9.90265		0		15		0.100996		0.100096				9.83778		0		0.0847698667		84.7698666667		9.8754666667		0.0174665167		11.6943		60.6314		60.8759		0.0606314		9.79352		0		11.5922		62.5152		60.3157		0.0625152		9.80522		0		0.0615733		9.79937		0.0013320478

																						15.4787		70.2068		69.5488		0.0702068		10.40657		0		15		90		89.4452		0.0902917		10.42345		0		15		0.104985		0.103866				10.35628		0		0.0884945		88.4945		10.3954333333		0.0174586152		12.2102		64.1612		63.0346		0.0641612		10.30942		0		12.1068		62.0313		62.2251		0.0620313		10.31982		0		0.06309625		10.31462		0.0015060667

																						15.9995		72.0857		71.9493		0.0720857		10.92737		0		16		92		93		0.0920565		10.94505		0		16		0.108813		0.107615				10.87368		0		0.0909850667		90.9850666667		10.9153666667		0.0183870775		12.7247		64.9529		65.1809		0.0649529		10.82392		0		12.6234		66.074		64.1384		0.066074		10.83642		0		0.06551345		10.83017		0.0007927374

																						16.5185		74.5651		74.3172		0.0745651		11.44637		0		17		96		96		0.0958054		11.46405		0		16		0.112568		0.11135				11.39118		0		0.0943128333		94.3128333333		11.4338666667		0.0190453648		13.2406		67.408		67.3259		0.067408		11.33982		0		13.1388		65.7581		66.0432		0.0657581		11.35182		0		0.06658305		11.34582		0.0011666555

																						17.0388		76.944		76.6672		0.076944		11.96667		0		17		99		99		0.098836		11.98565		0		17		0.116837		0.11508				11.90958		0		0.097539		97.539		11.9539666667		0.019978101		13.7573		68.986		69.4671		0.068986		11.85652		0		13.655		68.1222		67.9471		0.0681222		11.86802		0		0.0685541		11.86227		0.0006107988

																						17.5598		79.7615		78.9964		0.0797615		12.48767		0		18		102		102		0.102163		12.50545		0		17.48		0.118953		0.118816				12.43078		0		0.1002925		100.2925		12.4746333333		0.0196625913		14.2724		70.8999		71.5949		0.0708999		12.37162		0		14.1687		69.6148		69.8386		0.0696148		12.38172		0		0.07025735		12.37667		0.0009087029

																						18.0802		81.5221		81.2989		0.0815221		13.00807		0		18		105		105		0.105139		13.02625		0		18		0.123783		0.122508				12.94758		0		0.1034813667		103.4813666667		12.9939666667		0.0211791579		14.7896		72.9292		73.7245		0.0729292		12.88882		0		14.6844		71.643		71.7332		0.071643		12.89742		0		0.0722861		12.89312		0.0009094807

																						18.6015		83.9263		83.5826		0.0839263		13.52937		0		19		108		108		0.107809		13.54715		0		19		0.127471		0.12619				13.46478		0		0.1064021		106.4021		13.5137666667		0.0218064153		15.3042		74.9867		75.8366		0.0749867		13.40342		0		15.2003		74.1088		73.625		0.0741088		13.41332		0		0.07454775		13.40837		0.000620769

																						19.1205		85.4691		85.833		0.0854691		14.04837		0		19		110		111		0.10997		14.06615		0		19		0.130132		0.129857				13.98178		0		0.1085237		108.5237		14.0321		0.0223665486		15.819		78.0157		77.9429		0.0780157		13.91822		0		15.7154		75.0219		75.5102		0.0750219		13.92842		0		0.0765188		13.92332		0.0021169363

																						19.6412		87.9272		88.0678		0.0879272		14.56907		0		20		114		114		0.113615		14.58675		0		20		0.133946		0.133516				14.49948		0		0.1118294		111.8294		14.5517666667		0.0230613045		16.3349		78.7763		80.0468		0.0787763		14.43412		0		16.2326		76.0608		77.3993		0.0760608		14.44562		0		0.07741855		14.43987		0.0019201485

																						20.162		89.9011		90.2806		0.0899011		15.08987		0		20		116.428		117		0.116428		15.10765		0		20		0.137155		0.137161				15.01698		0		0.1144947		114.4947		15.0715		0.0236861986		16.8515		81.9269		82.1467		0.0819269		14.95072		0		16.75		78.9368		79.2857		0.0789368		14.96302		0		0.08043185		14.95687		0.00211432

																						20.682		91.7077		92.4676		0.0917077		15.60987		0		21		119		120		0.11887		15.62765		0		21		0.140597		0.140801				15.53558		0		0.1170582333		117.0582333333		15.5910333333		0.0244949543		17.3672		84.6696		84.2362		0.0846696		15.46642		0		17.2652		79.9112		81.1601		0.0799112		15.47822		0		0.0822904		15.47232		0.0033646969

																						21.2037		94.6637		94.6393		0.0946637		16.13157		0		21		122		123		0.122195		16.14925		0		21		0.143118		0.144414				16.05208		0		0.1199922333		119.9922333333		16.1109666667		0.0243021384		17.8833		84.7631		86.3209		0.0847631		15.98252		0		17.7823		81.4645		83.038		0.0814645		15.99532		0		0.0831138		15.98892		0.0023324624

																						21.7237		96.212		96.7822		0.096212		16.65157		0		22		124		125		0.124312		16.66825		0		22		0.146907		0.148009				16.56798		0		0.122477		122.477		16.6292666667		0.0253972671		18.398		88.712		88.3929		0.088712		16.49722		0		18.2995		83.9564		84.9123		0.0839564		16.51252		0		0.0863342		16.50487		0.003362717

																						22.245		98.3535		98.9088		0.0983535		17.17287		0		22		128		128		0.127665		17.18865		0		22		0.150164		0.151606				17.08598		0		0.1253941667		125.3941666667		17.1491666667		0.02597979		18.9128		89.7829		90.4589		0.0897829		17.01202		0		18.8153		86.0516		86.7781		0.0860516		17.02832		0		0.08791725		17.02017		0.0026384275

																						22.7663		100.384		101.014		0.100384		17.69417		0		23		130.353		131		0.130353		17.70945		0		23		0.15401		0.155195				17.60448		0		0.128249		128.249		17.6693666667		0.026874841		19.4288		91.4784		92.523		0.0914784		17.52802		0		19.3325		89.527		88.645		0.089527		17.54552		0		0.0905027		17.53677		0.0013798482

																						23.286		102.428		103.091		0.102428		18.21387		0		23		133		134		0.132748		18.23125		0		23		0.15794		0.158758				18.12108		0		0.1310386667		131.0386666667		18.1887333333		0.0277954475		19.9438		95.6661		94.5764		0.0956661		18.04302		0		19.8505		89.1317		90.5112		0.0891317		18.06352		0		0.0923989		18.05327		0.0046205186

																						23.805		104.687		105.144		0.104687		18.73287		0		24		136		137		0.135788		18.75315		0		24		0.161861		0.162321				18.63958		0		0.134112		134.112		18.7085333333		0.028623824		20.4588		95.1171		96.6233		0.0951171		18.55802		0		20.3672		91.5323		92.369		0.0915323		18.58022		0		0.0933247		18.56912		0.0025348364

																						24.3255		106.793		107.183		0.106793		19.25337		0		24.35		139		139		0.13888		19.27395		0		24		0.163963		0.165857				19.15598		0		0.1365453333		136.5453333333		19.2277666667		0.0286564168		20.9753		97.4556		98.6695		0.0974556		19.07452		0		20.8837		93.9991		94.2225		0.0939991		19.09672		0		0.09572735		19.08562		0.0024441146

																						24.8463		108.947		109.202		0.108947		19.77417		0		25		141		142		0.141446		19.79295		0		25		0.167952		0.169395				19.67448		0		0.1394483333		139.4483333333		19.7472		0.0295531811		21.4913		100.132		100.707		0.100132		19.59052		0		21.4008		95.3998		96.0748		0.0953998		19.61382		0		0.0977659		19.60217		0.0033461707

																						25.368		111.447		111.204		0.111447		20.29587		0		25		143		144.883		0.142607		20.31195		0		25		0.171165		0.172904				20.19058		0		0.1417396667		141.7396666667		20.2661333333		0.0298684462		22.0075		102.317		102.739		0.102317		20.10672		0		21.917		96.0233		97.9199		0.0960233		20.13002		0		0.09917015		20.11837		0.0044503179

																						25.8888		112.927		113.182		0.112927		20.81667		0		26		147		148		0.146509		20.83175		0		26		0.174234		0.176434				20.71148		0		0.1445566667		144.5566666667		20.7866333333		0.0307000939		22.524		104.308		104.765		0.104308		20.62322		0		22.4337		98.7425		99.7631		0.0987425		20.64672		0		0.10152525		20.63497		0.0039354028

																						26.4088		114.428		115.137		0.114428		21.33667		0		26		150		150		0.149575		21.35345		0		26		0.177529		0.179924				21.22848		0		0.1471773333		147.1773333333		21.3062		0.0316187548		23.0393		106.745		106.781		0.106745		21.13852		0		22.9492		101.114		101.599		0.101114		21.16222		0		0.1039295		21.15037		0.0039817183

																						26.9305		117.303		117.079		0.117303		21.85837		0		27		151		153		0.1509		21.87245		0		27		0.181707		0.183413				21.74698		0		0.14997		149.97		21.8259333333		0.0322120704		23.555		107.361		108.791		0.107361		21.65422		0		23.4648		103.551		103.431		0.103551		21.67782		0		0.105456		21.66602		0.0026940768

																						27.4505		117.834		118.995		0.117834		22.37837		0		27		155		155		0.154703		22.39245		0		27		0.184487		0.186889				22.26548		0		0.1523413333		152.3413333333		22.3454333333		0.0333892004		24.0717		110.47		110.799		0.11047		22.17092		0		23.9815		104.661		105.263		0.104661		22.19452		0		0.1075655		22.18272		0.0041075833

																						27.9712		121.122		120.894		0.121122		22.89907		0		28		157.29		158		0.15729		22.91115		0		28		0.187881		0.190357				22.78448		0		0.155431		155.431		22.8649		0.0334183023		24.5872		113.613		112.796		0.113613		22.68642		0		24.4982		106.637		107.092		0.106637		22.71122		0		0.110125		22.69882		0.0049327769

																						28.492		122.093		122.774		0.122093		23.41987		0		29		160		161		0.160394		23.43275		0		28		0.191379		0.193792				23.30048		0		0.1579553333		157.9553333333		23.3843666667		0.0347073158		25.1047		114.374		114.794		0.114374		23.20392		0		25.0157		108.437		108.92		0.108437		23.22872		0		0.1114055		23.21632		0.004198093

																						29.011		124.929		124.629		0.124929		23.93887		0		29		163		163		0.162913		23.95365		0		29		0.194026		0.197234				23.81928		0		0.1606226667		160.6226666667		23.9039333333		0.0346053908		25.6218		116.956		116.784		0.116956		23.72102		0		25.5313		109.805		110.738		0.109805		23.74432		0		0.1133805		23.73267		0.0050565206

																						29.5325		126.639		126.473		0.126639		24.46037		0		30		165		166		0.165493		24.47525		0		29		0.19712		0.200655				24.33678		0		0.163084		163.084		24.4241333333		0.0353021997		26.1385		118.967		118.766		0.118967		24.23772		0		26.0455		113.025		112.548		0.113025		24.25852		0		0.115996		24.24812		0.0042016285

																						30.0538		128.734		128.299		0.128734		24.98167		0		30		167		168		0.167332		24.99615		0		30		0.20114		0.204071				24.85548		0		0.1657353333		165.7353333333		24.9444333333		0.0362293971		26.6542		123.143		120.737		0.123143		24.75342		0		26.5612		115.488		114.359		0.115488		24.77422		0		0.1193155		24.76382		0.0054129024

																						30.5735		129.038		130.1		0.129038		25.50137		0		31		171		170.659		0.170626		25.51615		0		30		0.205196		0.207469				25.37308		0		0.1682866667		168.2866666667		25.4635333333		0.0381328546		27.1703		125.478		122.705		0.125478		25.26952		0		27.0772		114.714		116.167		0.114714		25.29022		0		0.120096		25.27987		0.0076112974

																						31.094		132.21		131.886		0.13221		26.02187		0		31		173		173		0.173143		26.03595		0		31		0.207631		0.210861				25.89158		0		0.1709946667		170.9946666667		25.9831333333		0.0377563678		27.686		124.774		124.664		0.124774		25.78522		0		27.595		118.182		117.979		0.118182		25.80802		0		0.121478		25.79662		0.0046612479

																						31.613		132.692		133.648		0.132692		26.54087		0		32		176		176		0.175861		26.55765		0		31		0.211177		0.214236				26.40948		0		0.1732433333		173.2433333333		26.5026666667		0.0393079247		28.2018		127.315		126.617		0.127315		26.30102		0		28.1125		119.712		119.785		0.119712		26.32552		0		0.1235135		26.31327		0.0053761329

																						32.1337		135.611		135.399		0.135611		27.06157		0		32		178		178		0.177524		27.07715		0		32		0.214971		0.217604				26.92798		0		0.1760353333		176.0353333333		27.0222333333		0.0397009382		28.718		128.418		128.566		0.128418		26.81722		0		28.6287		121.723		121.584		0.121723		26.84172		0		0.1250705		26.82947		0.0047340799

																						32.6528		136.803		137.127		0.136803		27.58067		0		33		180.638		180		0.180638		27.59895		0		32		0.219062		0.220939				27.44328		0		0.1788343333		178.8343333333		27.5409666667		0.0411591506		29.233		130.168		130.504		0.130168		27.33222		0		29.144		123.122		123.376		0.123122		27.35702		0		0.126645		27.34462		0.0049822744

																						33.1735		139.656		138.842		0.139656		28.10137		0		33		184		183		0.184049		28.11975		0		33		0.221148		0.224273				27.96008		0		0.1816176667		181.6176666667		28.0604		0.0408003683		29.7473		131.592		132.433		0.131592		27.84652		0		29.6602		124.389		125.168		0.124389		27.87322		0		0.1279905		27.85987		0.0050932901

																						33.6935		140.319		140.537		0.140319		28.62137		0		34		186.609		185		0.186609		28.64165		0		34		0.223815		0.227596				28.47728		0		0.183581		183.581		28.5801		0.0418302772		30.2643		133.815		134.365		0.133815		28.36352		0		30.1768		129.684		126.957		0.129684		28.38982		0		0.1317495		28.37667		0.0029210581

																						34.214		143.436		142.217		0.143436		29.14187		0		34		189		187		0.188869		29.16325		0		34		0.22801		0.230917				28.99578		0		0.1867716667		186.7716666667		29.1003		0.0423259905		30.7807		136.242		136.289		0.136242		28.87992		0		30.6908		129.351		128.734		0.129351		28.90382		0		0.1327965		28.89187		0.0048726728

																						34.7357		144.696		143.884		0.144696		29.66357		0		35		191		190		0.191365		29.68415		0		35		0.230085		0.23422				29.51328		0		0.1887153333		188.7153333333		29.6203333333		0.042756121		31.2962		137.698		138.204		0.137698		29.39542		0		31.2057		130.291		130.511		0.130291		29.41872		0		0.1339945		29.40707		0.0052375399

																						35.257		146.284		145.533		0.146284		30.18487		0		35		194		192		0.19378		30.20465		0		35		0.234088		0.237514				30.03128		0		0.191384		191.384		30.1402666667		0.0439510093		31.8097		140.322		140.106		0.140322		29.90892		0		31.7213		132.99		132.287		0.13299		29.93432		0		0.136656		29.92162		0.0051845069

																																														35		0.236584		0.237737																32.3245		142.349		142.006								32.2362		134.192		134.056

																																														37		0.2442		0.250442																32.8403		144.31		143.903								32.7523		137.436		135.826

																																														39		0.255688		0.262985

																																														41		0.267249		0.275357

																																														43		0.280162		0.287561

																																														45.2		0.292014		0.299592

																																														47		0.303547		0.311455

																																														49		0.316495		0.323167

																																														51.25		0.326833		0.334714

																																														53		0.34002		0.346112

																																														55		0.355162		0.35735

																																														57		0.369844		0.36844

																																														59		0.383523		0.379377

																																														61		0.394294		0.39017

																																														63		0.40563		0.400807

																																														65		0.416325		0.411302

																																														67		0.42683		0.421653

																																														69		0.437891		0.431865

																																														71		0.447967		0.441933

																																														73		0.458118		0.451865

																																														75		0.467279		0.461665

																																														77		0.476596		0.471327

																																														79		0.487823		0.480851

																																														82		0.496582		0.490252

																																														84		0.505321		0.499529

																																														86		0.515529		0.508682

																																														88		0.524114		0.517709

																																														90		0.532326		0.526605

																																														92		0.541935		0.535379

																																														94		0.550552		0.544038

																																														96		0.558415		0.552573

																																														98		0.566221		0.560989

																																														100		0.573199		0.569295

																																														102		0.58057		0.577487

																																														104		0.587667		0.585572

																																														106		0.594451		0.593547

																																														108		0.602558		0.601408

																																														110		0.609824		0.609169

																																														112		0.617215		0.616822

																																														114		0.623166		0.624372

																																														116		0.630879		0.631819

																																														118		0.639099		0.639159

																																														120		0.645326		0.646401

																																														122		0.651748		0.653549

																																														124		0.660606		0.660594

																																														126		0.667396		0.667539

																																														128		0.67557		0.674395

																																														130		0.681894		0.681157

																																														132		0.688954		0.687831

																																														134		0.694637		0.694411

																																														136		0.700915		0.700894

																																														138		0.706946		0.707293

																																														140		0.714482		0.713609

																																														142		0.72071		0.719845

																																														144		0.726617		0.725984

																																														146		0.735149		0.732041

																																														148		0.738971		0.738013

																																														150		0.746819		0.74391

																																														152		0.752465		0.749727

																																														154		0.757703		0.755465

																																														156.16		0.762649		0.761122

																																														158		0.768202		0.766699

																																														160		0.775228		0.772206

																																														162		0.779722		0.777634

																																														164.23		0.784656		0.782987

																																														166		0.789943		0.788272

																																														168		0.795337		0.793479

																																														170		0.800004		0.79862

																																														172.3		0.805142		0.803686

																																														174.32		0.80905		0.808692

																																														176		0.814717		0.813621

																																														178		0.818887		0.818483

																																														180		0.824072		0.823282

																																														182.39		0.829095		0.828016

																																														184		0.833457		0.832686

																																														186		0.838732		0.837288

																																														188		0.842896		0.841831

																																														190.46		0.847306		0.846308

																																														192		0.852875		0.850728

																																														194		0.856011		0.855085

																																														196.51		0.859445		0.859378

																																														198.53		0.862631		0.863623

																																														201		0.866751		0.867803

																																														203		0.872009		0.871934

																																														205		0.875254		0.876001

																																														207		0.878464		0.880009

																																														209		0.883402		0.883966

																																														210.63		0.887345		0.887866

																																														212.65		0.889617		0.891722

																																														215		0.892617		0.895523

																																														217		0.895745		0.899265

																																														218.7		0.901368		0.90296

																																														221		0.903862		0.906607

																																														223		0.90769		0.910207

																																														225		0.9098		0.913756

																																														227		0.91889		0.91725

																																														229		0.916464		0.920699

																																														231		0.919858		0.924104

																																														233		0.92292		0.927466

																																														235		0.9274		0.930776

																																														237		0.929732		0.934039

																																														239		0.931971		0.937259

																																														241		0.937972		0.940438

																																														243		0.941253		0.943579

																																														245		0.942522		0.94667

																																														247		0.945338		0.949716

																																														249		0.946587		0.952728

																																														251		0.949525		0.955694

																																														253		0.954969		0.958621

																																														255.02		0.956311		0.961509

																																														257		0.960826		0.964355

																																														259		0.962708		0.967163

																																														261		0.969064		0.969934

																																														263		0.968664		0.97267

																																														265		0.971371		0.975368

																																														267.13		0.974142		0.978028

																																														269		0.976953		0.980649

																																														271		0.977849		0.983236

																																														273		0.98478		0.985788

																																														275		0.984881		0.988305

																																														277.22		0.988025		0.990788

																																														279		0.988208		0.993237

																																														281		0.991618		0.995651

																																														283		0.994935		0.998036

																																														285		0.996518		1

																																														287.31		0.997841		1

																																														289		0.999699		1

																																														291		1		1

																																														293		1		1

																																														295		1		1

																																														297.4		1		1

																																														299		1		1

																																														301		1		1

																																														303		1		1

																																														305		1		1

																																														307.49		1		1

																																														309.51		1		1

																																														312		1		1

																																														314		1		1

																																														316		1		1

																																														317.58		1		1

																																														320		1		1

																																														322		1		1

																																														324		1		1

																																														326		1		1

																																														327.67		1		1

																																														330		1		1

																																														332		1		1

																																														334		1		1

																																														336		1		1

																																														337.76		1		1

																																														340		1		1

																																														342		1		1

																																														344		1		1

																																														346		1		1

																																														348		1		1

																																														350		1		1

																																														351.88		1		1

																																														353.9		1		1

																																														356		1		1

																																														358		1		1

																																														360		1		1

																																														362		1		1

																																														364		1		1

																																														366		1		1

																																														368.03		1		1





GLP-PX 5K 13 FULL 

		



GLP-PX 10K 1:3 FaSSIF

GLP-PX 10K 1:3 pH 6.8

Time (min)

Dissolved (mg)



GLP-PX 50K 12FULL 

		GLP-PX 25K 1:3								445.54																GLP-PX 25K -1				17K-08014								GLP-PX 25K -2				17K-08016								GLP-PX 25K -3				17K-08020				GLP-PX 25K 1:3 pH 6.8												GLP-PX 25K FaSSIF-1				17K-09014								GLP-PX 25K FaSSIF-2				17K-09011								GLP-PX 25K FaSSIF-3				17K-09006				GLP-PX 25K 1:3 FaSSIF

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/ml)		IDR (ug/min/cm2)

		GLP-PX 25K -1		17K-08014		0.570		16.332		0.24				0.00		23.5850		336.9286

		GLP-PX 25K -2		17K-08016		0.308		18.7		0.24				0.00		10.1560		145.0863				Dissolution Profile												Dissolution Profile												Dissolution Profile																				Dissolution Profile												Dissolution Profile												Dissolution Profile

		GLP-PX 25K -3		17K-08020		0.286		18.96		0.24				0.00		11.1010		158.5856																																								AVERAGE				TIME		SD																																						AVERAGE		TIME		SD

																						Time (minutes)		Weight (µg)		Weight (µg)		mg		Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (µg)		mg		Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (µg)		mg		Time zero (min)		%		mg		Weight (µg)						Time (minutes)		Weight (µg)		Weight (µg)		mg		Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (µg)		mg		Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (µg)		mg		Time zero (min)		%		mg

																						5.01015		67.1955		73.839		0.0671955		0		0		5.04037		37.0555		37.5105		0.0370555		0		0		5.0237		50.4591		84.7088		0.0504591		0		0		0.0437573		43.7573		0		0.0094777765		1.8138		4.53786		11.8095		0.00453786		0		126.1557451564		1.86875		13.3205		13.0108		0.0133205		0		371.777352799		1.91407		5.08731		17.6643		0.00508731		0		98.5827772605		0.0076485567		0		0.0049197235

		AVG				0.297								0.000		10.629		151.836				5.52787		78.2061		85.6807		0.0782061		0.51772		0		5.55652		43.2677		42.7685		0.0432677		0.51615		0		5.54297		56.8892		88.4443		0.0568892		0.51927		0		0.05007845		50.07845		0.51771		0.009631855		2.32943		16.1724		16.7357		0.0161724		0.51563		449.6042568452		2.38698		16.7931		17.5814		0.0167931		0.51823		468.6981917562		2.42968		16.7073		22.5791		0.0167073		0.51561		323.7569628201		0.0165576		0.51649		0.0003363401

		SD				0.016								0.000		0.668		9.545				6.04505		91.0987		97.3408		0.0910987		1.0349		0		6.075		48.8567		48.0289		0.0488567		1.03463		0		6.0599		67.0037		92.1449		0.0670037		1.0362		0		0.0579302		57.9302		1.035415		0.0128318668		2.84348		22.9402		21.6176		0.0229402		1.02968		637.7539247657		2.9026		23.2019		22.0955		0.0232019		1.03385		647.5688571681		2.94532		25.2766		27.4518		0.0252766		1.03125		489.8143474061		0.0238062333		1.0315933333		0.0012800802

		RSD				5.314								0.000		6.287		6.287				6.56407		105.853		108.874		0.105853		1.55392		0		6.59167		53.038		53.2499		0.053038		1.5513		0		6.57708		72.9893		95.8294		0.0729893		1.55338		0		0.06301365		63.01365		1.55234		0.0141076995		3.3573		26.8985		26.4684		0.0268985		1.5435		747.7974884836		3.41823		27.3046		26.5766		0.0273046		1.54948		762.0758910878		3.46042		32.3971		32.2776		0.0323971		1.54635		627.7966338174		0.0288667333		1.5464433333		0.0030641224

		GLP-PX 25K FaSSIF-1		17K-09014		0.254		15.3		0.24		3.60		7.06		10.32		147.39				7.0823		115.496		120.225		0.115496		2.07215		0		7.10782		61.5407		58.4446		0.0615407		2.06745		0		7.09505		79.4561		99.5016		0.0794561		2.07135		0		0.0704984		70.4984		2.0694		0.0126681008		3.87343		33.2319		31.3122		0.0332319		2.05963		923.8705265177		3.93463		31.1661		31.0315		0.0311661		2.06588		869.8509932111		3.975		39.146		37.0571		0.039146		2.06093		758.5779908516		0.0345146667		2.0621466667		0.0041417169

		GLP-PX 25K FaSSIF-2		17K-09011		0.228		15.24		0.24		3.58		6.37		8.63		123.22				7.6013		127.424		131.43		0.127424		2.59115		0		7.62422		65.5878		63.6209		0.0655878		2.58385		0		7.60833		84.7331		103.123		0.0847331		2.58463		0		0.07516045		75.16045		2.58424		0.0135377715		4.38907		40.1653		36.1226		0.0401653		2.57527		1116.6239925716		4.45027		35.5471		35.4472		0.0355471		2.58152		992.1254260487		4.4888		43.1106		41.7883		0.0431106		2.57473		835.4046986258		0.0396076667		2.5771733333		0.0038124597

		GLP-PX 25K FaSSIF-3		17K-09006		0.243		21.95		0.24		5.16		4.71		11.44		163.45				8.11927		141.563		142.452		0.141563		3.10912		0		8.13907		72.0752		68.761		0.0720752		3.0987		0		8.12527		90.885		106.753		0.090885		3.10157		0		0.0814801		81.4801		3.100135		0.0133005371		4.90313		44.6724		40.8898		0.0446724		3.08933		1241.9245877849		4.96432		38.3832		39.8171		0.0383832		3.09557		1071.2814449874		5.00338		48.6914		46.4861		0.0486914		3.08931		943.5504108657		0.0439156667		3.0914033333		0.0051955973

		AVG				0.242								6.046		10.128		144.687				8.63777		154.582		153.327		0.154582		3.62762		0		8.65443		75.7552		73.8856		0.0757552		3.61406		0		8.64063		95.1848		110.354		0.0951848		3.61693		0		0.08547		85.47		3.615495		0.0137388019		5.41745		49.7342		45.6312		0.0497342		3.60365		1382.6462387025		5.47943		42.6583		44.1641		0.0426583		3.61068		1190.6001913521		5.51718		55.359		51.1364		0.055359		3.60311		1072.7563223714		0.0492505		3.6058133333		0.0063641511

		SD				0.013								1.203		1.417		20.249				9.15573		165.538		164.035		0.165538		4.14558		0		9.1711		81.4684		79.0024		0.0814684		4.13073		0		9.15547		99.4754		113.934		0.0994754		4.13177		0		0.0904719		90.4719		4.13125		0.0127328718		5.93438		54.1852		50.3683		0.0541852		4.12058		1506.3872138959		5.99375		47.4708		48.4726		0.0474708		4.125		1324.9178603844		6.03333		59.4751		55.7678		0.0594751		4.11926		1152.5188234736		0.0537103667		4.1216133333		0.0060162201

		RSD				5.359								19.903		13.995		13.995				9.675		177.937		174.616		0.177937		4.66485		0		9.6875		84.4224		84.0961		0.0844224		4.64713		0		9.6711		105.916		117.502		0.105916		4.6474		0		0.0951692		95.1692		4.647265		0.0151982703		6.44948		58.5032		55.0606		0.0585032		4.63568		1626.4306942116		6.50885		53.9996		52.756		0.0539996		4.6401		1507.1377455955		6.5474		64.4259		60.3409		0.0644259		4.63333		1248.4562862311		0.0589762333		4.63637		0.0052292211

																						10.1914		190.106		184.987		0.190106		5.18125		0		10.2047		91.9313		89.1769		0.0919313		5.16433		0		10.1859		110.532		121.047		0.110532		5.1622		0		0.10123165		101.23165		5.163265		0.0131526811		6.96355		61.9345		59.7158		0.0619345		5.14975		1721.8232819854		7.025		57.8935		57.0168		0.0578935		5.15625		1615.8171370646		7.06355		68.7359		64.893		0.0687359		5.14948		1331.9762152295		0.0628546333		5.1518266667		0.0054794519

																						10.7086		199.073		195.226		0.199073		5.69845		0		10.7216		93.5544		94.2348		0.0935544		5.68123		0		10.7031		113.845		124.592		0.113845		5.6794		0		0.1036997		103.6997		5.680315		0.0143476209		7.47787		65.2932		64.3456		0.0652932		5.66407		1815.1975379688		7.5401		63.1173		61.2377		0.0631173		5.67135		1761.6142569588		7.57865		73.511		69.3967		0.073511		5.66458		1424.5089328537		0.0673071667		5.6666666667		0.0054817238

																						11.2234		213.014		205.273		0.213014		6.21325		0		11.2388		100.724		99.2748		0.100724		6.19843		0		11.2206		119.907		128.121		0.119907		6.1969		0		0.1103155		110.3155		6.197665		0.0135644294		7.99348		70.9499		68.9596		0.0709499		6.17968		1972.457833268		8.05468		66.9805		65.4235		0.0669805		6.18593		1869.4368063626		8.09375		77.3165		73.8616		0.0773165		6.17968		1498.2525731793		0.0717489667		6.1817633333		0.0052141255

																						11.7409		221.818		215.227		0.221818		6.73075		0		11.7539		103.874		104.274		0.103874		6.71353		0		11.7357		122.95		131.617		0.12295		6.712		0		0.113412		113.412		6.712765		0.013488769		8.5086		73.2682		73.5417		0.0732682		6.6948		2036.9082270651		8.57032		72.2541		69.5872		0.0722541		6.70157		2016.6238524736		8.60938		80.993		78.2927		0.080993		6.69531		1569.496429087		0.0755051		6.6972266667		0.0047796323

																						12.257		232.206		225.013		0.232206		7.24685		0		12.2682		108.834		109.246		0.108834		7.22783		0		12.2505		125.911		135.095		0.125911		7.2268		0		0.1173725		117.3725		7.227315		0.0120752625		9.02265		77.3359		78.0873		0.0773359		7.20885		2149.9931888252		9.08647		74.9459		73.7244		0.0749459		7.21772		2091.7524346037		9.12448		83.7252		82.6811		0.0837252		7.21041		1622.4414754929		0.078669		7.2123266667		0.0045389309

																						12.7734		240.795		234.665		0.240795		7.76325		0		12.7841		114.172		114.213		0.114172		7.74373		0		12.7648		131.583		138.552		0.131583		7.7411		0		0.1228775		122.8775		7.742415		0.0123114362		9.53932		80.2586		82.6288		0.0802586		7.72552		2231.2463337809		9.60157		77.9993		77.823		0.0779993		7.73282		2176.9733323956		9.63777		88.3126		87.0165		0.0883126		7.7237		1711.3369098983		0.0821901667		7.7273466667		0.0054211854

																						13.2893		253.179		244.169		0.253179		8.27915		0		13.2997		116.245		119.158		0.116245		8.25933		0		13.2805		135.429		142.001		0.135429		8.2568		0		0.125837		125.837		8.258065		0.0135651365		10.055		84.913		87.1344		0.084913		8.2412		2360.641974073		10.1172		82.3477		81.8957		0.0823477		8.24845		2298.3378938543		10.1534		92.1601		91.3342		0.0921601		8.23933		1785.8944335227		0.0864736		8.2429933333		0.0050889491

																						13.806		256.303		253.551		0.256303		8.79585		0		13.8172		120.079		124.1		0.120079		8.77683		0		13.7953		140.329		145.429		0.140329		8.7716		0		0.130204		130.204		8.774215		0.0143189123		10.5719		90.1953		91.6244		0.0901953		8.7581		2507.4936822879		10.6326		85.619		85.9366		0.085619		8.76385		2389.6404165983		10.669		97.1447		95.6149		0.0971447		8.75493		1882.4868785541		0.0909863333		8.75896		0.0058034249

																						14.3216		264.962		262.781		0.264962		9.31145		0		14.3323		125.018		129		0.125018		9.29193		0		14.3117		144.17		148.85		0.14417		9.288		0		0.134594		134.594		9.289965		0.0135425091		11.0852		92.6231		96.0561		0.0926231		9.2714		2574.9882541986		11.1479		89.0907		89.9479		0.0890907		9.27915		2486.536136407		11.1857		100.17		99.8671		0.10017		9.27163		1941.1116676953		0.0939612667		9.27406		0.0056595706

																						14.8378		275.647		271.888		0.275647		9.82765		0		14.8487		130.307		133.893		0.130307		9.80833		0		14.8279		148.362		152.253		0.148362		9.8042		0		0.1393345		139.3345		9.806265		0.0127668129		11.6013		96.6719		100.486		0.0966719		9.7875		2687.5477824761		11.6648		93.408		93.9418		0.093408		9.79605		2607.0326917345		11.7018		104.244		104.078		0.104244		9.78773		2020.0583476813		0.0981079667		9.7904266667		0.0055589063

																						15.3539		284.11		280.865		0.28411		10.34375		0		15.3643		134.379		138.758		0.134379		10.32393		0		15.3443		151.03		155.641		0.15103		10.3206		0		0.1427045		142.7045		10.322265		0.011774035		12.1169		101.601		104.886		0.101601		10.3031		2824.5802787299		12.1807		97.7365		97.8984		0.0977365		10.31195		2727.8418409098		12.2172		107.47		108.247		0.10747		10.30313		2082.5723363004		0.1022691667		10.30606		0.0049010295

																						15.8695		288.176		289.705		0.288176		10.85935		0		15.881		136.868		143.614		0.136868		10.84063		0		15.8586		156.437		159		0.156437		10.8349		0		0.1466525		146.6525		10.837765		0.0138373726		12.6305		104.523		109.241		0.104523		10.8167		2905.8139631863		12.6956		100.921		101.818		0.100921		10.82685		2816.7217613324		12.7323		112.431		112.378		0.112431		10.81823		2178.7074564306		0.1059583333		10.8205933333		0.0058877127

																						16.3854		297.116		298.423		0.297116		11.37525		0		16.3971		143.796		148.445		0.143796		11.35673		0		16.3747		157.559		162.353		0.157559		11.351		0		0.1506775		150.6775		11.353865		0.0097319106		13.1456		108.558		113.584		0.108558		11.3318		3017.9898416193		13.2107		104.997		105.711		0.104997		11.34195		2930.4835938468		13.249		117.146		116.486		0.117146		11.33493		2270.0755458105		0.1102336667		11.3362266667		0.0062454339

																						16.8987		304.301		306.974		0.304301		11.88855		0		16.9163		148.461		153.286		0.148461		11.87593		0		16.8902		162.783		165.686		0.162783		11.8665		0		0.155622		155.622		11.871215		0.0101271833		13.6617		111.552		117.91		0.111552		11.8479		3101.2251774381		13.7253		108.082		109.572		0.108082		11.85655		3016.5864528525		13.763		120.13		120.537		0.12013		11.84893		2327.9000163746		0.1132546667		11.8511266667		0.006201845

																						17.4153		310.738		315.458		0.310738		12.40515		0		17.4313		153.307		158.068		0.153307		12.39093		0		17.4063		167.758		169.008		0.167758		12.3826		0		0.1605325		160.5325		12.386765		0.0102184001		14.1771		114.54		122.204		0.11454		12.3633		3184.2937089766		14.2414		111.823		113.416		0.111823		12.37265		3120.998380094		14.2792		124.101		124.57		0.124101		12.36513		2404.850744461		0.1168213333		12.3670266667		0.0064490838

																						17.932		323.728		323.821		0.323728		12.92185		0		17.9468		160.05		162.835		0.16005		12.90643		0		17.9223		170.372		172.313		0.170372		12.8986		0		0.165211		165.211		12.902515		0.0072987562		14.6935		122.298		126.481		0.122298		12.8797		3399.9716432724		14.7547		116.838		117.21		0.116838		12.88595		3260.9678575376		14.7948		127.781		128.565		0.127781		12.88073		2476.162423977		0.1223056667		12.8821266667		0.005471504

																						18.4482		325.957		332.057		0.325957		13.43805		0		18.4622		164.621		167.581		0.164621		13.42183		0		18.4362		173.424		175.588		0.173424		13.4125		0		0.1690225		169.0225		13.417165		0.006224661		15.2104		128.599		130.737		0.128599		13.3966		3575.1439381935		15.2688		117.929		120.983		0.117929		13.40005		3291.4178475458		15.3102		131.268		132.523		0.131268		13.39613		2543.7341159532		0.125932		13.3975933333		0.0070581086

																						18.9643		338.281		340.175		0.338281		13.95415		0		18.9768		170.773		172.303		0.170773		13.93643		0		18.9515		178.192		178.856		0.178192		13.9278		0		0.1744825		174.4825		13.932115		0.0052460252		15.7255		135.693		134.952		0.135693		13.9117		3772.362198814		15.7831		122.159		124.73		0.122159		13.91435		3409.4778454692		15.825		135.272		136.443		0.135272		13.91093		2621.3243237744		0.1310413333		13.9123266667		0.0076952059

																						19.4788		344.463		348.151		0.344463		14.46865		0		19.4917		178.763		177.007		0.178763		14.45133		0		19.4672		181.168		182.111		0.181168		14.4435		0		0.1799655		179.9655		14.447415		0.0017005918		16.2412		138.868		139.147		0.138868		14.4274		3860.629463752		16.2992		126.743		128.463		0.126743		14.43045		3537.4180418005		16.3419		139		140.345		0.139		14.42783		2693.5661556319		0.1348703333		14.42856		0.0070387866

																						19.9955		348.104		356.047		0.348104		14.98535		0		20.007		182.116		181.697		0.182116		14.96663		0		19.9815		184.96		185.342		0.18496		14.9578		0		0.183538		183.538		14.962215		0.0020110117		16.7563		145.61		143.313		0.14561		14.9425		4048.0618732677		16.8162		130.116		132.174		0.130116		14.94745		3631.5590283244		16.858		141.623		144.207		0.141623		14.94393		2744.3951054609		0.1391163333		14.9446266667		0.008045405

																						20.5122		370.491		363.83		0.370491		15.50205		0		20.5218		189.261		186.363		0.189261		15.48143		0		20.4982		187.597		188.572		0.187597		15.4745		0		0.188429		188.429		15.477965		0.0011766257		17.2712		150.38		147.452		0.15038		15.4574		4180.6712760249		17.3328		134.065		135.856		0.134065		15.46405		3741.7762698846		17.3722		146.701		148.021		0.146701		15.45813		2842.7974719234		0.1437153333		15.45986		0.0085574798

																						21.0273		386.78		371.479		0.38678		16.01715		0		21.0365		192.511		191.009		0.192511		15.99613		0		21.0148		192.004		191.786		0.192004		15.9911		0		0.1922575		192.2575		15.993615		0.0003585031		17.7872		155.082		151.575		0.155082		15.9734		4311.3902302733		17.8463		137.669		139.488		0.137669		15.97755		3842.364504522		17.8888		150.847		151.821		0.150847		15.97473		2923.1393804217		0.147866		15.9752266667		0.0090811846

																						21.545		401.523		379.056		0.401523		16.53485		0		21.5527		196.628		195.65		0.196628		16.51233		0		21.5323		196.627		194.99		0.196627		16.5086		0		0.1966275		196.6275		16.510465		0.0000007071		18.3027		159.104		155.67		0.159104		16.4889		4423.2046994326		18.3617		142.108		143.107		0.142108		16.49295		3966.2577269292		18.4028		155.352		155.569		0.155352		16.48873		3010.4380533074		0.152188		16.4901933333		0.0089288396

																						22.0597		400.911		386.481		0.400911		17.04955		0		22.0695		201.962		200.279		0.201962		17.02913		0		22.048		200.773		198.167		0.200773		17.0243		0		0.2013675		201.3675		17.026715		0.00084075		18.8193		163.272		159.75		0.163272		17.0055		4539.0780727434		18.876		145.067		146.692		0.145067		17.00725		4048.8439051456		18.9195		157.264		159.304		0.157264		17.00543		3047.4891215777		0.155201		17.00606		0.0092761783

																						22.5773		396.686		393.842		0.396686		17.56715		0		22.586		207.098		204.885		0.207098		17.54563		0		22.5633		200.721		201.326		0.200721		17.5396		0		0.2039095		203.9095		17.542615		0.0045092199		19.3328		166.166		163.781		0.166166		17.519		4619.5333372254		19.3903		151.593		150.252		0.151593		17.52155		4230.9856418947		19.4347		162.505		162.996		0.162505		17.52063		3149.0501303667		0.160088		17.5203933333		0.0075811938

																						23.092		405.768		401.057		0.405768		18.08185		0		23.1027		212.034		209.475		0.212034		18.06233		0		23.0807		205.638		204.483		0.205638		18.057		0		0.208836		208.836		18.059665		0.004522655		19.8485		169.769		167.804		0.169769		18.0347		4719.6993074842		19.9078		154.837		153.806		0.154837		18.03905		4321.5262171344		19.9492		165.168		166.652		0.165168		18.03513		3200.6542071469		0.163258		18.0362933333		0.0076470407

																						23.6068		406.793		408.171		0.406793		18.59665		0		23.62		217.875		214.052		0.217875		18.57963		0		23.5987		210.193		207.628		0.210193		18.575		0		0.214034		214.034		18.577315		0.0054319943		20.364		174.218		171.803		0.174218		18.5502		4843.3846812509		20.423		157.124		157.319		0.157124		18.55425		4385.3567644751		20.4653		169.12		170.288		0.16912		18.55123		3277.2367499315		0.1668206667		18.5518933333		0.0087758993

																						24.1217		414.829		415.184		0.414829		19.11155		0		24.1362		222.541		218.6		0.222541		19.09583		0		24.1148		212.944		210.747		0.212944		19.0911		0		0.2177425		217.7425		19.093465		0.0067861038		20.8797		177.027		175.779		0.177027		19.0659		4921.4768850969		20.9385		161.804		160.809		0.161804		19.06975		4515.9763366457		20.9833		172.971		173.905		0.172971		19.06923		3351.8620971641		0.1706006667		19.0682933333		0.0078834505

																						24.6372		417.96		422.105		0.41796		19.62705		0		24.6513		226.419		223.122		0.226419		19.61093		0		24.6305		216.372		213.848		0.216372		19.6068		0		0.2213955		221.3955		19.608865		0.0071043018		21.3948		180.086		179.728		0.180086		19.581		5006.5192672844		21.4547		165.976		164.277		0.165976		19.58595		4632.4175449996		21.4985		176.142		177.471		0.176142		19.58443		3413.3102862253		0.174068		19.5837933333		0.0072800503

																						25.1522		427.033		428.922		0.427033		20.14205		0		25.1685		230.21		227.642		0.23021		20.12813		0		25.1472		219.571		216.94		0.219571		20.1235		0		0.2248905		224.8905		20.125815		0.007522909		21.9088		184.962		183.644		0.184962		20.095		5142.0755456585		21.9693		169.612		167.71		0.169612		20.10055		4733.8989049168		22.013		175.526		181.002		0.175526		20.09893		3401.3733311759		0.1767		20.09816		0.0077420496

																						25.6698		429.156		435.675		0.429156		20.65965		0		25.6837		235.274		232.127		0.235274		20.64333		0		25.6638		222.82		220.016		0.22282		20.6401		0		0.229047		229.047		20.641715		0.0088063079		22.4255		188.036		187.558		0.188036		20.6117		5227.5349385465		22.4848		172.258		171.123		0.172258		20.61605		4807.7492014902		22.5287		183.177		184.511		0.183177		20.61463		3549.6357387783		0.181157		20.6141266667		0.0080806325

																						26.1867		426.487		442.322		0.426487		21.17655		0		26.1995		239.171		236.6		0.239171		21.15913		0		26.1795		227.369		223.072		0.227369		21.1558		0		0.23327		233.27		21.157465		0.0083452742		22.9397		191.595		191.429		0.191595		21.1259		5326.4776774172		22.9992		176.337		174.503		0.176337		21.13045		4921.5947644996		23.0427		187.278		187.978		0.187278		21.12863		3629.1056294564		0.18507		21.1283266667		0.0078649914

																						26.7042		440.076		448.881		0.440076		21.69405		0		26.714		245.395		241.043		0.245395		21.67363		0		26.6955		230.784		226.116		0.230784		21.6718		0		0.2380895		238.0895		21.672715		0.0103315372		23.4547		194.354		195.283		0.194354		21.6409		5403.1798455948		23.5162		180.204		177.877		0.180204		21.64745		5029.5233725304		23.5588		189.533		191.43		0.189533		21.64473		3672.8034113337		0.1880303333		21.64436		0.0071936868

																						27.2185		437.621		455.308		0.437621		22.20835		0		27.231		247.391		245.49		0.247391		22.19063		0		27.2115		233.469		229.144		0.233469		22.1878		0		0.24043		240.43		22.189215		0.0098443406		23.9713		198.946		199.128		0.198946		22.1575		5530.8407213729		24.0297		181.709		181.203		0.181709		22.16095		5071.5281708459		24.0732		195.85		194.84		0.19585		22.15913		3795.2153351116		0.1921683333		22.1591933333		0.0091893713

																						27.7333		448.335		461.649		0.448335		22.72315		0		27.7473		250.882		249.914		0.250882		22.70693		0		27.7278		238.587		232.16		0.238587		22.7041		0		0.2447345		244.7345		22.705515		0.0086938779		24.4865		204.485		202.938		0.204485		22.6727		5684.8288727089		24.5435		186.315		184.506		0.186315		22.67475		5200.0823908071		24.5902		198.89		198.239		0.19889		22.67613		3854.1249834074		0.1965633333		22.6745266667		0.0093057648

																						28.2482		464.233		467.9		0.464233		23.23805		0		28.263		256.588		254.314		0.256588		23.22263		0		28.244		236.346		235.161		0.236346		23.2203		0		0.246467		246.467		23.221465		0.0143132555		25.0022		208.287		206.729		0.208287		23.1884		5790.5271849276		25.058		188.572		187.79		0.188572		23.18925		5263.0756331979		25.108		202.08		201.613		0.20208		23.19393		3915.9413577705		0.1996463333		23.1905266667		0.0100802954

																						28.7648		463.018		474.083		0.463018		23.75465		0		28.7797		260.653		258.704		0.260653		23.73933		0		28.7602		239.602		238.146		0.239602		23.7365		0		0.2501275		250.1275		23.737915		0.0148853049		25.5172		212.371		210.493		0.212371		23.7034		5904.0652983155		25.5742		192.566		191.06		0.192566		23.70545		5374.5488321829		25.6237		205.523		204.944		0.205523		23.70963		3982.6604101003		0.2034866667		23.70616		0.0100583048

																						29.2818		463.988		480.182		0.463988		24.27165		0		29.2963		263.354		263.077		0.263354		24.25593		0		29.2768		246.061		241.121		0.246061		24.2531		0		0.2547075		254.7075		24.254515		0.0122279976		26.0337		215.14		214.245		0.21514		24.2199		5981.0454736269		26.0875		195.068		194.289		0.195068		24.21875		5444.3800649972		26.1388		206.606		208.244		0.206606		24.22473		4003.6469723057		0.2056046667		24.2211266667		0.0100733955

																						29.7972		476.984		486.174		0.476984		24.78705		0		29.813		267.963		267.433		0.267963		24.77263		0		29.7943		250.769		244.085		0.250769		24.7706		0		0.259366		259.366		24.771615		0.012157994		26.548		219.921		217.959		0.219921		24.7342		6113.9606842312		26.6037		200.607		197.512		0.200607		24.73495		5598.9744688975		26.6545		212.937		211.518		0.212937		24.74043		4126.3301905165		0.211155		24.7365266667		0.0097795343

																						30.3122		480.325		492.078		0.480325		25.30205		0		30.3277		273.075		271.754		0.273075		25.28733		0		30.311		254.935		247.031		0.254935		25.2873		0		0.264005		264.005		25.287315		0.012826917		27.0635		223.604		221.66		0.223604		25.2497		6216.3507115593		27.1177		201.749		200.697		0.201749		25.24895		5630.8478773203		27.1685		216.223		214.753		0.216223		25.25443		4190.0068695626		0.2138586667		25.2510266667		0.0111176801

																						30.8265		486.558		497.889		0.486558		25.81635		0		30.842		276.153		276.055		0.276153		25.80163		0		30.826		256.127		249.953		0.256127		25.8023		0		0.26614		266.14		25.801965		0.0141605204		27.5797		227.461		225.344		0.227461		25.7659		6323.5780630131		27.6338		204.313		203.873		0.204313		25.76505		5702.4095403642		27.6842		218.068		217.971		0.218068		25.77013		4225.7596001895		0.216614		25.7670266667		0.0116422963

																						31.3427		492.929		503.638		0.492929		26.33255		0		31.357		278.251		280.345		0.278251		26.31663		0		31.3427		257.919		252.87		0.257919		26.319		0		0.268085		268.085		26.317815		0.0143768951		28.0943		230.334		228.995		0.230334		26.2805		6403.4495125145		28.1495		208.239		207.022		0.208239		26.28075		5811.9848481296		28.1992		221.66		221.158		0.22166		26.28513		4295.3660004128		0.2200776667		26.2821266667		0.0111321647

																						31.8598		504.189		509.316		0.504189		26.84965		0		31.8742		284.388		284.635		0.284388		26.83383		0		31.8592		263.319		255.772		0.263319		26.8355		0		0.2738535		273.8535		26.834665		0.0148980328		28.6088		233.466		232.623		0.233466		26.795		6490.5213467778		28.6663		211.5		210.156		0.2115		26.79755		5902.9998961742		28.7153		223.104		224.324		0.223104		26.80123		4323.3480833533		0.22269		26.7979266667		0.0109888505

																						32.3755		517.72		514.897		0.51772		27.36535		0		32.389		289.726		288.888		0.289726		27.34863		0		32.3755		268.496		258.659		0.268496		27.3518		0		0.279111		279.111		27.350215		0.015011877		29.1235		236.213		236.231		0.236213		27.3097		6566.889906395		29.1825		212.8		213.262		0.2128		27.31375		5939.283110666		29.2305		228.416		227.456		0.228416		27.31643		4426.2849424807		0.2258096667		27.3132933333		0.0119221169

																						32.8912		521.145		520.398		0.521145		27.88105		0		32.9063		291.537		293.145		0.291537		27.86593		0		32.8913		272.683		261.529		0.272683		27.8676		0		0.28211		282.11		27.866765		0.0133317913		29.6388		240.395		239.822		0.240395		27.825		6683.1524896929		29.6972		216.235		216.336		0.216235		27.82845		6035.1545274195		29.7448		232.079		230.557		0.232079		27.83073		4497.2671930425		0.2295696667		27.82806		0.012273914

																						33.4075		540.565		525.827		0.540565		28.39735		0		33.4195		292.446		297.351		0.292446		28.37913		0		33.4083		276.582		264.392		0.276582		28.3846		0		0.284514		284.514		28.381865		0.011217542		30.1528		241.819		243.383		0.241819		28.339		6722.7407055265		30.2133		218.827		219.397		0.218827		28.34455		6107.4976750833		30.2602		234.141		233.637		0.234141		28.34613		4537.22498738		0.2315956667		28.3432266667		0.0117054285

																						33.9222		546.004		531.162		0.546004		28.91205		0		33.9338		298.51		301.55		0.29851		28.89343		0		33.923		278.54		267.228		0.27854		28.8993		0		0.288525		288.525		28.896365		0.0141209224		30.669		245.223		246.937		0.245223		28.8552		6817.3743338254		30.7268		219.633		222.42		0.219633		28.85805		6129.9932680682		30.7768		238.728		236.698		0.238728		28.86273		4626.1126705158		0.234528		28.85866		0.0133019557

																						34.4397		557.071		536.449		0.557071		29.42955		0		34.4482		302.543		305.731		0.302543		29.40783		0		34.4402		282.731		270.065		0.282731		29.4165		0		0.292637		292.637		29.412165		0.0140091995		31.1837		247.773		250.46		0.247773		29.3699		6888.2661529095		31.2407		224.289		225.423		0.224289		29.37195		6259.942996279		31.2913		240.598		239.721		0.240598		29.37723		4662.3498554873		0.2375533333		29.3730266667		0.0120344115

																						34.956		569.734		541.649		0.569734		29.94585		0		34.9617		307.874		309.889		0.307874		29.92133		0		34.9552		285.573		272.875		0.285573		29.9315		0		0.2967235		296.7235		29.926415		0.0157691883		31.6992		253.832		253.968		0.253832		29.8854		7056.7106751959		31.7563		228.068		228.414		0.228068		29.88755		6365.4155097903		31.8047		243.306		242.71		0.243306		29.89063		4714.8259500876		0.2417353333		29.88786		0.0129536161

																																														34.9897		292.009		273.063																32.2133		254.494		257.446								32.2723		230.339		231.386

																																														37.006		297.335		283.934																32.7295		257.442		260.916								32.7865		231.024		234.325

																																														39.0237		308.862		294.608

																																														41.0403		320.996		305.077

																																														43.0557		329.492		315.343

																																														45.0713		345.69		325.418

																																														47.0867		354.246		335.302

																																														49.1042		362.728		345.011

																																														51.1205		376.351		354.533

																																														53.1362		389.71		363.873

																																														55.1532		392.577		373.044

																																														57.1695		405.164		382.04

																																														59.186		414.637		390.868

																																														61.2008		420.589		399.524

																																														63.2182		431.634		408.027

																																														65.2342		439.146		416.366

																																														67.2513		444.699		424.553

																																														69.2672		456.931		432.581

																																														71.2837		461.282		440.461

																																														73.299		461.286		448.188

																																														75.313		469.976		455.766

																																														77.33		479.586		463.213

																																														79.3458		480.563		470.517

																																														81.3612		487.824		477.681

																																														83.3758		490.395		484.709

																																														85.3912		503.278		491.607

																																														87.4068		514.584		498.377

																																														89.4232		512.657		505.023

																																														91.4398		519.238		511.545

																																														93.4568		523.256		517.945

																																														95.4722		528.129		524.221

																																														97.4885		529.363		530.381

																																														99.505		534.338		536.427

																																														101.522		542.743		542.36

																																														103.538		552.823		548.18

																																														105.555		552.419		553.892

																																														107.569		556.751		559.49

																																														109.586		562.863		564.991

																																														111.603		560.577		570.389

																																														113.618		572.223		575.682

																																														115.635		578.389		580.879

																																														117.651		581.359		585.976

																																														119.665		586.418		590.973

																																														121.682		591.169		595.883

																																														123.698		590.501		600.699

																																														125.713		594.181		605.423

																																														127.73		606.492		610.061

																																														129.746		608.954		614.612

																																														131.762		611.761		619.077

																																														133.777		617.825		623.456

																																														135.793		616.068		627.755

																																														137.809		624.655		631.972

																																														139.825		631.167		636.111

																																														141.841		628.12		640.174

																																														143.856		637.212		644.157

																																														145.87		638.024		648.065

																																														147.887		635.7		651.903

																																														149.902		647.984		655.666

																																														151.919		652.683		659.364

																																														153.934		654.937		662.988

																																														155.949		659.324		666.544

																																														157.965		660.352		670.035

																																														159.98		673.637		673.457

																																														161.997		667.148		676.821

																																														164.014		669.716		680.121

																																														166.03		675.479		683.357

																																														168.043		679.675		686.529

																																														170.06		682.505		689.646

																																														172.077		684.189		692.705

																																														174.093		682.771		695.706

																																														176.11		686.857		698.651

																																														178.127		687.549		701.541

																																														180.142		694.32		704.374

																																														182.16		688.409		707.159

																																														184.175		696.92		709.887

																																														186.19		694.921		712.564

																																														188.205		698.399		715.191

																																														190.222		704.805		717.77

																																														192.24		709.186		720.303

																																														194.255		716.455		722.785

																																														196.273		709.834		725.224

																																														198.287		720.678		727.612

																																														200.302		721.314		729.956

																																														202.32		723.306		732.261

																																														204.337		726.912		734.52

																																														206.352		727.387		736.735

																																														208.367		727.54		738.909

																																														210.383		732.87		741.044

																																														212.402		739.167		743.14

																																														214.417		740.114		745.194

																																														216.432		737.977		747.209

																																														218.448		739.666		749.188

																																														220.463		744.98		751.128

																																														222.482		744.232		753.035

																																														224.497		749.415		754.903

																																														226.513		748.312		756.738

																																														228.528		754.098		758.537

																																														230.545		758.482		760.303

																																														232.562		758.345		762.037

																																														234.578		755.266		763.738

																																														236.593		765.514		765.405

																																														238.608		754.554		767.041

																																														240.622		759.894		768.646

																																														242.64		765.559		770.224

																																														244.657		767.681		771.771

																																														246.672		767.562		773.288

																																														248.685		762.281		774.776

																																														250.7		764.035		776.236

																																														252.717		774.134		777.671

																																														254.733		770.658		779.078

																																														256.748		773.489		780.458

																																														258.763		776.13		781.813

																																														260.78		773.815		783.143

																																														262.798		776.616		784.449

																																														264.815		774.77		785.729

																																														266.832		780.13		786.985

																																														268.847		781.773		788.217

																																														270.862		780.315		789.426

																																														272.88		785.827		790.614

																																														274.895		782.974		791.778

																																														276.913		789.65		792.922

																																														278.928		785.054		794.043

																																														280.945		777.32		795.143

																																														282.963		795.198		796.224

																																														284.978		791.429		797.282

																																														286.995		798.481		798.322

																																														289.008		791.321		799.341

																																														291.022		795.288		800.34

																																														293.04		801.304		801.323

																																														295.057		797.401		802.287

																																														297.07		795.97		803.232

																																														299.087		800.626		804.16

																																														301.103		797.55		805.07

																																														303.123		801.937		805.966

																																														305.138		799.829		806.842

																																														307.153		808.951		807.701

																																														309.17		801.994		808.546

																																														311.187		807.525		809.374

																																														313.205		807.22		810.188

																																														315.222		811.813		810.985

																																														317.24		806.836		811.769

																																														319.255		817.03		812.536

																																														321.272		816.193		813.29

																																														323.29		813.475		814.03

																																														325.308		813.61		814.756

																																														327.323		806.105		815.467

																																														329.34		803.975		816.166

																																														331.357		811.009		816.851

																																														333.375		815.593		817.525

																																														335.39		823.213		818.184

																																														337.405		820.543		818.831

																																														339.422		818.475		819.467

																																														341.438		823.04		820.09

																																														343.457		832.25		820.703

																																														345.473		836.258		821.303

																																														347.49		844.829		821.892

																																														349.507		844.861		822.47

																																														351.522		855.825		823.037

																																														353.542		851.248		823.595

																																														355.557		864.505		824.14

																																														357.573		868.926		824.676

																																														359.588		864.913		825.202

																																														361.605		870.501		825.718

																																														363.623		874.585		826.225

																																														365.638		876.227		826.721

																																														367.655		879.985		827.209





GLP-PX 50K 12FULL 

		



GLP-PX 25K 1:3 FaSSIF

GLP-PX 25K 1:3 pH 6.8

Time (min)

Dissolved (mg)



 FULL ALL

		GLP-PX 50K 1:3								445.54																GLP-PX 50K -1				17J-31003								GLP-PX 50K -2				17J-31001								GLP-PX 50K -3				17K-02001				GLP-PX 50K 1:3 pH 6.8												GLP-PX 50K FaSSIF-1				17K-08002								GLP-PX 50K FaSSIF-2				17K-08004								GLP-PX 50K FaSSIF-3				17K-08006				GLP-PX 50K 1:3 FaSSIF

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/ml)		IDR (ug/min/cm2)

		GLP-PX 50K -1		17J-31003		0.381		16.332		0.24		3.84		9.93		13.0791		186.8441

		GLP-PX 50K -2		17J-31001		0.409		18.7		0.24		4.40		9.30		14.2532		203.6177				Dissolution Profile												Dissolution Profile												Dissolution Profile																				Dissolution Profile												Dissolution Profile												Dissolution Profile

		GLP-PX 50K -3		17K-02001		0.425		18.96		0.24		4.46		9.53		21.8965		312.8071																																								AVERAGE				TIME		SD																																						AVERAGE		TIME		SD

																						Time (minutes)		Weight (µg)		Weight (µg)		mg		Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (µg)		mg		Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)				Time zero (min)		%		mg		Weight (µg)						Time (minutes)		Weight (µg)				mg		Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (µg)		mg		Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (µg)		mg		Time zero (min)		%		mg

																						5		24		21		0.0242729		0		632.1638631322		5		9		-9		0.00917801		0		208.7633661407		5		0.0252023		0.130568				0		0.5653914216		0.01955107		19.55107		0		0.0122560546		1.83125		3.55054				0.00355054		0		98.7075448356		1.87005		5.26888		3.59808		0.00526888		0		147.0553101322		2.20468		5.21157		6.08559		0.00521157		0		100.9907091346		0.0046769967		0		0.0009759608

		AVG				0.405								9.587		16.410		234.423				6		32		29		0.0320204		0.5237		833.9398985304		6		13		1		0.0129996		0.52162		295.6893982991		6		0.0356872		0.135983				0.52136		0.800610926		0.0269024		26.9024		0.52253		0.0096365901		2.34897		8.33932				0.00833932		0.51772		231.8390449899		2.38958		15.7602		9.93595		0.0157602		0.51953		439.8697823342		2.71927		14.0604		13.5465		0.0140604		0.51459		272.4648746377		0.0127199733		0.51728		0.0038877915

		SD				0.022								0.321		4.788		68.399				6		39		37		0.0391721		1.04454		1020.1989075472		6		17		11		0.0173641		1.04272		394.9644820613		6		0.0478648		0.141362				1.0422		1.0738046652		0.0348003333		34.8003333333		1.04337		0.0117151567		2.86588		14.039				0.014039		1.03463		390.2942149496		2.90365		21.1729		16.2059		0.0211729		1.0336		590.9391323958		3.23412		18.5538		20.916		0.0185538		1.02944		359.5387607077		0.0179219		1.0325566667		0.0036086847

		RSD				5.448								3.348		29.178		29.178				7		47		44		0.0474368		1.56902		1235.4449094517		7		24		21		0.0242554		1.56147		551.7142551696		7		0.0650718		0.146719				1.56406		1.4598285674		0.045588		45.588		1.56654		0.0135090356		3.38515		15.6855				0.0156855		1.5539		436.0680895072		3.42032		26.6923		22.5062		0.0266923		1.55027		744.9864970622		3.75105		27.9017		28.2207		0.0279017		1.54637		540.6839914		0.0234265		1.55018		0.0067311197

		GLP-PX 50K FaSSIF-1		17K-08002		0.318		15.3		0.24		3.60		8.85		8.55		122.07				7		54		52		0.0540174		2.0935		1406.8301793506		7		30		30		0.0298619		2.0823		679.2399183872		7		0.0738963		0.152071				2.08855		1.657798459		0.0525918667		52.5918666667		2.091025		0.018006596		3.9013		21.72				0.02172		2.07005		603.8314943161		3.93698		30.8761		28.8053		0.0308761		2.06693		861.7570453629		4.26615		34.2566		35.4064		0.0342566		2.06147		663.8303479642		0.0289509		2.06615		0.0064862455

		GLP-PX 50K FaSSIF-2		17K-08004		0.370		15.24		0.24		3.58		10.34		9.98		142.62				8		61		59		0.0606473		2.61537		1579.4994193746		8		38		40		0.038031		2.60287		865.0545791187		8		0.0924418		0.157374				2.6112		2.0738504308		0.0637067		63.7067		2.613285		0.0181353833		4.41693		25.9182				0.0259182		2.58568		720.5444491706		4.45313		35.9072		35.0969		0.0359072		2.58308		1002.1758764629		4.78022		41.0396		42.4862		0.0410396		2.57554		795.2725007243		0.0342883333		2.5814333333		0.0076895859

		GLP-PX 50K FaSSIF-3		17K-08006		0.313		21.95		0.24		5.16		6.07		13.88		198.30				8		67		66		0.0674827		3.13699		1757.5207052554		9		45		49		0.0452387		3.12475		1029.0011987162		8		0.0928466		0.162595				3.12891		2.0829317626		0.0685226667		68.5226666667		3.13295		0.0236145607		4.93282		31.3096				0.0313096		3.10157		870.4292152137		4.96848		39.6152		41.3774		0.0396152		3.09843		1105.6667682597		5.2961		47.8337		49.5004		0.0478337		3.09142		926.9297512133		0.0395861667		3.09714		0.0082620883

		AVG				0.334								8.420		10.803		154.328				9		74		74		0.0742161		3.65782		1932.8855012218		9		55		59		0.0553144		3.64818		1258.1834558966		9		0.110163		0.167794				3.6474		2.4714099575		0.0798978333		79.8978333333		3.65261		0.0187662633		5.44843		35.0636				0.0350636		3.61718		974.7930931908		5.48438		44.3208		47.6633		0.0443208		3.61433		1237.0008406542		5.81147		56.2741		56.4179		0.0562741		3.60679		1090.4892891989		0.0452195		3.6127666667		0.0106337704

		SD				0.032								2.167		2.761		39.439				9		80		81		0.0804019		4.17787		2093.9885925114		10		63		68		0.0626254		4.17007		1424.4797412411		10		0.120347		0.173004				4.17006		2.6998790352		0.0877914333		87.7914333333		4.173965		0.0240192646		5.96355		39.9289				0.0399289		4.1323		1110.0519039318		5.99922		49.3492		53.935		0.0493492		4.12917		1377.3443143086		6.32605		61.6543		63.2368		0.0616543		4.12137		1194.7477397783		0.0503108		4.1276133333		0.0108945747

		RSD				9.478								25.739		25.555		25.555				10		87		88		0.0869104		4.69767		2263.4960886572		10		71		77		0.0706885		4.69275		1607.8833219224		10		0.13255		0.178181				4.69243		2.9736426011		0.0967163		96.7163		4.69505		0.0253216735		6.48022		43.8374				0.0438374		4.64897		1218.7109921241		6.51458		53.0963		60.212		0.0530963		4.64453		1481.9264935567		6.84272		68.3028		69.9958		0.0683028		4.63804		1323.5835281647		0.0550788333		4.6438466667		0.0123526021

																						10		94		95		0.0935444		5.21742		2436.2721091582		11		80		86		0.0796461		5.21325		1811.6332337815		11		0.138593		0.183282				5.21013		3.1092119881		0.1039278333		103.9278333333		5.213775		0.0274269399		6.99453		47.4045				0.0474045		5.16328		1317.878916773		7.02917		61.8427		66.4781		0.0618427		5.15912		1726.0399606578		7.35652		77.142		76.6314		0.077142		5.15184		1494.8710818544		0.0621297333		5.15808		0.0148708277

																						11		100		102		0.0998038		5.73642		2599.2920402291		11		89		95		0.0889062		5.73625		2022.2638221988		11		0.148674		0.188383				5.73103		3.3353703514		0.1124613333		112.4613333333		5.733725		0.0261155695		7.50885		52.1456				0.0521456		5.6776		1449.684878914		7.54402		66.8073		72.7463		0.0668073		5.67397		1864.6027657857		7.87265		85.9407		83.212		0.0859407		5.66797		1665.3738195059		0.0682978667		5.67318		0.0169467855

																						11		107		109		0.107277		6.25702		2793.9242012794		12		98.0204		104		0.0980204		6.25785		2229.5757636414		12		0.169928		0.193457				6.25213		3.8121851371		0.1250751333		125.0751333333		6.254575		0.0269727747		8.025		57.5501				0.0575501		6.19375		1599.9338343022		8.06093		74.301		79.0383		0.074301		6.19088		2073.7531691992		8.38985		92.788		89.7218		0.092788		6.18517		1798.0619888401		0.0748797		6.1899333333		0.0176260764

																						12		114		116		0.113944		6.77792		2967.5596743998		12		107		112		0.107115		6.77785		2436.4418827351		12		0.173985		0.198486				6.77163		3.9032003618		0.1316813333		131.6813333333		6.774775		0.0344633053		8.54115		60.9842				0.0609842		6.7099		1695.4042640734		8.5763		80.8136		85.3102		0.0808136		6.70625		2255.5209097374		8.90443		101.048		96.1159		0.101048		6.69975		1958.1257042755		0.0809486		6.7053		0.0200322412

																						12		121		123		0.120972		7.29952		3150.597038295		13		116		120.932		0.115686		7.29945		2631.3981762227		13		0.174604		0.20348				7.29063		3.9170870821		0.1370873333		137.0873333333		7.295075		0.0322415192		9.05963		64.5967				0.0645967		7.22838		1795.8343411092		9.09115		87.7686		91.5746		0.0877686		7.2211		2449.6361072688		9.42032		103.08		102.444		0.10308		7.21564		1997.5021533996		0.0851484333		7.2217066667		0.0193749852

																						13		127		130		0.127205		7.82082		3312.9294072704		13		124		129		0.124254		7.82115		2826.2862315956		13		0.191684		0.208418				7.80673		4.300261851		0.1477143333		147.7143333333		7.813775		0.0282562562		9.57578		70.2109				0.0702109		7.74453		1951.9131060903		9.60547		94.4433		97.8312		0.0944433		7.73542		2635.9280855525		9.93542		111.492		108.682		0.111492		7.73074		2160.5113512498		0.0920487333		7.7368966667		0.0207444635

																						13		135		137		0.1349		8.34192		3513.3381316834		14		131		138		0.130956		8.34015		2978.730179671		14		0.199825		0.213365				8.32683		4.4828980217		0.155227		155.227		8.334375		0.0339800622		10.0925		75.6816				0.0756816		8.26125		2104.0024687034		10.1198		99.5962		104.087		0.0995962		8.24975		2779.7463747487		10.4503		114.067		114.838		0.114067		8.24562		2210.4101487372		0.0964482667		8.2522066667		0.0193853513

																						14		141		143.748		0.140767		8.86122		3666.13838979		14		142		146		0.141543		8.86065		3219.5424861875		14		0.20367		0.21829				8.84763		4.5691572129		0.1619933333		161.9933333333		8.854425		0.0338753624		10.6102		79.6581				0.0796581		8.77895		2214.5520054045		10.6367		104.86		110.372		0.10486		8.76665		2926.6599012427		10.9667		123.896		120.933		0.123896		8.76202		2400.8782188358		0.1028047		8.7692066667		0.0221904516

																						14		148		150		0.147798		9.38022		3849.2538857416		15		150		154		0.149957		9.38255		3410.9276516763		15		0.212762		0.223176				9.36743		4.7731282316		0.1701723333		170.1723333333		9.373825		0.0316528778		11.1253		84.7097				0.0847097		9.29405		2354.9900890457		11.1508		111.601		116.622		0.111601		9.28075		3114.8023234654		11.4831		126.011		126.949		0.126011		9.27842		2441.8630563837		0.1074405667		9.2844066667		0.0209626155

																						15		155.514		157		0.155514		9.90102		4050.2095345486		15		160		163		0.159786		9.90415		3634.4984612305		15		0.229384		0.228034				9.88723		5.1460281737		0.1815613333		181.5613333333		9.894125		0.0318905421		11.6409		91.9148				0.0919148		9.80965		2555.2970089212		11.6646		117.602		122.868		0.117602		9.79455		3282.2912235928		11.9969		131.395		132.86		0.131395		9.79222		2546.1951440234		0.1136372667		9.7988066667		0.0200364887

																						15		161		164		0.161364		10.42162		4202.5670443362		16		168.057		171		0.168057		10.42555		3822.6309432555		16		0.227966		0.232866				10.40733		5.1142165916		0.1857956667		185.7956666667		10.414475		0.0374889263		12.156		97.7216				0.0977216		10.32475		2716.7301912967		12.1805		121.265		129.137		0.121265		10.31045		3384.5261579648		12.5141		142.233		138.733		0.142233		10.30942		2756.2157914676		0.1204065333		10.3148733333		0.0222681141

																						16		168		171		0.16816		10.94222		4379.5621958775		16		177		178		0.176862		10.94615		4022.9098096839		16		0.238832		0.237669				10.92733		5.3579857391		0.194618		194.618		10.934775		0.03231125		12.6732		102.603				0.102603		10.84195		2852.436593523		12.6956		126.535		135.396		0.126535		10.82555		3531.6127274818		13.0307		145.49		144.525		0.14549		10.82602		2819.330503474		0.124876		10.8311733333		0.0214915775

																						17		175		177		0.175147		11.46302		4561.5317550033		17		185		186		0.185114		11.46585		4210.6101169829		17		0.247147		0.242457				11.44873		5.5445254466		0.2024693333		202.4693333333		11.455875		0.0342557631		13.187		107.153				0.107153		11.35575		2978.9298393397		13.2115		132.518		141.663		0.132518		11.34145		3698.5992446393		13.5453		152.088		150.22		0.152088		11.34062		2947.1876940845		0.1305863333		11.34594		0.0225296928

																						17		181		183.629		0.180952		11.98312		4712.7172839464		17		193		194		0.193108		11.98565		4392.441946424		17		0.261134		0.247201				11.96843		5.8583114825		0.2117313333		211.7313333333		11.975775		0.035236723		13.7037		113.953				0.113953		11.87245		3167.9746902306		13.726		136.585		147.913		0.136585		11.85595		3812.1098856688		14.0625		155.908		155.871		0.155908		11.85782		3021.21231793		0.135482		11.8620733333		0.0209992372

																						18		187		190		0.187385		12.50462		4880.2584566752		18		201		202		0.201034		12.50735		4572.7270452669		18		0.264912		0.251907				12.48693		5.9430675877		0.217777		217.777		12.495775		0.0392369303		14.2175		119.919				0.119919		12.38625		3333.8337461739		14.2404		146.656		154.158		0.146656		12.37035		4093.1931573207		14.5781		159.498		161.432		0.159498		12.37342		3090.7799618056		0.1420243333		12.3766733333		0.0201919182

																						18		193		196.586		0.19347		13.02492		5038.7363108731		18		208		209.391		0.207707		13.02735		4724.5113582342		18		0.26924		0.25659				13.00593		6.0401624589		0.2234723333		223.4723333333		13.015425		0.0378132771		14.7328		125.088				0.125088		12.90155		3477.5356335644		14.7563		153.845		160.421		0.153845		12.88625		4293.8393334606		15.0979		167.703		166.966		0.167703		12.89322		3249.777877683		0.1488786667		12.8936733333		0.021737247

																						19		200		203		0.200143		13.54532		5212.528048106		19		215.363		217		0.215363		13.55155		4898.6550267607		19		0.275546		0.261276				13.52843		6.1816320194		0.2303506667		230.3506666667		13.536875		0.0363060485		15.2495		131.892				0.131892		13.41825		3666.6916873087		15.2729		165.371		166.692		0.165371		13.40285		4615.5318951784		15.6146		171.015		172.397		0.171015		13.40992		3313.9583892474		0.1560926667		13.41034		0.0211475267

																						19		205.812		209		0.205812		14.06542		5360.1715904968		19		224		224		0.224346		14.07455		5102.9826879903		19		0.281987		0.265901				14.04713		6.3261301861		0.2373816667		237.3816666667		14.056275		0.036119662		15.7656		136.697				0.136697		13.93435		3800.2741150338		15.7885		169.248		172.95		0.169248		13.91845		4723.739604859		16.1297		176.333		177.742		0.176333		13.92502		3417.0115174176		0.1607593333		13.92594		0.0211375547

																						20		212		216		0.212465		14.58512		5533.4424473544		20		233		232		0.232605		14.59665		5290.8422175568		20		0.289445		0.270539				14.57023		6.4934438528		0.2448383333		244.8383333333		14.577675		0.0357712874		16.2823		141.307				0.141307		14.45105		3928.4354036525		16.3031		180.298		179.193		0.180298		14.43305		5032.1469280398		16.6469		180.826		183.04		0.180826		14.44222		3504.077652218		0.167477		14.4421066667		0.0226654224

																						20		221		221.952		0.221172		15.10582		5760.2077187596		21		239.892		239		0.239892		15.11985		5456.5925979842		20		0.294473		0.275097				15.08743		6.606242608		0.2518456667		251.8456666667		15.096625		0.035277804		16.7968		143.299				0.143299		14.96555		3983.8144246781		16.8185		180.984		185.445		0.180984		14.94845		5051.2933012255		17.1607		187.359		188.235		0.187359		14.95602		3630.6752615327		0.1705473333		14.9566733333		0.0238120538

																						21		228		228		0.228136		15.62492		5941.5782654538		21		249		246		0.249121		15.63955		5666.5157846132		21		0.301721		0.279652				15.60723		6.7688451095		0.2596593333		259.6593333333		15.616075		0.0339061737		17.314		151.188				0.151188		15.48275		4203.1342524249		17.3328		188.809		191.683		0.188809		15.46275		5269.6903423014		17.6745		193.835		193.365		0.193835		15.46982		3756.1683149418		0.177944		15.4717733333		0.0233072483

																						21		235		234		0.235289		16.14482		6127.8711316949		22		258		253		0.257817		16.16015		5864.3153328769		21		0.307027		0.28416				16.12473		6.88788055		0.266711		266.711		16.134775		0.0337843224		17.832		156.687				0.156687		16.00075		4356.0103752262		17.8492		194.606		197.944		0.194606		15.97915		5431.4855687701		18.188		199.315		198.427		0.199315		15.98332		3862.3607072646		0.183536		15.98774		0.0233708209

																						22		243		241		0.242963		16.66542		6327.7329317137		22		265		260		0.265187		16.68255		6031.9536344757		22		0.319842		0.288638				16.64193		7.1753737973		0.2759973333		275.9973333333		16.653675		0.0325286742		18.3467		162.612				0.162612		16.51545		4520.7296019216		18.3662		205.451		204.212		0.205451		16.49615		5734.1713081271		18.7038		202.678		203.446		0.202678		16.49912		3927.5295056918		0.190247		16.5035733333		0.0239727408

																						22		250		247		0.250029		17.18692		6511.7599683221		23		272		267		0.271705		17.20655		6180.2123115206		23		0.322523		0.293141				17.16493		7.2355196729		0.281419		281.419		17.175925		0.0357325125		18.8633		169.1				0.1691		17.03205		4701.1006302422		18.8813		207.031		210.457		0.207031		17.01125		5778.2693688172		19.219		209.506		208.395		0.209506		17.01432		4059.8436762721		0.1952123333		17.0192066667		0.0226477785

																						23		257		252.743		0.25675		17.70882		6686.8018184559		23		279		274		0.278725		17.72815		6339.8894997464		23		0.326902		0.297572				17.68263		7.3337586842		0.287459		287.459		17.695725		0.0334844565		19.3837		177.138				0.177138		17.55245		4924.5627642805		19.3977		219.04		216.714		0.21904		17.52765		6113.4425402269		19.7347		213.547		213.285		0.213547		17.53002		4138.1508765233		0.2032416667		17.5367066667		0.0227726661

																						23		263		259		0.262832		18.22962		6845.2015405975		24		286		281		0.285957		18.24735		6504.3888480724		24		0.33115		0.301988				18.20163		7.4290588259		0.293313		293.313		18.215625		0.0324453991		19.901		183.617				0.183617		18.06975		5104.6835861808		19.9152		223.364		222.984		0.223364		18.04515		6234.1260936598		20.2508		219.808		218.118		0.219808		18.04612		4259.4776225694		0.2089296667		18.0536733333		0.0219933991

																						24		268		265		0.268378		18.74882		6989.6416686799		24		292		288		0.292297		18.76805		6648.5987303162		24		0.332267		0.30638				18.72073		7.4541177379		0.2976473333		297.6473333333		18.734775		0.0316806938		20.4148		191.012				0.191012		18.58355		5310.2698615246		20.4307		232.797		229.229		0.232797		18.56065		6497.4026800457		20.768		221.31		222.898		0.22131		18.56332		4288.5836395892		0.2150396667		18.5691733333		0.021586671

																						24		274		271		0.274181		19.27032		7140.7751095854		25		298		294		0.298308		19.28885		6785.3251659892		25		0.343606		0.310732				19.23823		7.7084982241		0.305365		305.365		19.254275		0.0291813559		20.9333		199.853				0.199853		19.10205		5556.0559683962		20.9467		237.132		235.478		0.237132		19.07665		6618.3932452935		21.283		229.329		227.597		0.229329		19.07832		4443.9772151433		0.2221046667		19.0856733333		0.0196614904

																						25		281		276.644		0.280803		19.79112		7313.2386018612		25		306		301.006		0.305519		19.80785		6949.3468475128		25		0.345616		0.315075				19.75773		7.7535908052		0.310646		310.646		19.774425		0.0316378387		21.4508		204.593				0.204593		19.61955		5687.8313497524		21.4607		245.667		241.702		0.245667		19.59065		6856.606503515		21.8003		232.442		232.257		0.232442		19.59562		4504.3014701252		0.2275673333		19.60194		0.0209664053

																						25		286		283		0.285884		20.31282		7445.5682612169		26		312		308		0.311919		20.32835		7094.9214920491		26		0.34742		0.319366				20.27393		7.7940619577		0.3150743333		315.0743333333		20.293375		0.0299477903		21.9652		212.559				0.212559		20.13395		5909.2918324284		21.9773		259.28		247.957		0.25928		20.10725		7236.5475795747		22.3163		239.18		236.845		0.23918		20.11162		4634.8716050651		0.2370063333		20.1176066667		0.0234362237

																						26		292		288.372		0.29186		20.83362		7601.2073173692		26		317		314		0.317491		20.84855		7221.6624169485		26.15		0.354975		0.323646				20.79193		7.963551734		0.321442		321.442		20.812775		0.0278076932		22.4823		220.265				0.220265		20.65105		6123.5241296292		22.493		258.028		254.199		0.258028		20.62295		7201.6040530025		22.8328		238.11		241.379		0.23811		20.62812		4614.1369591188		0.238801		20.63404		0.0188909807

																						26		297		294		0.296954		21.35362		7733.8755489689		27		325		320		0.324784		21.36805		7387.5492736053		27		0.353675		0.327923				21.31243		7.934387378		0.3251376667		325.1376666667		21.333025		0.0290185051		22.9973		224.927				0.224927		21.16605		6253.1310553429		23.0097		262.573		260.451		0.262573		21.13965		7328.455752899		23.348		244.13		245.844		0.24413		21.14332		4730.7935652836		0.2438766667		21.1496733333		0.0188242785

																						27		303.075		300		0.303075		21.87432		7893.2909878423		27		332		327		0.331505		21.88835		7540.4253964066		27		0.362373		0.332163				21.83163		8.1295193535		0.3323176667		332.3176666667		21.852975		0.0253644561		23.5117		231.4				0.2314		21.68045		6433.085072963		23.5277		266.583		266.718		0.266583		21.65765		7440.3755145239		23.8648		247.832		250.266		0.247832		21.66012		4802.5315646228		0.248605		21.6660733333		0.017604233

																						27		308		305.639		0.308129		22.39432		8024.9174586913		28		336.464		333		0.336464		22.40865		7653.222999884		28		0.364522		0.336372				22.34993		8.1777302773		0.3363716667		336.3716666667		22.372125		0.0271310402		24.0265		238.779				0.238779		22.19525		6638.2265368929		24.0443		275.397		272.968		0.275397		22.17425		7686.3757087786		24.381		257.864		254.625		0.257864		22.17632		4996.9334039991		0.2573466667		22.18194		0.0183144808

																						28		314		311.334		0.314093		22.91592		8180.2439866184		28		344		338.897		0.344092		22.92785		7826.7297793407		28		0.37035		0.340554				22.86793		8.3084763284		0.342845		342.845		22.891925		0.02536536		24.5435		243.766				0.243766		22.71225		6776.8686944507		24.5605		288.389		279.211		0.288389		22.69045		8048.9845723772		24.8997		260.546		258.949		0.260546		22.69502		5048.9056660811		0.2642336667		22.69924		0.0225389041

																						28		319		317		0.319048		23.43632		8309.2920996094		29		350		345		0.349875		23.44855		7958.2701183021		29		0.36976		0.344723				23.38743		8.2952401976		0.3462276667		346.2276666667		23.411875		0.025824487		25.0612		249.57				0.24957		23.22995		6938.2240348287		25.0778		290.21		285.467		0.29021		23.20775		8099.8089828308		25.4163		259.881		263.202		0.259881		23.21162		5036.0191805164		0.2665536667		23.21644		0.0211257133

																						29		325		322.586		0.324967		23.95712		8463.4466466919		29		355		351		0.35466		23.96765		8067.1099111312		29		0.378198		0.348837				23.90313		8.4845393019		0.3526083333		352.6083333333		23.930125		0.0227892412		25.5763		254.84				0.25484		23.74505		7084.7337942692		25.5932		297.528		291.697		0.297528		23.72315		8304.0555702549		25.933		263.887		267.4		0.263887		23.72832		5113.6481446852		0.272085		23.7321733333		0.0224938156

																						30		330.361		328		0.330361		24.47812		8603.9280839217		30		359		357		0.35918		24.48755		8169.922003835		30		0.383876		0.352979				24.42523		8.611920235		0.3578056667		357.8056666667		24.451675		0.0240852571		26.093		261.23				0.26123		24.26175		7262.3803526799		26.1097		301.591		297.94		0.301591		24.23965		8417.4545706244		26.4505		268.655		271.551		0.268655		24.24582		5206.0432772755		0.2771586667		24.2490733333		0.0214822448

																						30		335		334		0.33526		24.99632		8731.5177318618		30		365		363		0.365046		25.00805		8303.3502639678		30		0.387453		0.357109				24.94893		8.6921670821		0.3625863333		362.5863333333		24.972625		0.0245128883		26.6073		265.07				0.26507		24.77605		7369.1350920065		26.6242		305.703		304.157		0.305703		24.75415		8532.2211690787		26.9667		271.515		275.638		0.271515		24.76202		5261.4648542907		0.2807626667		24.7640733333		0.0218380328

																						31		340		339		0.339999		25.51692		8854.9403367992		31		370		369		0.369522		25.52885		8405.1615309903		31		0.387856		0.36118				25.46823		8.7012080325		0.3657923333		365.7923333333		25.492575		0.0239618113		27.1232		271.25				0.27125		25.29195		7540.9435006102		27.1402		316.439		310.392		0.316439		25.27015		8831.8647004514		27.4828		276.276		279.673		0.276276		25.27812		5353.7243396645		0.2879883333		25.2800733333		0.0247668225

																						31		344.792		345		0.344792		26.03692		8979.7693187499		31		375		374		0.375191		26.04965		8534.108821596		31		0.395123		0.365221				25.98673		8.8642367823		0.371702		371.702		26.011825		0.0221322145		27.6378		276.53				0.27653		25.80655		7687.7312671843		27.6563		323.937		316.627		0.323937		25.78625		9041.1351175744		27.999		281.947		283.656		0.281947		25.79432		5463.6179631795		0.294138		25.7957066667		0.0259484349

																						32		350		350		0.35027		26.55592		9122.4384535562		32		379		380		0.378702		26.56865		8613.9701617471		32		0.398882		0.369214				26.50213		8.9485666392		0.3759513333		375.9513333333		26.529025		0.0226929485		28.1532		280.914				0.280914		26.32195		7809.6095945822		28.1705		326.059		322.836		0.326059		26.30045		9100.3604876911		28.5147		286.039		287.584		0.286039		26.31002		5542.9134502935		0.2976706667		26.3108066667		0.024718202

																						32.13		354		355		0.353888		27.07662		9216.6657134556		32		384		385.652		0.38441		27.08935		8743.8045478429		32		0.407815		0.37322				27.02213		9.1489706328		0.3820376667		382.0376666667		27.049375		0.0229691507		28.6693		286.655				0.286655		26.83805		7969.2134900181		28.6848		333.511		329.047		0.333511		26.81475		9308.3470372243		29.0288		291.803		291.451		0.291803		26.82412		5654.6092439702		0.3039896667		26.82564		0.0256954727

																						32.65		360		360.759		0.359919		27.59662		9373.73719064		33		389		391		0.389007		27.61015		8848.3680854887		33		0.400528		0.377166				27.53743		8.9854932007		0.3831513333		383.1513333333		27.567025		0.0241311673		29.1855		290.426				0.290426		27.35425		8074.0499801225		29.1997		333.317		335.262		0.333317		27.32965		9302.9324652156		29.5438		294.15		295.275		0.29415		27.33912		5700.0898178355		0.3059643333		27.3410066667		0.0237611726

																						33		364		366		0.364448		28.11792		9491.6905516363		34		393		397		0.39318		28.13385		8943.287302934		33		0.417695		0.381142				28.05963		9.3706197381		0.3917743333		391.7743333333		28.088775		0.0190669318		29.7022		296.448				0.296448		27.87095		8241.4658760144		29.7163		340.496		341.498		0.340496		27.84625		9503.2995397056		30.0605		298.432		299.062		0.298432		27.85582		5783.067157968		0.311792		27.8576733333		0.0248781787

																						34		368		371		0.3678		28.63982		9578.9901025436		34		398		402		0.397668		28.65555		9045.3715224151		34		0.412793		0.385073				28.57893		9.260647682		0.3927536667		392.7536666667		28.609375		0.0251087275		30.2232		302.037				0.302037		28.39195		8396.8440630187		30.2325		349.064		347.727		0.349064		28.36245		9742.4338333718		30.5755		301.315		302.789		0.301315		28.37082		5838.9344329801		0.317472		28.3750733333		0.0273618561

																						34		373		377		0.372856		29.15992		9710.6686614302		35		400		407.569		0.400237		29.17555		9103.8060945735		34		0.42402		0.388978				29.09793		9.5125155468		0.3990376667		399.0376666667		29.128925		0.0204219501		30.7388		306.836				0.306836		28.90755		8530.2596864636		30.7492		350.12		353.961		0.35012		28.87915		9771.9069676052		31.0922		306.543		306.48		0.306543		28.88752		5940.2435255099		0.3211663333		28.8914066667		0.0250750388

																						35		378		382		0.37786		29.68042		9840.9929313408		35		405		413		0.405423		29.69685		9221.7670487243		35		0.420148		0.392886				29.62023		9.4256506343		0.4011436667		401.1436666667		29.650325		0.0232246743		31.2538		310.582				0.310582		29.42255		8634.4011587337		31.2643		361.071		360.175		0.361071		29.39425		10077.5511844516		31.6075		330.277		310.114		0.330277		29.40282		6400.1651020406		0.3339766667		29.40654		0.0254470122

																						35		381		387		0.381317		30.20042		9931.0271042187		36		409		418		0.408676		30.21615		9295.7599110175		35		0.424978		0.396737				30.13813		9.5340074338		0.4049903333		404.9903333333		30.169275		0.0199498046		31.7698		318.368				0.318368		29.93855		8850.8575130038		31.7802		370.43		366.396		0.37043		29.91015		10338.7624186279		32.1282		313.201		313.739		0.313201		29.92352		6069.2634065473		0.3339996667		29.9240733333		0.0316551949

																																														36		0.43036		0.39703																32.288		319.873										32.2953		364.382		372.608								32.6455		315.437		317.294

																																														38		0.441628		0.41182																32.805		325.48										32.8122		371.037		378.839								33.1628		319.578		320.804

																																														40		0.449587		0.426287

																																														42		0.467425		0.440434

																																														44		0.476646		0.454229

																																														46		0.491633		0.467717

																																														48		0.498722		0.480906

																																														50		0.508338		0.493811

																																														52		0.521434		0.506419

																																														54		0.532445		0.518755

																																														56		0.545634		0.53081

																																														58		0.569832		0.542583

																																														60		0.601224		0.554098

																																														62		0.611504		0.565371

																																														64		0.628691		0.576385

																																														66		0.638727		0.58715

																																														68		0.64477		0.597675

																																														70		0.650988		0.607953

																																														72		0.662656		0.61799

																																														74		0.667496		0.627809

																																														76		0.676483		0.637398

																																														78		0.682457		0.646768

																																														80		0.688207		0.655933

																																														82		0.693999		0.664899

																																														84		0.69787		0.67367

																																														86		0.702171		0.682229

																																														88		0.709384		0.690594

																																														90		0.714322		0.698779

																																														92		0.719754		0.706778

																																														94		0.729501		0.71459

																																														96		0.729456		0.72223

																																														98		0.73587		0.729703

																																														100		0.744635		0.737003

																																														102		0.745855		0.744149

																																														104		0.751555		0.751125

																																														106		0.756208		0.757947

																																														108		0.761493		0.764609

																																														110		0.767786		0.771123

																																														112		0.769949		0.777501

																																														114		0.771824		0.783722

																																														116		0.779377		0.789811

																																														118		0.783948		0.795769

																																														120		0.792375		0.801585

																																														122		0.793773		0.807277

																																														124		0.795388		0.812827

																																														126		0.797166		0.818255

																																														128		0.804432		0.823571

																																														130		0.804512		0.828767

																																														132		0.81402		0.833844

																																														134		0.812172		0.838797

																																														136		0.815666		0.843648

																																														138		0.82207		0.848383

																																														140		0.822662		0.853015

																																														143		0.829527		0.857548

																																														144.53		0.830617		0.861968

																																														147		0.831328		0.866289

																																														149		0.836763		0.870518

																																														151		0.837519		0.874651

																																														153		0.845996		0.878696

																																														155		0.845068		0.882653

																																														157		0.848783		0.886512

																																														159		0.851756		0.890282

																																														161		0.854823		0.89398

																																														163		0.859075		0.897589

																																														165		0.857382		0.901112

																																														167		0.862484		0.904561

																																														168.76		0.867958		0.907928

																																														171		0.87044		0.911217

																																														173		0.872919		0.914439

																																														175		0.875765		0.917581

																																														176.83		0.876228		0.92065

																																														179		0.881369		0.923655

																																														181		0.883755		0.926593

																																														183		0.886405		0.929466

																																														185		0.891952		0.932271

																																														187		0.894334		0.935014

																																														188.94		0.896009		0.937696

																																														191		0.897546		0.940317

																																														193		0.901079		0.942882

																																														195		0.902345		0.945386

																																														197		0.903718		0.947837

																																														199		0.905778		0.950232

																																														201		0.910969		0.952571

																																														203		0.914923		0.954857

																																														205.09		0.920417		0.957091

																																														207		0.92149		0.959275

																																														209		0.922718		0.961409

																																														211		0.925815		0.963495

																																														213		0.92726		0.965539

																																														215		0.928694		0.967535

																																														217.2		0.929362		0.969483

																																														219		0.931405		0.971388

																																														221		0.948703		0.973251

																																														223		0.948549		0.975076

																																														225		0.955387		0.976853

																																														227.29		0.955482		0.978592

																																														229		0.963645		0.980291

																																														231		0.964931		0.981954

																																														233		0.966829		0.98358

																																														235		0.972576		0.985168

																																														237		0.973957		0.986719

																																														239		0.977985		0.988236

																																														241		0.980953		0.989718

																																														243		0.983302		0.991167

																																														245		0.987188		0.992585

																																														247		0.987327		0.993972

																																														249		0.989223		0.995326

																																														252		0.993066		0.99665

																																														254		0.993314		0.997945

																																														255.54		0.994078		0.999211

																																														258		0.999884		1

																																														260		0.997056		1

																																														261.59		1		1

																																														263.61		1		1

																																														265.63		1		1

																																														268		1		1

																																														270		1		1

																																														272		1		1

																																														274		1		1

																																														276		1		1

																																														278		1		1

																																														280		1		1

																																														282		1		1

																																														284		1		1

																																														286		1		1

																																														288		1		1

																																														290		1		1

																																														292		1		1

																																														294		1		1

																																														296		1		1

																																														298		1		1

																																														300		1		1

																																														302		1		1

																																														304		1		1

																																														306		1		1

																																														308		1		1

																																														310		1		1

																																														312		1		1

																																														314		1		1

																																														316.08		1		1

																																														318		1		1

																																														320		1		1

																																														322		1		1

																																														324		1		1

																																														326		1		1

																																														328		1		1

																																														330.2		1		1

																																														332		1		1

																																														334		1		1

																																														336		1		1

																																														338.27		1		1

																																														340		1		1

																																														342		1		1

																																														344		1		1

																																														346		1		1

																																														348		1		1

																																														350		1		1

																																														352.4		1		1

																																														354		1		1

																																														356		1		1

																																														358		1		1

																																														360		1		1

																																														362		1		1

																																														365		1		1

																																														367		1		1

																																														369		1		1





 FULL ALL

		



GLP-PX 50K 1:3 FaSSIF

GLP-PX 50K 1:3 pH 6.8

Time (min)

Dissolved (mg)



 6.8 ALL 

		GLP-PX 50K 1:2								445.54																GLP-PX 50K -1				17B-28009								GLP-PX 50K -2				17C-09016								GLP-PX 50K -3				17E-10009								GLP-PX 50K -4				17E-10019				GLP-PEOX 50K 1:2 pH 6.8												GLP-PX 50K FaSSIF-1				17C-10005								GLP-PX 50K FaSSIF-2				17C-10007				GLP-PEOX 50K 1:2 FaSSIF

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/ml)		IDR (ug/min/cm2)

		GLP-PX 50K -1		17B-28009		0.452		15.03		0.30		4.58		9.88		12.5346		179.0661

		GLP-PX 50K -2		17C-09016		0.331		15.6		0.30		4.75		6.97		6.6379		94.8267				Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile																				Dissolution Profile												Dissolution Profile

		GLP-PX 50K -3		17E-10009		0.087		15.26		0.30		4.65		1.88		2.8461		40.6582																																																				AVERAGE				TIME		SD																										AVERAGE		TIME

		GLP-PX 50K -4		17E-10019		0.216		15.57		0.30		4.74		4.55		5.1604		73.7193				Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		%		Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		%		mg		Weight (µg)						Time (minutes)		Weight (µg)		Weight (µg)		Weight (mg)		Time zero (min)		%		Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		%		mg

		AVG				0.273								5.759		5.899		84.273				5.05522		15.7231				0.0157231		0		0.3434387517		5.0487		17.1085		0.0171085				0		0.360045541		5.12032		12.8997				0.0128997		0		0.2775205693		4.06953		20.6936				0.0206936		0		0.436332476		0.01890105		18.90105		0		0.0025350485		1.88022		10.7367		13.9759		0.0107367		0		0.2299316546		1.88672		14.2977				0.0142977		0		0.3071941401		0.0125172		0

		SD				0.081								1.708		1.045		14.925				5.57318		23.3344				0.0233344		0.51796		0.5096919315		5.56458		18.8299		0.0188299				0.51588		0.3962721181		5.63777		15.0446				0.0150446		0.51745		0.3236653532		4.58593		24.3018				0.0243018		0.5164		0.512412754		0.02156585		21.56585		0.51614		0.0038692176		2.39583		19.3197		20.7823		0.0193197		0.51561		0.4137407758		2.40182		22.0185				0.0220185		0.5151		0.4730798782		0.0206691		0.515355

		RSD				29.793								29.663		17.710		17.710				6.08932		25.0931				0.0250931		1.0341		0.5481071125		6.0789		21.6705		0.0216705				1.0302		0.4560520733		6.1526		16.9459				0.0169459		1.03228		0.3645693942		5.1013		28.2849				0.0282849		1.03177		0.5963979419		0.0249777		24.9777		1.030985		0.0046770871		2.91042		27.8134		27.5148		0.0278134		1.0302		0.5956374941		2.91797		29.2508				0.0292508		1.03125		0.6284699185		0.0285321		1.030725

		GLP-PX 50K FaSSIF-1		17C-10005		0.544		15.33		0.30		4.67		11.64		12.62		180.22				6.6039		30.6364				0.0306364		1.54868		0.6691890895		6.59505		27.0662		0.0270662				1.54635		0.5696036837		6.66848		19.0964				0.0190964		1.54816		0.410834655		5.61537		30.9885				0.0309885		1.54584		0.6534043826		0.02902735		29.02735		1.546095		0.0027734849		3.425		36.0571		34.1877		0.0360571		1.54478		0.7721803407		3.43255		32.4282				0.0324282		1.54583		0.6967381477		0.03424265		1.545305

		GLP-PX 50K FaSSIF-2		17C-10007		0.470		15.28		0.30		4.65		10.09		12.29		175.57				7.12188		40.5981				0.0405981		2.06666		0.8867819188		7.10912		30.1565		0.0301565				2.06042		0.6346385339		7.18333		20.8971				0.0208971		2.06301		0.4495744155		6.12917		32.9369				0.0329369		2.05964		0.6944871423		0.0315467		31.5467		2.06003		0.0019660397		3.94115		43.3593		40.8215		0.0433593		2.06093		0.9285605067		3.9487		38.2507				0.0382507		2.06198		0.8218378407		0.040805		2.061455

		AVG				0.507								10.87		12.45		177.89				7.63985		41.6008				0.0416008		2.58463		0.9086838361		7.62527		33.2458		0.0332458				2.57657		0.6996523393		7.69897		21.8778				0.0218778		2.57865		0.4706729234		6.6448		35.3093				0.0353093		2.57527		0.7445101043		0.03427755		34.27755		2.57592		0.0014591148		4.45573		50.3852		47.3766		0.0503852		2.57551		1.0790235737		4.46277		43.0038				0.0430038		2.57605		0.9239608722		0.0466945		2.57578

		SD				0.052								1.10		0.23		3.29				8.1573		46.5516				0.0465516		3.10208		1.0168238703		8.14037		37.0266		0.0370266				3.09167		0.7792186474		8.21302		23.3392				0.0233392		3.0927		0.5021130778		7.16042		39.2831				0.0392831		3.09089		0.8282991982		0.03815485		38.15485		3.09128		0.0015955865		4.97162		55.453		53.89		0.055453		3.0914		1.1875529766		4.97838		55.8123				0.0558123		3.09166		1.1991587113		0.05563265		3.09153

		RSD				10.338								10.11		1.85		1.85				8.67343		55.138				0.055138		3.61821		1.2043761022		8.65443		39.2014		0.0392014				3.60573		0.8249869522		8.72943		24.9674				0.0249674		3.60911		0.5371417212		7.67605		41.4419				0.0414419		3.60652		0.8738183224		0.04032165		40.32165		3.606125		0.0015842727		5.48802		61.7277		60.352		0.0617277		3.6078		1.3219287301		5.49402		60.2376				0.0602376		3.6073		1.2942387751		0.06098265		3.60755

																						9.18802		62.0578				0.0620578		4.1328		1.3555248881		9.17057		43.9059		0.0439059				4.12187		0.9239923734		9.2448		26.7076				0.0267076		4.12448		0.5745799015		8.19115		43.2856				0.0432856		4.12162		0.9126934426		0.04359575		43.59575		4.121745		0.0004386183		6.00287		66.7768		66.7374		0.0667768		4.12265		1.4300576633		6.01015		65.9681				0.0659681		4.12343		1.4173617963		0.06637245		4.12304

																						9.70598		76.0526				0.0760526		4.65076		1.6612124842		9.68385		46.0749		0.0460749				4.63515		0.9696386181		9.76198		27.2736				0.0272736		4.64166		0.5867566686		8.70598		45.9018				0.0459018		4.63645		0.9678570209		0.04598835		45.98835		4.6358		0.0001224002		6.51718		72.9994		73.0597		0.0729994		4.63696		1.56331767		6.52527		72.1762				0.0721762		4.63855		1.5507463225		0.0725878		4.637755

																						10.2216		75.4554				0.0754554		5.16638		1.6481678796		10.199		49.9997		0.0499997				5.1503		1.0522353823		10.2763		28.4236				0.0284236		5.15598		0.6114974498		9.22188		48.2764				0.0482764		5.15235		1.0179263707		0.04913805		49.13805		5.151325		0.0012185571		7.03333		76.8602		79.3483		0.0768602		5.15311		1.6459985806		7.04037		77.629				0.077629		5.15365		1.6679028027		0.0772446		5.15338

																						10.7372		90.317				0.090317		5.68198		1.9727889373		10.7143		54.4943		0.0544943				5.6656		1.1468234928		10.7922		28.8257				0.0288257		5.67188		0.6201481177		9.7388		50.7242				0.0507242		5.66927		1.0695391705		0.05260925		52.60925		5.667435		0.0026658633		7.54897		84.5038		85.5749		0.0845038		5.66875		1.8096899937		7.55443		83.7357				0.0837357		5.66771		1.7991086929		0.08411975		5.66823

																						11.2547		101.031				0.101031		6.19948		2.2068142114		11.2297		59.2104		0.0592104				6.181		1.246073034		11.3075		31.1683				0.0311683		6.18718		0.6705461646		10.255		52.9859				0.0529859		6.18547		1.1172279806		0.05609815		56.09815		6.183235		0.0044013862		8.0638		88.7044		91.7367		0.0887044		6.18358		1.8996478866		8.07057		89.4221				0.0894221		6.18385		1.9212842007		0.08906325		6.183715

																						11.7721		109.943				0.109943		6.71688		2.401478505		11.7458		64.2		0.0642				6.6971		1.3510783373		11.8242		32.5545				0.0325545		6.70388		0.700368487		10.7685		54.3274				0.0543274		6.69897		1.1455140216		0.0592637		59.2637		6.698035		0.0069809824		8.57995		95.5309		97.8594		0.0955309		6.69973		2.0458407056		8.58568		97.0794				0.0970794		6.69896		2.0858056055		0.09630515		6.699345

																						12.2901		112.394				0.112394		7.23488		2.4550155544		12.2651		69.8137		0.0698137				7.2164		1.4692177214		12.3401		33.4774				0.0334774		7.21978		0.7202235018		11.2818		58.4921				0.0584921		7.21227		1.233328315		0.0641529		64.1529		7.214335		0.0080055801		9.09505		101.438		103.915		0.101438		7.21483		2.1723441263		9.10182		104.725				0.104725		7.2151		2.2500756292		0.1030815		7.214965

																						12.8063		122.738				0.122738		7.75108		2.6809589401		12.7813		74.9644		0.0749644				7.7326		1.5776133475		12.8562		33.3989				0.0333989		7.73588		0.7185346745		11.7956		61.2592				0.0612592		7.72607		1.2916736776		0.0681118		68.1118		7.729335		0.0096910399		9.61015		111.028		109.918		0.111028		7.72993		2.3777186425		9.61745		112.174				0.112174		7.73073		2.4101215911		0.111601		7.73033

																						13.3237		133.257				0.133257		8.26848		2.9107248405		13.2953		80.716		0.080716				8.2466		1.6986548142		13.3716		35.2184				0.0352184		8.25128		0.7576788931		12.3112		65.69				0.06569		8.24167		1.3850987913		0.073203		73.203		8.244135		0.0106249865		10.1274		117.277		115.891		0.117277		8.24718		2.511544018		10.1331		122.191				0.122191		8.24638		2.6253424799		0.119734		8.24678

																						13.8412		138.477				0.138477		8.78598		3.0247449946		13.812		84.6106		0.0846106				8.7633		1.7806160244		13.8888		36.9422				0.0369422		8.76848		0.7947642483		12.8263		67.5126				0.0675126		8.75677		1.4235290099		0.0760616		76.0616		8.760035		0.0120901117		10.6427		124.761		121.79		0.124761		8.76248		2.6718175195		10.6477		128.596				0.128596		8.76098		2.7629575136		0.1266785		8.76173

																						14.3557		148.2				0.1482		9.30048		3.2371239137		14.3271		89.0801		0.0890801				9.2784		1.8746759096		14.405		37.2203				0.0372203		9.28468		0.8007472146		13.3419		71.5747				0.0715747		9.27237		1.5091799431		0.0803274		80.3274		9.275385		0.012378187		11.1563		136.343		127.617		0.136343		9.27608		2.9198516849		11.1617		134.792				0.134792		9.27498		2.8960820645		0.1355675		9.27553

																						14.8708		158.434				0.158434		9.81558		3.4606645759		14.8422		93.6649		0.0936649				9.7935		1.9711622641		14.9219		39.1725				0.0391725		9.80158		0.8427463042		13.857		74.4086				0.0744086		9.78747		1.5689338092		0.08403675		84.03675		9.790485		0.0136162603		11.6695		144.31		133.389		0.14431		9.78928		3.0904688664		11.6766		142.8				0.1428		9.78988		3.0681384564		0.143555		9.78958

																						15.3893		167.676				0.167676		10.33408		3.6625370402		15.357		99.5079		0.0995079				10.3083		2.0941272286		15.4367		41.2107				0.0412107		10.31638		0.8865955739		14.3727		76.8705				0.0768705		10.30317		1.6208439129		0.0881892		88.1892		10.305735		0.016007059		12.1849		152.947		139.133		0.152947		10.30468		3.2754344239		12.1958		152.545				0.152545		10.30908		3.2775152719		0.152746		10.30688

																						15.9073		178.007				0.178007		10.85208		3.8881964676		15.874		102.618		0.102618				10.8253		2.1595787666		15.9534		41.3889				0.0413889		10.83308		0.8904293192		14.8872		77.7337				0.0777337		10.81767		1.6390448153		0.09017585		90.17585		10.821485		0.0175958573		12.6997		162.173		144.82		0.162173		10.81948		3.4730137029		12.7143		163.234				0.163234		10.82758		3.5071744593		0.1627035		10.82353

																						16.4274		186.566				0.186566		11.37218		4.075150203		16.388		113.265		0.113265				11.3393		2.3836431133		16.4685		43.4589				0.0434589		11.34818		0.9349627253		15.4029		79.5099				0.0795099		11.33337		1.6764966721		0.09638745		96.38745		11.336335		0.0238684601		13.213		171.653		150.44		0.171653		11.33278		3.6760325156		13.2289		171.035				0.171035		11.34218		3.6747833396		0.171344		11.33748

																						16.943		198.199				0.198199		11.88778		4.3292491402		16.9013		119.754		0.119754				11.8526		2.5202030406		16.9842		44.642				0.044642		11.86388		0.9604156107		15.918		81.8656				0.0818656		11.84847		1.7261675082		0.1008098		100.8098		11.850535		0.0267911446		13.7287		177.369		156.036		0.177369		11.84848		3.7984434368		13.745		177.787				0.177787		11.85828		3.8198538638		0.177578		11.85338

																						17.4583		209.475				0.209475		12.40308		4.5755501472		17.417		126.427		0.126427				12.3683		2.6606352173		17.499		44.1966				0.0441966		12.37868		0.9508333986		16.4346		82.6981				0.0826981		12.36507		1.7437210893		0.10456255		104.56255		12.366685		0.0309210017		14.2432		188.947		161.571		0.188947		12.36298		4.0463919402		14.2591		186.935				0.186935		12.37238		4.016403798		0.187941		12.36768

																						17.973		218.905				0.218905		12.91778		4.7815290845		17.9325		132.844		0.132844				12.8838		2.7956799165		18.0138		45.7377				0.0457377		12.89348		0.9839881967		16.9515		86.1234				0.0861234		12.88197		1.8159448508		0.1094837		109.4837		12.882885		0.0330364531		14.7588		196.18		167.068		0.19618		12.87858		4.2012901546		14.7742		196.536				0.196536		12.88748		4.2226866924		0.196358		12.88303

																						18.4897		232.477				0.232477		13.43448		5.077981485		18.4467		138.845		0.138845				13.398		2.9219699648		18.5302		48.2002				0.0482002		13.40988		1.036965739		17.4672		88.9624				0.0889624		13.39767		1.8758062523		0.1139037		113.9037		13.397835		0.0352723247		15.274		205.602		172.51		0.205602		13.39378		4.403066869		15.2909		204.572				0.204572		13.40418		4.39534468		0.205087		13.39898

																						19.0047		236.158				0.236158		13.94948		5.1583853523		18.9628		144.117		0.144117				13.9141		3.0329183292		19.044		48.928				0.048928		13.92368		1.0526234264		17.9828		90.4017				0.0904017		13.91327		1.9061544437		0.11725935		117.25935		13.913685		0.0379824529		15.7901		213.134		177.916		0.213134		13.90988		4.5643683138		15.8042		212.035				0.212035		13.91748		4.5556914398		0.2125845		13.91368

																						19.5217		245				0.245		14.46648		5.3515206401		19.4768		148.556		0.148556				14.4281		3.126336347		19.5588		50.4429				0.0504429		14.43848		1.085214565		18.498		91.801				0.091801		14.42847		1.9356592197		0.1201785		120.1785		14.428285		0.0401318454		16.3062		221.083		183.273		0.221083		14.42598		4.7346000165		16.3188		217.356				0.217356		14.43208		4.6700161228		0.2192195		14.42903

																						20.0383		254.771				0.254771		14.98308		5.5649480204		19.9907		155.142		0.155142				14.942		3.2649376231		20.0742		51.5849				0.0515849		14.95388		1.1097832363		19.0148		94.2153				0.0942153		14.94527		1.9865656592		0.12467865		124.67865		14.943635		0.0430816827		16.8232		229.413		188.591		0.229413		14.94298		4.9129910196		16.832		226.133				0.226133		14.94528		4.8585949129		0.227773		14.94413

																						20.5542		280.516				0.280516		15.49898		6.1272945464		20.5063		160.048		0.160048				15.4576		3.3681835783		20.5907		52.6779				0.0526779		15.47038		1.1332977353		19.53		94.9153				0.0949153		15.46047		2.0013254272		0.12748165		127.48165		15.459035		0.0460557738		17.3388		236.776		193.848		0.236776		15.45858		5.0706732472		17.3472		232.701				0.232701		15.46048		4.9997120935		0.2347385		15.45953

																						21.0703		283.634				0.283634		16.01508		6.1954008376		21.0213		166.984		0.166984				15.9726		3.5141505463		21.1063		53.8124				0.0538124		15.98598		1.1577050537		20.0455		97.1216				0.0971216		15.97597		2.0478461071		0.1320528		132.0528		15.974285		0.0494001768		17.8528		248.8		199.042		0.2488		15.97258		5.3281730577		17.8633		240.354				0.240354		15.97658		5.1641411103		0.244577		15.97458

																						21.5878		293.083				0.293083		16.53258		6.4017947908		21.5375		175.543		0.175543				16.4888		3.6942732798		21.6227		55.7552				0.0557552		16.50238		1.1995019143		20.5622		98.9598				0.0989598		16.49267		2.0866052576		0.1372514		137.2514		16.490735		0.0541525		18.369		260.892		204.212		0.260892		16.48878		5.5871291212		18.3778		246.94				0.24694		16.49108		5.305645031		0.253916		16.48993

																						22.1023		305.659				0.305659		17.04708		6.6764916217		22.055		182.788		0.182788				17.0063		3.8467431015		22.1385		58.501				0.058501		17.01818		1.2585742942		21.0792		100.98				0.10098		17.00967		2.1292019478		0.141884		141.884		17.007985		0.0578469916		18.8837		276.162		209.321		0.276162		17.00348		5.9141436011		18.893		254.433				0.254433		17.00628		5.4666363577		0.2652975		17.00488

																						22.6185		312.042				0.312042		17.56328		6.8159151166		22.5705		188.217		0.188217				17.5218		3.9609955048		22.6538		58.5727				0.0585727		17.53348		1.2601168281		21.5943		102.755				0.102755		17.52477		2.1666285021		0.145486		145.486		17.523285		0.0604307597		19.3997		292.034		214.398		0.292034		17.51948		6.2540502039		19.408		260.028				0.260028		17.52128		5.586848085		0.276031		17.52038

																						23.138		323.734				0.323734		18.08278		7.0713027873		23.0847		193.931		0.193931				18.036		4.0812456858		23.169		58.5488				0.0585488		18.04868		1.2596026501		22.1088		106.469				0.106469		18.03927		2.2449396136		0.1502		150.2		18.037635		0.0618449733		19.9182		312.891		219.454		0.312891		18.03798		6.7007130072		19.9265		267.626				0.267626		18.03978		5.7500953959		0.2902585		18.03888

																						23.6545		334.705				0.334705		18.59928		7.3109416973		23.5985		198.644		0.198644				18.5498		4.180429988		23.686		61.4074				0.0614074		18.56568		1.321101778		22.6242		110.147				0.110147		18.55467		2.3224916512		0.1543955		154.3955		18.552235		0.0625768288		20.4342		324.507		224.441		0.324507		18.55398		6.9494752992		20.4422		272.444				0.272444		18.55548		5.8536128405		0.2984755		18.55473

																						24.173		333.368				0.333368		19.11778		7.2817376846		24.113		206.334		0.206334				19.0643		4.3422647608		24.2027		62.93				0.06293		19.08238		1.3538585722		23.1412		108.022				0.108022		19.07167		2.2776852129		0.157178		157.178		19.067985		0.0695170819		20.9503		341.843		229.386		0.341843		19.07008		7.3207341743		20.9592		279.342				0.279342		19.07248		6.0018202569		0.3105925		19.07128

																						24.6908		345.811				0.345811		19.63558		7.5535294043		24.6277		212.237		0.212237				19.579		4.4664924154		24.7175		64.8935				0.0648935		19.59718		1.3961007668		23.6552		111.641				0.111641		19.58567		2.353993213		0.161939		161.939		19.582335		0.0711321138		21.4638		354.854		234.261		0.354854		19.58358		7.59937107		21.4753		285.592				0.285592		19.58858		6.1361050283		0.320223		19.58608

																						25.206		357.547				0.357547		20.15078		7.8098781644		25.1422		219.315		0.219315				20.0935		4.6154477499		25.2333		65.1993				0.0651993		20.11298		1.4026796633		24.1708		135.678				0.135678		20.10127		2.8608225576		0.1774965		177.4965		20.097385		0.0591402899		21.9787		365.642		239.105		0.365642		20.09848		7.8304013391		21.9888		292.181				0.292181		20.10208		6.2776734057		0.3289115		20.10028

																						25.72		360.535				0.360535		20.66478		7.8751448733		25.6593		227.417		0.227417				20.6106		4.7859529943		25.7487		66.792				0.066792		20.62838		1.4369445695		24.6893		138.44				0.13844		20.61977		2.9190603847		0.1829285		182.9285		20.615185		0.0629162401		22.4945		376.269		243.916		0.376269		20.61428		8.0579837148		22.5032		295.725				0.295725		20.61648		6.3538182424		0.335997		20.61538

																						26.2347		365.073				0.365073		21.17948		7.9742681413		26.1755		234.81		0.23481				21.1268		4.9415374514		26.2625		67.6241				0.0676241		21.14218		1.4548461382		25.2033		146.454				0.146454		21.13377		3.0880386419		0.190632		190.632		21.130285		0.0624771268		23.0098		390.464		248.68		0.390464		21.12958		8.3619765466		23.0188		308.835				0.308835		21.13208		6.6354939789		0.3496495		21.13083

																						26.7505		373.487				0.373487		21.69528		8.1580546502		26.693		239.65		0.23965				21.6443		5.0433944475		26.7778		69.1938				0.0691938		21.65748		1.4886162287		25.72		153.877				0.153877		21.65047		3.2445554379		0.1967635		196.7635		21.647385		0.0606506699		23.5268		398.814		253.416		0.398814		21.64658		8.5407958594		23.5333		321.805				0.321805		21.64658		6.9141617364		0.3603095		21.64658

																						27.2663		369.439				0.369439		22.21108		8.0696344234		27.2092		245.767		0.245767				22.1605		5.1721256966		27.2913		70.9294				0.0709294		22.17098		1.5259554459		26.2357		158.634				0.158634		22.16617		3.3448586035		0.2022005		202.2005		22.163335		0.0616123352		24.0413		409.591		258.088		0.409591		22.16108		8.7715905582		24.0467		326.517				0.326517		22.15998		7.0154017113		0.368054		22.16053

																						27.781		374.755				0.374755		22.72578		8.1857514998		27.7242		252.605		0.252605				22.6755		5.3160302709		27.807		71.5568				0.0715568		22.68668		1.5394531556		26.7518		163.349				0.163349		22.68227		3.4442761831		0.207977		207.977		22.678885		0.0631135229		24.5552		413.267		262.713		0.413267		22.67498		8.8503138868		24.5622		342.198				0.342198		22.67548		7.3523168313		0.3777325		22.67523

																						28.2982		388.397				0.388397		23.24298		8.4837329063		28.2388		258.075		0.258075				23.1901		5.4311455124		28.3217		72.8625				0.0728625		23.20138		1.5675436234		27.2667		168.282				0.168282		23.19717		3.5482903761		0.2131785		213.1785		23.193635		0.0634932392		25.0708		430.197		267.313		0.430197		23.19058		9.2128780744		25.0788		351.45				0.35145		23.19208		7.551101264		0.3908235		23.19133

																						28.8122		400.056				0.400056		23.75698		8.7383997599		28.7538		264.765		0.264765				23.7051		5.5719354513		28.838		74.7657				0.0747657		23.71768		1.6084885405		27.7833		169.898				0.169898		23.71377		3.5823643546		0.2173315		217.3315		23.709435		0.067081099		25.5862		438.706		271.869		0.438706		23.70598		9.3951024495		25.5925		358.951				0.358951		23.70578		7.7122644753		0.3988285		23.70588

																						29.3283		397.145				0.397145		24.27308		8.6748149575		29.2718		271.362		0.271362				24.2231		5.7107682206		29.3547		75.6109				0.0756109		24.23438		1.626671939		28.299		177.296				0.177296		24.22947		3.738354016		0.224329		224.329		24.226285		0.0665147065		26.1027		447.384		276.395		0.447384		24.22248		9.580946042		26.108		369.716				0.369716		24.22128		7.9435565655		0.40855		24.22188

																						29.844		409.035				0.409035		24.78878		8.9345275306		29.787		275.38		0.27538				24.7383		5.7953263633		29.8695		75.8965				0.0758965		24.74918		1.6328162582		28.817		181.191				0.181191		24.74747		3.8204815817		0.2282855		228.2855		24.742885		0.0666016806		26.6172		452.628		280.863		0.452628		24.73698		9.6932488535		26.6237		380.647				0.380647		24.73698		8.1784152592		0.4166375		24.73698

																						30.3592		413.745				0.413745		25.30398		9.0374077846		30.3022		282.775		0.282775				25.2535		5.9509529101		30.3867		78.057				0.078057		25.26638		1.6792966562		29.3343		184.23				0.18423		25.26477		3.8845600598		0.2335025		233.5025		25.259135		0.0696818378		27.1323		466.02		285.298		0.46602		25.25208		9.9800450496		27.1388		388.744				0.388744		25.25208		8.3523838662		0.427382		25.25208

																						30.8747		418.075				0.418075		25.81948		9.1319877208		30.8188		289.292		0.289292				25.7701		6.0881020927		30.9027		78.9009				0.0789009		25.78238		1.6974520868		29.85		186.139				0.186139		25.78047		3.9248120554		0.2377155		237.7155		25.775285		0.0729401858		27.648		467.778		289.697		0.467778		25.76778		10.017693475		27.6568		400.6				0.4006		25.77008		8.6071167061		0.434189		25.76893

																						31.3898		423.88				0.42388		26.33458		9.2587859955		31.3362		295.591		0.295591				26.2875		6.2206635015		31.4175		80.2856				0.0802856		26.29718		1.7272421387		30.368		189.65				0.18965		26.29847		3.9988428342		0.2426205		242.6205		26.292985		0.0749115995		28.164		496.653		294.061		0.496653		26.28378		10.6360656496		28.1723		407.116				0.407116		26.28558		8.7471166374		0.4518845		26.28468

																						31.9057		428.818				0.428818		26.85048		9.3666464401		31.8503		301.284		0.301284				26.8016		6.340471741		31.9352		81.9853				0.0819853		26.81488		1.7638090132		30.8848		191.389				0.191389		26.81527		4.0355103148		0.2463365		246.3365		26.808435		0.0777074997		28.6797		492.381		298.382		0.492381		26.79948		10.544578691		28.687		417.249				0.417249		26.80028		8.9648298515		0.454815		26.79988

																						32.42		434.307				0.434307		27.36478		9.4865423454		32.3652		305.819		0.305819				27.3165		6.4359100628		32.449		82.4048				0.0824048		27.32868		1.7728340199		31.4		195.178				0.195178		27.33047		4.1154028299		0.2504985		250.4985		27.323485		0.0782350014		29.1938		506.241		302.653		0.506241		27.31358		10.8413973348		29.2032		426.799				0.426799		27.31648		9.1700169822		0.46652		27.31503

																						32.9357		448.226				0.448226		27.88048		9.7905742466		32.8792		309.919		0.309919				27.8305		6.5221938818		32.9625		83.6136				0.0836136		27.84218		1.798839808		31.9133		199.554				0.199554		27.84377		4.2076724647		0.2547365		254.7365		27.837135		0.0780398399		29.7097		515.816		306.9		0.515816		27.82948		11.0464506187		29.7205		436.723				0.436723		27.83378		9.3832397136		0.4762695		27.83163

																						33.4513		446.66				0.44666		28.39608		9.7563682003		33.3953		317.599		0.317599				28.3466		6.6838182063		33.4788		84.3953				0.0843953		28.35848		1.815657085		32.4288		203.225				0.203225		28.35927		4.2850769047		0.260412		260.412		28.352935		0.080874631		30.2255		531.996		311.109		0.531996		28.34528		11.3929531913		30.2357		443.722				0.443722		28.34898		9.5336171719		0.487859		28.34713

																						33.9663		446.711				0.446711		28.91108		9.7574821904		33.9117		321.858		0.321858				28.863		6.7734481539		33.9927		85.2755				0.0852755		28.87238		1.8345934638		32.9455		207.925				0.207925		28.87597		4.3841782035		0.2648915		264.8915		28.869485		0.0805627969		30.742		531.073		315.287		0.531073		28.86178		11.3731866972		30.7508		452.525				0.452525		28.86408		9.7227545867		0.491799		28.86293

																						34.4838		450.291				0.450291		29.42858		9.8356799205		34.4282		326.386		0.326386				29.3795		6.8687391619		34.5092		86.8642				0.0868642		29.38888		1.8687723151		33.4643		212.341				0.212341		29.39477		4.4772912537		0.2693635		269.3635		29.387135		0.0806419929		31.257		534.086		319.415		0.534086		29.37678		11.4377115582		31.267		462.096				0.462096		29.38028		9.9283929142		0.498091		29.37853

																						34.999		452.363				0.452363		29.94378		9.8809384951		34.9435		331.046		0.331046				29.8948		6.966808088		35.0258		87.4127				0.0874127		29.90548		1.880572592		33.9823		215.835				0.215835		29.91277		4.5509635809		0.2734405		273.4405		29.903785		0.0814664794		31.7723		543.739		323.509		0.543739		29.89208		11.6444352501		31.7815		469.656				0.469656		29.89478		10.0908237737		0.5066975		29.89343

																																																																														32.2875		556.025		327.565								32.2962		475.789

																																																																														32.8033		571.569		331.591								32.8125		483.976





 6.8 ALL 

		



GLP-PEOX 50K 1:2 FaSSIF

GLP-PEOX 50K 1:2 pH 6.8

Time (min)

Dissolved (mg)



		



GLP-PEOX 50K 1:2 FaSSIF

GLP-PEOX 50K 1:2 pH 6.8

Time (min)

Dissolved (mg)



		GLP-PL 1:5								445.54																GLP-PL -1				17B-27009								GLP-PL -2				17B-28011										GLP-PL 1:5 pH 6.8										GLP-PL FaSSIF-1												GLP-PL FaSSIF-2												GLP-PL FaSSIF-3								GLP-PL 1:5 FaSSIF

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/ml)		IDR (ug/min/cm2)

		GLP-PL -1		17B-27009		0.412		30		0.15				0.00		117.7973		1682.8189

		GLP-PL -2		17B-28011		0.795		30		0.15				0.00		131.8181		1883.1163				Dissolution Profile												Dissolution Profile																								Dissolution Profile												Dissolution Profile												Dissolution Profile

																																																				AVERAGE		TIME																																								AVERAGE		TIME

																						Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%								mg						Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)				Time zero (min)		%		mg

																						4.58098		0.25458						0		0		4.5711		0						0		0								0.12729		0												0		0										0		0										0		0		0		0

		AVG				0.604								0.000		124.808		1782.968				5.1		0.306395						0.51902		0		5.0862		0.501697						0.5151		0								0.404046		0.51706												0		0										0		0										0		0		0		0

		SD				0.270								0.000		9.914		141.632				5.62057		0.371861						1.03959		0		5.6026		0.552901						1.0315		0								0.462381		1.035545												0		0										0		0										0		0		0		0

		RSD				44.780								0.000		7.944		7.944				6.14297		0.428556						1.56199		0		6.12083		0.629268						1.54973		0								0.528912		1.55586												0		0										0		0										0		0		0		0

		GLP-PL FaSSIF-1		0.00		0.000				0.15		0.00		0.00		0.00		0.00				6.66537		0.460523						2.08439		0		6.63855		0.758638						2.06745		0								0.6095805		2.07592												0		0										0		0										0		0		0		0

		GLP-PL FaSSIF-2		0.00		0.000				0.15		0.00		0.00		0.00		0.00				7.18828		0.541198						2.6073		0		7.15365		1.00504						2.58255		0								0.773119		2.594925												0		0										0		0										0		0		0		0

		GLP-PL FaSSIF-3		0.00		0.000				0.15		0.00		0.00		0.00		0.00				7.71223		0.581235						3.13125		0		7.6698		1.03933						3.0987		0								0.8102825		3.114975												0		0										0		0										0		0		0		0

		AVG				0.000								0.00		0.00		0.00				8.2349		0.630226						3.65392		0		8.1901		1.15548						3.619		0								0.892853		3.63646												0		0										0		0										0		0		0		0

		SD				0.000								0.00		0.00		0.00				8.75313		0.689106						4.17215		0		8.70807		1.05416						4.13697		0								0.871633		4.15456												0		0										0		0										0		0		0		0

		RSD				0.000								0.00		0.00		0.00				9.27318		0.73876						4.6922		0		9.22605		1.14652						4.65495		0								0.94264		4.673575												0		0										0		0										0		0		0		0

																						9.7961		0.894928						5.21512		0		9.74402		0.772948						5.17292		0								0.833938		5.19402												0		0										0		0										0		0		0		0

																						10.3151		0.969001						5.73412		0		10.2576		0.869365						5.6865		0								0.919183		5.71031												0		0										0		0										0		0		0		0

																						10.8362		1.01564						6.25522		0		10.7719		0.79012						6.2008		0								0.90288		6.22801												0		0										0		0										0		0		0		0

																						11.3552		1.04395						6.77422		0		11.2859		0.760128						6.7148		0								0.902039		6.74451												0		0										0		0										0		0		0		0

																						11.8774		1.08779						7.29642		0		11.8026		0.825152						7.2315		0								0.956471		7.26396												0		0										0		0										0		0		0		0

																						12.3992		1.02326						7.81822		0		12.3172		0.830626						7.7461		0								0.926943		7.78216												0		0										0		0										0		0		0		0

																						12.9198		1.07667						8.33882		0		12.8331		0.798518						8.262		0								0.937594		8.30041												0		0										0		0										0		0		0		0

																						13.438		1.0051						8.85702		0		13.3484		0.791474						8.7773		0								0.898287		8.81716												0		0										0		0										0		0		0		0

																						13.9557		1.0296						9.37472		0		13.8646		0.878259						9.2935		0								0.9539295		9.33411												0		0										0		0										0		0		0		0

																						14.4784		1.05128						9.89742		0		14.3797		0.756912						9.8086		0								0.904096		9.85301												0		0										0		0										0		0		0		0

																						14.9971		0.830093						10.41612		0		14.895		0.796223						10.3239		0								0.813158		10.37001												0		0										0		0										0		0		0		0

																						15.5162		0.895772						10.93522		0		15.4102		0.76829						10.8391		0								0.832031		10.88716												0		0										0		0										0		0		0		0

																						16.0328		0.729066						11.45182		0		15.925		0.79852						11.3539		0								0.763793		11.40286												0		0										0		0										0		0		0		0

																						16.55		0.715305						11.96902		0		16.4412		0.814341						11.8701		0								0.764823		11.91956												0		0										0		0										0		0		0		0

																						17.0675		0.706436						12.48652		0		16.9568		0.828562						12.3857		0								0.767499		12.43611												0		0										0		0										0		0		0		0

																						17.5847		0.618212						13.00372		0		17.4723		0.79852						12.9012		0								0.708366		12.95246												0		0										0		0										0		0		0		0

																						18.1013		0.532367						13.52032		0		17.986		0.79852						13.4149		0								0.6654435		13.46761												0		0										0		0										0		0		0		0

																						18.6163		0.485142						14.03532		0		18.5013		0.814076						13.9302		0								0.649609		13.98276												0		0										0		0										0		0		0		0

																						19.1343		0.501531						14.55332		0		19.0177		0.789135						14.4466		0								0.645333		14.49996												0		0										0		0										0		0		0		0

																						19.6522		0.390611						15.07122		0		19.5328		0.782166						14.9617		0								0.5863885		15.01646												0		0										0		0										0		0		0		0

																						20.167		0.381953						15.58602		0		20.048		0.798521						15.4769		0								0.590237		15.53146												0		0										0		0										0		0		0		0

																						20.6837		0.41422						16.10272		0		20.563		0.805777						15.9919		0								0.6099985		16.04731												0		0										0		0										0		0		0		0

																						21.2013		0.381412						16.62032		0		21.0782		0.827217						16.5071		0								0.6043145		16.56371												0		0										0		0										0		0		0		0

																						21.718		0.395547						17.13702		0		21.5935		0.798521						17.0224		0								0.597034		17.07971												0		0										0		0										0		0		0		0

																						22.2347		0.363652						17.65372		0		22.1098		0.794854						17.5387		0								0.579253		17.59621												0		0										0		0										0		0		0		0

																						22.7513		0.394831						18.17032		0		22.6245		0.798521						18.0534		0								0.596676		18.11186												0		0										0		0										0		0		0		0

																						23.268		0.390635						18.68702		0		23.1402		0.798734						18.5691		0								0.5946845		18.62806												0		0										0		0										0		0		0		0

																						23.7823		0.348783						19.20132		0		23.6575		0.792015						19.0864		0								0.570399		19.14386												0		0										0		0										0		0		0		0

																						24.2997		0.39064						19.71872		0		24.1708		0.776548						19.5997		0								0.583594		19.65921												0		0										0		0										0		0		0		0

																						24.8167		0.347212						20.23572		0		24.6852		0.824105						20.1141		0								0.5856585		20.17491												0		0										0		0										0		0		0		0

																						25.3338		0.341403						20.75282		0		25.2015		0.849189						20.6304		0								0.595296		20.69161												0		0										0		0										0		0		0		0

																						25.8505		0.383563						21.26952		0		25.7177		0.771704						21.1466		0								0.5776335		21.20806												0		0										0		0										0		0		0		0

																						26.3693		0.364448						21.78832		0		26.2323		0.762851						21.6612		0								0.5636495		21.72476												0		0										0		0										0		0		0		0

																						26.8865		0.372337						22.30552		0		26.7477		0.77246						22.1766		0								0.5723985		22.24106												0		0										0		0										0		0		0		0

																						27.4015		0.384478						22.82052		0		27.2635		0.798522						22.6924		0								0.5915		22.75646												0		0										0		0										0		0		0		0

																						27.9193		0.390659						23.33832		0		27.7805		0.821766						23.2094		0								0.6062125		23.27386												0		0										0		0										0		0		0		0

																						28.4348		0.346387						23.85382		0		28.2967		0.795701						23.7256		0								0.571044		23.78971												0		0										0		0										0		0		0		0

																						28.9515		0.396439						24.37052		0		28.8107		0.808249						24.2396		0								0.602344		24.30506												0		0										0		0										0		0		0		0

																						29.467		0.308571						24.88602		0		29.3245		0.786005						24.7534		0								0.547288		24.81971												0		0										0		0										0		0		0		0

																						29.9838		0.390667						25.40282		0		29.8408		0.767584						25.2697		0								0.5791255		25.33626												0		0										0		0										0		0		0		0

																						30.501		0.383582						25.92002		0		30.3552		0.756102						25.7841		0								0.569842		25.85206												0		0										0		0										0		0		0		0

																						31.0182		0.46322						26.43722		0		30.8698		0.816943						26.2987		0								0.6400815		26.36796												0		0										0		0										0		0		0		0

																						31.5365		0.378971						26.95552		0		31.3865		0.789011						26.8154		0								0.583991		26.88546												0		0										0		0										0		0		0		0

																						32.0545		0.390673						27.47352		0		31.9015		0.802944						27.3304		0								0.5968085		27.40196												0		0										0		0										0		0		0		0

																						32.57		0.330728						27.98902		0		32.4157		0.824492						27.8446		0								0.57761		27.91681												0		0										0		0										0		0		0		0

																						33.0857		0.436543						28.50472		0		32.9318		0.766227						28.3607		0								0.601385		28.43271												0		0										0		0										0		0		0		0

																						33.6023		0.390678						29.02132		0		33.4468		0.767582						28.8757		0								0.57913		28.94851												0		0										0		0										0		0		0		0

																						34.1188		0.390679						29.53782		0		33.963		0.819054						29.3919		0								0.6048665		29.46486												0		0										0		0										0		0		0		0

																						34.6347		0.412415						30.05372		0		34.4777		0.794613						29.9066		0								0.603514		29.98016												0		0										0		0										0		0		0		0

																						35.1523		0.390681

																						35.6703		0.339455

																						36.1855		0.385228

																						36.7028		0.439928

																						37.2193		0.435482

																						37.7362		0.395663

																						38.2545		0.372369

																						38.7717		0.376516

																						39.289		0.383603

																						39.8057		0.367149

																						40.3227		0.355918

																						40.8397		0.390319

																						41.3568		0.3376

																						41.8727		0.380237

																						42.3903		0.390695

																						42.9052		0.362348

																						43.4212		0.390696

																						43.9383		0.359569

																						44.4533		0.392025

																						44.9693		0.412449

																						45.4847		0.351206

																						46.0005		0.395673

																						46.5158		0.354059

																						47.0338		0.344139

																						47.5492		0.369438

																						48.067		0.31643

																						48.5818		0.358205

																						49.0987		0.383584

																						49.6163		0.390699

																						50.1348		0.390699

																						50.6505		0.351477

																						51.1652		0.390699

																						51.6828		0.365293

																						52.1997		0.374244

																						52.7162		0.369439

																						53.2333		0.361148

																						53.75		0.322152

																						54.2652		0.377341

																						54.7833		0.3907

																						55.3		0.390699

																						55.8163		0.348178

																						56.3325		0.447985

																						56.8477		0.390699

																						57.3657		0.360071

																						57.8833		0.337

																						58.3997		0.377341

																						58.9157		0.380021

																						59.431		0.372934

																						59.9477		0.383613

																						60.4653		0.372381

																						60.982		0.363012

																						61.4987		0.339006

																						62.0153		0.357184

																						62.5338		0.372381

																						63.0513		0.385244

																						63.567		0.371031

																						64.0847		0.363788

																						64.6015		0.394049

																						65.1195		0.369439

																						65.6372		0.349363





		



GLP-PL -1

GLP-PL -2

Time (min)

Dissolved (mg)



		GLP-PEG 1:5								445.54																GLP-PEG -1				17B-27011								GLP-PEG -2				17B-28013										GLP-PEG 1:5 pH 6.8										GLP-PL FaSSIF-1												GLP-PL FaSSIF-2												GLP-PL FaSSIF-3								GLP-PL 1:5 FaSSIF

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/ml)		IDR (ug/min/cm2)

		GLP-PEG -1		17B-27011		1.024		30		0.15				0.00		0.0000		0.0000

		GLP-PEG -2		17B-28013		0.767		30		0.15				0.00		47.4115		677.3067				Dissolution Profile												Dissolution Profile																								Dissolution Profile												Dissolution Profile												Dissolution Profile

																																																				AVERAGE		TIME																																								AVERAGE		TIME

																						Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (µg)				Weight (mg)		Time zero (min)		%								mg						Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)				Time zero (min)		%		mg

																						4.43723		0						0		0		4.68073		313.226				0.313226		0		0								0.156613		0												0		0										0		0										0		0		0		0

		AVG				0.895								0.000		23.706		338.653				4.95625		0						0.51902		0		5.20052		349.225				0.349225		0.51979		0								0.1746125		0.519405												0		0										0		0										0		0		0		0

		SD				0.182								0.000		33.525		478.928				5.475		0						1.03777		0		5.72032		413.66				0.41366		1.03959		0								0.20683		1.03868												0		0										0		0										0		0		0		0

		RSD				20.300								0.000		141.421		141.421				5.99402		0						1.55679		0		6.23932		405.096				0.405096		1.55859		0								0.202548		1.55769												0		0										0		0										0		0		0		0

		GLP-PL FaSSIF-1		0.00		0.000				0.15		0.00		0.00		0.00		0.00				6.51328		0						2.07605		0		6.75912		473.826				0.473826		2.07839		0								0.236913		2.07722												0		0										0		0										0		0		0		0

		GLP-PL FaSSIF-2		0.00		0.000				0.15		0.00		0.00		0.00		0.00				7.03125		0						2.59402		0		7.27943		481.274				0.481274		2.5987		0								0.240637		2.59636												0		0										0		0										0		0		0		0

		GLP-PL FaSSIF-3		0.00		0.000				0.15		0.00		0.00		0.00		0.00				7.54922		0						3.11199		0		7.8		520.651				0.520651		3.11927		0								0.2603255		3.11563												0		0										0		0										0		0		0		0

		AVG				0.000								0.00		0.00		0.00				8.06823		0						3.631		0		8.32032		545.743				0.545743		3.63959		0								0.2728715		3.635295												0		0										0		0										0		0		0		0

		SD				0.000								0.00		0.00		0.00				8.58515		0						4.14792		0		8.83932		555.919				0.555919		4.15859		0								0.2779595		4.153255												0		0										0		0										0		0		0		0

		RSD				0.000								0.00		0.00		0.00				9.10338		0						4.66615		0		9.36068		567.175				0.567175		4.67995		0								0.2835875		4.67305												0		0										0		0										0		0		0		0

																						9.62213		0						5.1849		0		9.88047		558.499				0.558499		5.19974		0								0.2792495		5.19232												0		0										0		0										0		0		0		0

																						10.1412		0						5.70397		0		10.4003		593.597				0.593597		5.71957		0								0.2967985		5.71177												0		0										0		0										0		0		0		0

																						10.6602		0.909146						6.22297		0		10.9201		581.033				0.581033		6.23937		0								0.7450895		6.23117												0		0										0		0										0		0		0		0

																						11.1766		0.965767						6.73937		0		11.438		587.03				0.58703		6.75727		0								0.7763985		6.74832												0		0										0		0										0		0		0		0

																						11.6945		0.952881						7.25727		0		11.9589		594.674				0.594674		7.27817		0								0.7737775		7.26772												0		0										0		0										0		0		0		0

																						12.2136		0.933083						7.77637		0		12.4797		606.712				0.606712		7.79897		0								0.7698975		7.78767												0		0										0		0										0		0		0		0

																						12.7312		1.05172						8.29397		0		13		612.076				0.612076		8.31927		0								0.831898		8.30662												0		0										0		0										0		0		0		0

																						13.2484		1.00056						8.81117		0		13.5169		618.372				0.618372		8.83617		0								0.809466		8.82367												0		0										0		0										0		0		0		0

																						13.7651		0.97142						9.32787		0		14.0378		620.303				0.620303		9.35707		0								0.7958615		9.34247												0		0										0		0										0		0		0		0

																						14.2802		1.00889						9.84297		0		14.5575		627.208				0.627208		9.87677		0								0.818049		9.85987												0		0										0		0										0		0		0		0

																						14.7951		1.02992						10.35787		0		15.0784		671.621				0.671621		10.39767		0								0.8507705		10.37777												0		0										0		0										0		0		0		0

																						15.3128		1.06781						10.87557		0		15.5953		634.755				0.634755		10.91457		0								0.8512825		10.89507												0		0										0		0										0		0		0		0

																						15.8297		0.988269						11.39247		0		16.1162		637.529				0.637529		11.43547		0								0.812899		11.41397												0		0										0		0										0		0		0		0

																						16.3474		1.14366						11.91017		0		16.6349		631.959				0.631959		11.95417		0								0.8878095		11.93217												0		0										0		0										0		0		0		0

																						16.864		1.09114						12.42677		0		17.1552		628.667				0.628667		12.47447		0								0.8599035		12.45062												0		0										0		0										0		0		0		0

																						17.3807		0.999408						12.94347		0		17.6747		636.143				0.636143		12.99397		0								0.8177755		12.96872												0		0										0		0										0		0		0		0

																						17.895		1.05243						13.45777		0		18.195		624.675				0.624675		13.51427		0								0.8385525		13.48602												0		0										0		0										0		0		0		0

																						18.4105		1.06666						13.97327		0		18.7143		639.75				0.63975		14.03357		0								0.853205		14.00342												0		0										0		0										0		0		0		0

																						18.9287		1.01202						14.49147		0		19.2347		651.833				0.651833		14.55397		0								0.8319265		14.52272												0		0										0		0										0		0		0		0

																						19.4462		0.981658						15.00897		0		19.755		656.392				0.656392		15.07427		0								0.819025		15.04162												0		0										0		0										0		0		0		0

																						19.9617		1.07902						15.52447		0		20.2758		651.424				0.651424		15.59507		0								0.865222		15.55977												0		0										0		0										0		0		0		0

																						20.4795		1.0141						16.04227		0		20.7945		668.558				0.668558		16.11377		0								0.841329		16.07802												0		0										0		0										0		0		0		0

																						20.9962		1.0234						16.55897		0		21.3157		654.604				0.654604		16.63497		0								0.839002		16.59697												0		0										0		0										0		0		0		0

																						21.511		1.01899						17.07377		0		21.8367		647.387				0.647387		17.15597		0								0.8331885		17.11487												0		0										0		0										0		0		0		0

																						22.0263		0.994358						17.58907		0		22.3537		651.209				0.651209		17.67297		0								0.8227835		17.63102												0		0										0		0										0		0		0		0

																						22.5417		1.07149						18.10447		0		22.873		659.145				0.659145		18.19227		0								0.8653175		18.14837												0		0										0		0										0		0		0		0

																						23.0593		1.01328						18.62207		0		23.3913		647.957				0.647957		18.71057		0								0.8306185		18.66632												0		0										0		0										0		0		0		0

																						23.5773		1.00374						19.14007		0		23.914		643.816				0.643816		19.23327		0								0.823778		19.18667												0		0										0		0										0		0		0		0

																						24.094		1.04269						19.65677		0		24.4338		641.327				0.641327		19.75307		0								0.8420085		19.70492												0		0										0		0										0		0		0		0

																						24.6107		1.0562						20.17347		0		24.9547		654.277				0.654277		20.27397		0								0.8552385		20.22372												0		0										0		0										0		0		0		0

																						25.1273		1.11229						20.69007		0		25.475		669.521				0.669521		20.79427		0								0.8909055		20.74217												0		0										0		0										0		0		0		0

																						25.644		1.01049						21.20677		0		25.9948		707.318				0.707318		21.31407		0								0.858904		21.26042												0		0										0		0										0		0		0		0

																						26.1598		1.07727						21.72257		0		26.5152		741.136				0.741136		21.83447		0								0.909203		21.77852												0		0										0		0										0		0		0		0

																						26.6755		1.07348						22.23827		0		27.0348		692.339				0.692339		22.35407		0								0.8829095		22.29617												0		0										0		0										0		0		0		0

																						27.1908		0.963858						22.75357		0		27.5563		688.293				0.688293		22.87557		0								0.8260755		22.81457												0		0										0		0										0		0		0		0

																						27.7078		1.01917						23.27057		0		28.0763		784.723				0.784723		23.39557		0								0.9019465		23.33307												0		0										0		0										0		0		0		0

																						28.2245		1.02147						23.78727		0		28.5948		929.286				0.929286		23.91407		0								0.975378		23.85067												0		0										0		0										0		0		0		0

																						28.7408		1.01795						24.30357		0		29.1162		851.612				0.851612		24.43547		0								0.934781		24.36952												0		0										0		0										0		0		0		0

																						29.2587		0.973445						24.82147		0		29.6375		751.999				0.751999		24.95677		0								0.862722		24.88912												0		0										0		0										0		0		0		0

																						29.7755		1.01141						25.33827		0		30.1563		815.552				0.815552		25.47557		0								0.913481		25.40692												0		0										0		0										0		0		0		0

																						30.2922		0.992087						25.85497		0		30.6772		821.033				0.821033		25.99647		0								0.90656		25.92572												0		0										0		0										0		0		0		0

																						30.8075		1.05389						26.37027		0		31.1968		764.183				0.764183		26.51607		0								0.9090365		26.44317												0		0										0		0										0		0		0		0

																						31.3235		0.971405						26.88627		0		31.7195		778.915				0.778915		27.03877		0								0.87516		26.96252												0		0										0		0										0		0		0		0

																						31.8398		0.975252						27.40257		0		32.239		698.364				0.698364		27.55827		0								0.836808		27.48042												0		0										0		0										0		0		0		0

																						32.3565		1.08289						27.91927		0		32.7573		767.053				0.767053		28.07657		0								0.9249715		27.99792												0		0										0		0										0		0		0		0

																						32.8732		0.998389						28.43597		0		33.2787		706.444				0.706444		28.59797		0								0.8524165		28.51697												0		0										0		0										0		0		0		0

																						33.389		1.05696						28.95177		0		33.7987		738.337				0.738337		29.11797		0								0.8976485		29.03487												0		0										0		0										0		0		0		0

																						33.9065		0.944005						29.46927		0		34.3205		706.063				0.706063		29.63977		0								0.825034		29.55452												0		0										0		0										0		0		0		0

																						34.4222		1.02395						29.98497		0		34.8413		766.885				0.766885		30.16057		0								0.8954175		30.07277												0		0										0		0										0		0		0		0





		



GLP-PEG -1

GLP-PEG -2

Time (min)

Dissolved (mg)



		FULL								445.54																GLP pH 1.5-1				17B-26001								GLP pH 1.5-2				17B-26003						GLP pH 1.5										GLP pH 4-1				17B-26001								GLP pH 4-2				17B-26003						GLP pH 4										GLP pH 5.5-1				17B-26001								GLP pH 5.5-2				17B-26003						GLP pH 5.5										GLP pH 6.8-1				17B-26001								GLP pH 6.8-2				17B-26003						GLP pH 6.8

				Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/min)		IDR (ug/min/cm2)

				GLP pH 1.5-1		17B-26001		0.018		5.46		1.00		5.46		0.33		0.49		6.9657

				GLP pH 1.5-2		17B-26003		0.008		5.33		1.00		5.33		0.14		0.26		3.6446		Dissolution Profile												Dissolution Profile																				Dissolution Profile												Dissolution Profile																				Dissolution Profile												Dissolution Profile																				Dissolution Profile												Dissolution Profile

				GLP pH 4-1		17B-26001		0.024		5.46		1.00		5.46		0.44		0.17		2.38																												AVERAGE		TIME																														AVERAGE		TIME																														AVERAGE		TIME																														AVERAGE		TIME

				GLP pH 4-2		17B-26003		0.014		5.33		1.00		5.33		0.26		0.18		2.61		Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%				%						Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%				%						Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%				%						Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%				%

				GLP pH 5.5-1		17B-26001		0.023		5.46		1.00		5.46		0.42		0.07		1.06		4.44272		11.1339		0.0111339				0		0.2039175824		4.28802		3.87153		0.00387153				0		0.0726365854				0.1382770839		0				36.1282		21.1708		0.0211708				31.68548		0.3877435897		35.8838		11.5002		0.0115002				31.59578		0.2157636023				0.301753596		31.64063				67.6682		20.8508		0.0208508				63.22548		0.3818827839		67.4198		13.5086		0.0135086				63.13178		0.2534446529				0.3176637184		63.17863				99.4342		24.5921		0.0245921				94.99148		0.4504047619		99.1778		19.3387		0.0193387				94.88978		0.3628273921				0.406616077		94.94063

				GLP pH 5.5-2		17B-26003		0.017		5.33		1.00		5.33		0.33		0.12		1.73		4.9599		11.5194		0.0115194				0.51718		0.210978022		4.80522		3.82382		0.00382382				0.5172		0.0717414634				0.1413597427		0.51719				36.6462		21.3981		0.0213981				32.20348		0.3919065934		36.3992		12.4178		0.0124178				32.11118		0.2329793621				0.3124429778		32.15733				68.1838		20.3588		0.0203588				63.74108		0.3728717949		67.9355		13.4551		0.0134551				63.64748		0.2524409006				0.3126563477		63.69428				99.951		24.0195		0.0240195				95.50828		0.4399175824		99.6935		20.0416		0.0200416				95.40548		0.3760150094				0.4079662959		95.45688

				GLP pH 6.8-1		17B-26001		0.047		5.46		1.00		5.46		0.86		1.16		16.63		5.4776		11.8023		0.0118023				1.03488		0.2161593407		5.32213		4.6547		0.0046547				1.03411		0.0873302064				0.1517447735		1.034495				37.164		21.9119		0.0219119				32.72128		0.4013168498		36.9148		12.9878		0.0129878				32.62678		0.243673546				0.3224951979		32.67403				68.7015		19.4597		0.0194597				64.25878		0.3564047619		68.4537		14.024		0.014024				64.16568		0.2631144465				0.3097596042		64.21223				100.467		23.7165		0.0237165				96.02428		0.4343681319		100.209		20.3898		0.0203898				95.92098		0.3825478424				0.4084579871		95.97263

				GLP pH 6.8-2		17B-26003		0.047		5.33		1.00		5.33		0.88		1.02		14.57		5.99323		11.8754		0.0118754				1.55051		0.2174981685		5.83932		4.40174		0.00440174				1.5513		0.0825842402				0.1500412043		1.550905				37.6783		21.0171		0.0210171				33.23558		0.3849285714		37.4292		12.6468		0.0126468				33.14118		0.2372757974				0.3111021844		33.18838				69.2172		20.5598		0.0205598				64.77448		0.3765531136		68.9688		13.2998		0.0132998				64.68078		0.2495272045				0.313040159		64.72763				100.985		26.1685		0.0261685				96.54228		0.4792765568		100.726		20.6035		0.0206035				96.43798		0.3865572233				0.43291689		96.49013

																						6.50755		12.697		0.012697				2.06483		0.2325457875		6.35495		3.5933		0.0035933				2.06693		0.0674165103				0.1499811489		2.06588				38.1973		20.9158		0.0209158				33.75458		0.3830732601		37.9462		12.6809		0.0126809				33.65818		0.2379155722				0.3104944162		33.70638				69.7325		20.7447		0.0207447				65.28978		0.3799395604		69.4847		13.9298		0.0139298				65.19668		0.2613470919				0.3206433262		65.24323				101.505		26.1739		0.0261739				97.06228		0.4793754579		101.246		21.6337		0.0216337				96.95798		0.4058855535				0.4426305057		97.01013

																						7.02292		13.0046		0.0130046				2.5802		0.2381794872		6.87135		3.6561		0.0036561				2.58333		0.0685947467				0.1533871169		2.581765				38.713		21.9028		0.0219028				34.27028		0.4011501832		38.4612		13.1452		0.0131452				34.17318		0.2466266417				0.3238884124		34.22173				70.2515		19.4224		0.0194224				65.80878		0.3557216117		70.005		13.6325		0.0136325				65.71698		0.2557692308				0.3057454212		65.76288				102.023		26.2821		0.0262821				97.58028		0.4813571429		101.762		22.6663		0.0226663				97.47398		0.4252589118				0.4533080273		97.52713

																						7.54323		13.2595		0.0132595				3.10051		0.2428479853		7.38647		4.37268		0.00437268				3.09845		0.0820390244				0.1624435049		3.09948				39.2297		21.9166		0.0219166				34.78698		0.4014029304		38.9765		12.6189		0.0126189				34.68848		0.2367523452				0.3190776378		34.73773				70.7682		19.958		0.019958				66.32548		0.3655311355		70.5213		13.86		0.01386				66.23328		0.2600375235				0.3127843295		66.27938				102.539		26.2764		0.0262764				98.09628		0.4812527473		102.28		22.4276		0.0224276				97.99198		0.4207804878				0.4510166175		98.04413

																						8.05885		13.1866		0.0131866				3.61613		0.2415128205		7.90208		4.69985		0.00469985				3.61406		0.0881772983				0.1648450594		3.615095				39.745		22.1611		0.0221611				35.30228		0.4058809524		39.494		13.0881		0.0130881				35.20598		0.2455553471				0.3257181497		35.25413				71.283		20.0204		0.0200204				66.84028		0.3666739927		71.0383		14.0521		0.0140521				66.75028		0.263641651				0.3151578219		66.79528				103.053		27.6153		0.0276153				98.61028		0.5057747253		102.796		22.9685		0.0229685				98.50798		0.4309287054				0.4683517154		98.55913

																						8.57578		13.6113		0.0136113				4.13306		0.2492912088		8.41927		5.19696		0.00519696				4.13125		0.09750394				0.1733975744		4.132155				40.2617		22.654		0.022654				35.81898		0.4149084249		40.0107		12.5011		0.0125011				35.72268		0.2345422139				0.3247253194		35.77083				71.7995		20.7461		0.0207461				67.35678		0.3799652015		71.5538		13.9198		0.0139198				67.26578		0.2611594747				0.3205623381		67.31128				103.572		26.8023		0.0268023				99.12928		0.4908846154		103.313		23.8344		0.0238344				99.02498		0.4471744841				0.4690295497		99.07713

																						9.09088		13.6334		0.0136334				4.64816		0.2496959707		8.93542		5.39825		0.00539825				4.6474		0.1012804878				0.1754882293		4.64778				40.7783		21.6943		0.0216943				36.33558		0.3973315018		40.5253		12.8982		0.0128982				36.23728		0.2419924953				0.3196619986		36.28643				72.3167		20.0608		0.0200608				67.87398		0.3674139194		72.0693		13.8875		0.0138875				67.78128		0.2605534709				0.3139836952		67.82763				104.092		30.344		0.030344				99.64928		0.5557509158		103.831		23.953		0.023953				99.54298		0.4493996248				0.5025752703		99.59613

																		0.695				9.6086		12.8208		0.0128208				5.16588		0.2348131868		9.45105		4.85072		0.00485072				5.16303		0.0910078799				0.1629105334		5.164455				41.293		22.1909		0.0221909				36.85028		0.4064267399		41.0448		13.5741		0.0135741				36.75678		0.254673546				0.3305501429		36.80353				72.8362		20.8772		0.0208772				68.39348		0.3823663004		72.586		13.9697		0.0139697				68.29798		0.2620956848				0.3222309926		68.34573				104.61		29.7016		0.0297016				100.16728		0.543985348		104.349		24.3037		0.0243037				100.06098		0.4559793621				0.499982355		100.11413

																		0.3475680783				10.1253		14.5069		0.0145069				5.68258		0.2656941392		9.96927		5.25452		0.00525452				5.68125		0.0985838649				0.1821390021		5.681915				41.8083		21.8104		0.0218104				37.36558		0.3994578755		41.5635		13.0709		0.0130709				37.27548		0.2452326454				0.3223452604		37.32053				73.351		21.1014		0.0211014				68.90828		0.3864725275		73.1037		14.4625		0.0144625				68.81568		0.2713414634				0.3289069954		68.86198				105.125		30.7068		0.0307068				100.68228		0.5623956044		104.864		25.4893		0.0254893				100.57598		0.4782232645				0.5203094345		100.62913

																		4.9652582609				10.6425		14.3835		0.0143835				6.19978		0.2634340659		10.4867		5.39198		0.00539198				6.19868		0.1011628518				0.1822984589		6.19923				42.326		23.0855		0.0230855				37.88328		0.4228113553		42.0825		13.482		0.013482				37.79448		0.252945591				0.3378784732		37.83888				73.8677		21.1995		0.0211995				69.42498		0.3882692308		73.618		14.4139		0.0144139				69.32998		0.2704296435				0.3293494371		69.37748				105.642		31.2494		0.0312494				101.19928		0.5723333333		105.382		25.9696		0.0259696				101.09398		0.4872345216				0.5297839275		101.14663

																						11.1596		14.7084		0.0147084				6.71688		0.2693846154		11.0039		5.01972		0.00501972				6.71588		0.0941786116				0.1817816135		6.71638				42.843		23.3268		0.0233268				38.40028		0.4272307692		42.5985		13.1747		0.0131747				38.31048		0.2471801126				0.3372054409		38.35538				74.3847		21.076		0.021076				69.94198		0.386007326		74.1325		14.4092		0.0144092				69.84448		0.2703414634				0.3281743947		69.89323				106.158		31.2849		0.0312849				101.71528		0.5729835165		105.896		25.1605		0.0251605				101.60798		0.472054409				0.5225189627		101.66163

																						11.6766		14.0919		0.0140919				7.23388		0.2580934066		11.519		5.37026		0.00537026				7.23098		0.1007553471				0.1794243768		7.23243				43.3607		23.5911		0.0235911				38.91798		0.4320714286		43.1153		13.3116		0.0133116				38.82728		0.2497485929				0.3409100107		38.87263				74.9003		20.5698		0.0205698				70.45758		0.3767362637		74.648		14.7062		0.0147062				70.35998		0.2759136961				0.3263249799		70.40878				106.677		31.9285		0.0319285				102.23428		0.5847710623		106.414		26.7864		0.0267864				102.12598		0.5025590994				0.5436650809		102.18013

																						12.1932		14.9193		0.0149193				7.75048		0.2732472527		12.0352		5.61235		0.00561235				7.74718		0.1052973734				0.1892723131		7.74883				43.8773		23.4936		0.0234936				39.43458		0.4302857143		43.6328		13.1537		0.0131537				39.34478		0.2467861163				0.3385359153		39.38968				75.4177		20.6047		0.0206047				70.97498		0.3773754579		75.1647		14.3492		0.0143492				70.87668		0.2692157598				0.3232956089		70.92583				107.194		32.3082		0.0323082				102.75128		0.5917252747		106.932		27.2879		0.0272879				102.64398		0.5119681051				0.5518466899		102.69763

																						12.7104		14.7709		0.0147709				8.26768		0.270529304		12.5508		4.88932		0.00488932				8.26278		0.0917320826				0.1811306933		8.26523				44.393		23.4099		0.0234099				39.95028		0.4287527473		44.1508		13.2646		0.0132646				39.86278		0.2488667917				0.3388097695		39.90653				75.933		21.0364		0.0210364				71.49028		0.3852820513		75.6815		14.5598		0.0145598				71.39348		0.2731669794				0.3292245153		71.44188				107.713		31.4422		0.0314422				103.27028		0.5758644689		107.451		27.9728		0.0279728				103.16298		0.5248180113				0.5503412401		103.21663

																						13.2271		14.8317		0.0148317				8.78438		0.2716428571		13.0656		5.60924		0.00560924				8.77758		0.1052390244				0.1884409408		8.78098				44.9098		23.4921		0.0234921				40.46708		0.4302582418		44.6667		13.6062		0.0136062				40.37868		0.2552757974				0.3427670196		40.42288				76.451		21.0558		0.0210558				72.00828		0.3856373626		76.1982		14.9788		0.0149788				71.91018		0.2810281426				0.3333327526		71.95923				108.228		33.0799		0.0330799				103.78528		0.6058589744		107.969		29.0831		0.0290831				103.68098		0.5456491557				0.575754065		103.73313

																						13.7445		15.6637		0.0156637				9.30178		0.2868809524		13.5823		5.81417		0.00581417				9.29428		0.1090838649				0.1979824086		9.29803				45.4255		23.2211		0.0232211				40.98278		0.4252948718		45.1842		13.0198		0.0130198				40.89618		0.2442739212				0.3347843965		40.93948				76.9688		21.4961		0.0214961				72.52608		0.3937014652		76.7157		15.124		0.015124				72.42768		0.2837523452				0.3387269052		72.47688				108.743		33.6077		0.0336077				104.30028		0.615525641		108.488		29.0723		0.0290723				104.19998		0.5454465291				0.5804860851		104.25013

																						14.2609		15.4368		0.0154368				9.81818		0.2827252747		14.0992		5.89386		0.00589386				9.81118		0.1105789869				0.1966521308		9.81468				45.9425		24.3404		0.0243404				41.49978		0.4457948718		45.6997		12.8409		0.0128409				41.41168		0.2409174484				0.3433561601		41.45573				77.483		21.3762		0.0213762				73.04028		0.3915054945		77.2323		15.0359		0.0150359				72.94428		0.2820994371				0.3368024658		72.99228				109.264		33.1379		0.0331379				104.82128		0.6069212454		109.007		29.8248		0.0298248				104.71898		0.559564728				0.5832429867		104.77013

																						14.7805		15.6119		0.0156119				10.33778		0.2859322344		14.6167		6.16529		0.00616529				10.32868		0.1156714822				0.2008018583		10.33323				46.4588		23.3609		0.0233609				42.01608		0.4278553114		46.2175		12.9446		0.0129446				41.92948		0.2428630394				0.3353591754		41.97278				78.001		22.102		0.022102				73.55828		0.4047985348		77.7508		14.9701		0.0149701				73.46278		0.2808649156				0.3428317252		73.51053				109.781		34.3575		0.0343575				105.33828		0.6292582418		109.524		29.37		0.02937				105.23598		0.5510318949				0.5901450683		105.28713

																						15.2961		14.3977		0.0143977				10.85338		0.2636941392		15.1333		6.0779		0.0060779				10.84528		0.1140318949				0.1888630171		10.84933				46.9755		23.7332		0.0237332				42.53278		0.4346739927		46.733		13.4861		0.0134861				42.44498		0.2530225141				0.3438482534		42.48888				78.52		22.5088		0.0225088				74.07728		0.4122490842		78.267		15.2219		0.0152219				73.97898		0.2855891182				0.3489191012		74.02813				110.299		34.2933		0.0342933				105.85628		0.6280824176		110.04		30.0683		0.0300683				105.75198		0.5641332083				0.5961078129		105.80413

																						15.8125		15.3912		0.0153912				11.36978		0.2818901099		15.6492		6.21655		0.00621655				11.36118		0.1166332083				0.1992616591		11.36548				47.4925		23.8228		0.0238228				43.04978		0.4363150183		47.2508		13.2768		0.0132768				42.96278		0.2490956848				0.3427053516		43.00628				79.036		21.2637		0.0212637				74.59328		0.3894450549		78.7842		15.1877		0.0151877				74.49618		0.2849474672				0.3371962611		74.54473				110.816		34.4232		0.0344232				106.37328		0.6304615385		110.556		29.6182		0.0296182				106.26798		0.5556885553				0.5930750469		106.32063

																						16.3294		15.4386		0.0154386				11.88668		0.2827582418		16.1636		6.35158		0.00635158				11.87558		0.1191666041				0.2009624229		11.88113				48.0075		23.6082		0.0236082				43.56478		0.4323846154		47.768		13.351		0.013351				43.47998		0.2504878049				0.3414362101		43.52238				79.5533		21.733		0.021733				75.11058		0.398040293		79.3		15.2842		0.0152842				75.01198		0.2867579737				0.3423991334		75.06128				111.332		34.4222		0.0344222				106.88928		0.6304432234		111.071		31.2247		0.0312247				106.78298		0.5858292683				0.6081362459		106.83613

																						16.8472		14.8924		0.0148924				12.40448		0.2727545788		16.6802		5.77284		0.00577284				12.39218		0.1083084428				0.1905315108		12.39833				48.5258		22.8059		0.0228059				44.08308		0.4176904762		48.2838		13.2871		0.0132871				43.99578		0.2492889306				0.3334897034		44.03943				80.069		20.907		0.020907				75.62628		0.3829120879		79.8152		15.0217		0.0150217				75.52718		0.2818330206				0.3323725543		75.57673				111.853		35.6948		0.0356948				107.41028		0.6537509158		111.59		30.5334		0.0305334				107.30198		0.5728592871				0.6133051014		107.35613

																						17.3643		16.1468		0.0161468				12.92158		0.2957289377		17.198		6.22506		0.00622506				12.90998		0.1167928705				0.2062609041		12.91578				49.0408		21.9652		0.0219652				44.59808		0.4022930403		48.8005		13.2347		0.0132347				44.51248		0.2483058161				0.3252994282		44.55528				80.587		21.5352		0.0215352				76.14428		0.3944175824		80.3333		16.1979		0.0161979				76.04528		0.3039005629				0.3491590726		76.09478				112.368		36.1132		0.0361132				107.92528		0.6614139194		112.109		32.3002		0.0323002				107.82098		0.6060075047				0.6337107121		107.87313

																						17.88		15.7696		0.0157696				13.43728		0.2888205128		17.7135		6.4062		0.0064062				13.42548		0.1201913696				0.2045059412		13.43138				49.5592		23.5668		0.0235668				45.11648		0.4316263736		49.3188		13.1467		0.0131467				45.03078		0.2466547842				0.3391405789		45.07363				81.1023		21.7563		0.0217563				76.65958		0.398467033		80.8485		15.3935		0.0153935				76.56048		0.2888086304				0.3436378317		76.61003				112.886		36.0951		0.0360951				108.44328		0.6610824176		112.624		32.4927		0.0324927				108.33598		0.609619137				0.6353507773		108.38963

																						18.3972		15.8966		0.0158966				13.95448		0.2911465201		18.2288		5.93422		0.00593422				13.94078		0.1113362101				0.2012413651		13.94763				50.0765		21.5198		0.0215198				45.63378		0.3941355311		49.8343		12.8585		0.0128585				45.54628		0.2412476548				0.317691593		45.59003				81.6177		21.712		0.021712				77.17498		0.3976556777		81.3653		15.8844		0.0158844				77.07728		0.2980187617				0.3478372197		77.12613				113.403		36.6025		0.0366025				108.96028		0.6703754579		113.14		33.3334		0.0333334				108.85198		0.6253921201				0.647883789		108.90613

																						18.912		16.2253		0.0162253				14.46928		0.2971666667		18.7467		6.52371		0.00652371				14.45868		0.12239606				0.2097813634		14.46398				50.5932		22.27		0.02227				46.15048		0.4078754579		50.3503		13.0138		0.0130138				46.06228		0.2441613508				0.3260184044		46.10638				82.1343		21.7811		0.0217811				77.69158		0.3989212454		81.8828		15.4401		0.0154401				77.59478		0.2896829268				0.3443020861		77.64318				113.919		37.0864		0.0370864				109.47628		0.6792380952		113.655		33.0639		0.0330639				109.36698		0.6203358349				0.6497869651		109.42163

																						19.4318		15.8825		0.0158825				14.98908		0.2908882784		19.2622		6.12004		0.00612004				14.97418		0.1148225141				0.2028553962		14.98163				51.1092		22.4901		0.0224901				46.66648		0.4119065934		50.8677		13.2226		0.0132226				46.57968		0.2480787992				0.3299926963		46.62308				82.6515		22.1229		0.0221229				78.20878		0.4051813187		82.3995		16.0061		0.0160061				78.11148		0.3003020638				0.3527416912		78.16013				114.439		37.589		0.037589				109.99628		0.6884432234		114.176		33.8884		0.0338884				109.88798		0.635804878				0.6621240507		109.94213

																						19.948		17.1325		0.0171325				15.50528		0.3137820513		19.7792		6.64909		0.00664909				15.49118		0.1247484053				0.2192652283		15.49823				51.6278		22.2986		0.0222986				47.18508		0.4083992674		51.3847		12.9891		0.0129891				47.09668		0.2436979362				0.3260486018		47.14088				83.1713		22.041		0.022041				78.72858		0.4036813187		82.9208		15.4982		0.0154982				78.63278		0.2907729831				0.3472271509		78.68068				114.956		37.3165		0.0373165				110.51328		0.683452381		114.694		34.7608		0.0347608				110.40598		0.6521726079				0.6678124944		110.45963

																						20.4652		16.823		0.016823				16.02248		0.3081135531		20.2935		6.44314		0.00644314				16.00548		0.1208844278				0.2144989904		16.01398				52.1458		23.5272		0.0235272				47.70308		0.4309010989		51.9038		13.5273		0.0135273				47.61578		0.2537954972				0.342348298		47.65943				83.6862		21.6721		0.0216721				79.24348		0.3969249084		83.4375		16.0417		0.0160417				79.14948		0.3009699812				0.3489474448		79.19648				115.474		38.5376		0.0385376				111.03128		0.7058168498		115.209		34.9122		0.0349122				110.92098		0.6550131332				0.6804149915		110.97613

																						20.9815		16.609		0.016609				16.53878		0.3041941392		20.8112		6.80042		0.00680042				16.52318		0.1275876173				0.2158908782		16.53098				52.662		24.3706		0.0243706				48.21928		0.4463479853		52.4205		13.2433		0.0132433				48.13248		0.248467167				0.3474075762		48.17588				84.2032		22.3225		0.0223225				79.76048		0.4088369963		83.9545		15.5253		0.0155253				79.66648		0.2912814259				0.3500592111		79.71348				115.99		38.4809		0.0384809				111.54728		0.7047783883		115.726		34.9211		0.0349211				111.43798		0.6551801126				0.6799792504		111.49263

																						21.4967		15.9014		0.0159014				17.05398		0.2912344322		21.3268		5.97075		0.00597075				17.03878		0.112021576				0.2016280041		17.04638				53.1777		23.482		0.023482				48.73498		0.4300732601		52.9348		13.3878		0.0133878				48.64678		0.2511782364				0.3406257482		48.69088				84.7205		21.6298		0.0216298				80.27778		0.3961501832		84.4708		14.9313		0.0149313				80.18278		0.2801369606				0.3381435719		80.23028				116.506		38.758		0.038758				112.06328		0.7098534799		116.242		35.3567		0.0353567				111.95398		0.6633527205				0.6866031002		112.00863

																						22.012		16.6458		0.0166458				17.56928		0.3048681319		21.844		6.61581		0.00661581				17.55598		0.124124015				0.2144960734		17.56263				53.6927		23.5111		0.0235111				49.24998		0.4306062271		53.451		13.0554		0.0130554				49.16298		0.2449418386				0.3377740329		49.20648				85.2348		21.6316		0.0216316				80.79208		0.3961831502		84.9857		16.3351		0.0163351				80.69768		0.3064746717				0.3513289109		80.74488				117.024		39.2965		0.0392965				112.58128		0.7197161172		116.763		35.974		0.035974				112.47498		0.674934334				0.6973252256		112.52813

																						22.5288		16.5662		0.0165662				18.08608		0.3034102564		22.3612		6.72129		0.00672129				18.07318		0.1261030019				0.2147566291		18.07963				54.2098		23.7199		0.0237199				49.76708		0.4344304029		53.9657		12.4123		0.0124123				49.67768		0.2328761726				0.3336532878		49.72238				85.7523		21.5233		0.0215233				81.30958		0.3941996337		85.5045		16.0673		0.0160673				81.21648		0.3014502814				0.3478249576		81.26303				117.541		39.5458		0.0395458				113.09828		0.7242820513		117.28		36.9903		0.0369903				112.99198		0.6940018762				0.7091419637		113.04513

																						23.044		16.5258		0.0165258				18.60128		0.3026703297		22.8778		7.07465		0.00707465				18.58978		0.1327326454				0.2177014875		18.59553				54.7292		24.1492		0.0241492				50.28648		0.4422930403		54.4837		13.2748		0.0132748				50.19568		0.2490581614				0.3456756008		50.24108				86.2698		22.4429		0.0224429				81.82708		0.4110421245		86.0213		15.9961		0.0159961				81.73328		0.3001144465				0.3555782855		81.78018				118.056		38.9149		0.0389149				113.61328		0.7127271062		117.799		37.3261		0.0373261				113.51098		0.7003020638				0.706514585		113.56213

																						23.5598		16.3495		0.0163495				19.11708		0.2994413919		23.3945		6.98132		0.00698132				19.10648		0.1309816135				0.2152115027		19.11178				55.2448		24.4778		0.0244778				50.80208		0.4483113553		55.0013		13.1812		0.0131812				50.71328		0.2473020638				0.3478067096		50.75768				86.7848		21.7008		0.0217008				82.34208		0.3974505495		86.5393		15.6983		0.0156983				82.25128		0.2945272045				0.345988877		82.29668				118.573		40.4423		0.0404423				114.13028		0.7407014652		118.315		38.1163		0.0381163				114.02698		0.7151275797				0.7279145225		114.07863

																						24.0753		16.8602		0.0168602				19.63258		0.3087948718		23.9105		6.91263		0.00691263				19.62248		0.1296928705				0.2192438712		19.62753				55.7593		23.689		0.023689				51.31658		0.4338644689		55.518		13.3365		0.0133365				51.22998		0.2502157598				0.3420401144		51.27328				87.3003		21.993		0.021993				82.85758		0.4028021978		87.0568		15.9116		0.0159116				82.76878		0.2985290807				0.3506656392		82.81318				119.088		40.4699		0.0404699				114.64528		0.7412069597		118.834		37.7857		0.0377857				114.54598		0.7089249531				0.7250659564		114.59563

																						24.5907		16.6735		0.0166735				20.14798		0.3053754579		24.426		6.85811		0.00685811				20.13798		0.1286699812				0.2170227196		20.14298				56.2782		23.3168		0.0233168				51.83548		0.427047619		56.0347		13.2892		0.0132892				51.74668		0.2493283302				0.3381879746		51.79108				87.8157		21.7435		0.0217435				83.37298		0.3982326007		87.5735		16.2627		0.0162627				83.28548		0.3051163227				0.3516744617		83.32923				119.609		40.6073		0.0406073				115.16628		0.7437234432		119.354		38.5586		0.0385586				115.06598		0.7234258912				0.7335746672		115.11613

																						25.1052		16.8288		0.0168288				20.66248		0.3082197802		24.9438		6.89151		0.00689151				20.65578		0.1292966229				0.2187582016		20.65913				56.795		23.8299		0.0238299				52.35228		0.4364450549		56.5518		13.174		0.013174				52.26378		0.2471669794				0.3418060172		52.30803				88.3338		22.3274		0.0223274				83.89108		0.4089267399		88.0917		16.5628		0.0165628				83.80368		0.3107467167				0.3598367283		83.84738				120.126		40.8557		0.0408557				115.68328		0.7482728938		119.873		39.331		0.039331				115.58498		0.7379174484				0.7430951711		115.63413

																						25.6218		16.6752		0.0166752				21.17908		0.3054065934		25.4593		7.19697		0.00719697				21.17128		0.1350275797				0.2202170866		21.17518				57.3107		23.9823		0.0239823				52.86798		0.4392362637		57.0695		13.421		0.013421				52.78148		0.2518011257				0.3455186947		52.82473				88.8495		21.8896		0.0218896				84.40678		0.4009084249		88.6093		16.7382		0.0167382				84.32128		0.3140375235				0.3574729742		84.36403				120.643		41.8547		0.0418547				116.20028		0.7665695971		120.391		38.1976		0.0381976				116.10298		0.7166529081				0.7416112526		116.15163

																						26.1385		17.4804		0.0174804				21.69578		0.3201538462		25.976		7.02273		0.00702273				21.68798		0.1317585366				0.2259561914		21.69188				57.8247		24.6464		0.0246464				53.38198		0.4513992674		57.5862		13.4002		0.0134002				53.29818		0.2514108818				0.3514050746		53.34008				89.3663		21.8868		0.0218868				84.92358		0.4008571429		89.1253		16.0627		0.0160627				84.83728		0.3013639775				0.3511105602		84.88043				121.158		41.7574		0.0417574				116.71528		0.7647875458		120.909		39.4338		0.0394338				116.62098		0.7398461538				0.7523168498		116.66813

																						26.656		16.277		0.016277				22.21328		0.2981135531		26.4913		6.82324		0.00682324				22.20328		0.1280157598				0.2130646565		22.20828				58.3417		23.9714		0.0239714				53.89898		0.43903663		58.1038		13.2216		0.0132216				53.81578		0.2480600375				0.3435483338		53.85738				89.883		21.1075		0.0211075				85.44028		0.3865842491		89.6403		16.1962		0.0161962				85.35228		0.3038686679				0.3452264585		85.39628				121.674		42.2993		0.0422993				117.23128		0.7747124542		121.428		40.034		0.040034				117.13998		0.7511069418				0.762909698		117.18563

																						27.1718		17.2541		0.0172541				22.72908		0.3160091575		27.0092		7.33506		0.00733506				22.72118		0.1376183865				0.226813772		22.72513				58.858		23.2781		0.0232781				54.41528		0.4263388278		58.6195		12.6064		0.0126064				54.33148		0.2365178236				0.3314283257		54.37338				90.3982		22.4931		0.0224931				85.95548		0.4119615385		90.157		16.2816		0.0162816				85.86898		0.3054709193				0.3587162289		85.91223				122.194		42.6524		0.0426524				117.75128		0.7811794872		121.948		40.2066		0.0402066				117.65998		0.7543452158				0.7677623515		117.70563

																						27.6883		17.4447		0.0174447				23.24558		0.3195		27.5263		7.5185		0.0075185				23.23828		0.1410600375				0.2302800188		23.24193				59.375		24.5426		0.0245426				54.93228		0.4494981685		59.1365		13.4078		0.0134078				54.84848		0.2515534709				0.3505258197		54.89038				90.9162		21.9478		0.0219478				86.47348		0.401974359		90.6765		16.4721		0.0164721				86.38848		0.3090450281				0.3555096936		86.43098				122.712		43.2087		0.0432087				118.26928		0.7913681319		122.464		41.1115		0.0411115				118.17598		0.7713227017				0.7813454168		118.22263

																						28.2038		17.4691		0.0174691				23.76108		0.3199468864		28.0438		7.22993		0.00722993				23.75578		0.1356459662				0.2277964263		23.75843				59.8938		24.0762		0.0240762				55.45108		0.440956044		59.6552		13.3184		0.0133184				55.36718		0.2498761726				0.3454161083		55.40913				91.4328		22.6965		0.0226965				86.99008		0.4156868132		91.1925		16.1977		0.0161977				86.90448		0.3038968105				0.3597918118		86.94728				123.226		42.9929		0.0429929				118.78328		0.7874157509		122.98		40.5824		0.0405824				118.69198		0.7613958724				0.7744058117		118.73763

																						28.7218		17.4119		0.0174119				24.27908		0.3188992674		28.5617		7.44805		0.00744805				24.27368		0.1397382739				0.2293187707		24.27638				60.4087		24.3294		0.0243294				55.96598		0.4455934066		60.1718		13.7112		0.0137112				55.88378		0.2572457786				0.3514195926		55.92488				91.9505		22.4782		0.0224782				87.50778		0.4116886447		91.7098		16.4831		0.0164831				87.42178		0.3092514071				0.3604700259		87.46478				123.743		43.6197		0.0436197				119.30028		0.7988956044		123.494		41.9113		0.0419113				119.20598		0.7863283302				0.7926119673		119.25313

																						29.2372		17.3047		0.0173047				24.79448		0.3169358974		29.0783		6.90892		0.00690892				24.79028		0.1296232645				0.223279581		24.79238				60.925		24.8459		0.0248459				56.48228		0.4550531136		60.6885		13.468		0.013468				56.40048		0.2526829268				0.3538680202		56.44138				92.467		22.0487		0.0220487				88.02428		0.4038223443		92.2242		16.4032		0.0164032				87.93618		0.3077523452				0.3557873448		87.98023				124.261		44.2797		0.0442797				119.81828		0.8109835165		124.009		42.4756		0.0424756				119.72098		0.7969155722				0.8039495444		119.76963

																						29.7528		18.058		0.018058				25.31008		0.3307326007		29.5943		7.25318		0.00725318				25.30628		0.1360821764				0.2334073885		25.30818				61.4407		24.3115		0.0243115				56.99798		0.4452655678		61.2028		13.7052		0.0137052				56.91478		0.2571332083				0.351199388		56.95638				92.9842		22.5485		0.0225485				88.54148		0.4129761905		92.742		17.0974		0.0170974				88.45398		0.3207767355				0.366876463		88.49773				124.783		44.2337		0.0442337				120.34028		0.8101410256		124.528		42.9773		0.0429773				120.23998		0.8063283302				0.8082346779		120.29013

																						30.2672		18.1348		0.0181348				25.82448		0.3321391941		30.1107		7.38183		0.00738183				25.82268		0.1384958724				0.2353175333		25.82358				61.956		24.3922		0.0243922				57.51328		0.4467435897		61.7188		13.3895		0.0133895				57.43078		0.2512101313				0.3489768605		57.47203				93.5022		22.3048		0.0223048				89.05948		0.4085128205		93.2607		16.648		0.016648				88.97268		0.3123452158				0.3604290181		89.01608				125.298		43.8132		0.0438132				120.85528		0.8024395604		125.045		43.04		0.04304				120.75698		0.8075046904				0.8049721254		120.80613

																						30.7842		17.6111		0.0176111				26.34148		0.322547619		30.6277		7.76419		0.00776419				26.33968		0.145669606				0.2341086125		26.34058				62.4727		24.3173		0.0243173				58.02998		0.4453717949		62.2355		14.2743		0.0142743				57.94748		0.2678105066				0.3565911507		57.98873				94.0198		21.7755		0.0217755				89.57708		0.3988186813		93.7763		16.7124		0.0167124				89.48828		0.3135534709				0.3561860761		89.53268				125.814		44.4722		0.0444722				121.37128		0.8145091575		125.562		43.7465		0.0437465				121.27398		0.8207598499				0.8176345037		121.32263

																						31.3018		17.4673		0.0174673				26.85908		0.3199139194		31.144		7.64505		0.00764505				26.85598		0.143434334				0.2316741267		26.85753				62.9897		23.3392		0.0233392				58.54698		0.4274578755		62.7508		13.0801		0.0130801				58.46278		0.2454052533				0.3364315644		58.50488				94.5367		22.9725		0.0229725				90.09398		0.4207417582		94.292		16.8697		0.0168697				90.00398		0.3165046904				0.3686232243		90.04898				126.331		44.7539		0.0447539				121.88828		0.8196684982		126.08		43.9405		0.0439405				121.79198		0.8243996248				0.8220340615		121.84013

																						31.8195		17.7262		0.0177262				27.37678		0.3246556777		31.6587		7.65454		0.00765454				27.37068		0.1436123827				0.2341340302		27.37373				63.5038		23.6981		0.0236981				59.06108		0.4340311355		63.2662		12.9385		0.0129385				58.97818		0.2427485929				0.3383898642		59.01963				95.0547		22.4895		0.0224895				90.61198		0.4118956044		94.8087		16.9481		0.0169481				90.52068		0.3179756098				0.3649356071		90.56633				126.85		45.9381		0.0459381				122.40728		0.8413571429		126.596		43.8085		0.0438085				122.30798		0.8219230769				0.8316401099		122.35763

																						32.3352		16.8978		0.0168978				27.89248		0.3094835165		32.175		7.17478		0.00717478				27.88698		0.134611257				0.2220473868		27.88973				64.0217		24.1861		0.0241861				59.57898		0.4429688645		63.7807		12.7592		0.0127592				59.49268		0.2393846154				0.3411767399		59.53583				95.57		22.7833		0.0227833				91.12728		0.4172765568		95.325		16.9415		0.0169415				91.03698		0.3178517824				0.3675641696		91.08213				127.37		45.6615		0.0456615				122.92728		0.8362912088		127.116		45.1326		0.0451326				122.82798		0.8467654784				0.8415283436		122.87763

																						32.8528		18.4996		0.0184996				28.41008		0.3388205128		32.6917		7.81242		0.00781242				28.40368		0.1465744841				0.2426974984		28.40688				64.5372		24.2809		0.0242809				60.09448		0.4447051282		64.2985		13.8277		0.0138277				60.01048		0.2594315197				0.352068324		60.05248				96.089		23.253		0.023253				91.64628		0.4258791209		95.8422		16.7462		0.0167462				91.55418		0.3141876173				0.3700333691		91.60023				127.887		45.9074		0.0459074				123.44428		0.8407948718		127.631		45.5357		0.0455357				123.34298		0.8543283302				0.847561601		123.39363

																						33.37		18.0643		0.0180643				28.92728		0.3308479853		33.2073		7.89113		0.00789113				28.91928		0.1480512195				0.2394496024		28.92328				65.0542		24.1177		0.0241177				60.61148		0.4417161172		64.8163		13.9357		0.0139357				60.52828		0.2614577861				0.3515869517		60.56988				96.6057		23.1299		0.0231299				92.16298		0.4236245421		96.3575		16.7105		0.0167105				92.06948		0.3135178236				0.3685711829		92.11623				128.403		46.5555		0.0465555				123.96028		0.8526648352		128.147		46.4376		0.0464376				123.85898		0.871249531				0.8619571831		123.90963

																						33.8888		16.9825		0.0169825				29.44608		0.3110347985		33.7255		7.39435		0.00739435				29.43748		0.1387307692				0.2248827839		29.44178				65.5693		23.8206		0.0238206				61.12658		0.4362747253		65.3325		13.2599		0.0132599				61.04448		0.2487786116				0.3425266685		61.08553				97.1223		23.2002		0.0232002				92.67958		0.4249120879		96.874		17.6249		0.0176249				92.58598		0.330673546				0.3777928169		92.63278				128.918		47.0834		0.0470834				124.47528		0.8623333333		128.663		46.655		0.046655				124.37498		0.8753283302				0.8688308318		124.42513

																						34.4055		17.9582		0.0179582				29.96278		0.3289047619		34.242		7.69857		0.00769857				29.95398		0.1444384615				0.2366716117		29.95838				66.0862		23.883		0.023883				61.64348		0.4374175824		65.8487		13.7364		0.0137364				61.56068		0.2577185741				0.3475680783		61.60208				97.6397		23.0987		0.0230987				93.19698		0.4230531136		97.3883		17.4152		0.0174152				93.10028		0.326739212				0.3748961628		93.14863				129.437		46.713		0.046713				124.99428		0.8555494505		129.18		46.89		0.04689				124.89198		0.8797373358				0.8676433932		124.94313





		



GLP pH 1.5

GLP pH 4

GLP pH 5.5

GLP pH 6.8

Time (min)

% Dissolved



		GLP-PVP 1:1								445.54																GLP-PVP 1:1 -pH 1.5				17B-27001								GLP-PVP 1:1 -pH 4.0				17B-27001								GLP-PVP 1:1 -pH 5.5				17B-27001								GLP-PVP 1:1 -pH 6.8				17B-27001

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/min)		IDR (ug/min/cm2)

		GLP-PVP 1:1 -pH 1.5		17B-27001		0.128		10.38		0.44		4.61		2.78		4.5608		65.1550

		GLP-PVP 1:1 -pH 4.0		17B-27001		0.221		10.38		0.44		4.61		4.79		-0.0033		-0.0470				Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile

		GLP-PVP 1:1 -pH 5.5		17B-27001		0.382		10.38		0.44		4.61		8.30		23.53		336.20

		GLP-PVP 1:1 -pH 6.8		17B-27001		1.501		10.38		0.44		4.61		32.58		40.09		572.65				Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%

																						4.78047		0.0274011						0		0.5949510227		36.6787		0.210291						31.89823		4.5659789396		68.2693		0.270099						63.48883		5.864570265		100.072		1.01897						95.29153		22.1245586357

																						5.29713		0.0294653						0.51666		0.6397703147		37.1995		0.204367						32.41903		4.4373530867		68.7872		0.28131						64.00673		6.1079910005		100.591		1.06949						95.81053		23.2214826887

																						5.8151		0.0331818						1.03463		0.7204654501		37.7182		0.205261						32.93773		4.456764213		69.3038		0.281031						64.52333		6.1019331658		101.107		1.1101						96.32653		24.1032341889

																						6.33593		0.0354593						1.55546		0.7699160545		38.2375		0.195991						33.45703		4.2554877686		69.8205		0.279351						65.04003		6.0654558814		101.623		1.13772						96.84253		24.702938115

																						6.85547		0.0376113						2.075		0.8166417188		38.7532		0.197538						33.97273		4.289077268		70.3372		0.286236						65.55673		6.2149476095		102.143		1.16367						97.36253		25.2663818833

																						7.3724		0.0397686						2.59193		0.8634824603		39.2685		0.194816						34.48803		4.2299753822		70.8597		0.28866						66.07923		6.2675791199		102.661		1.1808						97.88053		25.6383199084

																						7.88985		0.0423661						3.10938		0.9198811188		39.7878		0.192869						35.00733		4.1877008151		71.3763		0.286033						66.59583		6.2105399376		103.178		1.19684						98.39753		25.9865911239

																		23.0769230769				8.40807		0.0449157						3.6276		0.9752397404		40.3038		0.190927						35.52333		4.1455348113		71.893		0.290129						67.11253		6.2994750311		103.694		1.21347						98.91353		26.3476728144

																		30				8.92657		0.0467905						4.1461		1.0159466528		40.8212		0.192628						36.04073		4.1824680617		72.408		0.297538						67.62753		6.4603441979		104.211		1.22571						99.43053		26.6134358866

																						9.44662		0.0491554						4.66615		1.0672949445		41.339		0.191137						36.55853		4.1500944718		72.9232		0.293004						68.14273		6.3618989553		104.732		1.24013						99.95153		26.9265325779

																						9.96302		0.0510858						5.18255		1.1092090813		41.8568		0.187914						37.07633		4.0801145387		73.4412		0.296115						68.66073		6.4294470695		105.249		1.25642						100.46853		27.2802319608

																						10.4833		0.0536451						5.70283		1.1647783158		42.3735		0.192032						37.59303		4.1695273108		73.9565		0.295972						69.17603		6.4263421578		105.765		1.2677						100.98453		27.5251508705

																						11.0018		0.0553411						6.22133		1.2016030029		42.8903		0.190452						38.10983		4.1352212934		74.4732		0.298594						69.69273		6.4832727767		106.283		1.2717						101.50253		27.6120015477

																						11.5216		0.0565265						6.74113		1.2273412011		43.4093		0.187768						38.62883		4.076944489		74.992		0.298281						70.21153		6.4764767112		106.798		1.2843						102.01753		27.8855811808

																						12.0414		0.058856						7.26093		1.2779208643		43.9282		0.185829						39.14773		4.0348436232		75.5115		0.299769						70.73103		6.5087851631		107.317		1.28948						102.53653		27.9980528078

																						12.5635		0.0609508						7.78303		1.3234045639		44.4438		0.191552						39.66333		4.1591052296		76.0292		0.302065						71.24873		6.5586374518		107.833		1.31621						103.05253		28.5784324582

																						13.082		0.0631976						8.30153		1.3721885893		44.9617		0.189455						40.18123		4.1135737621		76.5467		0.305659						71.76623		6.6366727853		108.349		1.31996						103.56853		28.6598549681

																						13.6034		0.0640041						8.82293		1.3896998571		45.4778		0.187097						40.69733		4.0623752879		77.0635		0.302866						72.28303		6.5760292999		108.867		1.32005						104.08653		28.6618091083

																						14.12		0.0656058						9.33953		1.4244770395		45.9962		0.190901						41.21573		4.1449702819		77.5787		0.310204						72.79823		6.7353568673		109.383		1.33448						104.60253		28.9751229263

																						14.637		0.0665905						9.85653		1.445857505		46.5128		0.193919						41.73233		4.2104991178		78.0962		0.314229						73.31573		6.8227503612		109.9		1.33116						105.11953		28.9030368642

																						15.155		0.0693286						10.37453		1.5053089648		47.0323		0.192168						42.25183		4.1724802339		78.6152		0.306314						73.83473		6.6508945837		110.417		1.34097						105.63653		29.11603815

																						15.6742		0.0713495						10.89373		1.5491880982		47.5513		0.192795						42.77083		4.1860940775		79.133		0.309579						74.35253		6.7217864489		110.934		1.34208						106.15353		29.140139213

																						16.1932		0.0736732						11.41273		1.5996418278		48.069		0.192014						43.28853		4.1691364828		79.6485		0.309115						74.86803		6.7117117704		111.451		1.35398						106.67053		29.3985199776

																						16.7125		0.0759705						11.93203		1.649522343		48.5843		0.190623						43.80383		4.1389341598		80.1663		0.310977						75.38583		6.7521407606		111.968		1.34505						107.18753		29.2046258408

																						17.233		0.0789663						12.45253		1.7145691577		49.099		0.190681						44.31853		4.1401934946		80.688		0.312755						75.90753		6.7907458866		112.488		1.35372						107.70753		29.3928746836

																						17.7528		0.0809326						12.97233		1.7572627793		49.6143		0.193892						44.83383		4.2099128757		81.2057		0.308481						76.42523		6.6979459381		113.003		1.37944						108.22253		29.951324538

																						18.2708		0.0833257						13.49033		1.8092233682		50.1325		0.193286						45.35203		4.1967549981		81.7212		0.318962						76.94073		6.925516425		113.52		1.37718						108.73953		29.9022539053

																						18.792		0.084281						14.01153		1.8299654812		50.6527		0.194371						45.87223		4.2203132443		82.2385		0.320346						77.45803		6.9555667593		114.036		1.3813						109.25553		29.9917101029

																						19.3112		0.0867128						14.53073		1.8827663504		51.1682		0.190848						46.38773		4.1438195104		82.756		0.323951						77.97553		7.0338409321		114.551		1.38065						109.77053		29.9775968678

																						19.83		0.0904765						15.04953		1.9644863238		51.6847		0.192273						46.90423		4.1747600641		83.2735		0.325759						78.49303		7.0730974382		115.07		1.36747						110.28953		29.6914238865

																						20.3527		0.0887838						15.57223		1.9277332885		52.2003		0.19539						47.41983		4.2424384544		83.794		0.322739						79.01353		7.0075251769		115.585		1.39333						110.80453		30.2529135145

																						20.8727		0.0914244						16.09223		1.9850677631		52.7182		0.198623						47.93773		4.3126355142		84.312		0.32533						79.53153		7.0637827031		116.102		1.39213						111.32153		30.2268583114

																						21.3925		0.0936118						16.61203		2.0325620559		53.2357		0.199655						48.45523		4.3350429889		84.8272		0.322152						80.04673		6.99477984		116.618		1.40577						111.83753		30.5230191206

																						21.9112		0.096467						17.13073		2.0945560693		53.7515		0.195489						48.97103		4.2445880086		85.3453		0.327313						80.56483		7.1068389263		117.136		1.39769						112.35553		30.3475807527

																						22.4282		0.0986871						17.64773		2.1427603664		54.2693		0.197141						49.48883		4.2804573383		85.864		0.33685						81.08353		7.3139126534		117.653		1.40187						112.87253		30.4383397103

																						22.9497		0.10099						18.16923		2.1927624725		54.7848		0.198849						50.00433		4.3175425775		86.382		0.337858						81.60153		7.3357990241		118.169		1.41492						113.38853		30.7216900447

																						23.4677		0.0984869						18.68723		2.13841349		55.3015		0.1985						50.52103		4.3099648559		86.8987		0.329313						82.11823		7.1502642649		118.684		1.41006						113.90353		30.6161664719

																						23.9838		0.102353						19.20333		2.2223568408		55.8205		0.199924						51.04003		4.340883697		87.4133		0.338469						82.63283		7.349065465		119.201		1.41605						114.42053		30.746225361

																						24.5055		0.103665						19.72503		2.2508438629		56.342		0.197977						51.56153		4.2986091298		87.9333		0.340349						83.15283		7.3898852833		119.718		1.42398						114.93753		30.9184068285

																						25.0272		0.107126						20.24673		2.3259914113		56.8628		0.201804						52.08233		4.3817035152		88.4505		0.340602						83.67003		7.3953785886		120.237		1.43142						115.45653		31.0799490881

																						25.5427		0.106202						20.76223		2.3059289049		57.381		0.205526						52.60053		4.4625180704		88.9695		0.33802						84.18903		7.3393164765		120.756		1.43576						115.97553		31.1741820729

																						26.0628		0.109119						21.28233		2.3692647612		57.8985		0.203806						53.11803		4.4251722792		89.4862		0.347053						84.70573		7.5354470183		121.274		1.43446						116.49353		31.1459556028

																						26.5847		0.110113						21.80423		2.3908471545		58.4158		0.203148						53.63533		4.4108853428		90.0045		0.34858						85.22403		7.5686022643		121.789		1.44347						117.00853		31.3415867532

																						27.1032		0.110359						22.32273		2.3961884712		58.933		0.206114						54.15253		4.4752851199		90.5223		0.35641						85.74183		7.7386124649		122.306		1.45723						117.52553		31.6403530827

																						27.6217		0.111596						22.84123		2.4230470431		59.4503		0.205105						54.66983		4.4533770366		91.038		0.348974						86.25753		7.577157056		122.826		1.44399						118.04553		31.3528773412

																						28.1425		0.113724						23.36203		2.4692516034		59.9675		0.206841						55.18703		4.4910702305		91.5565		0.351913						86.77603		7.6409705911		123.344		1.459						118.56353		31.6787845074

																						28.662		0.114449						23.88153		2.4849932886		60.4865		0.208552						55.70603		4.5282206077		92.0722		0.353682						87.29173		7.679380303		123.858		1.44391						119.07753		31.3511403277

																						29.1797		0.117861						24.39923		2.5590769163		61.0032		0.209767						56.22273		4.5546015009		92.5898		0.356916						87.80933		7.7495990756		124.374		1.46522						119.59353		31.8138373104

																						29.6967		0.117118						24.91623		2.542944403		61.5188		0.206643						56.73833		4.486771122		93.1065		0.350056						88.32603		7.6006501642		124.891		1.455						120.11053		31.5919338302

																						30.213		0.115075						25.43253		2.4985854196		62.0352		0.210268						57.25473		4.5654795482		93.624		0.358864						88.84353		7.7918953554		125.412		1.45821						120.63153		31.6616314987

																						30.7307		0.121781						25.95023		2.6441905799		62.5542		0.211411						57.77373		4.5902971292		94.1432		0.360612						89.36273		7.8298491013		125.929		1.48048						121.14853		32.1451726439

																						31.249		0.121092						26.46853		2.6292305508		63.0723		0.212609						58.29183		4.616308907		94.6598		0.356936						89.87933		7.7500333289		126.446		1.46256						121.66553		31.7560816101

																						31.7653		0.122684						26.98483		2.6637971203		63.5888		0.212734						58.80833		4.6190229907		95.176		0.367176						90.39553		7.9723710626		126.962		1.47155						122.18153		31.9512785071

																						32.2813		0.122246						27.50083		2.6542869711		64.1057		0.215086						59.32523		4.6700911889		95.6922		0.367399						90.91173		7.9772129878		127.477		1.48583						122.69653		32.2613354247

																						32.798		0.121939						28.01753		2.6476211817		64.6227		0.216252						59.84223		4.6954081613		96.2092		0.373727						91.42873		8.1146107591		127.997		1.47543						123.21653		32.035523664

																						33.3147		0.123059						28.53423		2.6719393713		65.1398		0.214865						60.35933		4.665292689		96.7307		0.365689						91.95023		7.9400843233		128.515		1.48669						123.73453		32.2800083203

																						33.8325		0.121113						29.05203		2.6296865168		65.656		0.216769						60.87553		4.7066336113		97.2462		0.368128						92.46573		7.9930415237		129.03		1.47604						124.24953		32.0487683923

																						34.3527		0.126441						29.57223		2.7453716188		66.1713		0.220178						61.39083		4.7806521009		97.7625		0.37497						92.98203		8.1415996071		129.548		1.48318						124.76753		32.2037968511

																						34.8712		0.127954						30.09073		2.7782228875		66.6883		0.220628						61.90783		4.7904228021		98.2787		0.38206						93.49823		8.2955424324		130.065		1.50057						125.28453		32.5813801702





		



GLP-PVP 1:1 -pH 1.5

GLP-PVP 1:1 -pH 4.0

GLP-PVP 1:1 -pH 5.5

GLP-PVP 1:1 -pH 6.8

Time (min)

% Dissolved



		GLP-PVP 1:2								445.54																GLP-PVP 1:2 pH 1.5				17C-09018								GLP-PVP 1:2 pH 4.0				17C-09018								GLP-PVP 1:2 pH 5.5				17C-09018								GLP-PVP 1:2 pH 6.8				17C-09018

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/min)		IDR (ug/min/cm2)

		GLP-PVP 1:2 pH 1.5		17C-09018		0.111		14.31		0.28		4.01		2.77		13.0298		186.1403

		GLP-PVP 1:2 pH 4.0		17C-09018		0.114		14.31		0.28		4.01		2.84		-1.3681		-19.5440				Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile

		GLP-PVP 1:2 pH 5.5		17C-09018		0.146		14.31		0.28		4.01		3.65		0.04		0.55

		GLP-PVP 1:2 pH 6.8		17C-09018		0.531		14.31		0.28		4.01		13.26		24.57		350.93				Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%

																						4.3698		42.2347		0.0422347				0		1.0540755715		35.9855		137.948		0.137948				31.6157		3.4428471598		67.5093		123.109		0.123109				63.1395		3.072501747		99.192		250.506		0.250506				94.8222		6.2520215633

																						4.88723		59.2164		0.0592164				0.51743		1.4778975741		36.501		137.514		0.137514				32.1312		3.4320155735		68.0235		123.804		0.123804				63.6537		3.0898472597		99.7088		276.98		0.27698				95.339		6.9127483278

																						5.40468		74.0283		0.0740283				1.03488		1.8475666367		37.0157		135.975		0.135975				32.6459		3.39360587		68.5397		124.642		0.124642				64.1699		3.1107617051		100.227		297.627		0.297627				95.8572		7.4280473196

																						5.92032		85.9732		0.0859732				1.55052		2.14568234		37.5313		135.363		0.135363				33.1615		3.3783318359		69.0552		125.849		0.125849				64.6854		3.1408854947		100.745		316.91		0.31691				96.3752		7.9093041829

																						6.43542		95.4449		0.0954449				2.06562		2.3820729759		38.0445		134.584		0.134584				33.6747		3.3588898872		69.5703		127.662		0.127662				65.2005		3.1861335729		101.262		331.496		0.331496				96.8922		8.2733353299

																						6.95338		102.154		0.102154				2.58358		2.5495158231		38.5607		134.514		0.134514				34.1909		3.3571428571		70.0883		127.437		0.127437				65.7185		3.1805181192		101.777		344.531		0.344531				97.4072		8.5986572826

																						7.46745		107.998		0.107998				3.09765		2.6953678746		39.0765		133.205		0.133205				34.7067		3.3244733952		70.6028		128.506		0.128506				66.233		3.2071977638		102.292		355.821		0.355821				97.9222		8.8804282719

																						7.98307		112.556		0.112556				3.61327		2.8091244884		39.5903		132.744		0.132744				35.2205		3.3129679545		71.1177		129.36		0.12936				66.7479		3.2285115304		102.808		365.497		0.365497				98.4382		9.1219177398

																						8.49688		115.769		0.115769				4.12708		2.8893131676		40.106		132.593		0.132593				35.7362		3.3091993611		71.6318		130.07		0.13007				67.262		3.2462314066		103.324		374.97		0.37497				98.9542		9.3583408206

																						9.01147		117.841		0.117841				4.64167		2.9410252571		40.6235		131.009		0.131009				36.2537		3.2696665668		72.148		130.458		0.130458				67.7782		3.2559149446		103.842		382.59		0.38259				99.4722		9.5485175202

																						9.52527		119.694		0.119694				5.15547		2.9872716382		41.1397		131		0.131				36.7699		3.2694419487		72.6648		130.436		0.130436				68.295		3.255365878		104.357		390.418		0.390418				99.9872		9.7438853948

																						10.0409		120.683		0.120683				5.6711		3.011954677		41.6565		129.984		0.129984				37.2867		3.2440850554		73.181		131.282		0.131282				68.8112		3.276479984		104.873		396.692		0.396692				100.5032		9.9004692024

																						10.555		122.362		0.122362				6.1852		3.0538584407		42.1718		129.517		0.129517				37.802		3.2324298692		73.6967		131.679		0.131679				69.3269		3.2863881402		105.387		403.048		0.403048				101.0172		10.0590995308

																						11.0688		122.12		0.12212				6.699		3.0478187082		42.6878		129.123		0.129123				38.318		3.2225965858		74.2117		131.919		0.131919				69.8419		3.2923779575		105.902		407.99		0.40799				101.5322		10.1824398523

																						11.5815		123.631		0.123631				7.2117		3.0855295997		43.2033		128.535		0.128535				38.8335		3.2079215334		74.7253		131.908		0.131908				70.3555		3.2921034242		106.421		413.769		0.413769				102.0512		10.3266696616

																						12.0977		123.839		0.123839				7.7279		3.0907207747		43.7208		128.383		0.128383				39.351		3.2041279824		75.2413		133.16		0.13316				70.8715		3.3233503045		106.935		417.226		0.417226				102.5652		10.4129479884

																						12.6162		123.861		0.123861				8.2464		3.0912698413		44.238		127.814		0.127814				39.8682		3.1899271239		75.757		133.497		0.133497				71.3872		3.3317610063		107.449		422.426		0.422426				103.0792		10.5427273635

																						13.1326		124.758		0.124758				8.7628		3.1136567835		44.7557		127.19		0.12719				40.3859		3.1743535989		76.2732		134.808		0.134808				71.9034		3.3644803833		107.964		426.723		0.426723				103.5942		10.6499700509

																						13.6482		123.852		0.123852				9.2784		3.0910452231		45.269		125.746		0.125746				40.8992		3.1383148647		76.7888		134.326		0.134326				72.419		3.3524508336		108.479		430.429		0.430429				104.1092		10.7424628132

																						14.1638		124.946		0.124946				9.794		3.118348807		45.783		126.541		0.126541				41.4132		3.1581561346		77.3038		133.857		0.133857				72.934		3.3407457323		108.998		435.279		0.435279				104.6282		10.863507038

																						14.6789		124.87		0.12487				10.3091		3.1164520315		46.2963		125.327		0.125327				41.9265		3.127857642		77.8213		135.237		0.135237				73.4515		3.3751871818		109.512		438.652		0.438652				105.1422		10.9476889288

																						15.1945		124.687		0.124687				10.8247		3.1118847958		46.812		124.967		0.124967				42.4422		3.118872916		78.336		136.182		0.136182				73.9662		3.3987720875		110.027		442.148		0.442148				105.6572		11.034940601

																						15.7112		125.092		0.125092				11.3414		3.1219926126		47.3282		125.051		0.125051				42.9584		3.1209693521		78.8515		135.664		0.135664				74.4817		3.3858440651		110.543		445.958		0.445958				106.1732		11.1300289508

																						16.2266		125.093		0.125093				11.8568		3.1220175701		47.8438		124.162		0.124162				43.474		3.0987820705		79.3667		136.653		0.136653				74.9969		3.4105271039		111.059		448.279		0.448279				106.6892		11.1879554757

																						16.7413		125.455		0.125455				12.3715		3.1310522112		48.3587		122.62		0.12262				43.9889		3.0602974943		79.88		135.978		0.135978				75.5102		3.3936807427		111.576		451.305		0.451305				107.2062		11.2634770889

																						17.2583		124.922		0.124922				12.8885		3.1177498253		48.873		123.144		0.123144				44.5032		3.0733752621		80.3973		137.423		0.137423				76.0275		3.4297444345		112.092		454.643		0.454643				107.7222		11.3467854647

																						17.7753		124.819		0.124819				13.4055		3.1151791954		49.3897		123.228		0.123228				45.0199		3.0754716981		80.9135		137.476		0.137476				76.5437		3.4310671858		112.609		457.905		0.457905				108.2392		11.428197065

																						18.2885		125.144		0.125144				13.9187		3.1232904063		49.9052		123.172		0.123172				45.5354		3.0740740741		81.4272		137.846		0.137846				77.0574		3.4403014875		113.122		461.813		0.461813				108.7522		11.5257312569

																						18.8037		124.863		0.124863				14.4339		3.1162773285		50.4198		122.587		0.122587				46.05		3.0594738944		81.9408		137.898		0.137898				77.571		3.4415992812		113.638		465.988		0.465988				109.2682		11.6299291205

																						19.3203		124.851		0.124851				14.9505		3.1159778377		50.936		122.942		0.122942				46.5662		3.0683338325		82.456		138.949		0.138949				78.0862		3.4678296895		114.156		469.405		0.469405				109.7862		11.7152091445

																						19.8365		125.081		0.125081				15.4667		3.1217180793		51.4515		121.994		0.121994				47.0817		3.0446740541		82.973		138.944		0.138944				78.6032		3.4677049017		114.671		473.471		0.473471				110.3012		11.8166866327

																						20.35		124.195		0.124195				15.9802		3.0996056704		51.969		121.081		0.121081				47.5992		3.0218877908		83.4872		139.203		0.139203				79.1174		3.4741689128		115.186		475.502		0.475502				110.8162		11.8673754617

																						20.8652		123.788		0.123788				16.4954		3.0894479385		52.4837		121.263		0.121263				48.1139		3.0264300689		84.0028		139.321		0.139321				79.633		3.4771139064		115.701		479.337		0.479337				111.3312		11.9630877508

																						21.3813		123.248		0.123248				17.0115		3.0759708496		52.9997		120.364		0.120364				48.6299		3.0039932115		84.518		140.116		0.140116				80.1482		3.4969551762		116.217		481.696		0.481696				111.8472		12.0219626635

																						21.8948		122.583		0.122583				17.525		3.0593740641		53.5143		120.131		0.120131				49.1445		2.9981780972		85.0325		140.059		0.140059				80.6627		3.4955325946		116.737		484.798		0.484798				112.3672		12.0993810522

																						22.411		122.166		0.122166				18.0412		3.0489667565		54.03		120.195		0.120195				49.6602		2.9997753819		85.5515		141.407		0.141407				81.1817		3.5291754018		117.253		486.596		0.486596				112.8832		12.1442547669

																						22.926		121.59		0.12159				18.5562		3.034591195		54.5467		120.554		0.120554				50.1769		3.0087351502		86.0667		140.981		0.140981				81.6969		3.5185434761		117.768		489.382		0.489382				113.3982		12.2137865628

																						23.4422		121.525		0.121525				19.0724		3.0329689528		55.0607		119.053		0.119053				50.6909		2.9712738345		86.5813		141.313		0.141313				82.2115		3.52682939		118.284		492.303		0.492303				113.9142		12.286687631

																						23.9573		121.129		0.121129				19.5875		3.0230857542		55.5753		119.589		0.119589				51.2055		2.9846510931		87.0948		141.495		0.141495				82.725		3.5313716682		118.8		493.846		0.493846				114.4302		12.3251971648

																						24.473		120.338		0.120338				20.1032		3.0033443147		56.0908		119.337		0.119337				51.721		2.978361785		87.6097		142.01		0.14201				83.2399		3.5442248178		119.319		496.252		0.496252				114.9492		12.3852450834

																						24.9885		120.009		0.120009				20.6187		2.9951332734		56.607		118.666		0.118666				52.2372		2.9616152541		88.1272		142.415		0.142415				83.7574		3.5543326345		119.834		499.1		0.4991				115.4642		12.4563242488

																						25.5047		119.522		0.119522				21.1349		2.9829789358		57.1245		118.195		0.118195				52.7547		2.9498602376		88.6432		142.981		0.142981				84.2734		3.5684586203		120.35		500.806		0.500806				115.9802		12.4989018668

																						26.0205		119.025		0.119025				21.6507		2.9705750225		57.639		118.369		0.118369				53.2692		2.9542028551		89.1573		142.517		0.142517				84.7875		3.5568783069		120.865		503.621		0.503621				116.4952		12.5691574324

																						26.5367		118.766		0.118766				22.1669		2.9641110113		58.1557		116.929		0.116929				53.7859		2.9182639513		89.6705		143.051		0.143051				85.3007		3.5702056504		121.38		504.788		0.504788				117.0102		12.598282919

																						27.0513		117.895		0.117895				22.6815		2.942372966		58.6708		117.227		0.117227				54.301		2.9257013078		90.1855		143.224		0.143224				85.8157		3.5745233104		121.898		506.699		0.506699				117.5282		12.6459768394

																						27.5662		117.819		0.117819				23.1964		2.9404761905		59.186		116.864		0.116864				54.8162		2.9166417091		90.7028		143.361		0.143361				86.333		3.5779424978		122.411		508.822		0.508822				118.0412		12.698961765

																						28.0848		117.12		0.11712				23.715		2.9230308476		59.701		117.169		0.117169				55.3312		2.9242537686		91.2175		143.977		0.143977				86.8477		3.5933163622		122.925		509.58		0.50958				118.5552		12.7178796047

																						28.601		116.658		0.116658				24.2312		2.9115004492		60.2167		115.828		0.115828				55.8469		2.8907856644		91.7333		143.213		0.143213				87.3635		3.5742487771		123.439		511.96		0.51196				119.0692		12.7772786263

																						29.1152		116.407		0.116407				24.7454		2.9052360986		60.7318		116.58		0.11658				56.362		2.9095537586		92.2482		143.922		0.143922				87.8784		3.5919436957		123.955		514.707		0.514707				119.5852		12.845837077

																						29.6302		115.563		0.115563				25.2604		2.8841719078		61.2473		116.52		0.11652				56.8775		2.9080563043		92.7643		144.436		0.144436				88.3945		3.6047718878		124.472		516.92		0.51692				120.1022		12.9010681841

																						30.145		115.549		0.115549				25.7752		2.8838225017		61.763		116.456		0.116456				57.3932		2.9064590197		93.2823		144.957		0.144957				88.9125		3.6177747829		124.986		518.725		0.518725				120.6162		12.9461166018

																						30.6587		114.845		0.114845				26.2889		2.866252371		62.2805		115.617		0.115617				57.9107		2.8855196167		93.7977		144.669		0.144669				89.4279		3.6105870021		125.501		520.409		0.520409				121.1312		12.9881451532

																						31.1777		114.194		0.114194				26.8079		2.8500049915		62.795		115.476		0.115476				58.4252		2.882000599		94.312		144.826		0.144826				89.9422		3.6145053409		126.017		520.85		0.52085				121.6472		12.9991514425

																						31.6922		113.648		0.113648				27.3224		2.8363781571		63.3107		115.713		0.115713				58.9409		2.8879155436		94.8272		145.377		0.145377				90.4574		3.6282569632		126.531		523.166		0.523166				122.1612		13.0569531796

																						32.2065		113.283		0.113283				27.8367		2.8272686433		63.8253		115.429		0.115429				59.4555		2.8808275931		95.3403		145.578		0.145578				90.9705		3.6332734352		127.051		524.512		0.524512				122.6812		13.0905460717

																						32.72		112.147		0.112147				28.3502		2.7989168414		64.339		114.143		0.114143				59.9692		2.8487321553		95.8583		145.544		0.145544				91.4885		3.6324248777		127.564		526.195		0.526195				123.1942		13.1325496656

																						33.237		111.836		0.111836				28.8672		2.7911550364		64.856		114.929		0.114929				60.4862		2.868348807		96.373		145.437		0.145437				92.0032		3.6297544175		128.079		527.492		0.527492				123.7092		13.1649196366

																						33.7513		111.19		0.11119				29.3815		2.7750324448		65.3693		114.155		0.114155				60.9995		2.8490316462		96.8897		145.991		0.145991				92.5199		3.6435809124		128.595		529.281		0.529281				124.2252		13.2095687332

																						34.2658		110.879		0.110879				29.896		2.7672706399		65.8855		113.748		0.113748				61.5157		2.8388739143		97.4042		146.384		0.146384				93.0344		3.6533892383		129.11		531.167		0.531167				124.7402		13.2566387142





		



GLP-PVP 1:2 pH 1.5

GLP-PVP 1:2 pH 4.0

GLP-PVP 1:2 pH 5.5

GLP-PVP 1:2 pH 6.8

Time (min)

% Dissolved



		GLP-PVP 1:2								445.54																GLP-PVP 1:2 pH 1.5				17B-27019								GLP-PVP 1:2 pH 4.0				17B-27019								GLP-PVP 1:2 pH 5.5				17B-27019								GLP-PVP 1:2 pH 6.8				17B-27019

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/min)		IDR (ug/min/cm2)

		GLP-PVP 1:2 pH 1.5		17B-27019		0.512		15.75		0.28		4.41		11.61		76.4608		1092.2977

		GLP-PVP 1:2 pH 4.0		17B-27019		0.355		15.75		0.28		4.41		8.04		-0.0325		-0.4638				Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile

		GLP-PVP 1:2 pH 5.5		17B-27019		0.443		15.75		0.28		4.41		10.04		13.88		198.22

		GLP-PVP 1:2 pH 6.8		17B-27019		1.501		15.75		0.28		4.41		34.04		67.93		970.38				Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%

																						4.39688		0.106057						0		2.4049206349		36.2143		0.637718						31.81742		14.4607256236		67.7755		0.424717						63.37862		9.6307709751		99.532		0.871843						95.13512		19.7696825397

																						4.91537		0.163208						0.51849		3.700861678		36.7343		0.620877						32.33742		14.0788435374		68.292		0.428014						63.89512		9.7055328798		100.048		0.946888						95.65112		21.47138322

																						5.43333		0.222265						1.03645		5.0400226757		37.2537		0.578269						32.85682		13.112675737		68.8063		0.433811						64.40942		9.836984127		100.563		1.01353						96.16612		22.9825396825

																						5.95208		0.271511						1.5552		6.1567120181		37.7723		0.560313						33.37542		12.7055102041		69.3217		0.427774						64.92482		9.7000907029		101.08		1.06442						96.68312		24.1365079365

																						6.4698		0.309521						2.07292		7.01861678		38.288		0.548953						33.89112		12.4479138322		69.8383		0.4336						65.44142		9.8321995465		101.6		1.11448						97.20312		25.2716553288

																						6.98828		0.348035						2.5914		7.8919501134		38.8038		0.526921						34.40692		11.9483219955		70.3542		0.428051						65.95732		9.7063718821		102.117		1.1412						97.72012		25.8775510204

																						7.50938		0.383855						3.1125		8.7041950113		39.3217		0.515257						34.92482		11.6838321995		70.8688		0.427056						66.47192		9.6838095238		102.632		1.16525						98.23512		26.4229024943

																						8.03098		0.418367						3.6341		9.4867800454		39.8378		0.496765						35.44092		11.2645124717		71.3865		0.432118						66.98962		9.7985941043		103.149		1.18923						98.75212		26.9666666667

																						8.5487		0.454286						4.15182		10.3012698413		40.357		0.477847						35.96012		10.8355328798		71.9022		0.437386						67.50532		9.9180498866		103.665		1.20903						99.26812		27.4156462585

																						9.06745		0.487768						4.67057		11.0604988662		40.8742		0.474039						36.47732		10.7491836735		72.4175		0.442105						68.02062		10.0250566893		104.186		1.26033						99.78912		28.5789115646

																						9.58438		0.523179						5.1875		11.8634693878		41.3917		0.451252						36.99482		10.2324716553		72.9355		0.43974						68.53862		9.9714285714		104.702		1.26194						100.30512		28.6154195011

																						10.1055		0.558419						5.70862		12.6625623583		41.9078		0.458895						37.51092		10.4057823129		73.4508		0.434885						69.05392		9.8613378685		105.218		1.28192						100.82112		29.0684807256

																						10.6247		0.594377						6.22782		13.4779365079		42.4245		0.446429						38.02762		10.123106576		73.9685		0.434275						69.57162		9.8475056689		105.734		1.29437						101.33712		29.3507936508

																						11.1453		0.626659						6.74842		14.2099546485		42.9407		0.44138						38.54382		10.00861678		74.4857		0.434878						70.08882		9.8611791383		106.251		1.30688						101.85412		29.6344671202

																						11.6638		0.655163						7.26692		14.8563038549		43.4575		0.436736						39.06062		9.9033106576		75.0032		0.445847						70.60632		10.1099092971		106.77		1.3238						102.37312		30.0181405896

																						12.182		0.682569						7.78512		15.477755102		43.9732		0.43239						39.57632		9.8047619048		75.5213		0.442323						71.12442		10.03		107.286		1.29231						102.88912		29.3040816327

																						12.6997		0.708489						8.30282		16.0655102041		44.4908		0.426377						40.09392		9.6684126984		76.037		0.443284						71.64012		10.0517913832		107.804		1.35418						103.40712		30.7070294785

																						13.219		0.72946						8.82212		16.5410430839		45.0065		0.425645						40.60962		9.651814059		76.5545		0.440918						72.15762		9.9981405896		108.32		1.3591						103.92312		30.8185941043

																						13.737		0.749623						9.34012		16.9982539683		45.524		0.421812						41.12712		9.5648979592		77.0713		0.439638						72.67442		9.9691156463		108.836		1.37214						104.43912		31.1142857143

																						14.2573		0.759938						9.86042		17.232154195		46.0398		0.409722						41.64292		9.2907482993		77.5875		0.444384						73.19062		10.0767346939		109.354		1.37324						104.95712		31.1392290249

																						14.7758		0.77448						10.37892		17.5619047619		46.5565		0.408676						42.15962		9.2670294785		78.1047		0.444999						73.70782		10.0906802721		109.872		1.38609						105.47512		31.4306122449

																						15.2951		0.785033						10.89822		17.8012018141		47.0718		0.40526						42.67492		9.189569161		78.6223		0.434034						74.22542		9.8420408163		110.392		1.39715						105.99512		31.6814058957

																						15.8156		0.793814						11.41872		18.0003174603		47.5865		0.399571						43.18962		9.0605668934		79.1383		0.449533						74.74142		10.1934920635		110.91		1.38712						106.51312		31.453968254

																						16.3359		0.796046						11.93902		18.0509297052		48.1042		0.387427						43.70732		8.7851927438		79.6557		0.444956						75.25882		10.0897052154		111.43		1.41041						107.03312		31.9820861678

																						16.855		0.802499						12.45812		18.1972562358		48.6235		0.393406						44.22662		8.9207709751		80.17		0.447222						75.77312		10.1410884354		111.952		1.40782						107.55512		31.9233560091

																						17.3737		0.800843						12.97682		18.1597052154		49.1407		0.392471						44.74382		8.899569161		80.688		0.439988						76.29112		9.9770521542		112.468		1.41168						108.07112		32.0108843537

																						17.893		0.793755						13.49612		17.9989795918		49.6578		0.387666						45.26092		8.7906122449		81.2037		0.438974						76.80682		9.9540589569		112.984		1.42583						108.58712		32.3317460317

																						18.4133		0.787995						14.01642		17.8683673469		50.1753		0.383961						45.77842		8.7065986395		81.7208		0.440884						77.32392		9.9973696145		113.502		1.4179						109.10512		32.1519274376

																						18.9323		0.778076						14.53542		17.643446712		50.6922		0.381632						46.29532		8.6537868481		82.2383		0.437772						77.84142		9.9268027211		114.017		1.42291						109.62012		32.2655328798

																						19.4538		0.766888						15.05692		17.3897505669		51.208		0.382217						46.81112		8.6670521542		82.7547		0.443754						78.35782		10.0624489796		114.534		1.4389						110.13712		32.6281179138

																						19.9723		0.748471						15.57542		16.9721315193		51.7253		0.374496						47.32842		8.4919727891		83.2727		0.444354						78.87582		10.0760544218		115.05		1.43664						110.65312		32.5768707483

																						20.4897		0.727871						16.09282		16.5050113379		52.244		0.372167						47.84712		8.4391609977		83.7872		0.442292						79.39032		10.0292970522		115.565		1.43697						111.16812		32.5843537415

																						21.0088		0.700554						16.61192		15.8855782313		52.7592		0.37355						48.36232		8.470521542		84.3042		0.441282						79.90732		10.0063945578		116.08		1.4416						111.68312		32.6893424036

																						21.5263		0.679044						17.12942		15.3978231293		53.2737		0.367721						48.87682		8.3383446712		84.8217		0.447309						80.42482		10.1430612245		116.597		1.43715						112.20012		32.5884353741

																						22.0458		0.65838						17.64892		14.9292517007		53.789		0.364547						49.39212		8.2663718821		85.3383		0.449069						80.94142		10.1829705215		117.116		1.44742						112.71912		32.8213151927

																						22.568		0.633483						18.17112		14.3646938776		54.3068		0.37166						49.90992		8.4276643991		85.857		0.44153						81.46012		10.0120181406		117.633		1.45433						113.23612		32.9780045351

																						23.0865		0.615174						18.68962		13.9495238095		54.8247		0.372629						50.42782		8.4496371882		86.3718		0.445323						81.97492		10.0980272109		118.149		1.45961						113.75212		33.0977324263

																						23.6073		0.59077						19.21042		13.3961451247		55.3403		0.369252						50.94342		8.3730612245		86.8888		0.441138						82.49192		10.0031292517		118.666		1.4588						114.26912		33.0793650794

																						24.1255		0.571043						19.72862		12.9488208617		55.8587		0.368284						51.46182		8.3511111111		87.4038		0.441787						83.00692		10.017845805		119.183		1.40233						114.78612		31.7988662132

																						24.648		0.55925						20.25112		12.6814058957		56.3747		0.371857						51.97782		8.4321315193		87.9205		0.447727						83.52362		10.1525396825		119.703		1.45957						115.30612		33.0968253968

																						25.1662		0.540141						20.76932		12.2480952381		56.8913		0.357896						52.49442		8.1155555556		88.4397		0.441855						84.04282		10.0193877551		120.218		1.46936						115.82112		33.3188208617

																						25.6828		0.530076						21.28592		12.0198639456		57.412		0.365539						53.01512		8.2888662132		88.9552		0.444771						84.55832		10.0855102041		120.733		1.44559						116.33612		32.7798185941

																						26.2018		0.520583						21.80492		11.8046031746		57.9277		0.369443						53.53082		8.3773922902		89.4718		0.435057						85.07492		9.8652380952		121.25		1.46953						116.85312		33.322675737

																						26.7205		0.509849						22.32362		11.5612018141		58.444		0.359045						54.04712		8.1416099773		89.9872		0.437345						85.59032		9.9171201814		121.767		1.47555						117.37012		33.4591836735

																						27.2412		0.508719						22.84432		11.5355782313		58.9607		0.361009						54.56382		8.1861451247		90.5042		0.44175						86.10732		10.0170068027		122.289		1.47474						117.89212		33.4408163265

																						27.7605		0.508168						23.36362		11.5230839002		59.48		0.355683						55.08312		8.0653741497		91.0218		0.443963						86.62492		10.0671882086		122.805		1.47491						118.40812		33.4446712018

																						28.2768		0.503494						23.87992		11.4170975057		59.9987		0.363751						55.60182		8.2483219955		91.5388		0.448119						87.14192		10.1614285714		123.321		1.48407						118.92412		33.6523809524

																						28.7945		0.504911						24.39762		11.4492290249		60.5158		0.366084						56.11892		8.3012244898		92.0555		0.442474						87.65862		10.0334240363		123.837		1.47826						119.44012		33.5206349206

																						29.3088		0.507862						24.91192		11.5161451247		61.0323		0.353669						56.63542		8.0197052154		92.5712		0.444646						88.17432		10.082675737		124.353		1.49027						119.95612		33.7929705215

																						29.8283		0.501356						25.43142		11.36861678		61.5487		0.358818						57.15182		8.136462585		93.0875		0.441782						88.69062		10.0177324263		124.874		1.4814						120.47712		33.5918367347

																						30.3472		0.503958						25.95032		11.4276190476		62.0653		0.355462						57.66842		8.0603628118		93.6045		0.442873						89.20762		10.0424716553		125.393		1.47525						120.99612		33.4523809524

																						30.8638		0.496514						26.46692		11.2588208617		62.5825		0.358045						58.18562		8.1189342404		94.1223		0.434596						89.72542		9.8547845805		125.911		1.4871						121.51412		33.7210884354

																						31.3852		0.496525						26.98832		11.2590702948		63.0992		0.353834						58.70232		8.023446712		94.6393		0.445696						90.24242		10.1064852608		126.428		1.49165						122.03112		33.8242630385

																						31.9022		0.493071						27.50532		11.1807482993		63.6163		0.364451						59.21942		8.2641950113		95.1573		0.447322						90.76042		10.1433560091		126.943		1.47765						122.54612		33.5068027211

																						32.4185		0.494776						28.02162		11.2194104308		64.1323		0.360689						59.73542		8.1788888889		95.6723		0.449416						91.27542		10.1908390023		127.461		1.49972						123.06412		34.0072562358

																						32.9365		0.497637						28.53962		11.2842857143		64.6482		0.354961						60.25132		8.0490022676		96.1907		0.449529						91.79382		10.1934013605		127.978		1.49892						123.58112		33.9891156463

																						33.4523		0.504173						29.05542		11.4324943311		65.1663		0.349915						60.76942		7.9345804989		96.7065		0.443518						92.30962		10.0570975057		128.495		1.49774						124.09812		33.9623582766

																						33.9703		0.504842						29.57342		11.4476643991		65.6838		0.357767						61.28692		8.1126303855		97.2237		0.445639						92.82682		10.1051927438		129.011		1.50551						124.61412		34.1385487528

																						34.489		0.51199						30.09212		11.6097505669		66.201		0.354599						61.80412		8.0407936508		97.7402		0.442746						93.34332		10.0395918367		129.528		1.50138						125.13112		34.0448979592





		



GLP-PVP 1:2 pH 1.5

GLP-PVP 1:2 pH 4.0

GLP-PVP 1:2 pH 5.5

GLP-PVP 1:2 pH 6.8

Time (min)

% Dissolved



		GLP-PVP 1:2								445.54																GLP-PVP 1:2 pH 1.5				17E-07009								GLP-PVP 1:2 pH 4.0				17E-07009								GLP-PVP 1:2 pH 5.5				17E-07009								GLP-PVP 1:2 pH 6.8				17E-07009

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/min)		IDR (ug/min/cm2)

		GLP-PVP 1:2 pH 1.5		17E-07009		0.300		14.589		0.28		4.08		7.35		52.5718		751.0250

		GLP-PVP 1:2 pH 4.0		17E-07009		0.166		14.589		0.28		4.08		4.07		-0.0085		-0.1217				Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile

		GLP-PVP 1:2 pH 5.5		17E-07009		0.233		14.589		0.28		4.08		5.70		16.38		234.04

		GLP-PVP 1:2 pH 6.8		17E-07009		1.157		14.589		0.28		4.08		28.32		58.53		836.19				Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%

																						4.29115		0.133335						0		3.2640786111		35.882		0.324119						31.59085		7.9345250335		67.4472		0.188742						63.15605		4.6204576834		99.2542		0.521697						94.96305		12.7712905026

																						4.80912		0.192776						0.51797		4.7192111473		36.398		0.318965						32.10685		7.808353652		67.9682		0.190459						63.67705		4.6624903303		99.7722		0.580798						95.48105		14.2180997425

																						5.3276		0.248658						1.03645		6.0872183543		36.914		0.31342						32.62285		7.6726104795		68.4825		0.191302						64.19135		4.6831272093		100.29		0.631316						95.99885		15.4547947083

																						5.84532		0.286455						1.55417		7.0124996328		37.4313		0.308221						33.14015		7.5453374852		69.0045		0.193028						64.71335		4.7253801788		100.809		0.675571						96.51785		16.5381696582

																						6.36093		0.314609						2.06978		7.7017175367		37.9462		0.303934						33.65505		7.4403905095		69.5222		0.195776						65.23105		4.7926519981		101.333		0.710127						97.04185		17.3841103375

																						6.8776		0.342599						2.58645		8.3869206741		38.4628		0.299353						34.17165		7.3282463304		70.0408		0.196102						65.74965		4.8006325705		101.854		0.740967						97.56285		18.1390822831

																						7.39583		0.368343						3.10468		9.0171410946		38.9787		0.295123						34.68755		7.2246947309		70.5592		0.197883						66.26805		4.8442319556		102.37		0.770218						98.07885		18.8551550581

																						7.91407		0.390509						3.62292		9.5597710604		39.4935		0.291531						35.20235		7.1367615522		71.0787		0.198677						66.78755		4.8636693007		102.888		0.792009						98.59685		19.3886049176

																						8.43022		0.408799						4.13907		10.0075154471		40.0117		0.286511						35.72055		7.0138705287		71.5958		0.199964						67.30465		4.8951754257		103.405		0.815407						99.11385		19.9613945928

																						8.9461		0.424208						4.65495		10.3847321367		40.5283		0.282222						36.23715		6.9088745924		72.1125		0.199612						67.82135		4.8865583659		103.926		0.834623						99.63485		20.4318077221

																						9.46147		0.43689						5.17032		10.6951910931		41.0462		0.279671						36.75505		6.846425389		72.6297		0.201593						68.33855		4.9350538077		104.444		0.852375						100.15285		20.8663817162

																						9.97682		0.449715						5.68567		11.00915073		41.5652		0.275348						37.27405		6.7405971231		73.1463		0.20286						68.85515		4.966070327		104.96		0.871266						100.66885		21.3288387533

																						10.494		0.461088						6.20285		11.2875649952		42.0795		0.271561						37.78835		6.6478902892		73.664		0.203659						69.37285		4.9856300735		105.481		0.8848						101.18985		21.6601549112

																						11.0088		0.469957						6.71765		11.5046806302		42.5972		0.26771						38.30605		6.5536167171		74.1795		0.204493						69.88835		5.00604663		105.996		0.899299						101.70485		22.0150945429

																						11.5232		0.476435						7.23205		11.6632639072		43.1133		0.264877						38.82215		6.4842640737		74.6967		0.20572						70.40555		5.036083938		106.515		0.912131						102.22385		22.3292255417

																						12.0391		0.481968						7.74795		11.7987133163		43.6292		0.260778						39.33805		6.3839193913		75.2143		0.205291						70.92315		5.0255818963		107.031		0.925132						102.73985		22.6474937086

																						12.555		0.486241						8.26385		11.903317568		44.1482		0.257979						39.85705		6.3153990776		75.7315		0.206519						71.44035		5.0556436846		107.547		0.936431						103.25585		22.9240964327

																						13.0716		0.490563						8.78045		12.0091213537		44.6667		0.254894						40.37555		6.2398774027		76.2505		0.207427						71.95935		5.0778717821		108.063		0.947309						103.77185		23.1903929575

																						13.5867		0.493894						9.29555		12.0906651783		45.1825		0.251671						40.89135		6.1609774488		76.767		0.208233						72.47585		5.0976028906		108.577		0.955935						104.28585		23.4015598837

																						14.1013		0.496969						9.81015		12.1659420503		45.6973		0.248485						41.40615		6.0829832653		77.2862		0.209429						72.99505		5.1268813098		109.098		0.966822						104.80685		23.668076731

																						14.6167		0.499658						10.32555		12.2317695328		46.213		0.245337						41.92185		6.0059193326		77.8047		0.209413						73.51355		5.1264896253		109.614		0.977438						105.32285		23.9279594215

																						15.1315		0.501035						10.84035		12.2654788833		46.7323		0.243002						42.44115		5.9487578704		78.323		0.211126						74.03185		5.168424351		110.134		0.985857						105.84285		24.1340589289

																						15.6479		0.502021						11.35675		12.2896164429		47.2495		0.23984						42.95835		5.8713512137		78.8407		0.211289						74.54955		5.1724146373		110.65		0.992771						106.35885		24.3033156096

																						16.1646		0.500773						11.87345		12.259065049		47.7657		0.237002						43.47455		5.8018761689		79.3557		0.211465						75.06455		5.1767231672		111.164		1.00019						106.87285		24.4849348335

																						16.6818		0.500669						12.39065		12.2565190995		48.2797		0.233715						43.98855		5.7214094768		79.8713		0.213272						75.58015		5.2209590396		111.684		1.00724						107.39285		24.6575208327

																						17.1972		0.49911						12.90605		12.2183543374		48.7955		0.231525						44.50435		5.6677976558		80.3935		0.213295						76.10235		5.2215220861		112.201		1.01584						107.90985		24.8680512715

																						17.713		0.495607						13.42185		12.132599904		49.3128		0.229058						45.02165		5.6074047962		80.9102		0.213439						76.61905		5.2250472469		112.719		1.02113						108.42785		24.9975519716

																						18.2297		0.493715						13.93855		12.0862832075		49.8318		0.227044						45.54065		5.558101505		81.4263		0.214883						77.13515		5.2603967764		113.236		1.02961						108.94485		25.2051447764

																						18.7482		0.491599						14.45705		12.0344829275		50.348		0.223564						46.05685		5.4729101182		81.9435		0.215117						77.65235		5.2661251628		113.751		1.03556						109.45985		25.3508024637

																						19.2635		0.488804						14.97235		11.9660605348		50.8643		0.220522						46.57315		5.3984410955		82.4622		0.216096						78.17105		5.2900913604		114.27		1.0407						109.97885		25.4766311213

																						19.7807		0.485198						15.48955		11.8777846323		51.3833		0.219839						47.09215		5.3817210619		82.9802		0.215897						78.68905		5.285219784		114.786		1.04584						110.49485		25.6024597789

																						20.2962		0.482752						16.00505		11.8179058586		51.9		0.216821						47.60885		5.307839566		83.4963		0.217248						79.20515		5.3182926471		115.302		1.05398						111.01085		25.8017292872

																						20.8115		0.479533						16.52035		11.7391038258		52.418		0.214295						48.12685		5.2460023697		84.0138		0.218041						79.72265		5.337705512		115.819		1.05926						111.52785		25.9309851845

																						21.3253		0.476435						17.03415		11.6632639072		52.938		0.212392						48.64685		5.19941639		84.531		0.217891						80.23985		5.3340334694		116.334		1.06425						112.04285		26.0531417996

																						21.8393		0.471224						17.54815		11.5356971495		53.4542		0.209849						49.16305		5.1371630289		85.0473		0.218333						80.75615		5.3448537548		116.853		1.06871						112.56185		26.1623238644

																						22.3552		0.468356						18.06405		11.4654876962		53.9682		0.207489						49.67705		5.0793895596		85.5648		0.219737						81.27365		5.3792240729		117.368		1.07524						113.07685		26.3221801161

																						22.869		0.463756						18.57785		11.3528783917		54.4855		0.205551						50.19435		5.0319467701		86.083		0.220523						81.79185		5.3984655758		117.883		1.07762						113.59185		26.3804431911

																						23.3843		0.459776						19.09315		11.2554468631		55.005		0.20353						50.71385		4.982472117		86.5992		0.222262						82.30805		5.441036789		118.398		1.0803						114.10685		26.446050351

																						23.8992		0.454275						19.60805		11.1207808231		55.5212		0.200815						51.23005		4.916008147		87.1158		0.22067						82.82465		5.4020641775		118.915		1.09012						114.62385		26.6864467358

																						24.4193		0.448117						20.12815		10.9700312368		56.037		0.198258						51.74585		4.8534120619		87.6313		0.221286						83.34015		5.4171440322		119.435		1.09137						115.14385		26.7170470903

																						24.9378		0.439569						20.64665		10.7607737728		56.5552		0.197456						52.26405		4.8337788745		88.151		0.222205						83.85985		5.4396414128		119.953		1.09485						115.66185		26.8022384771

																						25.4542		0.431389						21.16305		10.5605250531		57.0742		0.194788						52.78305		4.7684654779		88.6652		0.222769						84.37405		5.4534482927		120.469		1.09641						116.17785		26.8404277195

																						25.9708		0.422255						21.67965		10.3369221429		57.5922		0.191548						53.30105		4.6891493591		89.181		0.223531						84.88985		5.4721022688		120.986		1.10266						116.69485		26.9934294919

																						26.4885		0.41374						22.19735		10.1284725282		58.1087		0.190459						53.81755		4.6624903303		89.6958		0.224043						85.40465		5.484636174		121.5		1.1068						117.20885		27.0947778659

																						27.0032		0.405755						22.71205		9.9329974638		58.6242		0.189283						54.33305		4.6337015168		90.2102		0.224872						85.91905		5.5049303291		122.019		1.10899						117.72785		27.1483896869

																						27.5182		0.39685						23.22705		9.7150005386		59.1413		0.186421						54.85015		4.5636389452		90.726		0.225121						86.43485		5.5110259197		122.536		1.11526						118.24485		27.301881065

																						28.0338		0.389544						23.74265		9.5361475867		59.6587		0.18438						55.36755		4.5136746864		91.242		0.225605						86.95085		5.522874377		123.053		1.11459						118.76185		27.285479275

																						28.5513		0.381003						24.26015		9.3270614847		60.175		0.183763						55.88385		4.4985703514		91.7615		0.2269						87.47035		5.5545763442		123.568		1.11916						119.27685		27.397354171

																						29.0682		0.3728						24.77705		9.1262497185		60.6912		0.181264						56.40005		4.4373941228		92.2787		0.227292						87.98755		5.5641726154		124.086		1.12453						119.79485		27.5288132938

																						29.5838		0.365176						25.29265		8.9396120365		61.2093		0.180055						56.91815		4.4077974599		92.7958		0.226965						88.50465		5.5561675626		124.604		1.12512						120.31285		27.5432566611

																						30.101		0.356796						25.80985		8.7344672601		61.7297		0.178178						57.43855		4.3618479676		93.3148		0.227985						89.02365		5.5811374519		125.12		1.12819						120.82885		27.6184111317

																						30.6177		0.349343						26.32655		8.5520157065		62.2468		0.176153						57.95565		4.3122753934		93.831		0.22789						89.53985		5.578811825		125.635		1.13443						121.34385		27.7711681012

																						31.1347		0.342401						26.84355		8.3820735779		62.7635		0.174061						58.47235		4.2610626401		94.3463		0.228392						90.05515		5.5911009273		126.152		1.13393						121.86085		27.7589279594

																						31.6492		0.333593						27.35805		8.1664512402		63.28		0.172242						58.98885		4.2165330043		94.8663		0.229516						90.57515		5.6186167661		126.666		1.13859						122.37485		27.8730060809

																						32.1647		0.327373						27.87355		8.0141838763		63.799		0.171568						59.50785		4.2000332932		95.383		0.23018						91.09185		5.6348716744		127.184		1.14029						122.89285		27.914622563

																						32.6842		0.320604						28.39305		7.8484768368		64.3153		0.17059						60.02415		4.1760915758		95.9038		0.231835						91.61265		5.6753865437		127.702		1.14258						123.41085		27.9706824124

																						33.2005		0.313979						28.90935		7.686294958		64.8357		0.169438						60.54455		4.1478902892		96.4218		0.230755						92.13065		5.6489478374		128.216		1.14831						123.92485		28.1109544373

																						33.719		0.306845						29.42785		7.511652615		65.35		0.167683						61.05885		4.1049273915		96.9383		0.231089						92.64715		5.6571242521		128.734		1.15026						124.44285		28.1586909903

																						34.2362		0.300264						29.94505		7.3505478687		65.867		0.166132						61.57585		4.0669584716		97.456		0.232771						93.16485		5.6983000891		129.249		1.15679						124.95785		28.3185472421





		



GLP-PVP 1:2 pH 1.5

GLP-PVP 1:2 pH 4.0

GLP-PVP 1:2 pH 5.5

GLP-PVP 1:2 pH 6.8

Time (min)

% Dissolved



		GLP-PX 5K 1:2								445.54																GLP-PX 5K 1:2 pH 1.5				17B-27015								GLP-PX 5K 1:2 pH 4.0				17B-27015								GLP-PX 5K 1:2 pH 5.5				17B-27015								GLP-PX 5K 1:2 pH 6.8				17B-27015

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/min)		IDR (ug/min/cm2)

		GLP-PX 5K 1:2 pH 1.5		17B-27015		0.099		16.65		0.31		5.13		1.93		6.2301		89.0007

		GLP-PX 5K 1:2 pH 4.0		17B-27015		0.124		16.65		0.31		5.13		2.42		-0.0051		-0.0734				Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile

		GLP-PX 5K 1:2 pH 5.5		17B-27015		0.226		16.65		0.31		5.13		4.41		18.65		266.40

		GLP-PX 5K 1:2 pH 6.8		17B-27015		1.875		16.65		0.31		5.13		36.55		47.04		671.96				Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%

																						4.3914		0.0292338						0		0.5696897417		36.1737		0.172726						31.7823		3.3659746703		67.8125		0.182914						63.4211		3.5645119487		99.617		1.08872						95.2256		21.216284422

																						4.90782		0.0342155						0.51642		0.6667699497		36.689		0.166397						32.2976		3.2426391349		68.3292		0.184925						63.9378		3.6037010404		100.135		1.17231						95.7436		22.845233293

																						5.42448		0.0396246						1.03308		0.7721790577		37.2102		0.162928						32.8188		3.1750374645		68.8453		0.187829						64.4539		3.6602923495		100.653		1.22257						96.2616		23.8246682763

																						5.94688		0.0441343						1.55548		0.8600612293		37.7277		0.158597						33.3363		3.0906376851		69.3602		0.187587						64.9688		3.655576407		101.17		1.26656						96.7786		24.6819174788

																						6.46927		0.0482223						2.07787		0.9397255789		38.2432		0.155775						33.8518		3.03564434		69.876		0.188611						65.4846		3.6755314692		101.69		1.30582						97.2986		25.4469914431

																						6.9875		0.0520101						2.5961		1.0135398215		38.7607		0.153022						34.3693		2.9819956231		70.3958		0.190496						66.0044		3.7122651529		102.21		1.31364						97.8186		25.5993826403

																						7.50547		0.0536952						3.11407		1.0463779808		39.2778		0.152526						34.8864		2.9723298899		70.9128		0.191668						66.5214		3.7351043451		102.726		1.32241						98.3346		25.7702868345

																						8.0224		0.0574704						3.631		1.1199466826		39.7977		0.149272						35.4063		2.908918003		71.4318		0.190128						67.0404		3.7050938024		103.243		1.34625						98.8516		26.2348656249

																						8.54063		0.0587159						4.14923		1.1442181961		40.3133		0.1476						35.9219		2.8763351281		71.9508		0.194051						67.5594		3.7815427368		103.759		1.36037						99.3676		26.5100272238

																						9.06042		0.0620059						4.66902		1.2083316282		40.8323		0.144219						36.4409		2.8104483458		72.4662		0.191953						68.0748		3.7406582442		104.278		1.37416						99.8866		26.7787579923

																						9.58177		0.0638189						5.19037		1.2436622216		41.3513		0.143776						36.9599		2.801815443		72.9833		0.192678						68.5919		3.7547865841		104.796		1.38739						100.4046		27.0365758361

																						10.1023		0.0655631						5.7109		1.2776520843		41.8685		0.14076						37.4771		2.743041549		73.4987		0.196482						69.1073		3.828916522		105.316		1.39521						100.9246		27.1889670332

																						10.6177		0.0676846						6.2263		1.3189945299		42.3875		0.140078						37.9961		2.7297511658		74.014		0.195365						69.6226		3.8071491349		105.832		1.40458						101.4406		27.3715636467

																						11.1344		0.0692616						6.743		1.3497261051		42.9038		0.140039						38.5124		2.7289911586		74.5323		0.19755						70.1409		3.8497290282		106.348		1.4146						101.9566		27.5668270477

																						11.6524		0.0708329						7.261		1.3803466023		43.4185		0.137133						39.0271		2.6723608748		75.0497		0.196455						70.6583		3.8283903631		106.87		1.41538						102.4786		27.5820271927

																						12.1703		0.0716111						7.7789		1.39551167		43.9372		0.138042						39.5458		2.6900748899		75.5688		0.194287						71.1774		3.786141755		107.389		1.41586						102.9976		27.591381128

																						12.6891		0.0728645						8.2977		1.4199371338		44.4565		0.13715						40.0651		2.67269216		76.089		0.197245						71.6976		3.8437853817		107.904		1.43635						103.5126		27.9906772444

																						13.2081		0.0750646						8.8167		1.4628112863		44.9753		0.134613						40.5839		2.6232527141		76.6047		0.197408						72.2133		3.8469618223		108.42		1.42765						104.0286		27.8211371657

																						13.7273		0.0755748						9.3359		1.4727537401		45.4935		0.134843						41.1021		2.6277348081		77.1223		0.195971						72.7309		3.8189584783		108.935		1.43436						104.5436		27.9518973873

																						14.2453		0.0784955						9.8539		1.5296704881		46.0107		0.135259						41.6193		2.6358415521		77.638		0.196108						73.2466		3.8216282473		109.452		1.43587						105.0606		27.981323309

																						14.7646		0.0773798						10.3732		1.5079284346		46.5258		0.132453						42.1344		2.5811600049		78.157		0.198261						73.7656		3.863584545		109.968		1.4429						105.5766		28.1183194876

																						15.2813		0.0796673						10.8899		1.5525057829		47.0425		0.133796						42.6511		2.6073315366		78.674		0.196496						74.2826		3.8291893451		110.484		1.45192						106.0926		28.2940955232

																						15.7987		0.0792154						11.4073		1.5436994425		47.5573		0.133186						43.1659		2.5954442437		79.1943		0.200036						74.8029		3.8981746185		111.002		1.4401						106.6106		28.0637548645

																						16.3156		0.0807294						11.9242		1.5732033136		48.0732		0.132088						43.6818		2.5740471166		79.7098		0.198458						75.3184		3.8674235559		111.518		1.45329						107.1266		28.3207932137

																						16.8372		0.0818682						12.4458		1.5953955253		48.5922		0.128953						44.2008		2.5129542261		80.2253		0.200288						75.8339		3.9030854346		112.036		1.45741						107.6446		28.401081159

																						17.3593		0.0816332						12.9679		1.5908159944		49.108		0.129154						44.7166		2.5168711866		80.7462		0.198902						76.3548		3.8760759462		112.553		1.45881						108.1616		28.4283634705

																						17.8773		0.0823747						13.4859		1.6052658759		49.626		0.129528						45.2346		2.5241594612		81.262		0.199837						76.8706		3.8942966328		113.069		1.46215						108.6776		28.4934512709

																						18.394		0.0829173						14.0026		1.6158397203		50.1448		0.128795						45.7534		2.5098752224		81.7788		0.202435						77.3874		3.944924808		113.586		1.47097						109.1946		28.6653298334

																						18.9107		0.0838861						14.5193		1.6347190799		50.6607		0.127787						46.2693		2.4902319581		82.299		0.199711						77.9076		3.8918412247		114.101		1.47388						109.7096		28.7220380666

																						19.4255		0.0834627						15.0341		1.6264681294		51.181		0.12876						46.7896		2.5091931646		82.8153		0.20049						78.4239		3.9070218824		114.62		1.48384						110.2286		28.9161322257

																						19.9455		0.0859998						15.5541		1.6759095241		51.698		0.12626						47.3066		2.4604747512		83.3325		0.200252						78.9411		3.9023838894		115.136		1.48138						110.7446		28.8681933069

																						20.4647		0.0848666						16.0733		1.6538264416		52.2148		0.126704						47.8234		2.4691271414		83.8508		0.209691						79.4594		4.0863251311		115.652		1.4966						111.2606		29.1647910078

																						20.9837		0.0881654						16.5923		1.7181113625		52.7313		0.128626						48.3399		2.5065818577		84.3685		0.211022						79.9771		4.1122628144		116.17		1.49975						111.7786		29.2261762087

																						21.5027		0.0865239						17.1113		1.6861228522		53.2473		0.125346						48.8559		2.4426632992		84.8865		0.211192						80.4951		4.1155756665		116.686		1.49971						112.2946		29.225396714

																						22.0193		0.0892064						17.6279		1.7383977098		53.764		0.125391						49.3726		2.4435402307		85.4028		0.214286						81.0114		4.175869575		117.206		1.50068						112.8146		29.2442994584

																						22.5388		0.0890999						18.1474		1.7363223054		54.2833		0.127428						49.8919		2.4832359939		85.9213		0.213752						81.5299		4.1654633219		117.722		1.50749						113.3306		29.3770084166

																						23.0575		0.0902767						18.6661		1.759255037		54.801		0.126469						50.4096		2.4645476106		86.4397		0.214015						82.0483		4.1705884989		118.239		1.50362						113.8476		29.3015923126

																						23.5745		0.0908624						19.1831		1.7706687869		55.3185		0.125264						50.9271		2.4410653353		86.9568		0.214859						82.5654		4.1870358353		118.754		1.51212						114.3626		29.4672349182

																						24.0958		0.089495						19.7044		1.7440217635		55.8372		0.124155						51.4458		2.4194538471		87.4755		0.2167						83.0841		4.222912075		119.269		1.50071						114.8776		29.2448840794

																						24.6152		0.0915174						20.2238		1.7834330112		56.3532		0.126223						51.9618		2.4597537187		87.995		0.215711						83.6036		4.2036390706		119.789		1.51046						115.3976		29.4348858917

																						25.1372		0.0933582						20.7458		1.8193053534		56.87		0.12477						52.4786		2.4314385768		88.5148		0.21515						84.1234		4.1927066586		120.304		1.50903						115.9126		29.4070189593

																						25.6515		0.0923779						21.2601		1.8002018891		57.387		0.123153						52.9956		2.399927507		89.033		0.217353						84.6416		4.2356373245		120.819		1.53092						116.4276		29.8335973871

																						26.1713		0.0904963						21.7799		1.7635344624		57.9073		0.123679						53.5159		2.4101778612		89.5492		0.21507						85.1578		4.1911476694		121.336		1.53797						116.9446		29.970983313

																						26.6913		0.0936766						22.2999		1.8255101305		58.424		0.121647						54.0326		2.3705795348		90.0652		0.217097						85.6738		4.230648559		121.851		1.52513						117.4596		29.7207655417

																						27.2073		0.0931471						22.8159		1.8151915705		58.9393		0.123687						54.5479		2.4103337601		90.583		0.219661						86.1916		4.2806141638		122.372		1.54911						117.9806		30.1880725632

																						27.7237		0.093389						23.3323		1.8199055642		59.4575		0.12367						55.0661		2.4100024749		91.1005		0.221773						86.7091		4.3217714795		122.887		1.53642						118.4956		29.9407778967

																						28.2388		0.0949921						23.8474		1.8511457596		59.9742		0.123702						55.5828		2.4106260706		91.618		0.216591						87.2266		4.2207879521		123.404		1.59656						119.0126		31.1127480498

																						28.7565		0.0946657						24.3651		1.8447850836		60.4908		0.123968						56.0994		2.4158097098		92.1343		0.220868						87.7429		4.3041354138		123.923		1.6035						119.5316		31.2479903654

																						29.2732		0.0944435						24.8818		1.840454991		61.0115		0.124572						56.6201		2.4275800785		92.6523		0.221081						88.2609		4.3082862226		124.44		1.61903						120.0486		31.5506291496

																						29.7912		0.0947514						25.3998		1.8464551508		61.5287		0.122788						57.1373		2.3928146186		93.1705		0.221312						88.7791		4.312787804		124.961		1.69466						120.5696		33.0244585923

																						30.3083		0.0960043						25.9169		1.8708708709		62.0453		0.123818						57.6539		2.412886605		93.6893		0.218794						89.2979		4.263718618		125.478		1.71777						121.0866		33.4748116059

																						30.8235		0.0960059						26.4321		1.8709020507		62.561		0.123064						58.1696		2.3981931315		94.2045		0.223841						89.8131		4.362071351		125.993		1.75322						121.6016		34.1656387081

																						31.3412		0.0963183						26.9498		1.8769899036		63.0755		0.123884						58.6841		2.4141727711		94.7203		0.221033						90.3289		4.3073508291		126.509		1.77114						122.1176		34.5148522955

																						31.8605		0.0963988						27.4691		1.8785586365		63.5925		0.122194						59.2011		2.3812391236		95.2357		0.223285						90.8443		4.3512363759		127.025		1.76923						122.6336		34.4776314277

																						32.3772		0.0977658						27.9858		1.905197865		64.1088		0.123146						59.7174		2.3997910954		95.7533		0.225246						91.3619		4.3894510994		127.546		1.77017						123.1546		34.4959495511

																						32.8962		0.0981708						28.5048		1.9130902479		64.6242		0.122779						60.2328		2.3926392324		96.2727		0.221776						91.8813		4.3218299416		128.064		1.76895						123.6726		34.4721749654

																						33.413		0.0968593						29.0216		1.8875325683		65.1435		0.121897						60.7521		2.3754513761		96.7893		0.220934						92.3979		4.3054215799		128.581		1.8501						124.1896		36.0535746649

																						33.9295		0.0959193						29.5381		1.8692144448		65.6597		0.120367						61.2683		2.3456357071		97.305		0.225023						92.9136		4.3851054169		129.098		1.80122						124.7066		35.1010322457

																						34.4462		0.0987945						30.0548		1.9252445177		66.1792		0.123927						61.7878		2.4150107278		97.8212		0.226171						93.4298		4.4074769123		129.615		1.87535						125.2236		36.5456306404





		



GLP-PX 5K 1:2 pH 1.5

GLP-PX 5K 1:2 pH 4.0

GLP-PX 5K 1:2 pH 5.5

GLP-PX 5K 1:2 pH 6.8

Time (min)

% Dissolved



		GLP-PX 5K 1:3								445.54																GLP-PX 5K 1:3 pH 1.5				17E-07007								GLP-PX 5K 1:3 pH 4.0				17E-07007								GLP-PX 5K 1:3 pH 5.5				17E-07007								GLP-PX 5K 1:3 pH 6.8				17E-07007

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/min)		IDR (ug/min/cm2)

		GLP-PX 5K 1:3 pH 1.5		17E-07007		0.125		19.56		0.24		4.60		2.72		5.1232		73.1881

		GLP-PX 5K 1:3 pH 4.0		17E-07007		0.233		19.56		0.24		4.60		5.07		-0.0033		-0.0478				Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile

		GLP-PX 5K 1:3 pH 5.5		17E-07007		0.509		19.56		0.24		4.60		11.07		9.32		133.18

		GLP-PX 5K 1:3 pH 6.8		17E-07007		2.752		19.56		0.24		4.60		59.85		96.48		1378.33				Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%		Time (minutes)		Weight (mg)						Time zero (min)		%

																						4.40807		0.0344504						0		0.7491569093		36.0855		0.219347						31.67743		4.7699103806		67.6282		0.333906						63.22013		7.2611054427		99.3417		1.74433						94.93363		37.93212478

																						4.92448		0.0390493						0.51641		0.8491643899		36.6045		0.215472						32.19643		4.6856447981		68.1453		0.337417						63.73723		7.3374554969		99.8583		1.88889						95.45023		41.0757202913

																						5.44272		0.0429168						1.03465		0.9332668777		37.1213		0.216121						32.71323		4.699757924		68.662		0.343896						64.25393		7.4783475508		100.374		1.9811						95.96593		43.0809149655

																						5.95885		0.0457775						1.55078		0.9954755362		37.637		0.210239						33.22893		4.5718482063		69.1773		0.34722						64.76923		7.5506311112		100.893		2.04931						96.48493		44.5642066771

																						6.47473		0.0474823						2.06666		1.0325480433		38.1542		0.210347						33.74613		4.5741967696		69.6935		0.35722						65.28543		7.7680906789		101.409		2.10384						97.00093		45.7500137

																						6.99193		0.0527149						2.58386		1.1463359368		38.6727		0.210324						34.26463		4.5736966126		70.2125		0.36089						65.80443		7.8478983403		101.924		2.19676						97.51593		47.7706480034

																						7.50963		0.0545489						3.10156		1.1862180215		39.1875		0.205967						34.77943		4.4789494789		70.7282		0.358417						66.32013		7.7941205892		102.439		2.23822						98.03093		48.6722353713

																						8.02605		0.0559691						3.61798		1.2171016293		39.7028		0.202152						35.29473		4.3959886538		71.2443		0.366976						66.83623		7.9802442332		102.954		2.24503						98.54593		48.8203253369

																						8.54245		0.0592524						4.13438		1.2885001292		40.2172		0.205254						35.80913		4.4634446117		71.7587		0.363701						67.35063		7.9090262248		103.469		2.28049						99.06093		49.5914369641

																						9.05755		0.0608809						4.64948		1.3239134198		40.7355		0.203723						36.32743		4.4301515519		72.2782		0.373884						67.87013		8.1304653026		103.988		2.29671						99.57993		49.944156383

																						9.57265		0.0625847						5.16458		1.3609641809		41.2497		0.203098						36.84163		4.4165603289		72.7948		0.380612						68.38673		8.2767720998		104.502		2.32804						100.09393		50.6254572087

																						10.0891		0.06395						5.68103		1.3906539357		41.7662		0.197306						37.35813		4.2906077473		73.3097		0.37614						68.90163		8.1795241811		105.015		2.33058						100.60693		50.6806919389

																						10.6076		0.065186						6.19953		1.4175319383		42.2852		0.201331						37.87713		4.3781352233		73.8232		0.384001						69.41513		8.3504691473		105.532		2.37878						101.12393		51.7288470555

																						11.1234		0.065985						6.71533		1.4349069577		42.8028		0.2001						38.39473		4.3513659505		74.339		0.380504						69.93093		8.2744235364		106.049		2.40546						101.64093		52.3090291822

																						11.6401		0.0677696						7.23203		1.4737147922		43.319		0.200419						38.91093		4.3583029107		74.8563		0.387916						70.44823		8.435604568		106.568		2.40086						102.15993		52.208997781

																						12.1568		0.0693802						7.74873		1.5087388302		43.8338		0.196621						39.42573		4.2757117669		75.373		0.389656						70.96493		8.4734425328		107.085		2.38085						102.67693		51.773861186

																						12.6711		0.0704483						8.26303		1.5319656866		44.3515		0.200091						39.94343		4.3511702369		75.889		0.388873						71.48093		8.4564154487		107.599		2.41852						103.19093		52.5930313777

																						13.1875		0.070132						8.77943		1.5250874405		44.8688		0.196656						40.46073		4.2764728754		76.4032		0.377067						71.99513		8.199682683		108.113		2.48557						103.70493		54.0510977794

																						13.7034		0.0721421						9.29533		1.5687989882		45.3842		0.194777						40.97613		4.2356122226		76.918		0.388941						72.50993		8.4578941737		108.628		2.4534						104.21993		53.35153035

																						14.2172		0.0726811						9.80913		1.5805200589		45.9013		0.204263						41.49323		4.4418943686		77.432		0.400863						73.02393		8.7171494704		109.145		2.47188						104.73693		53.7533956312

																						14.7333		0.0737249						10.32523		1.6032184886		46.4203		0.20359						42.01223		4.4272593397		77.9492		0.387217						73.54113		8.4204041443		109.659		2.55895						105.25093		55.6468160875

																						15.2479		0.0747711						10.83983		1.6259691086		46.939		0.208432						42.53093		4.5325532624		78.4647		0.394235						74.05663		8.5730172689		110.173		2.56489						105.76493		55.7759870707

																						15.7628		0.0753261						11.35473		1.6380381146		47.4547		0.202886						43.04663		4.4119501861		78.9818		0.395901						74.57373		8.6092460329		110.688		2.58308						106.27993		56.1715460244

																						16.2792		0.0758121						11.87113		1.6486066496		47.9708		0.207243						43.56273		4.5066973198		79.4972		0.390398						75.08913		8.4895780328		111.204		2.57806						106.79593		56.0623813214

																						16.7977		0.0773089						12.38963		1.6811559977		48.4872		0.204712						44.07913		4.4516583032		80.0143		0.401654						75.60623		8.7343505222		111.723		2.59563						107.31493		56.444457782

																						17.3153		0.0787651						12.90723		1.7128224599		49.0027		0.207208						44.59463		4.5059362113		80.531		0.393131						76.12293		8.5490097326		112.238		2.62312						107.82993		57.0422541337

																						17.8297		0.0791597						13.42163		1.7214034145		49.5193		0.206061						45.11123		4.4809935989		81.0463		0.411604						76.63823		8.9507227921		112.753		2.59699						108.34493		56.4740322832

																						18.3455		0.0805233						13.93743		1.7510562011		50.0365		0.209682						45.62843		4.5597357083		81.5593		0.407674						77.15123		8.865261182		113.269		2.61001						108.86093		56.7571646404

																						18.861		0.0823771						14.45293		1.7913688558		50.5555		0.206405						46.14743		4.488474208		82.0747		0.409125						77.66663		8.8968145653		113.784		2.61067						109.37593		56.7715169718

																						19.3747		0.0834044						14.96663		1.8137084772		51.0698		0.207771						46.66173		4.5181791849		82.5927		0.418999						78.18463		9.1115341425		114.303		2.6287						109.89493		57.1635965725

																						19.8898		0.0850778						15.48173		1.8500981612		51.5857		0.212421						47.17763		4.6192978839		83.112		0.428888						78.70393		9.326579909		114.819		2.65012						110.41093		57.6293949666

																						20.4052		0.0864479						15.99713		1.8798922966		52.1005		0.207483						47.69243		4.5119163494		83.6292		0.426463						79.22113		9.2738459638		115.334		2.60685						110.92593		56.688447417

																						20.9232		0.0917819						16.51513		1.9958852301		52.6148		0.209286						48.20673		4.5511243095		84.143		0.434784						79.73493		9.4547940701		115.851		2.63783						111.44293		57.3621371578

																						21.445		0.0960703						17.03693		2.0891405911		53.1318		0.21001						48.72373		4.5668683822		84.6578		0.441935						80.24973		9.610299407		116.365		2.63589						111.95693		57.3199500017

																						21.9658		0.098085						17.55773		2.1329521702		53.6467		0.206615						49.23863		4.4930408589		85.1727		0.443924						80.76463		9.6535521151		116.882		2.64626						112.47393		57.5454555734

																						22.4848		0.100437						18.07673		2.1840986605		54.1625		0.209279						49.75443		4.5509720878		85.6897		0.440712						81.28163		9.5837041019		117.398		2.6477						112.98993		57.5767697512

																						23.0015		0.10168						18.59343		2.2111288848		54.6792		0.210309						50.27113		4.5733704232		86.2038		0.442522						81.79573		9.6230642837		117.912		2.67555						113.50393		58.1823946474

																						23.5193		0.106728						19.11123		2.3209024746		55.1963		0.207614						50.78823		4.5147650697		86.7198		0.444983						82.31173		9.6765810833		118.429		2.69169						114.02093		58.5333743897

																						24.033		0.104291						19.62493		2.2679075779		55.7135		0.209793						51.30543		4.5621495095		87.2342		0.451163						82.82613		9.8109710961		118.943		2.66505						114.53493		57.9540621012

																						24.5472		0.105709						20.13913		2.2987433446		56.2288		0.209483						51.82073		4.5554082629		87.7505		0.453721						83.34243		9.8665972536		119.463		2.67738						115.05493		58.2221897483

																						25.0635		0.108828						20.65543		2.3665689838		56.7462		0.206629						52.33813		4.4933453023		88.2667		0.468187						83.85863		10.1811742643		119.979		2.68412						115.57093		58.3687574969

																						25.5802		0.110019						21.17213		2.3924684183		57.2633		0.214341						52.85523		4.661050121		88.781		0.469261						84.37293		10.2045294218		120.495		2.69782						116.08693		58.6666771047

																						26.0958		0.110442						21.68773		2.4016669581		57.7787		0.21482						53.37063		4.6714664342		89.2973		0.453017						84.88923		9.8512881		121.009		2.69981						116.60093		58.7099515587

																						26.6098		0.113782						22.20173		2.4742984537		58.2945		0.214662						53.88643		4.6680305731		89.8122		0.467873						85.40413		10.1743460338		121.526		2.67595						117.11793		58.1910930301

																						27.1277		0.113732						22.71963		2.4732111558		58.8105		0.212783						54.40243		4.6271699203		90.3277		0.46401						85.91963		10.0903414028		122.045		2.67613						117.63693		58.1950073023

																						27.6443		0.112898						23.23623		2.4550750279		59.3302		0.215523						54.92213		4.6867538419		90.8448		0.475498						86.43673		10.3401589542		122.562		2.68653						118.15393		58.4211652527

																						28.1602		0.114938						23.75213		2.4994367797		59.8473		0.214393						55.43923		4.6621809107		91.3592		0.470786						86.95113		10.2376920059		123.077		2.70819						118.66893		58.8921826765

																						28.6777		0.115605						24.26963		2.5139413329		60.3628		0.224338						55.95473		4.8784444508		91.8755		0.484695						87.46743		10.5401565187		123.592		2.72183						119.18393		59.1887975269

																						29.1922		0.118338						24.78413		2.5733730328		60.8807		0.227345						56.47263		4.9438345428		92.3903		0.49342						87.98223		10.7298899916		124.108		2.73961						119.69993		59.5754406383

																						29.7112		0.117329						25.30313		2.5514313624		61.3985		0.226016						56.99043		4.9149341663		92.9052		0.497445						88.49713		10.8174174676		124.626		2.72038						120.21793		59.1572658896

																						30.2273		0.118789						25.81923		2.5831804593		61.9138		0.228291						57.50573		4.964406218		93.4232		0.502693						89.01513		10.9315402487		125.143		2.68421						120.73493		58.370714633

																						30.7432		0.118629						26.33513		2.5797011062		62.431		0.229929						58.02293		5.0000260951		93.9378		0.503023						89.52973		10.9387164145		125.659		2.76186						121.25093		60.0592881765

																						31.2605		0.121241						26.85243		2.6365015453		62.9492		0.233037						58.54113		5.0676125288		94.4537		0.496285						90.04563		10.7921921577		126.174		2.6808						121.76593		58.2965609204

																						31.7765		0.124435						27.36843		2.7059581312		63.4657		0.224071						59.05763		4.8726382804		94.9703		0.494616						90.56223		10.7558981559		126.69		2.73631						122.28193		59.503678981

																						32.2925		0.123064						27.88443		2.6761444245		63.9825		0.230924						59.57443		5.0216633221		95.4852		0.500348						91.07713		10.8805459801		127.21		2.7379						122.80193		59.5382550522

																						32.8078		0.122513						28.39973		2.6641624023		64.498		0.232139						60.08993		5.0480846596		96.0047		0.50872						91.59663		11.0626031302		127.725		2.75284						123.31693		59.8631396464

																						33.326		0.125724						28.91793		2.7339886695		65.014		0.224259						60.60593		4.8767265202		96.52		0.504076						92.11193		10.9616149069		128.238		2.78061						123.82993		60.4670248661

																						33.8432		0.124375						29.43513		2.7046533738		65.53		0.22898						61.12193		4.9793891822		97.0365		0.50985						92.62843		11.0871760614		128.754		2.78663						124.34593		60.5979355258

																						34.3598		0.125086						29.95173		2.7201147491		66.0462		0.232979						61.63813		5.0663512633		97.5527		0.50893						93.14463		11.0671697811		129.269		2.75209						124.86093		59.8468301789





		



GLP-PX 5K 1:3 pH 1.5

GLP-PX 5K 1:3 pH 4.0

GLP-PX 5K 1:3 pH 5.5

GLP-PX 5K 1:3 pH 6.8

Time (min)

% Dissolved



		GLP-PX 50K 1:2								445.54																GLP-PX 50K 1:2 pH 1.5				17B-27017								GLP-PX 50K 1:2 pH 4.0				17B-27017								GLP-PX 50K 1:2 pH 5.5				17B-27017								GLP-PX 50K 1:2 pH 6.8				17B-27017

		Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve		Slpoe (ug/min)		IDR (ug/min/cm2)

		GLP-PX 50K 1:2 pH 1.5		17B-27017		0.070		15.48		0.30		4.72		1.49		3.0270		43.2432

		GLP-PX 50K 1:2 pH 4.0		17B-27017		0.117		15.48		0.30		4.72		2.47		0.1610		2.2998				Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile

		GLP-PX 50K 1:2 pH 5.5		17B-27017		0.221		15.48		0.30		4.72		4.68		0.02		0.35

		GLP-PX 50K 1:2 pH 6.8		17B-27017		0.948		15.48		0.30		4.72		20.11		38.46		549.43				Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%

																						4.3862		5.79816		0.00579816				0		0.1229672159		36.1297		109.862		0.109862				31.7435		2.3299502376		67.6867		124.095		0.124095				63.3005		2.6318033054		99.5383		488.217		0.488217				95.1521		10.3540925448

																						4.90417		6.75722		0.00675722				0.51797		0.1433069336		36.649		108.026		0.108026				32.2628		2.2910124007		68.2042		127.305		0.127305				63.818		2.699880896		100.057		534.605		0.534605				95.6708		11.3378879574

																						5.42135		8.40438		0.00840438				1.03515		0.1782398571		37.167		109.435		0.109435				32.7808		2.3208944335		68.7212		131.358		0.131358				64.335		2.7858368072		100.577		569.561		0.569561				96.1908		12.0792338323

																						5.9375		9.53498		0.00953498				1.5513		0.2022175904		37.6838		108.786		0.108786				33.2976		2.3071304596		69.239		138.041		0.138041				64.8528		2.9275696852		101.095		597.66		0.59766				96.7088		12.6751566421

																						6.45313		10.5016		0.0105016				2.06693		0.2227176405		38.2		109.551		0.109551				33.8138		2.3233545583		69.758		143.745		0.143745				65.3718		3.0485399584		101.614		620.691		0.620691				97.2278		13.1635974489

																						6.97135		12.027		0.012027				2.58515		0.2550682812		38.717		109.713		0.109713				34.3308		2.3267902498		70.2795		147.536		0.147536				65.8933		3.1289393808		102.131		640.57		0.64057				97.7448		13.5851907275

																						7.48802		13.4151		0.0134151				3.10182		0.2845070673		39.2342		109.272		0.109272				34.848		2.317437534		70.7968		152.468		0.152468				66.4106		3.2335370995		102.648		658.86		0.65886				98.2618		13.9730845384

																						8.00547		15.9256		0.0159256				3.61927		0.3377496815		39.7515		110.081		0.110081				35.3653		2.3345947835		71.3175		154.059		0.154059				66.9313		3.2672789832		103.168		673.947		0.673947				98.7818		14.2930492144

																						8.52343		18.0541		0.0180541				4.13723		0.3828908502		40.2708		109.503		0.109503				35.8846		2.3223365756		71.832		157.622		0.157622				67.4458		3.3428429881		103.684		687.864		0.687864				99.2978		14.5882005629

																						9.0448		19.1787		0.0191787				4.6586		0.4067413357		40.7885		109.796		0.109796				36.4023		2.3285505115		72.3513		161.978		0.161978				67.9651		3.4352249148		104.205		697.81		0.69781				99.8188		14.7991350541

																						9.56198		21.1366		0.0211366				5.17578		0.4482644244		41.305		110.194		0.110194				36.9188		2.3369912844		72.873		165.012		0.165012				68.4868		3.4995699023		104.722		712.4		0.7124				100.3358		15.1085593679

																						10.0784		22.4246		0.0224246				5.6922		0.4755802925		41.8198		109.594		0.109594				37.4336		2.3242665011		73.3907		167.362		0.167362				69.0045		3.5494086369		105.238		722.069		0.722069				100.8518		15.3136192507

																						10.5992		24.9375		0.0249375				6.213		0.5288738058		42.3375		109.25		0.10925				37.9513		2.3169709587		73.9128		170.238		0.170238				69.5266		3.6104027648		105.754		730.831		0.730831				101.3678		15.4994435028

																						11.1167		27.4477		0.0274477				6.7305		0.5821100575		42.8538		109.629		0.109629				38.4676		2.3250087801		74.4357		171.425		0.171425				70.0495		3.6355766278		106.272		740.57		0.74057				101.8858		15.7059879437

																						11.6344		29.0388		0.0290388				7.2482		0.615854062		43.368		109.569		0.109569				38.9818		2.3237363018		74.9547		174.878		0.174878				70.5685		3.7088077557		106.793		748.756		0.748756				102.4068		15.8795964038

																						12.1521		30.8145		0.0308145				7.7659		0.6535130582		43.8838		110.275		0.110275				39.4976		2.3387091301		75.474		176.447		0.176447				71.0878		3.742083064		107.309		755.932		0.755932				102.9228		16.031784812

																						12.669		32.5623		0.0325623				8.2828		0.6905803519		44.4032		110.474		0.110474				40.017		2.3429295166		75.9955		178.292		0.178292				71.6093		3.7812117726		107.827		763.482		0.763482				103.4408		16.1919050019

																						13.1883		34.3319		0.0343319				8.8021		0.7281099795		44.9198		110.329		0.110329				40.5336		2.3398543606		76.5117		180.574		0.180574				72.1255		3.8296083651		108.345		773.872		0.773872				103.9588		16.4122558326

																						13.7063		36.2289		0.0362289				9.3201		0.7683415026		45.4352		110.353		0.110353				41.049		2.3403633519		77.03		182.809		0.182809				72.6438		3.8770081829		108.861		780.542		0.780542				104.4748		16.5537130069

																						14.2273		37.4956		0.0374956				9.8411		0.795205641		45.9527		110.683		0.110683				41.5665		2.3473619828		77.5477		184.481		0.184481				73.1615		3.9124679123		109.38		789.549		0.789549				104.9938		16.7447332122

																						14.744		39.1728		0.0391728				10.3578		0.8307756519		46.4695		110.289		0.110289				42.0833		2.3390060417		78.0647		185.108		0.185108				73.6785		3.9257653109		109.897		793.688		0.793688				105.5108		16.832513009

																						15.2596		40.7004		0.0407004				10.8734		0.8631729502		46.9875		111.492		0.111492				42.6013		2.3645192322		78.58		186.173		0.186173				74.1938		3.9483518012		110.417		801.712		0.801712				106.0308		17.0026857776

																						15.7779		41.3626		0.0413626				11.3917		0.8772168693		47.5032		111.312		0.111312				43.117		2.3607017972		79.1015		187.466		0.187466				74.7153		3.9757737092		110.934		808.352		0.808352				106.5478		17.1435067127

																						16.2969		42.6912		0.0426912				11.9107		0.9053937811		48.0208		110.781		0.110781				43.6346		2.349440364		79.6193		188.178		0.188178				75.2331		3.9908737854		111.45		815.484		0.815484				107.0638		17.2947619702

																						16.8122		42.5611		0.0425611				12.426		0.902634624		48.5365		111.052		0.111052				44.1503		2.3551877245		80.1372		190.546		0.190546				75.751		4.0410942635		111.969		822.685		0.822685				107.5828		17.4474805777

																						17.33		44.5311		0.0445311				12.9438		0.9444143291		49.0523		111.137		0.111137				44.6661		2.3569904021		80.6568		190.998		0.190998				76.2706		4.0506802669		112.487		829.113		0.829113				108.1008		17.5838054228

																						17.8467		45.8494		0.0458494				13.4605		0.9723727988		49.5722		110.878		0.110878				45.186		2.3514975373		81.1753		192.003		0.192003				76.7891		4.0719942789		113.004		837.39		0.83739				108.6178		17.7593438084

																						18.3625		47.216		0.047216				13.9763		1.0013556136		50.0888		111.725		0.111725				45.7026		2.3694606898		81.6943		192.744		0.192744				77.3081		4.0877093863		113.52		842.216		0.842216				109.1338		17.861693482

																						18.8792		48.0549		0.0480549				14.493		1.0191469814		50.6045		111.15		0.11115				46.2183		2.3572661058		82.2148		194.258		0.194258				77.8286		4.1198182562		114.038		846.869		0.846869				109.6518		17.9603741765

																						19.3968		49.7799		0.0497799				15.0106		1.0557307334		51.1213		111.873		0.111873				46.7351		2.3725994696		82.7333		197.4		0.1974				78.3471		4.1864537047		114.557		851.801		0.851801				110.1708		18.0649718952

																						19.9147		50.2837		0.0502837				15.5285		1.0664153098		51.637		112.272		0.112272				47.2508		2.3810614505		83.2505		195.943		0.195943				78.8643		4.1555536893		115.076		854.183		0.854183				110.6898		18.1154892849

																						20.4318		50.5827		0.0505827				16.0456		1.0727564935		52.1555		112.308		0.112308				47.7693		2.3818249375		83.7718		199.107		0.199107				79.3856		4.2226557132		115.594		860.085		0.860085				111.2078		18.2406587366

																						20.9468		52.4885		0.0524885				16.5606		1.1131746468		52.6712		112.946		0.112946				48.285		2.3953556238		84.2935		198.604		0.198604				79.9073		4.2119881032		116.111		863.353		0.863353				111.7248		18.3099663896

																						21.4647		51.9514		0.0519514				17.0785		1.101783845		53.1883		112.304		0.112304				48.8021		2.3817401056		84.8125		200.846		0.200846				80.4263		4.2595363768		116.626		868.337		0.868337				112.2398		18.4156669229

																						21.9813		53.3531		0.0533531				17.5951		1.1315110595		53.7037		112.874		0.112874				49.3175		2.3938286498		85.3283		200.854		0.200854				80.9421		4.2597060405		117.144		876.184		0.876184				112.7578		18.5820858804

																						22.4977		55.0714		0.0550714				18.1115		1.1679527181		54.2213		112.431		0.112431				49.8351		2.3844335181		85.8468		202.239		0.202239				81.4606		4.289079082		117.66		881.005		0.881005				113.2738		18.6843295142

																						23.0158		55.9426		0.0559426				18.6296		1.1864291034		54.7383		113.289		0.113289				50.3521		2.4026299582		86.3625		202.657		0.202657				81.9763		4.2979440143		118.178		884.343		0.884343				113.7918		18.7551217253

																						23.5328		56.5559		0.0565559				19.1466		1.1994359528		55.2545		113.002		0.113002				50.8683		2.3965432702		86.882		203.561		0.203561				82.4958		4.3171160212		118.694		885.112		0.885112				114.3078		18.7714306559

																						24.0505		57.3497		0.0573497				19.6643		1.2162708411		55.7718		113.165		0.113165				51.3856		2.4000001697		87.3972		204.416		0.204416				83.011		4.3352488374		119.211		888.939		0.888939				114.8248		18.8525935653

																						24.5675		58.5705		0.0585705				20.1813		1.2421615335		56.2867		114.025		0.114025				51.9005		2.4182390257		87.914		205.952		0.205952				83.5278		4.3678242826		119.73		892.049		0.892049				115.3438		18.9185503588

																						25.0855		58.0062		0.0580062				20.6993		1.2301938748		56.805		113.741		0.113741				52.4188		2.4122159616		88.4328		207.346		0.207346				84.0466		4.3973881958		120.246		895.156		0.895156				115.8598		18.9844435283

																						25.6032		60.5852		0.0605852				21.217		1.284889235		57.3217		113.957		0.113957				52.9355		2.4167968836		88.9485		206.848		0.206848				84.5623		4.3868266257		120.763		900.935		0.900935				116.3768		19.1070043994

																						26.1198		59.6315		0.0596315				21.7336		1.264663192		57.8383		114.482		0.114482				53.4521		2.427931069		89.4675		208.85		0.20885				85.0813		4.4292849859		121.28		901.334		0.901334				116.8938		19.1154663803

																						26.6357		61.5649		0.0615649				22.2495		1.3056666853		58.356		114.28		0.11428				53.9698		2.4236470586		89.9818		208.304		0.208304				85.5956		4.4177054331		121.799		903.484		0.903484				117.4128		19.1610635204

																						27.1555		62.0983		0.0620983				22.7693		1.3169790177		58.8737		114.693		0.114693				54.4875		2.4324059511		90.4992		209.473		0.209473				86.113		4.4424975526		122.32		911.667		0.911667				117.9338		19.3346083566

																						27.6713		63.389		0.063389				23.2851		1.3443521473		59.3907		114.462		0.114462				55.0045		2.4275069096		91.0188		211.687		0.211687				86.6326		4.489452003		122.838		913.008		0.913008				118.4518		19.3630482473

																						28.188		63.416		0.063416				23.8018		1.3449247626		59.9087		114.465		0.114465				55.5225		2.4275705335		91.5388		209.872		0.209872				87.1526		4.4509595335		123.354		915.739		0.915739				118.9678		19.4209672193

																						28.7047		64.4801		0.0644801				24.3185		1.3674921658		60.4258		114.379		0.114379				56.0396		2.4257466479		92.0532		209.937		0.209937				87.667		4.4523380517		123.871		922.714		0.922714				119.4848		19.5688928251

																						29.2263		64.9333		0.0649333				24.8401		1.3771036188		60.945		114.701		0.114701				56.5588		2.4325756149		92.5703		211.742		0.211742				88.1841		4.4906184414		124.388		924.177		0.924177				120.0018		19.5999200884

																						29.7427		64.7977		0.0647977				25.3565		1.3742278177		61.4602		115.567		0.115567				57.074		2.4509417188		93.0883		211.541		0.211541				88.7021		4.486355639		124.908		927.69		0.92769				120.5218		19.6744236946

																						30.2635		66.0342		0.0660342				25.8773		1.4004514753		61.9772		115.039		0.115039				57.591		2.4397439095		93.607		213.235		0.213235				89.2208		4.5222819439		125.426		928.908		0.928908				121.0398		19.7002550047

																						30.7787		66.4804		0.0664804				26.3925		1.4099144725		62.4943		114.386		0.114386				58.1081		2.4258951037		94.1237		216.225		0.216225				89.7375		4.5856937806		125.946		930.339		0.930339				121.5598		19.7306036128

																						31.2953		65.9198		0.0659198				26.9091		1.3980252833		63.0112		116.074		0.116074				58.625		2.4616941607		94.6413		215.646		0.215646				90.2551		4.5734143648		126.462		930.696		0.930696				122.0758		19.7381748589

																						31.8122		67.706		0.067706				27.426		1.4359069632		63.5283		115.592		0.115592				59.1421		2.4514719181		95.157		214.911		0.214911				90.7708		4.5578265052		126.979		934.695		0.934695				122.5928		19.8229855396

																						32.3295		68.1484		0.0681484				27.9433		1.4452893701		64.0458		116.085		0.116085				59.6596		2.4619274484		95.6717		216.844		0.216844				91.2855		4.5988215154		127.501		936.238		0.936238				123.1148		19.8557094406

																						32.8495		68.4008		0.0684008				28.4633		1.4506422622		64.5615		116.045		0.116045				60.1753		2.4610791295		96.194		217.895		0.217895				91.8078		4.6211110941		128.019		940.683		0.940683				123.6328		19.9499788769

																						33.3658		67.8611		0.0678611				28.9796		1.4391963197		65.0782		115.983		0.115983				60.692		2.4597642352		96.7097		220.008		0.220008				92.3235		4.6659235393		128.536		940.607		0.940607				124.1498		19.948367071

																						33.886		68.6461		0.0686461				29.4998		1.4558445778		65.5943		116.521		0.116521				61.2081		2.4711741242		97.225		218.969		0.218969				92.8388		4.6438884562		129.053		944.553		0.944553				124.6668		20.0320537291

																						34.4037		70.177		0.070177				30.0175		1.4883118624		66.1112		116.559		0.116559				61.725		2.4719800272		97.7427		220.903		0.220903				93.3565		4.6849046744		129.57		948.086		0.948086				125.1838		20.1069814948





		



GLP-PX 50K 1:2 pH 1.5

GLP-PX 50K 1:2 pH 4.0

GLP-PX 50K 1:2 pH 5.5

GLP-PX 50K 1:2 pH 6.8

Time (min)

% Dissolved



		FULL								445.54																GLP				17B-26003								GLP-PVP 1:1				17B-28001								GLP-PVP 1:2				17E-07009								GLP-PX 5K 1:2				17B-27015								GLP-PX 50K 1:2				17B-27017								GLP-PVP 1:2				17B-27019								GLP-PEOX 1:3				17E-07007

						Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve

						GLP		17B-26003		0.047		5.33		1.00		5.33		0.88

						GLP-PVP 1:1		17B-28001		1.501		10.56		0.44		4.69		32.03				Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile

						GLP-PVP 1:2		17E-07009		1156.790		14.31		0.28		4.01		28870.67

						GLP-PX 5K 1:2		17B-27015		1.875		16.65		0.31		5.13		36.55				Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (µg)				Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (µg)				Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (µg)				Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (µg)				Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (µg)				Time zero (min)		%

						GLP-PX 50K 1:2		17B-27017		0.948		15.48		0.30		4.72		20.11				4.28802		3.87153		0.00387153				0		0.0726365854		4.78047		0.0274011		27.4011				0		0.5848098121		4.29115		0.133335		133.335				0		3327.7178796047		4.3914		0.0292338		29.2338				0		0.5696897417		4.3862		5.79816		0.00579816				0		0.1229672159		4.39688		0.106057		106.057				0		2.4049206349		4.40807		0.0344504		34.4504				0		0.7045071575

						GLP-PVP 1:2		17B-27019		1.501		15.75		0.28		4.41		34.04				4.80522		3.82382		0.00382382				0.5172		0.0717414634		5.29713		0.0294653		29.4653				0.51666		0.6288651389		4.80912		0.192776		192.776				0.51797		4811.2209244285		4.90782		0.0342155		34.2155				0.51642		0.6667699497		4.90417		6.75722		0.00675722				0.51797		0.1433069336		4.91537		0.163208		163.208				0.51849		3.700861678		4.92448		0.0390493		39.0493				0.51641		0.7985541922

						GLP-PX 5K 1:3		17E-07007		2.752		19.56		0.25		4.89		56.28				5.32213		4.6547		0.0046547				1.03411		0.0873302064		5.8151		0.0331818		33.1818				1.03463		0.7081847891		5.3276		0.248658		248.658				1.03645		6205.8999700509		5.42448		0.0396246		39.6246				1.03308		0.7721790577		5.42135		8.40438		0.00840438				1.03515		0.1782398571		5.43333		0.222265		222.265				1.03645		5.0400226757		5.44272		0.0429168		42.9168				1.03465		0.8776441718

																						5.83932		4.40174		0.00440174				1.5513		0.0825842402		6.33593		0.0354593		35.4593				1.55546		0.7567924854		5.84532		0.286455		286.455				1.55417		7149.2213237496		5.94688		0.0441343		44.1343				1.55548		0.8600612293		5.9375		9.53498		0.00953498				1.5513		0.2022175904		5.95208		0.271511		271.511				1.5552		6.1567120181		5.95885		0.0457775		45.7775				1.55078		0.9361451943

																						6.35495		3.5933		0.0035933				2.06693		0.0674165103		6.85547		0.0376113		37.6113				2.075		0.8027216895		6.36093		0.314609		314.609				2.06978		7851.876809424		6.46927		0.0482223		48.2223				2.07787		0.9397255789		6.45313		10.5016		0.0105016				2.06693		0.2227176405		6.4698		0.309521		309.521				2.07292		7.01861678		6.47473		0.0474823		47.4823				2.06666		0.97100818

																						6.87135		3.6561		0.0036561				2.58333		0.0685947467		7.3724		0.0397686		39.7686				2.59193		0.8487640093		6.8776		0.342599		342.599				2.58645		8550.4392532694		6.9875		0.0520101		52.0101				2.5961		1.0135398215		6.97135		12.027		0.012027				2.58515		0.2550682812		6.98828		0.348035		348.035				2.5914		7.8919501134		6.99193		0.0527149		52.7149				2.58386		1.0780143149

																						7.38647		4.37268		0.00437268				3.09845		0.0820390244		7.88985		0.0423661		42.3661				3.10938		0.904201327		7.39583		0.368343		368.343				3.10468		9192.9469901168		7.50547		0.0536952		53.6952				3.11407		1.0463779808		7.48802		13.4151		0.0134151				3.10182		0.2845070673		7.50938		0.383855		383.855				3.1125		8.7041950113		7.50963		0.0545489		54.5489				3.10156		1.1155194274

																						7.90208		4.69985		0.00469985				3.61406		0.0881772983		8.40807		0.0449157		44.9157				3.6276		0.9586163358		7.91407		0.390509		390.509				3.62292		9746.1565338924		8.0224		0.0574704		57.4704				3.631		1.1199466826		8.00547		15.9256		0.0159256				3.61927		0.3377496815		8.03098		0.418367		418.367				3.6341		9.4867800454		8.02605		0.0559691		55.9691				3.61798		1.1445623722

																						8.41927		5.19696		0.00519696				4.13125		0.09750394		8.92657		0.0467905		46.7905				4.1461		0.9986293803		8.43022		0.408799		408.799				4.13907		10202.6305281022		8.54063		0.0587159		58.7159				4.14923		1.1442181961		8.52343		18.0541		0.0180541				4.13723		0.3828908502		8.5487		0.454286		454.286				4.15182		10.3012698413		8.54245		0.0592524		59.2524				4.13438		1.2117055215

																						8.93542		5.39825		0.00539825				4.6474		0.1012804878		9.44662		0.0491554		49.1554				4.66615		1.049102417		8.9461		0.424208		424.208				4.65495		10587.2017570131		9.06042		0.0620059		62.0059				4.66902		1.2083316282		9.0448		19.1787		0.0191787				4.6586		0.4067413357		9.06745		0.487768		487.768				4.67057		11.0604988662		9.05755		0.0608809		60.8809				4.64948		1.24500818

																						9.45105		4.85072		0.00485072				5.16303		0.0910078799		9.96302		0.0510858		51.0858				5.18255		1.0903021083		9.46147		0.43689		436.89				5.17032		10903.7136867326		9.58177		0.0638189		63.8189				5.19037		1.2436622216		9.56198		21.1366		0.0211366				5.17578		0.4482644244		9.58438		0.523179		523.179				5.1875		11.8634693878		9.57265		0.0625847		62.5847				5.16458		1.2798507157

																						9.96927		5.25452		0.00525452				5.68125		0.0985838649		10.4833		0.0536451		53.6451				5.70283		1.14492414		9.97682		0.449715		449.715				5.68567		11223.7945492662		10.1023		0.0655631		65.5631				5.7109		1.2776520843		10.0784		22.4246		0.0224246				5.6922		0.4755802925		10.1055		0.558419		558.419				5.70862		12.6625623583		10.0891		0.06395		63.95				5.68103		1.3077709611

																						10.4867		5.39198		0.00539198				6.19868		0.1011628518		11.0018		0.0553411		55.3411				6.22133		1.1811211336		10.494		0.461088		461.088				6.20285		11507.637017071		10.6177		0.0676846		67.6846				6.2263		1.3189945299		10.5992		24.9375		0.0249375				6.213		0.5288738058		10.6247		0.594377		594.377				6.22782		13.4779365079		10.6076		0.065186		65.186				6.19953		1.3330470348

																						11.0039		5.01972		0.00501972				6.71588		0.0941786116		11.5216		0.0565265		56.5265				6.74113		1.2064206125		11.0088		0.469957		469.957				6.71765		11728.9857242687		11.1344		0.0692616		69.2616				6.743		1.3497261051		11.1167		27.4477		0.0274477				6.7305		0.5821100575		11.1453		0.626659		626.659				6.74842		14.2099546485		11.1234		0.065985		65.985				6.71533		1.3493865031

																						11.519		5.37026		0.00537026				7.23098		0.1007553471		12.0414		0.058856		58.856				7.26093		1.2561381223		11.5232		0.476435		476.435				7.23205		11890.6608765099		11.6524		0.0708329		70.8329				7.261		1.3803466023		11.6344		29.0388		0.0290388				7.2482		0.615854062		11.6638		0.655163		655.163				7.26692		14.8563038549		11.6401		0.0677696		67.7696				7.23203		1.3858813906

																						12.0352		5.61235		0.00561235				7.74718		0.1052973734		12.5635		0.0609508		60.9508				7.78303		1.3008465316		12.0391		0.481968		481.968				7.74795		12028.7511230907		12.1703		0.0716111		71.6111				7.7789		1.39551167		12.1521		30.8145		0.0308145				7.7659		0.6535130582		12.182		0.682569		682.569				7.78512		15.477755102		12.1568		0.0693802		69.3802				7.74873		1.4188179959

																						12.5508		4.88932		0.00488932				8.26278		0.0917320826		13.082		0.0631976		63.1976				8.30153		1.3487990111		12.555		0.486241		486.241				8.26385		12135.3948287911		12.6891		0.0728645		72.8645				8.2977		1.4199371338		12.669		32.5623		0.0325623				8.2828		0.6905803519		12.6997		0.708489		708.489				8.30282		16.0655102041		12.6711		0.0704483		70.4483				8.26303		1.4406605317

																						13.0656		5.60924		0.00560924				8.77758		0.1052390244		13.6034		0.0640041		64.0041				8.82293		1.3660117913		13.0716		0.490563		490.563				8.78045		12243.2614555256		13.2081		0.0750646		75.0646				8.8167		1.4628112863		13.1883		34.3319		0.0343319				8.8021		0.7281099795		13.219		0.72946		729.46				8.82212		16.5410430839		13.1875		0.070132		70.132				8.77943		1.434192229

																						13.5823		5.81417		0.00581417				9.29428		0.1090838649		14.12		0.0656058		65.6058				9.33953		1.4001961809		13.5867		0.493894		493.894				9.29555		12326.3951282819		13.7273		0.0755748		75.5748				9.3359		1.4727537401		13.7063		36.2289		0.0362289				9.3201		0.7683415026		13.737		0.749623		749.623				9.34012		16.9982539683		13.7034		0.0721421		72.1421				9.29533		1.4752985685

																						14.0992		5.89386		0.00589386				9.81118		0.1105789869		14.637		0.0665905		66.5905				9.85653		1.4212122066		14.1013		0.496969		496.969				9.81015		12403.1396625736		14.2453		0.0784955		78.4955				9.8539		1.5296704881		14.2273		37.4956		0.0374956				9.8411		0.795205641		14.2573		0.759938		759.938				9.86042		17.232154195		14.2172		0.0726811		72.6811				9.80913		1.4863210634

																						14.6167		6.16529		0.00616529				10.32868		0.1156714822		15.155		0.0693286		69.3286				10.37453		1.4796502892		14.6167		0.499658		499.658				10.32555		12470.2505740242		14.7646		0.0773798		77.3798				10.3732		1.5079284346		14.744		39.1728		0.0391728				10.3578		0.8307756519		14.7758		0.77448		774.48				10.37892		17.5619047619		14.7333		0.0737249		73.7249				10.32523		1.5076666667

																						15.1333		6.0779		0.0060779				10.84528		0.1140318949		15.6742		0.0713495		71.3495				10.89373		1.5227814828		15.1315		0.501035		501.035				10.84035		12504.6171508436		15.2813		0.0796673		79.6673				10.8899		1.5525057829		15.2596		40.7004		0.0407004				10.8734		0.8631729502		15.2951		0.785033		785.033				10.89822		17.8012018141		15.2479		0.0747711		74.7711				10.83983		1.5290613497

																						15.6492		6.21655		0.00621655				11.36118		0.1166332083		16.1932		0.0736732		73.6732				11.41273		1.5723752057		15.6479		0.502021		502.021				11.35675		12529.2253169612		15.7987		0.0792154		79.2154				11.4073		1.5436994425		15.7779		41.3626		0.0413626				11.3917		0.8772168693		15.8156		0.793814		793.814				11.41872		18.0003174603		15.7628		0.0753261		75.3261				11.35473		1.5404110429

																						16.1636		6.35158		0.00635158				11.87558		0.1191666041		16.7125		0.0759705		75.9705				11.93203		1.6214054849		16.1646		0.500773		500.773				11.87345		12498.0782669462		16.3156		0.0807294		80.7294				11.9242		1.5732033136		16.2969		42.6912		0.0426912				11.9107		0.9053937811		16.3359		0.796046		796.046				11.93902		18.0509297052		16.2792		0.0758121		75.8121				11.87113		1.5503496933

																						16.6802		5.77284		0.00577284				12.39218		0.1083084428		17.233		0.0789663		78.9663				12.45253		1.685343547		16.6818		0.500669		500.669				12.39065		12495.4826794449		16.8372		0.0818682		81.8682				12.4458		1.5953955253		16.8122		42.5611		0.0425611				12.426		0.902634624		16.855		0.802499		802.499				12.45812		18.1972562358		16.7977		0.0773089		77.3089				12.38963		1.5809591002

																						17.198		6.22506		0.00622506				12.90998		0.1167928705		17.7528		0.0809326		80.9326				12.97233		1.7273094365		17.1972		0.49911		499.11				12.90605		12456.5738244984		17.3593		0.0816332		81.6332				12.9679		1.5908159944		17.33		44.5311		0.0445311				12.9438		0.9444143291		17.3737		0.800843		800.843				12.97682		18.1597052154		17.3153		0.0787651		78.7651				12.90723		1.6107382413

																						17.7135		6.4062		0.0064062				13.42548		0.1201913696		18.2708		0.0833257		83.3257				13.49033		1.7783843335		17.713		0.495607		495.607				13.42185		12369.1474493361		17.8773		0.0823747		82.3747				13.4859		1.6052658759		17.8467		45.8494		0.0458494				13.4605		0.9723727988		17.893		0.793755		793.755				13.49612		17.9989795918		17.8297		0.0791597		79.1597				13.42163		1.618807771

																						18.2288		5.93422		0.00593422				13.94078		0.1113362101		18.792		0.084281		84.281				14.01153		1.7987728878		18.2297		0.493715		493.715				13.93855		12321.9277228711		18.394		0.0829173		82.9173				14.0026		1.6158397203		18.3625		47.216		0.047216				13.9763		1.0013556136		18.4133		0.787995		787.995				14.01642		17.8683673469		18.3455		0.0805233		80.5233				13.93743		1.6466932515

																						18.7467		6.52371		0.00652371				14.45868		0.12239606		19.3112		0.0867128		86.7128				14.53073		1.8506737422		18.7482		0.491599		491.599				14.45705		12269.1175002496		18.9107		0.0838861		83.8861				14.5193		1.6347190799		18.8792		48.0549		0.0480549				14.493		1.0191469814		18.9323		0.778076		778.076				14.53542		17.643446712		18.861		0.0823771		82.3771				14.45293		1.684603272

																						19.2622		6.12004		0.00612004				14.97418		0.1148225141		19.83		0.0904765		90.4765				15.04953		1.9310007615		19.2635		0.488804		488.804				14.97235		12199.3610861535		19.4255		0.0834627		83.4627				15.0341		1.6264681294		19.3968		49.7799		0.0497799				15.0106		1.0557307334		19.4538		0.766888		766.888				15.05692		17.3897505669		19.3747		0.0834044		83.4044				14.96663		1.7056114519

																						19.7792		6.64909		0.00664909				15.49118		0.1247484053		20.3527		0.0887838		88.7838				15.57223		1.8948741984		19.7807		0.485198		485.198				15.48955		12109.3640810622		19.9455		0.0859998		85.9998				15.5541		1.6759095241		19.9147		50.2837		0.0502837				15.5285		1.0664153098		19.9723		0.748471		748.471				15.57542		16.9721315193		19.8898		0.0850778		85.0778				15.48173		1.7398323108

																						20.2935		6.44314		0.00644314				16.00548		0.1208844278		20.8727		0.0914244		91.4244				16.09223		1.9512313807		20.2962		0.482752		482.752				16.00505		12048.3178596386		20.4647		0.0848666		84.8666				16.0733		1.6538264416		20.4318		50.5827		0.0505827				16.0456		1.0727564935		20.4897		0.727871		727.871				16.09282		16.5050113379		20.4052		0.0864479		86.4479				15.99713		1.7678507157

																						20.8112		6.80042		0.00680042				16.52318		0.1275876173		21.3925		0.0936118		93.6118				16.61203		1.9979161118		20.8115		0.479533		479.533				16.52035		11967.9794349606		20.9837		0.0881654		88.1654				16.5923		1.7181113625		20.9468		52.4885		0.0524885				16.5606		1.1131746468		21.0088		0.700554		700.554				16.61192		15.8855782313		20.9232		0.0917819		91.7819				16.51513		1.8769304703

																						21.3268		5.97075		0.00597075				17.03878		0.112021576		21.9112		0.096467		96.467				17.13073		2.058853409		21.3253		0.476435		476.435				17.03415		11890.6608765099		21.5027		0.0865239		86.5239				17.1113		1.6861228522		21.4647		51.9514		0.0519514				17.0785		1.101783845		21.5263		0.679044		679.044				17.12942		15.3978231293		21.445		0.0960703		96.0703				17.03693		1.9646278119

																						21.844		6.61581		0.00661581				17.55598		0.124124015		22.4282		0.0986871		98.6871				17.64773		2.106236042		21.8393		0.471224		471.224				17.54815		11760.6069681541		22.0193		0.0892064		89.2064				17.6279		1.7383977098		21.9813		53.3531		0.0533531				17.5951		1.1315110595		22.0458		0.65838		658.38				17.64892		14.9292517007		21.9658		0.098085		98.085				17.55773		2.0058282209

																						22.3612		6.72129		0.00672129				18.07318		0.1261030019		22.9497		0.10099		100.99				18.16923		2.1553858395		22.3552		0.468356		468.356				18.06405		11689.0286512928		22.5388		0.0890999		89.0999				18.1474		1.7363223054		22.4977		55.0714		0.0550714				18.1115		1.1679527181		22.568		0.633483		633.483				18.17112		14.3646938776		22.4848		0.100437		100.437				18.07673		2.0539263804

																						22.8778		7.07465		0.00707465				18.58978		0.1327326454		23.4677		0.0984869		98.4869				18.68723		2.1019632601		22.869		0.463756		463.756				18.57785		11574.2238195068		23.0575		0.0902767		90.2767				18.6661		1.759255037		23.0158		55.9426		0.0559426				18.6296		1.1864291034		23.0865		0.615174		615.174				18.68962		13.9495238095		23.0015		0.10168		101.68				18.59343		2.0793456033

																						23.3945		6.98132		0.00698132				19.10648		0.1309816135		23.9838		0.102353		102.353				19.20333		2.1844757583		23.3843		0.459776		459.776				19.09315		11474.8926824399		23.5745		0.0908624		90.8624				19.1831		1.7706687869		23.5328		56.5559		0.0565559				19.1466		1.1994359528		23.6073		0.59077		590.77				19.21042		13.3961451247		23.5193		0.106728		106.728				19.11123		2.1825766871

																						23.9105		6.91263		0.00691263				19.62248		0.1296928705		24.5055		0.103665		103.665				19.72503		2.2124772061		23.8992		0.454275		454.275				19.60805		11337.6010781671		24.0958		0.089495		89.495				19.7044		1.7440217635		24.0505		57.3497		0.0573497				19.6643		1.2162708411		24.1255		0.571043		571.043				19.72862		12.9488208617		24.033		0.104291		104.291				19.62493		2.1327402863

																						24.426		6.85811		0.00685811				20.13798		0.1286699812		25.0272		0.107126		107.126				20.24673		2.2863438305		24.4193		0.448117		448.117				20.12815		11183.9123490067		24.6152		0.0915174		91.5174				20.2238		1.7834330112		24.5675		58.5705		0.0585705				20.1813		1.2421615335		24.648		0.55925		559.25				20.25112		12.6814058957		24.5472		0.105709		105.709				20.13913		2.1617382413

																						24.9438		6.89151		0.00689151				20.65578		0.1292966229		25.5427		0.106202		106.202				20.76223		2.2666232986		24.9378		0.439569		439.569				20.64665		10970.5750224618		25.1372		0.0933582		93.3582				20.7458		1.8193053534		25.0855		58.0062		0.0580062				20.6993		1.2301938748		25.1662		0.540141		540.141				20.76932		12.2480952381		25.0635		0.108828		108.828				20.65543		2.2255214724

																						25.4593		7.19697		0.00719697				21.17128		0.1350275797		26.0628		0.109119		109.119				21.28233		2.3288795665		25.4542		0.431389		431.389				21.16305		10766.4220824598		25.6515		0.0923779		92.3779				21.2601		1.8002018891		25.6032		60.5852		0.0605852				21.217		1.284889235		25.6828		0.530076		530.076				21.28592		12.0198639456		25.5802		0.110019		110.019				21.17213		2.2498773006

																						25.976		7.02273		0.00702273				21.68798		0.1317585366		26.5847		0.110113		110.113				21.80423		2.350094078		25.9708		0.422255		422.255				21.67965		10538.4596186483		26.1713		0.0904963		90.4963				21.7799		1.7635344624		26.1198		59.6315		0.0596315				21.7336		1.264663192		26.2018		0.520583		520.583				21.80492		11.8046031746		26.0958		0.110442		110.442				21.68773		2.2585276074

																						26.4913		6.82324		0.00682324				22.20328		0.1280157598		27.1032		0.110359		110.359				22.32273		2.3553443495		26.4885		0.41374		413.74				22.19735		10325.9458919836		26.6913		0.0936766		93.6766				22.2999		1.8255101305		26.6357		61.5649		0.0615649				22.2495		1.3056666853		26.7205		0.509849		509.849				22.32362		11.5612018141		26.6098		0.113782		113.782				22.20173		2.3268302658

																						27.0092		7.33506		0.00733506				22.72118		0.1376183865		27.6217		0.111596		111.596				22.84123		2.3817451049		27.0032		0.405755		405.755				22.71205		10126.6596785465		27.2073		0.0931471		93.1471				22.8159		1.8151915705		27.1555		62.0983		0.0620983				22.7693		1.3169790177		27.2412		0.508719		508.719				22.84432		11.5355782313		27.1277		0.113732		113.732				22.71963		2.325807771

																						27.5263		7.5185		0.0075185				23.23828		0.1410600375		28.1425		0.113724		113.724				23.36203		2.4271620874		27.5182		0.39685		396.85				23.22705		9904.4124987521		27.7237		0.093389		93.389				23.3323		1.8199055642		27.6713		63.389		0.063389				23.2851		1.3443521473		27.7605		0.508168		508.168				23.36362		11.5230839002		27.6443		0.112898		112.898				23.23623		2.3087525562

																						28.0438		7.22993		0.00722993				23.75578		0.1356459662		28.662		0.114449		114.449				23.88153		2.4426354485		28.0338		0.389544		389.544				23.74265		9722.0724767895		28.2388		0.0949921		94.9921				23.8474		1.8511457596		28.188		63.416		0.063416				23.8018		1.3449247626		28.2768		0.503494		503.494				23.87992		11.4170975057		28.1602		0.114938		114.938				23.75213		2.3504703476

																						28.5617		7.44805		0.00744805				24.27368		0.1397382739		29.1797		0.117861		117.861				24.39923		2.515456287		28.5513		0.381003		381.003				24.26015		9508.9098532495		28.7565		0.0946657		94.6657				24.3651		1.8447850836		28.7047		64.4801		0.0644801				24.3185		1.3674921658		28.7945		0.504911		504.911				24.39762		11.4492290249		28.6777		0.115605		115.605				24.26963		2.3641104294

																						29.0783		6.90892		0.00690892				24.79028		0.1296232645		29.6967		0.117118		117.118				24.91623		2.4995987597		29.0682		0.3728		372.8				24.77705		9304.1828890885		29.2732		0.0944435		94.4435				24.8818		1.840454991		29.2263		64.9333		0.0649333				24.8401		1.3771036188		29.3088		0.507862		507.862				24.91192		11.5161451247		29.1922		0.118338		118.338				24.78413		2.42

																						29.5943		7.25318		0.00725318				25.30628		0.1360821764		30.213		0.115075		115.075				25.43253		2.4559958954		29.5838		0.365176		365.176				25.29265		9113.9063591894		29.7912		0.0947514		94.7514				25.3998		1.8464551508		29.7427		64.7977		0.0647977				25.3565		1.3742278177		29.8283		0.501356		501.356				25.43142		11.36861678		29.7112		0.117329		117.329				25.30313		2.3993660532

																						30.1107		7.38183		0.00738183				25.82268		0.1384958724		30.7307		0.121781		121.781				25.95023		2.5991191496		30.101		0.356796		356.796				25.80985		8904.7619047619		30.3083		0.0960043		96.0043				25.9169		1.8708708709		30.2635		66.0342		0.0660342				25.8773		1.4004514753		30.3472		0.503958		503.958				25.95032		11.4276190476		30.2273		0.118789		118.789				25.81923		2.4292229039

																						30.6277		7.76419		0.00776419				26.33968		0.145669606		31.249		0.121092		121.092				26.46853		2.5844141209		30.6177		0.349343		349.343				26.32655		8718.7531196965		30.8235		0.0960059		96.0059				26.4321		1.8709020507		30.7787		66.4804		0.0664804				26.3925		1.4099144725		30.8638		0.496514		496.514				26.46692		11.2588208617		30.7432		0.118629		118.629				26.33513		2.4259509202

																						31.144		7.64505		0.00764505				26.85598		0.143434334		31.7653		0.122684		122.684				26.98483		2.6183914876		31.1347		0.342401		342.401				26.84355		8545.4976539882		31.3412		0.0963183		96.3183				26.9498		1.8769899036		31.2953		65.9198		0.0659198				26.9091		1.3980252833		31.3852		0.496525		496.525				26.98832		11.2590702948		31.2605		0.121241		121.241				26.85243		2.4793660532

																						31.6587		7.65454		0.00765454				27.37068		0.1436123827		32.2813		0.122246		122.246				27.50083		2.6090434432		31.6492		0.333593		333.593				27.35805		8325.6713586902		31.8605		0.0963988		96.3988				27.4691		1.8785586365		31.8122		67.706		0.067706				27.426		1.4359069632		31.9022		0.493071		493.071				27.50532		11.1807482993		31.7765		0.124435		124.435				27.36843		2.5446830266

																						32.175		7.17478		0.00717478				27.88698		0.134611257		32.798		0.121939		121.939				28.01753		2.6024912752		32.1647		0.327373		327.373				27.87355		8170.4352600579		32.3772		0.0977658		97.7658				27.9858		1.905197865		32.3295		68.1484		0.0681484				27.9433		1.4452893701		32.4185		0.494776		494.776				28.02162		11.2194104308		32.2925		0.123064		123.064				27.88443		2.5166462168

																						32.6917		7.81242		0.00781242				28.40368		0.1465744841		33.3147		0.123059		123.059				28.53423		2.6263949502		32.6842		0.320604		320.604				28.39305		8001.4974543276		32.8962		0.0981708		98.1708				28.5048		1.9130902479		32.8495		68.4008		0.0684008				28.4633		1.4506422622		32.9365		0.497637		497.637				28.53962		11.2842857143		32.8078		0.122513		122.513				28.39973		2.5053783231

																						33.2073		7.89113		0.00789113				28.91928		0.1480512195		33.8325		0.121113		121.113				29.05203		2.5848623148		33.2005		0.313979		313.979				28.90935		7836.1535389837		33.413		0.0968593		96.8593				29.0216		1.8875325683		33.3658		67.8611		0.0678611				28.9796		1.4391963197		33.4523		0.504173		504.173				29.05542		11.4324943311		33.326		0.125724		125.724				28.91793		2.5710429448

																						33.7255		7.39435		0.00739435				29.43748		0.1387307692		34.3527		0.126441		126.441				29.57223		2.6985755117		33.719		0.306845		306.845				29.42785		7658.106219427		33.9295		0.0959193		95.9193				29.5381		1.8692144448		33.886		68.6461		0.0686461				29.4998		1.4558445778		33.9703		0.504842		504.842				29.57342		11.4476643991		33.8432		0.124375		124.375				29.43513		2.5434560327

																						34.242		7.69857		0.00769857				29.95398		0.1444384615		34.8712		0.127954		127.954				30.09073		2.7308668156		34.2362		0.300264		300.264				29.94505		7493.8604372567		34.4462		0.0987945		98.7945				30.0548		1.9252445177		34.4037		70.177		0.070177				30.0175		1.4883118624		34.489		0.51199		511.99				30.09212		11.6097505669		34.3598		0.125086		125.086				29.95173		2.55799591

																						35.8838		11.5002		0.0115002				31.59578		0.2157636023		36.6787		0.210291		210.291				31.89823		4.4881497531		35.882		0.324119		324.119				31.59085		8089.2233203554		36.1737		0.172726		172.726				31.7823		3.3659746703		36.1297		109.862		0.109862				31.7435		2.3299502376		36.2143		0.637718		637.718				31.81742		14.4607256236		36.0855		0.219347		219.347				31.67743		4.4856237219

																						36.3992		12.4178		0.0124178				32.11118		0.2329793621		37.1995		0.204367		204.367				32.41903		4.3617163863		36.398		0.318965		318.965				32.10685		7960.5919936109		36.689		0.166397		166.397				32.2976		3.2426391349		36.649		108.026		0.108026				32.2628		2.2910124007		36.7343		0.620877		620.877				32.33742		14.0788435374		36.6045		0.215472		215.472				32.19643		4.4063803681

																						36.9148		12.9878		0.0129878				32.62678		0.243673546		37.7182		0.205261		205.261				32.93773		4.3807966412		36.914		0.31342		313.42				32.62285		7822.2022561645		37.2102		0.162928		162.928				32.8188		3.1750374645		37.167		109.435		0.109435				32.7808		2.3208944335		37.2537		0.578269		578.269				32.85682		13.112675737		37.1213		0.216121		216.121				32.71323		4.4196523517

																						37.4292		12.6468		0.0126468				33.14118		0.2372757974		38.2375		0.195991		195.991				33.45703		4.1829510453		37.4313		0.308221		308.221				33.14015		7692.4478386743		37.7277		0.158597		158.597				33.3363		3.0906376851		37.6838		108.786		0.108786				33.2976		2.3071304596		37.7723		0.560313		560.313				33.37542		12.7055102041		37.637		0.210239		210.239				33.22893		4.2993660532

																						37.9462		12.6809		0.0126809				33.65818		0.2379155722		38.7532		0.197538		197.538				33.97273		4.2159679964		37.9462		0.303934		303.934				33.65505		7585.4547269642		38.2432		0.155775		155.775				33.8518		3.03564434		38.2		109.551		0.109551				33.8138		2.3233545583		38.288		0.548953		548.953				33.89112		12.4479138322		38.1542		0.210347		210.347				33.74613		4.3015746421

																						38.4612		13.1452		0.0131452				34.17318		0.2466266417		39.2685		0.194816		194.816				34.48803		4.1578735291		38.4628		0.299353		299.353				34.17165		7471.1240890486		38.7607		0.153022		153.022				34.3693		2.9819956231		38.717		109.713		0.109713				34.3308		2.3267902498		38.8038		0.526921		526.921				34.40692		11.9483219955		38.6727		0.210324		210.324				34.26463		4.3011042945

																						38.9765		12.6189		0.0126189				34.68848		0.2367523452		39.7878		0.192869		192.869				35.00733		4.1163195512		38.9787		0.295123		295.123				34.68755		7365.5535589498		39.2778		0.152526		152.526				34.8864		2.9723298899		39.2342		109.272		0.109272				34.848		2.317437534		39.3217		0.515257		515.257				34.92482		11.6838321995		39.1875		0.205967		205.967				34.77943		4.21200409

																						39.494		13.0881		0.0130881				35.20598		0.2455553471		40.3038		0.190927		190.927				35.52333		4.0748722861		39.4935		0.291531		291.531				35.20235		7275.9059598682		39.7977		0.149272		149.272				35.4063		2.908918003		39.7515		110.081		0.110081				35.3653		2.3345947835		39.8378		0.496765		496.765				35.44092		11.2645124717		39.7028		0.202152		202.152				35.29473		4.1339877301

																						40.0107		12.5011		0.0125011				35.72268		0.2345422139		40.8212		0.192628		192.628				36.04073		4.1111759925		40.0117		0.286511		286.511				35.72055		7150.6189477888		40.3133		0.1476		147.6				35.9219		2.8763351281		40.2708		109.503		0.109503				35.8846		2.3223365756		40.357		0.477847		477.847				35.96012		10.8355328798		40.2172		0.205254		205.254				35.80913		4.1974233129

																						40.5253		12.8982		0.0128982				36.23728		0.2419924953		41.339		0.191137		191.137				36.55853		4.0793542251		40.5283		0.282222		282.222				36.23715		7043.5759209344		40.8323		0.144219		144.219				36.4409		2.8104483458		40.7885		109.796		0.109796				36.4023		2.3285505115		40.8742		0.474039		474.039				36.47732		10.7491836735		40.7355		0.203723		203.723				36.32743		4.1661145194

																						41.0448		13.5741		0.0135741				36.75678		0.254673546		41.8568		0.187914		187.914				37.07633		4.0105671318		41.0462		0.279671		279.671				36.75505		6979.9091544375		41.3513		0.143776		143.776				36.9599		2.801815443		41.305		110.194		0.110194				36.9188		2.3369912844		41.3917		0.451252		451.252				36.99482		10.2324716553		41.2497		0.203098		203.098				36.84163		4.1533333333

																						41.5635		13.0709		0.0130709				37.27548		0.2452326454		42.3735		0.192032		192.032				37.59303		4.0984558226		41.5652		0.275348		275.348				37.27405		6872.0175701308		41.8685		0.14076		140.76				37.4771		2.743041549		41.8198		109.594		0.109594				37.4336		2.3242665011		41.9078		0.458895		458.895				37.51092		10.4057823129		41.7662		0.197306		197.306				37.35813		4.0348875256

																						42.0825		13.482		0.013482				37.79448		0.252945591		42.8903		0.190452		190.452				38.10983		4.0647345668		42.0795		0.271561		271.561				37.78835		6777.5032444844		42.3875		0.140078		140.078				37.9961		2.7297511658		42.3375		109.25		0.10925				37.9513		2.3169709587		42.4245		0.446429		446.429				38.02762		10.123106576		42.2852		0.201331		201.331				37.87713		4.117198364

																						42.5985		13.1747		0.0131747				38.31048		0.2471801126		43.4093		0.187768		187.768				38.62883		4.007451117		42.5972		0.26771		267.71				38.30605		6681.3916342218		42.9038		0.140039		140.039				38.5124		2.7289911586		42.8538		109.629		0.109629				38.4676		2.3250087801		42.9407		0.44138		441.38				38.54382		10.00861678		42.8028		0.2001		200.1				38.39473		4.0920245399

																						43.1153		13.3116		0.0133116				38.82728		0.2497485929		43.9282		0.185829		185.829				39.14773		3.9660678796		43.1133		0.264877		264.877				38.82215		6610.6868323849		43.4185		0.137133		137.133				39.0271		2.6723608748		43.368		109.569		0.109569				38.9818		2.3237363018		43.4575		0.436736		436.736				39.06062		9.9033106576		43.319		0.200419		200.419				38.91093		4.0985480573

																						43.6328		13.1537		0.0131537				39.34478		0.2467861163		44.4438		0.191552		191.552				39.66333		4.0882113904		43.6292		0.260778		260.778				39.33805		6508.3857442348		43.9372		0.138042		138.042				39.5458		2.6900748899		43.8838		110.275		0.110275				39.4976		2.3387091301		43.9732		0.43239		432.39				39.57632		9.8047619048		43.8338		0.196621		196.621				39.42573		4.0208793456

																						44.1508		13.2646		0.0132646				39.86278		0.2488667917		44.9617		0.189455		189.455				40.18123		4.0434560275		44.1482		0.257979		257.979				39.85705		6438.5294998503		44.4565		0.13715		137.15				40.0651		2.67269216		44.4032		110.474		0.110474				40.017		2.3429295166		44.4908		0.426377		426.377				40.09392		9.6684126984		44.3515		0.200091		200.091				39.94343		4.0918404908

																						44.6667		13.6062		0.0136062				40.37868		0.2552757974		45.4778		0.187097		187.097				40.69733		3.9931302545		44.6667		0.254894		254.894				40.37555		6361.5353898373		44.9753		0.134613		134.613				40.5839		2.6232527141		44.9198		110.329		0.110329				40.5336		2.3398543606		45.0065		0.425645		425.645				40.60962		9.651814059		44.8688		0.196656		196.656				40.46073		4.021595092

																						45.1842		13.0198		0.0130198				40.89618		0.2442739212		45.9962		0.190901		190.901				41.21573		4.0743173793		45.1825		0.251671		251.671				40.89135		6281.0971348707		45.4935		0.134843		134.843				41.1021		2.6277348081		45.4352		110.353		0.110353				41.049		2.3403633519		45.524		0.421812		421.812				41.12712		9.5648979592		45.3842		0.194777		194.777				40.97613		3.9831697342

																						45.6997		12.8409		0.0128409				41.41168		0.2409174484		46.5128		0.193919		193.919				41.73233		4.1387292465		45.6973		0.248485		248.485				41.40615		6201.5823100729		46.0107		0.135259		135.259				41.6193		2.6358415521		45.9527		110.683		0.110683				41.5665		2.3473619828		46.0398		0.409722		409.722				41.64292		9.2907482993		45.9013		0.204263		204.263				41.49323		4.1771574642

																						46.2175		12.9446		0.0129446				41.92948		0.2428630394		47.0323		0.192168		192.168				42.25183		4.1013584117		46.213		0.245337		245.337				41.92185		6123.0158730159		46.5258		0.132453		132.453				42.1344		2.5811600049		46.4695		110.289		0.110289				42.0833		2.3390060417		46.5565		0.408676		408.676				42.15962		9.2670294785		46.4203		0.20359		203.59				42.01223		4.163394683

																						46.733		13.4861		0.0134861				42.44498		0.2530225141		47.5513		0.192795		192.795				42.77083		4.1147402012		46.7323		0.243002		243.002				42.44115		6064.7399420984		47.0425		0.133796		133.796				42.6511		2.6073315366		46.9875		111.492		0.111492				42.6013		2.3645192322		47.0718		0.40526		405.26				42.67492		9.189569161		46.939		0.208432		208.432				42.53093		4.2624130879

																						47.2508		13.2768		0.0132768				42.96278		0.2490956848		48.069		0.192014		192.014				43.28853		4.0980716564		47.2495		0.23984		239.84				42.95835		5985.8240990316		47.5573		0.133186		133.186				43.1659		2.5954442437		47.5032		111.312		0.111312				43.117		2.3607017972		47.5865		0.399571		399.571				43.18962		9.0605668934		47.4547		0.202886		202.886				43.04663		4.148997955

																						47.768		13.351		0.013351				43.47998		0.2504878049		48.5843		0.190623		190.623				43.80383		4.0683841457		47.7657		0.237002		237.002				43.47455		5914.9945093341		48.0732		0.132088		132.088				43.6818		2.5740471166		48.0208		110.781		0.110781				43.6346		2.349440364		48.1042		0.387427		387.427				43.70732		8.7851927438		47.9708		0.207243		207.243				43.56273		4.2380981595

																						48.2838		13.2871		0.0132871				43.99578		0.2492889306		49.099		0.190681		190.681				44.31853		4.0696220146		48.2797		0.233715		233.715				43.98855		5832.9589697514		48.5922		0.128953		128.953				44.2008		2.5129542261		48.5365		111.052		0.111052				44.1503		2.3551877245		48.6235		0.393406		393.406				44.22662		8.9207709751		48.4872		0.204712		204.712				44.07913		4.1863394683

																						48.8005		13.2347		0.0132347				44.51248		0.2483058161		49.6143		0.193892		193.892				44.83383		4.1381529972		48.7955		0.231525		231.525				44.50435		5778.3018867925		49.108		0.129154		129.154				44.7166		2.5168711866		49.0523		111.137		0.111137				44.6661		2.3569904021		49.1407		0.392471		392.471				44.74382		8.899569161		49.0027		0.207208		207.208				44.59463		4.2373824131

																						49.3188		13.1467		0.0131467				45.03078		0.2466547842		50.1325		0.193286		193.286				45.35203		4.1252194016		49.3128		0.229058		229.058				45.02165		5716.7315563542		49.626		0.129528		129.528				45.2346		2.5241594612		49.5722		110.878		0.110878				45.186		2.3514975373		49.6578		0.387666		387.666				45.26092		8.7906122449		49.5193		0.206061		206.061				45.11123		4.2139263804

																						49.8343		12.8585		0.0128585				45.54628		0.2412476548		50.6527		0.194371		194.371				45.87223		4.1483760868		49.8318		0.227044		227.044				45.54065		5666.4670060896		50.1448		0.128795		128.795				45.7534		2.5098752224		50.0888		111.725		0.111725				45.7026		2.3694606898		50.1753		0.383961		383.961				45.77842		8.7065986395		50.0365		0.209682		209.682				45.62843		4.2879754601

																						50.3503		13.0138		0.0130138				46.06228		0.2441613508		51.1682		0.190848		190.848				46.38773		4.0731862233		50.348		0.223564		223.564				46.05685		5579.6146550863		50.6607		0.127787		127.787				46.2693		2.4902319581		50.6045		111.15		0.11115				46.2183		2.3572661058		50.6922		0.381632		381.632				46.29532		8.6537868481		50.5555		0.206405		206.405				46.14743		4.2209611452

																						50.8677		13.2226		0.0132226				46.57968		0.2480787992		51.6847		0.192273		192.273				46.90423		4.1035993812		50.8643		0.220522		220.522				46.57315		5503.6937206748		51.181		0.12876		128.76				46.7896		2.5091931646		51.1213		111.873		0.111873				46.7351		2.3725994696		51.208		0.382217		382.217				46.81112		8.6670521542		51.0698		0.207771		207.771				46.66173		4.2488957055

																						51.3847		12.9891		0.0129891				47.09668		0.2436979362		52.2003		0.19539		195.39				47.41983		4.1701241625		51.3833		0.219839		219.839				47.09215		5486.6476989119		51.698		0.12626		126.26				47.3066		2.4604747512		51.637		112.272		0.112272				47.2508		2.3810614505		51.7253		0.374496		374.496				47.32842		8.4919727891		51.5857		0.212421		212.421				47.17763		4.3439877301

																						51.9038		13.5273		0.0135273				47.61578		0.2537954972		52.7182		0.198623		198.623				47.93773		4.2391246816		51.9		0.216821		216.821				47.60885		5411.3257462314		52.2148		0.126704		126.704				47.8234		2.4691271414		52.1555		112.308		0.112308				47.7693		2.3818249375		52.244		0.372167		372.167				47.84712		8.4391609977		52.1005		0.207483		207.483				47.69243		4.243006135

																						52.4205		13.2433		0.0132433				48.13248		0.248467167		53.2357		0.199655		199.655				48.45523		4.2611502107		52.418		0.214295		214.295				48.12685		5348.2829190376		52.7313		0.128626		128.626				48.3399		2.5065818577		52.6712		112.946		0.112946				48.285		2.3953556238		52.7592		0.37355		373.55				48.36232		8.470521542		52.6148		0.209286		209.286				48.20673		4.2798773006

																						52.9348		13.3878		0.0133878				48.64678		0.2511782364		53.7515		0.195489		195.489				48.97103		4.1722370766		52.938		0.212392		212.392				48.64685		5300.7886592792		53.2473		0.125346		125.346				48.8559		2.4426632992		53.1883		112.304		0.112304				48.8021		2.3817401056		53.2737		0.367721		367.721				48.87682		8.3383446712		53.1318		0.21001		210.01				48.72373		4.2946830266

																						53.451		13.0554		0.0130554				49.16298		0.2449418386		54.2693		0.197141		197.141				49.48883		4.2074949973		53.4542		0.209849		209.849				49.16305		5237.3215533593		53.764		0.125391		125.391				49.3726		2.4435402307		53.7037		112.874		0.112874				49.3175		2.3938286498		53.789		0.364547		364.547				49.39212		8.2663718821		53.6467		0.206615		206.615				49.23863		4.2252556237

																						53.9657		12.4123		0.0124123				49.67768		0.2328761726		54.7848		0.198849		198.849				50.00433		4.2439481017		53.9682		0.207489		207.489				49.67705		5178.4216831387		54.2833		0.127428		127.428				49.8919		2.4832359939		54.2213		112.431		0.112431				49.8351		2.3844335181		54.3068		0.37166		371.66				49.90992		8.4276643991		54.1625		0.209279		209.279				49.75443		4.2797341513

																						54.4837		13.2748		0.0132748				50.19568		0.2490581614		55.3015		0.1985		198.5				50.52103		4.2364995458		54.4855		0.205551		205.551				50.19435		5130.0539083558		54.801		0.126469		126.469				50.4096		2.4645476106		54.7383		113.289		0.113289				50.3521		2.4026299582		54.8247		0.372629		372.629				50.42782		8.4496371882		54.6792		0.210309		210.309				50.27113		4.300797546

																						55.0013		13.1812		0.0131812				50.71328		0.2473020638		55.8205		0.199924		199.924				51.04003		4.2668913612		55.005		0.20353		203.53				50.71385		5079.6146550863		55.3185		0.125264		125.264				50.9271		2.4410653353		55.2545		113.002		0.113002				50.8683		2.3965432702		55.3403		0.369252		369.252				50.94342		8.3730612245		55.1963		0.207614		207.614				50.78823		4.2456850716

																						55.518		13.3365		0.0133365				51.22998		0.2502157598		56.342		0.197977		197.977				51.56153		4.2253373833		55.5212		0.200815		200.815				51.23005		5011.8548467605		55.8372		0.124155		124.155				51.4458		2.4194538471		55.7718		113.165		0.113165				51.3856		2.4000001697		55.8587		0.368284		368.284				51.46182		8.3511111111		55.7135		0.209793		209.793				51.30543		4.2902453988

																						56.0347		13.2892		0.0132892				51.74668		0.2493283302		56.8628		0.201804		201.804				52.08233		4.3070153871		56.037		0.198258		198.258				51.74585		4948.0383348308		56.3532		0.126223		126.223				51.9618		2.4597537187		56.2867		114.025		0.114025				51.9005		2.4182390257		56.3747		0.371857		371.857				51.97782		8.4321315193		56.2288		0.209483		209.483				51.82073		4.2839059305

																						56.5518		13.174		0.013174				52.26378		0.2471669794		57.381		0.205526		205.526				52.60053		4.3864524214		56.5552		0.197456		197.456				52.26405		4928.0223619846		56.87		0.12477		124.77				52.4786		2.4314385768		56.805		113.741		0.113741				52.4188		2.4122159616		56.8913		0.357896		357.896				52.49442		8.1155555556		56.7462		0.206629		206.629				52.33813		4.2255419223

																						57.0695		13.421		0.013421				52.78148		0.2518011257		57.8985		0.203806		203.806				53.11803		4.3497432062		57.0742		0.194788		194.788				52.78305		4861.4355595488		57.387		0.123153		123.153				52.9956		2.399927507		57.3217		113.957		0.113957				52.9355		2.4167968836		57.412		0.365539		365.539				53.01512		8.2888662132		57.2633		0.214341		214.341				52.85523		4.3832515337

																						57.5862		13.4002		0.0134002				53.29818		0.2514108818		58.4158		0.203148		203.148				53.63533		4.3356997972		57.5922		0.191548		191.548				53.30105		4780.573025856		57.9073		0.123679		123.679				53.5159		2.4101778612		57.8383		114.482		0.114482				53.4521		2.427931069		57.9277		0.369443		369.443				53.53082		8.3773922902		57.7787		0.21482		214.82				53.37063		4.3930470348

																						58.1038		13.2216		0.0132216				53.81578		0.2480600375		58.933		0.206114		206.114				54.15253		4.3990018508		58.1087		0.190459		190.459				53.81755		4753.3942298093		58.424		0.121647		121.647				54.0326		2.3705795348		58.356		114.28		0.11428				53.9698		2.4236470586		58.444		0.359045		359.045				54.04712		8.1416099773		58.2945		0.214662		214.662				53.88643		4.3898159509

																						58.6195		12.6064		0.0126064				54.33148		0.2365178236		59.4503		0.205105		205.105				54.66983		4.3774672007		58.6242		0.189283		189.283				54.33305		4724.0441249875		58.9393		0.123687		123.687				54.5479		2.4103337601		58.8737		114.693		0.114693				54.4875		2.4324059511		58.9607		0.361009		361.009				54.56382		8.1861451247		58.8105		0.212783		212.783				54.40243		4.351390593

																						59.1365		13.4078		0.0134078				54.84848		0.2515534709		59.9675		0.206841		206.841				55.18703		4.414517897		59.1413		0.186421		186.421				54.85015		4652.6155535589		59.4575		0.12367		123.67				55.0661		2.4100024749		59.3907		114.462		0.114462				55.0045		2.4275069096		59.48		0.355683		355.683				55.08312		8.0653741497		59.3302		0.215523		215.523				54.92213		4.4074233129

																						59.6552		13.3184		0.0133184				55.36718		0.2498761726		60.4865		0.208552		208.552				55.70603		4.4510350291		59.6587		0.18438		184.38				55.36755		4601.677148847		59.9742		0.123702		123.702				55.5828		2.4106260706		59.9087		114.465		0.114465				55.5225		2.4275705335		59.9987		0.363751		363.751				55.60182		8.2483219955		59.8473		0.214393		214.393				55.43923		4.3843149284

																						60.1718		13.7112		0.0137112				55.88378		0.2572457786		61.0032		0.209767		209.767				56.22273		4.476966248		60.175		0.183763		183.763				55.88385		4586.2783268444		60.4908		0.123968		123.968				56.0994		2.4158097098		60.4258		114.379		0.114379				56.0396		2.4257466479		60.5158		0.366084		366.084				56.11892		8.3012244898		60.3628		0.224338		224.338				55.95473		4.5876891616

																						60.6885		13.468		0.013468				56.40048		0.2526829268		61.5188		0.206643		206.643				56.73833		4.4102920688		60.6912		0.181264		181.264				56.40005		4523.909354098		61.0115		0.124572		124.572				56.6201		2.4275800785		60.945		114.701		0.114701				56.5588		2.4325756149		61.0323		0.353669		353.669				56.63542		8.0197052154		60.8807		0.227345		227.345				56.47263		4.6491820041

																						61.2028		13.7052		0.0137052				56.91478		0.2571332083		62.0352		0.210268		210.268				57.25473		4.4876588741		61.2093		0.180055		180.055				56.91815		4493.735649396		61.5287		0.122788		122.788				57.1373		2.3928146186		61.4602		115.567		0.115567				57.074		2.4509417188		61.5487		0.358818		358.818				57.15182		8.136462585		61.3985		0.226016		226.016				56.99043		4.62200409

																						61.7188		13.3895		0.0133895				57.43078		0.2512101313		62.5542		0.211411		211.411				57.77373		4.5120534281		61.7297		0.178178		178.178				57.43855		4446.8902865129		62.0453		0.123818		123.818				57.6539		2.412886605		61.9772		115.039		0.115039				57.591		2.4397439095		62.0653		0.355462		355.462				57.66842		8.0603628118		61.9138		0.228291		228.291				57.50573		4.6685276074

																						62.2355		14.2743		0.0142743				57.94748		0.2678105066		63.0723		0.212609		212.609				58.29183		4.5376218234		62.2468		0.176153		176.153				57.95565		4396.351202955		62.561		0.123064		123.064				58.1696		2.3981931315		62.4943		114.386		0.114386				58.1081		2.4258951037		62.5825		0.358045		358.045				58.18562		8.1189342404		62.431		0.229929		229.929				58.02293		4.7020245399

																						62.7508		13.0801		0.0130801				58.46278		0.2454052533		63.5888		0.212734		212.734				58.80833		4.5402896442		62.7635		0.174061		174.061				58.47235		4344.1399620645		63.0755		0.123884		123.884				58.6841		2.4141727711		63.0112		116.074		0.116074				58.625		2.4616941607		63.0992		0.353834		353.834				58.70232		8.023446712		62.9492		0.233037		233.037				58.54113		4.7655828221

																						63.2662		12.9385		0.0129385				58.97818		0.2427485929		64.1057		0.215086		215.086				59.32523		4.5904873618		63.28		0.172242		172.242				58.98885		4298.7421383648		63.5925		0.122194		122.194				59.2011		2.3812391236		63.5283		115.592		0.115592				59.1421		2.4514719181		63.6163		0.364451		364.451				59.21942		8.2641950113		63.4657		0.224071		224.071				59.05763		4.5822290389

																						63.7807		12.7592		0.0127592				59.49268		0.2393846154		64.6227		0.216252		216.252				59.84223		4.6153727949		63.799		0.171568		171.568				59.50785		4281.9207347509		64.1088		0.123146		123.146				59.7174		2.3997910954		64.0458		116.085		0.116085				59.6596		2.4619274484		64.1323		0.360689		360.689				59.73542		8.1788888889		63.9825		0.230924		230.924				59.57443		4.7223721881

																						64.2985		13.8277		0.0138277				60.01048		0.2594315197		65.1398		0.214865		214.865				60.35933		4.5857706545		64.3153		0.17059		170.59				60.02415		4257.5122292103		64.6242		0.122779		122.779				60.2328		2.3926392324		64.5615		116.045		0.116045				60.1753		2.4610791295		64.6482		0.354961		354.961				60.25132		8.0490022676		64.498		0.232139		232.139				60.08993		4.7472188139

																						64.8163		13.9357		0.0139357				60.52828		0.2614577861		65.656		0.216769		216.769				60.87553		4.626406902		64.8357		0.169438		169.438				60.54455		4228.7611061196		65.1435		0.121897		121.897				60.7521		2.3754513761		65.0782		115.983		0.115983				60.692		2.4597642352		65.1663		0.349915		349.915				60.76942		7.9345804989		65.014		0.224259		224.259				60.60593		4.5860736196

																						65.3325		13.2599		0.0132599				61.04448		0.2487786116		66.1713		0.220178		220.178				61.39083		4.6991637129		65.35		0.167683		167.683				61.05885		4184.960567036		65.6597		0.120367		120.367				61.2683		2.3456357071		65.5943		116.521		0.116521				61.2081		2.4711741242		65.6838		0.357767		357.767				61.28692		8.1126303855		65.53		0.22898		228.98				61.12193		4.6826175869

																						65.8487		13.7364		0.0137364				61.56068		0.2577185741		66.6883		0.220628		220.628				61.90783		4.708767868		65.867		0.166132		166.132				61.57585		4146.2513726665		66.1792		0.123927		123.927				61.7878		2.4150107278		66.1112		116.559		0.116559				61.725		2.4719800272		66.201		0.354599		354.599				61.80412		8.0407936508		66.0462		0.232979		232.979				61.63813		4.764396728

																						67.4198		13.5086		0.0135086				63.13178		0.2534446529		68.2693		0.270099		270.099				63.48883		5.7646059991		67.4472		0.188742		188.742				63.15605		4710.5420784666		67.8125		0.182914		182.914				63.4211		3.5645119487		67.6867		124.095		0.124095				63.3005		2.6318033054		67.7755		0.424717		424.717				63.37862		9.6307709751		67.6282		0.333906		333.906				63.22013		6.8283435583

																						67.9355		13.4551		0.0134551				63.64748		0.2524409006		68.7872		0.28131		281.31				64.00673		6.0038775176		67.9682		0.190459		190.459				63.67705		4753.3942298093		68.3292		0.184925		184.925				63.9378		3.6037010404		68.2042		127.305		0.127305				63.818		2.699880896		68.292		0.428014		428.014				63.89512		9.7055328798		68.1453		0.337417		337.417				63.73723		6.9001431493

																						68.4537		14.024		0.014024				64.16568		0.2631144465		69.3038		0.281031		281.031				64.52333		5.9979229414		68.4825		0.191302		191.302				64.19135		4774.4334631127		68.8453		0.187829		187.829				64.4539		3.6602923495		68.7212		131.358		0.131358				64.335		2.7858368072		68.8063		0.433811		433.811				64.40942		9.836984127		68.662		0.343896		343.896				64.25393		7.0326380368

																						68.9688		13.2998		0.0132998				64.68078		0.2495272045		69.8205		0.279351		279.351				65.04003		5.9620674289		69.0045		0.193028		193.028				64.71335		4817.5102326046		69.3602		0.187587		187.587				64.9688		3.655576407		69.239		138.041		0.138041				64.8528		2.9275696852		69.3217		0.427774		427.774				64.92482		9.7000907029		69.1773		0.34722		347.22				64.76923		7.1006134969

																						69.4847		13.9298		0.0139298				65.19668		0.2613470919		70.3372		0.286236		286.236				65.55673		6.1090110025		69.5222		0.195776		195.776				65.23105		4886.0936408106		69.876		0.188611		188.611				65.4846		3.6755314692		69.758		143.745		0.143745				65.3718		3.0485399584		69.8383		0.4336		433.6				65.44142		9.8321995465		69.6935		0.35722		357.22				65.28543		7.3051124744

																						70.005		13.6325		0.0136325				65.71698		0.2557692308		70.8597		0.28866		288.66				66.07923		6.1607453849		70.0408		0.196102		196.102				65.74965		4894.2298093241		70.3958		0.190496		190.496				66.0044		3.7122651529		70.2795		147.536		0.147536				65.8933		3.1289393808		70.3542		0.428051		428.051				65.95732		9.7063718821		70.2125		0.36089		360.89				65.80443		7.3801635992

																						70.5213		13.86		0.01386				66.23328		0.2600375235		71.3763		0.286033		286.033				66.59583		6.1046784614		70.5592		0.197883		197.883				66.26805		4938.679245283		70.9128		0.191668		191.668				66.5214		3.7351043451		70.7968		152.468		0.152468				66.4106		3.2335370995		70.8688		0.427056		427.056				66.47192		9.6838095238		70.7282		0.358417		358.417				66.32013		7.329591002

																						71.0383		14.0521		0.0140521				66.75028		0.263641651		71.893		0.290129		290.129				67.11253		6.1920976158		71.0787		0.198677		198.677				66.78755		4958.4955575522		71.4318		0.190128		190.128				67.0404		3.7050938024		71.3175		154.059		0.154059				66.9313		3.2672789832		71.3865		0.432118		432.118				66.98962		9.7985941043		71.2443		0.366976		366.976				66.83623		7.5046216769

																						71.5538		13.9198		0.0139198				67.26578		0.2611594747		72.408		0.297538		297.538				67.62753		6.3502246945		71.5958		0.199964		199.964				67.30465		4990.6159528801		71.9508		0.194051		194.051				67.5594		3.7815427368		71.832		157.622		0.157622				67.4458		3.3428429881		71.9022		0.437386		437.386				67.50532		9.9180498866		71.7587		0.363701		363.701				67.35063		7.4376482618

																						72.0693		13.8875		0.0138875				67.78128		0.2605534709		72.9232		0.293004		293.004				68.14273		6.2534574959		72.1125		0.199612		199.612				67.82135		4981.8308874913		72.4662		0.191953		191.953				68.0748		3.7406582442		72.3513		161.978		0.161978				67.9651		3.4352249148		72.4175		0.442105		442.105				68.02062		10.0250566893		72.2782		0.373884		373.884				67.87013		7.6458895706

																						72.586		13.9697		0.0139697				68.29798		0.2620956848		73.4412		0.296115		296.115				68.66073		6.3198542217		72.6297		0.201593		201.593				68.33855		5031.2718378756		72.9833		0.192678		192.678				68.5919		3.7547865841		72.873		165.012		0.165012				68.4868		3.4995699023		72.9355		0.43974		439.74				68.53862		9.9714285714		72.7948		0.380612		380.612				68.38673		7.7834764826

																						73.1037		14.4625		0.0144625				68.81568		0.2713414634		73.9565		0.295972		295.972				69.17603		6.3168022347		73.1463		0.20286		202.86				68.85515		5062.893081761		73.4987		0.196482		196.482				69.1073		3.828916522		73.3907		167.362		0.167362				69.0045		3.5494086369		73.4508		0.434885		434.885				69.05392		9.8613378685		73.3097		0.37614		376.14				68.90163		7.6920245399

																						73.618		14.4139		0.0144139				69.32998		0.2704296435		74.4732		0.298594		298.594				69.69273		6.3727624453		73.664		0.203659		203.659				69.37285		5082.8341818908		74.014		0.195365		195.365				69.6226		3.8071491349		73.9128		170.238		0.170238				69.5266		3.6104027648		73.9685		0.434275		434.275				69.57162		9.8475056689		73.8232		0.384001		384.001				69.41513		7.8527811861

																						74.1325		14.4092		0.0144092				69.84448		0.2703414634		74.992		0.298281		298.281				70.21153		6.3660822218		74.1795		0.204493		204.493				69.88835		5103.648797045		74.5323		0.19755		197.55				70.1409		3.8497290282		74.4357		171.425		0.171425				70.0495		3.6355766278		74.4857		0.434878		434.878				70.08882		9.8611791383		74.339		0.380504		380.504				69.93093		7.7812678937

																						74.648		14.7062		0.0147062				70.35998		0.2759136961		75.5115		0.299769		299.769				70.73103		6.3978399615		74.6967		0.20572		205.72				70.40555		5134.2717380453		75.0497		0.196455		196.455				70.6583		3.8283903631		74.9547		174.878		0.174878				70.5685		3.7088077557		75.0032		0.445847		445.847				70.60632		10.1099092971		74.8563		0.387916		387.916				70.44823		7.9328425358

																						75.1647		14.3492		0.0143492				70.87668		0.2692157598		76.0292		0.302065		302.065				71.24873		6.4468424953		75.2143		0.205291		205.291				70.92315		5123.5649396027		75.5688		0.194287		194.287				71.1774		3.786141755		75.474		176.447		0.176447				71.0878		3.742083064		75.5213		0.442323		442.323				71.12442		10.03		75.373		0.389656		389.656				70.96493		7.9684253579

																						75.6815		14.5598		0.0145598				71.39348		0.2731669794		76.5467		0.305659		305.659				71.76623		6.523547681		75.7315		0.206519		206.519				71.44035		5154.2128381751		76.089		0.197245		197.245				71.6976		3.8437853817		75.9955		178.292		0.178292				71.6093		3.7812117726		76.037		0.443284		443.284				71.64012		10.0517913832		75.889		0.388873		388.873				71.48093		7.9524130879

																						76.1982		14.9788		0.0149788				71.91018		0.2810281426		77.0635		0.302866		302.866				72.28303		6.4639378914		76.2505		0.207427		207.427				71.95935		5176.8743136668		76.6047		0.197408		197.408				72.2133		3.8469618223		76.5117		180.574		0.180574				72.1255		3.8296083651		76.5545		0.440918		440.918				72.15762		9.9981405896		76.4032		0.377067		377.067				71.99513		7.7109815951

																						76.7157		15.124		0.015124				72.42768		0.2837523452		77.5787		0.310204		310.204				72.79823		6.6205496479		76.767		0.208233		208.233				72.47585		5196.9901168014		77.1223		0.195971		195.971				72.7309		3.8189584783		77.03		182.809		0.182809				72.6438		3.8770081829		77.0713		0.439638		439.638				72.67442		9.9691156463		76.918		0.388941		388.941				72.50993		7.953803681

																						77.2323		15.0359		0.0150359				72.94428		0.2820994371		78.0962		0.314229		314.229				73.31573		6.70645348		77.2862		0.209429		209.429				72.99505		5226.8393730658		77.638		0.196108		196.108				73.2466		3.8216282473		77.5477		184.481		0.184481				73.1615		3.9124679123		77.5875		0.444384		444.384				73.19062		10.0767346939		77.432		0.400863		400.863				73.02393		8.197607362

																						77.7508		14.9701		0.0149701				73.46278		0.2808649156		78.6152		0.306314		306.314				73.83473		6.5375270624		77.8047		0.209413		209.413				73.51355		5226.4400519117		78.157		0.198261		198.261				73.7656		3.863584545		78.0647		185.108		0.185108				73.6785		3.9257653109		78.1047		0.444999		444.999				73.70782		10.0906802721		77.9492		0.387217		387.217				73.54113		7.9185480573

																						78.267		15.2219		0.0152219				73.97898		0.2855891182		79.133		0.309579		309.579				74.35253		6.6072105436		78.323		0.211126		211.126				74.03185		5269.192372966		78.674		0.196496		196.496				74.2826		3.8291893451		78.58		186.173		0.186173				74.1938		3.9483518012		78.6223		0.434034		434.034				74.22542		9.8420408163		78.4647		0.394235		394.235				74.05663		8.0620654397

																						78.7842		15.1877		0.0151877				74.49618		0.2849474672		79.6485		0.309115		309.115				74.86803		6.5973075925		78.8407		0.211289		211.289				74.54955		5273.2604572227		79.1943		0.200036		200.036				74.8029		3.8981746185		79.1015		187.466		0.187466				74.7153		3.9757737092		79.1383		0.449533		449.533				74.74142		10.1934920635		78.9818		0.395901		395.901				74.57373		8.0961349693

																						79.3		15.2842		0.0152842				75.01198		0.2867579737		80.1663		0.310977		310.977				75.38583		6.6370474522		79.3557		0.211465		211.465				75.06455		5277.6529899171		79.7098		0.198458		198.458				75.3184		3.8674235559		79.6193		188.178		0.188178				75.2331		3.9908737854		79.6557		0.444956		444.956				75.25882		10.0897052154		79.4972		0.390398		390.398				75.08913		7.983599182

																						79.8152		15.0217		0.0150217				75.52718		0.2818330206		80.688		0.312755		312.755				75.90753		6.6749945363		79.8713		0.213272		213.272				75.58015		5322.7513227513		80.2253		0.200288		200.288				75.8339		3.9030854346		80.1372		190.546		0.190546				75.751		4.0410942635		80.17		0.447222		447.222				75.77312		10.1410884354		80.0143		0.401654		401.654				75.60623		8.2137832311

																						80.3333		16.1979		0.0161979				76.04528		0.3039005629		81.2057		0.308481		308.481				76.42523		6.583776405		80.3935		0.213295		213.295				76.10235		5323.3253469103		80.7462		0.198902		198.902				76.3548		3.8760759462		80.6568		190.998		0.190998				76.2706		4.0506802669		80.688		0.439988		439.988				76.29112		9.9770521542		80.531		0.393131		393.131				76.12293		8.0394887526

																						80.8485		15.3935		0.0153935				76.56048		0.2888086304		81.7212		0.318962		318.962				76.94073		6.8074678496		80.9102		0.213439		213.439				76.61905		5326.9192372966		81.262		0.199837		199.837				76.8706		3.8942966328		81.1753		192.003		0.192003				76.7891		4.0719942789		81.2037		0.438974		438.974				76.80682		9.9540589569		81.0463		0.411604		411.604				76.63823		8.4172597137

																						81.3653		15.8844		0.0158844				77.07728		0.2980187617		82.2385		0.320346		320.346				77.45803		6.8370059623		81.4263		0.214883		214.883				77.13515		5362.9579714485		81.7788		0.202435		202.435				77.3874		3.944924808		81.6943		192.744		0.192744				77.3081		4.0877093863		81.7208		0.440884		440.884				77.32392		9.9973696145		81.5593		0.407674		407.674				77.15123		8.3368916155

																						81.8828		15.4401		0.0154401				77.59478		0.2896829268		82.756		0.323951		323.951				77.97553		6.9139459162		81.9435		0.215117		215.117				77.65235		5368.7980433263		82.299		0.199711		199.711				77.9076		3.8918412247		82.2148		194.258		0.194258				77.8286		4.1198182562		82.2383		0.437772		437.772				77.84142		9.9268027211		82.0747		0.409125		409.125				77.66663		8.3665644172

																						82.3995		16.0061		0.0160061				78.11148		0.3003020638		83.2735		0.325759		325.759				78.49303		6.9525332773		82.4622		0.216096		216.096				78.17105		5393.231506439		82.8153		0.20049		200.49				78.4239		3.9070218824		82.7333		197.4		0.1974				78.3471		4.1864537047		82.7547		0.443754		443.754				78.35782		10.0624489796		82.5927		0.418999		418.999				78.18463		8.5684867076

																						82.9208		15.4982		0.0154982				78.63278		0.2907729831		83.794		0.322739		322.739				79.01353		6.888078725		82.9802		0.215897		215.897				78.68905		5388.2649495857		83.3325		0.200252		200.252				78.9411		3.9023838894		83.2505		195.943		0.195943				78.8643		4.1555536893		83.2727		0.444354		444.354				78.87582		10.0760544218		83.112		0.428888		428.888				78.70393		8.7707157464

																						83.4375		16.0417		0.0160417				79.14948		0.3009699812		84.312		0.32533		325.33				79.53153		6.9433773161		83.4963		0.217248		217.248				79.20515		5421.9826295298		83.8508		0.209691		209.691				79.4594		4.0863251311		83.7718		199.107		0.199107				79.3856		4.2226557132		83.7872		0.442292		442.292				79.39032		10.0292970522		83.6292		0.426463		426.463				79.22113		8.7211247444

																						83.9545		15.5253		0.0155253				79.66648		0.2912814259		84.8272		0.322152		322.152				80.04673		6.8755506382		84.0138		0.218041		218.041				79.72265		5441.7739842268		84.3685		0.211022		211.022				79.9771		4.1122628144		84.2935		198.604		0.198604				79.9073		4.2119881032		84.3042		0.441282		441.282				79.90732		10.0063945578		84.143		0.434784		434.784				79.73493		8.8912883436

																						84.4708		14.9313		0.0149313				80.18278		0.2801369606		85.3453		0.327313		327.313				80.56483		6.9856996264		84.531		0.217891		217.891				80.23985		5438.0303484077		84.8865		0.211192		211.192				80.4951		4.1155756665		84.8125		200.846		0.200846				80.4263		4.2595363768		84.8217		0.447309		447.309				80.42482		10.1430612245		84.6578		0.441935		441.935				80.24973		9.0375255624

																						84.9857		16.3351		0.0163351				80.69768		0.3064746717		85.864		0.33685		336.85				81.08353		7.1892436877		85.0473		0.218333		218.333				80.75615		5449.061595288		85.4028		0.214286		214.286				81.0114		4.175869575		85.3283		200.854		0.200854				80.9421		4.2597060405		85.3383		0.449069		449.069				80.94142		10.1829705215		85.1727		0.443924		443.924				80.76463		9.078200409

																						85.5045		16.0673		0.0160673				81.21648		0.3014502814		86.382		0.337858		337.858				81.60153		7.2107569952		85.5648		0.219737		219.737				81.27365		5484.1020265549		85.9213		0.213752		213.752				81.5299		4.1654633219		85.8468		202.239		0.202239				81.4606		4.289079082		85.857		0.44153		441.53				81.46012		10.0120181406		85.6897		0.440712		440.712				81.28163		9.0125153374

																						86.0213		15.9961		0.0159961				81.73328		0.3001144465		86.8987		0.329313		329.313				82.11823		7.0283847604		86.083		0.220523		220.523				81.79185		5503.718678247		86.4397		0.214015		214.015				82.0483		4.1705884989		86.3625		202.657		0.202657				81.9763		4.2979440143		86.3718		0.445323		445.323				81.97492		10.0980272109		86.2038		0.442522		442.522				81.79573		9.0495296524

																						86.5393		15.6983		0.0156983				82.25128		0.2945272045		87.4133		0.338469		338.469				82.63283		7.2237973037		86.5992		0.222262		222.262				82.30805		5547.1198961765		86.9568		0.214859		214.859				82.5654		4.1870358353		86.882		203.561		0.203561				82.4958		4.3171160212		86.8888		0.441138		441.138				82.49192		10.0031292517		86.7198		0.444983		444.983				82.31173		9.0998568507

																						87.0568		15.9116		0.0159116				82.76878		0.2985290807		87.9333		0.340349		340.349				83.15283		7.2639213296		87.1158		0.22067		220.67				82.82465		5507.3874413497		87.4755		0.2167		216.7				83.0841		4.222912075		87.3972		204.416		0.204416				83.011		4.3352488374		87.4038		0.441787		441.787				83.00692		10.017845805		87.2342		0.451163		451.163				82.82613		9.2262372188

																						87.5735		16.2627		0.0162627				83.28548		0.3051163227		88.4505		0.340602		340.602				83.67003		7.269320999		87.6313		0.221286		221.286				83.34015		5522.7613057802		87.995		0.215711		215.711				83.6036		4.2036390706		87.914		205.952		0.205952				83.5278		4.3678242826		87.9205		0.447727		447.727				83.52362		10.1525396825		87.7505		0.453721		453.721				83.34243		9.2785480573

																						88.0917		16.5628		0.0165628				83.80368		0.3107467167		88.9695		0.33802		338.02				84.18903		7.2142144911		88.151		0.222205		222.205				83.85985		5545.6973145652		88.5148		0.21515		215.15				84.1234		4.1927066586		88.4328		207.346		0.207346				84.0466		4.3973881958		88.4397		0.441855		441.855				84.04282		10.0193877551		88.2667		0.468187		468.187				83.85863		9.5743762781

																						88.6093		16.7382		0.0167382				84.32128		0.3140375235		89.4862		0.347053		347.053				84.70573		7.4070018986		88.6652		0.222769		222.769				84.37405		5559.7733852451		89.033		0.217353		217.353				84.6416		4.2356373245		88.9485		206.848		0.206848				84.5623		4.3868266257		88.9552		0.444771		444.771				84.55832		10.0855102041		88.781		0.469261		469.261				84.37293		9.5963394683

																						89.1253		16.0627		0.0160627				84.83728		0.3013639775		90.0045		0.34858		348.58				85.22403		7.4395919984		89.181		0.223531		223.531				84.88985		5578.7910552062		89.5492		0.21507		215.07				85.1578		4.1911476694		89.4675		208.85		0.20885				85.0813		4.4292849859		89.4718		0.435057		435.057				85.07492		9.8652380952		89.2973		0.453017		453.017				84.88923		9.2641513292

																						89.6403		16.1962		0.0161962				85.35228		0.3038686679		90.5223		0.35641		356.41				85.74183		7.6067042979		89.6958		0.224043		224.043				85.40465		5591.5693321354		90.0652		0.217097		217.097				85.6738		4.230648559		89.9818		208.304		0.208304				85.5956		4.4177054331		89.9872		0.437345		437.345				85.59032		9.9171201814		89.8122		0.467873		467.873				85.40413		9.5679550102

																						90.157		16.2816		0.0162816				85.86898		0.3054709193		91.038		0.348974		348.974				86.25753		7.4480009698		90.2102		0.224872		224.872				85.91905		5612.259159429		90.583		0.219661		219.661				86.1916		4.2806141638		90.4992		209.473		0.209473				86.113		4.4424975526		90.5042		0.44175		441.75				86.10732		10.0170068027		90.3277		0.46401		464.01				85.91963		9.4889570552

																						90.6765		16.4721		0.0164721				86.38848		0.3090450281		91.5565		0.351913		351.913				86.77603		7.5107267742		90.726		0.225121		225.121				86.43485		5618.4735948887		91.1005		0.221773		221.773				86.7091		4.3217714795		91.0188		211.687		0.211687				86.6326		4.489452003		91.0218		0.443963		443.963				86.62492		10.0671882086		90.8448		0.475498		475.498				86.43673		9.7238854806

																						91.1925		16.1977		0.0161977				86.90448		0.3038968105		92.0722		0.353682		353.682				87.29173		7.5484817752		91.242		0.225605		225.605				86.95085		5630.5530597983		91.618		0.216591		216.591				87.2266		4.2207879521		91.5388		209.872		0.209872				87.1526		4.4509595335		91.5388		0.448119		448.119				87.14192		10.1614285714		91.3592		0.470786		470.786				86.95113		9.6275255624

																						91.7098		16.4831		0.0164831				87.42178		0.3092514071		92.5898		0.356916		356.916				87.80933		7.6175036368		91.7615		0.2269		226.9				87.47035		5662.8731157033		92.1343		0.220868		220.868				87.7429		4.3041354138		92.0532		209.937		0.209937				87.667		4.4523380517		92.0555		0.442474		442.474				87.65862		10.0334240363		91.8755		0.484695		484.695				87.46743		9.9119631902

																						92.2242		16.4032		0.0164032				87.93618		0.3077523452		93.1065		0.350056		350.056				88.32603		7.4710936273		92.2787		0.227292		227.292				87.98755		5672.6564839772		92.6523		0.221081		221.081				88.2609		4.3082862226		92.5703		211.742		0.211742				88.1841		4.4906184414		92.5712		0.444646		444.646				88.17432		10.082675737		92.3903		0.49342		493.42				87.98223		10.0903885481

																						92.742		17.0974		0.0170974				88.45398		0.3207767355		93.624		0.358864		358.864				88.84353		7.6590789573		92.7958		0.226965		226.965				88.50465		5664.4953578916		93.1705		0.221312		221.312				88.7791		4.312787804		93.0883		211.541		0.211541				88.7021		4.486355639		93.0875		0.441782		441.782				88.69062		10.0177324263		92.9052		0.497445		497.445				88.49713		10.1726993865

																						93.2607		16.648		0.016648				88.97268		0.3123452158		94.1432		0.360612		360.612				89.36273		7.6963857643		93.3148		0.227985		227.985				89.02365		5689.9520814615		93.6893		0.218794		218.794				89.2979		4.263718618		93.607		213.235		0.213235				89.2208		4.5222819439		93.6045		0.442873		442.873				89.20762		10.0424716553		93.4232		0.502693		502.693				89.01513		10.2800204499

																						93.7763		16.7124		0.0167124				89.48828		0.3135534709		94.6598		0.356936		356.936				89.87933		7.6179304881		93.831		0.22789		227.89				89.53985		5687.5811121094		94.2045		0.223841		223.841				89.8131		4.362071351		94.1237		216.225		0.216225				89.7375		4.5856937806		94.1223		0.434596		434.596				89.72542		9.8547845805		93.9378		0.503023		503.023				89.52973		10.2867689162

																						94.292		16.8697		0.0168697				90.00398		0.3165046904		95.176		0.367176		367.176				90.39553		7.836478374		94.3463		0.228392		228.392				90.05515		5700.1098133174		94.7203		0.221033		221.033				90.3289		4.3073508291		94.6413		215.646		0.215646				90.2551		4.5734143648		94.6393		0.445696		445.696				90.24242		10.1064852608		94.4537		0.496285		496.285				90.04563		10.1489775051

																						94.8087		16.9481		0.0169481				90.52068		0.3179756098		95.6922		0.367399		367.399				90.91173		7.8412377664		94.8663		0.229516		229.516				90.57515		5728.1621243885		95.2357		0.223285		223.285				90.8443		4.3512363759		95.157		214.911		0.214911				90.7708		4.5578265052		95.1573		0.447322		447.322				90.76042		10.1433560091		94.9703		0.494616		494.616				90.56223		10.1148466258

																						95.325		16.9415		0.0169415				91.03698		0.3178517824		96.2092		0.373727		373.727				91.42873		7.9762935303		95.383		0.23018		230.18				91.09185		5744.7339522811		95.7533		0.225246		225.246				91.3619		4.3894510994		95.6717		216.844		0.216844				91.2855		4.5988215154		95.6723		0.449416		449.416				91.27542		10.1908390023		95.4852		0.500348		500.348				91.07713		10.2320654397

																						95.8422		16.7462		0.0167462				91.55418		0.3141876173		96.7307		0.365689		365.689				91.95023		7.8047419769		95.9038		0.231835		231.835				91.61265		5786.0387341519		96.2727		0.221776		221.776				91.8813		4.3218299416		96.194		217.895		0.217895				91.8078		4.6211110941		96.1907		0.449529		449.529				91.79382		10.1934013605		96.0047		0.50872		508.72				91.59663		10.4032719836

																						96.3575		16.7105		0.0167105				92.06948		0.3135178236		97.2462		0.368128		368.128				92.46573		7.8567964978		96.4218		0.230755		230.755				92.13065		5759.0845562544		96.7893		0.220934		220.934				92.3979		4.3054215799		96.7097		220.008		0.220008				92.3235		4.6659235393		96.7065		0.443518		443.518				92.30962		10.0570975057		96.52		0.504076		504.076				92.11193		10.3083026585

																						96.874		17.6249		0.0176249				92.58598		0.330673546		97.7625		0.37497		374.97				92.98203		8.0028223411		96.9383		0.231089		231.089				92.64715		5767.4203853449		97.305		0.225023		225.023				92.9136		4.3851054169		97.225		218.969		0.218969				92.8388		4.6438884562		97.2237		0.445639		445.639				92.82682		10.1051927438		97.0365		0.50985		509.85				92.62843		10.4263803681

																						97.3883		17.4152		0.0174152				93.10028		0.326739212		98.2787		0.38206		382.06				93.49823		8.154141141		97.456		0.232771		232.771				93.16485		5809.3990216632		97.8212		0.226171		226.171				93.4298		4.4074769123		97.7427		220.903		0.220903				93.3565		4.6849046744		97.7402		0.442746		442.746				93.34332		10.0395918367		97.5527		0.50893		508.93				93.14463		10.4075664622

																						99.1778		19.3387		0.0193387				94.88978		0.3628273921		100.072		1.01897		1018.97				95.29153		21.7474354772		99.2542		0.521697		521.697				94.96305		13020.2905061396		99.617		1.08872		1088.72				95.2256		21.216284422		99.5383		488.217		0.488217				95.1521		10.3540925448		99.532		0.871843		871.843				95.13512		19.7696825397		99.3417		1.74433		1744.33				94.93363		35.6713701431

																						99.6935		20.0416		0.0200416				95.40548		0.3760150094		100.591		1.06949		1069.49				95.81053		22.8256619611		99.7722		0.580798		580.798				95.48105		14495.3079764401		100.135		1.17231		1172.31				95.7436		22.845233293		100.057		534.605		0.534605				95.6708		11.3378879574		100.048		0.946888		946.888				95.65112		21.47138322		99.8583		1.88889		1888.89				95.45023		38.627607362

																						100.209		20.3898		0.0203898				95.92098		0.3825478424		101.107		1.1101		1110.1				96.32653		23.6923836062		100.29		0.631316		631.316				95.99885		15756.1146051712		100.653		1.22257		1222.57				96.2616		23.8246682763		100.577		569.561		0.569561				96.1908		12.0792338323		100.563		1.01353		1013.53				96.16612		22.9825396825		100.374		1.9811		1981.1				95.96593		40.5132924335

																						100.726		20.6035		0.0206035				96.43798		0.3865572233		101.623		1.13772		1137.72				96.84253		24.2818653062		100.809		0.675571		675.571				96.51785		16860.6119596686		101.17		1.26656		1266.56				96.7786		24.6819174788		101.095		597.66		0.59766				96.7088		12.6751566421		101.08		1.06442		1064.42				96.68312		24.1365079365		100.893		2.04931		2049.31				96.48493		41.9081799591

																						101.246		21.6337		0.0216337				96.95798		0.4058855535		102.143		1.16367		1163.67				97.36253		24.8357049194		101.333		0.710127		710.127				97.04185		17723.0458221024		101.69		1.30582		1305.82				97.2986		25.4469914431		101.614		620.691		0.620691				97.2278		13.1635974489		101.6		1.11448		1114.48				97.20312		25.2716553288		101.409		2.10384		2103.84				97.00093		43.0233128834

																						101.762		22.6663		0.0226663				97.47398		0.4252589118		102.661		1.1808		1180.8				97.88053		25.2013030918		101.854		0.740967		740.967				97.56285		18492.7373465109		102.21		1.31364		1313.64				97.8186		25.5993826403		102.131		640.57		0.64057				97.7448		13.5851907275		102.117		1.1412		1141.2				97.72012		25.8775510204		101.924		2.19676		2196.76				97.51593		44.9235173824

																						102.28		22.4276		0.0224276				97.99198		0.4207804878		103.178		1.19684		1196.84				98.39753		25.5436378662		102.37		0.770218		770.218				98.07885		19222.771288809		102.726		1.32241		1322.41				98.3346		25.7702868345		102.648		658.86		0.65886				98.2618		13.9730845384		102.632		1.16525		1165.25				98.23512		26.4229024943		102.439		2.23822		2238.22				98.03093		45.7713701431

																						102.796		22.9685		0.0229685				98.50798		0.4309287054		103.694		1.21347		1213.47				98.91353		25.8985647551		102.888		0.792009		792.009				98.59685		19766.6217430368		103.243		1.34625		1346.25				98.8516		26.2348656249		103.168		673.947		0.673947				98.7818		14.2930492144		103.149		1.18923		1189.23				98.75212		26.9666666667		102.954		2.24503		2245.03				98.54593		45.9106339468

																						103.313		23.8344		0.0238344				99.02498		0.4471744841		104.211		1.22571		1225.71				99.43053		26.1597977749		103.405		0.815407		815.407				99.11385		20350.5790156734		103.759		1.36037		1360.37				99.3676		26.5100272238		103.684		687.864		0.687864				99.2978		14.5882005629		103.665		1.20903		1209.03				99.26812		27.4156462585		103.469		2.28049		2280.49				99.06093		46.6357873211

																						103.831		23.953		0.023953				99.54298		0.4493996248		104.732		1.24013		1240.13				99.95153		26.4675575908		103.926		0.834623		834.623				99.63485		20830.1637216732		104.278		1.37416		1374.16				99.8866		26.7787579923		104.205		697.81		0.69781				99.8188		14.7991350541		104.186		1.26033		1260.33				99.78912		28.5789115646		103.988		2.29671		2296.71				99.57993		46.9674846626

																						104.349		24.3037		0.0243037				100.06098		0.4559793621		105.249		1.25642		1256.42				100.46853		26.8152280069		104.444		0.852375		852.375				100.15285		21273.2105420785		104.796		1.38739		1387.39				100.4046		27.0365758361		104.722		712.4		0.7124				100.3358		15.1085593679		104.702		1.26194		1261.94				100.30512		28.6154195011		104.502		2.32804		2328.04				100.09393		47.6081799591

																						104.864		25.4893		0.0254893				100.57598		0.4782232645		105.765		1.2677		1267.7				100.98453		27.0559721625		104.96		0.871266		871.266				100.66885		21744.6840371369		105.316		1.39521		1395.21				100.9246		27.1889670332		105.238		722.069		0.722069				100.8518		15.3136192507		105.218		1.28192		1281.92				100.82112		29.0684807256		105.015		2.33058		2330.58				100.60693		47.6601226994

																						105.382		25.9696		0.0259696				101.09398		0.4872345216		106.283		1.2717		1271.7				101.50253		27.1413424304		105.481		0.8848		884.8				101.18985		22082.4598183089		105.832		1.40458		1404.58				101.4406		27.3715636467		105.754		730.831		0.730831				101.3678		15.4994435028		105.734		1.29437		1294.37				101.33712		29.3507936508		105.532		2.37878		2378.78				101.12393		48.645807771

																						105.896		25.1605		0.0251605				101.60798		0.472054409		106.798		1.2843		1284.3				102.01753		27.4102587744		105.996		0.899299		899.299				101.70485		22444.3196565838		106.348		1.4146		1414.6				101.9566		27.5668270477		106.272		740.57		0.74057				101.8858		15.7059879437		106.251		1.30688		1306.88				101.85412		29.6344671202		106.049		2.40546		2405.46				101.64093		49.1914110429

																						106.414		26.7864		0.0267864				102.12598		0.5025590994		107.317		1.28948		1289.48				102.53653		27.5208132713		106.515		0.912131		912.131				102.22385		22764.5752221224		106.87		1.41538		1415.38				102.4786		27.5820271927		106.793		748.756		0.748756				102.4068		15.8795964038		106.77		1.3238		1323.8				102.37312		30.0181405896		106.568		2.40086		2400.86				102.15993		49.0973415133

																						106.932		27.2879		0.0272879				102.64398		0.5119681051		107.833		1.31621		1316.21				103.05253		28.0913000867		107.031		0.925132		925.132				102.73985		23089.0486173505		107.389		1.41586		1415.86				102.9976		27.591381128		107.309		755.932		0.755932				102.9228		16.031784812		107.286		1.29231		1292.31				102.88912		29.3040816327		107.085		2.38085		2380.85				102.67693		48.6881390593

																						107.451		27.9728		0.0279728				103.16298		0.5248180113		108.349		1.31996		1319.96				103.56853		28.1713347129		107.547		0.936431		936.431				103.25585		23371.0442248178		107.904		1.43635		1436.35				103.5126		27.9906772444		107.827		763.482		0.763482				103.4408		16.1919050019		107.804		1.35418		1354.18				103.40712		30.7070294785		107.599		2.41852		2418.52				103.19093		49.4584867076

																						107.969		29.0831		0.0290831				103.68098		0.5456491557		108.867		1.32005		1320.05				104.08653		28.1732555439		108.063		0.947309		947.309				103.77185		23642.5326944195		108.42		1.42765		1427.65				104.0286		27.8211371657		108.345		773.872		0.773872				103.9588		16.4122558326		108.32		1.3591		1359.1				103.92312		30.8185941043		108.113		2.48557		2485.57				103.70493		50.8296523517

																						108.488		29.0723		0.0290723				104.19998		0.5454465291		109.383		1.33448		1334.48				104.60253		28.4812287855		108.577		0.955935		955.935				104.28585		23857.8167115903		108.935		1.43436		1434.36				104.5436		27.9518973873		108.861		780.542		0.780542				104.4748		16.5537130069		108.836		1.37214		1372.14				104.43912		31.1142857143		108.628		2.4534		2453.4				104.21993		50.1717791411

																						109.007		29.8248		0.0298248				104.71898		0.559564728		109.9		1.33116		1331.16				105.11953		28.4103714631		109.098		0.966822		966.822				104.80685		24129.5297993411		109.452		1.43587		1435.87				105.0606		27.981323309		109.38		789.549		0.789549				104.9938		16.7447332122		109.354		1.37324		1373.24				104.95712		31.1392290249		109.145		2.47188		2471.88				104.73693		50.5496932515

																						109.524		29.37		0.02937				105.23598		0.5510318949		110.417		1.34097		1340.97				105.63653		28.6197420452		109.614		0.977438		977.438				105.32285		24394.4793850454		109.968		1.4429		1442.9				105.5766		28.1183194876		109.897		793.688		0.793688				105.5108		16.832513009		109.872		1.38609		1386.09				105.47512		31.4306122449		109.659		2.55895		2558.95				105.25093		52.3302658487

																						110.04		30.0683		0.0300683				105.75198		0.5641332083		110.934		1.34208		1342.08				106.15353		28.6434322945		110.134		0.985857		985.857				105.84285		24604.5971847859		110.484		1.45192		1451.92				106.0926		28.2940955232		110.417		801.712		0.801712				106.0308		17.0026857776		110.392		1.39715		1397.15				105.99512		31.6814058957		110.173		2.56489		2564.89				105.76493		52.4517382413

																						110.556		29.6182		0.0296182				106.26798		0.5556885553		111.451		1.35398		1353.98				106.67053		28.8974088416		110.65		0.992771		992.771				106.35885		24777.1538384746		111.002		1.4401		1440.1				106.6106		28.0637548645		110.934		808.352		0.808352				106.5478		17.1435067127		110.91		1.38712		1387.12				106.51312		31.453968254		110.688		2.58308		2583.08				106.27993		52.8237218814

																						111.071		31.2247		0.0312247				106.78298		0.5858292683		111.968		1.34505		1345.05				107.18753		28.7068197185		111.164		1.00019		1000.19				106.87285		24962.3140660876		111.518		1.45329		1453.29				107.1266		28.3207932137		111.45		815.484		0.815484				107.0638		17.2947619702		111.43		1.41041		1410.41				107.03312		31.9820861678		111.204		2.57806		2578.06				106.79593		52.7210633947

																						111.59		30.5334		0.0305334				107.30198		0.5728592871		112.488		1.35372		1353.72				107.70753		28.8918597742		111.684		1.00724		1007.24				107.39285		25138.2649495857		112.036		1.45741		1457.41				107.6446		28.401081159		111.969		822.685		0.822685				107.5828		17.4474805777		111.952		1.40782		1407.82				107.55512		31.9233560091		111.723		2.59563		2595.63				107.31493		53.0803680982

																						112.109		32.3002		0.0323002				107.82098		0.6060075047		113.003		1.37944		1379.44				108.22253		29.440790597		112.201		1.01584		1015.84				107.90985		25352.9000698812		112.553		1.45881		1458.81				108.1616		28.4283634705		112.487		829.113		0.829113				108.1008		17.5838054228		112.468		1.41168		1411.68				108.07112		32.0108843537		112.238		2.62312		2623.12				107.82993		53.6425357873

																						112.624		32.4927		0.0324927				108.33598		0.609619137		113.52		1.37718		1377.18				108.73953		29.3925563956		112.719		1.02113		1021.13				108.42785		25484.9256264351		113.069		1.46215		1462.15				108.6776		28.4934512709		113.004		837.39		0.83739				108.6178		17.7593438084		112.984		1.42583		1425.83				108.58712		32.3317460317		112.753		2.59699		2596.99				108.34493		53.1081799591

																						113.14		33.3334		0.0333334				108.85198		0.6253921201		114.036		1.3813		1381.3				109.25553		29.4804877716		113.236		1.02961		1029.61				108.94485		25696.5658380753		113.586		1.47097		1470.97				109.1946		28.6653298334		113.52		842.216		0.842216				109.1338		17.861693482		113.502		1.4179		1417.9				109.10512		32.1519274376		113.269		2.61001		2610.01				108.86093		53.3744376278

																						113.655		33.0639		0.0330639				109.36698		0.6203358349		114.551		1.38065		1380.65				109.77053		29.466615103		113.751		1.03556		1035.56				109.45985		25845.0633922332		114.101		1.47388		1473.88				109.7096		28.7220380666		114.038		846.869		0.846869				109.6518		17.9603741765		114.017		1.42291		1422.91				109.62012		32.2655328798		113.784		2.61067		2610.67				109.37593		53.3879345603

																						114.176		33.8884		0.0338884				109.88798		0.635804878		115.07		1.36747		1367.47				110.28953		29.1853200702		114.27		1.0407		1040.7				109.97885		25973.345312968		114.62		1.48384		1483.84				110.2286		28.9161322257		114.557		851.801		0.851801				110.1708		18.0649718952		114.534		1.4389		1438.9				110.13712		32.6281179138		114.303		2.6287		2628.7				109.89493		53.7566462168

																						114.694		34.7608		0.0347608				110.40598		0.6521726079		115.585		1.39333		1393.33				110.80453		29.7372388524		114.786		1.04584		1045.84				110.49485		26101.6272337027		115.136		1.48138		1481.38				110.7446		28.8681933069		115.076		854.183		0.854183				110.6898		18.1154892849		115.05		1.43664		1436.64				110.65312		32.5768707483		114.819		2.65012		2650.12				110.41093		54.1946830266

																						115.209		34.9122		0.0349122				110.92098		0.6550131332		116.102		1.39213		1392.13				111.32153		29.711627772		115.302		1.05398		1053.98				111.01085		26304.7818708196		115.652		1.4966		1496.6				111.2606		29.1647910078		115.594		860.085		0.860085				111.2078		18.2406587366		115.565		1.43697		1436.97				111.16812		32.5843537415		115.334		2.60685		2606.85				110.92593		53.3098159509

																						115.726		34.9211		0.0349211				111.43798		0.6551801126		116.618		1.40577		1405.77				111.83753		30.0027403856		115.819		1.05926		1059.26				111.52785		26436.5578516522		116.17		1.49975		1499.75				111.7786		29.2261762087		116.111		863.353		0.863353				111.7248		18.3099663896		116.08		1.4416		1441.6				111.68312		32.6893424036		115.851		2.63783		2637.83				111.44293		53.9433537832

																						116.242		35.3567		0.0353567				111.95398		0.6633527205		117.136		1.39769		1397.69				112.35553		29.8302924444		116.334		1.06425		1064.25				112.04285		26561.0961365678		116.686		1.49971		1499.71				112.2946		29.225396714		116.626		868.337		0.868337				112.2398		18.4156669229		116.597		1.43715		1437.15				112.20012		32.5884353741		116.365		2.63589		2635.89				111.95693		53.9036809816

																						116.763		35.974		0.035974				112.47498		0.674934334		117.653		1.40187		1401.87				112.87253		29.9195043744		116.853		1.06871		1068.71				112.56185		26672.406908256		117.206		1.50068		1500.68				112.8146		29.2442994584		117.144		876.184		0.876184				112.7578		18.5820858804		117.116		1.44742		1447.42				112.71912		32.8213151927		116.882		2.64626		2646.26				112.47393		54.1157464213

																						117.28		36.9903		0.0369903				112.99198		0.6940018762		118.169		1.41492		1414.92				113.38853		30.1980248735		117.368		1.07524		1075.24				113.07685		26835.3798542478		117.722		1.50749		1507.49				113.3306		29.3770084166		117.66		881.005		0.881005				113.2738		18.6843295142		117.633		1.45433		1454.33				113.23612		32.9780045351		117.398		2.6477		2647.7				112.98993		54.145194274

																						117.799		37.3261		0.0373261				113.51098		0.7003020638		118.684		1.41006		1410.06				113.90353		30.094299998		117.883		1.07762		1077.62				113.59185		26894.778875911		118.239		1.50362		1503.62				113.8476		29.3015923126		118.178		884.343		0.884343				113.7918		18.7551217253		118.149		1.45961		1459.61				113.75212		33.0977324263		117.912		2.67555		2675.55				113.50393		54.7147239264

																						118.315		38.1163		0.0381163				114.02698		0.7151275797		119.201		1.41605		1416.05				114.42053		30.2221419742		118.398		1.0803		1080.3				114.10685		26961.6651692123		118.754		1.51212		1512.12				114.3626		29.4672349182		118.694		885.112		0.885112				114.3078		18.7714306559		118.666		1.4588		1458.8				114.26912		33.0793650794		118.429		2.69169		2691.69				114.02093		55.0447852761

																						118.834		37.7857		0.0377857				114.54598		0.7089249531		119.718		1.42398		1423.98				114.93753		30.3913885303		118.915		1.09012		1090.12				114.62385		27206.7485275032		119.269		1.50071		1500.71				114.8776		29.2448840794		119.211		888.939		0.888939				114.8248		18.8525935653		119.183		1.40233		1402.33				114.78612		31.7988662132		118.943		2.66505		2665.05				114.53493		54.5

																						119.354		38.5586		0.0385586				115.06598		0.7234258912		120.237		1.43142		1431.42				115.45653		30.5501772287		119.435		1.09137		1091.37				115.14385		27237.9454926625		119.789		1.51046		1510.46				115.3976		29.4348858917		119.73		892.049		0.892049				115.3438		18.9185503588		119.703		1.45957		1459.57				115.30612		33.0968253968		119.463		2.67738		2677.38				115.05493		54.7521472393

																						119.873		39.331		0.039331				115.58498		0.7379174484		120.756		1.43576		1435.76				115.97553		30.6428039694		119.953		1.09485		1094.85				115.66185		27324.7978436658		120.304		1.50903		1509.03				115.9126		29.4070189593		120.246		895.156		0.895156				115.8598		18.9844435283		120.218		1.46936		1469.36				115.82112		33.3188208617		119.979		2.68412		2684.12				115.57093		54.8899795501

																						120.391		38.1976		0.0381976				116.10298		0.7166529081		121.274		1.43446		1434.46				116.49353		30.6150586323		120.469		1.09641		1096.41				116.17785		27363.7316561845		120.819		1.53092		1530.92				116.4276		29.8335973871		120.763		900.935		0.900935				116.3768		19.1070043994		120.733		1.44559		1445.59				116.33612		32.7798185941		120.495		2.69782		2697.82				116.08693		55.1701431493

																						120.909		39.4338		0.0394338				116.62098		0.7398461538		121.789		1.44347		1443.47				117.00853		30.8073551608		120.986		1.10266		1102.66				116.69485		27519.7164819806		121.336		1.53797		1537.97				116.9446		29.970983313		121.28		901.334		0.901334				116.8938		19.1154663803		121.25		1.46953		1469.53				116.85312		33.322675737		121.009		2.69981		2699.81				116.60093		55.2108384458

																						121.428		40.034		0.040034				117.13998		0.7511069418		122.306		1.45723		1457.23				117.52553		31.1010288825		121.5		1.1068		1106.8				117.20885		27623.040830588		121.851		1.52513		1525.13				117.4596		29.7207655417		121.799		903.484		0.903484				117.4128		19.1610635204		121.767		1.47555		1475.55				117.37012		33.4591836735		121.526		2.67595		2675.95				117.11793		54.7229038855

																						121.948		40.2066		0.0402066				117.65998		0.7543452158		122.826		1.44399		1443.99				118.04553		30.8184532956		122.019		1.10899		1108.99				117.72785		27677.697913547		122.372		1.54911		1549.11				117.9806		30.1880725632		122.32		911.667		0.911667				117.9338		19.3346083566		122.289		1.47474		1474.74				117.89212		33.4408163265		122.045		2.67613		2676.13				117.63693		54.7265848671

																						122.464		41.1115		0.0411115				118.17598		0.7713227017		123.344		1.459		1459				118.56353		31.138805226		122.536		1.11526		1115.26				118.24485		27834.1818907857		122.887		1.53642		1536.42				118.4956		29.9407778967		122.838		913.008		0.913008				118.4518		19.3630482473		122.805		1.47491		1474.91				118.40812		33.4446712018		122.562		2.68653		2686.53				118.15393		54.9392638037

																						122.98		40.5824		0.0405824				118.69198		0.7613958724		123.858		1.44391		1443.91				119.07753		30.8167458903		123.053		1.11459		1114.59				118.76185		27817.4603174603		123.404		1.59656		1596.56				119.0126		31.1127480498		123.354		915.739		0.915739				118.9678		19.4209672193		123.321		1.48407		1484.07				118.92412		33.6523809524		123.077		2.70819		2708.19				118.66893		55.382208589

																						123.494		41.9113		0.0419113				119.20598		0.7863283302		124.374		1.46522		1465.22				119.59353		31.2715559927		123.568		1.11916		1119.16				119.27685		27931.5164220825		123.923		1.6035		1603.5				119.5316		31.2479903654		123.871		922.714		0.922714				119.4848		19.5688928251		123.837		1.47826		1478.26				119.44012		33.5206349206		123.592		2.72183		2721.83				119.18393		55.6611451943

																						124.009		42.4756		0.0424756				119.72098		0.7969155722		124.891		1.455		1455				120.11053		31.0534349581		124.086		1.12453		1124.53				119.79485		28065.5385844065		124.44		1.61903		1619.03				120.0486		31.5506291496		124.388		924.177		0.924177				120.0018		19.5999200884		124.353		1.49027		1490.27				119.95612		33.7929705215		124.108		2.73961		2739.61				119.69993		56.0247443763

																						124.528		42.9773		0.0429773				120.23998		0.8063283302		125.412		1.45821		1458.21				120.63153		31.1219445981		124.604		1.12512		1125.12				120.31285		28080.2635519617		124.961		1.69466		1694.66				120.5696		33.0244585923		124.908		927.69		0.92769				120.5218		19.6744236946		124.874		1.4814		1481.4				120.47712		33.5918367347		124.626		2.72038		2720.38				120.21793		55.6314928425

																						125.045		43.04		0.04304				120.75698		0.8075046904		125.929		1.48048		1480.48				121.14853		31.5972435648		125.12		1.12819		1128.19				120.82885		28156.8832983927		125.478		1.71777		1717.77				121.0866		33.4748116059		125.426		928.908		0.928908				121.0398		19.7002550047		125.393		1.47525		1475.25				120.99612		33.4523809524		125.143		2.68421		2684.21				120.73493		54.8918200409

																						125.562		43.7465		0.0437465				121.27398		0.8207598499		126.446		1.46256		1462.56				121.66553		31.2147847645		125.635		1.13443		1134.43				121.34385		28312.6185484676		125.993		1.75322		1753.22				121.6016		34.1656387081		125.946		930.339		0.930339				121.5598		19.7306036128		125.911		1.4871		1487.1				121.51412		33.7210884354		125.659		2.76186		2761.86				121.25093		56.4797546012

																						126.08		43.9405		0.0439405				121.79198		0.8243996248		126.962		1.47155		1471.55				122.18153		31.4066544416		126.152		1.13393		1133.93				121.86085		28300.1397624039		126.509		1.77114		1771.14				122.1176		34.5148522955		126.462		930.696		0.930696				122.0758		19.7381748589		126.428		1.49165		1491.65				122.03112		33.8242630385		126.174		2.6808		2680.8				121.76593		54.8220858896

																						126.596		43.8085		0.0438085				122.30798		0.8219230769		127.477		1.48583		1485.83				122.69653		31.7114262981		126.666		1.13859		1138.59				122.37485		28416.4420485175		127.025		1.76923		1769.23				122.6336		34.4776314277		126.979		934.695		0.934695				122.5928		19.8229855396		126.943		1.47765		1477.65				122.54612		33.5068027211		126.69		2.73631		2736.31				122.28193		55.9572597137

																						127.116		45.1326		0.0451326				122.82798		0.8467654784		127.997		1.47543		1475.43				123.21653		31.4894636015		127.184		1.14029		1140.29				122.89285		28458.8699211341		127.546		1.77017		1770.17				123.1546		34.4959495511		127.501		936.238		0.936238				123.1148		19.8557094406		127.461		1.49972		1499.72				123.06412		34.0072562358		127.21		2.7379		2737.9				122.80193		55.9897750511

																						127.631		45.5357		0.0455357				123.34298		0.8543283302		128.515		1.48669		1486.69				123.73453		31.7297809057		127.702		1.14258		1142.58				123.41085		28516.0227613058		128.064		1.76895		1768.95				123.6726		34.4721749654		128.019		940.683		0.940683				123.6328		19.9499788769		127.978		1.49892		1498.92				123.58112		33.9891156463		127.725		2.75284		2752.84				123.31693		56.2952965235

																						128.147		46.4376		0.0464376				123.85898		0.871249531		129.03		1.47604		1476.04				124.24953		31.5024825674		128.216		1.14831		1148.31				123.92485		28659.0296495957		128.581		1.8501		1850.1				124.1896		36.0535746649		128.536		940.607		0.940607				124.1498		19.948367071		128.495		1.49774		1497.74				124.09812		33.9623582766		128.238		2.78061		2780.61				123.82993		56.863190184

																						128.663		46.655		0.046655				124.37498		0.8753283302		129.548		1.48318		1483.18				124.76753		31.6548684956		128.734		1.15026		1150.26				124.44285		28707.6969152441		129.098		1.80122		1801.22				124.7066		35.1010322457		129.053		944.553		0.944553				124.6668		20.0320537291		129.011		1.50551		1505.51				124.61412		34.1385487528		128.754		2.78663		2786.63				124.34593		56.9862985685

																						129.18		46.89		0.04689				124.89198		0.8797373358		130.065		1.50057		1500.57				125.28453		32.0260157354		129.249		1.15679		1156.79				124.95785		28870.6698612359		129.615		1.87535		1875.35				125.2236		36.5456306404		129.57		948.086		0.948086				125.1838		20.1069814948		129.528		1.50138		1501.38				125.13112		34.0448979592		129.269		2.75209		2752.09				124.86093		56.2799591002
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		pH 6.8								445.54																GLP				17B-26005								GLP-PVP 1:1				17B-28001								GLP-PVP 1:2				17B-27003								GLP-PEOX 5K 1:2				17B-27005								GLP-PEOX 50K 1:2				17B-28009

						Sector		File		mg final		mg initial		Assay		GLP initial wieght		% Dissolve

						GLP		17B-26005		0.051		5.04		1.00		5.04		1.01

						GLP-PVP 1:1		17B-28001		1.104		10.56		0.44		4.69		23.56				Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile												Dissolution Profile

						GLP-PVP 1:2		17B-27003		2.839		14.64		0.28		4.10		69.25

						GLP-PEOX 5K 1:2		17B-27005		1.081		15.9		0.31		4.90		22.06				Time (minutes)		Weight (µg)		Weight (µg)		Weight (mg)		Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (mg)		Weight (mg)				Time zero (min)		%		Time (minutes)		Weight (µg)		Weight (µg)		Weight (mg)		Time zero (min)		%

						GLP-PEOX 50K 1:2		17B-28009		0.452		15.03		0.30		4.58		9.88				5.03593		16.9765		18.8308		0.0169765		0		0.3368353175		5.3948		0.0752367		0.0638378				0		1.6057443092		5.06797		0.497706		0.503458				0		12.1415398126		5.04375		0.150816		0.142544				0		3.077638877		5.05522		15.7231		-5.58648		0.0157231		0		0.3434387517

																						5.55182		18.1418		19.4427		0.0181418		0.51589		0.3599563492		5.9151		0.0975581		0.0933033				0.5203		2.0821402838		5.58777		0.58089		0.584812				0.5198		14.1708138173		5.56172		0.182355		0.174936				0.51797		3.7212420261		5.57318		23.3344		3.99792		0.0233344		0.51796		0.5096919315

																						6.07135		19.4759		20.0566		0.0194759		1.03542		0.3864265873		6.43022		0.123665		0.12201				1.03542		2.6393285458		6.10443		0.662257		0.663887				1.03646		16.1557620999		6.08152		0.211867		0.20639				1.03777		4.3234810362		6.08932		25.0931		13.5095		0.0250931		1.0341		0.5481071125

																						6.58647		20.2703		20.6631		0.0202703		1.55054		0.4021884921		6.94765		0.150762		0.150386				1.55285		3.2176480833		6.6224		0.754497		0.741411				1.55443		18.40595726		6.6		0.238921		0.236749				1.55625		4.8755606708		6.6039		30.6364		22.9541		0.0306364		1.54868		0.6691890895

																						7.10287		21.0371		21.2689		0.0210371		2.06694		0.4174027778		7.46615		0.175434		0.178367				2.07135		3.7442118958		7.14245		0.823165		0.817522				2.07448		20.081113388		7.11875		0.265544		0.26614				2.075		5.4188450692		7.12188		40.5981		32.4224		0.0405981		2.06666		0.8867819188

																						7.61953		21.5162		21.8728		0.0215162		2.5836		0.4269087302		7.98385		0.202423		0.205858				2.58905		4.3202264361		7.65912		0.892934		0.891465				2.59115		21.7831284153		7.63568		0.29073		0.294483				2.59193		5.932805211		7.63985		41.6008		41.8518		0.0416008		2.58463		0.9086838361

																						8.13515		22.1003		22.4733		0.0221003		3.09922		0.4384980159		8.50208		0.231934		0.232938				3.10728		4.9500669303		8.17708		0.961144		0.963958				3.10911		23.4471116315		8.15313		0.316097		0.321938				3.10938		6.450458944		8.1573		46.5516		51.2335		0.0465516		3.10208		1.0168238703

																						8.64973		22.8796		23.0704		0.0228796		3.6138		0.4539603175		9.01718		0.258635		0.259426				3.62238		5.5199348113		8.69375		1.03117		1.03467				3.62578		25.1553961749		8.67213		0.343456		0.348584				3.62838		7.0087625858		8.67343		55.138		60.5532		0.055138		3.61821		1.2043761022

																						9.16667		23.8191		23.6681		0.0238191		4.13074		0.4726011905		9.5336		0.28532		0.285559				4.1388		6.0894612112		9.21407		1.10138		1.10431				4.1461		26.8681693989		9.19063		0.367946		0.374344				4.14688		7.5085197474		9.18802		62.0578		69.8072		0.0620578		4.1328		1.3555248881

																						9.68307		24.3262		24.263		0.0243262		4.64714		0.4826626984		10.0503		0.310869		0.311288				4.6555		6.634742455		9.73542		1.16079		1.17253				4.66745		28.3174765808		9.71198		0.388906		0.399405				4.66823		7.9362416792		9.70598		76.0526		79.0842		0.0760526		4.65076		1.6612124842

																						10.2011		24.9532		24.8576		0.0249532		5.16517		0.4951031746		10.5688		0.335287		0.336696				5.174		7.1558852555		10.2539		1.23333		1.23888				5.18593		30.0870901639		10.23		0.412058		0.423496				5.18625		8.4086948359		10.2216		75.4554		88.2818		0.0754554		5.16638		1.6481678796

																						10.7206		26.4499		25.4517		0.0264499		5.68467		0.5247996032		11.0867		0.358285		0.361673				5.6919		7.646721611		10.7732		1.29929		1.30385				5.70523		31.6961846214		10.7477		0.434915		0.446797				5.70395		8.8751280513		10.7372		90.317		97.4418		0.090317		5.68198		1.9727889373

																						11.2357		26.3681		26.0387		0.0263681		6.19977		0.5231765873		11.6042		0.382489		0.386226				6.2094		8.1632971022		11.2906		1.36615		1.36716				6.22263		33.3272345824		11.2675		0.461879		0.469435				6.22375		9.4253710937		11.2547		101.031		106.597		0.101031		6.19948		2.2068142114

																						11.7529		27.0566		26.6259		0.0270566		6.71697		0.5368373016		12.1224		0.405062		0.410424				6.7276		8.6450628667		11.8099		1.43107		1.42929				6.74193		34.9109582358		11.7844		0.485478		0.491221				6.74065		9.9069459919		11.7721		109.943		115.715		0.109943		6.71688		2.401478505

																						12.2698		27.7016		27.2106		0.0277016		7.23387		0.5496349206		12.6396		0.42892		0.434188				7.2448		9.1542538297		12.3297		1.49093		1.49011				7.26173		36.3712431694		12.3011		0.510197		0.512293				7.25735		10.4113762606		12.2901		112.394		124.805		0.112394		7.23488		2.4550155544

																						12.7857		28.3975		27.7921		0.0283975		7.74977		0.5634424603		13.157		0.449412		0.457585				7.7622		9.5916057123		12.8487		1.55216		1.54948				7.78073		37.8649492584		12.819		0.534113		0.532736				7.77525		10.899420045		12.8063		122.738		133.826		0.122738		7.75108		2.6809589401

																						13.3018		28.6851		28.3718		0.0286851		8.26587		0.5691488095		13.6745		0.474291		0.480608				8.2797		10.1225874362		13.3659		1.61014		1.60734				8.29793		39.2793715847		13.3372		0.557033		0.552528				8.29345		11.3671388749		13.3237		133.257		142.833		0.133257		8.26848		2.9107248405

																						13.8164		29.3547		28.9476		0.0293547		8.78047		0.5824345238		14.1925		0.488082		0.503287				8.7977		10.4169227775		13.8813		1.66737		1.66372				8.81333		40.6754976581		13.8544		0.580051		0.571643				8.81065		11.8368575498		13.8412		138.477		151.803		0.138477		8.78598		3.0247449946

																						14.3323		29.8696		29.5228		0.0298696		9.29637		0.5926507937		14.7094		0.522498		0.525559				9.3146		11.1514485627		14.399		1.72512		1.71912				9.33103		42.0843091335		14.3716		0.5999		0.59014				9.32785		12.2419077704		14.3557		148.2		160.688		0.1482		9.30048		3.2371239137

																						14.8484		29.7455		30.0961		0.0297455		9.81247		0.5901884921		15.2273		0.546691		0.547519				9.8325		11.6677892857		14.9156		1.78359		1.77318				9.84763		43.5106850117		14.8906		0.616998		0.608103				9.84685		12.5908194875		14.8708		158.434		169.545		0.158434		9.81558		3.4606645759

																						15.3643		30.9932		30.6672		0.0309932		10.32837		0.6149444444		15.743		0.569347		0.569032				10.3482		12.1513264832		15.4323		1.82913		1.82604				10.36433		44.6216334895		15.4083		0.636939		0.625441				10.36455		12.9977471135		15.3893		167.676		178.424		0.167676		10.33408		3.6625370402

																						15.8797		32.0944		31.2355		0.0320944		10.84377		0.6367936508		16.2599		0.591051		0.590256				10.8651		12.614545557		15.9477		1.88082		1.87762				10.87973		45.8826112412		15.9245		0.651997		0.64217				10.88075		13.3050294059		15.9073		178.007		187.258		0.178007		10.85208		3.8881964676

																						16.3974		32.7752		31.8044		0.0327752		11.36147		0.6503015873		16.7772		0.616072		0.611156				11.3824		13.1485579254		16.4669		1.92448		1.92843				11.39893		46.9476971116		16.4412		0.664902		0.658376				11.39745		13.56837633		16.4274		186.566		196.092		0.186566		11.37218		4.075150203

																						16.9147		33.2121		32.3708		0.0332121		11.87877		0.6589702381		17.2945		0.639942		0.631724				11.8997		13.6580049993		16.986		1.97055		1.9781				11.91803		48.0715749415		16.9588		0.68323		0.674089				11.91505		13.9423881413		16.943		198.199		204.815		0.198199		11.88778		4.3292491402

																						17.432		34.9248		32.9351		0.0349248		12.39607		0.692952381		17.8125		0.6578		0.651991				12.4177		14.0391405604		17.5032		2.02104		2.0265				12.43523		49.3032786885		17.4753		0.695378		0.689261				12.43155		14.1902872838		17.4583		209.475		213.497		0.209475		12.40308		4.5755501472

																						17.9492		34.3838		33.4973		0.0343838		12.91327		0.682218254		18.33		0.681819		0.671915				12.9352		14.5517676768		18.0195		2.0552		2.07375				12.95153		50.1366120219		17.9925		0.706769		0.703963				12.94875		14.4227386448		17.973		218.905		222.133		0.218905		12.91778		4.7815290845

																						18.4685		36.8173		34.0597		0.0368173		13.43257		0.7305019841		18.8497		0.701548		0.691602				13.4549		14.9728351807		18.5372		2.10525		2.12008				13.46923		51.3575819672		18.5102		0.718681		0.718204				13.46645		14.6658218342		18.4897		232.477		230.767		0.232477		13.43448		5.077981485

																						18.986		35.5922		34.6181		0.0355922		13.95007		0.7061944444		19.3682		0.722368		0.71093				13.9734		15.4171874253		19.0552		2.14665		2.16541				13.98723		52.3675351288		19.0255		0.732165		0.731924				13.98175		14.9409841686		19.0047		236.158		239.339		0.236158		13.94948		5.1583853523

																						19.5037		36.1002		35.1746		0.0361002		14.46777		0.7162738095		19.8855		0.735611		0.729907				14.4907		15.6998270398		19.5732		2.18117		2.20974				14.50523		53.2096506635		19.5435		0.742912		0.74527				14.49975		15.1602936915		19.5217		245		247.908		0.245		14.46648		5.3515206401

																						20.023		34.7127		35.7309		0.0347127		14.98707		0.6887440476		20.4008		0.753826		0.74851				15.006		16.0885818974		20.0912		2.21079		2.25309				15.02323		53.9322306792		20.0598		0.752879		0.758144				15.01605		15.3636860815		20.0383		254.771		256.438		0.254771		14.98308		5.5649480204

																						20.5413		36.0353		36.2841		0.0360353		15.50537		0.7149861111		20.9188		0.771754		0.766912				15.524		16.4712114382		20.6073		2.26241		2.29533				15.53933		55.1915007806		20.5742		0.766681		0.770556				15.53045		15.6453377085		20.5542		280.516		264.919		0.280516		15.49898		6.1272945464

																						21.0575		36.4163		36.833		0.0364163		16.02157		0.7225456349		21.4365		0.791893		0.785007				16.0417		16.9010293947		21.123		2.2968		2.33661				16.05503		56.0304449649		21.0902		0.771072		0.782608				16.04645		15.7349430044		21.0703		283.634		273.371		0.283634		16.01508		6.1954008376

																						21.5745		37.2294		37.3808		0.0372294		16.53857		0.7386785714		21.9532		0.798838		0.80278				16.5584		17.0492535224		21.6412		2.32186		2.37717				16.57323		56.6417837627		21.6078		0.785353		0.794308				16.56405		16.0263693836		21.5878		293.083		281.81		0.293083		16.53258		6.4017947908

																						22.0897		37.4758		37.9247		0.0374758		17.05377		0.7435674603		22.4703		0.823151		0.820287				17.0755		17.5681553534		22.1587		2.36691		2.41678				17.09073		57.7407786885		22.123		0.798027		0.805577				17.07925		16.2850023876		22.1023		305.659		290.167		0.305659		17.04708		6.6764916217

																						22.6075		38.1955		38.4694		0.0381955		17.57157		0.7578472222		22.986		0.840244		0.837464				17.5912		17.9329638508		22.6765		2.39332		2.45554				17.60853		58.3850507416		22.6375		0.807456		0.81647				17.59375		16.4774160371		22.6185		312.042		298.516		0.312042		17.56328		6.8159151166

																						23.1253		38.6358		39.0121		0.0386358		18.08937		0.7665833333		23.5033		0.856105		0.854423				18.1085		18.2714783057		23.1932		2.42977		2.49336				18.12523		59.2742486339		23.1555		0.823038		0.827084				18.11175		16.7953913778		23.138		323.734		306.885		0.323734		18.08278		7.0713027873

																						23.6448		38.9901		39.5546		0.0389901		18.60887		0.7736130952		24.0227		0.863101		0.871176				18.6279		18.4207909043		23.7088		2.45172		2.53027				18.64083		59.8097189696		23.6763		0.834966		0.83741				18.63255		17.0388010726		23.6545		334.705		315.172		0.334705		18.59928		7.3109416973

																						24.1622		39.1708		40.0929		0.0391708		19.12627		0.7771984127		24.5388		0.875819		0.88756				19.144		18.6922256712		24.2268		2.47216		2.56653				19.15883		60.3083528493		24.1945		0.850699		0.84735				19.15075		17.3598578069		24.173		333.368		323.457		0.333368		19.11778		7.2817376846

																						24.6782		39.8796		40.6278		0.0398796		19.64227		0.7912619048		25.0563		0.889955		0.903725				19.6615		18.993924198		24.7472		2.51493		2.60215				19.67923		61.3517271663		24.7107		0.866328		0.856933				19.66695		17.6787922569		24.6908		345.811		331.698		0.345811		19.63558		7.5535294043

																						25.1943		40.8701		41.1609		0.0408701		20.15837		0.8109146825		25.5737		0.901985		0.919627				20.1789		19.2506752788		25.2628		2.55669		2.63667				20.19483		62.3704625293		25.2283		0.880572		0.866233				20.18455		17.9694635926		25.206		357.547		339.863		0.357547		20.15078		7.8098781644

																						25.7115		41.3604		41.6932		0.0413604		20.67557		0.8206428571		26.0893		0.912176		0.935225				20.6945		19.4681773789		25.7782		2.59455		2.67041				20.71023		63.294057377		25.7448		0.89562		0.875213				20.70105		18.2765418192		25.72		360.535		347.977		0.360535		20.66478		7.8751448733

																						26.2292		41.5201		42.224		0.0415201		21.19327		0.8238115079		26.6063		0.926105		0.950615				21.2115		19.7654579944		26.2963		2.63613		2.70359				21.22833		64.3084016393		26.2638		0.910885		0.883945				21.22005		18.5880482738		26.2347		365.073		356.068		0.365073		21.17948		7.9742681413

																						26.7448		42.5724		42.7509		0.0425724		21.70887		0.8446904762		27.1218		0.933686		0.965715				21.727		19.9272559947		26.8138		2.67074		2.73599				21.74583		65.1527127244		26.7807		0.924671		0.892359				21.73695		18.8693733955		26.7505		373.487		364.144		0.373487		21.69528		8.1580546502

																						27.2625		43.3161		43.2778		0.0433161		22.22657		0.8594464286		27.638		0.944033		0.980595				22.2432		20.1480875353		27.333		2.71121		2.76777				22.26503		66.1399785324		27.2962		0.940076		0.900482				22.25245		19.1837367714		27.2663		369.439		372.188		0.369439		22.21108		8.0696344234

																						27.7782		44.6235		43.8009		0.0446235		22.74227		0.8853869048		28.1545		0.9592		0.995248				22.7597		20.4717902487		27.8482		2.72971		2.79862				22.78023		66.5912861046		27.8115		0.953207		0.90834				22.76775		19.4516955828		27.781		374.755		380.181		0.374755		22.72578		8.1857514998

																						28.2977		44.1005		44.3259		0.0441005		23.26177		0.8750099206		28.6722		0.967124		1.0097				23.2774		20.6409087494		28.3653		2.7593		2.8289				23.29733		67.3131342701		28.3297		0.961688		0.915988				23.28595		19.6247637938		28.2982		388.397		388.18		0.388397		23.24298		8.4837329063

																						28.8128		44.2909		44.8446		0.0442909		23.77687		0.8787876984		29.1872		0.978771		1.02385				23.7924		20.8894856271		28.8842		2.7835		2.85861				23.81623		67.9034933646		28.8482		0.974933		0.923392				23.80445		19.8950489554		28.8122		400.056		396.098		0.400056		23.75698		8.7383997599

																						29.3295		44.9015		45.363		0.0449015		24.29357		0.8909027778		29.7042		0.989318		1.03782				24.3094		21.114585681		29.4063		2.80153		2.88784				24.33833		68.3433352849		29.364		0.993014		0.930521				24.32025		20.2640203413		29.3283		397.145		404.017		0.397145		24.27308		8.6748149575

																						29.8458		45.997		45.8791		0.045997		24.80987		0.9126388889		30.2198		0.999584		1.05154				24.825		21.3336884736		29.9227		2.82509		2.91611				24.85473		68.9180815769		29.881		1.00158		0.937436				24.83725		20.4388231117		29.844		409.035		411.896		0.409035		24.78878		8.9345275306

																						30.3643		46.1679		46.3956		0.0461679		25.32837		0.9160297619		30.7375		1.01098		1.0651				25.3427		21.576908367		30.4422		2.83102		2.94392				25.37423		69.06274395		30.3997		1.00879		0.944148				25.35595		20.5859545586		30.3592		413.745		419.736		0.413745		25.30398		9.0374077846

																						30.8828		45.7385		46.9101		0.0457385		25.84687		0.9075099206		31.2547		1.02231		1.07842				25.8599		21.8187196509		30.958		2.83551		2.97093				25.89003		69.1722775176		30.9177		1.00873		0.950636				25.87395		20.5847301638		30.8747		418.075		427.549		0.418075		25.81948		9.1319877208

																						31.401		47.1791		47.4225		0.0471791		26.36507		0.936093254		31.7727		1.03345		1.09155				26.3779		22.056475847		31.4777		2.84764		2.99753				26.40973		69.4681889149		31.4343		1.02957		0.956898				26.39055		21.0100033059		31.3898		423.88		435.325		0.42388		26.33458		9.2587859955

																						31.9188		47.4079		47.9326		0.0474079		26.88287		0.9406329365		32.2912		1.04321		1.10449				26.8964		22.2647793008		31.9948		2.84469		3.02342				26.92683		69.3962236534		31.9523		1.04001		0.962973				26.90855		21.2230480085		31.9057		428.818		443.08		0.428818		26.85048		9.3666464401

																						32.4342		48.2616		48.4385		0.0482616		27.39827		0.9575714286		32.8087		1.05196		1.11719				27.4139		22.4515267619		32.5117		2.83957		3.04873				27.44373		69.2713212334		32.4717		1.05789		0.968867				27.42795		21.5879176717		32.42		434.307		450.781		0.434307		27.36478		9.4865423454

																						32.9487		48.4023		48.9417		0.0484023		27.91277		0.9603630952		33.326		1.06965		1.12969				27.9312		22.8290767718		33.0283		2.85004		3.07346				27.96033		69.5267369243		32.9872		1.06039		0.974529				27.94345		21.6389341235		32.9357		448.226		458.47		0.448226		27.88048		9.7905742466

																						33.4667		49.4119		49.4465		0.0494119		28.43077		0.9803948413		33.8413		1.07645		1.14194				28.4465		22.9742062272		33.544		2.84638		3.09761				28.47603		69.43745121		33.5047		1.06723		0.980029				28.46095		21.7785151356		33.4513		446.66		466.128		0.44666		28.39608		9.7563682003

																						33.9837		50.0193		49.9485		0.0500193		28.94777		0.9924464286		34.3568		1.08558		1.154				28.962		23.1690638638		34.0622		2.8491		3.12134				28.99423		69.5038056206		34.0217		1.07275		0.985347				28.97795		21.8911594611		33.9663		446.711		473.746		0.446711		28.91108		9.7574821904

																						34.5057		50.8666		50.4535		0.0508666		29.46977		1.0092579365		34.875		1.09688		1.16593				29.4802		23.4102348707		34.5787		2.84417		3.14447				29.51073		69.3835382514		34.5393		1.07807		0.990499				29.49555		21.9997224705		34.4838		450.291		481.369		0.450291		29.42858		9.8356799205

																						35.0217		51.1525		50.9509		0.0511525		29.98577		1.0149305556		35.3927		1.10384		1.17765				29.9979		23.5587791369		35.0932		2.83878		3.167				30.02523		69.2520491803		35.0583		1.08103		0.995498				30.01455		22.0601259494		34.999		452.363		488.927		0.452363		29.94378		9.8809384951

																																														39.5903		132.744		0.132744				34.52233		3.2382903981

																																														40.106		132.593		0.132593				35.03803		3.2346067525

																																														40.6235		131.009		0.131009				35.55553		3.1959650664

																																														41.1397		131		0.131				36.07173		3.1957455113

																																														41.6565		129.984		0.129984				36.58853		3.1709601874

																																														42.1718		129.517		0.129517				37.10383		3.1595677205

																																														42.6878		129.123		0.129123				37.61983		3.149956089

																																														43.2033		128.535		0.128535				38.13533		3.1356118267

																																														43.7208		128.383		0.128383				38.65283		3.1319037861

																																														44.238		127.814		0.127814				39.17003		3.1180230289

																																														44.7557		127.19		0.12719				39.68773		3.1028005464

																																														45.269		125.746		0.125746				40.20103		3.0675741608

																																														45.783		126.541		0.126541				40.71503		3.0869681889

																																														46.2963		125.327		0.125327				41.22833		3.0573526542

																																														46.812		124.967		0.124967				41.74403		3.0485704528

																																														47.3282		125.051		0.125051				42.26023		3.0506196331

																																														47.8438		124.162		0.124162				42.77583		3.0289324746

																																														48.3587		122.62		0.12262				43.29073		2.9913153786

																																														48.873		123.144		0.123144				43.80503		3.0040983607

																																														49.3897		123.228		0.123228				44.32173		3.006147541

																																														49.9052		123.172		0.123172				44.83723		3.0047814208

																																														50.4198		122.587		0.122587				45.35183		2.9905103435

																																														50.936		122.942		0.122942				45.86803		2.9991705699

																																														51.4515		121.994		0.121994				46.38353		2.9760441062

																																														51.969		121.081		0.121081				46.90103		2.9537714676

																																														52.4837		121.263		0.121263				47.41573		2.9582113583

																																														52.9997		120.364		0.120364				47.93173		2.9362802498

																																														53.5143		120.131		0.120131				48.44633		2.9305962139

																																														54.03		120.195		0.120195				48.96203		2.9321574941

																																														54.5467		120.554		0.120554				49.47873		2.9409153005

																																														55.0607		119.053		0.119053				49.99273		2.9042983997

																																														55.5753		119.589		0.119589				50.50733		2.9173741218

																																														56.0908		119.337		0.119337				51.02283		2.9112265808

																																														56.607		118.666		0.118666				51.53903		2.8948575332

																																														57.1245		118.195		0.118195				52.05653		2.8833674863

																																														57.639		118.369		0.118369				52.57103		2.887612217

																																														58.1557		116.929		0.116929				53.08773		2.8524834114

																																														58.6708		117.227		0.117227				53.60283		2.8597531226

																																														59.186		116.864		0.116864				54.11803		2.8508977361		59.4575		0.12367						54.41375		2.5236818369

																																														59.701		117.169		0.117169				54.63303		2.8583382123		59.9742		0.123702						54.93045		2.5243348475

																																														60.2167		115.828		0.115828				55.14873		2.8256245121		60.4908		0.123968						55.44705		2.529762998

																																														60.7318		116.58		0.11658				55.66383		2.843969555		61.0115		0.124572						55.96775		2.5420885727

																																														61.2473		116.52		0.11652				56.17933		2.8425058548		61.5287		0.122788						56.48495		2.5056832327

																																														61.763		116.456		0.116456				56.69503		2.8409445746		62.0453		0.123818						57.00155		2.5267020109

																																														62.2805		115.617		0.115617				57.21253		2.8204771663		62.561		0.123064						57.51725		2.511315449

																																														62.795		115.476		0.115476				57.72703		2.8170374707		63.0755		0.123884						58.03175		2.5280488452

																																														63.3107		115.713		0.115713				58.24273		2.8228190867		63.5925		0.122194						58.54875		2.4935617238

																																														63.8253		115.429		0.115429				58.75733		2.8158909055		64.1088		0.123146						59.06505		2.5129887886

																																														64.339		114.143		0.114143				59.27103		2.7845189305		64.6242		0.122779						59.58045		2.5054995735

																																														64.856		114.929		0.114929				59.78803		2.8036934036		65.1435		0.121897						60.09975		2.4875009693

																																														65.3693		114.155		0.114155				60.30133		2.7848116706		65.6597		0.120367						60.61595		2.4562789008

																																														65.8855		113.748		0.113748				60.81753		2.774882904		66.1792		0.123927						61.13545		2.5289263282

																																														67.5093		123.109		0.123109				62.44133		3.0032445355		67.8125		0.182914						62.76875		3.7326493047

																																														68.0235		123.804		0.123804				62.95553		3.0201990632		68.3292		0.184925						63.28545		3.7736869386

																																														68.5397		124.642		0.124642				63.47173		3.0406420765		68.8453		0.187829						63.80155		3.832947649

																																														69.0552		125.849		0.125849				63.98723		3.0700868462		69.3602		0.187587						64.31645		3.8280092564

																																														69.5703		127.662		0.127662				64.50233		3.1143149883		69.876		0.188611						64.83225		3.8489055951

																																														70.0883		127.437		0.127437				65.02033		3.1088261124		70.3958		0.190496						65.35205		3.8873719997

																																														70.6028		128.506		0.128506				65.53483		3.1349043716		70.9128		0.191668						65.86905		3.9112885123

																																														71.1177		129.36		0.12936				66.04973		3.1557377049		71.4318		0.190128						66.38805		3.879862378

																																														71.6318		130.07		0.13007				66.56383		3.1730581577		71.9508		0.194051						66.90705		3.9599173942

																																														72.148		130.458		0.130458				67.08003		3.1825234192		72.4662		0.191953						67.42245		3.9171043878

																																														72.6648		130.436		0.130436				67.59683		3.1819867291		72.9833		0.192678						67.93955		3.9318991588

																																														73.181		131.282		0.131282				68.11303		3.2026249024		73.4987		0.196482						68.45495		4.0095257919

																																														73.6967		131.679		0.131679				68.62873		3.212309719		74.014		0.195365						68.97025		3.9867316412

																																														74.2117		131.919		0.131919				69.14373		3.2181645199		74.5323		0.19755						69.48855		4.0313200201

																																														74.7253		131.908		0.131908				69.65733		3.2178961749		75.0497		0.196455						70.00595		4.0089748142

																																														75.2413		133.16		0.13316				70.17333		3.2484387198		75.5688		0.194287						70.52505		3.9647333472

																																														75.757		133.497		0.133497				70.68903		3.2566598361		76.089		0.197245						71.04525		4.025096013

																																														76.2732		134.808		0.134808				71.20523		3.2886416862		76.6047		0.197408						71.56095		4.0284222856

																																														76.7888		134.326		0.134326				71.72083		3.2768832943		77.1223		0.195971						72.07855		3.9990980291

																																														77.3038		133.857		0.133857				72.23583		3.2654420375		77.638		0.196108						72.59425		4.0018937307





		



GLP

GLP-PVP 1:1

GLP-PVP 1:2

GLP-PEOX 5K 1:2

GLP-PEOX 50K 1:2

Time (min)

mg dissolved



		0		0				0				0				0

		0.51585		0.51694				0.5151				0.51563				0.5138

		1.0346		1.03255				1.02892				1.03021				1.0289

		1.55918		1.54714				1.54375				1.54375				1.54402

		2.0365066667		2.06224				2.06017				2.05755				2.05937

		2.5843		2.57839				2.58047				2.57083				2.57473

		3.09906		3.09349				3.0974				3.08698				3.08985

		3.6153866667		3.60912				3.61355				3.60051				3.60598

		4.1335166667		4.12657				4.12814				4.11641				4.12213

		4.6520466667		4.64219				4.64272				4.63176				4.63672

		5.1652666667		5.15962				5.15597				5.14613				5.1518

		5.6852666667		5.67652				5.67217				5.66173				5.6669

		6.1991666667		6.19192				6.18777				6.17583				6.182

		6.7187333333		6.70882				6.70237				6.68963				6.6982

		7.2357		7.22342				7.22087				7.20473				7.2138

		7.7528666667		7.73832				7.73697				7.71923				7.7292

		8.2708		8.25182				8.25337				8.23313				8.243

		8.7845666667		8.76802				8.76847				8.74843				8.7586

		9.3054		9.28592				9.28357				9.26383				9.2747

		9.8173333333		9.80102				9.79977				9.77833				9.7904

		10.3354		10.31592				10.31717				10.29483				10.3044

		10.8513666667		10.83172				10.83287				10.81013				10.8208

		11.3686333333		11.34712				11.34847				11.32523				11.3367

		11.8836333333		11.86142				11.86537				11.84083				11.8518

		12.3998333333		12.37472				12.37867				12.35603				12.367

		12.9161333333		12.89042				12.89667				12.87183				12.882

		13.4336666667		13.40602				13.41167				13.38723				13.3981

		13.9497333333		13.92092				13.93017				13.90423				13.9128

		14.4690666667		14.43392				14.44637				14.41983				14.429

		15.0166666667		14.94792				14.96117				14.93483				14.9458

		15.4958666667		15.46402				15.47607				15.45103				15.462

		16.0171		15.97742				15.99167				15.96853				15.9786

		16.535		16.49302				16.51207				16.48303				16.4948

		17.0479666667		17.00852				17.03117				16.99833				17.0096

		17.567		17.52342				17.54737				17.51433				17.5258

		18.0826		18.03772				18.06667				18.02933				18.0415

		18.6003333333		18.55392				18.58237				18.54273				18.5565

		19.119		19.06952				19.10137				19.06023				19.0735

		19.6316333333		19.58472				19.61487				19.57583				19.5885

		20.1481		20.10492				20.13157				20.09183				20.1046

		20.6671666667		20.61902				20.64737				20.60703				20.6198

		21.1828		21.13392				21.16407				21.12173				21.1378

		21.6996		21.64792				21.67967				21.63623				21.6523

		22.2176666667		22.16172				22.19607				22.15203				22.168

		22.7326333333		22.67922				22.71267				22.66503				22.6841

		23.2508333333		23.19422				23.22737				23.18123				23.1993

		23.7688666667		23.71222				23.74537				23.69583				23.7133

		24.2827333333		24.23122				24.26157				24.21033				24.23

		24.8003666667		24.74772				24.77657				24.72523				24.7451

		25.3187666667		25.26392				25.29067				25.24033				25.2606

		25.8333666667		25.78172				25.81017				25.75383				25.7776

		26.3504333333		26.30152				26.32817				26.27003				26.2938

		26.8676666667		26.82142				26.84537				26.78573				26.8091

		27.3843		27.33992				27.36257				27.30133				27.3235

		27.8990666667		27.85722				27.88107				27.81923				27.8396

		28.4225666667		28.37452				28.39457				28.33483				28.3541

		28.9345666667		28.89272				28.91117				28.85053				28.8703

		29.4535		29.40792				29.42867				29.36503				29.3855

		29.9704		29.92292				29.94367				29.88023				29.9005



GLP

GLP-PVP 1:1 PM

GLP-PVP 1:1

GLP-PVP 1:2 PM

GLP-PVP 1:2

GLP-PEOX 5K 1:2 PM

GLP-PEOX 5K 1:2

GLP-PEOX 50K 1:2 PM

GLP-PEOX 50K 1:2

Time (min)

mg Dissolved

0.0143071

0.00955478

0.0103427

0.0107029

0.0194524

0.0125881

0.015379

0.0141699

0.0246502

0.0142018

0.0155472

0.0154066

0.0265817

0.0160661

0.0168696

0.0171354

0.030794

0.0199472

0.0187964

0.0188642

0.0338099

0.0211897

0.018954

0.0199355

0.0372978

0.0226409

0.0203526

0.0230872

0.0396589

0.0255881

0.0234404

0.0240098

0.0436288

0.0272877

0.0247595

0.0251984

0.0441048

0.0313552

0.0268357

0.0275043

0.0494215

0.0328689

0.027971

0.0256317

0.0514756

0.0354417

0.0301373

0.0300331

0.0539919

0.0378167

0.0299096

0.0292113

0.0571166

0.0413912

0.0318907

0.0309148

0.0593998

0.0439195

0.0331359

0.032514

0.0627476

0.046662

0.0344465

0.0328054

0.0649118

0.0489881

0.0364211

0.0338189

0.0679083

0.0532705

0.0368091

0.0345965

0.0711099

0.0560469

0.0400404

0.035822

0.073893

0.0590672

0.0376046

0.0358239

0.073299

0.0619224

0.0404633

0.0371678

0.0777921

0.0670391

0.0421996

0.0383482

0.0806686

0.0689545

0.0433464

0.0391816

0.0826094

0.0728825

0.0441904

0.0403368

0.0854129

0.0761713

0.0456439

0.0411846

0.0876262

0.0789669

0.0468598

0.0414145

0.0911948

0.0823978

0.0482715

0.0423266

0.0924155

0.0860223

0.0487469

0.0431128

0.0940781

0.0911473

0.0501367

0.0431187

0.0966715

0.08947

0.0497119

0.044791

0.0993194

0.0958231

0.0543911

0.0453796

0.101546

0.100214

0.0525261

0.0460357

0.105097

0.102629

0.055701

0.0467075

0.107695

0.106861

0.0558742

0.0481899

0.110656

0.11079

0.0574851

0.0483336

0.11291

0.114435

0.0581738

0.0502488

0.116033

0.117775

0.0599318

0.0499319

0.119638

0.120842

0.0608835

0.0500743

0.122213

0.125233

0.0623126

0.0516719

0.123377

0.12752

0.0621544

0.0516912

0.124955

0.131494

0.0648373

0.052597

0.127833

0.135477

0.0648856

0.0533017

0.131083

0.138452

0.066094

0.0535073

0.135408

0.14231

0.0658326

0.0544996

0.137541

0.14456

0.068014

0.0546933

0.139403

0.148483

0.0690085

0.0556335

0.141815

0.152369

0.0706309

0.0551642

0.144287

0.155766

0.0699755

0.057194

0.14898

0.15858

0.0725975

0.0579769

0.15227

0.161835

0.073849

0.0570616

0.155648

0.166092

0.074319

0.0585126

0.160032

0.170995

0.0757188

0.0595341

0.162713

0.172462

0.078353

0.0581313

0.167123

0.176469

0.0776474

0.0610992

0.169713

0.177361

0.0794393

0.0608639

0.173194

0.181584

0.0800545

0.0616529

0.17675

0.185811

0.0815026

0.062348

0.180601

0.18947

0.0823281

0.0623137

0.183293

0.19228

0.0834299

0.0632306



		0

		0.51585

		1.0346

		1.55918

		2.0365066667

		2.5843

		3.09906

		3.6153866667

		4.1335166667

		4.6520466667

		5.1652666667

		5.6852666667

		6.1991666667

		6.7187333333

		7.2357

		7.7528666667

		8.2708

		8.7845666667

		9.3054

		9.8173333333

		10.3354

		10.8513666667

		11.3686333333

		11.8836333333

		12.3998333333

		12.9161333333

		13.4336666667

		13.9497333333

		14.4690666667

		15.0166666667

		15.4958666667

		16.0171

		16.535

		17.0479666667

		17.567

		18.0826

		18.6003333333

		19.119

		19.6316333333

		20.1481

		20.6671666667

		21.1828

		21.6996

		22.2176666667

		22.7326333333

		23.2508333333

		23.7688666667

		24.2827333333

		24.8003666667

		25.3187666667

		25.8333666667

		26.3504333333

		26.8676666667

		27.3843

		27.8990666667

		28.4225666667

		28.9345666667

		29.4535

		29.9704



GLP

GLP-PEOX 5K 1:2

GLP-PEOX 50K 1:2

GLP-PVP 1:1

GLP-PVP 1:2

Time (min)

mg Dissolved




