Time-resolved photoluminescence of CdSe/CdS/CdZnS colloidal quantum dots.

I. V. Beloussov, V. I. Pavlenko, and I. I. Dobynde, Institute of Applied Physics, Kishinev, Republic of Moldova

### Abstract

We used highly luminescent CdSe/CdS/CdZnS colloidal quantum dots (QDs) prepared by a standard chemical synthesis method dispersed in low concentration into toluen in a 1 mm length quartz cuvette. The inner shell between the core and the outer shell allows one to reduce mechanical stresses inside the QD, since CdS has a lattice parameter intermediate between CdSe and CdZnS, which allows obtaining a significant PL quantum yield of these QDs (up to 85%). A sample with the photoluminescense (PL) peak at 628 nm was studied by transmission electron microscopy, optical absorption spectroscopy, and luminescence spectroscopy. It was determined that the diameter of the CdSe nucleus of QD amounts to 5.4 nm with the size dispersion of 8%. The thickness of the CdS/CdZnS shell was 2.6 nm. The PL in QDs was excited by a single 30 ps pulse of the second harmonic (539 nm) of a mode-locked YAlO3: Nd3+ laser at room temperature. The spectral decomposition of the PL signal collected from the front face of the cuvette was performed using a polychromator. The PL kinetics was recorded by a streak camera. The PL spectrum is located along the streak camera entrance slit. The image of time-resolved PL spectrum of QDs obtained on the streak camera screen was registered by a digital camera. The spectral resolution was about 5 meV and 9 meV for the time-integrated mode and the time-resolved mode, respectively, and an overall time resolution of about 40 ps was obtained. The time-resolved kinetics of PL is presented in Figure 1.

To describe the results of our measurements and find the decay times of the exciton and biexciton components of radiation, we propose simple theoretical models. We determine the spectral position and widths of the exciton and biexciton bands of photoluminescence and the biexciton binding energy.

### Recent Publications

### 1. V. I. Pavlenko, I. I. Dobinda, I. V. Beloussov, On the Determination of Quantum Dot Sizes by Spectroscopic Methods, J. Nanoelectron. Optoelectron. 9, (2014) 312-315.

2. P. I. Khadzhi O. F. Vasilieva, I. V. Belousov, Dynamics of an optical parametric oscillator based on dipolaritons, Optics and Spectroscopy 120, (2016), 760–765.

### 3. I.V. Beloussov, Generalized Bipolariton Model.Propagation of a Ultrashort Laser Pulse Through a Thin Semiconductor Film in the Conditions of Two-Photon Generation of Biexcitons, Proceedings of the 2nd International Conference on Nanotechnologies and Biomedical Engineering, April 18-20, 2013, Chisinau, Republic of Moldova, p.138-142.

### 4. I.V. Beloussov, Another Formulation of the Wick's Theorem. Farewell, Pairing?, Spec. Matrices 3, (2015), 169–174.

### 5. P. I. Khadzhi O. F. Vasilieva, I. V. Belousov, Dynamics of a dipolariton optical parametric oscillator in a semiconductor microcavity, JETP, 126, (2018),No 2.

Biography

Professor I.V. Beloussov is a Principal Researcher in the Institute of Applied Physics of the Republic of Moldova. He published more than 40 papers in reputed journals and is prominent in condensed matter physics with international recognition. V.I. Pavlenko and Dr. I.I. Dobynde are Senior Researchers in the same Institute.

Email: igor.beloussov@phys.asm.md

DETAILS OF PRESENTING AUTHOR

Full name:			Igor V. Beloussov

Electronic address:		igor.beloussov@phys.asm.md

Contact number:		+37369362943

Alternate contact number:	+37322738084

Linked In account:		Igor Beloussov

Track name:			Beloussov

Presentation: (Oral/ Poster) 	Poster