Recycling and reuse of MSWI fly ash for the synthesis of zeolite: Effects of different operation conditions

Jyh-Cherng Chen, Professor, Feng-Chia University, Taiwan 
Yi-Jie Lin, Master, Hungkuang University, Taiwan

Abstract (300 word limit)

The purpose of this research is to investigate the treatment and reuse of fly ash in the municipal solid waste incinerator (MSWI). The fly ash was treated with the alkali fusion hydrothermal method to synthesize the zeolite for reuse. The effects of different operation conditions and the optimum synthesis parameters were explored. The specific surface area, surface morphology, species identification, adsorption capacity, and the reuse potentials of the synthesized zeolites were analyzed and evaluated.

For the results of zeolite synthesized from the boiler ash, the optimum operation conditions were Si/Al=40, alkali/ash=1.5, alkali fusion reaction with NaOH at 400oC for 40 mins, hydrolysis with L/S=100 at 105oC for 24 hr, and hydrothermal synthesis at 105oC for 48 hr. The largest specific surface area of synthesized zeolite could up to be 881.24m2/g. The influence of different operation parameters on the synthesis of zeolite from boiler ash followed the sequence of Si/Al> alkali/ash> hydrolysis L/S> hydrothermal time> alkali fusion temperature. The XRD patterns of synthesized zeolites were identified to be similar with the Zeolite theta-1, ZSM-5, Terranovaite, and Zeolite Sigma-2. The adsorption capacity of synthesized zeolite for iodine was higher than that for methylene blue. The adsorption capacity of synthesized zeolite for iodine was increased as the rising specific surface area of synthesized zeolite, and the highest value could up to be 1881mg/g. This result verified that the synthesized zeolites from MSWI fly ash had great adsorption capacity and reuse potentials, they were not inferior to the commercial adsorbent such as the activated carbon.

In summary, MSWI fly ash can be used to synthesize the zeolite with high specific surface area by the alkali fusion and hydrothermal method. The zeolite can be reuse for the adsorption of various pollutants, their developing potentials are limitless.

Image

Recent Publications (minimum 5)

- Chen JC, Cheng YC (2017) Effects of different poison factors on the deactivation and characteristics of catalysts. International Journal of Advances in Science, Engineering and Technology 5(3):57-62.

- Chen JC, You CS, Cheng JS (2016) Reuse and recycling of spent lithium battery for the synthesis of catalysts. Industrial Pollution Prevention and Control 35(4):1-17.

- Lu CH, Chen JC, Chuang KH, Wey MY (2015) The different properties of lightweight aggregates with the ﬂy ashes of ﬂuidized-bed and mechanical incinerators. Construction and Building Materials 101:380-388.

- Hwang LL, Wey MY, Chen JC (2014) Effects of membrane compositions and operating conditions on the filtration and backwashing performance of the activated carbon polymer composite membranes. Desalination 352:181-189.

- Chen JC, Lin YZ, Chen WZ (2014) Waste to biofuel by torrefaction technology. International Journal of Chemical, Nuclear, Metallurgical and Materials Engineering 8(6): 447-450.

Biography (150 word limit)

Professor Jyh-Cherng Chen has his expertise in waste treatment and management; waste recycling, reuse and recovery technology; waste incineration, combustion and thermal treatment; waste to energy and fuel technology; and the synthesis, application and recovery of catalysts. He has more than 15 years of experience in research, teaching and administration. He has published more than 70 journal papers and 70 conference papers.

Email: jcchen2@mail.fcu.edu.tw

Notes/Comments: