# Title: Using of iron filings for copper recovery from spent copper etching solution by cementation process

Nanthanat Sriprasert, PhD, Mahasarakham university, Thailand

Pakpong Sriprasert, MEng, Mahasarakham university, Thailand

### Abstract

### This research aimed to study cementation technique to recover copper from spent copper etching solution using iron filings. High acidity spent etchant (pH 0.56) containing total Cu concentration of 17,260 mg/L ( 99 % is soluble Cu form). Conditions to enhance the efficiency of Cu recovery including reaction time, temperature, initial pH and amount of iron filings were optimized. Initial pH were tested at 0.5, 1.5, 2.0, 2.5 and 3.0 with iron filings amount of 0.5, 1, 2 and 3-folds of stoichiometry under reaction time of 0 - 60 mins and reaction temperature of 27 (room temperature), 50 and 80 C. After cementation, settling parameters of metals flocs were assessed as a guideline for solid-liquid separation process. Obtained metals sludge samples have been dried and ground, thereafter, morphologies of metal powders were observed by SEM. SEM-EDS also adopted to examine semi-quantitative elemental results of samples regions. Crystalline components analyzed by XRD and copper content in dried sludge were evaluated.

### The iron filings were found distributing in range of 45-1,000 m with majority size of 125-500 m (79% w/w). Results indicated that cementation requires reaction time for at least 6 mins. Among the optimal conditions examined, the amount of iron fillings showed a pronounce positive effect. Temperature and initial pH (0.5-3), however, clearly demonstrated an insignificant effect on Cu recovery yield. High Cu recovery for all adopt initial pH were found with 2-folds of stoichiometry for iron filings applying amount. The effective initial pH is suggested to be 0.5 (without adjustment), corresponding to 99 % of Cu recovery.

### Zero valent iron acts as reducing agent/ an electron donor for Cu ion by metallic replacement or cementation mechanisms. The blue Cu solutions immediately changed to colorless after cementation process. Dense easily settled metals sludge was formed.  Cu was the majority element for the obtained reddish brown sludge which the remainders were Pb, Fe, Sn, Si, Ni, Cr and O. Cu fraction in dried sludge was 80.4 % (w/w) which metallic copper (Cu) and copper (I) oxide (Cu2O) were mainly detected.

### Image

Recent Publications

- Sriprasert N., Zhang Y. and Banks C.J. (2015), Trace element requirements for long-term stable mesophilic digestion. Presented to the 14th World Congress on Anaerobic Digestion, Viña del Mar, Chile, 15th - 18th November.

- Sriprasert N., Zhang Y. and Banks C.J. (2016), Fe and Co distribution profiles in anaerobic digesters: The dynamic changes during washing-out stage. Presented to the Biogas Science 2016 Conference, Szeged, Hungary, 21st - 24th August.

- Sriprasert N., Zhang Y. and Banks C.J. (2016), Dynamic changes of metals (Fe and Co) distribution profiles in anaerobic digesters during their diluting-out phase. Presented to the Metals in Biology: The elements of biotechnology and bio-energy-Networks in Industrial Biotechnology and Bioenergy (BBSRC NIBB) Community Meeting for Early Stage Career Researchers, Durham, The UK, 19th - 20th December.

- Zhang Y., He S., Sriprasert N., Banks C.J. and Heaven S. (2017), Competition for trace elements between different players in anaerobic digesters. Presented to the Anaerobic Digestion and Bioresources Association Research & Innovation (ADBA R&I) forum 2017, The Building Centre, London, The UK, the 28th - 29th March.

- Zhang Y., He S., Sriprasert N., Banks C.J. and Heaven S. (2017), Competing demands for trace elements in anaerobic digesters. Presented to the 1st International Congress on Metals in Anaerobic Biotechnologies (IMAB17), Seville, Spain, the 4th - 6th October. Page

Biography

Dr Nanthanat Sriprasert and Pakpong Sriprasert are lecturer in Environmental Technology within Faculty of Environment and Resource Studies at Mahasarakham University, Maha Sarakham, Thailand. They enjoy both their research and the educational role of supporting students on their professional and personal development.  Their research has currently focused on pollution control and environmental sustainability, especially, the process of utilising industrial and agricultural waste/wastewater into useful products by recycling. They have their expertise in waste recycling and waste management, particularly, technologies of base and precious metals recovery from E-waste and PCBs manufacturing wastewater. They have built valuable results after years of experience in these researches. Dr Sriprasert, the first and corresponding author, obtained a BEng and MEng in Environmental Engineering from Suranaree University of Technology, Thailand. She was awarded her PhD by University of Southampton, the UK, for the work on requirement and distribution of trace elements in mesophilic anaerobic digestion. After her PhD study, she also retains a great interest in her PhD research area which is directly related to current practice in bioenergy production via anaerobic digestion and is the key research area at present for both renewable energy production and organic waste management.

Email: nanthanat@msu.ac.th

- Full Name: Nanthanat Sriprasert

- Personal Email: nanthanat@msu.ac.th

- Mobile Number: +66639954566

- Linked In: -

- Facebook: -

- Session Name/ number: Industrial Waste Recycling/Track 7

- Category: (Oral presentation/ Poster presentation): E-poster

- Date of Birth: 23 December 1979

- Postal Address: Mahasarakham University, Faculty of Environment and Resource Studies, Maha Sarakham, 44150, Thailand

Notes or Comments: