Influence of synthesized organic nitrogenous compounds in poly (ethylene oxide) blended with poly (vinylidene fluoride) and poly(methlyl methacrylate) polymer electrolyte in nanocrystalline dye-sensitized solar cells

S. Ganesan

Department of Chemistry, Faculty of Engineering and Technology, SRM University, 
    SRM Nagar, Kattankulathur-603203, Kancheepuram District, Tamil Nadu, India

Abstract

A novel work, reports on the performance of synthesized organic nitrogenous compounds  in poly(ethylene oxide) (PEO)/poly(vinylidene fluoride) (PVdF)/poly(methyl methacrylate) blend polymer electrolyte containing redox couple (I-/I3-) and application in solar energy conversion to electric energy source such as Di-tetrabutylammonium cis-bis(isothiocyanato)bis(2,2’-bipyridyl-4,4’-dicarboxylato)ruthenium(II) (N719dye) photo sensitized nanocrystalline TiO2 solar cells. The lone pair of electrons in the synthesized organic compounds  can easily coordinate with iodine in the redox couple (I−/I3−) to minimize the sublimation of iodine and resulted in improves the conductivity of PEO/PVdF/PMMA polymer electrolyte. The DSSC fabricated using the synthesized organic compound particularly 2,6 bis (N pyrazolyl) iso nicotinic acid (BNIN) doped polymer blend electrolyte (PEO/PVdF/PMMA) reports open-circuit voltage (Voc), short-current (Jsc), fill factor (ff) and conversion efficiency (η) values of 885 mV, 13.5 mA cm−2, 0.52 and 8.87% respectively, under illumination of 70 mW cm−2. The structural and electrical characteristics were analysed by scanning electron microscope (SEM), differential scanning calorimetry (DSC) and X-ray diffraction (XRD) and UV–vis spectroscopy whereas the photoelectrochemical studies (I–V) curves were characterized using a electrochemical analyser.

Key words: dye-sensitized solar cells, poly (vinylidene fluoride), poly (ethylene oxide), poly(methyl methacrylate) synthesized organic compounds, redox couple

Recent publications

1  Influence of organic nitrogenous compounds phenothiazine anddiphenyl  amine in poly(vinylidene fluoride) blended withpoly(ethylene  oxide) polymer electrolyte in dye-sensitized solar cells

S . Ganesan, Vinod Mathew, B. Joseph Paul, P. Maruthamuthu, S. Austin Suthanthiraraj

Electrochimica Acta 102 (2013) 219– 224

2 Enhanced performance of Dye-Sensitized Solar Cell using triazole based phenothiazine dendrimers as additives

Perumal Rajakumar, Chinnadurai Satheeshkumar, Mahalingam Ravivarm, Shanmugam Ganesan and Pichai Maruthamuthu

J. Mater. Chem. A, 2013, 1, 13941–13948

3 Synthesis of benzothiazole–benzoxazole dendrimers with triazole as bridging unit and their application in dye-sensitized solar cells

Perumal Rajakumar, Venkatesan Kalpana, Shanmugam Ganesan and Pichai Maruthamuthu

New J. Chem., 2013, 37, 3692—3700

4 A bright entry to improve the performance of DSSCs with the influence of novel optoelectronic acridinedione based macromolecules in I_/I3_ electrolytes

Govindasami Periyasami,  Raju Rajesh, Natarajan Arumugam, Raghavachary Raghunathan, Shanmugam Ganesan and Pichai Maruthamuthu

J. Mater. Chem. A  DOI: 1, 2013,14666–14674

5 A poly (ethylene oxide), poly (vinylidene fluoride) and polycapro lactone polymer blend doped with an indigenous nitrogen–sulfur based organic compound as a novel electrolyte system for dye-sensitized solar cell applications

S. Ganesan, P. Karthika, R. Rajarathinam, M. Arthanareeswari, Vinod Mathew, 
  P. Maruthamuthu

Solar Energy 135 (2016) 84-91

Biography

A variety of different polymer electrolytes based on Poly (ethylene oxide) and poly(vinylidene fluoride) along with potassium iodide and iodine has been prepared and their structural, thermal, spectral and electrochemical characteristics have been studied profoundly. These systems have been identified with appreciably high electrical conductivities at room temperatures and when employed in dye-sensitized solar cells are found to enhance their efficiency. Further, some of these electrolytes that showed good photo-conversion efficiency have been doped with eco-friendly materials from plants and bird wastages.

Department of Chemistry, Faculty of Engineering and Technology, SRM University, 
    SRM Nagar, Kattankulathur-603203, Kancheepuram District, Tamil Nadu, India

Email: ganesan.sh@ktr.srmuniv.ac.in

sakthi_ganesan@rediffmail.com

Mobile: 91-9940403220