Antibacterial Effects of Green synthesized Silver Nanoparticles on Surface Ultrastructure and Nanomechanical Properties of Gram-Negative Bacteria viz. Escherichia coli and Pseudomonas aeruginosa

Baskaran Ramalingam,†,≠ Thanusu Parandhaman,†,‡,≠ and Sujoy K. Das*,†,‡

†Biological Materials Laboratory, Council of Scientific and Industrial Research (CSIR)Central leather Research Institute (CLRI), Chennai600020, India, and ‡Academy of Scientific and Innovative Research (AcSIR), New Delhi110001, India.

≠Both have equal contribution

ABSTRACT: Silver nanoparticle mediated water purification is still under developmental stage. Understanding the interactions of silver nanoparticles (AgNPs) with the cell surface is crucial for the evaluation of bactericidal activity and for advanced environmental and biomedical applications. Biosynthesis of AgNPs was carried out through in situ reduction of silver nitrate (AgNO3) by cell free protein of Rhizopus oryzae and the synthesized AgNPs was characterized by UV-vis spectroscopy, high resolution transmission electron microscopy (HRTEM), dynamic light scattering (DLS), Zeta potential analysis and FTIR spectroscopy. The antibacterial activity of the biosynthesized AgNPs ( = 17.1 ± 1.2 mV) with average size of 9.1 ± 1.6 nm was evaluated against Gram-negative bacteria such as Escherichia coli and Pseudomonas aeruginosa. The results showed that AgNPs exhibited concentration dependent antibacterial activity and 100% killing of E. coli and P. aeruginosa achieved when the cells were treated with 4.5 and 2.7 µg/mL AgNPs, respectively for 4 h. Furthermore, the intracellular reactive oxygen species (ROS) production suppressed the antioxidant defense and exerted mechanical damage on the membrane. AgNPs also induced surface charge neutralization and altered of the cell membrane permeability causing non-viability of the cells. Atomic force microscopic (AFM) studies depicted alteration of ultrastructural and nanomechanical properties of the cell surface following interaction with AgNPs, while FTIR spectroscopic analysis demonstrated that cell membrane of the treated cells underwent an order-to-disorder transition during the killing process and chemical composition of the cell membrane including fatty acids, proteins, and carbohydrates was decomposed following interaction with AgNPs.

KEYWORDS: Silver nanoparticles, Antibacterial activity, Reactive oxygen species, Force spectroscopy, Nanomechanical properties.