Investigation on the Swelling characteristics and unsaturated shear strength of expansive soils from Arba Minch in Ethiopia.

Bantayehu Uba, MSc. School of Civil Engineering, Hawassa University, Hawassa, Ethiopia

### Abstract

### In  Ethiopia,  many  researches  were  done  on  characterizing expansive  soils  but  only  a  very  limited  number  of  studies  were conducted on Addis Ababa expansive soil, exists on the unsaturated shear  strength  behavior.  The  present  study  addresses  examining expansive soils in Arba Minch – a town in the Rift Valley with great portion  of  its  terrain  covered  by  the  same  soil  but  not  considered previously. Laboratory-testing program was planned and performed on  undisturbed  soil  samples  taken  from  10  locations  for  swelling pressure  testing;  and  among  these,  one  pit  was  allotted  for unsaturated  shear  strength  study.  The  laboratory  test  results revealed  swelling  pressure  ranges  from  74.53  to  571.29  kPa, Plasticity Index from 49 to 77%, Shrinkage Index from 81 to 117% and Free Swell from 94.0 to 165.0%. The results from unsaturated shear strength tests performed  with a 50kN modified  double wall triaxial  machine  on  an  undisturbed  sample  setting  matric suction 100  kPa,  150  kPa  and  200kPa  for  an  effective  consolidation pressure of 200kPa have clearly indicated the saturated case to yield smaller  shear  strength  than  the  unsaturated  one.  The maximum deviator stress showed to increase from 107.61kPa to 174.35kPa with an increase in matric suction but the shape of the stress-strain diagram remained identical.

Recent Publications

- Abed, A.  (2008). Numerical Modelling of Expansive Soil Behavior.  Ph.D.  Dissertation, Institut für  Geotechnik, Universität Stuttgart, Germany.

- Alla  P.  (2009). Dynamic behavior of unsaturated soils. Msc.  Thesis, Graduate Faculty of the Louisiana State University, U.S.A.

- Förch,  G.  (2009). CICD Series Vol.3:  Summary of Master Theses from Arba Minch University, Ethiopia. Printing Office, Universität Siegen, Germany.

- Gebre,  H.  (2010). Unsaturated Shear Strength Characteristics and Stress Strain Behavior of Expansive Soils of Addis Ababa. Msc. Thesis, Addis Ababa University, Addis Ababa, Ethiopia.

- Hilf, J.W. (1956). An Investigation of pore-water pressure in compacted cohesive soils. Ph.D.  Dissertation, Texas Tech University, Texas.

- Nigussie  D.  (2007). In-depth  Investigation  of  Relationship between  Index  Property  and Swelling Characteristics  of Expansive  soil  in  Bahir  Dar.  Msc.  Thesis, Addis Ababa University, Addis Ababa, Ethiopia.

- W/Medhin G.,  (2010). A  Study  on  Shear  Strength Characteristics  of  Addis  Ababa  Red  Clay  Soil  for Unsaturated  Case. Msc Thesis, Addis Ababa University, Addis Ababa, Ethiopia.

Bantayehu Uba was born in Arba Minch, Ethiopia, 21 October 1984. He received the B.Sc.  Degree in Civil Engineering and M.Sc.  Degree in Civil Engineering (Geotechnical Engineering) in 2007 and 2011, from Mekelle and Addis Ababa Universities respectively. His present occupation as an academician is Lecturer in the Institute of Technology, School of Civil Engineering, Hawassa University since March 24, 2015. He has also served as part-time Lecturer in Institute of Urban Development Studies, Ethiopian Civil Service University from March 2009 up to Feberuary 2011 and also as Assistant Lecturer at Civil Engineering Department of Technology Faculty, Arba Minch University from September 2007, up to September 2008, Ethiopia. On his professional carrier, he has   worked with contractor and consulting private firms in road and building construction and design since September 2009 and now he is serving as a project manager at Santamaria Construction PLC. Since November 2015.

Email: ubabanti@gmail.com/bantayehuu@hu.edu.et

Notes/Comments: