Commercial Polyester Fabric Repair of Abdominal

Defects and Hernias

M.Shokry

Hernias are common surgical affections of human and animals and their treatments may vary from simple herniorrhaphy to hernioplasty with prosthetic materials. Each prosthetic material has advantages and disadvantages in terms of tissue ingrowth, adhesion formation, biocompatibility, ,incidence of infection recurrent,  migration and shrinkage profiles.

Purpose

This work was designed to study the feasibility of using commercial polyester fabric (CPF) as a prosthetic mesh for  reconstruction of abdominal hernias and defects in experimental and clinically affected animals. model with induced abdominal wall defects. Pertinent data will include surgical details including the site of implantation, postoperative outcomes, long-term follow-up evaluation and histopathological examinations.

Methods

The subjects of the experimental work were 12 dogs, 3 goats and 3 donkeys. Following anesthesia, an artificial abdominal defect was then produced by resectiom of a piece of abdominal muscle in 3 different abdominal regions, such as the epigastrium (3 cases), in which partial resection of the rectus abdominis muscle unilaterally, both the external and internal abdominal oblique muscles and the transversus abdominis muscle was made; the mesogastrium (12 cases) in which bilateral partial resection of the rectus abdominis muscle was made; and the hypogastrium (3 cases) in which partial resection of both the external and internal abdominal oblique muscles and the transverse abdominis muscle was made. These defects measured 5X12 cm in dogs and goats and 12X20cm in the don keys. An appropriate piece of sterilized CPF was implanted either in 2 layers in small animals or in 4 layers (folded) in large animals in the abdominal defects. The technique of implantation used were reteroperitoneal/subfascial (6 cases)in which the CPF was implanted between the internal rectus sheath and peritoneum, intraperitoneal implantation either with (3 cases) or without (3 cases) omentalisation; and double sandwish (3 cases) in which one layer of CPF was implanted between the internal rectus sheath and the peritoneum and the outer layer was implanted superficial to the external rectus sheath. The two layers of CPF were sutured in position using a staple stitch. The subcutaneous  tissues were opposed over the prosthetic material using Vicryl 0 sutures in a simple continuous pattern. The skin was closed routinely. Preoperative prophylactic ampicillin (25 mg/kg i.v.)was administered to all animals twice daily for 7 days. Morphological and histopathological examinations were carried out on full thickness sections after euthanasia at 1, 2 ,3 ,4, 5 & 6 months  postoperatively. The Clinically affected animals comprised 2 bovine and 2 buffalo calves ( aged 6 to 18 months and weighing 100 to 150 kg), one adult dog, 5 ewes, 3 adult goats and one female donkey with umbilical hernias (4 cases) and ventral abdominal hernias (10 cases) which were recurrent, incisional and traumatic in origin. All had large hernia rings. The technique of herniorrhaphy using CPF as a prosthetic material  either a retroperitoneal/subfascial (11 cases) or intraperitoneal with omentalisation (3 cases). The Skin was closed routinely.An  antibiotic was given as before in the experimental work.

Results

Gross examination of the abdominal wall at the experimental implantation site at monthly intervals for 6 months showed the unaltered integrity of the CPF and uniform infiltration of the prosthetic material with a layer of white connective tissue of variable thickness (4 to 10 cm). No detectable adhesions or signs of rejection were noticed. In omentalisation cases the omental pedicle was adhered to the visceral surface of the CPF mesh. Histological features correlated well with the gross examination in that fibroplasia was demonstrated throughout both layers of the CPF mesh. By the 6th postoperative month the CPF mesh was uniformly infiltrated by fibrous tissue and firmly incorporated into the abdominal wall. Complications related to herniorrhaphy in the clinical cases have been rarely serious.

Conclusion

CPF has excellent biocompatibility and no adverse histological changes. Low cost CPF therefore offers a worthwhile alternative prosthesis for mesh herniorrhaphy.

Professor Emeritus, Dept. of Vet Surgery, Faculty of Veterinary Medicine, Cairo University

http://scholar.cu.edu.eg/mshokry

Email: mshokry@cu.edu.eg

Notes/Comments: