Cytotoxicity comparison of zirconia& high noble alloy & base metal alloy on human gingival fibroblast cells

Purpose: cell toxicity is one of the most important side effect of using dental materials in mouth ambience.dental materials release ions & elements during erosion ,abrasion & bacterial activity that have harmful effect on mouth tissues.the purpose of this study was evaluate & compare cell toxicity of high noble alloy,base metal alloy & zirconia on human gingival fibroblast cells with use of MTT test in Tehran azad university of dental science in 2016.

Methods & materials: in this experimental research 6 disc with 5mm diameter & 2mm thickness of high noble alloy,base metal alloy & zirconia prepared. DMEM as negative control & DMSO as positive control considered. Samples extract was prepared in two dilation (200ml &400 ml)

Cell toxicity & cell viability of samples extract next to the human fibroblat cells in duration of 24-48-72hour was measured with MTT test.conclusion of MTT test analyzed by ANOVA & post hoc (Tukeys) analyze.

Result: in 24 ,48 ,72 hours and in 200ml & 400ml density, less average Optical density(DO)was belonged to positive control DMSO then base metal alloy sample  then zirconia sample then high noble alloy sample.the most DO belonged to negative control DMEM.

Conclusion: base metal alloy sample showed the most cell toxicity & less cell viability,high noble alloy sample showed less cell toxicity & the most cell viability and zircona sample was in midpoint in cell toxicity and cell viability.

Keywords:Zirconia,alloy,base metal,high noble,cell toxicity,tissue compatibility,cell viability,MTT