A Comparative Evaluation of Apical Seal Associated with

Ultrasonic Retrograde Cavities Filled with Bioactive

Material (In Vitro Study)

Raghad A. Al-Hashimi, B.D.S., M.Sc., Ph.D. (1)

Maha A. Habeeb, B.D.S., M.Sc. (2)

Athil A. Al-Kinani, B.D.S., M.Sc. (3)

ABSTRACT

Background: The aim of this study was to evaluate and compare the apical microleakage around retrograde

cavities prepared with ultrasonic technique and filled with (Biodentine™)

Materials and methods: 40 extracted single rooted human permanent maxillary teeth with mature apices were

selected. The roots were prepared chemo-mechanically using k-files with crown-down technique and then

obturated with lateral condensation gutta-percha technique. Teeth were divided into four main groups according to

the cavity preparation method either manual or ultrasonic technique:

Group A (n=10): A class I retrograde cavity at root end was prepared with traditional handpeice equipped and

placement of Biodentine with manual condensation.

Group B (n=10): A class I retrograde cavity at root end was prepared with Piezoelectric ultrasonic device equipped

with ultrasonic tip with only manual compaction of the material.

Group C (n=10): traditional handpeice and placement of Biodentine using both manual compaction and 5 second

ultrasonic activation.

Group D (n=10): Piezoelectric ultrasonic device and placement of Biodentine with both manual compaction and 5

second ultrasonic compaction. The teeth were immersed in 1% aqueous Methylene blue dye for 72 hr. Then they

were sectioned longitudinally with a diamond disc and the depth of dye penetration was examined under high

magnification 20X.

Results: Statistical analysis showed a highly significant difference in microleakage among the tested groups in which

Piezoelectric technique has proved superiority in retrograde cavity preparation and compaction of Biodentin when

dye penetration scores were compared. So microleakage was highest with cavities prepared with handpeice and

manual application of retrograde material group A (2.73±0.39) followed by microprepared cavities group C

(1.86±0.16), and it was lowest with ultrasonically-prepared cavities group B (1.09±0.28) and group D (0.26±0.19).

Conclusion: ultrasonic preparation produced significantly less microleakage than conventional method. Also less

microleakage was observed with ultrasonic compaction of Biodentin when compared with conventional method of

compaction.

Keywords: Endodontic surgery, microleakage, Biodentine, Piezoelectric ultrasonic device, retrograde cavities.

(1)Assist. Professor. Department of Conservative Dentistry, College of Dentistry, University of Baghdad.

(2) Lecturer. Department of Conservative Dentistry, College of Dentistry, University of Baghdad.

(3) Oral and maxillofacial surgeon. Ministry of Health, Iraq.