Comparative study of the adsorption efficiency of biomass modified bentonite for dyes
Alimoh H. Alabi, Kelechukwu K. Ibe and Paul Abi
University of Ibadan, Nigeria
Abstract
Effluents discharges extensively released from various industries is concentrated with different types of dyes and has been considered as a grave environmental problem stimulating attention all over the world because of their effects to humans and the environment (aquatic and terrestrial), if not properly treated before disposal. In the light of this and among various agricultural wastes, this study seeks to examine comparatively the adsorption efficiency of bentonite and its modification with groundnut shell and palm kernel shell by calcination in the removal of methylene blue and Congo red dyes from aqueous solution with a view of evaluating the adsorption properties of the modified products for possible improved adsorption.
The bentonite and biomass modified bentonites were characterized by Fourier Transform Infrared (FTIR) Spectroscopy, Scanning Electron Microscopy (SEM), Energy Dispersive Spectroscopy (EDS) and Brunauer-Emmett-Teller (BET) theory. The effects of adsorbent dosage, pH, dye concentration, contact time and temperature on the practicability, effectiveness and comparative efficiency of bentonite and biomass modified bentonite for adsorption of dyes were investigated using the batch process. The degrees of adsorption were monitored using uv-visible spectroscopy of the dyes. The thermodynamics, adsorption equilibrium isotherm and kinetics for the adsorption processes were also evaluated.
Equilibrium data analyses using Langmuir, Freundlich, Temkin and Dubinin-Raduskevich isotherms showed that Temkin and Freundlich isotherms were the most suitable for the adsorption of the dye molecules with maximum adsorption capacity of 10.6078 mg/g, 10.8537 mg/g and 10.9326 mg/g for methylene blue removal by bentonite, Bentonite modified with Groundnut Shell (BGS) and Bentonite modified with Palm Kernel Shell (BPKS) and 8.8299 mg/g, 6.8671 mg/g and 5.8630 mg/g for Congo red removal by bentonite, BGS and BPKS respectively. Among the pseudo-first order, pseudo-second order, Elovich and intra-particle diffusion, the pseudo-second order kinetic model favoured the adsorption process of the dye molecules with high R2 values ranging for 0.9696–1 for the adsorbents. Thermodynamic parameters such as ΔGo, ΔHo and ΔSo showed that the adsorption process was spontaneous for the dye removal from aqueous solution by the adsorbent; endothermic and exothermic for Congo red and methylene blue adsorption respectively and some degree of randomness at the solid-liquid interface.
The results further suggested that the biomass modified bentonite enhanced adsorption capacity for the removal of methylene blue from aqueous solution. Conversely, the modification did not enhance the adsorption capacity of the biomass modified bentonite for the removal of Congo red from aqueous solution but easier separation of the adsorbent from the solution as compared to bentonite was observed. The study therefore concludes that the biomass modified bentonite is a cost effective, non-toxic, easily available, greener approach for the removal of methylene blue from aqueous solution.
[bookmark: _GoBack]Conclusion: The study modified bentonite clay using agricultural wastes products (groundnut shell and palm kernel shell) and investigated the adsorption efficiency of the modified products in comparison to bentonite in the removal of organic dyes (methylene blue and Congo red) from aqueous solution. It concludes that the modification of bentonite with groundnut shell and palm kernel shell for removal of cationic and anionic dye from aqueous solution is possible. Although the modified products did not improve the efficiency of bentonite for the removal of Congo red from the aqueous solution with a decrease in the adsorption capacity in the order: bentonite>BGS>BPKS, the modified products demonstrated improved adsorption in methylene blue removal following the order BPKS>BGS>bentonite. The study also suggests that the enhanced separation of the modified product from aqueous solution, economic viability, environmental sustainability and friendliness, availability and non-toxicity of the wastes in large quantities should be explored and leveraged.
Importance of Research
Activated carbon is the most widely used adsorbent because of its great capacity for adsorption of organic materials. However, this adsorbent is difficult to regenerate at a high cost. In this context, the use of bentonite and its modification with groundnut shell and palm kernel shell as adsorbent is of great interest because of possible improvement in efficiency, easy accessibility and availability, cost effectiveness and waste recycling for sustainable development; thus providing alternative effective and efficient adsorbent at low cost and proper waste management of the agricultural wastes.
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