Development of mosquito repellent-UV protective polyester using a disperse dye synthesized from 4-hydroxy coumarin

# Ankit Singh* and Javed Sheikh

Indian Institute of Technology, India

Abstract

The development of functional textile fibers using novel routes is an urgent requirement. Mosquito repellent textile is one of the best choices for manufacturing protective clothing. Polyester fiber is widely utilized in apparel and technical textile applications. In the present work, a novel disperse dye was prepared by reacting diazotized sulfadiazine with 4-hydroxy coumarin. The developed dye was characterized by Fourier-transform infrared spectroscopy (FTIR), 1H NMR, 13C NMR, CHN analyzer, and UV-Vis spectroscopy. The prepared disperse dye was utilized for the dyeing of polyester fabric. The exhaustion (%), fixation (%), and coloration properties (L*, a*, b*, C*, K/S) were studied. Wash-durability of dyed fabrics against repeated laundering treatments was additionally determined. The standard methods were used to measure the fastness and functional properties (mosquito repellency and UV protection) of dyed polyester. The dyed polyester indicated wash-durable mosquito repellency (100% after 20 washes) and excellent UV protection. X-Ray Diffraction (XRD) and Thermo Gravimetric Analysis (TGA) of dyed fabrics were also done to characterize the dyed polyester.

Biography

Currently, Ankit Singh is working as a PhD student at IIT Delhi. His research areas are functionalization of textiles using bio-molecules combined dyeing finishing, synthesis of dyes. I have strong expertise in the characterizations of organic molecules such as FTIR, 1HNMR, 13CNMR, TGA, DSC, UV -Vis spectroscopy, mass spectroscopy.