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Abstract
Wrinkled Silica Nanoparticles (WSNs) with central-radial pore structure were hydrophobized by chemical vapor deposition of perfluorodecyltriethoxysilane (PDTES): surface functionalization was used to design a hydrophobic surface to induce interfacial activation of lipase by lid opening. In fact, lipases are unique often require interfacial activation for full catalytic performance. Actually, since lipids are water insoluble, lipases act on emulsified systems. Upon adsorption at a hydrophobic/hydrophilic interface, lipase undergoes a conformational change from the inactive to the active conformation. This change is promoted by the movement of a helical loop from the ‘closed’ form in which the catalytic site is inaccessible to the ‘open’ active one. To further modulate the closed/open form equilibrium, n-hexane was added to the water/lipase solution, creating a micro-oily environment [Figure 1]. 
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Figure 1. Hydrophobization of wrinkled silica nanoparticles and lipase immobilization procedure.
Three different supports were prepared, varying the degree of hydrophobicity. The effect of the different hydrophobicity and of the addition of n-hexane on the adsorption of lipase was evaluated. The best biocatalyst obtained was tested in the transesterification of sunflower seed oil to produce biodiesel, showing hyperactivation. The reaction yields were 93% for the immobilized enzyme and 56% for the free one. The results suggest that both the hydrophobicity of the support and the addition of n-hexane favor the adsorption of lipase in the active conformation.
Methodology: Physicochemical characterization of supports was carried out by solid state 29Si Nuclear Magnetic Resonance (NMR), the Brunauer–Emmett–Teller (BET) method, Thermo-Gravimetric (TG) analysis, Contact Angle (CA) measurement, Scanning Electron Microscopy (SEM) and Fourier Transform Infrared (FT-IR) Spectroscopy.
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Figure 1. Hydrophobization of wrinkled silica nanoparticles and lipase
immobilization procedure




