Nanostructured polysaccharides materials for water purification

Sabu Thomas

Mahatma Gandhi University, India

Abstract

The design and synthesis of nano-architected cellulose and chitin can act as efficient materials for water purification. The talk aims to study and compare the performance of a Polyvinylidene Fluoride (PVDF) electrospun membrane, unmodified Cellulose Nano-Fiber (CNF) based PVDF membrane and Meldrum’s acid (2,2-dimethyl-1,3-dioxane-4,6-dione) modified CNF-based PVDF membranes against the Fe2O3 nanoparticle filtration and Crystal Violet (CV) dye adsorption. Herein, we introduced a facile method to produce a unique green adsorbent material from Cellulose Nano-Fibers (CNFs) via a non-solvent assisted procedure using Meldrum’s acid as an esterification agent to enhance the adsorption toward positively charged crystal violet dyes. Most of the surface modifications of cellulose nanofibers have been done using toxic organic solvents like pyridine, dimethyl acetate, (2,2,6,6-tetramethylpiperidin-1-yl)oxyl (TEMPO), etc. So far, this is the first report on the surface modification of cellulose nanofibers via a non-solvent assisted procedure. Both CNF-based PVDF membranes were prepared by successive coating of modified and unmodified CNFs on to the surface of a PVDF electrospun membrane. All the demonstrated membranes showed high filtration capacity against the Fe2O3 nanoparticles. With the 10 mg/L of Crystal Violet (CV) aqueous solution, CV adsorption of PVDF electrospun membrane and unmodified CNF-based PVDF membrane was around 1.368 and 2.948 mg/g of the membrane respectively, whereas it was 3.984 mg/g of the membrane by Meldrum’s acid CNF-based PVDF membrane. The demonstrated Meldrum’s acid modified CNF-based PVDF membrane was proven to be the efficient media that can concurrently eliminate the Fe2O3 nanoparticles and CV dyes from the water. The investigation into the surface chemistries of cellulose nanofibers beyond the adoption of toxic solvents can enhance the economic usefulness of the process and also yield a new eco-friendly adsorbent material that is agreeable to adsorbing various toxic pollutants.

Biography

Sabu Thomas is currently Vice Chancellor of Mahatma Gandhi University, Kottayam, Kerala, India. He is an outstanding leader with sustained international acclaims for his work in Nanoscience, Polymer Science and Engineering, Polymer Nanocomposites, Elastomers, Polymer Blends, Interpenetrating Polymer Networks, Polymer Membranes, Green Composites and Nanocomposites, Nanomedicine and Green Nanotechnology. In collaboration with India’s premier tyre company, Apollo Tyres, His group invented new high performance barrier rubber nanocomposite membranes for inner tubes and inner liners for tyres. He has received more than 30 national and international awards which include, FRSC, Distinguished Professorship from Josef Stefan Institute, Slovenia, MRSI medal, CRSI medal, Distinguished Faculty Award, He is in the list of most productive researchers in India and holds a position of No.5. He has been conferred Honoris Causa (D.Sc) by the University of South Brittany, Lorient, France, Siberian Federal University, Russia and University of Lorraine, Nancy, France, awarded Senior Fulbright Fellowship, National Education Leadership Award-2017 for Excellence in Education. He also won 6th contest of "mega-grants"-Russian Federation. Very recently, he received the coveted Kailali award from Govt of Kerala. He also received the Chancellors Trophy for the best University of the state from the Chancellor. Very recently he has been ranked by Stanford University under 2 percent top leading researchers in the world. He has published over 1400 peer reviewed research papers, reviews and book chapters. He has co-edited 200 books inventor of 16 patents. The H index of him is 127 and has more than 80,000 citations. He has delivered over 350 Plenary/Inaugural and Invited lectures in national/international meetings over 30 countries. He has supervised 120 PhD programme and his students occupy leading positions in academia and industry in India and abroad.