Investigation of the abrasion behaviour of GNP and B4C reinforced magnesium composites

Simge Bayhatun1*, Volkan Karakurt1, Hayrettin Ahlatci1, Mustafa Babanli2, Nurlan Gurbanov2 and Yunus Turen1

1Karabuk University, Turkey

2Azerbaijan State Oil and Industry University, Azerbaijan

Abstract

In this study, 0.5% nano GNP (Graphene Nano-Particle) and 15% B4C reinforced composites with AZ71 Mg alloy matrix were produced and extruded by melt-based induction casting. The microstructures, mechanical and dry abrasion behavior of the produced composites were investigated. While Nano GNP is used because they exhibit high thermal conductivity and low friction coefficient, B4C particle has benefited from its high strength. In addition, another purpose of choosing B4C and GNP; Due to the high wettability between B4C, GNP and Mg matrix, the interfacial bond between the composite matrix and the reinforcement is also strong to obtain a final product. The abrasion tests of the extrusion specimens were carried out by measuring the weight loss under a constant 20 N load, at a constant speed of 100 mm/sec and a total sliding distance of 1000 m in a back-and-forth abrasion test device. In the studies, although the hardness value of the AZ71+15% B4C composite is high, the abrasion behavior of the nano Graphene reinforced AZ71+0.5% GNP composite has improved because it reduces the friction coefficient.

Biography

Simge Bayhatun graduated from Karabuk University Metallurgy and Materials Engineering. He is doing his master's degree at the same university. He lives in İzmir Karşıyaka. During his time at his school, he actively used the metallography devices in the department laboratory. He is familiar with wear device, fatigue devices and tensile testing.