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Abstract (300 word limit)
Statement of the Problem:. 3D printing selective laser melting additive manufacturing considered as the future for removable partial denture (RPD) fabrication. Fitness accuracy is an important criteria for removable partial dentures that will affect its success 
The purpose of this study is to compare the fitness accuracy of digitally produced RPD using selective laser melting additive manufacturing technology with ones that were produced by lost wax/ casting method and with combined digital and conventional frameworks 
Methodology: Cl I Kennedy classification RPD frameworks were fabricated. There were 3 groups: 3DP-G1 where frameworks produced digitally through digital designing and then the frameworks printed by selective laser melting additive manufacturing. C-G2 where the framework produced by lost wax/casting method. and the third group (SP-G3 ) where the framework produced by scanning wax-up of the framework and then printed as in the first group. 6 frameworks were produced from each group, Fitness accuracy of the frameworks was assessed by three methods: 1. subjective clinician assessment through specific criteria. 2. by calculating spaces at five specified locations under the frameworks when seated on the master casts using images imported from micro-CT . Finally, spaces at the same locations were measured by using light-body polyvinyl siloxane impression materials. 
Results: Clinicians found that all frameworks were seated well without rocking of rotation or lateral movement. There was no significant difference among the spaces calculated underneath the18 frameworks for the three various groups at significance level of (α=.05). Although the spaces detected in the micro-CT images were remarkably higher than the ones from the silicone registration materials.
Conclusions: RPD frameworks that produced by 3D printing technology using selective laser melting additive manufacturing have a high level of fitness accuracy that are comparable to the ones produced by lost wax/casting method.
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