# Comparative Study of the Adsorption Efficiency of Biomass Modified Bentonite for Dyes

Alimoh H. Alabi, *Kelechukwu K. Ibe and **Paul Abi helenalabie3@yahoo.com, *ibekelechukwu@gmail.com, **abipaul490@gmail.com Department of Chemistry, University of Ibadan, Ibadan, Nigeria

# Biography

Abstract

Alimoh H. Alabi, PhD, is a senior lecturer in the Department of Chemistry, Faculty of Science, University of Ibadan, Ibadan, Nigeria. She obtained her Bachelor of Science, Master of Science and PhD degrees from the University of Ibadan. Her area of specialization on research is analytical/environmental chemistry. Currently, she is the Sub-dean, Faculty of Science, University of Ibadan, Ibadan.

Kelechukwu K. Ibe is an industrial and environmental chemist. He holds a Bachelor of Science Degree in Pure and Industrial Chemistry (2015) from Nnamdi Azikiwe University, Awka; and a Master of Science Degree in Environmental Chemistry and Pollution Control (2021) from the University of Ibadan, Ibadan, both in Nigeria. His research interests are water quality, wastewater treatment, environmental (sustainability) impact assessment, plastic pollution assessment and control, waste recycling and management etc.

Paul Abi is a certified and seasoned educator with over 3 years of experience facilitating learning in private and public schools in Nigeria. He has earned a four-year Bachelor of Science degree and a two-year Master of Science Degree in Education and Chemistry and Analytical Chemistry respectively. He has passion for education, leadership and development which inspired him to join Teach for Nigeria (a nonprofit organization) serving as an impact-driven teacher-leader in Ogun State, Nigeria.

Effluents discharges extensively released from various industries is concentrated with different types of dyes and has been considered as a grave environmental problem stimulating attention all over the world because of their effects to humans and the environment (aquatic and terrestrial), if not properly treated before disposal. In the light of this and among various agricultural wastes, this study seeks to examine comparatively the adsorption efficiency of bentonite and its modification with groundnut shell and palm kernel shell by calcination in the removal of methylene blue and Congo red dyes from aqueous solution with a view of evaluating the adsorption properties of the modified products for possible improved adsorption.

The bentonite and biomass modified bentonites were characterized by Fourier Transform Infrared (FTIR) Spectroscopy, Scanning Electron Microscopy (SEM), Energy Dispersive Spectroscopy

(EDS) and Brunauer-Emmett-Teller (BET) theory. The effects of adsorbent dosage, pH, dye concentration, contact time and temperature on the practicability, effectiveness and comparative efficiency of bentonite and biomass modified bentonite for adsorption of dyes were investigated using the batch process. The degree of adsorption were monitored using uv-visible spectroscopy of the dyes. The thermodynamics, adsorption equilibrium isotherm and kinetics for the adsorption processes were also evaluated.

Equilibrium data analyses using Langmuir, Freundlich, Temkin and Dubinin-Raduskevich isotherms showed that Temkin and Freundlich isotherms were the most suitable for the adsorption of the dye molecules with maximum adsorption capacity of 10.6078 mg/g, 10.8537 mg/g and 10.9326 mg/g for methylene blue removal by bentonite, bentonite modified with groundnut shell (BGS) and bentonite modified with palm kernel shell (BPKS) and 8.8299 mg/g, 6.8671 mg/g and 5.8630 mg/g for Congo red removal by bentonite, BGS and BPKS respectively. Among the pseudo-first order, pseudo-second order, Elovich and intra-particle diffusion, the pseudo-second order kinetic model favoured the adsorption process of the dye molecules with high R2 values ranging for 0.9696 – 1 for the adsorbents. Thermodynamic parameters such as ΔGo, ΔHo and ΔSo showed that the adsorption process was spontaneous for the dye removal from aqueous solution by the adsorbent; endothermic and exothermic for Congo red and methylene blue adsorption respectively and some degree of randomness at the solid-liquid interface.

The results further suggested that the biomass modified bentonite enhanced adsorption capacity for the removal of methylene blue from aqueous solution. Conversely, the modification did not enhance the adsorption capacity of the biomass modified bentonite for the removal of Congo red from aqueous solution but easier separation of the adsorbent from the solution as compared to bentonite was observed. The study therefore concludes that the biomass modified bentonite is a cost effective, non-toxic, easily available, greener approach for the removal of methylene blue from aqueous solution.

Conclusion: The study modified bentonite clay using agricultural wastes products (groundnut shell and palm kernel shell) and investigated the adsorption efficiency of the modified products in comparison to bentonite in the removal of organic dyes (methylene blue and Congo red) from aqueous solution. It concludes that the modification of bentonite with groundnut shell and palm kernel shell for removal of cationic and anionic dye from aqueous solution is possible. Although the modified products did not improve the efficiency of bentonite for the removal of Congo red from the aqueous solution with a decrease in the adsorption capacity in the order: bentonite > BGS

> BPKS, the modified products demonstrated improved adsorption in methylene blue removal following the order BPKS > BGS > bentonite. The study also suggests that the enhanced separation of the modified product from aqueous solution, economic viability, environmental sustainability and friendliness, availability and non-toxicity of the wastes in large quantities should be explored and leveraged.

# Importance of Research

Activated carbon is the most widely used adsorbent because of its great capacity for adsorption of organic materials. However, this adsorbent is difficult to regenerate at a high cost. In this context, the use of bentonite and its modification with groundnut shell and palm kernel shell as adsorbent is of great interest because of possible improvement in efficiency, easy accessibility and availability, cost effectiveness and waste recycling for sustainable development; thus providing alternative effective and efficient adsorbent at low cost and proper waste management of the agricultural wastes.

# About University

Established in 1948, the University of Ibadan, UI as it is fondly referred to, is the first University in Nigeria. Until 1962 when it became a full-fledged independent University, it was a College of the University of London in a special relationship scheme. The University, which took off with academic programmes in Arts, Science and Medicine, is now a comprehensive citadel of learning with academic programmes in sixteen Faculties namely, Arts, Science, Basic Medical Sciences, Clinical Sciences, Agriculture, the Social Sciences, Education, Veterinary Medicine, Pharmacy, Technology, Law, Public Health, Dentistry, Economics, Renewable Natural Resources and

Environmental Design and Management. Through its alumni and alumnae, the University of Ibadan has, in the past six decades contributed significantly to the political, industrial, economic and cultural development of Nigeria. No doubt, the University’s commitment enables them to fly high.

# References

- Abdullah, S.L.; Audu, A.A. Comparative analysis on chemical composition of bentonite clays obtained from Ashaka and Tango deposits in Gombe State, Nigeria. ChemSearch Journal 2017, 8, 35-40.

- Alabi, A.H.; Oladele, E.O.; Adeleke, A.; Oni, F.C.; Olarewaju, C.A. Equilibrium, Kinetics and Thermodynamic Studies of Biosorption of methylene blue on goethite modified baobab fruit pod (Adansonia Digitata L.). J. Appl. Sci. Environ. Manag. 2020, 24, 1229- 1243.

- Alhujally, A.; Yu, H.; Zhang, X.; Ma, F. Adsorptive removal of anionic dyes from aqueous solutions using spent mushroom waste. Appl. Water Sci. 2020, 10, 183.

- Baby, R.; Saifullah, B.; Hussein, M.Z. Palm Kernel Shell as an effective adsorbent for the treatment of heavy metal contaminated water. Sci. Rep. 2019, 9, 1-11.

- Boumediene, M.; Benaïssa, H.; George, B.; Molina, S.; Merlin, A. Effects of pH and ionic strength on methylene blue removal from synthetic aqueous solutions by sorption onto orange peel and desorption study. J. Mater. Environ. Sci. 2018, 9, 1700–1711.

- Gherbia, A.; Chargui, A.; Yeddou, A.R.; Selatnia, A.S.; Boubekeur, N. Removal of methylene blue using activated carbon prepared from date stone activated NaOH. Glob. Nest J. 2019, 21, 374-380.

- Imam, S.S.; Abdullahi, M. Adsorption removal of methylene blue using groundnut shell activated carbon coated with Fe2O3. IOSR J. Appl. Chem. 2017, 10, 12-21.

- Khaniabadi, Y.O.; Mohammadi, M.J.; Shegerd, M.; Sadeghi, S.; Seedi, S.; Basiri, H. Removal of Congo red from aqueous solution by a low-cost adsorbent: activated carbon prepared from aloe vera leaves shell. EHEMJ 2017, 4, 29-35.

- Nnadozie, E.C.; Ajibade, P.A. Isotherm, kinetics, thermodynamics studies and effects of carbonization temperature on adsorption of Indigo Carmine (IC) dye using C. odorata biochar. Chem. Data Collect. 2021, 33, 1-11.

- Oladele, E.O.; Alabi, A.H.; Olawale, M.D.; Ishaya, F.A. Adsorption of methylene blue dye from simulated wastewater onto modified and unmodified cassis fistula pods: kinetics, thermodynamics and equilibrium studies. Uniosun J. Sci. 2019, 4, 1-14.

- Olu-Owolabi, B.I.; Alabi, A.H.; Unuabonah, E.I.; Diagboya, P.N.; Böhm, L.; Düring, R. Calcined biomass-modified bentonite clay for removal of aqueous metal ions. J. Environ. Chem. Eng. 2016, 4, 1376-1382.

- Shaban, M.; Abukhadra, M.R.; Shaheim, M.G.; Ibrahim, S.S. Novel bentonite/zeolite-NaP composite efficiently removes methylene blue and Congo red dyes. Environ. Chem. Lett. 2017, 1-6.

- Srivastava, V.; Sillanpaa, M. Synthesis of malachite@clay nanocomposite for rapid scavenging of cationic and anionic dyes from synthetic wastewater. J. Eviron. Sci. 2017, 51, 97-110.

- Tamimi, M.; Bougdour, N.; Alahaine, S.; Sennaoui, A.; Assabbane, A. A study of the remove cationic and anionic dyes in aqueous solutions by a new natural clay. Int. J. Eng. Tech. Mgmt Res 2018, 5, 64-74.

- Adebayo, M.; Adebomi, J.I.; Abe, T.O.; Areo, F.I. Removal of aqueous Congo red and malachite green using ackee apple seed–bentonite composite, Colloid and Interface Science Communications. 2020, 38, 100311.

- Ajeigbe, H.A.; Vabi, M.B.; Inuwa, A.H.; AbdulAzeez, T.; Akinseye, F.M. Handbook on Improved Agronomic Practices of Groundnut Production in North East Nigeria. Feed the Future: The US Government’s Global Hunger and Food Security Initiative (2020). Pp 1.

- Kaykhaii, M.; Sasani, M.; Marghzari, S. Removal of dyes from the environment by adsorption process, Chemical and Materials Engineering. 2018, 6(2), 31 – 35.

- Ozola-Davidane, R.; Burlakovs, J.; Tamm, T.; Zeltkalne, S.; Krauklis, A.E.; Klavins, M. Bentonite-ionic liquid composites for Congo red removal from aqueous solutions, Journal of Molecular Liquids 2021, 337, 116373

- Pandey, S.; Ramontja1, J. Natural bentonite clay and its composites for dye removal: current state and future potential, American Journal of Chemistry and Applications 2016, 3(2), 8 − 19.

- Unuabonah, E.I.; Gunter, C.; Weber, J.; Lubahn, S.; Taubert, A. Hybrid clay a new highly efficient adsorbent for water treatment, ACS Sustain, Chemical Engineering Journal. 2013, 1, 966 – 973.

- Zakariyya, U.Z.; Saifullahi, S.I. Evaluation of microcrystalline cellulose from groundnut shell for the removal of crystal violet and methylene blue, Nanoscience and Nanotechnology 2018, 8(1), 1 – 6.