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Abstract (300 word limit)
Thermoresponsive surfaces enable the detachment of cells or cell sheets by decreasing the temperature of the surface when harvesting the cells. However, human pluripotent stem cells (hPSCs), such as embryonic stem cells and induced pluripotent stem cells, cannot be directly cultured on a thermoresponsive surface; hPSCs need a specific extracellular matrix to bind to the integrin receptors on their surfaces. We prepared a thermoresponsive surface by using poly (N -isopropylacrylamide-co-butylacrylate) and recombinant vit- ronectin to provide an optimal coating concentration for the hPSC culture. hPSCs can be cultured on the same thermoresponsive surface for 5 passages by partial detachment of the cells from the surface by de- creasing the temperature for 30 min; then, the remaining hPSCs were subsequently cultured on the same dishes following the addition of new cultivation media. The detached cells, even after continual culture for five passages, showed high pluripotency, the ability to differentiate into cells derived from the 3 germ layers and the ability to undergo cardiac differentiation.
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Fig. 3. The response of the hydrophobicity-hydrophilicity of the thermoresponsive PN88-coated plates to temperature. (A) Photos of water droplets evaluated by the sessile drop method performed on the TCP, PN88(1)-TCP, PN88(3)-TCP, PN88(5.5)-TCP, PN88(8)-TCP, PN88(10.5)-TCP, PN88(13)-TCP plates at 37 °C and 9 °C. (B) Photos of water droplets evaluated by the sessile drop assay performed on the TCP, rVN-PN88(1)-TCP, rVN-PN88(3)-TCP, rVN-PN88(5.5)-TCP, rVN-PN88(8)-TCP, rVN-PN88(10.5)-TCP, rVN- PN88(13)-TCP plates at 37 °C and 9 °C. (C) The water contact angle on the TCP, PN88(1)-TCP, PN88(3)-TCP, PN88(5.5)-TCP, PN88(8)-TCP, PN88(10.5)-TCP, PN88(13)-TCP plates at 37 °C (red circle) and 9 °C (blue square). (D) The water contact angle on the rVN-TCP, rVN-PN88(1)-TCP, rVN-PN88(3)-TCP, rVN-PN88(5.5)-TCP, rVN-PN88(8)-TCP, rVN- PN88(10.5)-TCP, and rVN-PN88(13)-TCP plates at 37 °C (red circle) and 9 °C (blue square).
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