# Performance analysis of carbonization systems and characterization of charcoal produced in the city of Douala

ZAM Jean Freddy, Master 2 Research in wood sciences. Laboratory of Forest Resources and Wood Valorization, Training Unit for Engineering Science, Post graduate School of Fundamental and Applied Sciences, University of Douala, PO Box: 1872, Douala, Cameroon

# Abstract

In the city of Douala, the production of charcoal with sawing waste is an activity that is gaining momentum and constitutes a real alternative to overcome the phenomenon of degradation of peri-urban ecosystems. However, the performance of the technologies used as well as the characteristics of the charcoals produced remain little studied. This study assesses the performance of the carbonization technologies used and characterizes the charcoal produced. In three major production sites in the city, 45 traditional kilns: 36 earth mounds and 9 earth pits were evaluated. In each carbonization site, the mass yield and economic yield was determined. Charcoals of different species (Tali; Okan; Azobe and Doussie) carbonized in pits and mound were sampled and analyzed to determine their properties. The results obtained show that the properties of charcoals are strongly influenced by the species of wood and the type of kiln. The best yields and charcoal properties were obtained by pit carbonization (25.39±4.88%) and by Azobe wood. These properties vary as follows: moisture contents (6.12% to 3.36%); ash content (0.66% to 2.17%); volatile matter content (16.10 to 24.19%); basal densities (0.49 g.cm-1 to 0.67 g.cm-1); fixed carbon content (67.42% to 78.66%) and higher calorific values of (29.91 to 34.24 MJ. Kg-1). These results lead to the conclusion that the carbonization systems used in Douala have yields similar to those of improved production systems and that the charcoal from sawing waste is of good quality for domestic use.

# Image

Figure 1: Different forms of sawing waste used for the production of charcoal in the city of Douala

# Recent Publications (minimum 5)

1. Freddy, Zam Jean, et al. "Physicochemical and hygroscopic properties of charcoals produced from residues of two tropical woods from Cameroon." International Journal of Coal Preparation and Utilization (2022): 1-24.

Biography

ZAM Jean Freddy is a teacher-researcher at the Higher Teacher Training College for Technical Education of the University of Douala, PhD student in engineering sciences at the Laboratory for the Valorization of Forest Resources and Wood (LaReFoB) within the postgraduate school for pure and Applied Sciences of the University of Douala in Cameroon, holder of a Master 2 Research in wood sciences. He has a background as a teacher of high schools and colleges of technical education in science and technology of wood. He is interested in the issues of renewable energy, particularly the energy recovery of woody biomass and the issues of hygroscopic behavior of fuels based on wood material. He is also in charge of teaching some teaching units at the University of Douala: technological and energetic valorization and industrial transformation of wood material.

Email: freddyzam83@gmail.com

# Notes/Comments:

Presenting author details

## Full name: ZAM Jean Freddy Contact number:+237 698466724 Twitter account:@Freddy29726813

Linked In account:https://www.linkedin.com/in/zam-jeqn-freddy-403baa191 Session name/ number:

## Category: (Poster presentation)