Title: New Directions in Aesthetic Medicine: A Novel and Hybrid Filler Based on Hyaluronic Acid and Lactose Modified Chitosan

Giulio Bianchini*

Jointherapeutics Srl, Italy

Abstract

Accorindg to Market Dynamics, rising disposable income and strong influence of social media are the key factors encouraging the dermal filler market growth. This global growth can be attributable to growing awareness and importance of quality of life and overall health among the population worldwide. Fillers based on crosslinked hyaluronic acid (HA) are becoming increasingly important in this field, for instance in the treatment of wrinkles or for volumizing purposes. Improvement of the benefit/risk ratio is the primary output for new products development therefore minimisation of side effects and improvement of performances are the main drivers. Through our research on an innovative lactose modified chitosan (CTL) we discovered unprecedent biological performances and physical-chemical synergism with HA. We therefore developed new fillers based on HA, crosslinked with reduced amounts of 1,4‐butanediol diglycidyl ether (BDDE) and formulated with CTL. Due to its cationic nature, CTL interacts with the anionic HA and enhance the elastic properties of the filler. Fillers manufactured with this novel technology (HACL‐CTL) were characterized and compared with several fillers available in the market. In particular, resistance against hyaluronidase, swelling, cohesivity and rheological properties were investigated. Cohesivity, resistance to hydrolysis and swelling of HACL‐CTL were comparable to commercial products. Interestingly, HACL‐CTL fillers showed excellent elastic performance that reached 94% of elasticity in response to shear stresses. Surprisingly, these fillers also showed a resistance to compression higher than that of currently marketed products, making them very promising for their lifting effect.

References

1. Bianchini G, F et al (2019)

Effects of Intra Articular Hyaluronic Acid Associated to Chitlac (Arty Duo®) in a Rat Knee Osteoarthritis Model. J Orthop Res . 2019 Apr;37(4):867-876.

2. Brun, P et al (2020)

Anti Inflammatory Performance of Lactose Modified Chitosan and Hyaluronic Acid Mixtures in an In Vitro Macrophage Mediated Inflammation Osteoarthritis Model. Cells 2020 May 26;9(6):1328.

3. Ladie, R et al (2021)

Supramolecular structuring of hyaluronan lactose modified chitosan matrix Paving the way towards high performance biopolymers with excellent biodegradation. Biomolecole 2021 , 11 (3), 389;

4. Tschon, M (2021)

Boosting the Intra-Articular Efficacy of Low Dose Corticosteroid through a Biopolymeric Matrix:

An In Vivo Model of Osteoarthritis. Cells. 2020 Jul; 9(7): 1571.

5 Tarricone, E et al (2021)

The Viability and Anti-Inflammatory Effects of Hyaluronic Acid-Chitlac-Tracimolone Acetonide- β-Cyclodextrin Complex on Human Chondrocytes. Cartilage. 2021 Dec; 13(2 Suppl): 920S–924S.

6 Daminato, E et al (2022)

New Directions in Aesthetic Medicine: A Novel and Hybrid Filler Based on Hyaluronic Acid and Lactose Modified Chitosan. Gels 2022, 8, 326

7 Donato, A et al (2022)

Anti-Inflammatory and Pro-Regenerative Effects of Hyaluronan-Chitlac Mixture in Human Dermal Fibroblasts: A Skin Ageing Perspective. Polymers 2022, 14, 1817.

Biography

Giulio Bianchini has completed his PhD in chemical sciencs from Ca’ Foscari University in 2013 and postdoctoral studies from University of Bristol (UK) School of Chemistry in 2015. Later on, he joined Jointherapeutics, an innovative Italian SME focused in the development of new biopolymers for healthcare purposes, and since than he coordinated several research projects, including chemical-physical, in vitro and in vivo studies, in collaboration with International Research Centres.. He has published several papers in reputed journals and he is inventor of more than 10 patents.

Presenting author details 
Full name: Giulio Bianchini
Personal email id: giulio.bianchini@jointherapeutics.com

Mobile Number: +39 3473034975
Telephone Number:  +39 049 8765215
Twitter account: n.a.
Linked In account: https://www.linkedin.com/in/giulio-bianchini-9a3a5869

Session name/ number: Aesthetic practices & Skin Care
Category: Oral presentation