# Nanocomposite magnetite/titania nanocomposite photocatalytic and magnetic properties

M.A. Ahmed1, N. Eassa2 and Z. A. Talib3

1National Ribat University, Sudan 
2Al Neelain University, Sudan
3Universiti Putra Malaysia, Malaysia

# Abstract

# Recently scientists have been working in developing and functionalizing the nanostructures for the application of environmental contaminant’s remediation as it serves the sustainable development Goals (3) the good health and well-being and the goal (6) of the healthy water and sanitation. The core-shell structure Magnetite and Titanium Dioxide (Fe3O4@TiO2) have been introduced for their synergetic photocatalysis and magnetic properties that can be exploited in UV treatment and magnetic separation from the treated water. The core-shell composite structures were prepared with different core/shell ratios; all prepared materials were characterized for their structural, optical, and magnetic properties. The synthesized structure has an absorption peak in the UV region, it has spherical shapes, a structure size ranging from 23-50 nm, and with magnetic saturation moment inversely proportional to the TiO2 shell thickness, the structure has the highest magnetic Saturation of 41.6 emu/g for the sample of lowest shell thickness, compared to similar structures.

# The properties of the as prepared photocatalyst nanocomposite will be suitable for magnetic separation and can be used in application of environmental purification.

# Recent Publications:

1. Ali A. Adam; Nihad A. A. Elhag; Fakhreldeen Abbas Saeed, Mohamed Yagob, Fayha Mohamed,  N. Eassa, Hanaa S. Abdalaziz, M A. Ahmed, Sharief F. Babiker: IEEE, DOI: 10.1109/ICOTEN52080.2021.9493517

# 2. M. Ali Ahmed, A. Taj Elsir, F. Mohammed, H. A. Elbushra, S. Tawer, N. Eassa, MRS Advances,    3(42-43), 2667-2674, DOI: 10.1557/adv.2018.3133

# 3. H. Elbushra, M. Ahmed, H.Wardi, N. Eassa, MRS Advances 3, no. 42-43 (2018): 2527-2535., DOI: 10.1557/adv.2018.230

Keywords: Titanium Dioxide, Magnetite, Photocatalyst, Magnetic, photocatalyst.

Biography:  

M.A. Ahmed is a faculty staff member (Assistant professor) and the head department of Basic Sciences Department, National Ribat University, Sudan. I received a PhD degree in Material Science; Physics discipline the field of nanoscience and nanotechnology from Al-Neelain University Sudan. Received a sandwich training six months Ph.D. fellowship from the organization of Women in Science for the developing world (OWSD), at University Putra Malaysia (UPM), Serdang, Malaysia in the period from May to October 2019. I also have two MSc degrees in general physics from University of Khartoum, and in the Radiation and Environmental Protection from Sudan Academy of Science.