# Investigation of the Abrasion Behaviour of GNP and B4C Reinforced Magnesium Composites

Simge Bayhatun, Master, Karabük Üniversitesi, Türkiye

Volkan Karakurt, Master, Karabük Üniversitesi, Türkiye

Hayrettin Ahlatcı, Prof.Dr., Karabük Üniversitesi, Türkiye

Mustafa Babanli, Azerbaijan State Oil and Industry University,Azerbaycan

Nurlan Gurbanov, Azerbaijan State Oil and Industry University, Azerbaycan

Yunus Türen, Doç.Dr., Karabük Üniversitesi, Türkiye

### Abstract

### In this study, 0.5% nano GNP (graphene nanoparticle) and 15% B4C reinforced composites with AZ71 Mg alloy matrix were produced and extruded by melt-based induction casting. The microstructure, mechanical and dry abrasion behavior of the produced composites were investigated. While Nano GNP is used because they exhibit high thermal conductivity and low friction coefficient, B4C particle has benefited from its high strength. In addition, another purpose of choosing B4C and GNP; Due to the high wettability between B4C, GNP and Mg matrix, the interfacial bond between the composite matrix and the reinforcement is also strong to obtain a final product. The abrasion tests of the extrusion specimens were carried out by measuring the weight loss under a constant 20 N load, at a constant speed of 100 mm/sec and a total sliding distance of 1000 m in a back-and-forth abrasion test device. In the studies, although the hardness value of the AZ71+15%B4C composite is high, the abrasion behavior of the nano Graphene reinforced AZ71+0.5%GNP composite has improved because it reduces the friction coefficient.

Recent Publications (minimum 5)

- Sager, A.M.M., Esen, İ., Ahlatcı, H., Türen, Y., Akın, B. (2021) "INVESTIGATION OF THE EFFECT OF ZK60/15% SILICON CARBIDE AND 0.2 - 0.5% NANO ALUMINUM NITRIDE REINFORCED COMPOSITES ON THE MICROSTRUCTURE, HARDNESS, AND CORROSION PROPERTIES", 6th INTERNATIONAL CONGRESS ON INNOVATIVE SCIENTIFIC APPROACHES , (pp. 315-326), (Aralık 2021)

- Boztaş, H., Akın, B., Keskin, E., Ahlatcı, H., Esen, İ., Türen, Y., Yaşın, S. (2022) "INVESTIGATION OF WEAR PERFORMANCE OF SILICON CARBIDE AND ALUMINIUM NITRIDE REINFORCED AZ91 ALLOY", 5TH INTERNATIONAL CONFERENCE ON INNOVATIVE STUDIES OF CONTEMPORARY SCIENCES , Tokyo, Japonya, (Ocak 2022)

Biography

# I'm Simge Bayhatun. I graduated from Karabuk University Metallurgy and Materials Engineering. I am doing my master's degree at the same university. I am live İzmir Karşıyaka. During my time at my school, I actively used the metallography devices in the department laboratory. I am familiar with wear device, fatigue devices and tensile testing.

# Email: simge.bayhatun@gmail.com

Notes/Comments:

Presenting author details 
Full name: Simge Bayhatun
Contact number:05413177267

Session name/ number: Simge Bayhatun
Category: Oral presentation