# Title: Hierarchically porous manganese based metal-organic-framework for potential battery-supercapacitor applications

Umer Aziz, Muhammad Zahir Iqbal

Nanotechnology Research Laboratory, Faculty of Engineering Sciences, GIK Institute of Engineering Sciences and Technology, Topi, 23640, Khyber Pakhtunkhwa, Pakistan

# Abstract

The application of nontoxic metal-organic-frameworks (MOFs) has recently obtained ground in batteries, hybrid supercapacitor, and water splitting. Here, we prepared unprecedented Manganese based MOF (Trimesic acid used as linker) via hydrothermal approach to scrutinize their electrochemical properties. A three electrode setup were developed in which the Mn MOF revealed remarkable specific capacity of 1569.24 C g-1 at 3.6 A g-1 with long lasting capacity retention. Furthermore, a hybrid device was fabricated in such a way that the Mn MOF and activated carbon was functionalized as positive and negative electrodes, respectively. The constructed Mn MOF//AC device attained exceptional specific capacity, energy and power are 248.3 C/g, 60 Wh kg-1, and 2550 W kg-1, correspondingly. After 1000 galvanostatic cycles, the hybrid device results in outstanding cycling stability of 98.57% and coulombic efficiency of 96.97%. The nature of the device was validated through the Power’s law and Dunn’s model. Due to its electrochemical properties, Mn MOF//AC is a promising choice for battery-supercapacitor devices in portable electronics.

# Biography

Umer Aziz is graduated from Islamia College University, Peshawar with a field of interest in Physics, and material science. He is currently expertise in Applied Physics at Ghulam Ishaq Khan institute, Pakistan. Umer’s past research has focused on Lead-free piezoelectric ceramics and currently studying different nanomaterials for hybrid supercapacitors applications. He is currently interested in perusing his PhD. In the area of batteries and supercapacitors. After completion of the program, Umer aspires to work as a researcher in the industry.

Presenting author details Full name: Mr. Umer Aziz Contact number:

Category: Oral presentation