# Electrocatalyst for Water Oxidation: Iron/Nickel/Zinc mixed oxide

Sepideh Madadkhani, PhD, IASBS, IRAN

## Abstract

Statement of the Problem: Switching from fossil fuels to renewable energies is an inevitable task that should be performed in the near future to provide clean and sustainable energies for human beings. Water splitting toward hydrogen production is a promising approach to store such energies. In this regard, there are some bottlenecks for water splitting systems. Among different solutions, electrocatalytic water oxidation process is considered to be a breakthrough in water- splitting technology. Among the metal oxides, Ni/ Fe (oxy)hydroxide, which can be synthesized with different morphologies, stoichiometries and crystallinities, are able to catalyze the water-oxidation reaction in alkaline electrolyte solutions. Additionally, some research groups previously   reported   that   Ni/Fe   (oxy)hydroxides   have   the   lowest overpotential toward water oxidation under the alkaline conditions. The purpose of this study is to describe a new procedure to synthesize an  efficient  Fe/Ni/Zn-based  water-oxidizing  catalyst  by  the  thermal decomposition of a trimetallic organometallic compound. Characterization Methods: The catalyst were studied using scanning electron microscopy, transmission electron microscopy, electrochemical methods, X-ray diffraction, X-ray absorption spectroscopy, and X-ray photoelectron spectroscopy. Findings: In addition to Ni and Fe as important ions for water oxidation, the present organometallic compound includes Zn ion as an amphoteric ion which can be removed in the presence of KOH solution to obtain more active sites on the surface of the catalyst and thus a self-improvement is observed during reaction. On the basis of the obtained results, a structure similar to (Ni, Zn)Fe2O4 is proposed. The obtained nanosized oxide on FTO at pH=13  showed  a  current density  of  12  mA/cm2  at  1.2  V.  Long-time amperometry also indicated an increase in the current density. Continued CVs showed that the water-oxidizing activity of the compound increased during the cyclic voltammetry process. Since Zn ions are amphoteric, they can be soluble in KOH solution and results in a self-improvement for the catalyst. Removing the Zn ions from the NiFeZnOx structure may be a promising method to increase the catalytic activity of the present oxide. Conclusion & Significance: Introducing a new procedure to synthesize an efficient Fe/Ni/Zn-based water-oxidizing catalyst by the thermal decomposition of a trimetallic organometallic compound. The catalyst showed a good long-term stability and performance. The composition of the compound was characterized by some common methods and found to be an efficient wateroxidizing catalyst.

## Image

Figure 1: Amperometry for Fe/ Ni/Zn oxide in KOH (0.1M) at 1.1V (left). Continuous  CVs  of  Fe/Ni/Zn  oxide  at  100  mV/s  in  KOH  (0.1M)  (right). 30μL of oxide was dispersed in water (1.0 mg/mL) and dripped on the FTO electrode and dried at 60 °C. Then, 10 µL of 0.5 wt% Nafion solution was cast on the surface of the FTO electrode (1.0 cm2).

## Recent Publications

- Lewis, N. S. & Nocera, D. G. Powering the planet: Chemical challenges in solar energy utilization. Proc. Natl Acad. Sci. 103, 15729–15735 (2006).

- Trześniewski, B. J. et al. In situ observation of active oxygen species in Fe-containing Ni-based oxygen evolution catalysts: the effect of pH on electrochemical activity. J. Am. Chem. Soc. 137, 15112– 15121 (2015).

- Lu, X. & Zhao, C. Electrodeposition of hierarchically structured three-dimensional nickel–iron electrodes for efficient oxygen evolution at high current densities. Nat. Commun. 6, 6616 (2015).

- Görlin, M. et al. Dynamical changes of a Ni-Fe oxide water splitting catalyst investigated at different pH. Catal. Today 262, 65–73 (2016).

- Dionigi, F. & Strasser, P. NiFe‐Based (Oxy) hydroxide Catalysts for Oxygen Evolution Reaction in Non‐Acidic Electrolytes. Adv. Energy Mater. 6 (2016).

Biography

Dr. Sepideh Madadkhani is currently postdoctoral researcher in Institute for Advanced Studies in Basic Sciences (IASBS), Zanjan, Iran. She has a background in Inorganic Chemistry and focuses on Water Splitting. She is enthusiastic about transition metal compounds as electrocatalysts for sustainable energy conversion and storage applications. She is interested in developing operando experiments. Due to her years of research in the field of water oxidation, she was chosen as the best research student during her Ph.D. in her country.

Email: smadadkhani@yahoo.com

Notes/Comments:

Presenting author details

# Full name: Sepideh Madadkhani Contact number: +989362958504 Mail id: smadadkhani@yahoo.com Category: (Oral presentation)