Anticancer drug eumelanin and its composition with  silver nanoparticles

N.M. Permyakova, T.B. Zheltonozhskaya, V.V. Klepko,

Institute of Macromolecular Chemistry, NAS of Ukraine, Kyiv, Ukraine

T.O. Kondratiuk

Scientifically-Educational Center “Institute of Biology and Medicine”, Taras Shevchenko National University of Kyiv, Kyiv, Ukraine

D.O. Klymchuk, Institute of Botany, NAS of Ukraine, Kyiv, Ukraine

Abstract

In recent years, there has been a rapid expansion in the use of noble metal nanoparticles in biomedicine, pharmacology, cosmetology, and other areas related to human health. Today, the particular attention is paid to the inclusion of gold and silver nanoparticles in various drugs or nanocarriers with drugs in order to combine their medicinal properties with the ability to control their pharmacokinetics in a living organism. In this context, the current report presents a detailed study of in situ synthesis of silver nanoparticles (AgNPs) in a poorly soluble drug eumelanin (EMel) in an aqueous medium.

Well known, that the melanins are a broad class of polyphenolic functional biopolymers found throughout in nature. These biopolymers with good biocompatibility and biodegradability, binding ability to drugs and ions, intrinsic photoacoustic properties can serve as an efficient endogenous nanosystem for imaging-guided tumor chemotherapy. Sample EMel was obtained as a vital activity product of black yeast “Nadsoniella nigra sp. X-1”. The chemical structure and polyampholytic properties of this sample were studied using 1H NMR and FTIR spectroscopy and potentiometric titration.

The processes of borohydride reduction of silver salt to metal nanoparticles in EMel nanostructures in an aqueous medium were studied using UV-Vis spectroscopy and TEM. The kinetic features of the formation of silver particles in EMel nanostructures were monitored by changes in the position and integrated intensity of the AgNP surface plasmon resonance band at about 400 nm in time.  It was shown that EMel matrices provide high yield and stabilization of AgNPs in an aqueous medium. The morphology of the AgNPs/EMel composition is mainly represented by various EMel nanostructures containing metal nanoparticles of ~1.5-12 nm in size (Figure a). However, in single large EMel structures existing in the initial drug dispersion, the size of AgNPs can reach ~50 nm (Figure b).

Image

| a | b |
| --- | --- |
| Figure. TEM images of the composition with smaller (a) and larger (b) AgNP |  |

Recent Publications

- Permyakova NM, Zheltonozhskaya TB, Beregova TV, Klymchuk DO, Falalyeyeva TM, Grishchenko LN (2016) Micellar nanocarriers for anticancer drug melanin. Mol Cryst Liq Cryst 640(1):122–133

- T. Zheltonozhskaya, N. Permyakova, T. Kondratiuk, T. Beregova, V. Klepko, B. Melnik (2019) Hybrid-stabilized silver nanoparticles and their biological impact on hospital infections, healing wounds, and wheat cultivation. French-Ukr. Journal of Chemistry 7(2):20-39

- N.M. Permyakova, T.B. Zheltonozhskaya, V.I. Karpovsky, R.V. Postoy, V.I. Maksin, S.V. Partsevskaya, L.N. Grishchenko, D.O. Klymchuk, V.V. Klepko (2022) Compositions of α-tocopheryl acetate with micellar nanocarriers and their possible use as biologically active additives. Applied Nanoscience 12:1295-1313

- Permyakova N, Zheltonozhskaya T, Ignatovskaya M, Maksin V, O, Klymchuk D (2018) Stimuli-responsive properties of special micellar nanocarriers and their application for delivery of vitamin E and its analogues. Coll Polym Sci 296:295–307

- Shevchenko L.V., Dovbnia Y.Y.,  Zheltonozhskaya T.B., Permyakova N.M., Vygovska L.M., Ushkalov V.O. (2021) The effect of nanosilver in carriers based on polymer/inorganic hybrids on the quality and safety of edible chicken eggs. Regulatory Mechanisms in biosystems 12(3)

Biography

Nataliya Permyakova graduated from the faculty of Chemistry of Taras Shevchenko National University of Kyiv in the speciality of physical chemistry and colloids. From 1980 to 2018 worked as the scientific researcher at the department of Macromolecular Chemistry of  Faculty of Chemistry Taras Shevchenko National University of Kyiv. Since 2019 works as the scientific researcher at the department of Polymer Physics of the Institute of Macromolecular Chemistry of the NAS of Ukraine. Research direction and interests: design and research of physicochemical and functional properties of heteropolymers, polymer/inorganic hybrids and multicomponent systems, based on them, for nanotechnology, biomedicine, environment and agriculture, in particular, synthesis of metal nanoparticles in polymer matrices and creation of micellar nanocarriers for drug delivery.

Email: permmyakova@ukr.net

Notes/Comments:

Presenting author details 
Full name: Permyakova Nataliya
Contact number: +38 0634827782
Twitter account:
Linked In account:

Session name/ number: 19. Nano Biotechnology
Category: Poster presentation