Biobased sustainable films from the Algerian Opuntia ficus-indica cladodes powder: Effect of plasticizer content

Nadia Chougui 1*, Nawal Makhloufi 1, Farouk Rezgui 2, Elias Benramdane 1, Carmen S. R. Freire 3, Carla Vilela 3, Armando J. D. Silvestre 3

1Faculty of Natural and Life Sciences, University of Bejaia, Algeria

2Laboratory of Organic Materials, Faculty of Technology, University of Bejaia, Algeria

3CICECO – Aveiro Institute of Materials, Department of Chemistry, University of Aveiro, Portugal

Abstract

Native of Mexico, Opuntia ficus-indica was introduced in southern Spain, thereafter, it was spread throughout the Mediterranean Basin by the Spanish conquerors in the 16th and 17th century.  O. ficus-indica is a tropical and subtropical plant able to grow in arid and semi-arid regions, such as the Mediterranean and Central America regions. The culture of Opuntia covers about 200,000 ha in North Africa. This tree is used against soil erosion and desertification, for fruit production and is encouraged to promote the livestock sector. It has recently received an ever increasing attention from researchers world-wide for multivalent pharmaceutical and cosmetical potential of its different compartments (fruits, seeds, cladodes…).

The present study investigated the elaboration by casting method and characterization of new biodegradable films composed of cladodes powder (CP) of the plant raw-material mentioned above, and a marine seaweed derivative, namely agar (A). The effect of glycerol concentration on the properties of the films was evaluated at four different contents (30, 40, 50 and 60 wt.%). The films present UV-blocking properties, thermal stability as well as moderate mechanical performance and water vapor transmission rate (WVTR). The results point to an increase in thickness, elongation at break, moisture content, water solubility, and WVTR with increasing glycerol content. On the contrary, Young’s modulus, tensile strength and contact angle decreased as glycerol concentration increased. The best combination is obtained for the film with 30% glycerol, based on an intermediate compromise between physical, mechanical, thermal and barrier properties. All these outcomes express the potentiality of the powder obtained from grinding the OFI cladodes as raw material to produce low-cost films for the development of sustainable packaging materials.

Keywords: Opuntia ficus-indica cladodes powder; agar; biobased films; effect of plasticizer; sustainable packaging

Biography

Nadia Chougui is a professor at Faculty of Natural and Life Sciences, University of Bejaia, Algeria.